Monocacy Aqueduct

Physical Analysis, Condition Assessment and

Alternative Schematic Design Proposals

Milepost 42.19 in the Chesapeake & Ohio Canal National Historical Park

Dickerson, Maryland

prepared for:		National Park Service

United States Department of the Interior

C&O Canal National Historical Park

National Capital Region

prepared by:		architrave p.c., architects

420 10th Street SE

Washington, DC 20003

202-544-1640

McMullan & Associates

8381 Old Courthouse Road, Suite 350

Vienna, Virginia 22182

703-556-0651

Bregman & Company, Inc.

4827 Rugby Avenue, Suite 300

Bethesda, Maryland 20814

301-652-4818

1 April 1999

Final Submission

Credits

U.S. Department of the Interior

National Park Service

Douglas Faris

Superintendent

C & O Canal National Historical Park

Kevin Brandt

Assistant Superintendent

C & O Canal National Historical Park

Douglas Stover

Chief, Branch of Resource Management

C & O Canal National Historical Park

Robert J. Kapsch, Ph.D.

Government Technical Representative

National Capital Region

National Park Service

Robert A. Weinstein, Project Manager

Margaret Mook

architrave p.c., architects

420 10th Street SE

Washington, DC 20003

202-544-1640

Denis McMullan

Abba Lichtenstein

Douglas Bond

McMullan & Associates

8281 Old Courthouse Road, Suite 350

Vienna, Virginia 22182

703-556-0651

Nader Bazzazieh

Bregman & Company, Inc.

4857 Rugby Avenue, Suite 300

Bethesda, Maryland 20814

301-652-4818

Table of Contents

Cover Page										           												Page

Credits.....................................................................................................................................	 2

Table of Contents......................................................................................................................	 3

Executive Summary..................................................................................................................	 5

I.	Introduction............................................................................................................ I-1 to I-2

A.	Background

B.	Administrative History

C.	Inspection and Reporting Methodology

II.	Historical Significance of the Aqueduct..............................................................II-1 to II-6

A.	Overview

B.	Architectural Description

C.	Brief History of the Aqueduct

D.	Statement of Significance and Historical Context

E.	Identification of Historic Fabric to be Preserved

F.	Proposed Use and Treatment of the Aqueduct

III.	Physical Condition of the Aqueduct....................................................................III-1 to III-15

A.	Condition Assessment

1.	Arches

2.	Piers (Above the water line)

3.	Abutments

4.	Upstream Parapet

5.	Downstream Parapet (Towpath)

6.	Steel Banding

7.	Interior Steel Rod Reinforcement

8.	Test Pits

9.	Identification of Aqueduct Stone

10.	Railing

11.	Emergency Stabilization (Above Water Line)

B.	Structural Analysis

1.	Methodology

2.	Historic Construction Technologies

3.	Material Properties

4.	Ultimate Masonry Strength for Arches

5.	Allowable Stresses for Arch Masonry

6.	Design Loading

7.	Comparison of Applied and Allowable Stresses

8.	Historic Performance of C&O Canal Aqueducts

9.	Analysis of Monocacy Aqueduct

10.	Summary

IV.	Conceptual Design Alternatives......................................................................................IV-1 to IV-6

A.	Design Alternatives

B.	Alternative 1 - Preservation through Stabilization of Existing Structure with the

Steel Banding

C.	Alternative 2 - Preservation through Stabilization of Existing Structure without 				the Steel Banding

D.	Railing Design

E.	Other Considerations

1.	Maintenance

2.	Construction

3.	Environment

4.	Preservation

5.	Accessibility

V.	Appendices..................................................................................................................

A.	Sketches

1.	Structural Sketches

2.	Railing Sketches

B.	Photographs

1.	Existing Condition Photographs

2.	Reproductions of Historic Photographs

C.	Stone and Mortar Testing

D.	Structural Calculation

E.	Annotated Bibliographies

F.	Field Notes

G.	Cost Estimate

VI.	Environmental Assessment.......................................................................................

VII.	Bureau of Reclamation Report.................................................................................

EXECUTIVE SUMMARY

The Monocacy Aqueduct, located at mile post 42.19 of the C & O Canal National Historic Park (NHP), is the longest of the eleven aqueducts constructed for the Canal and is considered to be one of the most important engineering accomplishments of early canal construction in this country.  It is a significant structure as defined by the National Register of Historic Places, because of its role in our national history of transportation, as an important structure within the Park, and by its being an exemplary example of a stone aqueduct.  Due to severe deterioration caused by the ravages of time and repeated flooding, in 1998 it was placed on the National Trust for Historic Preservation’s list of the 11 most endangered historic structures.

Currently the structure is encased by a metal cage of steel banding, installed in 1975 after severe damage was inflicted by Hurricane Agnes in 1972.  This steel banding undoubtedly has saved the structure from further deterioration or even collapse.

The object of this report is to explore and evaluate two options for the care and maintenance of the structure. The first option is to stabilize the structure with the steel banding in place; the second is to restore the structure so that the steel banding can be removed.  Included in this report is an analysis of each option, including a cost estimate, studies for railing designs, a statement of historical significance, and an environmental assessment of the impact of the proposed alternatives on the site.

The following two schematic design alternatives were considered, with an estimated construction cost developed for each:

Alternative 1: Stabilization without removing steel banding$3,105,000			Alternative 2: Restoration of Aqueduct and removal of steel banding....$5,634,000

Both alternatives are structurally acceptable.  The removal of the steel banding proposed in Alternate 2 not only returns the aqueduct to its original unwatered appearance, but also enhances its use by removing encumbrances to movement across the structure, by allowing people and maintenance vehicles to travel inside the canal prism across the Monocacy River.

The environmental analysis recommends a Finding of No Significant Impact for both proposed schemes.  In both schemes any disturbance is due to construction and is temporary and mitigatable.

We recommend Alternative 2 be chosen.  The increased benefits of this design over Alternative 1 far outweigh the increased cost.   This option will return the aqueduct to its original unwatered  historic appearance, and will provide safer and fuller use of the towpath and the canal bed.

BACKGROUND

Aqueduct No. 2 of the Chesapeake and Ohio (C&O) Canal, known as the Monocacy Aqueduct, carried the Canal across the Monocacy River.  It was completed in 1833, five years after the start of construction on the Canal.  At a length of 516 feet, it is the longest aqueduct on the canal, and was heralded as an engineering achievement. Unlike other canal structures plagued by poor craftsmanship and substandard materials, the Monocacy Aqueduct was distinguished by excellent craftsmanship and fine stone.  It, and the other aqueducts, were essential to the operation of the canal.

The Canal was originally intended to connect the waterways of the Chesapeake in the East to the Ohio River in the West.  By 1850 it was extended as far as Cumberland, Maryland, which became its western terminus.  This invaluable connection to the interior resulted in a boon to agriculture in western Maryland and southwestern Pennsylvania, the development of milling and manufacturing along the Potomac Valley, and, most importantly, created access to the coal fields in Cumberland and the surrounding areas.  In 1875, at the height of its operation, more than 500 boats carried 904,898 tons of coal and 68,907 tons of other cargo over the canal.

Due to their  immediate proximity to the Potomac River, the canal structures were subjected to repeated flooding.  Several structures were also ravaged in the Civil War. Because of its quality of construction and because it was relatively untouched in the Civil War (unlike the Conococheague Aqueduct, which both sides tried to blow up), the Monocacy Aqueduct fared better than most.  Over the last 35 years, the structure has been overtopped by Monocacy River flood waters roughly once a decade: twice in 1998, in 1985, and in 1972. The Aqueduct was relatively intact until 1972 when the flood borne debris of Hurricane Agnes subjected the structure to repeated pounding and battering.  The handrail on the towpath (downstream) side consisted of vertical pickets set into the coping stones.  It acted like a strainer for debris until it was ripped off, taking the coping stones with it.  Over time the upstream wall has been significantly weakened by  hydraulic forces and/or other mechanisms.  Subsequently, the Aqueduct was stabilized and held together by a framework of steel banding and other measures.

Major milestones in the history of the Monocacy Aqueduct are:

1828		Construction begun on the C&O Canal

1829-1833	Construction of the Monocacy Aqueduct

1835	First Section of the canal from Georgetown to Williamsport, including the Monocacy Aqueduct, is officially opened

1850		Balance of the Canal opened

1861-1865	Civil War

1889		Major flood throws Canal into receivership with B&O Railroad

1924		Major flood & closing of the Canal

1924-1937	Deterioration of the Canal

1937		National Park Service (NPS) acquisition of the Canal

1961		Canal declared a National Historic Monument

1971		C&O Canal becomes a national park

1972		Hurricane Agnes inflicted significant damage to the Monocacy Aqueduct

1975		Steel bracing installed to stabilize structure of Monocacy Aqueduct

ADMINISTRATIVE HISTORY

“The 19,390-acre C&O Canal NHP possesses a variety of features including canal-based resources such as aqueducts, dams, the towpath, lockkeepers houses, culverts, holding and loading basins, associated resources such as warehouses, mills, bridges, and railroad-related building and structures.  A small portion of the park, approximately 124 acres, lies in West Virginia: the remainder is in Maryland and Washington, D.C.

“In September 1938, NPS purchased the 184.5-mile C&O Canal right-of-way between Georgetown and Cumberland, Maryland, using funds provided by the Federal Emergency Administrator of Public Works.  Immediately following this purchase, NPS initiated restoration and rehabilitation of the 23-mile stretch between Washington, D.C., and Seneca, Maryland, to be maintained for public recreation.  North of Seneca, however, the canal and canal-related resources received minimal attention.  According to a 1948 survey of the canal area, ‘the canal and the structures in this area have received little or no maintenance attention, have become overgrown, are inadequately policed, in some areas constitute unhealthful conditions and give rise to constant problems of administration.’  Despite its condition, the canal was declared a National Historical Monument in 1961.  A new phase of NPS management began in 1971 with Congressional passage of Public Law 91-664, which created the C&O Canal NHP to preserve and restore the canal’s resources for historical interpretation and public recreation.  Known as the ‘Chesapeake and Ohio Development Act,’ the law authorized the Secretary of the Interior to maintain and restore the canal for recreational purposes.  The act also provided for acquisition of specific lands in the canal corridor by the state of Maryland.  Existing utility easements, special use permits, and other rights were protected by the act.  Almost three-quarters of the Park’s lands are owned by NPS; the remainder are divided equally between state and local areas and private property."

(From Cultural Landscape Report, Chesapeake & Ohio Canal, Land and Community Associates, 1994)

INSPECTION AND REPORTING

Historic

architrave's field inspection of the Aqueduct focused on architectural elements of the structure, particularly the railing, to provide a descriptive narrative and to aid in the development of the railing studies.  We examined  historic photographs from the C&O Canal Library, Historic American Buildings Survey (HABS) drawings,  and the 1975 Construction Drawings of the stabilization project prepared by the Federal Highway Administration of the U. S. Department of Transportation.  Additionally, we studied the written documents referenced in the general bibliography.

Structural

See Section III for detailed structural inspection, testing and analysis methodology.

National Park Service, U.S. Department of the Interior. Chesapeake and Ohio Canal. Official National Park Handbook

142.  Washington, D.C.: U.S. Department of the Interior, 1991.  pp 64-65.

The term "purchased" is misleading. Actually, Secretary of the Interior Harold Ickes received the deed for the

Chesapeake and Ohio Canal from the receivers of the Baltimore and Ohio Railroad for two million dollars which was

applied to the Baltimore and Ohio Railroad's debt to the Reconstruction Finance Corporation.