## Slide 1: Entropy evaluation of subsurface materials and defects in Concrete Slabs using GPR
Mohammed Abdul Rahmana, Dipesh Dondaa, Fawzi Latosha, Alexander Tarussovb, Ashutosh Bagchia
  aDepartment of Building, Civil and Environmental Engineering, Concordia University, Montreal, bRadex Detection Inc., 4 Place du Commerce, Suite 101, Verdun
Presenter:
Mohammed Abdul Rahman
Project in collaboration with:

## Slide 2: Gpr Background

## Slide 3
Principle
Processing
B –Scan
Recorded Signal
Radar Principle
A –scan
Top Layer
Reinforcement Layer
Ground Penetrating
Radar (GPR)

## Slide 4
Picking of rebar location
Condition map
Numerical Amplitude Analysis

## Slide 5
Limitations of Numerical Analysis
Neglects majority of information in the profile
Various factors like surface anomalies are ignored
Results obtained are noisy, vague and not reliable completely
Improper correlation when compared to actual ground condition
Depth correction is required
Limits of corrosion are subjective

## Slide 6
Method
Highly subjective
Prone to human error
Slow speed of analysis
Inconsistent results
Marking attenuated areas
Condition map
Anomaly and corrosion
A. Tarussov, M. Vandry, and A. De La Haza, “Condition assessment of concrete structures using a new analysis method: Ground-penetrating radar computer-assisted visual interpretation,” Constr. Build. Mater., vol. 38, pp. 1246–1254, Jan. 2013, doi: 10.1016/j.conbuildmat.2012.05.026.
Visual image-based Analysis

## Slide 7
Method
z – random variable representing intensity
P(zi) – respective histogram; i= 0,1,2…., L-1
L- number of distinct intensity levels
Amplitude picking vs. Entropy
Automated image Analysis
Detect
Entropy
Cluster
M. Abdul Rahman, T. Zayed, and A. Bagchi, “Deterioration Mapping of RC Bridge Elements Based on Automated Analysis of GPR Images,” Remote Sensing, vol. 14, no. 5. 2022, doi: 10.3390/rs14051131.

## Slide 8: Experimental Setup

## Slide 9: Test Slabs
Three plain concrete slabs
Compressive strength - 35 MPa.
Three arrangements :
  Slab 1 over Slab 3
  Slab 2 over Slab 3
  Slab 1+2 over Slab 3
GSSI Model 51600S GPR
Antenna frequency :1600 MHz
Pulse duration: 0.7 ns.
Samples/Scan :512
Bits/sample: 16
Dielectric constant – 6.0;
Depth range – 35 cm.
Handheld mini-cart
Scanning parameters

## Slide 10: Study of REBARS, Air and Water Gap
(a) Various sizes of rebars Used (Left to Right; 6mm, 10mm, 18mm, 20mm, & FRP 21.8 mm)
(b) Schematic diagram showing an arrangement to simulate water and air gap (1 mm, 3 mm, & 4.8 mm )
(a)
(b)

## Slide 11: results

## Slide 12: Rebars
Diameter increases, Amplitude & entropy values increases
Average drop with respect to depth
  5 cm to 10 cm : 76% (Amplitude), 24% (Entropy)
  10 cm to 15 cm: 20% (Amplitude), 6.4% (Entropy)
Size of rebar has less impact, depth has significant impact
Notes: Three scans were repeated for each rebar size at every depth with the GPR to ensure the conformity of the lab tests.

## Slide 13: Air gaps
Air gaps increases, increase in both factors (less impact)
Average change with respect to depth
  5 cm to 10 cm : 75% (Amplitude), 29% (Entropy)
  10 cm to 15 cm: -14% (Amplitude), 11% (Entropy)
Inconsistent rise in amplitude at greater depth unlike entropy
Notes: Three scans were repeated for each rebar size at every depth with the GPR to ensure the conformity of the lab tests.

## Slide 14: water gaps
3mm to 5.8mm gap, similar across all depths – small gap sizes, less impact
5.8mm to 8.8 mm decreases: 20% (amplitude), 7% (entropy)
Average change with respect to depth
  5 cm to 10 cm : 69% (Amplitude), 20% (Entropy)
  10 cm to 15 cm: -25% (Amplitude), 10% (Entropy)
Water and/or moisture significantly effect GPR signals consistency
Notes: Three scans were repeated for each rebar size at every depth with the GPR to ensure the conformity of the lab tests.

## Slide 15: Comparison for different materials
With increase in depth, consistent drop in entropy for all materials
Inconsistency in air gaps for amplitude values
Reflection values range: Water > Rebars > Air gaps
Drop higher from 5cm to 10 cm than from 10 cm to 15 cm
High energy loss closer to surface
Amplitude (mV) |  |  | 
Depth↓ | Rebars | Air Gaps | Water Gaps
5 cm | 4.94 x 106 | 1.80 x 106 | 8.02 x 106
10 cm | 1.21 x 106 | 4.44 x 105 | 2.48 x 106
15 cm | 7.12 x 105 | 5.06 x 105 | 1.87 x 106
Entropy values |  |  | 
Depth↓ | Rebars | Air Gaps | Water Gaps
5 cm | 6.78 | 5.39 | 7.23
10 cm | 5.12 | 3.80 | 5.80
15 cm | 4.79 | 3.40 | 5.24

## Slide 16: CONCLUSIONS AND FUTURE WORK
GPR can be used to detect and distinguish subsurface materials and defects at differing depths
Entropy yielded consistent results
Limitations: length of the slab, rebars not embedded, and actual cracks/gaps contain other impurities
Future Works: Analyze GPR signals with varying degrees of rebar corrosion, compare with in-situ concrete
Research aim to improve GPR reliance as a condition assessment tool