On vibration analysis of MRE based sandwich plates using finite element method

Maryam Zare, Ramin Sedaghati

Department of Mechanical Industrial and Aerospace Engineering, Gina Cody School of Engineering and Computer Science, Concordia University, Montreal, Quebec, Canada, H3G 1M8

Email : maryam.zare@mail.concordia.ca, ramin.sedaghari@concordia.ca

Magnetorheological elastomers (MREs) are smart elastomeric materials, with magnetic field-dependent stiffness and damping properties. In this study, the vibration characteristics of sandwich plates with integrated MREs as the core layer are investigated. MRE based sandwich plates can be effectively used in development of novel adaptive structures for real-time vibration control applications. In this study, the free-vibration governing equations of the MRE sandwich plate in finite element form have been derived using Hamilton’s principle. The effect of the applied magnetic field on the first three natural frequencies of the MRE plate is investigated.  Results show a noticeable increase of 13.3%, 11.9%, and 10% in the first, second, and third natural frequencies of a clamped MRE plate, respectively under the application of 600 mT magnetic flux density.

KEYWORDS: Magnetorheological elastomer, Finite element method, Sandwich MRE embedded plate

# INTRODUCTION

Magnetorheological elastomers (MREs) are a class of smart elastomeric materials which are made of the polymeric matrix and embedded micro-ferromagnetic particles, such as carbonyl iron particles due to their high saturation limit. MREs can be in the form of isotropic (cured in the absence of an external magnetic field) in which iron particles are randomly dispersed or the inform of anisotropic (cured in the presence of an external magnetic field) in which iron particles are structured in the direction of the field. Due to their unique field-dependent variable stiffness and damping properties, MREs have been effectively utilized in many adaptive devices to semi-actively isolate or absorb vibration. MREs have also been used as core layers in sandwich plates to develope adaptive continuous structures whose vibration modes can be tuned using applied magnetic field.  A number of studies have investigated the behavior of sandwich structures with MRE core layers. Nayak et.al [1], studied the behavior of a magnetorheological MRE cored sandwich beam subjected to time-varying axial load. In their study, the finite element method and the Guyana reduction method were applied to derive and solve the governing equations.

Eshaghi et.al [2] studied the vibration characteristics of a partially treated MR fluid sandwich plate by developing a finite element method, as well as, laboratory experiments. In their study, slippage between the constraining top and bottom layers is considered.

The finite element dynamic analysis of an orthotropic rectangular sandwich plate with an electrorheological (ER) fluid core layer was studied by Jia-Yi et.al [3]. In their study, the effect of the layers’ geometrical properties on the natural frequencies and modal loss factors is discussed.

In this study, the variation of natural frequencies of MRE sandwich plates under varying applied magnetic fields is investigated using the finite element method. A 4-node quadrilateral element having 28 DOFs together with Hamilton’s principle has been used to formulate the free-vibration governing equations in finite element format.

# finite ELEMENT modeling of the MRE SANDWICH plate

Figure 1 shows the schematic view of the multilayer plate considered in this study. The sandwich structure consists of bottom and top elastic Aluminum layers and the MRE  as the core layer.  Kirchoff’s plate theory is used for modeling the top and bottom layers.  Also, the core layer is assumed to be isotropic MRE operating in linear viscoelasticity region. It is noted that the layers are considered completely bonded to each other without any Slippage.

Figure 1: Schematic view of the MRE core sandwich plate

The sandwich plate is discretized using 4-noded rectangular elements as shown in Figure.2.

Figure 2: Four-node rectangular element [4]

Each node has seven degrees of freedom as:

|  | (1) |
| --- | --- |

where, uc,vc,up,vp are the longitudinal displacements of the top and bottom layers and w is the transverse deflection of the layers. Also, the slopes of the deflection line about x and y axes are described by θx and θy.

The displacement of any point through the thickness of the structure can be expressed as:

|  | (2) |
| --- | --- |

The potential and kinetic energy of the sandwich plate element can be then expressed as:

|  | (3) |
| --- | --- |

where V1, an V3 are the total strain energies of the top and bottom layers, respectively, while V2 represents the shear strain energy of the core layer. T1  and T3 are also the kinetic energy associated with the transverse and axial deformations in the top and bottom layers, respectively, and T2  denotes the kinetic energy due to rotational deformation of the core layer.

Considering Eq.s (1-3) and applying Hamilton’s principle, one can obtain the following eigenvalue equations describing the free-vibration of the MRE sandwich plate in the finite element form.  In this equation, K and M are the complex stiffness and mass matrixes of the sandwich plate and  is the natural frequency of the plate.

|  | (4) |
| --- | --- |

# RESULTS AND DISCUSSIONS

For the purpose of investigating the accuracy of the developed finite element model, a viscoelastic sandwich plate with the following properties is considered. Note that the plate is considered clamped at four sides.

Table 1: Mechanical properties of the clamped sandwich plate

| Top and bottom layers | Young’s modulus | 71 Gpa |
| --- | --- | --- |
|  | Poison’s ratio | 0.3 |
|  | Mass density | 2700 kg/m3 |
|  | Top layer thickness | 0.001 m |
|  | Bottom layer thickness | 0.003 m |
| Core layer | Shear modulus | 0.896 Mpa |
|  | Poison’s ratio | 0.498 |
|  | Mass density | 999 kg/m3 |
|  | Loss factor | 0.9683 |
|  | Thickness | 0.001 m |
| Structure size | Length | 0.4 m |
|  | Width | 0.4 m |

The comparison between the obtained natural frequencies and those by Huang et al. [4] is provided in Table 2 which shows an error of less than 1% for the first three modes.

Table 2: Comparison of present natural frequencies with available literature

| Natural frequencies | Present method | Huang et.al [4] | Error (%) |
| --- | --- | --- | --- |
| First | 94.18 | 95.09 | 0.95 |
| Second | 113.29 | 112.70 | 0.52 |
| Third | 186.04 | 187.25 | 0.65 |

The validated finite element model is then effectively used to investigate the effect of the applied magnetic field on the natural frequencies of the MRE sandwich plate. Results are provided in Table 3. (Note that the shear modulus of the MRE layer is a function of the applied magnetic field given in Ref. [1]).

Table 3: Effect of magnetic field on the natural frequencies

| Magnetic field (T) | Natural Frequency (HZ) |  |  |
| --- | --- | --- | --- |
|  | First | Second | Third |
| B=0 | 104.52 | 124.34 | 205.59 |
| B=0.2 | 110.94 | 131.17 | 216.87 |
| B=0.4 | 116.52 | 137.11 | 226.25 |
| B=0.6 | 118.37 | 139.09 | 229.30 |

Results clearly show the adaptability of the MRE sandwich plate whose natural frequencies increase by increasing the applied field. This is mainly due to the stiffening effect of MREs under the applied magnetic field.

# cONCLUSION

In this study, a finite element method is developed to investigate the vibration characteristics of MRE sandwich plates. 4 node rectangular elements with 28 DOFs are used to discretize the continuous MRE sandwich plate. The validated finite element model was then used to investigate the effect of the magnetic field on the vibration characteristics of the MRE sandwich plate. Results show that increasing the magnetic field leads to an increase in natural frequencies mainly due to the magnetic field stiffening of MREs.

# references

B. Nayak, S.K. Dwivedy, K.S.R.K. Murthy, Dynamic stability of magnetorheological elastomer-based adaptive sandwich beam with conductive skins using FEM and the harmonic balance method, International Journal of Mechanical Sciences, 2013, pp. 205-216,

M. Eshaghi, R. Sedaghati, and S.Rakheja ,  Dynamic characterization of partially treated MR based sandwich plate: finite element modeling and experimental study. In: Proceedings of the ASME 2014 smart materials, adaptive structures and intelligent systems, Newport, RI, 8–10 September.

J.Y. Yeh, L.W. Chen, Finite element dynamic analysis of orthotropic sandwich plates with an electrorheological fluid core layer, Composite Structures, 2007, pp. 368-376.

Z. Huang, Z. Qin, F. Chu. Vibration and damping characteristics of sandwich plates with viscoelastic core. Journal of Vibration and Control. 2016, pp. 1876-1888.