# Effect of thermal excitation mechanism on detection of subsurface defects in concrete using infrared thermography

Masoud Pedram1, Su Taylor1, Gerard Hamill1, Desmond Robinson1

1School of Natural and Built Environment, Queen’s University Belfast, Belfast, BT7 1NN

Email : mpedram01@qub.ac.uk, s.e.taylor@qub.ac.uk, g.a.hamill@qub.ac.uk, des.robinson@qub.ac.uk

ABSTRACT: Healthy bridges are the foundation of a resilient transport network and thereby are necessary for sustainable development. This paper presents the latest findings on the application of infrared thermography (IRT) as a Structural Health Monitoring (SHM) technique for diagnosing subsurface damage in the concrete elements of bridges. In this research, the effect of the thermal excitation mechanism for the purpose of subsurface defect detection was studied by comparing the test results from three heat sources, namely convection heat exchange, step-heating using an IR heater and solar irradiance. A sequence of IR images was collected for each test slab, with varying depths of subsurface defects, and the temperature record was analysed to evaluate the thermal contrast variation for each of the three heat excitation mechanisms. From the analysis of the IRT images, it was shown that the excitation mechanism affects the trend and magnitude of the temporal variation of thermal contrast. The thermal contrast variation trend with the defect's depth was nonlinear for all the thermal excitation sources. Since the thermal excitation directly correlates to the input power, these observations emphasise the importance of the input power as the parameter for further experimental and numerical studies. This corroborates optimised practical implementation of IRT for SHM of concrete bridges toward intelligent diagnostics of hidden defects and assessing the changing rate of subsurface damage regarding the safety of concrete structures.

KEY WORDS: Concrete bridge; Infrared thermography (IRT); Subsurface defect detection; Thermal excitation; Structural health monitoring (SHM).

# Introduction

Civil engineering infrastructure that supports sustainable transport, underpins our economy, and can drive towards a low carbon future.  It is essential for achievement of sustainable development goals of eradicating poverty and hunger, enhanced safety, promoting quality education, economic growth, reduced inequalities, prosperous communities and tackling climate change. Sustainable transport requires more investment in resilient bridge infrastructure network and road safety to minimise the traffic and road accidents that incurs human casualties. Therefore, continued research is required for deployment of cutting-edge technologies for the development of new solutions and refinement of the existing ones[1, 2]. In this regard, infrared thermography (IRT) is a solution for non-contact and wide-area monitoring of subsurface defects in concrete bridges’ elements such as decks, girders, soffits, abutments, and foundations [3-6] at earliest possible stage and thereby contributes to prospects of structural health monitoring (SHM). This technique has been in use since 1980s for localisation of delamination and disintegration in bridges[7].

This paper presents recent findings from experimental programme that continues and complements the studies previously presented [8]. This research highlights the effect of three different thermal excitation mechanism for detecting subsurface damage in concrete using IRT; namely, convection heat exchange, step heating using an IR heater and solar irradiance. The studies described in [8] highlights the importance of the positioning of the slabs during active IRT experiments. Therefore, the positioning of the slabs during IRT was examined in this study. A description of the methodology of experiments, and the thermal contrast results of the three excitation methods are presented here. The variation of the thermal contrasts with defect depth and thermal excitation mechanism is discussed and the IR images have been analysed to assess the trends with each variable. Based on these observations and discussions, the conclusions and the direction of future studies are outlined.

# Material and Methods

## Models and equipment

In this study, the experiments were conducted on six 250 ×250×100 mm concrete slabs. Five of these slabs had subsurface defects in the form of embedded polystyrene foam in depths of 5 to 25 mm (coded as D5 – D25) and the sixth slab was the control slab (coded as CS) with no defect. All the slabs were cast from a mix typical of the UK bridge construction industry composed of 375 kg/m3 Portland cement, 612 kg/m3 medium graded natural sand, 1137 kg/m3 coarse aggregate of maximum 10 mm diameter and 225 kg/m3 water. Therefore, all the slabs had similar thermal conductivity, diffusivity, and specific heat properties.

In these experiments a FLIR B335 thermal camera, a hand-held thermo-hygrometer, trollies, and a tripod with booming arm were used. Furthermore, an environmental chamber, and a free standing 2kW electric IR heater were used for the thermal excitation of the slabs for convection tests and IR heater tests, respectively.

## Methodology of experiments

Initially a round of preliminary arrangements was performed to identify the pixels corresponding to nine designated points on the surface of slabs for data processing purposes. In previous round of experiments using convection heat exchange, described in [8], the slabs were placed vertically during thermography. Hence, a bottom to top thermal profile was observed on the surface of slabs, and most clearly observable on the control slab. Hence, for this series of convection tests, the slabs were positioned horizontally. Likewise, for the other tests using an IR heater and solar irradiance, this positioning was preserved. All the tests were conducted with a camera to target distance of one metre and a camera to target angle of 45 degree. For all tests the IR images were recorded at 5 minutes intervals. Figure 1 shows the schematic of the test setup with three different excitation mechanisms (EM).

Figure 1. Schematic of the test setup

### IR heater tests

During the experiments, the temperature and relative humidity (RH) of test environment were measured using a hygro-thermometer, at the time of taking each IR image. The values were used as the input parameters for the IR camera software. Since the IR heater was a thermal radiation source, the background temperature was measured using a diffuse reflector test (ASTM E 1862-97). The record of reflected temperature measurement was used during thermography of samples. In this study, the IR heater tests were performed in two modes of one hour (60 minutes) and half an hour (30 minutes) heating. At the end of the planned heating period, the heater was turned off. The slabs were left to cool down through convection heat exchange in the tests room environment. After an initial analysis of temperature profile on the surface, a point was selected on the sound concrete and a point was selected on the centre of void cover for thermal contrast calculation. The thermal contrast of IR heater experiments was calculated based on equation (1). In this equation TD is the temperature on defective concrete surface and TI is the temperature on the sound concrete surface.

| ∆T=TDt-TIt | (1) |
| --- | --- |

### Convection tests

For the convection tests a range of target initial temperatures were determined and achieved by placing the slab test specimens overnight in an environmental chamber.  Target temperatures of -20, 0, 40 and 60°C, were chosen to allow the effects of positive and negative changes of temperature (warming and cooling) to be investigated. Once a sample attained the requisite target temperature, it was removed from the chamber, enclosed in the insulation box, and transferred to the thermography environment. The data collection from each slab continued about 180 minutes for the tests starting from 0, 40 and 60°C and 240 minutes for the tests starting from -20°C.

### Solar irradiance tests

Solar irradiance tests were conducted on a sunny afternoon in June 2021, when the environmental variables such as wind speed, ambient temperature, pressure, and ambient humidity were relatively consistent. A sequence of IR images was collected for experiments on each slab. The initial image of each slab was recorded when the slab was in the laboratory environment, and other images were collected after the slabs were transferred to the experiment location in the parking area of the School of Natural and Built Environment (SNBE) on the campus of Queen’s University Belfast. The reflected temperatures from sun and sky were measured using a diffuse reflector board at the start of each round of thermography, and the ambient temperature and humidity were measured before every IR image. These parameters were applied in the thermal camera’s software prior to capturing each image. These tests are explained with more details in [9].

# Results

## IR heater tests

The temporal variation of thermal contrasts for each void depth during heating and cooling stages for the thirty-minute-heating tests, are shown in Figure 2. The thermal contrast reaches a maximum value at the end of heating time.

Figure 2. Thermal contrast variation of IR heater tests, Thirty minute heating mode

## Convection tests

The variation of the average thermal contrast on the surface of slabs with time, for the heat-up test from -20°C is presented in Figure 3. In this case of heat-up tests from below freezing temperatures, a second peak is observed on the scatter charts, which corresponded to the frost thawing phenomenon in the slabs, which was also visible in images at this time increment.

Figure 3. Thermal contrast variation during a set of heat-up tests from -20°C using convection heat exchange

## Solar irradiance tests

The average and standard deviation of temperature contrasts on the surface of the slabs are presented in Figure 4. In this testing condition (specific date and time), the thermal contrast in slabs D5, D10, D15 and in the CS was clearly distinguished. The maximum thermal difference of D20 and D25 models, were almost equal. This weather condition with ambient variables, such as sunshine angle, wind speed, ambient temperature, and relative humidity, did not supply sufficient thermal energy for realisation of a significant thermal contrast difference in slabs D20 and D25.

Figure 4. Average temperature difference variation on slabs during solar irradiance tests

## Discussion of the results

The maximum thermal contrasts of the slabs with pseudo subsurface defects with respect to the three different thermal excitation mechanisms are given in Table 1.

Table 1. Maximum absolute thermal contrast comparison

| Slab code |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Thermal excitation mechanism | D05 | D10 | D15 | D20 | D25 |
| IR heater (60 minutes heating) | 15.1 | 9.3 | 7.2 | 5.5 | 4.1 |
| IR heater (30 minutes heating) | 14.1 | 7.9 | 5.9 | 3.9 | 2.6 |
| Convection heat-up from IT=0°C | 3.6 | 2.0 | 1.5 | 1.1 | 0.9 |
| Convection cool-down from IT=40°C | 3.9 | 2.2 | 1.9 | 1.45 | 0.9 |
| Convection heat-up from IT=-20°C | 8.0 | 5.0 | 3.73 | 2.6 | 1.7 |
| Convection cool-down from IT=60°C | 7.04 | 4.9 | 3.6 | 2.8 | 2.33 |
| Solar irradiance heating (29/06/2021) | 7.6 | 5.3 | 4.2 | 2.4 | 2.4 |

The variation of maximum absolute thermal contrasts with the defect depth for three thermal excitation mechanisms is also presented in Figure 5. This figure shows that the variation of thermal contrasts with defect depth follows a nonlinear trend, presented as power function, embedded in the legend of this figure, irrespective of the thermal excitation method.

According to Figure 5, the excitation mechanism affects the magnitude of thermal contrast directly. That is, step heating tests with IR heater of 2kW for 30 and 60 minutes, causes a maximum thermal contrast higher than maximum thermal contrast caused by convection heat exchange and solar irradiance (for that specific day in Belfast, Northern Ireland). Moreover, solar irradiance test, for that day, caused a thermal difference almost equal to the contrast of convection tests with 40°C temperature range, which is almost two times higher than the contrast caused by 20°C temperature range.

Figure 5. Variation of maximum thermal contrast (°C) with depth of defect and thermal excitation mechanism

The Figure 6 presents and compares the snapshots of the D5 slab at maximum thermal contrast for the three excitation mechanisms. The Figure 7 shows the snapshots of the D25 slab at maximum contrast for the three excitation mechanisms. The comparison of Figure 6 and Figure 7, shows that there is a significant difference between the contrast of slabs depending on the depth of defect and the excitation mechanism.

| a) IR heater | b) Convection | c)Solar irradiance |
| --- | --- | --- |
| Figure 6. IR snapshots of D5 slab at maximum contrast |  |  |

| a) IR heater | b) Convection | c)Solar irradiance |
| --- | --- | --- |
| Figure 7. IR snapshots of D25 slab at maximum contrast |  |  |

# Conclusions

This paper presents the latest findings of research on the effect of thermal excitation sources for the detection of sub surface defects at various depths in concrete using IRT. For this purpose, three different thermal excitation methods; namely, convection heat exchange, step heating using an IR heater and solar irradiance heating, were compared. The thermal contrasts and the derivatives of thermal contrasts on surface were analysed. This analysis showed that the trend of thermal contrasts is dependent upon the defect depth and the magnitude of this depends on heat excitation source. Owing to the variation in the amount of input heat power in the thermal excitation sources, the input power will be considered as the variable for the future research. This will also be investigated by numerical analysis to promote the practical implementation of IRT for damage detection in concrete bridges and structures.

# ACKNOWLEDGMENTS

This paper presents results from postgraduate research

supported by the Engineering and Physical Sciences Research Council (EPSRC) in collaboration with USA-Ireland funded project ‘Mobile Automated Rovers Fly-By (MARS-FLY) for Bridge Network Resiliency’ and thanks to DfE who supported the NI part of the research.

# References

[1].United Nations. Sustainable transport, Sustainable development, in Interagency report for second Global Sustainable Transport Conference 2021.

[2].United Nations. The 17 goals. 2022; Available from: https://sdgs.un.org/goals.

[3].Kashif Ur Rehman, S., Z. Ibrahim, S.A. Memon, and M. Jameel, Nondestructive test methods for concrete bridges: A review. Construction and Building Materials, 2016. 107: p. 58-86.DOI: https://doi.org/10.1016/j.conbuildmat.2015.12.011.

[4].Vaghefi, K., T.M. Ahlborn, D.K. Harris, and C.N. Brooks, Combined Imaging Technologies for Concrete Bridge Deck Condition Assessment. Journal of Performance of Constructed Facilities, 2013. 29(4): p. 04014102-04014102.DOI: 10.1061/(asce)cf.1943-5509.0000465.

[5].Hiasa, S., R. Birgul, M. Matsumoto, and F. Necati Catbas, Experimental and numerical studies for suitable infrared thermography implementation on concrete bridge decks. Measurement: Journal of the International Measurement Confederation, 2018. 121.DOI: 10.1016/j.measurement.2018.02.019.

[6].Raja, B.N.K., et al., The influence of ambient environmental conditions in detecting bridge concrete deck delamination using infrared thermography (IRT). Structural Control & Health Monitoring, 2020. 27(4).DOI: https://doi.org/10.1002/stc.2506.

[7].Watase, A., et al., Practical identification of favorable time windows for infrared thermography for concrete bridge evaluation. Construction and Building Materials, 2015. 101: p. 1016-1030.DOI: https://doi.org/10.1016/j.conbuildmat.2015.10.156.

[8].Pedram, M., et al., Experimental investigation of subsurface defect detection in concretes by infrared thermography and convection heat exchange. Journal of Civil Structural Health Monitoring, 2022.DOI: 10.1007/s13349-022-00550-y.

[9].Pedram, M., S. Taylor, G. Hamill, and D. Robinson, Subsurface defect detection in concretes by active infrared thermography, in IABSE Symposium: Challenges for Existing and Oncoming Structures. 2022: Prague, Czech Republic. p. 431-436.