## Slide 1: Axial-Flexural Interaction for FRP-Confined Reinforced Masonry Columns
Khalid Saqer Alotaibi
Belal AbdelRahman
Khaled Galal
Imam Abdulrahman Bin Faisal University
Concordia University

## Slide 2: Introduction
Masonry has been used as a structural material in modern or historical building construction across the world, due to:
Its durability
Economy
Its resistance to fire

## Slide 3: Introduction
FRP Composite Materials offers robust characteristics such as:
High strength and high stiffness-to-weight ratio.
Excellent corrosion resistance.
Ease of application.
Fiber Reinforced Polymer (FRP) sheet
FRP Jacketing of Masonry Columns

## Slide 4: Objective
Proposing a simplified analytical methodology to compute the axial load-moment interaction diagram of prismatic fully grouted reinforced concrete masonry columns confined with FRP jacket and controlled by compression failure.
Proposing practical values for the equivalent rectangular stress block parameters.
Comparing experimental results and theoretical predictions obtained by the proposed methodology.

## Slide 5: Scope of Work
Chart: Bending moment M (kN.m)
| 0
 | 0
β
c
ε
mu
c
ε
si
ε
si
N
.
A
.

## Slide 6: Scope of Work
Chart: Bending moment M (kN.m)
| 0
 | 0
Chart: Bending moment M (kN.m)

## Slide 7: Scope of Work
Chart: Bending moment M (kN.m)
After Strengthening | 2661.7548 | 1743.8936 | 1701.7639 | 1659.0253 | 1615.6339 | 1571.5414 | 1526.6948 | 1481.0354 | 1434.4984 | 1387.0119 | 1346.7694 | 1297.1346 | 1246.2813 | 1194.0973 | 1140.4563 | 1085.2155 | 1028.2128 | 969.2634 | 908.1559 | 844.6469 | 778.4552 | 709.2536 | 0
β
c
ε
mcu
c
ε
si
ε
si
N
.
A
.

## Slide 8: Test Matrix of Experimental Work
Group | Test configuration | Number of tested columns | Test eccentricity (mm)
1 | L1-e0 | 3 | 0
 | L1-e20 | 3 | 20
 | L1-e40 | 3 | 40
2 | L2-e0 | 3 | 0
 | L2-e20 | 3 | 20
 | L2-e40 | 3 | 40
The primary variables in experimental tests are:
The number of FRP layers
The loading method

## Slide 9: Columns construction and preparation
18 half-scale fully grouted reinforced concrete masonry columns were constructed.

## Slide 10: Test setup and instrumentation
Load
Spherical head
Wrapped or
unwrapped
masonry column
Strong floor
Upper
&
lower
bearing platens
4
Displacement
sensors
2
Displacement
sensors at
compression face
Wrapped or
unwrapped
masonry column
2
Displacement
sensors at
tension face
Loading heads
Displacement
sensor
B
Eccentric loading
A
Concentric loading
Load
Load

## Slide 11: Predicting the strength gain
The refined CNR-DT 200 R1 theoretical model gave a good prediction of the strength gain of FRP confined concrete masonry.
The refined CNR-DT 200 R1 theoretical model is tested against reinforced concrete masonry columns.

## Slide 12: Predicting the strength gain
Comparing the theoretical predictions to the experimental data
0
5
10
15
20
25
0.000
0.005
0.010
0.015
0.020
Stress (MPa)
Axial strain (mm/mm)
L2-e0-1
L2-e0-2
L2-e0-3
Average
0
5
10
15
20
25
0.000
0.005
0.010
0.015
0.020
Stress (MPa)
Axial strain (mm/mm)
L1-e0-1
L1-e0-2
L1-e0-3
Average

## Slide 13: Predicting the strength gain
Comparing the theoretical predictions to the experimental data
0.0026
(mm/mm),
22.39
(MPa)
0
5
10
15
20
25
0.000
0.005
0.010
0.015
0.020
Stress (MPa)
Axial strain (mm/mm)
L2 - with steel
contribution
0.0026
(mm/mm),
15.75
(MPa)
L2 - without steel
contribution
0.0027
(mm/mm),
21.51
(MPa)
0
5
10
15
20
25
0.000
0.005
0.010
0.015
0.020
Stress (MPa)
Axial strain (mm/mm)
L1 - with steel
contribution
0.0027
(mm/mm),
14.80
(MPa)
L1 - without steel
contribution

## Slide 14: Predicting the strength gain
Comparing the theoretical predictions to the experimental data
Column | Experimental value (MPa) | CNR-DT 200 R1/2013 prediction (MPa) | Absolute error (%)
L1-e0 | 14.80 | 14.51 | 1.9
L2-e0 | 15.75 | 15.99 | 1.5

## Slide 15: Predicting ultimate strain gain
0.5
1.0
1.5
2.0
2.5
0.00
0.02
0.04
0.06
0.08

## Slide 16: Equivalent stress block parameters
β
c
ε
mcu
c
ε
si
ε
si
N
.
A
.

## Slide 17: Equivalent stress block parameters
An approach can be developed to account for strain gradient by calibrating the force and moment equilibriums in the confined section for each eccentrically tested column by changing the parameters and the neutral axis depth .

## Slide 18: Equivalent stress block parameters
columns | (MPa) | (mm) |  | Average (St. Dev.) |  | Average (St. Dev.) | 
L1 | 14.80 | 0.381 | 0.72 | 0.81 (0.12) | 0.80 | 0.78 (0.02) | 175.2
 |  |  | 0.94 |  | 0.80 |  | 175.0
 |  |  | 0.78 |  | 0.78 |  | 177.5
 |  |  | 0.68 |  | 0.78 |  | 139.2
 |  |  | 0.91 |  | 0.75 |  | 139.0
L2 | 15.75 | 0.762 | 0.89 | 0.82 (0.06) | 0.83 | 0.82 (0.02) | 172.2
 |  |  | 0.88 |  | 0.79 |  | 175.3
 |  |  | 0.81 |  | 0.81 |  | 133.3
 |  |  | 0.77 |  | 0.82 |  | 132.9
 |  |  | 0.78 |  | 0.82 |  | 133.9
Selected value |  |  |  | 0.80 |  | 0.80 | 
columns |  |  |  | Average (St. Dev.) |  | Average (St. Dev.) | 
L1 | 14.80 | 0.381 | 0.72 | 0.81 (0.12) | 0.80 | 0.78 (0.02) | 175.2
 |  |  | 0.94 |  | 0.80 |  | 175.0
 |  |  | 0.78 |  | 0.78 |  | 177.5
 |  |  | 0.68 |  | 0.78 |  | 139.2
 |  |  | 0.91 |  | 0.75 |  | 139.0
L2 | 15.75 | 0.762 | 0.89 | 0.82 (0.06) | 0.83 | 0.82 (0.02) | 172.2
 |  |  | 0.88 |  | 0.79 |  | 175.3
 |  |  | 0.81 |  | 0.81 |  | 133.3
 |  |  | 0.77 |  | 0.82 |  | 132.9
 |  |  | 0.78 |  | 0.82 |  | 133.9
Selected value |  |  |  | 0.80 |  | 0.80 | 

## Slide 19: Proposed design methodology
The proposed design methodology only addresses the compression-controlled region.
The compressive strength can be determined by the refined CNR-DT 200 R1 confinement model
The ultimate strain () is calculated by:

## Slide 20: Proposed design methodology
The pure nominal axial strength, point A, can be calculated by
The axial load and moment capacities at points B and C can be found by

## Slide 21: Proposed design methodology
The values of parameters α and β are 0.80
The depth of neutral axis c for the points B and C can be determined by

## Slide 22: Accuracy of the proposed design methodology
Chart: L1
| 0 | 9.594315806315791 | 10.306247247567567 | 10.995485759999998 | 11.663110948571429 | 12.310329430588236 | 12.93849408 | 13.549126880000001 | 14.143946198709678 | 14.724899520000001 | 15.294202946206898 | 15.710635693714286 | 16.264612608 | 16.815735487999998 | 17.367896448 | 17.925636288 | 18.494285512347826 | 19.080143807999999 | 19.690710802285711 | 20.260310528000002 | 20.673481273263157 | 20.823075369798349 | 0
theo | 765.5673 | 511.31 | 497.7646 | 483.9569 | 469.8642 | 455.4616 | 440.7207 | 425.6098 | 410.0933 | 394.1304 | 377.6751 | 363.6694 | 346.063 | 327.781 | 308.7421 | 288.8518 | 267.9991 | 246.0526 | 222.8563 | 196.6667 | 164.6247 | 152.896 | 0
exp | 759.0648 | 814.0032 | 777.3776 | 446.3741 | 531.9863 | 469.265 | 321.3893 | 382.7372
Chart: L1
| 0 | 9.594315806315791 | 10.306247247567567 | 10.995485759999998 | 11.663110948571429 | 12.310329430588236 | 12.93849408 | 13.549126880000001 | 14.143946198709678 | 14.724899520000001 | 15.294202946206898 | 15.710635693714286 | 16.264612608 | 16.815735487999998 | 17.367896448 | 17.925636288 | 18.494285512347826 | 19.080143807999999 | 19.690710802285711 | 20.260310528000002 | 20.673481273263157 | 20.823075369798349 | 0
theo | 765.5673 | 511.31 | 497.7646 | 483.9569 | 469.8642 | 455.4616 | 440.7207 | 425.6098 | 410.0933 | 394.1304 | 377.6751 | 363.6694 | 346.063 | 327.781 | 308.7421 | 288.8518 | 267.9991 | 246.0526 | 222.8563 | 196.6667 | 164.6247 | 152.896 | 0
exp | 759.0648 | 814.0032 | 777.3776 | 446.3741 | 531.9863 | 469.265 | 321.3893 | 382.7372
Chart: L2
| 0 | 9.9989274442105263 | 10.780502711351351 | 11.536905280000003 | 12.269310720000002 | 12.979032903529413 | 13.667544960000003 | 14.336504160000002 | 14.987781615483872 | 15.623497920000004 | 16.246066162758623 | 16.699828032000003 | 17.304782165333336 | 17.906165951999998 | 18.508217471999998 | 19.115881152000004 | 19.734961318956525 | 20.372317632000001 | 21.036116352000001 | 21.736156992000002 | 22.332267384222487 | 0
theo | 818.2316 | 549.9987 | 535.1336 | 519.9829 | 504.5219 | 488.7233 | 472.5564 | 455.9868 | 438.9753 | 421.4779 | 403.4442 | 388.1172 | 368.8301 | 348.8073 | 327.9604 | 306.1865 | 283.3645 | 259.3516 | 233.9777 | 207.0386 | 184.1156 | 0
exp | 861.62 | 819.5 | 762.73 | 540.23 | 527.87 | 629.5 | 366.71 | 352.52 | 359.85
Chart: L2
| 0 | 9.9989274442105263 | 10.780502711351351 | 11.536905280000003 | 12.269310720000002 | 12.979032903529413 | 13.667544960000003 | 14.336504160000002 | 14.987781615483872 | 15.623497920000004 | 16.246066162758623 | 16.699828032000003 | 17.304782165333336 | 17.906165951999998 | 18.508217471999998 | 19.115881152000004 | 19.734961318956525 | 20.372317632000001 | 21.036116352000001 | 21.736156992000002 | 22.332267384222487 | 0
theo | 818.2316 | 549.9987 | 535.1336 | 519.9829 | 504.5219 | 488.7233 | 472.5564 | 455.9868 | 438.9753 | 421.4779 | 403.4442 | 388.1172 | 368.8301 | 348.8073 | 327.9604 | 306.1865 | 283.3645 | 259.3516 | 233.9777 | 207.0386 | 184.1156 | 0
exp | 861.62 | 819.5 | 762.73 | 540.23 | 527.87 | 629.5 | 366.71 | 352.52 | 359.85
3

## Slide 23: Conclusions
The simplified methodology that predicts the axial load-moment interaction diagram of fully grouted reinforced concrete masonry column strengthened with FRP jackets provides a good correlation with experimental tests.

## Slide 24
Thank YOU