ARIZONA SPS-10 PROJECT: I-40 SUN VALLEY

(04AAXX)

# MATERIALS SAMPLING AND TESTING PLAN

Contents

GENERAL LAYOUT INFORMATION	2

MATERIALS SAMPLING AND FIELD TESTING	6

LABORATORY MATERIALS TESTING	31

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Arizona SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers and indicates transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Exact station numbering in Table 2 will remain incomplete until more information is provided regarding exact test section locations. Additionally, Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION

| Section Number | SHRP ID | Description |
| --- | --- | --- |
| AA01 | 04AA01 | HMA Control Section with 20% RAP and PG 70-22 |
| AA02 | 04AA02 | WMA – Foaming Process with 20% RAP and PG 70-22 |
| AA03 | 04AA03 | WMA – Evotherm with 20% RAP and PG 70-22 |
| AA59 | 04AA59 | HMA Control Section with 30% RAP and PG 70-22 |
| AA60 | 04AA60 | WMA – Foaming Process with 30% RAP and PG 70-22 |
| AA61 | 04AA61 | WMA – Evotherm with 30% RAP and PG 70-22 |

TABLE 2: TEST SECTION LAYOUT

| Begin STA | End STA | Description | Section ID |
| --- | --- | --- | --- |
| 2238+11 |  | Transition | 04AA01 |
|  |  | Sampling Area |  |
|  |  | Buffer Area |  |
|  |  | Monitoring Area |  |
|  |  | Buffer Area |  |
|  |  | Sampling Area |  |
|  | 2246+56 | Transition |  |
| 2246+56 |  | Transition | 04AA02 |
|  |  | Sampling Area |  |
|  |  | Buffer Area |  |
|  |  | Monitoring Area |  |
|  |  | Buffer Area |  |
|  |  | Sampling Area |  |
|  | 2262+93 | Transition |  |
| 2262+93 |  | Transition | 04AA03 |
|  |  | Sampling Area |  |
|  |  | Buffer Area |  |
|  |  | Monitoring Area |  |
|  |  | Buffer Area |  |
|  |  | Sampling Area |  |
|  | 2279+30 | Transition |  |
| 2279+30 |  | Transition | 04AA59 |
|  |  | Sampling Area |  |
|  |  | Buffer Area |  |
|  |  | Monitoring Area |  |
|  |  | Buffer Area |  |
|  |  | Sampling Area |  |
|  | 2295+67 | Transition |  |
| 2295+67 |  | Transition | 04AA60 |
|  |  | Sampling Area |  |
|  |  | Buffer Area |  |
|  |  | Monitoring Area |  |
|  |  | Buffer Area |  |
|  |  | Sampling Area |  |
|  | 2312+04 | Transition |  |

| Begin STA | End STA | Description | Section ID |
| --- | --- | --- | --- |
| 2312+04 |  | Transition | 04AA61 |
|  |  | Sampling Area |  |
|  |  | Buffer Area |  |
|  |  | Monitoring Area |  |
|  |  | Buffer Area |  |
|  |  | Sampling Area |  |
|  | 2328+41 | Transition |  |

AC Mix 3

AC Mix 2

AC Mix 1

Buffer Area (50 ft)

04AA01

HMA Control section with PG 70-22 and 20% RAP

Buffer Area (50 ft)

Sampling Area 2 (100 ft)

Transition zone (ft)

04AA02

WMA Foaming Process and 20% RAP

04AA03

WMA with Evotherm and 20% RAP

Transition zone (ft)

Transition zone (ft)

Sampling Area 4 (100 ft)

Buffer Area (50 ft)

Sampling Area 3 (100 ft)

Buffer Area (50 ft)

Buffer Area (50 ft)

Sampling Area 5 (100 ft)

Buffer Area (50 ft)

Sampling Area 6 (100 ft)

Transition zone (ft)

Sampling Area 1 (100 ft)

Transition zone (ft)

Transition zone (ft)

800 ft

800 ft

800 ft

Match Line

Direction of Traffic (EB)

2262+93

2246+56

2279+30

2238+11

AC Mix 4

AC Mix 6

AC Mix 5

Sampling Area 11 (100 ft)

Buffer Area (50 ft)

04AA61

WMA Supplemental section 3 with Evotherm with 30% RAP

Transition zone (150 ft)

04AA60

WMA Supplemental Section 2 with Foaming Process and 30% RAP

Buffer Area (50 ft)

04AA59

Supplemental Section 1: HMA Control with 30% RAP

Sampling Area 7 (100 ft)

Transition zone (150 ft)

Buffer Area (50 ft)

Sampling Area 8 (100 ft)

Transition zone (1050 ft)

Buffer Area (50 ft)

Sampling Area 9 (100 ft)

Buffer Area (50 ft)

Sampling Area 10 (100 ft)

Transition zone (1050 ft)

Transition zone (150 ft)

Buffer Area (50 ft)

Sampling Area 12 (100 ft)

800 ft

800 ft

800 ft

Transition zone (1050 ft)

Match Line

Direction of Traffic (EB)

2279+30

2312+04

2295+67

2328+41

FIGURE 1: ARIZONA SPS-10 PROJECT LAYOUT

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at time zero (t0 is at time of construction).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 2 through 15 show the locations for the many samples and tests scheduled.  Figures 2 through 7 show the material sampling locations for each section as well as the location of DCP testing and Figures 8 through 13 show density measurement layouts.

Tables 6 through 12 list the samples acquired from each of the six test sections as well as the asphalt plant.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 13 through 15 list samples to be shipped to the central lab testing contractor laboratory, the LTPP Materials Reference Library (MRL), and the Turner-Fairbank Highway Research Center, respectively.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Arizona SPS-10, R = “W,” representing western region)

- C = Construction event (For Arizona SPS-10, C = 5 for 04AAXX , representing the fifth constructed SPS-10)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 59

  - B – 60

  - C – 61

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C –6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

The layer numbering system was applied for each of the seven sections. Based on data provided by the Arizona State DOT, the sublayers were considered for each of the six sections and categorized and numbered as outlined in the tables below.

The reported layers and layer numbering for all six test sections in 04AAxx are given in Table 3 below. The sublayers for all sections are identical with only the overlay layer differentiating each.

TABLE 3: LAYER NUMBERING FOR ALL 04AAXX SECTIONS

| Test section | Layer number | Project Layer code | Layer thickness (in) * | Material code | Year built | Material Description |
| --- | --- | --- | --- | --- | --- | --- |
| 04AA01 | 6 | F | 4 | 01 | 2016 | HMA Overlay with 20% RAP |
|  | 5 | E | 0.5 | 85 |  | AR-ACFC |
|  | 4 | D | 12-14 | 01 | 1996 | AC & ARAC |
|  | 3 | C | 3.5 | 22 |  | Aggregate Base |
|  | 2 | B | 3-14 |  |  | Select Material (Subbase) |
|  | 1 | A |  |  |  | Subgrade |
| 04AA02 | 6 | G | 4 | 91 | 2016 | WMA Overlay with 20% RAP |
|  | 5 | E | 0.5 | 85 |  | AR-ACFC |
|  | 4 | D | 12-14 | 01 | 1996 | AC & ARAC |
|  | 3 | C | 3.5 | 22 |  | Aggregate Base |
|  | 2 | B | 3-14 |  |  | Select Material (Subbase) |
|  | 1 | A |  |  |  | Subgrade |
| 04AA03 | 6 | H | 4 | 91 | 2016 | WMA Overlay with 20% RAP |
|  | 5 | E | 0.5 | 85 |  | AR-ACFC |
|  | 4 | D | 12-14 | 01 | 1996 | AC & ARAC |
|  | 3 | C | 3.5 | 22 |  | Aggregate Base |
|  | 2 | B | 3-14 |  |  | Select Material (Subbase) |
|  | 1 | A |  |  |  | Subgrade |
| 04AA59 | 6 | I | 4 | 01 | 2016 | HMA Overlay with 30% RAP |
|  | 5 | E | 0.5 | 85 |  | AR-ACFC |
|  | 4 | D | 12-14 | 01 | 1996 | AC & ARAC |
|  | 3 | C | 3.5 | 22 |  | Aggregate Base |
|  | 2 | B | 3-14 |  |  | Select Material (Subbase) |
|  | 1 | A |  |  |  | Subgrade |
| 04AA60 | 6 | J | 4 | 91 | 2016 | WMA Overlay with 30% RAP |
|  | 5 | E | 0.5 | 85 |  | AR-ACFC |
|  | 4 | D | 12-14 | 01 | 1996 | AC & ARAC |
|  | 3 | C | 3.5 | 22 |  | Aggregate Base |
|  | 2 | B | 3-14 |  |  | Select Material (Subbase) |
|  | 1 | A |  |  |  | Subgrade |
| 04AA61 | 6 | K | 4 | 91 | 2016 | WMA Overlay with 30% RAP |
|  | 5 | E | 0.5 | 85 |  | AR-ACFC |
|  | 4 | D | 12-14 | 01 | 1996 | AC & ARAC |
|  | 3 | C | 3.5 | 22 |  | Aggregate Base |
|  | 2 | B | 3-14 |  |  | Select Material (Subbase) |
|  | 1 | A |  |  |  | Subgrade |

(*) Reported from nomination forms

Construction station: 2239+11

0-68

0-67

0-66

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-70

0-50

Section STA:

Shoulder

C02001

2’

1’

3’

C01001

C03001

2’

C04001

C05001

C07001

C09001

C11001

C13001

C06001

C08001

C10001

C12001

C14001

3’

A01001

A02001

DCP

Key

12” Core

6” Core

Experimental AC sample only

Experimental AC and existing AC

Experimental AC , existing AC, aggregate base, subbase, and subgrade

2’

Alternative or additional locations for subgrade, subbase, and base bulk samples only

FIGURE 2: ARIZONA SPS-10 PROJECT LAYOUT FOR SECTION 04AA01

Construction station: 2255+11

0-50

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-67

0-70

0-66

0-68

Section STA:

Shoulder

C02002

2’

1’

3’

C01002

C03002

2’

C04002

C05002

C07002

C09002

C11002

C13002

C06002

C08002

C10002

C12002

C14002

3’

A01002

A02002

DCP

Key

12” Core

6” Core

Experimental AC sample only

Experimental AC, existing AC

FIGURE 3: ARIZONA SPS-10 PROJECT LAYOUT FOR SECTION 04AA02

Construction station: 2271+11

0-50

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-67

0-70

0-66

0-68

Section STA:

Shoulder

C02003

2’

1’

3’

C01003

C03003

2’

C04003

C05003

C07003

C09003

C11003

C13003

C06003

C08003

C10003

C12003

C14003

3’

A01003

A02003

DCP

Key

12” Core

6” Core

Experimental AC sample only

Experimental AC and existing AC

FIGURE 4: ARIZONA SPS-10 PROJECT LAYOUT FOR SECTION 04AA03

Construction station: 2287+11

0-50

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-67

0-70

0-66

0-68

Section STA:

Shoulder

C02059

2’

1’

3’

C01059

C03059

2’

C04059

C05059

C07059

C09059

C11059

C13059

C06059

C08059

C10059

C12059

C14059

3’

A01059

A02059

DCP

Key

12” Core

6” Core

Experimental AC sample only

Experimental AC and existing AC

FIGURE 5: ARIZONA SPS-10 PROJECT LAYOUT FOR SECTION 04AA59

Construction station: 2303+11

0-68

0-66

0-70

0-67

0-65

0-64

0-63

0-62

0-61

0-60

0-59

0-50

0-55

0-56

0-57

0-58

Section STA:

Shoulder

C02060

2’

1’

3’

C01060

C03060

2’

C04060

C05060

C07060

C09060

C11060

C13060

C06060

C08060

C10060

C12060

C14060

3’

A01060

A02060

DCP

Key

12” Core

6” Core

Experimental AC sample only

Experimental AC and existing AC

FIGURE 6: ARIZONA SPS-10 PROJECT LAYOUT FOR SECTION 04AA60

Construction station: 2319+11

0-68

0-66

0-70

0-67

0-65

0-64

0-63

0-62

0-61

0-60

0-59

0-58

0-57

0-56

0-55

0-50

Section STA:

Shoulder

C02061

2’

1’

3’

C01061

C03061

2’

C04061

C05061

C07061

C09061

C11061

C13061

C06061

C08061

C10061

C12061

C14061

3’

A01061

A02061

DCP

Key

12” Core

6” Core

Experimental AC sample only

Experimental AC, existing AC, aggregate base, subbase, and subgrade sample

Alternative or additional locations for subgrade, subbase, and base bulk samples only

Experimental AC and existing AC

FIGURE 7: ARIZONA SPS-10 PROJECT LAYOUT FOR SECTION 04AA61

Section 04AA01 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T01001

T02001

T03001

Traffic

FIGURE 8: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 04AA01 ARIZONA SPS-10

Section 04AA02 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T01002

T02002

T03002

Traffic

FIGURE 9: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 04AA02 ARIZONA SPS-10

Section 04AA03 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T01003

T02003

T03003

Traffic

FIGURE 10: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 04AA03 ARIZONA SPS-10

Section 04AA59 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T01059

T02059

T03059

Traffic

FIGURE 11: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 04AA59 ARIZONA SPS-10

Section 04AA60 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T01060

T02060

T03060

Traffic

FIGURE 12: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 04AA60 ARIZONA SPS-10

Section 04AA61 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T01061

T02061

T03061

Traffic

FIGURE 13: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 04AA61 ARIZONA SPS-10

TABLE 4: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
|  | DURING CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 5-gallon buckets uncompacted AC mix | 90 | F01001, F01002, F01003, F01059, F01060, F01061 |
|  | 1-gallon can virgin AC Binder (PG 70-22) | 10 | H01001 |
|  | 5-gallon bucket combined aggregate with 20% RAP | 20 | H02001 |
|  | 5-gallon bucket combined aggregate with 30% RAP | 20 | H02001 |
|  | 50 lb bulk sample RAP | 1 | H04001 |
|  | 5-gallon buckets RAP | 10 | H04001 |
|  | 1-gallon chemical additive (Evotherm) | 3 | H01003 |
|  | POST-CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 12" Core | 12 | A01001-A02001, A01002-A02002, A01003-A02003, A01059-A02059, A01060-A02060, A01061-A02061 |
|  | 6" Core | 84 | C01001-C14001, C01002-C14002, C01003-C14003, C01059-C14059, C01060-C14060, C01061-C14061 |
| B. | ORIGINAL HMAC |  |  |
|  | 12" Core | 2 | A01001-A02001, A01061-A02061 |
|  | 6" Core | 5 | C01002, C01003, C01059, C01060, C01061 |
| E. | SUBGRADE |  |  |
|  | 150 lb bulk sample | 2 | A01001-A02001, A01061-A02061 |
|  | Moisture content jar sample | 2 | A01001-A02001, A01061-A02061 |

TABLE 5: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | PRE-CONSTRUCTION TESTING |  |  |
| A. | ORIGINAL HMAC |  |  |
|  | Elevation Survey | 6 | All Sections |
|  | POST-CONSTRUCTION TESTING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Elevation Survey | 6 | All Sections |
|  | In situ density measurement | 18 | T01001-T03001, T01002-T03002, T01003-T03003, T01059 -T03059, T01060-T03060, T01061 -T03061 |
|  | Core Examination and Thickness (P01/AC01) | 96 | C01001-C14001, C01002-C14002, C01003-C14003, C01059-C14059, C01060-C14060, C01061-C14061, C01062-C14062, A01001-A02001, A01002-A02002, A01003-A02003, A01059-A02059, A01060-A02060, A01061-A02061 |
| B. | ORIGINAL HMAC |  |  |
|  | Core Examination and Thickness | 7 | A01001, A01061, C01002, C01003, C01059, C01060, C01061 |
| C. | AGGREGATE BASE |  |  |
|  | DCP | 6 | A01001, C01002, C01003, C01059, C01060, C01061 |
| D. | SOIL-AGGREGATE MIX (UNBOUND BASE) |  |  |
|  | DCP | 6 | A01001, C01002, C01003, C01059, C01060, C01061 |
| E. | SUBGRADE |  |  |
|  | DCP | 6 | A01001, C01002, C01003, C01059, C01060, C01061 |

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 04AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01001 | 5 | BA01001 | W51A01L05 | 12" Core |
|  | 4 | BA03001 | W51A01L04 | 12" Core |
|  | 3 | BA05001 | W51A01L03 | 12" Core |
| A02001 | 5 | BA020 01 | W51A02L05 | 12" Core |
|  | 4 | BA04001 | W51A02L04 | 12" Core |
|  | 3 | BA06001 | W51A02L03 | 12" Core |
| A01001, A02001 | 3 | BG01001 | W51A01L01 | 150 lb Bulk Sample |
|  | 2 | BG02001 | W51A03L02 | 150 lb Bulk Sample |
|  | 1 | BS01001 | W51A03L01 | 150 lb Bulk Sample (combination of samples from loc A01001 and A02001) |
|  | 1 | MS01001 | W51A03W01 | Moisture content jar sample |
| C01001 | 5 | CA01001 | W51C01L05 | 6" Core |
| C02001 | 5 | CA02001 | W51C02L05 | 6" Core |
| C03001 | 5 | CA03001 | W51C03L05 | 6" Core |
| C04001 | 5 | CA04001 | W51C04L05 | 6" Core |
| C05001 | 5 | CA05001 | W51C05L05 | 6" Core |
| C06001 | 5 | CA06001 | W51C06L05 | 6" Core |
| C07001 | 5 | CA07001 | W51C07L05 | 6" Core |
| C08001 | 5 | CA08001 | W51C08L05 | 6" Core |
| C09001 | 5 | CA09001 | W51C09L05 | 6" Core |
| C10001 | 5 | CA10001 | W51C10L05 | 6" Core |
| C11001 | 5 | CA11001 | W51C11L05 | 6" Core |
| C12001 | 5 | CA12001 | W51C12L05 | 6" Core |
| C13001 | 5 | CA13001 | W51C13L05 | 6" Core |
| C14001 | 5 | CA14001 | W51C14L05 | 6" Core |
| F01001 | 5 | BA09001 | W51F01L05 | 15 5-gallon buckets uncompacted AC mix |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 04AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01002 | 5 | BA01002 | W52A01L05 | 12" Core |
| A02002 | 5 | BA02002 | W52A01L05 | 12" Core |
| C01002 | 5 | CA01002 | W52C01L05 | 6" Core |
|  | 4 | CA15002 | W52C01L04 | 6" Core |
|  | 3 | CA16002 | W52C01L03 | 6" Core |
| C02002 | 5 | CA02002 | W52C02L05 | 6" Core |
| C03002 | 5 | CA03002 | W52C03L05 | 6" Core |
| C04002 | 5 | CA04002 | W52C04L05 | 6" Core |
| C05002 | 5 | CA05002 | W52C05L05 | 6" Core |
| C06002 | 5 | CA06002 | W52C06L05 | 6" Core |
| C07002 | 5 | CA07002 | W52C07L05 | 6" Core |
| C08002 | 5 | CA08002 | W52C08L05 | 6" Core |
| C09002 | 5 | CA09002 | W52C09L05 | 6" Core |
| C10002 | 5 | CA10002 | W52C10L05 | 6" Core |
| C11002 | 5 | CA11002 | W52C11L05 | 6" Core |
| C12002 | 5 | CA12002 | W52C12L05 | 6" Core |
| C13002 | 5 | CA13002 | W52C13L05 | 6" Core |
| C14002 | 5 | CA14002 | W52C14L05 | 6" Core |
| F01002 | 5 | BA06002 | W52F01L05 | 15 5-gallon buckets uncompacted AC mix |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 04AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01003 | 5 | BA01003 | W53A01L05 | 12" Core |
| A02003 | 5 | BA02003 | W53A01L05 | 12" Core |
| C01003 | 5 | CA01003 | W53C01L05 | 6" Core |
|  | 4 | CA15003 | W53C01L04 | 6" Core |
|  | 3 | CA16003 | W53C01L03 | 6" Core |
| C02003 | 5 | CA02003 | W53C02L05 | 6" Core |
| C03003 | 5 | CA03003 | W53C03L05 | 6" Core |
| C04003 | 5 | CA04003 | W53C04L05 | 6" Core |
| C05003 | 5 | CA05003 | W53C05L05 | 6" Core |
| C06003 | 5 | CA06003 | W53C06L05 | 6" Core |
| C07003 | 5 | CA07003 | W53C07L05 | 6" Core |
| C08003 | 5 | CA08003 | W53C08L05 | 6" Core |
| C09003 | 5 | CA09003 | W53C09L05 | 6" Core |
| C10003 | 5 | CA10003 | W53C10L05 | 6" Core |
| C11003 | 5 | CA11003 | W53C11L05 | 6" Core |
| C12003 | 5 | CA12003 | W53C12L05 | 6" Core |
| C13003 | 5 | CA13003 | W53C13L05 | 6" Core |
| C14003 | 5 | CA14003 | W53C14L05 | 6" Core |
| F01003 | 5 | BA03003 | W53F01L05 | 15 5-gallon buckets uncompacted AC mix |

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 04AA59

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01059 | 5 | BA01059 | W5AA01L05 | 12" Core |
| A02059 | 5 | BA02059 | W5AA01L05 | 12" Core |
| C01059 | 5 | CA01059 | W5AC01L05 | 6" Core |
|  | 4 | CA15059 | W5AC01L04 | 6" Core |
|  | 3 | CA16059 | W5AC01L03 | 6" Core |
| C02059 | 5 | CA02059 | W5AC02L05 | 6" Core |
| C03059 | 5 | CA03059 | W5AC03L05 | 6" Core |
| C04059 | 5 | CA04059 | W5AC04L05 | 6" Core |
| C05059 | 5 | CA05059 | W5AC05L05 | 6" Core |
| C06059 | 5 | CA06059 | W5AC06L05 | 6" Core |
| C07059 | 5 | CA07059 | W5AC07L05 | 6" Core |
| C08059 | 5 | CA08059 | W5AC08L05 | 6" Core |
| C09059 | 5 | CA09059 | W5AC09L05 | 6" Core |
| C10059 | 5 | CA10059 | W5AC10L05 | 6" Core |
| C11059 | 5 | CA11059 | W5AC11L05 | 6" Core |
| C12059 | 5 | CA12059 | W5AC12L05 | 6" Core |
| C13059 | 5 | CA13059 | W5AC13L05 | 6" Core |
| C14059 | 5 | CA14059 | W5AC14L05 | 6" Core |
| F01059 | 5 | BA03059 | W5AF01L05 | 15 5-gallon buckets uncompacted AC mix |

TABLE 10: SAMPLES ACQUIRED FROM TEST SECTION 04AA60

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01060 | 5 | BA01060 | W5BA01L05 | 12" Core |
| A02060 | 5 | BA02060 | W5BA01L05 | 12" Core |
| C01060 | 5 | CA01060 | W5BC01L05 | 6" Core |
|  | 4 | CA15060 | W5BC01L04 | 6" Core |
|  | 3 | CA16060 | W5BC01L03 | 6" Core |
| C02060 | 5 | CA02060 | W5BC02L05 | 6" Core |
| C03060 | 5 | CA03060 | W5BC03L05 | 6" Core |
| C04060 | 5 | CA04060 | W5BC04L05 | 6" Core |
| C05060 | 5 | CA05060 | W5BC05L05 | 6" Core |
| C06060 | 5 | CA06060 | W5BC06L05 | 6" Core |
| C07060 | 5 | CA07060 | W5BC07L05 | 6" Core |
| C08060 | 5 | CA08060 | W5BC08L05 | 6" Core |
| C09060 | 5 | CA09060 | W5BC09L05 | 6" Core |
| C10060 | 5 | CA10060 | W5BC10L05 | 6" Core |
| C11060 | 5 | CA11060 | W5BC11L05 | 6" Core |
| C12060 | 5 | CA12060 | W5BC12L05 | 6" Core |
| C13060 | 5 | CA13060 | W5BC13L05 | 6" Core |
| C14060 | 5 | CA14060 | W5BC14L05 | 6" Core |
| F01060 | 5 | BA03060 | W5BF01L05 | 15 5-gallon buckets uncompacted AC mix |

TABLE 11: SAMPLES ACQUIRED FROM TEST SECTION 04AA61

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01061 | 5 | BA01061 | W5CA01L05 | 12" Core |
|  | 4 | BA03061 | W5CA01L04 | 12" Core |
|  | 3 | BA05061 | W5CA01L03 | 12" Core |
| A02061 | 5 | BA02061 | W5CA01L05 | 12" Core |
|  | 5 | BA04061 | W5CA01L04 | 12" Core |
|  | 3 | BA06061 | W5CA01L03 | 12" Core |
| A01061, A02061 | 3 | BG01061 | W5CA01L01 | 150 lb Bulk Sample |
|  | 2 | BG02061 | W5CA03L02 | 150 lb Bulk Sample |
|  | 1 | BS01061 | W5CA03L01 | 150 lb Bulk Sample |
|  | 1 | MS01061 | W5CA03W01 | Moisture content jar sample |
| C01061 | 5 | CA01061 | W5CC01L05 | 6" Core |
|  | 4 | CA15061 | W5CC01L04 | 6" Core |
|  | 3 | CA16061 | W5CC01L03 | 6" Core |
| C02061 | 5 | CA02061 | W5CC02L05 | 6" Core |
| C03061 | 5 | CA03061 | W5CC03L05 | 6" Core |
| C04061 | 5 | CA04061 | W5CC04L05 | 6" Core |
| C05061 | 5 | CA05061 | W5CC05L05 | 6" Core |
| C06061 | 5 | CA06061 | W5CC06L05 | 6" Core |
| C07061 | 5 | CA07061 | W5CC07L05 | 6" Core |
| C08061 | 5 | CA08061 | W5CC08L05 | 6" Core |
| C09061 | 5 | CA09061 | W5CC09L05 | 6" Core |
| C10061 | 5 | CA10061 | W5CC10L05 | 6" Core |
| C11061 | 5 | CA11061 | W5CC11L05 | 6" Core |
| C12061 | 5 | CA12061 | W5CC12L05 | 6" Core |
| C13061 | 5 | CA13061 | W5CC13L05 | 6" Core |
| C14061 | 5 | CA14061 | W5CC14L05 | 6" Core |
| F01061 | 5 | BA03061 | W5CF01L05 | 15 5-gallon buckets uncompacted AC mix |

TABLE 12: SAMPLES ACQUIRED FROM PLANT

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| H01001 | 5 | BC01001 | W51H01L05 | 1 1-gallon can virgin AC binder (PG 70-22) |
| H01001 | 5 | BC02001 | W51H02L05 | 1 1-gallon can virgin AC binder (PG 70-22) |
| H01001 | 5 | BC03001 | W51H03L05 | 8 1-gallon cans virgin AC binder (PG 70-22) |
| H01059 | 5 | BC01059 | W5AH01L05 | 1 1-gallon can virgin AC binder (PG 64-28) |
| H01059 | 5 | BC02059 | W5AH02L05 | 1 1-gallon can virgin AC binder (PG 64-28) |
| H01059 | 5 | BC03059 | W5AH03L05 | 8 1-gallon cans virgin AC binder (PG 64-28) |
| H02059 | 5 | BU01001 | W51H04L05 | 20 5-gallon buckets combined aggregate (20% RAP) |
| H03059 | 5 | BU01059 | W5AH05L05 | 20 5-gallon buckets combined aggregate (30% RAP) |
| H04001 | 5 | BR01001 | W51H06L05 | 50 lb Bulk Sample RAP |
| H04001 | 5 | BR02001 | W51H07L05 | 10 5-gallon buckets RAP |
| H05001 | 5 | BR03001 | W51H08L05 | 5 5-gallon buckets 1/2” RAP |
| H06001 | 5 | BR04001 | W51H09L05 | 5 5-gallon buckets 3/8” RAP |
| H01003 | 5 | BW01003 | W53H01L05 | 2 1-gallon chemical additive (Evotherm) in manufacturer prescribed containers, with MSDS |

TABLE 13: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| W51A01L05 | 12” core |
| W51A02L05 | 12” core |
| W51C01L05 | 6” core |
| W51C02L05 | 6” core |
| W51C03L05 | 6” core |
| W51C04L05 | 6” core |
| W51C05L05 | 6” core |
| W51C06L05 | 6” core |
| W51C07L05 | 6” core |
| W51C08L05 | 6” core |
| W51C09L05 | 6” core |
| W51C10L05 | 6” core |
| W52A01L05 | 12” core |
| W52A02L05 | 12” core |
| W52C01L05 | 6” core |
| W52C02L05 | 6” core |
| W52C03L05 | 6” core |
| W52C04L05 | 6” core |
| W52C05L05 | 6” core |
| W52C06L05 | 6” core |
| W52C07L05 | 6” core |
| W52C08L05 | 6” core |
| W52C09L05 | 6” core |
| W52C10L05 | 6” core |
| W53A01L05 | 12” core |
| W53A02L05 | 12” core |
| W53C01L05 | 6” core |
| W53C02L05 | 6” core |
| W53C03L05 | 6” core |
| W53C04L05 | 6” core |
| W53C05L05 | 6” core |
| W53C06L05 | 6” core |
| W53C07L05 | 6” core |
| W53C08L05 | 6” core |

TABLE 13: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| W53C09L05 | 6” core |
| W53C10L05 | 6” core |
| W5AA01L05 | 12” core |
| W5AA02L05 | 12” core |
| W5AC01L05 | 6” core |
| W5AC02L05 | 6” core |
| W5AC03L05 | 6” core |
| W5AC04L05 | 6” core |
| W5AC05L05 | 6” core |
| W5AC06L05 | 6” core |
| W5AC07L05 | 6” core |
| W5AC08L05 | 6” core |
| W5AC09L05 | 6” core |
| W5AC10L05 | 6” core |
| W5BA01L05 | 12” core |
| W5BA02L05 | 12” core |
| W5BC01L05 | 6” core |
| W5BC02L05 | 6” core |
| W5BC03L05 | 6” core |
| W5BC04L05 | 6” core |
| W5BC05L05 | 6” core |
| W5BC06L05 | 6” core |
| W5BC07L05 | 6” core |
| W5BC08L05 | 6” core |
| W5BC09L05 | 6” core |
| W5BC10L05 | 6” core |
| W5CA01L05 | 12” core |
| W5CA02L05 | 12” core |
| W5CC01L05 | 6” core |
| W5CC02L05 | 6” core |
| W5CC03L05 | 6” core |
| W5CC04L05 | 6” core |
| W5CC05L05 | 6” core |
| W5CC06L05 | 6” core |
| W5CC07L05 | 6” core |
| W5CC08L05 | 6” core |

TABLE 13: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| W5CC09L05 | 6” core |
| W5CC10L05 | 6” core |
| W51H01L05 | 1 1-gallon can of virgin AC binder (PG 70-22) |
| W51H05L05 | 50 lb Bulk Sample RAP |
| Original HMAC |  |
| W51A01L04 | 12” core |
| W51A01L03 |  |
| W52C01L04 | 6” core |
| W52C01L03 |  |
| W53C01L04 | 6” core |
| W53C01L03 |  |
| W5AC01L04 | 6” core |
| W5AC01L03 |  |
| W5BC01L04 | 6” core |
| W5BC01L03 |  |
| W5CC01L04 | 6” core |
| W5CC01L03 |  |
| W5CA01L04 | 12” core |
| W5CA01L03 |  |
| Aggregate Base |  |
| W51A03L02 | 150 lb Bulk Sample |
| W5CA03L02 | 150 lb Bulk Sample |
| Select Materials (Subbase) |  |
| W51A03L02 | 150 lb Bulk Sample |
| W5CA03L02 | 150 lb Bulk Sample |
| Subgrade |  |
| W51A03L01 | 150 lb Bulk Sample |
| W5CA03L01 | 150 lb Bulk Sample |
| W51A03W01 | Moisture content jar sample |
| W5CA03W01 | Moisture content jar sample |

TABLE 14: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| W51C11L05 | 6" Core |
| W51C12L05 | 6" Core |
| W51C13L05 | 6" Core |
| W51C14L05 | 6" Core |
| W52C11L05 | 6" Core |
| W52C12L05 | 6" Core |
| W52C13L05 | 6" Core |
| W52C14L05 | 6" Core |
| W53C11L05 | 6" Core |
| W53C12L05 | 6" Core |
| W53C13L05 | 6" Core |
| W53C14L05 | 6" Core |
| W5AC11L05 | 6" Core |
| W5AC12L05 | 6" Core |
| W5AC13L05 | 6" Core |
| W5AC14L05 | 6" Core |
| W5BC11L05 | 6" Core |
| W5BC12L05 | 6" Core |
| W5BC13L05 | 6" Core |
| W5BC14L05 | 6" Core |
| W5CC11L05 | 6" Core |
| W5CC12L05 | 6" Core |
| W5CC13L05 | 6" Core |
| W5CC14L05 | 6" Core |
| W51H03L05 | 8 1-gallon cans of virgin AC binder (PG 70-22) |
| W51F01L05 | 15 5-gallon buckets uncompacted AC mix |
| W52F01L05 | 15 5-gallon buckets uncompacted AC mix |
| W53F01L05 | 15 5-gallon buckets uncompacted AC mix |
| W5AF01L05 | 15 5-gallon buckets uncompacted AC mix |
| W5BF01L05 | 15 5-gallon buckets uncompacted AC mix |
| W5CF01L05 | 15 5-gallon buckets uncompacted AC mix |
| W51H04L05 | 20 5-gallon buckets combined aggregate (20% RAP) |
| W5AH04L05 | 20 5-gallon buckets combined aggregate (30% RAP) |
| W51H07L05 | 10 5-gallon buckets RAP |
| W53H01L05 | 3 gallon chemical additive (Evotherm) in manufacturer prescribed containers, with MSDS |

TABLE 15: SAMPLES TO BE SHIPPED TO THE TURNER FAIRBANKS RESEARCH CENTER

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC Layer |  |
| W51H02L05 | 1 1-gallon can of virgin AC binder (PG 70-22) |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Arizona SPS-10 project.  The previous section ended with lists of samples to be shipped to each of the two laboratories, the central lab testing contractor laboratory and the Turner-Fairbank Highway Research center.  In this section, the tests to be performed on each sample are listed.

Table 16 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Table 17 provides new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 18 through 24 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 16: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 70 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 14 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 7 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 7 | X |  |
|  | Hamburg Wheel Track | AC09 | P75 | 14 | X |  |
|  | Fenix Fracture Energy | AC10 | P79 | 21 | X |  |
|  | Specific Gravity at 60 ° F | AE03 | P23 | 14 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 21 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 14 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 14 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 7 | X |  |
|  | PPA and Motor Oil Test | AE11 | P76 | 1 |  | X |
| B. | ORIGINAL HMAC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 12 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 2 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 2 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 2 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 2 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 2 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 2 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 2 | X |  |

TABLE 16: SPS-10 LABORATORY TESTING PLANS (Continued)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| C. | AGGREGATE BASE |  |  |  |  |  |
|  | Washed Sieve Analysis | UG02 | P41 | 2 | X |  |
|  | Standard Proctor | UG05 | P44 | 2 | X |  |
|  | Atterberg Limits | UG04 | P43 | 2 | X |  |
|  | Resilient Modulus | UG07 | P46 | 2 | X |  |
|  | Classification and Description | UG08 | P47 | 2 | X |  |
| D. | SELECT MATERIALS (SUBBASE) |  |  |  |  |  |
|  | Washed Sieve Analysis | UG02 | P41 | 2 | X |  |
|  | Standard Proctor | UG05 | P44 | 2 | X |  |
|  | Atterberg Limits | UG04 | P43 | 2 | X |  |
|  | Resilient Modulus | UG07 | P46 | 2 | X |  |
|  | Classification and Description | UG08 | P47 | 2 | X |  |
| E. | SUBGRADE |  |  |  |  |  |
|  | Sieve Analysis | SS01 | P51 | 4 | X |  |
|  | Atterberg Limits | SS03 | P43 | 4 | X |  |
|  | Classification and Description | SS04 | P52 | 4 | X |  |
|  | Standard Proctor | SS05 | P55 | 4 | X |  |
|  | Resilient Modulus | SS07 | P46 | 4 | X |  |
|  | Natural Moisture Content | SS09 | P49 | 4 | X |  |

TABLE 17: ORIGINAL AND COMBINED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BA01001 | BAE1001 |
|  | Specimen ID | W51A01L05 | W51A01A05 |
|  | Sample No. | BA01002 | BAE1002 |
|  | Specimen ID | W52A01L05 | W52A01A05 |
|  | Sample No. | BA01003 | BAE1003 |
|  | Specimen ID | W53A01L05 | W53A01A05 |
|  | Sample No. | BA01059 | BAE1059 |
|  | Specimen ID | W5AA01L05 | W5AA01A05 |
|  | Sample No. | BA01060 | BAE1060 |
|  | Specimen ID | W5BA01L05 | W5BA01A05 |
|  | Sample No. | BA01061 | BAE1061 |
|  | Specimen ID | W5CA01L05 | W5CA01A05 |
|  | Sample No. |  |  |
|  | Specimen ID |  |  |
|  | Sample No. |  |  |
|  | Specimen ID |  |  |
|  | Sample No. |  |  |
|  | Specimen ID |  |  |
|  | Sample No. |  |  |
|  | Specimen ID |  |  |
|  | Sample No. | BR01001 | BRE1001 |
|  | Specimen ID | W51H05L05 | W51H05M05 |

TABLE 17: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BA01001 | BAE1001 |
|  | Specimen ID | W51A01L05 | W51A01A05 |
|  | Sample No. | BA01002 | BAE1002 |
|  | Specimen ID | W52A01L05 | W52A01A05 |
|  | Sample No. | BA01003 | BAE1003 |
|  | Specimen ID | W53A01L05 | W53A01A05 |
|  | Sample No. | BA01059 | BAE1059 |
|  | Specimen ID | W5AA01L05 | W5AA01A05 |
|  | Sample No. | BA01060 | BAE1060 |
|  | Specimen ID | W5BA01L05 | W5BA01A05 |
|  | Sample No. | BA01061 | BAE1061 |
|  | Specimen ID | W5CA01L05 | W5CA01A05 |
|  | Sample No. |  |  |
|  | Specimen ID |  |  |
|  | Sample No. |  |  |
|  | Specimen ID |  |  |
|  | Sample No. |  |  |
|  | Specimen ID |  |  |
|  | Sample No. |  |  |
|  | Specimen ID |  |  |
|  | Sample No. | BR01001 | BRE1001 |
|  | Specimen ID | W51H05L05 | W51H05M05 |
| PAV | Sample No. | BAE1001 | BAP1001 |
|  | Specimen ID | W51A01A05 | W51A01B05 |
|  | Sample No. | BAE1002 | BAP1002 |
|  | Specimen ID | W52A01A05 | W52A01B05 |
|  | Sample No. | BAE1003 | BAP1003 |
|  | Specimen ID | W53A01A05 | W53A01B05 |
|  | Sample No. | BAE1059 | BAP1059 |
|  | Specimen ID | W5AA01A05 | W5AA01B05 |
|  | Sample No. | BAE1060 | BAP1060 |
|  | Specimen ID | W5BA01A05 | W5BA01B05 |
|  | Sample No. | BAE1061 | BAP1061 |
|  | Specimen ID | W5CA01A05 | W5CA01B05 |

TABLE 17: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS (Continued)

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| RTFO | Sample No. | BC01001 | BCR1001 |
|  | Specimen ID | W51H01L05 | W51H01M05 |
|  | Sample No. | BC01059 | BCR1059 |
|  | Specimen ID | W5AH01L05 | W5AH01M05 |
|  | Sample No. | BC01060 | BCR1060 |
|  | Specimen ID | W5BH01L05 | W5BH01M05 |
| RTFO + PAV | Sample No. | BC01001 | BCZ1001 |
|  | Specimen ID | W51H01L05 | W51H01M05 |
|  | Sample No. | BC01059 | BCZ1059 |
|  | Specimen ID | W5AH01L05 | W5AH01M05 |
|  | Sample No. | BC01060 | BCZ1060 |
|  | Specimen ID | W5BH01L05 | W5BH01M05 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W51A01L05 | P03/AC03 |  |  |  |  | Yes | C |
| W51A02L05 | P03/AC03 |  |  |  |  | Yes | C |
| W52A01L05 | P03/AC03 |  |  |  |  | Yes | C |
| W52A02L05 | P03/AC03 |  |  |  |  | Yes | C |
| W53A01L05 | P03/AC03 |  |  |  |  | Yes | C |
| W53A02L05 | P03/AC03 |  |  |  |  | Yes | C |
| W5AA01L05 | P03/AC03 |  |  |  |  | Yes | C |
| W5AA02L05 | P03/AC03 |  |  |  |  | Yes | C |
| W5BA01L05 | P03/AC03 |  |  |  |  | Yes | C |
| W5BA02L05 | P03/AC03 |  |  |  |  | Yes | C |
| W5CA01L05 | P03/AC03 |  |  |  |  | Yes | C |
| W5CA02L05 | P03/AC03 |  |  |  |  | Yes | C |
| W51A01M05 | P04/AC04 |  |  |  |  | No | E |
| W52A01M05 | P04/AC04 |  |  |  |  | No | E |
| W53A01M05 | P04/AC04 |  |  |  |  | No | E |
| W5AA01M05 | P04/AC04 |  |  |  |  | No | E |
| W5BA01M05 | P04/AC04 |  |  |  |  | No | E |
| W5CA01M05 | P04/AC04 |  |  |  |  | No | E |
| W51A01A05 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W52A01A05 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W53A01A05 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W5AA01A05 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W5BA01A05 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W5CA01A05 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W51A01B05 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W52A01B05 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W53A01B05 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W5AA01B05 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W5BA01B05 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W5CA01B05 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W51C01L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W51C02L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W51C03L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W51C04L05 | P02/AC02 |  |  |  |  | Yes | S |
| W51C05L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W51C06L05 | P02/AC02 |  |  |  |  | Yes | S |
| W51C07L05 | P02/AC02 |  |  |  |  | Yes | S |
| W51C08L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W51C09L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W51C10L05 | P02/AC02 |  |  |  |  | Yes | S |
| W52C01L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W52C02L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W52C03L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W52C04L05 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W52C05L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W52C06L05 | P02/AC02 |  |  |  |  | Yes | S |
| W52C07L05 | P02/AC02 |  |  |  |  | Yes | S |
| W52C08L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W52C09L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W52C10L05 | P02/AC02 |  |  |  |  | Yes | S |
| W53C01L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W53C02L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W53C03L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W53C04L05 | P02/AC02 |  |  |  |  | Yes | S |
| W53C05L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W53C06L05 | P02/AC02 |  |  |  |  | Yes | S |
| W53C07L05 | P02/AC02 |  |  |  |  | Yes | S |
| W53C08L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W53C09L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W53C10L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5AC01L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W5AC02L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W5AC03L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W5AC04L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5AC05L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W5AC06L05 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W5AC07L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5AC08L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W5AC09L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W5AC10L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5BC01L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W5BC02L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W5BC03L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W5BC04L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5BC05L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W5BC06L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5BC07L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5BC08L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W5BC09L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W5BC10L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5CC01L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W5CC02L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W5CC03L05 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W5CC04L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5CC05L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W5CC06L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5CC07L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5CC08L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W5CC09L05 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W5CC10L05 | P02/AC02 |  |  |  |  | Yes | S |

1. Next Process

D 	Remaining sample should be disposed
			S 	Remaining sample should be stored
			C	Remaining sample will be combined with another sample
			E 	Perform further testing on extracted sample
			P 	Perform further testing with PAV
			R 	Perform further testing with RFTO

TABLE 19: TRACKING TABLE OF EXPERIMENTAL ASPHALT TANK BINDER IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W51H01L05 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| W51H01M05 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| W51H01A05 | P27/AE07 | P28/AE08 |  |  |  | No | D |

TABLE 20: TRACKING TABLE OF STOCKPILE RAP IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W51H05L05 | P04/AC04 |  |  |  |  | Yes | E, S |
| W51H05M05 | P23/AE03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 | No | D |

TABLE 21: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W51A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W51A01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W51A02L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W51A02L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W5CA01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W5CA01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W5CA02L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W5CA02L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W51A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W51A01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W51A02M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W51A02M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W5CA01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W5CA01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |

TABLE 21: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W5CA02M05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W5CA02M04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W5CA02M03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W52C01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W53C01L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5AC01L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5BC01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W5CC01L05 | P02/AC02 |  |  |  |  | Yes | S |
| W52C01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W53C01L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5AC01L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5BC01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W5CC01L05 | P02/AC02 |  |  |  |  | Yes | S |
| W52C01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W53C01L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5AC01L05 | P02/AC02 |  |  |  |  | Yes | S |
| W5BC01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W5CC01L05 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 22: TRACKING TABLE OF SUBGRADE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W51A03L01 | P51/SS01 | P43/SS03 | P52/SS04 | P55/SS05 | P46/SS07 | Yes1 | S |
| W5CA03L01 | P51/SS01 | P43/SS03 | P52/SS04 | P55/SS05 | P46/SS07 | Yes1 | S |
| W51A03W01 | P49/SS09 |  |  |  |  | No1 | D |
| W5CA03W01 | P49/SS09 |  |  |  |  | No1 | D |

1. The moisture content sample may be disposed after testing.  However, any remaining bulk sample should be stored.

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE OVERLAY IN THE TURNER FAIRBANKS HIGHWAY RESEARCH CENTER

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W51H02L05 | P76/AE11 |  |  |  |  | Yes | S |
| W5AH02L05 | P76/AE11 |  |  |  |  | Yes | S |