ARIZONA SPS-10 PROJECT

(04BA00)

# MATERIALS SAMPLING AND TESTING PLAN:

# T1 and T2 INTERVAL SAMPLING

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Arizona SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION

| Section Number | SHRP ID | Description |
| --- | --- | --- |
| BA01 | 04BA01 | HMA Control Section with 20% RAP and PG 64-28 binder |
| BA02 | 04BA02 | WMA – Foaming Process with 20% RAP and PG 64-28 binder |
| BA03 | 04BA03 | WMA – Evotherm with 20% RAP and PG 64-28 binder |
| BA59 | 04BA59 | HMA Control Section with 30% RAP and PG 64-28 binder |
| BA60 | 04BA60 | WMA – Foaming Process with 30% RAP and PG 64-28 binder |
| BA61 | 04BA61 | WMA – Evotherm with 30% RAP and PG 64-28 binder |

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at the post-construction testing intervals t1, t2, and t3 following construction of 6 months, 12 months, and 18 months, respectively.  Table 2 provides the scope of material sampling, and Table 3 provides the scope of field testing.

Figures 1 through 6 show the locations for the many samples and tests scheduled across all three time intervals. Figures 1 through 6 show the material sampling locations for each section at time interval t1.

Tables 4 through 9 list the samples acquired from each of the six test sections at time interval t1. These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 10 and 11 list samples to be shipped to the central lab testing contractor laboratory and the LTPP Materials Reference Library (MRL), respectively. This includes all samples across all three time intervals. The Western Regional Support Contractor will be responsible for all labeling and shipping of samples.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Arizona SPS-10, R = “W,” representing western region)

- C = Construction event (For Arizona SPS-10, C = 6 for 04BAXX , representing the first constructed SPS-10)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 59

  - B – 60

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C –6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

5+70

5+52

5+50

5+53

5+54

5+55

5+56

5+57

A01101

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06101

C05101

C04101

2’

C03101

C01101

3’

1’

2’

C02101

Shoulder

Section STA:

FIGURE 1: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA01 AT T1

5+57

5+54

5+70

5+56

5+55

5+53

5+50

5+52

A01102

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06102

C05102

C04102

2’

C03102

C01102

3’

1’

2’

C02102

Shoulder

Section STA:

FIGURE 2: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA02 AT T1

A01103

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06103

C05103

C04103

2’

C03103

C01103

3’

1’

2’

C02103

Shoulder

Section STA:

5+70

5+57

5+56

5+55

5+54

5+53

5+50

5+52

FIGURE 3: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA03 AT T1

5+52

5+50

5+53

5+54

5+55

5+56

5+57

5+70

A01159

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06159

C05159

C04159

2’

C03159

C01159

3’

1’

2’

C02159

Shoulder

Section STA:

FIGURE 4: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA59 AT T1

5+70

5+57

5+56

5+55

5+54

5+53

5+50

5+52

A01160

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06160

C05160

C04160

2’

C03160

C01160

3’

1’

2’

C02160

Shoulder

Section STA:

FIGURE 5: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA60 AT T1

5+70

5+57

5+56

5+55

5+54

5+53

5+50

5+52

A01161

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06161

C05161

C04161

2’

C03161

C01161

3’

1’

2’

C02161

Shoulder

Section STA:

FIGURE 6: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA61 AT T1

0-83

0-88

0-90

0-87

0-86

0-70

A01201

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06201

C05201

C04201

2’

C03201

C01201

3’

1’

2’

C02201

Shoulder

0-85

0-84

FIGURE 7: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA01 AT T2

0-83

0-88

0-90

0-87

0-86

0-70

A01202

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06202

C05202

C04202

2’

C03202

C01202

3’

1’

2’

C02202

Shoulder

0-85

0-84

FIGURE 8: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA02 AT T2

0-70

0-83

0-84

0-85

0-86

0-87

0-90

0-88

A01203

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06203

C05203

C04203

2’

C03203

C01203

3’

1’

2’

C02203

Shoulder

Section STA:

FIGURE 9: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA03 AT T2

0-70

0-83

0-84

0-85

0-86

0-87

0-90

0-88

A01259

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C06259

C05259

C04259

2’

C03259

C01259

3’

1’

2’

C02259

Shoulder

Section STA:

FIGURE 10: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA59 AT T2

0-70

0-83

0-84

0-85

0-86

0-87

0-90

0-88

A01260

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C05260

2’

3’

1’

2’

Shoulder

Section STA:

C06260

C02260

C04260

C01260

C03260

FIGURE 11: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA60 AT T2

0-70

0-83

0-84

0-85

0-86

0-87

0-90

0-88

A01261

Direction of Traffic

Key

12” Core of experimental surface AC only

6” Core of experimental surface AC only

C05261

2’

3’

1’

2’

Shoulder

Section STA:

C06261

C02261

C04261

C01261

C03261

FIGURE 12: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA61 AT T2

TABLE 2: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
| A. | Experimental AC at t1 |  |  |
|  | 12" Core | 6 | A01101, A01102, A01103, A01159, A01160, A01161 |
|  | 6" Core | 36 | C01101-C06101, C01102-C06102, C01103-C06103, C01159-C06159, C01160-C06160, C01161-C06161 |
| B. | Experimental AC at t2 |  |  |
|  | 12" Core | 6 | A01201, A01202, A01203, A01259, A01260, A01261 |
|  | 6" Core | 36 | C01201-C06201, C01202-C06202, C01203-C06203, C01259-C06259, C01260-C06260, C01261-C06261 |
| C. | Experimental AC at t3 |  |  |
|  | 12" Core | 6 | A01301, A01302, A01303, A01359, A01360, A01361 |
|  | 6" Core | 36 | C01301-C06301, C01302-C06302, C01303-C06303, C01359-C06359, C01360-C06360, C01361-C06361 |

TABLE 3: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
| A. | Experimental AC at t1 |  |  |
|  | Core Examination and Thickness (P01/AC01) | 42 | A01101, A01102, A01103, A01159, A01160, A01161, C01101-C06101, C01102-C06102, C01103-C06103, C01159-C06159, C01160-C06160, C01161-C06161 |
| B. | Experimental AC at t2 |  |  |
|  | Core Examination and Thickness (P01/AC01) | 42 | A01201, A01202, A01203, A01259, A01260, A01261, C01201-C06201, C01202-C06202, C01203-C06203, C01259-C06259, C01260-C06260, C01261-C06261 |
| C. | Experimental AC at t3 |  |  |
|  | Core Examination and Thickness (P01/AC01) | 42 | A01301, A01302, A01303, A01359, A01360, A01361, C01301-C06301, C01302-C06302, C01303-C06303, C01359-C06359, C01360-C06360, C01361-C06361 |

TABLE 4: SAMPLES ACQUIRED FROM TEST SECTION 04BA01 AT T1

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01101 | 7 | BA01101 | W61A011L7 | 12" Core |
| C01101 | 7 | CA01101 | W61C011L7 | 6" Core |
| C02101 | 7 | CA02101 | W61C021L7 | 6" Core |
| C03101 | 7 | CA03101 | W61C031L7 | 6" Core |
| C04101 | 7 | CA04101 | W61C041L7 | 6" Core |
| C05101 | 7 | CA05101 | W61C051L7 | 6" Core |
| C06101 | 7 | CA06101 | W61C061L7 | 6" Core |

TABLE 5: SAMPLES ACQUIRED FROM TEST SECTION 04BA02 AT T1

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01102 | 7 | BA01102 | W62A011L7 | 12" Core |
| C01102 | 7 | CA01102 | W62C011L7 | 6" Core |
| C02102 | 7 | CA02102 | W62C021L7 | 6" Core |
| C03102 | 7 | CA03102 | W62C031L7 | 6" Core |
| C04102 | 7 | CA04102 | W62C041L7 | 6" Core |
| C05102 | 7 | CA05102 | W62C051L7 | 6" Core |
| C06102 | 7 | CA06102 | W62C061L7 | 6" Core |

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 04BA03 AT T1

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01103 | 7 | BA01103 | W63A011L7 | 12" Core |
| C01103 | 7 | CA01103 | W63C011L7 | 6" Core |
| C02103 | 7 | CA02103 | W63C021L7 | 6" Core |
| C03103 | 7 | CA03103 | W63C031L7 | 6" Core |
| C04103 | 7 | CA04103 | W63C041L7 | 6" Core |
| C05103 | 7 | CA05103 | W63C051L7 | 6" Core |
| C06103 | 7 | CA06103 | W63C061L7 | 6" Core |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 04BA59 AT T1

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01159 | 7 | BA01159 | W6AA011L7 | 12" Core |
| C01159 | 7 | CA01159 | W6AC011L7 | 6" Core |
| C02159 | 7 | CA02159 | W6AC021L7 | 6" Core |
| C03159 | 7 | CA03159 | W6AC031L7 | 6" Core |
| C04159 | 7 | CA04159 | W6AC041L7 | 6" Core |
| C05159 | 7 | CA05159 | W6AC051L7 | 6" Core |
| C06159 | 7 | CA06159 | W6AC061L7 | 6" Core |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 04BA60 AT T1

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01160 | 7 | BA01160 | W6BA011L7 | 12" Core |
| C01160 | 7 | CA01160 | W6BC011L7 | 6" Core |
| C02160 | 7 | CA02160 | W6BC021L7 | 6" Core |
| C03160 | 7 | CA03160 | W6BC031L7 | 6" Core |
| C04160 | 7 | CA04160 | W6BC041L7 | 6" Core |
| C05160 | 7 | CA05160 | W6BC051L7 | 6" Core |
| C06160 | 7 | CA06160 | W6BC061L7 | 6" Core |

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 04BA61 AT T1

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01161 | 7 | BA01161 | W6CA011L7 | 12" Core |
| C01161 | 7 | CA01161 | W6CC011L7 | 6" Core |
| C02161 | 7 | CA02161 | W6CC021L7 | 6" Core |
| C03161 | 7 | CA03161 | W6CC031L7 | 6" Core |
| C04161 | 7 | CA04161 | W6CC041L7 | 6" Core |
| C05161 | 7 | CA05161 | W6CC051L7 | 6" Core |
| C06161 | 7 | CA06161 | W6CC061L7 | 6" Core |

TABLE 10: SAMPLES ACQUIRED FROM TEST SECTION 04BA01 AT T2

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01201 | 7 | BA01201 | W61A012L7 | 12" Core |
| C01201 | 7 | CA01201 | W61C012L7 | 6" Core |
| C02201 | 7 | CA02201 | W61C022L7 | 6" Core |
| C03201 | 7 | CA03201 | W61C032L7 | 6" Core |
| C04201 | 7 | CA04201 | W61C042L7 | 6" Core |
| C05201 | 7 | CA05201 | W61C052L7 | 6" Core |
| C06201 | 7 | CA06201 | W61C062L7 | 6" Core |

TABLE 11: SAMPLES ACQUIRED FROM TEST SECTION 04BA02 AT T2

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01202 | 7 | BA01202 | W62A012L7 | 12" Core |
| C01202 | 7 | CA01202 | W62C012L7 | 6" Core |
| C02202 | 7 | CA02202 | W62C022L7 | 6" Core |
| C03202 | 7 | CA03202 | W62C032L7 | 6" Core |
| C04202 | 7 | CA04202 | W62C042L7 | 6" Core |
| C05202 | 7 | CA05202 | W62C052L7 | 6" Core |
| C06202 | 7 | CA06202 | W62C062L7 | 6" Core |

TABLE 12: SAMPLES ACQUIRED FROM TEST SECTION 04BA03 AT T2

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01203 | 7 | BA01203 | W63A012L7 | 12" Core |
| C01203 | 7 | CA01203 | W63C012L7 | 6" Core |
| C02203 | 7 | CA02203 | W63C022L7 | 6" Core |
| C03203 | 7 | CA03203 | W63C032L7 | 6" Core |
| C04203 | 7 | CA04203 | W63C042L7 | 6" Core |
| C05203 | 7 | CA05203 | W63C052L7 | 6" Core |
| C06203 | 7 | CA06203 | W63C062L7 | 6" Core |

TABLE 13: SAMPLES ACQUIRED FROM TEST SECTION 04BA59 AT T2

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01259 | 7 | BA01259 | W6AA012L7 | 12" Core |
| C01259 | 7 | CA01259 | W6AC012L7 | 6" Core |
| C02259 | 7 | CA02259 | W6AC022L7 | 6" Core |
| C03259 | 7 | CA03259 | W6AC032L7 | 6" Core |
| C04259 | 7 | CA04259 | W6AC042L7 | 6" Core |
| C05259 | 7 | CA05259 | W6AC052L7 | 6" Core |
| C06259 | 7 | CA06259 | W6AC062L7 | 6" Core |

TABLE 14: SAMPLES ACQUIRED FROM TEST SECTION 04BA60 AT T2

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01260 | 7 | BA01260 | W6BA012L7 | 12" Core |
| C01260 | 7 | CA01260 | W6BC012L7 | 6" Core |
| C02260 | 7 | CA02260 | W6BC022L7 | 6" Core |
| C03260 | 7 | CA03260 | W6BC032L7 | 6" Core |
| C04260 | 7 | CA04260 | W6BC042L7 | 6" Core |
| C05260 | 7 | CA05260 | W6BC052L7 | 6" Core |
| C06260 | 7 | CA06260 | W6BC062L7 | 6" Core |

TABLE 15: SAMPLES ACQUIRED FROM TEST SECTION 04BA61 AT T2

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01261 | 7 | BA01261 | W6CA012L7 | 12" Core |
| C01261 | 7 | CA01261 | W6CC012L7 | 6" Core |
| C02261 | 7 | CA02261 | W6CC022L7 | 6" Core |
| C03261 | 7 | CA03261 | W6CC032L7 | 6" Core |
| C04261 | 7 | CA04261 | W6CC042L7 | 6" Core |
| C05261 | 7 | CA05261 | W6CC052L7 | 6" Core |
| C06261 | 7 | CA06261 | W6CC062L7 | 6" Core |

TABLE 16: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC at t1 |  |  |
| BA01101 | W61A011L7 | 12” core |
| CA01101 | W61C011L7 | 6” core |
| CA02101 | W61C021L7 | 6” core |
| CA03101 | W61C031L7 | 6” core |
| BA01102 | W62A011L7 | 12” core |
| CA01102 | W62C011L7 | 6” core |
| CA02102 | W62C021L7 | 6” core |
| CA03102 | W62C031L7 | 6” core |
| BA01103 | W63A011L7 | 12” core |
| CA01103 | W63C011L7 | 6” core |
| CA02103 | W63C021L7 | 6” core |
| CA03103 | W63C031L7 | 6” core |
| BA01159 | W6AA011L7 | 12” core |
| CA01159 | W6AC011L7 | 6” core |
| CA02159 | W6AC021L7 | 6” core |
| CA03159 | W6AC031L7 | 6” core |
| BA01160 | W6BA011L7 | 12” core |
| CA01160 | W6BC011L7 | 6” core |
| CA02160 | W6BC021L7 | 6” core |
| CA03160 | W6BC031L7 | 6” core |
| BA01161 | W6CA011L7 | 12” core |
| CA01161 | W6CC011L7 | 6” core |
| CA02161 | W6CC021L7 | 6” core |
| CA03161 | W6CC031L7 | 6” core |

TABLE 17: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC at t1 |  |  |
| CA04101 | W61C041L7 | 6” core |
| CA05101 | W61C051L7 | 6” core |
| CA06101 | W61C061L7 | 6” core |
| CA04102 | W62C041L7 | 6” core |
| CA05102 | W62C051L7 | 6” core |
| CA06102 | W62C061L7 | 6” core |
| CA04103 | W63C041L7 | 6” core |
| CA05103 | W63C051L7 | 6” core |
| CA06103 | W63C061L7 | 6” core |
| CA04159 | W6AC041L7 | 6” core |
| CA05159 | W6AC051L7 | 6” core |
| CA06159 | W6AC061L7 | 6” core |
| CA04160 | W6BC041L7 | 6” core |
| CA05160 | W6BC051L7 | 6” core |
| CA06160 | W6BC061L7 | 6” core |
| CA04161 | W6CC041L7 | 6” core |
| CA05161 | W6CC051L7 | 6” core |
| CA06161 | W6CC061L7 | 6” core |

TABLE 18: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC at t2 |  |  |
| BA01201 | W61A012L7 | 12” core |
| CA01201 | W61C012L7 | 6” core |
| CA02201 | W61C022L7 | 6” core |
| CA03201 | W61C032L7 | 6” core |
| BA01202 | W62A012L7 | 12” core |
| CA01202 | W62C012L7 | 6” core |
| CA02202 | W62C022L7 | 6” core |
| CA03202 | W62C032L7 | 6” core |
| BA01203 | W63A012L7 | 12” core |
| CA01203 | W63C012L7 | 6” core |
| CA02203 | W63C022L7 | 6” core |
| CA03203 | W63C032L7 | 6” core |
| BA01259 | W6AA012L7 | 12” core |
| CA01259 | W6AC012L7 | 6” core |
| CA02259 | W6AC022L7 | 6” core |
| CA03259 | W6AC032L7 | 6” core |
| BA01260 | W6BA012L7 | 12” core |
| CA01260 | W6BC012L7 | 6” core |
| CA02260 | W6BC022L7 | 6” core |
| CA03260 | W6BC032L7 | 6” core |
| BA01261 | W6CA012L7 | 12” core |
| CA01261 | W6CC012L7 | 6” core |
| CA02261 | W6CC022L7 | 6” core |
| CA03261 | W6CC032L7 | 6” core |

TABLE 19: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC at t2 |  |  |
| CA04201 | W61C042L7 | 6” core |
| CA05201 | W61C052L7 | 6” core |
| CA06201 | W61C062L7 | 6” core |
| CA04202 | W62C042L7 | 6” core |
| CA05202 | W62C052L7 | 6” core |
| CA06202 | W62C062L7 | 6” core |
| CA04203 | W63C042L7 | 6” core |
| CA05203 | W63C052L7 | 6” core |
| CA06203 | W63C062L7 | 6” core |
| CA04259 | W6AC042L7 | 6” core |
| CA05259 | W6AC052L7 | 6” core |
| CA06259 | W6AC062L7 | 6” core |
| CA04260 | W6BC042L7 | 6” core |
| CA05260 | W6BC052L7 | 6” core |
| CA06260 | W6BC062L7 | 6” core |
| CA04261 | W6CC042L7 | 6” core |
| CA05261 | W6CC052L7 | 6” core |
| CA06261 | W6CC062L7 | 6” core |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Arizona SPS-10 project.  The previous section ended with lists of samples to be shipped to the central lab testing contractor laboratory.  In this section, the tests to be performed on each sample are listed. Differentiation in specimen based on time interval is listed in each table of this section.

Table 20 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Table 21 provides new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 22 and 23 provides tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 20: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer1 | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 3 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 3 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 2 | X |  |
|  | Fenix Fracture Energy | AC10 | P79 | 1 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 1 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 1 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 1 | X |  |

1 Numbers given are per time interval since testing is identical at time intervals 1, 2, and 3

TABLE 21: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BA01101 | BAE1101 |
|  | Specimen ID | W61A011L7 | W61A011A7 |
|  | Sample No. | BA01102 | BAE1102 |
|  | Specimen ID | W62A011L7 | W62A011A7 |
|  | Sample No. | BA01103 | BAE1103 |
|  | Specimen ID | W63A011L7 | W63A011A7 |
|  | Sample No. | BA01159 | BAE1159 |
|  | Specimen ID | W6AA011L7 | W6AA011A7 |
|  | Sample No. | BA01160 | BAE1160 |
|  | Specimen ID | W6BA011L7 | W6BA011A7 |
|  | Sample No. | BA01161 | BAE1160 |
|  | Specimen ID | W6CA012L7 | W6BA012A7 |
|  | Sample No. | BA01201 | BAE1201 |
|  | Specimen ID | W61A012L7 | W61A012A7 |
|  | Sample No. | BA01202 | BAE1202 |
|  | Specimen ID | W62A012L7 | W62A012A7 |
|  | Sample No. | BA01203 | BAE1203 |
|  | Specimen ID | W63A012L7 | W63A012A7 |
|  | Sample No. | BA01259 | BAE1259 |
|  | Specimen ID | W6AA012L7 | W6AA012A7 |
|  | Sample No. | BA01260 | BAE1260 |
|  | Specimen ID | W6BA012L7 | W6BA012A7 |
|  | Sample No. | BA01261 | BAE1260 |
|  | Specimen ID | W6CA012L7 | W6BA012A7 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

Table 14 below utilize the following codes to dictate the ‘next process’ undergone by each specimen.

D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	E 	Perform further testing on extracted sample

TABLE 22: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY FOR T1

| Sample No. | Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  |  | First | Second | Third | Fourth | Fifth |  |  |
| BA01101 | W61A011L7 | P04/AC04 |  |  |  |  | No | E |
| BA01102 | W62A011L7 | P04/AC04 |  |  |  |  | No | E |
| BA01103 | W63A011L7 | P04/AC04 |  |  |  |  | No | E |
| BA01159 | W6AA011L7 | P04/AC04 |  |  |  |  | No | E |
| BA01160 | W6BA011L7 | P04/AC04 |  |  |  |  | No | E |
| BA01161 | W6CA011L7 | P04/AC04 |  |  |  |  | No | E |
| BAE1101 | W61A011A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1102 | W62A011A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1103 | W63A011A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1159 | W6AA011A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1160 | W6BA011A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1161 | W6CA011A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| CA01101 | W61C011L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02101 | W61C021L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03101 | W61C031L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01102 | W62C011L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02102 | W62C021L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03102 | W62C031L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01103 | W63C011L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02103 | W63C021L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03103 | W63C031L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01159 | W6AC011L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02159 | W6AC021L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |

TABLE 22: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY FOR T1 (Continued)

| Sample No. | Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  |  | First | Second | Third | Fourth | Fifth |  |  |
| CA03159 | W6AC031L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01160 | W6BC011L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02160 | W6BC021L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03160 | W6CC031L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01161 | W6CC011L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02161 | W6CC021L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03161 | W6CC031L7 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY FOR T2

| Sample No. | Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  |  | First | Second | Third | Fourth | Fifth |  |  |
| BA01201 | W61A012L7 | P04/AC04 |  |  |  |  | No | E |
| BA01202 | W62A012L7 | P04/AC04 |  |  |  |  | No | E |
| BA01203 | W63A012L7 | P04/AC04 |  |  |  |  | No | E |
| BA01259 | W6AA012L7 | P04/AC04 |  |  |  |  | No | E |
| BA01260 | W6BA012L7 | P04/AC04 |  |  |  |  | No | E |
| BA01261 | W6CA012L7 | P04/AC04 |  |  |  |  | No | E |
| BAE1201 | W61A012A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1202 | W62A012A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1203 | W63A012A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1259 | W6AA012A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1260 | W6BA012A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| BAE1261 | W6CA012A7 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| CA01201 | W61C012L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02201 | W61C022L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03201 | W61C032L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01202 | W62C012L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02202 | W62C022L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03202 | W62C032L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01203 | W63C012L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02203 | W63C022L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03203 | W63C032L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01259 | W6AC012L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02259 | W6AC022L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY FOR T2 (Continued)

| Sample No. | Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  |  | First | Second | Third | Fourth | Fifth |  |  |
| CA03259 | W6AC032L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01260 | W6BC012L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02260 | W6BC022L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03260 | W6CC032L7 | P02/AC02 |  |  |  |  | Yes | S |
| CA01261 | W6CC012L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA02261 | W6CC022L7 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| CA03261 | W6CC032L7 | P02/AC02 |  |  |  |  | Yes | S |