ARIZONA SPS-10

PROJECT 04BA00

MATERIAL SAMPLING AND TESTING PLAN

Time Interval 3 Sampling

(19 Months after Construction)

Contents

GENERAL LAYOUT INFORMATION	2

MATERIALS SAMPLING AND FIELD TESTING	4

LABORATORY MATERIALS TESTING	15

# GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Arizona SPS-10 project in terms of the location of the test sections along the roadway. Table 1 lists each section and its respective description. Figure 1 provides a visual representation of the overall project layout.

Table 1: TEST SECTION IDENTIFICATION AND DESCRIPTION – 04BA00

| SHRP ID | Description |
| --- | --- |
| 04BA01 | HMA Control: PG 70-22 and 20% RAP |
| 04BA02 | WMA – Foaming Process: PG 70-22 and 20% RAP |
| 04BA03 | WMA – Evotherm: PG 70-22and 20% RAP |
| 04BA59 | HMA Control: PG 70-22 and 30% RAP |
| 04BA60 | WMA – Foaming Process: PG 70-22 and 30% RAP |
| 04BA61 | WMA – Evotherm: PG 70-22 and 30% RAP |

GPS Location for 0+00 at each section

| Test Section | Latitude | Longitude |
| --- | --- | --- |
| 04BA01 | 33.64891 | -113.90649 |
| 04BA02 | 33.64775 | -113.89706 |
| 04BA03 | 33.64839 | -113.90243 |
| 04BA59 | 33.64583 | -113.88098 |
| 04BA60 | 33.64709 | -113.89169 |
| 04BA61 | 33.64646 | -113.88634 |

Arizona SPS 10 Test Section Layout

04BA00, Quartzite, AZ ─ I-10 Eastbound MP 37.21

Direction of Traffic

STATE SPS

04BA01

STATE SPS 04BA03

0.0	152.4	381.0	533.4	883.9	1036.3	1386.8	1539.2	1889.8	2042.2	2392.7	2545.1

0	500	1250	1750	2900	3400	4550	5050	6200	6700	7850	8350

228.6	350.5	350.5	350.5	350.5

750	1150	1150	1150	1150

1960+00	1965+00	1972+50	1977+50	1989+00	1994+00	2005+50	2010+50	2022+00	2027+00	2038+50	2043+50

37.25	37.34	37.48	37.58	37.80	37.89	38.11	38.20	38.42	38.52	38.73	38.83

152.4

500

HMA

PG 70-22

20% RAP

152.4

500

WMA

(Evotherm)

PG 70-22

20% RAP

STATE SPS

04BA02

152.4

500

WMA

(Foaming)

PG 70-22

20% RAP

STATE SPS

04BA60

152.4

500

WMA

(Foaming)

PG 70-22

30% RAP

STATE SPS

04BA61

152.4

500

WMA

(Evotherm)

PG 70-22

30% RAP

STATE SPS

04BA59

152.4

500

HMA

PG 70-22

30% RAP

Figure 1: TEST SECTION LAYOUT – 04BA00

# MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at the post-construction testing time interval 3 (t3). Time interval 2 was supposed to occur at 12 months from construction (constructed in October 2016), but could not occur and will be omitted.

Figures 2 through 8 show the material sampling locations for each section. Tables 2 through 7 list the samples acquired from each of the six test sections at time interval t3. These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected. In total, six 12-inch core and 36 6-inch cores are to be collected. Seven cores are collected from each of the six sections for material testing. Of the seven cores, the 12-inch core and three of the six 6-inch cores will be shipped to the Central Laboratory Testing Contractor (CLTC) for testing and the remaining three 6-inch cores will be kept in storage at the Material Reference Library (MRL).

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-t-L-#

- R = RSC Code (For Arizona SPS-10, R = “W,” representing western region)

- C = Construction event (For Arizona SPS-10, C = 6 for 04BAXX , representing the sixth constructed SPS-10 in the Western Region)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 59

  - B – 60

  - C – 61

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- t  = Sampling time interval

- L = “L,” representing layer

- # = Layer Number

Labeling

The Data Collection Contractor (DCC) will be responsible for all labeling, shipping of samples, and completion of all LTPP Field Operations Information Sheets. Each sample shall be labeled before packaging. As a minimum, the following information shall be included on a tag or label attached to the specimen:

- SPECIMEN ID

- STATE CODE

- SHRP ID

- LOCATION DESIGNATION

- SAMPLE NUMBER

- DATE (mm-dd-yy, sampling date)

- FIELD SET (one digit number which will be 1 for the first round of sampling)

For cores, the LOCATION DESIGNATION shall be written directly on the core.  If the core contains more than one layer, layer boundaries shall be clearly marked, and each layer numbered.

Packaging

Suggestions for labeling and combining the samples for shipment are as follows:

- Each core shall be surrounded with "bubble-wrap" or other acceptable cushioning material on all sides within the shipping box.

- All shipping boxes should be wood of suitable grade and construction to withstand shipping and subsequent moving without breakage of the box or damaging of samples.

- All boxes should be adequately secured by nails or screws prior to shipping.

LTPP Field Operations Information Sheets 1 and 2 shall be sent with each shipment of materials samples.

A01301

C02301		C04301		C06301

C01301		C03301		C05301

Direction of Traffic

2’	1’	3’

2’	1’	1’	1’	1’	1’

Section STA:	5+70	5+90

Shoulder

Key

6” Core of experimental surface AC only – Layer 7 average thickness is 3.8” at STA5

12” Core of experimental surface AC only

04BA01

Figure 2: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA01 AT TIME INTERVAL 3

A01302

C02302		C04302		C06302

C01302		C03302		C05302

Direction of Traffic

2’	1’	3’

2’	1’	1’	1’	1’	1’

Section STA:	5+70	5+90

Key

6” Core of experimental surface AC only – Layer 7 average thickness is 3.9” at STA5

12” Core of experimental surface AC only

04BA02

Shoulder

Figure 3: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA02 AT TIME INTERVAL 3

A01303

C02303		C04303		C06303

C01303		C03303		C05303

Direction of Traffic

2’	1’	3’

2’	1’	1’	1’	1’	1’

Section STA:	5+70	5+90

Shoulder

Key

6” Core of experimental surface AC only – Layer 7 average thickness is 3.8” at STA5

12” Core of experimental surface AC only

04BA03

Figure 5: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA03 AT TIME INTERVAL 3

A01359

C02359		C04359		C06359

C01359		C03359		C05359

Direction of Traffic

2’	1’	3’

2’	1’	1’	1’	1’	1’

Section STA:	5+70	5+90

Shoulder

Key

6” Core of experimental surface AC only – Layer 7 average thickness is 4.0” at STA5

12” Core of experimental surface AC only

04BA59

Figure 6: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA59 AT TIME INTERVAL 3

A01360

C02360		C04360		C06360

C01360		C03360		C05360

Direction of Traffic

2’	1’	3’

2’	1’	1’	1’	1’	1’

Section STA:	5+70	5+90

Shoulder

Key

6” Core of experimental surface AC only – Layer 7 average thickness is 3.8” at STA5

12” Core of experimental surface AC only

04BA60

Figure 7: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA60 AT TIME INTERVAL 3

A01361

C02361		C04361		C06361

C01361		C03361		C05361

Direction of Traffic

2’	1’	3’

2’	1’	1’	1’	1’	1’

Section STA:	5+70	5+90

Shoulder

Key

6” Core of experimental surface AC only – Layer 7 average thickness is 3.7” at STA5

12” Core of experimental surface AC only

04BA61

Figure 8: ARIZONA SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 04BA61 AT TIME INTERVAL 3

Table 2: SAMPLES ACQUIRED FROM TEST SECTION 04BA01 AT T3

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01301 | 7 | BA01301 | W61A013L7 | 12" Core |
| C01301 | 7 | CA01301 | W61C013L7 | 6" Core |
| C02301 | 7 | CA02301 | W61C023L7 | 6" Core |
| C03301 | 7 | CA03301 | W61C033L7 | 6" Core |
| C04301 | 7 | CA04301 | W61C043L7 | 6" Core |
| C05301 | 7 | CA05301 | W61C053L7 | 6" Core |
| C06301 | 7 | CA06301 | W61C063L7 | 6" Core |

Table 3: SAMPLES ACQUIRED FROM TEST SECTION 04BA02 AT T3

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01302 | 7 | BA01302 | W62A013L7 | 12" Core |
| C01302 | 7 | CA01302 | W62C013L7 | 6" Core |
| C02302 | 7 | CA02302 | W62C023L7 | 6" Core |
| C03302 | 7 | CA03302 | W62C033L7 | 6" Core |
| C04302 | 7 | CA04302 | W62C043L7 | 6" Core |
| C05302 | 7 | CA05302 | W62C053L7 | 6" Core |
| C06302 | 7 | CA06302 | W62C063L7 | 6" Core |

Table 4: SAMPLES ACQUIRED FROM TEST SECTION 04BA03 AT T3

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01303 | 7 | BA01303 | W63A013L7 | 12" Core |
| C01303 | 7 | CA01303 | W63C013L7 | 6" Core |
| C02303 | 7 | CA02303 | W63C023L7 | 6" Core |
| C03303 | 7 | CA03303 | W63C033L7 | 6" Core |
| C04303 | 7 | CA04303 | W63C043L7 | 6" Core |
| C05303 | 7 | CA05303 | W63C053L7 | 6" Core |
| C06303 | 7 | CA06303 | W63C063L7 | 6" Core |

Table 5: SAMPLES ACQUIRED FROM TEST SECTION 04BA59 AT T3

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01359 | 7 | BA01359 | W6AA013L7 | 12" Core |
| C01359 | 7 | CA01359 | W6AC013L7 | 6" Core |
| C02359 | 7 | CA02359 | W6AC023L7 | 6" Core |
| C03359 | 7 | CA03359 | W6AC033L7 | 6" Core |
| C04359 | 7 | CA04359 | W6AC043L7 | 6" Core |
| C05359 | 7 | CA05359 | W6AC053L7 | 6" Core |
| C06359 | 7 | CA06359 | W6AC063L7 | 6" Core |

Table 6: SAMPLES ACQUIRED FROM TEST SECTION 04BA60 AT T3

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01360 | 7 | BA01360 | W6BA013L7 | 12" Core |
| C01360 | 7 | CA01360 | W6BC013L7 | 6" Core |
| C02360 | 7 | CA02360 | W6BC023L7 | 6" Core |
| C03360 | 7 | CA03360 | W6BC033L7 | 6" Core |
| C04360 | 7 | CA04360 | W6BC043L7 | 6" Core |
| C05360 | 7 | CA05360 | W6BC053L7 | 6" Core |
| C06360 | 7 | CA06360 | W6BC063L7 | 6" Core |

Table 7: SAMPLES ACQUIRED FROM TEST SECTION 04BA61 AT T3

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01361 | 7 | BA01361 | W6CA013L7 | 12" Core |
| C01361 | 7 | CA01361 | W6CC013L7 | 6" Core |
| C02361 | 7 | CA02361 | W6CC023L7 | 6" Core |
| C03361 | 7 | CA03361 | W6CC033L7 | 6" Core |
| C04361 | 7 | CA04361 | W6CC043L7 | 6" Core |
| C05361 | 7 | CA05361 | W6CC053L7 | 6" Core |
| C06361 | 7 | CA06361 | W6CC063L7 | 6" Core |

# LABORATORY MATERIALS TESTING

The purpose of this section is to provide an outline for the laboratory testing that is planned for the Arizona SPS-10 cores taken at time interval 3.  The previous section ended with lists of samples to be collected for t3.  In this section, the samples listed for either shipment to CLTC or storage at the MRL, and the tests to be performed on each sample.

Table 8 provides listings of laboratory tests to be performed for the experimental layer. The table includes the associated laboratory testing protocol for each laboratory test. It is imperative that the protocols listed be strictly followed during testing.

Tables 9 through 14 are the tracking tables for tests to be conducted on each material specimen.  These tables provide indication of how to process a sample after a particular test is complete. These tables also provide new sample numbers and specimen IDs for samples that will either be combined or modified in the laboratory. The provided sample numbers and specimen IDs should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Table 8: SPS-10 LABORATORY TESTING PLANS FOR TIME INTERVAL 3

| Material Type and Properties | LTPP Designation | LTPP Protocol | Test Conducted By: | Test Conducted By: |
| --- | --- | --- | --- | --- |
|  |  |  | CLTC | RSC |
| Core Examination and Thickness | AC01 | P01 |  | X |
| Bulk Specific Gravity | AC02 | P02 | X |  |
| Asphalt Content (Extracted) | AC04 | P04 | X |  |
| Dynamic Modulus | AC08 | P74 | X |  |
| Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | X |  |
| Bending Beam Rheometer (BBR) Test | AE08 | P28 | X |  |
| Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | X |  |

Table 9: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE SECTION 04BA01

| Specimen ID | 1st Test | 2nd Test | 3rd Test | NP1 |
| --- | --- | --- | --- | --- |
| W61C013L7 | AC01 | AC02 | AC082 + 1 spare | D |
| W61C023L7 | AC01 | AC02 |  | D |
| W61C033L7 | AC01 | AC02 |  | D |
| W61C043L7 | AC01 | Stored at MRL |  |  |
| W61C053L7 | AC01 |  |  |  |
| W61C063L7 | AC01 |  |  |  |

| Specimen ID | 1st Test | NP1 | Combined Specimen ID3 | 2nd Test | NP1 | Modified Specimen ID4 | 3rd Test | 4th Test | 5th Test | NP1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| W61A013L7 | AC01 | C | W61A013M7 | AC04 | E | W61A013A7 | AE07 | AE08 | AE10 | D |

1 Next Process:

D 	Remaining sample should be disposed

C	Remaining sample will be combined with another sample

E 	Perform further testing on extracted sample

2 Two dynamic modulus tests are performed on different specimens from the three cores. The third core will be a spare.

3 Specimen ID of a sample that was combined from other samples

4 Specimen ID of a sample that was extracted from another sample

Table 10: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE SECTION 04BA02

| Specimen ID | 1st Test | 2nd Test | 3rd Test | NP1 |
| --- | --- | --- | --- | --- |
| W62C013L7 | AC01 | AC02 | AC082 + 1 spare | D |
| W62C023L7 | AC01 | AC02 |  | D |
| W62C033L7 | AC01 | AC02 |  | D |
| W62C043L7 | AC01 | Stored at MRL |  |  |
| W62C053L7 | AC01 |  |  |  |
| W62C063L7 | AC01 |  |  |  |

| Specimen ID | 1st Test | NP1 | Combined Specimen ID3 | 2nd Test | NP1 | Modified Specimen ID4 | 3rd Test | 4th Test | 5th Test | NP1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| W62A013L7 | AC01 | C | W62A013M7 | AC04 | E | W62A013A7 | AE07 | AE08 | AE10 | D |

1 Next Process:

D 	Remaining sample should be disposed

C	Remaining sample will be combined with another sample

E 	Perform further testing on extracted sample

2 Two dynamic modulus tests are performed on different specimens from the three cores. The third core will be a spare.

3 Specimen ID of a sample that was combined from other samples

4 Specimen ID of a sample that was extracted from another sample

Table 11: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE SECTION 04BA03

| Specimen ID | 1st Test | 2nd Test | 3rd Test | NP1 |
| --- | --- | --- | --- | --- |
| W63C013L7 | AC01 | AC02 | AC082 + 1 spare | D |
| W63C023L7 | AC01 | AC02 |  | D |
| W63C033L7 | AC01 | AC02 |  | D |
| W63C043L7 | AC01 | Stored at MRL |  |  |
| W63C053L7 | AC01 |  |  |  |
| W63C063L7 | AC01 |  |  |  |

| Specimen ID | 1st Test | NP1 | Combined Specimen ID3 | 2nd Test | NP1 | Modified Specimen ID4 | 3rd Test | 4th Test | 5th Test | NP1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| W63A013L7 | AC01 | C | W63A013M7 | AC04 | E | W63A013A7 | AE07 | AE08 | AE10 | D |

1 Next Process:

D 	Remaining sample should be disposed

C	Remaining sample will be combined with another sample

E 	Perform further testing on extracted sample

2 Two dynamic modulus tests are performed on different specimens from the three cores. The third core will be a spare.

3 Specimen ID of a sample that was combined from other samples

4 Specimen ID of a sample that was extracted from another sample

Table 12: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE SECTION 04BA59

| Specimen ID | 1st Test | 2nd Test | 3rd Test | NP1 |
| --- | --- | --- | --- | --- |
| W6AC013L7 | AC01 | AC02 | AC082 + 1 spare | D |
| W6AC023L7 | AC01 | AC02 |  | D |
| W6AC033L7 | AC01 | AC02 |  | D |
| W6AC043L7 | AC01 | Stored at MRL |  |  |
| W6AC053L7 | AC01 |  |  |  |
| W6AC063L7 | AC01 |  |  |  |

| Specimen ID | 1st Test | NP1 | Combined Specimen ID3 | 2nd Test | NP1 | Modified Specimen ID4 | 3rd Test | 4th Test | 5th Test | NP1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| W6AA013L7 | AC01 | C | W6AA013M7 | AC04 | E | W6AA013A7 | AE07 | AE08 | AE10 | D |

1 Next Process:

D 	Remaining sample should be disposed

C	Remaining sample will be combined with another sample

E 	Perform further testing on extracted sample

2 Two dynamic modulus tests are performed on different specimens from the three cores. The third core will be a spare.

3 Specimen ID of a sample that was combined from other samples

4 Specimen ID of a sample that was extracted from another sample

Table 13: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE SECTION 04BA60

| Specimen ID | 1st Test | 2nd Test | 3rd Test | NP1 |
| --- | --- | --- | --- | --- |
| W6BC013L7 | AC01 | AC02 | AC082 + 1 spare | D |
| W6BC023L7 | AC01 | AC02 |  | D |
| W6BC033L7 | AC01 | AC02 |  | D |
| W6BC043L7 | AC01 | Stored at MRL |  |  |
| W6BC053L7 | AC01 |  |  |  |
| W6BC063L7 | AC01 |  |  |  |

| Specimen ID | 1st Test | NP1 | Combined Specimen ID3 | 2nd Test | NP1 | Modified Specimen ID4 | 3rd Test | 4th Test | 5th Test | NP1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| W6BA013L7 | AC01 | C | W6BA013M7 | AC04 | E | W6BA013A7 | AE07 | AE08 | AE10 | D |

1 Next Process:

D 	Remaining sample should be disposed

C	Remaining sample will be combined with another sample

E 	Perform further testing on extracted sample

2 Two dynamic modulus tests are performed on different specimens from the three cores. The third core will be a spare.

3 Specimen ID of a sample that was combined from other samples

4 Specimen ID of a sample that was extracted from another sample

Table 14: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE SECTION 04BA61

| Specimen ID | 1st Test | 2nd Test | 3rd Test | NP1 |
| --- | --- | --- | --- | --- |
| W6CC013L7 | AC01 | AC02 | AC082 + 1 spare | D |
| W6CC023L7 | AC01 | AC02 |  | D |
| W6CC033L7 | AC01 | AC02 |  | D |
| W6CC043L7 | AC01 | Stored at MRL |  |  |
| W6CC053L7 | AC01 |  |  |  |
| W6CC063L7 | AC01 |  |  |  |

| Specimen ID | 1st Test | NP1 | Combined Specimen ID3 | 2nd Test | NP1 | Modified Specimen ID4 | 3rd Test | 4th Test | 5th Test | NP1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| W6CA013L7 | AC01 | C | W6CA013M7 | AC04 | E | W6CA013A7 | AE07 | AE08 | AE10 | D |

1 Next Process:

D 	Remaining sample should be disposed

C	Remaining sample will be combined with another sample

E 	Perform further testing on extracted sample

2 Two dynamic modulus tests are performed on different specimens from the three cores. The third core will be a spare.

3 Specimen ID of a sample that was combined from other samples

4 Specimen ID of a sample that was extracted from another sample