FLORIDA SPS-10

MATERIALS SAMPLING AND TESTING PLAN

t-1 CORING

Contents

I.	GENERAL LAYOUT INFORMATION	1

I.1.	SPS-10 test sections	1

I.2.	Materials Sampling and Field Testing	4

I.3.	Identification Codes	5

I.4.	Material Sampling	6

I.4.1.	Core Test Sections	6

I.4.2.	Supplemental Test Section	6

I.5.	Samples to be shipped	11

I.6.	Note to Change the Section ID	12

II.	LABORATORY MATERIAL TESTING	12

II.1.	Testing Plans	12

II.2.	Tracking Tables	15

# GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the SPS-10 project in terms of the location of the test sections along the roadway. Table 1 lists each section and its respective description.

Table 1. Test sections identification and description

| Section Number | Section ID | Description |
| --- | --- | --- |
| 01 | 12AA01 | HMA Control Section |
| 02 | 12AA02 | WMA (Foaming) |
| 03 | 12AA03 | WMA (Chemical Additive) |
| 61 | 12AA61 | WMA (Chemical Additive) Placed @ HMA Temperature |

## SPS-10 test sections

Table 2 tracks the SPS-10 test sections from the beginning of the initial transition area at station 00+00 to the end of the last section at station 87+00.  Table 2 indicates transition areas between each section as well as the buffer and monitoring areas for each section.  The transition areas are not in same length in all cases.

Figure 1 and Figure 2 represent the four test sections, where 12AA01, 12AA03, and 12AA02 are core test sections and 12AA61 is supplemental test section. 12AA02, 12AA03, and 12AA61 are close to each other. However, 12AA01 control HMA section is 2500 feet far from the supplemental test section 12AA61.

Figure 1 and Figure 2 provides a visual representation of the core test sections layout. Here, odd (011, 031, 051, and 071) sampling areas are used at t0, t2, t4, t6, t8, t10; and even (021, 041, 061 and 081) sampling areas are used for t1, t3, t5, t7, t9 (Figure 1 and Figure 2).

Table 2. Core test sections layout

| Description | Test Sections |  |  | Test Section |
| --- | --- | --- | --- | --- |
|  | Begin STA | End STA | Section ID |  |
| Transition | 00+00 | 10+00 |  |  |
| Sampling Area | 10+00 | 11+00 | 12AA02 | WMA (Foaming) Test Section (Core Test Section) |
| Buffer Area | 11+00 | 11+50 |  |  |
| Monitoring Area | 11+50 | 16+50 |  |  |
| Buffer Area | 16+50 | 17+00 |  |  |
| Sampling Area | 17+00 | 18+00 |  |  |
| Transition | 18+00 | 28+00 |  |  |
| Sampling Area | 28+00 | 29+00 | 12AA03 | WMA (Chemical Additive) (Core Test Section) |
| Buffer Area | 29+00 | 29+50 |  |  |
| Monitoring Area | 29+50 | 34+50 |  |  |
| Buffer Area | 34+50 | 35+00 |  |  |
| Sampling Area | 35+00 | 36+00 |  |  |
| Transition | 36+00 | 46+00 |  |  |
| Sampling Area | 46+00 | 47+00 | 12AA61 | WMA (Chemical Additive) Placed@ HMA Temperature (Supplemental Test Section) |
| Buffer Area | 47+00 | 47+50 |  |  |
| Monitoring Area | 47+50 | 52+50 |  |  |
| Buffer Area | 52+50 | 53+00 |  |  |
| Sampling Area | 53+00 | 54+00 |  |  |
| Transition | 54+00 | 79+00 |  |  |
| Sampling Area | 79+00 | 80+00 | 12AA01 | HMA Control Section (Core Test Section) |
| Buffer Area | 80+00 | 80+50 |  |  |
| Monitoring Area | 80+50 | 85+50 |  |  |
| Buffer Area | 85+50 | 86+00 |  |  |
| Sampling Area | 86+00 | 87+00 |  |  |

MP 2.827

MP 2.855

Sampling Area 031

Buffer Area (50 ft)

12AA02

WMA (Foaming)

Buffer Area (50 ft)

Sampling Area 041

Transition (700 ft)

Sampling Area 051

Buffer Area (50 ft)

12AA03

WMA

(Chemical Additive)

Buffer Area (50 ft)

Sampling Area 061

Transition (700 ft)

Buffer Area (50 ft)

12AA61

WMA

(Chemical Additive)

@HMA Temperature

Buffer Area (50 ft)

Sampling Area 081

Sampling Area 071

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic

18+00

25+00

10+00

33+00

40+00

48+00

11+50

16+50

26+50

31+50

41+50

46+50

MP 3.423

MP 3.272

MP 3.139

MP 2.988

MP 3.395

MP 3.300

MP 3.311

MP 3.016

MP 2.732

MP 2.694

Figure 1. Florida SPS-10 WMA test sections layout

1.  Odd sampling areas are used for t0, t2, t4, t8, t10; even sampling areas are used for t1, t3, t5, t7, t9

MP 2.230

MP 2.079

MP 2.107

MP 2.202

Sampling Area 011

Buffer Area (50 ft)

12AA01

HMA

Control Test Section

Buffer Area (50 ft)

Sampling Area 021

800ft

500ft

100ft

100ft

Traffic

81+00

73+00

74+50

79+50

Figure 2. Florida HMA control test section layout.

1. Odd sampling areas are used for t0, t2, t4, t8, t10; even sampling areas are used for t1, t3, t5, t7, t9

## Materials Sampling and Field Testing

This section of the plan provides for the material sampling and testing activities that occur in the field as part of time 1 (t1 is six months after construction).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4  and Table 5 provide the scope of material sampling for core sections and supplemental test sections, respectively. Table 6 to Table 9 are the sample collected from section 12AA01, 12AA02, 12AA03, and 12AA61, respectively.

Table 10  and Table 11 are the list of samples to be shipped to the central lab testing contractor laboratory and LTPP MRL, respectively. Finally, Table 12, Table 13, and Table 14 are the list of tests to be conducted and Table 15 is for the materials tracking system.

## Identification Codes

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID.   A description of each code format described here.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Florida SPS-10, R = “S,” representing southern region)

- C = Construction event (For Florida SPS-10, C = 5)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - 4 – 61

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

Table 3. Project layer numbering

| Layer No. | Description |
| --- | --- |
| 1 | Subgrade |
| 2 | Unbound Base |
| 3 | Original HMAC |
| 4 | Experimental AC |

## Material Sampling

### Core Test Sections

Table 4. Scope of material sampling for core test sections

| Material and Sample Description |  | No. of Samples per section |  |  | Sample Location |
| --- | --- | --- | --- | --- | --- |
|  |  | 01 | 02 | 03 |  |
|  | POST-CONSTRUCTION SAMPLING: t1 CORING |  |  |  |  |
| A. | EXPERIMENTAL AC |  |  |  |  |
|  | 6" Core | 7 | 7 | 7 | C16101-C22101, C16102-C22102, C16103-C22103 |

### Supplemental Test Section

Table 5. Scope of material sampling for supplemental test section

| Material and Sample Description |  | No. of Samples per section |  | Sample Location |
| --- | --- | --- | --- | --- |
|  |  | 61 |  |  |
|  | POST-CONSTRUCTION SAMPLING: t1 CORING |  |  |  |
| A | EXPERIMENTAL AC |  |  |  |
|  | 6" Core | 7 | C16161-C22161 |  |

Table 6. Samples acquired from core test section 12AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t1 sampling |  |  |  |  |
| C16101 | 10 | CA01101 | S51C16L10 | 6" Core |
| C17101 | 10 | CA02101 | S51C17L10 | 6" Core |
| C18101 | 10 | CA03101 | S51C18L10 | 6" Core |
| C19101 | 10 | CA04101 | S51C19L10 | 6" Core |
| C20101 | 10 | CA05101 | S51C20L10 | 6" Core |
| C21101 | 10 | CA06101 | S51C21L10 | 6" Core |
| C22101 | 10 | CA07101 | S51C22L10 | 6" Core |

Table 7. Samples acquired from core test section 12AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t1 sampling |  |  |  |  |
| C16102 | 10 | CA01102 | S52C16L10 | 6" Core |
| C17102 | 10 | CA02102 | S52C17L10 | 6" Core |
| C18102 | 10 | CA03102 | S52C18L10 | 6" Core |
| C19102 | 10 | CA04102 | S52C19L10 | 6" Core |
| C20102 | 10 | CA05102 | S52C20L10 | 6" Core |
| C21102 | 10 | CA06102 | S52C21L10 | 6" Core |
| C22102 | 10 | CA07102 | S52C22L10 | 6" Core |

Table 8. Samples acquired from core test section 12AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t1 sampling |  |  |  |  |
| C16103 | 10 | CA01103 | S53C16L10 | 6" Core |
| C17103 | 10 | CA02103 | S53C17L10 | 6" Core |
| C18103 | 10 | CA03103 | S53C18L10 | 6" Core |
| C19103 | 10 | CA04103 | S53C19L10 | 6" Core |
| C20103 | 10 | CA05103 | S53C20L10 | 6" Core |
| C21103 | 10 | CA06103 | S53C21L10 | 6" Core |
| C22103 | 10 | CA07103 | S53C22L10 | 6" Core |

5+50

5+70

Section STA:

Section: 12AA0X

Description: Core Test Sections

Sampling Area: 02, 04, 06

Sampling Interval: t1

Shoulder

C1710X

C1910X

C2110X

2’

1’

2’

2’

2’

2’

C1610X	X

C1810X

C2010X

C2210X

3’

2’

1’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

Figure 3. Sampling plan for core test sections AA01, AA02, and AA03 at post-construction time 1 (t1) Florida SPS-10

5+50

5+70

Section STA:

Section: 12AA61

Description: Supplemental Test Section

Sampling Area: 08

Sampling Interval: t1

Shoulder

C17161

C19161

C21161

2’

1’

2’

2’

2’

2’

C16161

C18161

C20161

C22161

3’

2’

1’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

Figure 4. Sampling plan for supplemental test section AA61 at post-construction time 1 (t1) Florida SPS-10

Table 9. Samples acquired from supplemental test section 12AA61

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t1 sampling |  |  |  |  |
| C16161 | 10 | CA01161 | S54C16L10 | 6" Core |
| C17161 | 10 | CA02161 | S54C17L10 | 6" Core |
| C18161 | 10 | CA03161 | S54C18L10 | 6" Core |
| C19161 | 10 | CA04161 | S54C19L10 | 6" Core |
| C20161 | 10 | CA05161 | S54C20L10 | 6" Core |
| C21161 | 10 | CA06161 | S54C21L10 | 6" Core |
| C22161 | 10 | CA07161 | S54C22L10 | 6" Core |

## Samples to be shipped

Table 10. Samples to be shipped to central lab testing contractor laboratory

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S51C16L10 | 6" Core |
| S51C17L10 | 6" Core |
| S51C18L10 | 6" Core |
| S51C19L10 | 6" Core |
| S52C16L10 | 6" Core |
| S52C17L10 | 6" Core |
| S52C18L10 | 6" Core |
| S52C19L10 | 6" Core |
| S53C16L10 | 6" Core |
| S53C17L10 | 6" Core |
| S53C18L10 | 6" Core |
| S53C19L10 | 6" Core |
| S54C16L10 | 6" Core |
| S54C17L10 | 6" Core |
| S54C18L10 | 6" Core |
| S54C19L10 | 6" Core |

Table 11. Samples to be shipped to the LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| S51C20L10 | 6" Core |
| S51C21L10 | 6" Core |
| S51C22L10 | 6" Core |
| S52C20L10 | 6" Core |
| S52C21L10 | 6" Core |
| S52C22L10 | 6" Core |
| S53C20L10 | 6" Core |
| S53C21L10 | 6" Core |
| S53C22L10 | 6" Core |
| S54C20L10 | 6" Core |
| S54C21L10 | 6" Core |
| S54C22L10 | 6" Core |

## Note to Change the Section ID

Initially, the SPS-10 FL sections were assigned as AA01, AA02, AA03, and AA61 for control HMA, WMA (Chemical), WMA (Foaming), and WMA (Chemical) at HMA temperature, respectively. In order to maintain the consistency among SPS-10 sections within the LTPP Southern region, AA02 section should be WMA (Foaming) and AA03 should be WMA (Chemical). That’s why, the AA02 FL section has been changed to WMA (Foaming) and AA03 has been changed to WMA (Chemical) and updated everything for preconstruction activities. This change in naming convention of SPS-10 FL sections has been followed for all activities after preconstruction inspection.

# LABORATORY MATERIAL TESTING

This section includes the material testing plan and material tracking system for Florida SPS-10 sections. In material testing plan (Table 12), the tests have been detailed by each material type, LTPP designation, LTPP protocol, no of tests per layer, and the responsible department for testing. Table 13 and Table 14 include the sample no and specimen id for combined and modified materials.

## Testing Plans

Table 12. Laboratory testing plan for SPS-10 FL

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Core Exam. and Thickness | AC01 | P01 | 28 | RSC |  |
|  | Bulk Specific Gravity | AC02 | P02 | 12 | CLTC |  |
|  | Dynamic Modulus | AC08 | P74 | 4 | CLTC |  |
|  | Asphalt Extraction | AC04 | P04 | 16 | CLTC |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 4 | CLTC |  |
|  | Bending Beam Rheometer | AE08 | P28 | 4 | CLTC |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 4 | CLTC |  |

* SPS-10 Sampling and Testing guide suggests UG03 which does not exist in LTPP IMS guide.

Table 13. Original and combined specimen descriptions

1 Sample No.:  After combination, the third character is changed to “X,” and the fourth character is assigned numerically.  The other four characters follow the original format. (Sample Number Format: S-M-##-t-XX)

Specimen ID:  After combination, “L” is changed to “M.”

| Description Type | Status |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Original |  |  |  | Combined1 |
| Sample No. | CA01101 | CA02101 | CA03101 | CA04101 | CAX1101 |
| Specimen ID | S51C16L10 | S51C17L10 | S51C18L10 | S51C19L10 | S51C16M10 |
| Sample No. | CA01102 | CA02102 | CA03102 | CA04102 | CAX1102 |
| Specimen ID | S52C16L10 | S52C17L10 | S52C18L10 | S52C19L10 | S52C16M10 |
| Sample No. | CA01103 | CA02103 | CA03103 | CA04103 | CAX1103 |
| Specimen ID | S53C16L10 | S53C17L10 | S53C18L10 | S53C19L10 | S53C16M10 |
| Sample No. | CA01161 | CA02161 | CA03161 | CA04161 | CAX1161 |
| Specimen ID | S54C16L10 | S54C17L10 | S54C18L10 | S54C19L10 | S54C16M10 |

Table 14. Original and modified specimen descriptions

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | CAX1101 | CAE1101 |
|  | Specimen ID | S51C16M10 | S51C16A10 |
|  | Sample No. | CAX1102 | CAE1102 |
|  | Specimen ID | S52C16M10 | S52C16A10 |
|  | Sample No. | CAX1103 | CAE1103 |
|  | Specimen ID | S53C16M10 | S53C16A10 |
|  | Sample No. | CAX1161 | CAE1161 |
|  | Specimen ID | S54C16M10 | S54C16A10 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.

## Tracking Tables

Table 15. Tracking table for experimental asphalt concrete in the central lab testing contractor laboratory

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |
| S51C16L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S51C17L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S51C18L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S52C16L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S52C17L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S52C18L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S53C16L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S53C17L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S53C18L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S54C16L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S54C17L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S54C18L10 | P01/AC01 | P02/AC02 | P74/AC08 | Yes | C |
| S51C19L10 | P01/AC01 |  |  | Yes | C |
| S52C19L10 | P01/AC01 |  |  | Yes | C |
| S53C19L10 | P01/AC01 |  |  | Yes | C |
| S54C19L10 | P01/AC01 |  |  | Yes | C |
| S51C16M10 | P04/AC04 |  |  | No | E |
| S52C16M10 | P04/AC04 |  |  | No | E |
| S53C16M10 | P04/AC04 |  |  | No | E |
| S54C16M10 | P04/AC04 |  |  | No | E |
| S51C16A10 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |
| S52C16A10 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |
| S53C16A10 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |
| S54C16A10 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |

1 Next Process
	D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV