MISSOURI SPS-10 PROJECT 29AA00

# MATERIALS SAMPLING AND TESTING PLAN

For t0 (At and Immediately After Construction)

Contents

MATERIALS SAMPLING AND TESTING PLAN	0

GENERAL LAYOUT INFORMATION	1

MATERIALS SAMPLING AND FIELD TESTING	7

LABORATORY MATERIALS TESTING	64

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Missouri SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  These tables indicate transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Additionally, Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION – 29AA00

| Test Section | SHRP ID | Description |
| --- | --- | --- |
| 1 | HMA Control 29AA01 | Control Section 2” SP125C w/ PG 64-22H, 24 % RAP; 0 % RAS Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| 2 | WMA Section 1 29AA02 | Foamed Asphalt Warm Mix Section with 2.0% water 2” SP125C w/ PG 64-22H, 25 % RAP; 0 % RAS Astec ® Mixing Unit, Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| 3 | WMA Section 2 29AA03 | Chemical Warm Mix Section 2” SP125C w/ PG 64-22H, 25 % RAP; 0 % RAS Evotherm® Chemical Additive 0.5%/AC Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| A | Supp. Section 1 29AA61 | Virgin Mix Section 2” SP125C w/ PG 64-22H 0 % RAP; 0 % RAS, Morlife® T280 1%/AC Combined Aggregate Gradation #2 (w/SG) |
| B | Supp. Section 2 29AA62 | RAP Mix Section 2” SP125C w/Final Extracted Binder = PG 77.1-22.3 Virgin Binder = PG 64-22H 35 % RAP, 0 % RAS , EvoFlex® Chemical Additive 3.0%/AC, Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| C | Supp. Section 3 29AA63 | RAS Mix Section 2” SP125C w/ PG 58-28S 0 % RAP; 17 % RAS, Morlife® T280 1%/AC Combined Aggregate Gradation #2 (w/SG) |
| D | Supp. Section 4 29AA64 | RAP/RAS Mix Section 2” SP125C w/ PG 58-28S 18 % RAP & 15 % RAS, Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| E | Supp. Section 5 29AA65 | RAP Mix Section 2” SP125C w/ PG 58-28S 33 % RAP, 0 % RAS, Minimum 15.0 % VMA Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| F | Supp. Section 6 29AA66 | RAP/RAS Mix Section 2” SP125C w/ Final Extracted Binder = PG 72-26.1 Virgin Binder = PG 46-34S 16 % RAP, 30 % RAS, Morlife® T280 2%/AC Combined Aggregate Gradation #1 |
| G | Supp. Section 7 29AA67 | RAS Mix Section 2” SP125C w/Final Extracted Binder = PG 77.8-25.6 Virgin Binder = PG 58-28S 0 % RAP, 33 % RAS, EvoFlex® Chemical Additive 3.5%/AC AC Modifier IPC-70 3.5%/AC, Morlife® T280 1%/AC Combined Aggregate Gradation #3 (w/MAN SAND) |

TABLE 2: TEST SECTION LAYOUT – 29AA00

| Tentative Log Mile Begin STA | Tentative Log Mile End STA | Experiment Begin STA feet | Experiment End STA feet | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
| 135.660 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA01 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 135.868 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 136.171 | 5+150 | 5+1099 | Transition |  |
| 136.171 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA02 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 136.379 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 136.696 | 5+150 | 5+1024.3 | Transition |  |
| 136.696 |  | 0-1024.3 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA03 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 136.918 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 137.207 | 5+150 | 5+876.5 | Transition |  |
| 137.207 |  | 0-876.5 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA61 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 137.401 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 137.704 | 5+150 | 5+1099 | Transition |  |
| 137.704 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA62 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 137.912 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 138.111 | 5+150 | 5+401.3 | Transition |  |

TABLE 2: TEST SECTION LAYOUT – 29AA00 (Continued)

| Tentative Log Mile Begin STA | Tentative Log Mile End STA | Experiment Begin STA feet | Experiment End STA feet | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
| 138.111 |  | 0-401.3 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA63 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 138.215 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 138.518 | 5+150 | 5+1099 | Transition |  |
| 138.726 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA64 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 138.934 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 139.237 | 5+150 | 5+1099 | Transition |  |
| 139.740 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA65 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 139.948 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 140.185 | 5+150 | 5+599.3 | Transition |  |
| 140.185 |  | 0-599.3 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA66 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 140.326 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 140.582 | 5+150 | 5+702.2 | Transition |  |
| 140.582 |  | 0-702.2 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA67 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 140.743 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 141.045 | 5+150 | 5+1096.4 | Transition |  |

Sampling Area 061

Buffer Area (50 ft)

29AA03

WMA Evotherm® Chemical Section

2” SP125C w/ PG 64-22H

25 % RAP; 0 % RAS

Buffer Area (50 ft)

Sampling Area 051

Transition (length variable)

Sampling Area 041

Buffer Area (50 ft)

29AA02

WMA Foaming Process with 2.0% water - Astec® Mixing Unit

2” SP125C w/ PG 64-22H

25 % RAP; 0 % RAS

Buffer Area (50 ft)

Sampling Area 031

Transition (length variable)

Buffer Area (50 ft)

29AA01

HMA Control Section 2” SP125C w/ PG 64-22H

24 % RAP; 0 % RAS

Buffer Area (50 ft)

Sampling Area 011

Sampling Area 021

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic (WB)

136.696

137.207

136.171

135.660

5+00

0+00

5+00

0+00

5+00

0+00

Sampling Area 101

Buffer Area (50 ft)

29AA62

RAP Mix Section

2” SP125C w/ Contractor Designed Grade

35 % RAP; 0 % RAS

Final Extracted Binder

= PG 77.1-22.3

Buffer Area (50 ft)

Sampling Area 091

Transition (length variable)

Sampling Area 081

Buffer Area (50 ft)

29AA61

Virgin Mix Section

2” SP125C w/ PG 64-22H

0 % RAP; 0 % RAS

Buffer Area (50 ft)

Sampling Area 071

Transition (length variable)

800ft

800ft

500ft

500ft

100ft

100ft

100ft

100ft

Traffic (WB)

138.111

137.704

137.207

5+00

0+00

5+00

0+00

FIGURE 1: MISSOURI SPS-10 PROJECT LAYOUT – 29AA00

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

Sampling Area 161

Buffer Area (50 ft)

29AA65

RAP Mix Section

2” SP125C w/ PG 58-28S

33 % RAP; 0 % RAS

Minimum 15.0% VMA

Buffer Area (50 ft)

Sampling Area 151

Transition (length variable)

Sampling Area 141

Buffer Area (50 ft)

29AA64

RAP/RAS Mix Section

2” SP125C w/ PG 58-28S

18 % RAP; 15 % RAS

Buffer Area (50 ft)

Sampling Area 131

Transition (length variable)

Buffer Area (50 ft)

29AA63

RAS Mix Section

2” SP125C w/ PG 58-28S

0 % RAP; 17 % RAS

Buffer Area (50 ft)

Sampling Area 111

Sampling Area 121

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic (WB)

139.740

139.237

140.185

138.726138.518

138.111

5+00

0+00

5+00

0+00

5+00

0+00

Sampling Area 201

Buffer Area (50 ft)

29AA67

RAS Mix Section

2” SP125C w/ Contractor Designed Grade

0 % RAP; 36 % RAS

Final Extracted Binder

= PG 77.8-25.6

Buffer Area (50 ft)

Sampling Area 191

Transition (length variable)

Sampling Area 181

Buffer Area (50 ft)

29AA66

RAP/RAS Mix Section

2” SP125C w/ Contractor Designed Grade

16 % RAP; 30 % RAS

Final Extracted Binder

= PG 72-26.1

Buffer Area (50 ft)

Sampling Area 171

Transition (length variable)

800ft

800ft

500ft

500ft

100ft

100ft

100ft

100ft

Traffic (WB)

141.045

140.582

140.185

5+00

0+00

5+00

0+00

FIGURE 1: MISSOURI SPS-10 PROJECT LAYOUT – 29AA00 (Continued)

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at time zero (t0 is at time of construction).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 2 through 21 show the locations for the many samples and tests scheduled.  Figures 2 through 11 show density measurement layouts and Figures 12 through 21 show the material sampling locations for each section as well as the location of Dynamic Cone Penetrometer (DCP) testing.

Tables 6 through 16 list the samples acquired from each of the ten test sections as well as the asphalt plant.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 17 through 19 list samples to be shipped to the Central Lab Testing Contractor (CLTC) laboratory, the LTPP Materials Reference Library (MRL), and the Turner-Fairbank Highway Research Center (TFHRC), respectively.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Missouri SPS-10, R = “C,” representing north central region)

- C = Construction event (For Missouri SPS-10, C = 2, representing second constructed SPS-10 in the north central region)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 61

  - B – 62

  - C – 63

  - D – 64

  - E – 65

  - F – 66

  - G – 67

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

Labels and Tags

Each sample shall be labeled before packing in boxes and cartons. As a minimum, the following information shall be included on a tag or label attached to the specimen:

- SPECIMEN ID

- STATE CODE

- SHRP ID

- LOCATION DESIGNATION

- SAMPLE NUMBER

- DATE (mm-dd-yy, sampling date)

- FIELD SET (one digit number which will be 1 for the first round of sampling)

For cores, the HOLE ID shall be written directly on the core.  If the core contains more than one layer, layer boundaries shall be clearly marked, and each layer numbered.  For bulk samples, the SPECIMEN ID shall be written directly on the bag, bucket or can that contains the sample.

Packaging

Suggestions for labeling and combining the samples for shipment are as follows:

- All samples of like material (e.g., asphaltic concrete surface and binder) shall be placed in separate boxes or separate compartments of one box.

- Each sample shall have a label or tag attached that clearly identifies the material.  It is recommended that the label be color-coded by destination (e.g., contract Lab, FHWA lab, MRL, etc.).

- Each core shall be surrounded with "bubble-wrap" or other acceptable cushioning material on all sides within the shipping box.

- All bulk samples shall be marked with two labels or tags. One shall be placed inside the bag and one attached to the outside. A jar sample for moisture testing of each bulk sample shall be placed inside the bulk sample bag.

- All shipping boxes should be wood of suitable grade and construction to withstand shipping and subsequent moving without breakage of the box or damaging of samples.

- All boxes should be adequately secured by nails or screws prior to shipping.

LTPP Field Operations Information Sheets 1 and 2 shall be sent with each shipment of materials samples.

TABLE 3: PROJECT LAYER NUMBERING

| Layer No. | Project Layer Code | Thickness | Material Code | Description |
| --- | --- | --- | --- | --- |
| 1 | A |  | 51 | Subgrade - Clay |
| 2 | B | 4.0” | 23 | Base – Crushed Stone/Gravel |
| 3 | C | 2.5” | 01 | Existing AC Pavement |
| 4 | D | 1.5” | 01 | Existing AC Pavement |
| 5 | E | 2.75” | 01 | Existing AC Pavement |
| 6 | F | 2.25” | 01 | Existing AC Pavement |
| 7 | G | 1.75 – 2.0” | 01 | Experimental AC Overlay |

TABLE 4: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples (Ship to) | Sample Location |
| --- | --- | --- | --- |
|  | DURING CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC (PLANT) |  |  |
|  | 1-gallon can virgin AC Binder Grade 64-22H | 1 (CLTC) | H01001 |
|  |  | 1 (TFHRC) | H02001 |
|  |  | 10 (MRL) | H03001, H01002-H03002, H01003-H03003, H01061-H02061 H03062 |
|  | 1-gallon can virgin AC Binder Grade 58-28S | 1 (CLTC) | H01063 |
|  |  | 1 (TFHRC) | H02063 |
|  |  | 22 (MRL) | H03063-H04063, H01064-H04064, H01065-H04065, H01067-H06067, H12067-H17067 |
|  | 1-gallon can virgin AC Binder Grade 46-34S | 1 (CLTC) | H01066 |
|  |  | 1 (TFHRC) | H02066 |
|  |  | 10 (MRL) | H03066-H12066 |
|  | 5-gallon bucket combined aggregate Gradation #1 | 35 (MRL) | H04001-H05001, H09001-H11001, H04002-H05002,H08002-H10002, H04003-H05003, H11003-H13003, H07062-H08062, H10062-H12062, H05064-H06064, H10064-H12064, H05065-H06065, H08065-H10065, H13066-H14066, H18066-H20066 |
|  | 5-gallon bucket combined aggregate Gradation #2 (w/SG) | 10 (MRL) | H04061-H05061, H06061-H08061, H05063-H06063, H11063-H13063 |
|  | 5-gallon bucket combined aggregate Gradation #3 (w/MAN SAND) | 5 (MRL) | H07067-H08067, H18067-H20067 |
|  | 50 lb bulk sample RAP | 1 (CLTC) | H06001 |
|  | 5-gallon bucket RAP | 10 (MRL) | H07001-H08001, H06002-H07002, H06003-H07003, H09062, H07064, H07065, H15066 |
|  | 50 lb bulk sample RAS | 1 (CLTC) | H07063 |
|  | 5-gallon bucket RAS | 10 (MRL) | H08063-H10063, H08064-H09064 H16066-H17066, H09067-H11067 |
|  | 1-gallon chemical additive (Evotherm®) | 3 (MRL) | H08003-H10003 |
|  | 1-gallon chemical additive (EvoFlex®) | 3 (MRL) | H21067, H13062, H14062 |
|  | 1-gallon anti-strip agent (Morlife T280) | 3 (MRL) | H12001, H11002, H14003 |
|  | 1-gallon asphalt modifier (IPC-70) | 3 (MRL) | H22067-H24067 |

TABLE 4: SCOPE OF MATERIAL SAMPLING (Continued)

| Material and Sample Description |  | No. of Samples (Ship to) | Sample Location |
| --- | --- | --- | --- |
| A. | EXPERIMENTAL AC (FIELD) |  |  |
|  | 5-gallon buckets uncompacted AC mix | 150 (MRL) | F01001-F15001, F01002-F15002, F01003-F15003, F01061-F15061, F01062-F15062, F01063-F15063, F01064-F15064, F01065-F15065, F01066-F15066, F01067-F15067 |
|  | 12" Core | 20 (CLTC) | A01001-A02001, A01002-A02002, A01003-A02003, A01061-A02061, A01062-A02062, A01063-A02063, A01064-A02064, A01065-A02065, A01066-A02066, A01067-A02067 |
|  | 6" Core | 140 (100 to CLTC) (40 to MRL) | C01001-C14001, C01002-C14002, C01003-C14003, C01061-C14061, C01062-C14062, C01063-C14063, C01064-C14064, C01065-C14065, C01066-C14066, C01067-C14067 |
| B. | ORIGINAL HMAC LAYERS (4 LAYERS) |  |  |
|  | 12" Core | 2 (CLTC) | A01001, A01003 |
|  | 6" Core | 6 (CLTC) | C01001-C03001, C01003-C03003 |
| C. | CRUSHED STONE/GRAVEL BASE |  |  |
|  | 150 lb bulk sample | 2 (CLTC) | A01001-A02001, A01003-A02003 |
| D. | SUBGRADE |  |  |
|  | 150 lb bulk sample | 2 (CLTC) | A01001-A02001, A01003-A02003 |
|  | Moisture content jar sample | 2 (CLTC) | A01001-A02001, A01003-A02003 |

TABLE 5: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | PRE-CONSTRUCTION TESTING |  |  |
| A. | ORIGINAL HMAC |  |  |
|  | Elevation Survey | 10 | All Sections |
|  | POST-CONSTRUCTION TESTING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Elevation Survey | 10 | All Sections |
|  | In situ density measurement | 30 | T01001-T03001, T01002-T03002, T01003-T03003, T01061-T03061, T01062-T03062, T01063-T03063, T01064-T03064, T01065-T03065, T01066-T03066, T01067-T03067 |
|  | Core Examination and Thickness (P01/AC01) | 160 | A01001-A02001, A01002-A02002, A01003-A02003, A01061-A02061, A01062-A02062, A01063-A02063, A01064-A02064, A01065-A02065, A01066-A02066, A01067-A02067, C01001-C14001, C01002-C14002, C01003-C14003, C01061-C14061, C01062-C14062, C01063-C14063, C01064-C14064, C01065-C14065, C01066-C14066, C01067-C14067 |
| B. | ORIGINAL HMAC LAYERS (4 LAYERS) |  |  |
|  | Core Examination and Thickness (P01/AC01) | 8 | A01001, A01003, C01001-C03001, C01003-C03003 |
| C. | CRUSHED STONE/GRAVEL BASE |  |  |
|  | DCP | 10 | C14001,C14002,C14003,C14061,C14062, C14063, C14064, C14065, C14066, C14067 |
| D. | SUBGRADE |  |  |
|  | DCP | 10 | C14001,C14002,C14003,C14061,C14062, C14063, C14064, C14065, C14066, C14067 |

Section 29AA01 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03001

T02001

T01001

Traffic

FIGURE 2: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA01 MISSOURI SPS-10

Section 29AA02 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03002

T02002

T01002

Traffic

FIGURE 3: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA02 MISSOURI SPS-10

Section 29AA03 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03003

T02003

T01003

Traffic

FIGURE 4: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA03 MISSOURI SPS-10

Section 29AA61 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03061

T02061

T01061

Traffic

FIGURE 5: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA61 MISSOURI SPS-10

Section 29AA62 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03062

T02062

T01062

Traffic

FIGURE 6: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA62 MISSOURI SPS-10

Section 29AA63 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03063

T02063

T01063

Traffic

FIGURE 7: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA63 MISSOURI SPS-10

Section 29AA64 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03064

T02064

T01064

Traffic

FIGURE 8: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA64 MISSOURI SPS-10

Section 29AA65 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03065

T02065

T01065

Traffic

FIGURE 9: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA65 MISSOURI SPS-10

Section 29AA66 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03066

T02066

T01066

Traffic

FIGURE 10: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA66 MISSOURI SPS-10

Section 29AA67 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03067

T02067

T01067

Traffic

FIGURE 11: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 29AA67 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA01

Description: HMAC Control Section

2” SP125C w/ PG 64-22H

24 % RAP; 0 % RAS

Morlife® T280 1%/AC

Sampling Area: 01

Sampling Interval: t0

Shoulder

C02001

C04001

C06001

C08001

C10001

C12001

C14001

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01001

C03001

C05001

C07001

C09001

C11001

C13001

A01001

A02001

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

12” Core Experimental AC; Auger Base and Subgrade

12” Core Experimental AC and Original HMAC; Auger Base and Subgrade; DCP

FIGURE 12: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA01 AT TIME 0 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA02

Description: WMA with Foaming Process with 2.0% water - Astec ® Mixing Unit

2” SP125C w/ PG 64-22H

25 % RAP; 0 % RAS

Morlife® T280 1%/AC

Sampling Area: 03

Sampling Interval: t0

Shoulder

C02002

C04002

C06002

C08002

C10002

C12002

C14002

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01002

C03002

C05002

C07002

C09002

C11002

C13002

A01002

A02002

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 13: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA02 AT TIME 0 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA03

Description: WMA with Evotherm® Chem. Additive 0.5%/AC

2” SP125C w/ PG 64-22H

25 % RAP; 0 % RAS

Morlife® T280 1%/AC

Sampling Area: 05

Sampling Interval: t0

Shoulder

C02003

C04003

C06003

C08003

C10003

C12003

C14003

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01003

C03003

C05003

C07003

C09003

C11003

C13003

A01003

A02003

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

12” Core Experimental AC; Auger Base and Subgrade

12” Core Experimental AC and Original HMAC; Auger Base and Subgrade; DCP

FIGURE 14: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA03 AT TIME 0 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA61

Description: Supplemental Section - Virgin Mix

2” SP125C w/ PG 64-22H

0 % RAP; 0 % RAS

Morlife® T280 1%/AC

Sampling Area: 07

Sampling Interval: t0

Shoulder

C02061

C04061

C06061

C08061

C10061

C12061

C14061

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01061

C03061

C05061

C07061

C09061

C11061

C13061

A01061

A02061

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 15: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA61 AT TIME 0 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA62

Description: Supplemental Section - RAP Mix

2” SP125C w/ Final Extracted Binder = PG 77.1-22.3

Virgin Binder = PG 64-22H

35 % RAP; 0 % RAS

EvoFlex® Chemical Additive 3.0%/AC

Morlife® T280 1%/AC

Sampling Area: 09

Sampling Interval: t0

Shoulder

C02062

C04062

C06062

C08062

C10062

C12062

C14062

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01062

C03062

C05062

C07062

C09062

C11062

C13062

A01062

A02062

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 16: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA62 AT TIME 0 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA63

Description: Supplemental Section - RAS Mix

2” SP125C w/ PG 58-28S

0 % RAP; 17 % RAS

Morlife® T280 1%/AC

Sampling Area: 11

Sampling Interval: t0

Shoulder

C02063

C04063

C06063

C08063

C10063

C12063

C14063

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01063

C03063

C05063

C07063

C09063

C11063

C13063

A01063

A02063

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 17: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA63 AT TIME 0 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA64

Description: Supplemental Section – RAP/RAS Mix

2” SP125C w/ PG 58-28S

18 % RAP; 15 % RAS

Morlife® T280 1%/AC

Sampling Area: 13

Sampling Interval: t0

Shoulder

C02064

C04064

C06064

C08064

C10064

C12064

C14064

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01064

C03064

C05064

C07064

C09064

C11064

C13064

A01064

A02064

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 18: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA64 AT TIME 0 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA65

Description: Supplemental Section - RAP Mix

2” SP125C w/ PG 58-28S

33 % RAP; 0 % RAS

Minimum 15.0% VMA

Morlife® T280 1%/AC

Sampling Area: 15

Sampling Interval: t0

Shoulder

C02065

C04065

C06065

C08065

C10065

C12065

C14065

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01065

C03065

C05065

C07065

C09065

C11065

C13065

A01065

A02065

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 19: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA65 AT TIME 0 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA66

Description: Supplemental Section – RAP/RAS Mix

2” SP125C w/ Final Extracted Binder Grade = PG 72-26.1

Virgin Binder = PG46-34S

16 % RAP; 30 % RAS

Morlife® T280 2%/AC

Sampling Area: 17

Sampling Interval: t0

Shoulder

C02066

C04066

C06066

C08066

C10066

C12066

C14066

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01066

C03066

C05066

C07066

C09066

C11066

C13066

A01066

A02066

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 20: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA66 AT TIME 0 MISSOURI SPS-10

0-70

0-50

Section STA:

Section: 29AA67

Description: Supplemental Section - RAS Mix

2” SP125C w/ Final Extracted Binder = PG 77.8-25.6

Virgin Binder = PG58-28S

0 % RAP; 36 % RAS

EvoFlex® 3.5%AC, AC Modifier IPC-70 3.5%/AC

Morlife® T280 1%/AC

Sampling Area: 19

Sampling Interval: t0

Shoulder

C02067

C04067

C06067

C08067

C10067

C12067

C14067

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01067

C03067

C05067

C07067

C09067

C11067

C13067

A01067

A02067

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 21: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA67 AT TIME 0 MISSOURI SPS-10

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 29AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01001 | 7 | BA01001 | C21A01L07 | 12" Core | CLTC |
|  | 6 |  | C21A01L06 |  |  |
|  | 5 |  | C21A01L05 |  |  |
|  | 4 |  | C21A01L04 |  |  |
|  | 3 |  | C21A01L03 |  |  |
|  | 2 | BG01001 | C21A01L02 | 75 lb. Bulk Sample |  |
|  | 1 | BS01001 | C21A01L01 | 75 lb. Bulk Sample |  |
|  | 1 | MS01001 | C21AM1L01 | Moisture Content Jar Sample |  |
| A02001 | 7 | BA02001 | C21A02L07 | 12" Core Layer |  |
|  | 6 | BA02001 | C21A02L06 | 12" Core Layer |  |
|  | 5 | BA02001 | C21A02L05 | 12" Core Layer |  |
|  | 4 | BA02001 | C21A02L04 | 12" Core Layer |  |
|  | 3 | BA02001 | C21A02L03 | 12" Core Layer |  |
|  | 2 | BG02001 | C21A02L02 | 75 lb. Bulk Sample |  |
|  | 1 | BS02001 | C21A02L01 | 75 lb. Bulk Sample |  |
|  | 1 | MS02001 | C21AM2L01 | Moisture Content Jar Sample |  |
| C01001 | 7 | CA01001 | C21C01L07 | 6" Core | CLTC |
|  | 6 |  | C21C01L06 |  |  |
|  | 5 |  | C21C01L05 |  |  |
|  | 4 |  | C21C01L04 |  |  |
|  | 3 |  | C21C01L03 |  |  |
| C02001 | 7 | CA02001 | C21C02L07 | 6" Core |  |
|  | 6 |  | C21C02L06 |  |  |
|  | 5 |  | C21C02L05 |  |  |
|  | 4 |  | C21C02L04 |  |  |
|  | 3 |  | C21C02L03 |  |  |
| C03001 | 7 | CA03001 | C21C03L07 | 6" Core |  |
|  | 6 |  | C21C03L06 |  |  |
|  | 5 |  | C21C03L05 |  |  |
|  | 4 |  | C21C03L04 |  |  |
|  | 3 |  | C21C03L03 |  |  |

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 29AA01 (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| C04001 | 7 | CA04001 | C21C04L07 | 6" Core | CLTC |
| C05001 | 7 | CA05001 | C21C05L07 | 6" Core |  |
| C05001 | 6 | CA05001 | C21C05L06 | 6" Core |  |
| C06001 | 7 | CA06001 | C21C06L07 | 6" Core |  |
| C07001 | 7 | CA07001 | C21C07L07 | 6" Core |  |
| C08001 | 7 | CA08001 | C21C08L07 | 6" Core |  |
| C09001 | 7 | CA09001 | C21C09L07 | 6" Core |  |
| C10001 | 7 | CA10001 | C21C10L07 | 6" Core |  |
| C11001 | 7 | CA11001 | C21C11L07 | 6" Core | MRL |
| C12001 | 7 | CA12001 | C21C12L07 | 6" Core |  |
| C13001 | 7 | CA13001 | C21C13L07 | 6" Core |  |
| C14001 | 7 | CA14001 | C21C14L07 | 6" Core |  |
| F01001 | 7 | BA03001 | C21F01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02001 | 7 | BA04001 | C21F02L07 |  |  |
| F03001 | 7 | BA05001 | C21F03L07 |  |  |
| F04001 | 7 | BA06001 | C21F04L07 |  |  |
| F05001 | 7 | BA07001 | C21F05L07 |  |  |
| F06001 | 7 | BA08001 | C21F06L07 |  |  |
| F07001 | 7 | BA09001 | C21F07L07 |  |  |
| F08001 | 7 | BA10001 | C21F08L07 |  |  |
| F09001 | 7 | BA11001 | C21F09L07 |  |  |
| F10001 | 7 | BA12001 | C21F10L07 |  |  |
| F11001 | 7 | BA13001 | C21F11L07 |  |  |
| F12001 | 7 | BA14001 | C21F12L07 |  |  |
| F13001 | 7 | BA15001 | C21F13L07 |  |  |
| F14001 | 7 | BA16001 | C21F14L07 |  |  |
| F15001 | 7 | BA17001 | C21F15L07 |  |  |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 29AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01002 | 7 | BA01002 | C22A01L07 | 12" Core | CLTC |
| A02002 | 7 | BA02002 | C22A02L07 | 12" Core |  |
| C01002 | 7 | CA01002 | C22C01L07 | 6" Core | CLTC |
| C02002 | 7 | CA02002 | C22C02L07 | 6" Core |  |
| C03002 | 7 | CA03002 | C22C03L07 | 6" Core |  |
| C04002 | 7 | CA04002 | C22C04L07 | 6" Core |  |
| C05002 | 7 | CA05002 | C22C05L07 | 6" Core |  |
| C06002 | 7 | CA06002 | C22C06L07 | 6" Core |  |
| C07002 | 7 | CA07002 | C22C07L07 | 6" Core |  |
| C08002 | 7 | CA08002 | C22C08L07 | 6" Core |  |
| C09002 | 7 | CA09002 | C22C09L07 | 6" Core |  |
| C10002 | 7 | CA10002 | C22C10L07 | 6" Core |  |
| C11002 | 7 | CA11002 | C22C11L07 | 6" Core | MRL |
| C12002 | 7 | CA12002 | C22C12L07 | 6" Core |  |
| C13002 | 7 | CA13002 | C22C13L07 | 6" Core |  |
| C14002 | 7 | CA14002 | C22C14L07 | 6" Core |  |
| F01002 | 7 | BA03002 | C22F01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02002 | 7 | BA04002 | C22F02L07 |  |  |
| F03002 | 7 | BA05002 | C22F03L07 |  |  |
| F04002 | 7 | BA06002 | C22F04L07 |  |  |
| F05002 | 7 | BA07002 | C22F05L07 |  |  |
| F06002 | 7 | BA08002 | C22F06L07 |  |  |
| F07002 | 7 | BA09002 | C22F07L07 |  |  |
| F08002 | 7 | BA10002 | C22F08L07 |  |  |
| F09002 | 7 | BA11002 | C22F09L07 |  |  |
| F10002 | 7 | BA12002 | C22F10L07 |  |  |
| F11002 | 7 | BA13002 | C22F11L07 |  |  |
| F12002 | 7 | BA14002 | C22F12L07 |  |  |
| F13002 | 7 | BA15002 | C22F13L07 |  |  |
| F14002 | 7 | BA16002 | C22F14L07 |  |  |
| F15002 | 7 | BA17002 | C22F15L07 |  |  |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 29AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01003 | 7 | BA01003 | C23A01L07 | 12" Core | CLTC |
|  | 6 | BA01003 | C23A01L06 |  |  |
|  | 5 | BA01003 | C23A01L05 |  |  |
|  | 4 | BA01003 | C23A01L04 |  |  |
|  | 3 | BA01003 | C23A01L03 |  |  |
|  | 2 | BG01003 | C23A01L02 | 75 lb. Bulk Sample |  |
|  | 1 | BS01003 | C23A01L01 | 75 lb. Bulk Sample |  |
|  | 1 | MS01003 | C23AM1L01 | Moisture Content Jar Sample |  |
| A02003 | 7 | BA02003 | C23A02L07 | 12" Core |  |
|  | 2 | BG02003 | C23A02L02 | 75 lb. Bulk Sample |  |
|  | 1 | BS02003 | C23A02L01 | 75 lb. Bulk Sample |  |
|  | 1 | MS02003 | C23AM2L01 | Moisture Content Jar Sample |  |
| C01003 | 7 | CA01003 | C23C01L07 | 6" Core | CLTC |
|  | 6 |  | C23C01L06 |  |  |
|  | 5 |  | C23C01L05 |  |  |
|  | 4 |  | C23C01L04 |  |  |
|  | 3 |  | C23C01L03 |  |  |
| C02003 | 7 | CA02003 | C23C02L07 | 6" Core |  |
|  | 6 |  | C23C02L06 |  |  |
|  | 5 |  | C23C02L05 |  |  |
|  | 4 |  | C23C02L04 |  |  |
|  | 3 |  | C23C02L03 |  |  |
| C03003 | 7 | CA03003 | C23C03L07 | 6" Core |  |
|  | 6 |  | C23C03L06 |  |  |
|  | 5 |  | C23C03L05 |  |  |
|  | 4 |  | C23C03L04 |  |  |
|  | 3 |  | C23C03L03 |  |  |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 29AA03 (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| C04003 | 7 | CA04003 | C23C04L07 | 6" Core | CLTC |
| C05003 | 7 | CA05003 | C23C05L07 | 6" Core |  |
| C06003 | 7 | CA06003 | C23C06L07 | 6" Core |  |
| C07003 | 7 | CA07003 | C23C07L07 | 6" Core |  |
| C08003 | 7 | CA08003 | C23C08L07 | 6" Core |  |
| C09003 | 7 | CA09003 | C23C09L07 | 6" Core |  |
| C10003 | 7 | CA10003 | C23C10L07 | 6" Core |  |
| C11003 | 7 | CA11003 | C23C11L07 | 6" Core | MRL |
| C12003 | 7 | CA12003 | C23C12L07 | 6" Core |  |
| C13003 | 7 | CA13003 | C23C13L07 | 6" Core |  |
| C14003 | 7 | CA14003 | C23C14L07 | 6" Core |  |
| F01003 | 7 | BA03003 | C23F01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02003 | 7 | BA04003 | C23F02L07 |  |  |
| F03003 | 7 | BA05003 | C23F03L07 |  |  |
| F04003 | 7 | BA06003 | C23F04L07 |  |  |
| F05003 | 7 | BA07003 | C23F05L07 |  |  |
| F06003 | 7 | BA08003 | C23F06L07 |  |  |
| F07003 | 7 | BA09003 | C23F07L07 |  |  |
| F08003 | 7 | BA10003 | C23F08L07 |  |  |
| F09003 | 7 | BA11003 | C23F09L07 |  |  |
| F10003 | 7 | BA12003 | C23F10L07 |  |  |
| F11003 | 7 | BA13003 | C23F11L07 |  |  |
| F12003 | 7 | BA14003 | C23F12L07 |  |  |
| F13003 | 7 | BA15003 | C23F13L07 |  |  |
| F14003 | 7 | BA16003 | C23F14L07 |  |  |
| F15003 | 7 | BA17003 | C23F15L07 |  |  |

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 29AA61

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01061 | 7 | BA01061 | C2AA01L07 | 12" Core |  |
| A01061 | 6 | BA01061 | C2AA01L06 | 12" Core |  |
| A01061 | 5 | BA01061 | C2AA01L05 | 12" Core |  |
| A01061 | 4 | BA01061 | C2AA01L04 | 12" Core |  |
| A01061 | 3 | BA01061 | C2AA01L03 | 12" Core | CLTC |
| A02061 | 7 | BA02061 | C2AA02L07 | 12" Core |  |
| C01061 | 7 | CA01061 | C2AC01L07 | 6" Core | CLTC |
| C02061 | 7 | CA02061 | C2AC02L07 | 6" Core |  |
| C03061 | 7 | CA03061 | C2AC03L07 | 6" Core |  |
| C04061 | 7 | CA04061 | C2AC04L07 | 6" Core |  |
| C05061 | 7 | CA05061 | C2AC05L07 | 6" Core |  |
| C06061 | 7 | CA06061 | C2AC06L07 | 6" Core |  |
| C07061 | 7 | CA07061 | C2AC07L07 | 6" Core |  |
| C08061 | 7 | CA08061 | C2AC08L07 | 6" Core |  |
| C09061 | 7 | CA09061 | C2AC09L07 | 6" Core |  |
| C10061 | 7 | CA10061 | C2AC10L07 | 6" Core |  |
| C11061 | 7 | CA11061 | C2AC11L07 | 6" Core | MRL |
| C12061 | 7 | CA12061 | C2AC12L07 | 6" Core |  |
| C13061 | 7 | CA13061 | C2AC13L07 | 6" Core |  |
| C14061 | 7 | CA14061 | C2AC14L07 | 6" Core |  |
| F01061 | 7 | BA03061 | C2AF01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02061 | 7 | BA04061 | C2AF02L07 |  |  |
| F03061 | 7 | BA05061 | C2AF03L07 |  |  |
| F04061 | 7 | BA06061 | C2AF04L07 |  |  |
| F05061 | 7 | BA07061 | C2AF05L07 |  |  |
| F06061 | 7 | BA08061 | C2AF06L07 |  |  |
| F07061 | 7 | BA09061 | C2AF07L07 |  |  |
| F08061 | 7 | BA10061 | C2AF08L07 |  |  |
| F09061 | 7 | BA11061 | C2AF09L07 |  |  |
| F10061 | 7 | BA12061 | C2AF10L07 |  |  |
| F11061 | 7 | BA13061 | C2AF11L07 |  |  |
| F12061 | 7 | BA14061 | C2AF12L07 |  |  |
| F13061 | 7 | BA15061 | C2AF13L07 |  |  |
| F14061 | 7 | BA16061 | C2AF14L07 |  |  |
| F15061 | 7 | BA17061 | C2AF15L07 |  |  |

TABLE 10: SAMPLES ACQUIRED FROM TEST SECTION 29AA62

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01062 | 7 | BA01062 | C2BA01L07 | 12" Core | CLTC |
| A01062 | 6 | BA01062 | C2BA01L06 | 12" Core |  |
| A01062 | 5 | BA01062 | C2BA01L05 | 12" Core |  |
| A01062 | 4 | BA01062 | C2BA01L04 | 12" Core |  |
| A01062 | 3 | BA01062 | C2BA01L03 | 12" Core |  |
| A02062 | 7 | BA02062 | C2BA02L07 | 12" Core |  |
| A02062 | 6 | BA02062 | C2BA02L06 | 12" Core |  |
| A02062 | 5 | BA02062 | C2BA02L05 | 12" Core |  |
| A02062 | 4 | BA02062 | C2BA02L04 | 12" Core |  |
| A02062 | 3 | BA02062 | C2BA02L03 | 12" Core |  |
| C01062 | 7 | CA01062 | C2BC01L07 | 6" Core | CLTC |
| C02062 | 7 | CA02062 | C2BC02L07 | 6" Core |  |
| C03062 | 7 | CA03062 | C2BC03L07 | 6" Core |  |
| C04062 | 7 | CA04062 | C2BC04L07 | 6" Core |  |
| C05062 | 7 | CA05062 | C2BC05L07 | 6" Core |  |
| C06062 | 7 | CA06062 | C2BC06L07 | 6" Core |  |
| C07062 | 7 | CA07062 | C2BC07L07 | 6" Core |  |
| C08062 | 7 | CA08062 | C2BC08L07 | 6" Core |  |
| C09062 | 7 | CA09062 | C2BC09L07 | 6" Core |  |
| C10062 | 7 | CA10062 | C2BC10L07 | 6" Core |  |
| C11062 | 7 | CA11062 | C2BC11L07 | 6" Core | MRL |
| C12062 | 7 | CA12062 | C2BC12L07 | 6" Core |  |
| C13062 | 7 | CA13062 | C2BC13L07 | 6" Core |  |
| C14062 | 7 | CA14062 | C2BC14L07 | 6" Core |  |
| F01062 | 7 | BA03062 | C2BF01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02062 | 7 | BA04062 | C2BF02L07 |  |  |
| F03062 | 7 | BA05062 | C2BF03L07 |  |  |
| F04062 | 7 | BA06062 | C2BF04L07 |  |  |
| F05062 | 7 | BA07062 | C2BF05L07 |  |  |
| F06062 | 7 | BA08062 | C2BF06L07 |  |  |
| F07062 | 7 | BA09062 | C2BF07L07 |  |  |
| F08062 | 7 | BA10062 | C2BF08L07 |  |  |
| F09062 | 7 | BA11062 | C2BF09L07 |  |  |
| F10062 | 7 | BA12062 | C2BF10L07 |  |  |
| F11062 | 7 | BA13062 | C2BF11L07 |  |  |
| F12062 | 7 | BA14062 | C2BF12L07 |  |  |
| F13062 | 7 | BA15062 | C2BF13L07 |  |  |
| F14062 | 7 | BA16062 | C2BF14L07 |  |  |
| F15062 | 7 | BA17062 | C2BF15L07 |  |  |

TABLE 11: SAMPLES ACQUIRED FROM TEST SECTION 29AA63

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01063 | 7 | BA01063 | C2CA01L07 | 12" Core | CLTC |
| A01063 | 6 | BA01063 | C2CA01L06 | 12" Core | CLTC |
| A01063 | 5 | BA01063 | C2CA01L05 | 12" Core | CLTC |
| A01063 | 4 | BA01063 | C2CA01L04 | 12" Core | CLTC |
| A01063 | 3 | BA01063 | C2CA01L03 | 12" Core | CLTC |
| A02063 | 7 | BA02063 | C2CA02L07 | 12" Core |  |
| A02063 | 6 | BA02063 | C2CA02L06 | 12" Core |  |
| A02063 | 5 | BA02063 | C2CA02L05 | 12" Core |  |
| A02063 | 4 | BA02063 | C2CA02L04 | 12" Core |  |
| A02063 | 3 | BA02063 | C2CA02L03 | 12" Core |  |
| C01063 | 7 | CA01063 | C2CC01L07 | 6" Core | CLTC |
| C02063 | 7 | CA02063 | C2CC02L07 | 6" Core |  |
| C03063 | 7 | CA03063 | C2CC03L07 | 6" Core |  |
| C04063 | 7 | CA04063 | C2CC04L07 | 6" Core |  |
| C05063 | 7 | CA05063 | C2CC05L07 | 6" Core |  |
| C06063 | 7 | CA06063 | C2CC06L07 | 6" Core |  |
| C07063 | 7 | CA07063 | C2CC07L07 | 6" Core |  |
| C08063 | 7 | CA08063 | C2CC08L07 | 6" Core |  |
| C09063 | 7 | CA09063 | C2CC09L07 | 6" Core |  |
| C10063 | 7 | CA10063 | C2CC10L07 | 6" Core |  |
| C11063 | 7 | CA11063 | C2CC11L07 | 6" Core | MRL |
| C12063 | 7 | CA12063 | C2CC12L07 | 6" Core |  |
| C13063 | 7 | CA13063 | C2CC13L07 | 6" Core |  |
| C14063 | 7 | CA14063 | C2CC14L07 | 6" Core |  |
| F01063 | 7 | BA03063 | C2CF01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02063 | 7 | BA04063 | C2CF02L07 |  |  |
| F03063 | 7 | BA05063 | C2CF03L07 |  |  |
| F04063 | 7 | BA06063 | C2CF04L07 |  |  |
| F05063 | 7 | BA07063 | C2CF05L07 |  |  |
| F06063 | 7 | BA08063 | C2CF06L07 |  |  |
| F07063 | 7 | BA09063 | C2CF07L07 |  |  |
| F08063 | 7 | BA10063 | C2CF08L07 |  |  |
| F09063 | 7 | BA11063 | C2CF09L07 |  |  |
| F10063 | 7 | BA12063 | C2CF10L07 |  |  |
| F11063 | 7 | BA13063 | C2CF11L07 |  |  |
| F12063 | 7 | BA14063 | C2CF12L07 |  |  |
| F13063 | 7 | BA15063 | C2CF13L07 |  |  |
| F14063 | 7 | BA16063 | C2CF14L07 |  |  |
| F15063 | 7 | BA17063 | C2CF15L07 |  |  |

TABLE 12: SAMPLES ACQUIRED FROM TEST SECTION 29AA64

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01064 | 7 | BA01064 | C2DA01L07 | 12" Core | CLTC |
| A01064 | 6 | BA01064 | C2DA01L06 | 12" Core | CLTC |
| A01064 | 5 | BA01064 | C2DA01L05 | 12" Core | CLTC |
| A01064 | 4 | BA01064 | C2DA01L04 | 12" Core | CLTC |
| A01064 | 3 | BA01064 | C2DA01L03 | 12" Core | CLTC |
| A02064 | 7 | BA02064 | C2DA02L07 | 12" Core |  |
| A02064 | 6 | BA02064 | C2DA02L06 | 12" Core |  |
| A02064 | 5 | BA02064 | C2DA02L05 | 12" Core |  |
| A02064 | 4 | BA02064 | C2DA02L04 | 12" Core |  |
| A02064 | 3 | BA02064 | C2DA02L03 | 12" Core |  |
| C01064 | 7 | CA01064 | C2DC01L07 | 6" Core | CLTC |
| C02064 | 7 | CA02064 | C2DC02L07 | 6" Core |  |
| C03064 | 7 | CA03064 | C2DC03L07 | 6" Core |  |
| C04064 | 7 | CA04064 | C2DC04L07 | 6" Core |  |
| C05064 | 7 | CA05064 | C2DC05L07 | 6" Core |  |
| C06064 | 7 | CA06064 | C2DC06L07 | 6" Core |  |
| C07064 | 7 | CA07064 | C2DC07L07 | 6" Core |  |
| C08064 | 7 | CA08064 | C2DC08L07 | 6" Core |  |
| C09064 | 7 | CA09064 | C2DC09L07 | 6" Core |  |
| C10064 | 7 | CA10064 | C2DC10L07 | 6" Core |  |
| C11064 | 7 | CA11064 | C2DC11L07 | 6" Core | MRL |
| C12064 | 7 | CA12064 | C2DC12L07 | 6" Core |  |
| C13064 | 7 | CA13064 | C2DC13L07 | 6" Core |  |
| C14064 | 7 | CA14064 | C2DC14L07 | 6" Core |  |
| F01064 | 7 | BA03064 | C2DF01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02064 | 7 | BA04064 | C2DF02L07 |  |  |
| F03064 | 7 | BA05064 | C2DF03L07 |  |  |
| F04064 | 7 | BA06064 | C2DF04L07 |  |  |
| F05064 | 7 | BA07064 | C2DF05L07 |  |  |
| F06064 | 7 | BA08064 | C2DF06L07 |  |  |
| F07064 | 7 | BA09064 | C2DF07L07 |  |  |
| F08064 | 7 | BA10064 | C2DF08L07 |  |  |
| F09064 | 7 | BA11064 | C2DF09L07 |  |  |
| F10064 | 7 | BA12064 | C2DF10L07 |  |  |
| F11064 | 7 | BA13064 | C2DF11L07 |  |  |
| F12064 | 7 | BA14064 | C2DF12L07 |  |  |
| F13064 | 7 | BA15064 | C2DF13L07 |  |  |
| F14064 | 7 | BA16064 | C2DF14L07 |  |  |
| F15064 | 7 | BA17064 | C2DF15L07 |  |  |

TABLE 13: SAMPLES ACQUIRED FROM TEST SECTION 29AA65

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01065 | 7 | BA01065 | C2EA01L07 | 12" Core |  |
| A01065 | 6 | BA01065 | C2EA01L06 | 12" Core |  |
| A01065 | 5 | BA01065 | C2EA01L05 | 12" Core |  |
| A01065 | 4 | BA01065 | C2EA01L04 | 12" Core |  |
| A01065 | 3 | BA01065 | C2EA01L03 | 12" Core | CLTC |
| A02065 | 7 | BA02065 | C2EA02L07 | 12" Core |  |
| A02065 | 6 | BA02065 | C2EA02L06 | 12" Core |  |
| A02065 | 5 | BA02065 | C2EA02L05 | 12" Core |  |
| A02065 | 4 | BA02065 | C2EA02L04 | 12" Core |  |
| A02065 | 3 | BA02065 | C2EA02L03 | 12" Core |  |
| C01065 | 7 | CA01065 | C2EC01L07 | 6" Core | CLTC |
| C02065 | 7 | CA02065 | C2EC02L07 | 6" Core |  |
| C03065 | 7 | CA03065 | C2EC03L07 | 6" Core |  |
| C04065 | 7 | CA04065 | C2EC04L07 | 6" Core |  |
| C05065 | 7 | CA05065 | C2EC05L07 | 6" Core |  |
| C06065 | 7 | CA06065 | C2EC06L07 | 6" Core |  |
| C07065 | 7 | CA07065 | C2EC07L07 | 6" Core |  |
| C08065 | 7 | CA08065 | C2EC08L07 | 6" Core |  |
| C09065 | 7 | CA09065 | C2EC09L07 | 6" Core |  |
| C10065 | 7 | CA10065 | C2EC10L07 | 6" Core |  |
| C11065 | 7 | CA11065 | C2EC11L07 | 6" Core | MRL |
| C12065 | 7 | CA12065 | C2EC12L07 | 6" Core |  |
| C13065 | 7 | CA13065 | C2EC13L07 | 6" Core |  |
| C14065 | 7 | CA14065 | C2EC14L07 | 6" Core |  |
| F01065 | 7 | BA03065 | C2EF01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02065 | 7 | BA04065 | C2EF02L07 |  |  |
| F03065 | 7 | BA05065 | C2EF03L07 |  |  |
| F04065 | 7 | BA06065 | C2EF04L07 |  |  |
| F05065 | 7 | BA07065 | C2EF05L07 |  |  |
| F06065 | 7 | BA08065 | C2EF06L07 |  |  |
| F07065 | 7 | BA09065 | C2EF07L07 |  |  |
| F08065 | 7 | BA10065 | C2EF08L07 |  |  |
| F09065 | 7 | BA11065 | C2EF09L07 |  |  |
| F10065 | 7 | BA12065 | C2EF10L07 |  |  |
| F11065 | 7 | BA13065 | C2EF11L07 |  |  |
| F12065 | 7 | BA14065 | C2EF12L07 |  |  |
| F13065 | 7 | BA15065 | C2EF13L07 |  |  |
| F14065 | 7 | BA16065 | C2EF14L07 |  |  |
| F15065 | 7 | BA17065 | C2EF15L07 |  |  |

TABLE 14: SAMPLES ACQUIRED FROM TEST SECTION 29AA66

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01066 | 7 | BA01066 | C2FA01L07 | 12" Core |  |
| A01066 | 6 | BA01066 | C2FA01L06 | 12" Core |  |
| A01066 | 5 | BA01066 | C2FA01L05 | 12" Core |  |
| A01066 | 4 | BA01066 | C2FA01L04 | 12" Core |  |
| A01066 | 3 | BA01066 | C2FA01L03 | 12" Core | CLTC |
| A02066 | 7 | BA02066 | C2FA02L07 | 12" Core |  |
| A02066 | 6 | BA02066 | C2FA02L06 | 12" Core |  |
| A02066 | 5 | BA02066 | C2FA02L05 | 12" Core |  |
| A02066 | 4 | BA02066 | C2FA02L04 | 12" Core |  |
| A02066 | 3 | BA02066 | C2FA02L03 | 12" Core |  |
| C01066 | 7 | CA01066 | C2FC01L07 | 6" Core | CLTC |
| C02066 | 7 | CA02066 | C2FC02L07 | 6" Core |  |
| C03066 | 7 | CA03066 | C2FC03L07 | 6" Core |  |
| C04066 | 7 | CA04066 | C2FC04L07 | 6" Core |  |
| C05066 | 7 | CA05066 | C2FC05L07 | 6" Core |  |
| C06066 | 7 | CA06066 | C2FC06L07 | 6" Core |  |
| C07066 | 7 | CA07066 | C2FC07L07 | 6" Core |  |
| C08066 | 7 | CA08066 | C2FC08L07 | 6" Core |  |
| C09066 | 7 | CA09066 | C2FC09L07 | 6" Core |  |
| C10066 | 7 | CA10066 | C2FC10L07 | 6" Core |  |
| C11066 | 7 | CA11066 | C2FC11L07 | 6" Core | MRL |
| C12066 | 7 | CA12066 | C2FC12L07 | 6" Core |  |
| C13066 | 7 | CA13066 | C2FC13L07 | 6" Core |  |
| C14066 | 7 | CA14066 | C2FC14L07 | 6" Core |  |
| F01066 | 7 | BA03066 | C2FF01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02066 | 7 | BA04066 | C2FF02L07 |  |  |
| F03066 | 7 | BA05066 | C2FF03L07 |  |  |
| F04066 | 7 | BA06066 | C2FF04L07 |  |  |
| F05066 | 7 | BA07066 | C2FF05L07 |  |  |
| F06066 | 7 | BA08066 | C2FF06L07 |  |  |
| F07066 | 7 | BA09066 | C2FF07L07 |  |  |
| F08066 | 7 | BA10066 | C2FF08L07 |  |  |
| F09066 | 7 | BA11066 | C2FF09L07 |  |  |
| F10066 | 7 | BA12066 | C2FF10L07 |  |  |
| F11066 | 7 | BA13066 | C2FF11L07 |  |  |
| F12066 | 7 | BA14066 | C2FF12L07 |  |  |
| F13066 | 7 | BA15066 | C2FF13L07 |  |  |
| F14066 | 7 | BA16066 | C2FF14L07 |  |  |
| F15066 | 7 | BA17066 | C2FF15L07 |  |  |

TABLE 15: SAMPLES ACQUIRED FROM TEST SECTION 29AA67

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01067 | 7 | BA01067 | C2GA01L07 | 12" Core |  |
| A01067 | 6 | BA01067 | C2GA01L06 | 12" Core |  |
| A01067 | 5 | BA01067 | C2GA01L05 | 12" Core |  |
| A01067 | 4 | BA01067 | C2GA01L04 | 12" Core |  |
| A01067 | 3 | BA01067 | C2GA01L03 | 12" Core | CLTC |
| A02067 | 7 | BA02067 | C2GA02L07 | 12" Core |  |
| A02067 | 6 | BA02067 | C2GA02L06 | 12" Core |  |
| A02067 | 5 | BA02067 | C2GA02L05 | 12" Core |  |
| A02067 | 4 | BA02067 | C2GA02L04 | 12" Core |  |
| A02067 | 3 | BA02067 | C2GA02L03 | 12" Core |  |
| C01067 | 7 | CA01067 | C2GC01L07 | 6" Core | CLTC |
| C02067 | 7 | CA02067 | C2GC02L07 | 6" Core |  |
| C03067 | 7 | CA03067 | C2GC03L07 | 6" Core |  |
| C04067 | 7 | CA04067 | C2GC04L07 | 6" Core |  |
| C05067 | 7 | CA05067 | C2GC05L07 | 6" Core |  |
| C06067 | 7 | CA06067 | C2GC06L07 | 6" Core |  |
| C07067 | 7 | CA07067 | C2GC07L07 | 6" Core |  |
| C08067 | 7 | CA08067 | C2GC08L07 | 6" Core |  |
| C09067 | 7 | CA09067 | C2GC09L07 | 6" Core |  |
| C10067 | 7 | CA10067 | C2GC10L07 | 6" Core |  |
| C11067 | 7 | CA11067 | C2GC11L07 | 6" Core | MRL |
| C12067 | 7 | CA12067 | C2GC12L07 | 6" Core |  |
| C13067 | 7 | CA13067 | C2GC13L07 | 6" Core |  |
| C14067 | 7 | CA14067 | C2GC14L07 | 6" Core |  |
| F01067 | 7 | BA03067 | C2GF01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02067 | 7 | BA04067 | C2GF02L07 |  |  |
| F03067 | 7 | BA05067 | C2GF03L07 |  |  |
| F04067 | 7 | BA06067 | C2GF04L07 |  |  |
| F05067 | 7 | BA07067 | C2GF05L07 |  |  |
| F06067 | 7 | BA08067 | C2GF06L07 |  |  |
| F07067 | 7 | BA09067 | C2GF07L07 |  |  |
| F08067 | 7 | BA10067 | C2GF08L07 |  |  |
| F09067 | 7 | BA11067 | C2GF09L07 |  |  |
| F10067 | 7 | BA12067 | C2GF10L07 |  |  |
| F11067 | 7 | BA13067 | C2GF11L07 |  |  |
| F12067 | 7 | BA14067 | C2GF12L07 |  |  |
| F13067 | 7 | BA15067 | C2GF13L07 |  |  |
| F14067 | 7 | BA16067 | C2GF14L07 |  |  |
| F15067 | 7 | BA17067 | C2GF15L07 |  |  |

TABLE 16: SAMPLES ACQUIRED FROM PLANT

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| H01001 | 7 | BC01001 | C21H01L07 | 1 1-gallon can virgin AC Binder (PG 64-22H) | CLTC |
| H02001 | 7 | BC02001 | C21H02L07 | 1 1-gallon can virgin AC Binder (PG 64-22H) | TFHRC |
| H03001 | 7 | BC03001 | C21H03L07 | 10 1-gallon cans virgin AC Binder (PG 64-22H) | MRL |
| H01002 |  | BC01002 | C22H01L07 |  |  |
| H02002 |  | BC02002 | C22H02L07 |  |  |
| H03002 |  | BC03002 | C22H03L07 |  |  |
| H01003 |  | BC01003 | C23H01L07 |  |  |
| H02003 |  | BC02003 | C23H02L07 |  |  |
| H03003 |  | BC03003 | C23H03L07 |  |  |
| H01061 |  | BC01061 | C2AH01L07 |  |  |
| H02061 |  | BC02061 | C2AH02L07 |  |  |
| H03062 |  | BC03062 | C2BH03L07 |  |  |
| H01063 | 7 | BC01063 | C2CH01L07 | 1 1-gallon can virgin AC Binder (PG 58-28S) | CLTC |
| H02063 | 7 | BC02063 | C2CH02L07 | 1 1-gallon can virgin AC Binder (PG 58-28S) | TFHRC |
| H03063 | 7 | BC03063 | C2CH03L07 | 22 1-gallon cans virgin AC Binder (PG 58-28S) | MRL |
| H04063 |  | BC04063 | C2CH04L07 |  |  |
| H01064 |  | BC01064 | C2DH01L07 |  |  |
| H02064 |  | BC02064 | C2DH02L07 |  |  |
| H03064 |  | BC03064 | C2DH03L07 |  |  |
| H04064 |  | BC04064 | C2DH04L07 |  |  |
| H01065 |  | BC01065 | C2EH01L07 |  |  |
| H02065 |  | BC02065 | C2EH02L07 |  |  |
| H03065 |  | BC03065 | C2EH03L07 |  |  |
| H04065 |  | BC04065 | C2EH04L07 |  |  |
| H01067 |  | BC01067 | C2GH01L07 |  |  |
| H02067 |  | BC02067 | C2GH02L07 |  |  |
| H03067 |  | BC03067 | C2GH03L07 |  |  |
| H04067 |  | BC04067 | C2GH04L07 |  |  |
| H05067 |  | BC05067 | C2GH05L07 |  |  |
| H06067 |  | BC06067 | C2GH06L07 |  |  |
| H12067 |  | BC12067 | C2GH12L07 |  |  |
| H13067 |  | BC13067 | C2GH13L07 |  |  |
| H14067 |  | BC14067 | C2GH14L07 |  |  |
| H15067 |  | BC15067 | C2GH15L07 |  |  |
| H16067 |  | BC16067 | C2GH16L07 |  |  |
| H17067 |  | BC17067 | C2GH17L07 |  |  |

TABLE 16: SAMPLES ACQUIRED FROM PLANT (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| H01066 | 7 | BC01066 | C2FH01L07 | 1 1-gallon can virgin AC Binder (PG 46-34S) | CLTC |
| H02066 | 7 | BC02066 | C2FH02L07 | 1 1-gallon can virgin AC Binder (PG 46-34S) | TFHRC |
| H03066 | 7 | BC03066 | C2FH03L07 | 10 1-gallon cans virgin AC Binder (PG 46-34S) | MRL |
| H04066 |  | BC04066 | C2FH04L07 |  |  |
| H05066 |  | BC05066 | C2FH05L07 |  |  |
| H06066 |  | BC06066 | C2FH06L07 |  |  |
| H07066 |  | BC07066 | C2FH07L07 |  |  |
| H08066 |  | BC08066 | C2FH08L07 |  |  |
| H09066 |  | BC09066 | C2FH09L07 |  |  |
| H10066 |  | BC10066 | C2FH10L07 |  |  |
| H11066 |  | BC11066 | C2FH11L07 |  |  |
| H12066 |  | BC12066 | C2FH12L07 |  |  |

TABLE 16: SAMPLES ACQUIRED FROM PLANT (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| H04001 | 7 | BU01001 | C21H04L07 | 35 5-gallon buckets combined aggregate Gradation #1 | MRL |
| H05001 | 7 | BU02001 | C21H05L07 |  |  |
| H09001 | 7 | BU03001 | C21H09L07 |  |  |
| H10001 | 7 | BU04001 | C21H10L07 |  |  |
| H11001 | 7 | BU05001 | C21H11L07 |  |  |
| H04002 | 7 | BU01002 | C22H04L07 |  |  |
| H05002 | 7 | BU02002 | C22H05L07 |  |  |
| H08002 | 7 | BU03002 | C22H08L07 |  |  |
| H09002 | 7 | BU04002 | C22H09L07 |  |  |
| H10002 | 7 | BU05002 | C22H10L07 |  |  |
| H04003 | 7 | BU01003 | C23H04L07 |  |  |
| H05003 | 7 | BU02003 | C23H05L07 |  |  |
| H11003 | 7 | BU03003 | C23H11L07 |  |  |
| H12003 | 7 | BU04003 | C23H12L07 |  |  |
| H13003 | 7 | BU05003 | C23H13L07 |  |  |
| H07062 | 7 | BU01062 | C2BH07L07 |  |  |
| H08062 | 7 | BU02062 | C2BH08L07 |  |  |
| H10062 | 7 | BU03062 | C2BH10L07 |  |  |
| H11062 | 7 | BU04062 | C2BH11L07 |  |  |
| H12062 | 7 | BU05062 | C2BH12L07 |  |  |
| H05064 | 7 | BU01064 | C2DH05L07 |  |  |
| H06064 | 7 | BU02064 | C2DH06L07 |  |  |
| H10064 | 7 | BU03064 | C2DH10L07 |  |  |
| H11064 | 7 | BU04064 | C2DH11L07 |  |  |
| H12064 | 7 | BU05064 | C2DH12L07 |  |  |
| H05065 | 7 | BU01065 | C2EH05L07 |  |  |
| H06065 | 7 | BU02065 | C2EH06L07 |  |  |
| H08065 | 7 | BU03065 | C2EH08L07 |  |  |
| H09065 | 7 | BU04065 | C2EH09L07 |  |  |
| H10065 | 7 | BU05065 | C2EH10L07 |  |  |
| H13066 | 7 | BU01066 | C2FH13L07 |  |  |
| H14066 | 7 | BU02066 | C2FH14L07 |  |  |
| H18066 | 7 | BU03066 | C2FH18L07 |  |  |
| H19066 | 7 | BU04066 | C2FH19L07 |  |  |
| H20066 | 7 | BU05066 | C2FH20L07 |  |  |

TABLE 16: SAMPLES ACQUIRED FROM PLANT (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| H04061 | 7 | BU01061 | C2AH04L07 | 10 5-gallon buckets combined aggregate Gradation #2 (w/SG) | MRL |
| H05061 | 7 | BU02061 | C2AH05L07 |  |  |
| H06061 | 7 | BU03061 | C2AH06L07 |  |  |
| H07061 | 7 | BU04061 | C2AH07L07 |  |  |
| H08061 | 7 | BU05061 | C2AH08L07 |  |  |
| H05063 | 7 | BU01063 | C2CH05L07 |  |  |
| H06063 | 7 | BU02063 | C2CH06L07 |  |  |
| H11063 | 7 | BU03063 | C2CH11L07 |  |  |
| H12063 | 7 | BU04063 | C2CH12L07 |  |  |
| H13063 | 7 | BU05063 | C2CH13L07 |  |  |
| H07067 | 7 | BU01067 | C2GH07L07 | 5 5-gallon buckets combined aggregate Gradation #3 (w/MAN SAND) |  |
| H08067 | 7 | BU02067 | C2GH08L07 |  |  |
| H18067 | 7 | BU03067 | C2GH18L07 |  |  |
| H19067 | 7 | BU04067 | C2GH19L07 |  |  |
| H20067 | 7 | BU05067 | C2GH20L07 |  |  |

TABLE 16: SAMPLES ACQUIRED FROM PLANT (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |

| H06001 | 7 | BR01001 | C21H06L07 | 50 lb. Bulk Sample RAP | CLTC |
| --- | --- | --- | --- | --- | --- |
| H07001 | 7 | BR02001 | C21H07L07 | 10 5-gallon buckets RAP | MRL |
| H08001 | 7 | BR03001 | C21H08L07 |  |  |
| H06002 | 7 | BR01002 | C22H06L07 |  |  |
| H07002 | 7 | BR02002 | C22H07L07 |  |  |
| H06003 | 7 | BR01003 | C23H06L07 |  |  |
| H07003 | 7 | BR02003 | C23H07L07 |  |  |
| H09062 | 7 | BR01062 | C2BH09L07 |  |  |
| H07064 | 7 | BR01064 | C2DH07L07 |  |  |
| H07065 | 7 | BR01065 | C2EH07L07 |  |  |
| H15066 | 7 | BR01066 | C2FH15L07 |  |  |
| H07063 | 7 | BR01063 | C2CH07L07 | 50 lb. Bulk Sample RAS | CLTC |
| H08063 | 7 | BR02063 | C2CH08L07 | 10 5-gallon buckets RAS | MRL |
| H09063 | 7 | BR03063 | C2CH09L07 |  |  |
| H10063 | 7 | BR04063 | C2CH10L07 |  |  |
| H08064 | 7 | BR02064 | C2DH08L07 |  |  |
| H09064 | 7 | BR03064 | C2DH09L07 |  |  |
| H16066 | 7 | BR02066 | C2FH16L07 |  |  |
| H17066 | 7 | BR03066 | C2FH17L07 |  |  |
| H09067 | 7 | BR01067 | C2GH09L07 |  |  |
| H10067 | 7 | BR02067 | C2GH10L07 |  |  |
| H11067 | 7 | BR03067 | C2GH11L07 |  |  |
| H21067 | 7 | BW04067 | C2GH21L07 | 3 1-gallon can chemical additive EvoFlex® in manufacturer prescribed containers, with MSDS | MRL |
| H13062 | 7 | BW05062 | C2BH13L07 |  |  |
| H14062 | 7 | BW06062 | C2BH14L07 |  |  |
| H12001 | 7 | BW07001 | C21H12L07 | 3 1-gallon can Anti-Strip Agent Morlife T280 in manufacturer prescribed containers, with MSDS | MRL |
| H11002 | 7 | BW08002 | C22H11L07 |  |  |
| H14003 | 7 | BW09003 | C23H14L07 |  |  |
| H08003 | 7 | BW01003 | C23H08L07 | 3 1-gallon can chemical additive Evotherm® in manufacturer prescribed containers, with MSDS | MRL |
| H09003 | 7 | BW02003 | C23H09L07 |  |  |
| H10003 | 7 | BW03003 | C23H10L07 |  |  |
| H22067 | 7 | BW10067 | C2GH22L07 | 3 1-gallon can AC Modifier IPC-70® in manufacturer prescribed containers, with MSDS | MRL |
| H23067 | 7 | BW11067 | C2GH23L07 |  |  |
| H24067 | 7 | BW12067 | C2GH24L07 |  |  |

TABLE 17: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C21A01L07 | 12" Core |
| C21A02L07 | 12" Core |
| C22A01L07 | 12" Core |
| C22A02L07 | 12" Core |
| C23A01L07 | 12" Core |
| C23A02L07 | 12" Core |
| C2AA01L07 | 12" Core |
| C2AA02L07 | 12" Core |
| C2BA01L07 | 12" Core |
| C2BA02L07 | 12" Core |
| C2CA01L07 | 12" Core |
| C2CA02L07 | 12" Core |
| C2DA01L07 | 12" Core |
| C2DA02L07 | 12" Core |
| C2EA01L07 | 12" Core |
| C2EA02L07 | 12" Core |
| C2FA01L07 | 12" Core |
| C2FA02L07 | 12" Core |
| C2GA01L07 | 12" Core |
| C2GA02L07 | 12" Core |
| C21C01L07 | 6" Core |
| C21C02L07 | 6" Core |
| C21C03L07 | 6" Core |
| C21C04L07 | 6" Core |
| C21C05L07 | 6" Core |
| C21C06L07 | 6" Core |
| C21C07L07 | 6" Core |
| C21C08L07 | 6" Core |
| C21C09L07 | 6" Core |
| C21C10L07 | 6" Core |

TABLE 17: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C22C01L07 | 6" Core |
| C22C02L07 | 6" Core |
| C22C03L07 | 6" Core |
| C22C04L07 | 6" Core |
| C22C05L07 | 6" Core |
| C22C06L07 | 6" Core |
| C22C07L07 | 6" Core |
| C22C08L07 | 6" Core |
| C22C09L07 | 6" Core |
| C22C10L07 | 6" Core |
| C23C01L07 | 6" Core |
| C23C02L07 | 6" Core |
| C23C03L07 | 6" Core |
| C23C04L07 | 6" Core |
| C23C05L07 | 6" Core |
| C23C06L07 | 6" Core |
| C23C07L07 | 6" Core |
| C23C08L07 | 6" Core |
| C23C09L07 | 6" Core |
| C23C10L07 | 6" Core |
| C2AC01L07 | 6" Core |
| C2AC02L07 | 6" Core |
| C2AC03L07 | 6" Core |
| C2AC04L07 | 6" Core |
| C2AC05L07 | 6" Core |
| C2AC06L07 | 6" Core |
| C2AC07L07 | 6" Core |
| C2AC08L07 | 6" Core |
| C2AC09L07 | 6" Core |
| C2AC10L07 | 6" Core |
| C2BC01L07 | 6" Core |
| C2BC02L07 | 6" Core |
| C2BC03L07 | 6" Core |
| C2BC04L07 | 6" Core |
| C2BC05L07 | 6" Core |

TABLE 17: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2BC06L07 | 6" Core |
| C2BC07L07 | 6" Core |
| C2BC08L07 | 6" Core |
| C2BC09L07 | 6" Core |
| C2BC10L07 | 6" Core |
| C2CC01L07 | 6" Core |
| C2CC02L07 | 6" Core |
| C2CC03L07 | 6" Core |
| C2CC04L07 | 6" Core |
| C2CC05L07 | 6" Core |
| C2CC06L07 | 6" Core |
| C2CC07L07 | 6" Core |
| C2CC08L07 | 6" Core |
| C2CC09L07 | 6" Core |
| C2CC10L07 | 6" Core |
| C2DC01L07 | 6" Core |
| C2DC02L07 | 6" Core |
| C2DC03L07 | 6" Core |
| C2DC04L07 | 6" Core |
| C2DC05L07 | 6" Core |
| C2DC06L07 | 6" Core |
| C2DC07L07 | 6" Core |
| C2DC08L07 | 6" Core |
| C2DC09L07 | 6" Core |
| C2DC10L07 | 6" Core |
| C2EC01L07 | 6" Core |
| C2EC02L07 | 6" Core |
| C2EC03L07 | 6" Core |
| C2EC04L07 | 6" Core |
| C2EC05L07 | 6" Core |
| C2EC06L07 | 6" Core |
| C2EC07L07 | 6" Core |
| C2EC08L07 | 6" Core |
| C2EC09L07 | 6" Core |
| C2EC10L07 | 6" Core |

TABLE 17: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2FC01L07 | 6" Core |
| C2FC02L07 | 6" Core |
| C2FC03L07 | 6" Core |
| C2FC04L07 | 6" Core |
| C2FC05L07 | 6" Core |
| C2FC06L07 | 6" Core |
| C2FC07L07 | 6" Core |
| C2FC08L07 | 6" Core |
| C2FC09L07 | 6" Core |
| C2FC10L07 | 6" Core |
| C2GC01L07 | 6" Core |
| C2GC02L07 | 6" Core |
| C2GC03L07 | 6" Core |
| C2GC04L07 | 6" Core |
| C2GC05L07 | 6" Core |
| C2GC06L07 | 6" Core |
| C2GC07L07 | 6" Core |
| C2GC08L07 | 6" Core |
| C2GC09L07 | 6" Core |
| C2GC10L07 | 6" Core |
| C21H01L07 | 1 1-gallon can virgin AC Binder (PG 64-22H) |
| C2CH01L07 | 1 1-gallon can virgin AC Binder (PG 58-28S) |
| C2FH01L07 | 1 1-gallon can virgin AC Binder (PG 46-34S) |
| C21H06L07 | 50 lb. Bulk Sample RAP |
| C2CH07L07 | 50 lb. Bulk Sample RAS |

TABLE 17: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Original HMAC |  |
| C21A01L03 | 12" Core |
| C21A01L04 | 12" Core |
| C21A01L05 | 12" Core |
| C21A01L06 | 12" Core |
| C23A01L03 | 12" Core |
| C23A01L04 | 12" Core |
| C23A01L05 | 12" Core |
| C23A01L06 | 12" Core |
| C21C01L03 | 6" Core |
| C21C01L04 | 6" Core |
| C21C01L05 | 6" Core |
| C21C01L06 | 6" Core |
| C21C02L03 | 6" Core |
| C21C02L04 | 6" Core |
| C21C02L05 | 6" Core |
| C21C02L06 | 6" Core |
| C21C03L03 | 6" Core |
| C21C03L04 | 6" Core |
| C21C03L05 | 6" Core |
| C21C03L06 | 6" Core |
| C23C01L03 | 6" Core |
| C23C01L04 | 6" Core |
| C23C01L05 | 6" Core |
| C23C01L06 | 6" Core |
| C23C02L03 | 6" Core |
| C23C02L04 | 6" Core |
| C23C02L05 | 6" Core |
| C23C02L06 | 6" Core |
| C23C03L03 | 6" Core |
| C23C03L04 | 6" Core |
| C23C03L05 | 6" Core |
| C23C03L06 | 6" Core |

TABLE 17: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Crushed Stone/Gravel Base |  |
| C21A01L02 | 75 lb. Bulk Sample |
| C21A02L02 | 75 lb. Bulk Sample |
| C23A01L02 | 75 lb. Bulk Sample |
| C23A02L02 | 75 lb. Bulk Sample |
| Subgrade |  |
| C21A01L01 | 75 lb. Bulk Sample |
| C21AM1L01 | Moisture Content Jar Sample |
| C21A02L01 | 75 lb. Bulk Sample |
| C21AM2L01 | Moisture Content Jar Sample |
| C23A01L01 | 75 lb. Bulk Sample |
| C23AM1L01 | Moisture Content Jar Sample |
| C23A02L01 | 75 lb. Bulk Sample |
| C23AM2L01 | Moisture Content Jar Sample |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C21C11L07 | 6" Core |
| C21C12L07 | 6" Core |
| C21C13L07 | 6" Core |
| C21C14L07 | 6" Core |
| C22C11L07 | 6" Core |
| C22C12L07 | 6" Core |
| C22C13L07 | 6" Core |
| C22C14L07 | 6" Core |
| C23C11L07 | 6" Core |
| C23C12L07 | 6" Core |
| C23C13L07 | 6" Core |
| C23C14L07 | 6" Core |
| C2AC11L07 | 6" Core |
| C2AC12L07 | 6" Core |
| C2AC13L07 | 6" Core |
| C2AC14L07 | 6" Core |
| C2BC11L07 | 6" Core |
| C2BC12L07 | 6" Core |
| C2BC13L07 | 6" Core |
| C2BC14L07 | 6" Core |
| C2CC11L07 | 6" Core |
| C2CC12L07 | 6" Core |
| C2CC13L07 | 6" Core |
| C2CC14L07 | 6" Core |
| C2DC11L07 | 6" Core |
| C2DC12L07 | 6" Core |
| C2DC13L07 | 6" Core |
| C2DC14L07 | 6" Core |
| C2EC11L07 | 6" Core |
| C2EC12L07 | 6" Core |
| C2EC13L07 | 6" Core |
| C2EC14L07 | 6" Core |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2FC11L07 | 6" Core |
| C2FC12L07 | 6" Core |
| C2FC13L07 | 6" Core |
| C2FC14L07 | 6" Core |
| C2GC11L07 | 6" Core |
| C2GC12L07 | 6" Core |
| C2GC13L07 | 6" Core |
| C2GC14L07 | 6" Core |
| C21F01L07 | 15 5-gallon buckets uncompacted AC mix |
| C21F02L07 |  |
| C21F03L07 |  |
| C21F04L07 |  |
| C21F05L07 |  |
| C21F06L07 |  |
| C21F07L07 |  |
| C21F08L07 |  |
| C21F09L07 |  |
| C21F10L07 |  |
| C21F11L07 |  |
| C21F12L07 |  |
| C21F13L07 |  |
| C21F14L07 |  |
| C21F15L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C22F01L07 | 15 5-gallon buckets uncompacted AC mix |
| C22F02L07 |  |
| C22F03L07 |  |
| C22F04L07 |  |
| C22F05L07 |  |
| C22F06L07 |  |
| C22F07L07 |  |
| C22F08L07 |  |
| C22F09L07 |  |
| C22F10L07 |  |
| C22F11L07 |  |
| C22F12L07 |  |
| C22F13L07 |  |
| C22F14L07 |  |
| C22F15L07 |  |
| C23F01L07 | 15 5-gallon buckets uncompacted AC mix |
| C23F02L07 |  |
| C23F03L07 |  |
| C23F04L07 |  |
| C23F05L07 |  |
| C23F06L07 |  |
| C23F07L07 |  |
| C23F08L07 |  |
| C23F09L07 |  |
| C23F10L07 |  |
| C23F11L07 |  |
| C23F12L07 |  |
| C23F13L07 |  |
| C23F14L07 |  |
| C23F15L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2AF01L07 | 15 5-gallon buckets uncompacted AC mix |
| C2AF02L07 |  |
| C2AF03L07 |  |
| C2AF04L07 |  |
| C2AF05L07 |  |
| C2AF06L07 |  |
| C2AF07L07 |  |
| C2AF08L07 |  |
| C2AF09L07 |  |
| C2AF10L07 |  |
| C2AF11L07 |  |
| C2AF12L07 |  |
| C2AF13L07 |  |
| C2AF14L07 |  |
| C2AF15L07 |  |
| C2BF01L07 | 15 5-gallon buckets uncompacted AC mix |
| C2BF02L07 |  |
| C2BF03L07 |  |
| C2BF04L07 |  |
| C2BF05L07 |  |
| C2BF06L07 |  |
| C2BF07L07 |  |
| C2BF08L07 |  |
| C2BF09L07 |  |
| C2BF10L07 |  |
| C2BF11L07 |  |
| C2BF12L07 |  |
| C2BF13L07 |  |
| C2BF14L07 |  |
| C2BF15L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2CF01L07 | 15 5-gallon buckets uncompacted AC mix |
| C2CF02L07 |  |
| C2CF03L07 |  |
| C2CF04L07 |  |
| C2CF05L07 |  |
| C2CF06L07 |  |
| C2CF07L07 |  |
| C2CF08L07 |  |
| C2CF09L07 |  |
| C2CF10L07 |  |
| C2CF11L07 |  |
| C2CF12L07 |  |
| C2CF13L07 |  |
| C2CF14L07 |  |
| C2CF15L07 |  |
| C2DF01L07 | 15 5-gallon buckets uncompacted AC mix |
| C2DF02L07 |  |
| C2DF03L07 |  |
| C2DF04L07 |  |
| C2DF05L07 |  |
| C2DF06L07 |  |
| C2DF07L07 |  |
| C2DF08L07 |  |
| C2DF09L07 |  |
| C2DF10L07 |  |
| C2DF11L07 |  |
| C2DF12L07 |  |
| C2DF13L07 |  |
| C2DF14L07 |  |
| C2DF15L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2EF01L07 | 15 5-gallon buckets uncompacted AC mix |
| C2EF02L07 |  |
| C2EF03L07 |  |
| C2EF04L07 |  |
| C2EF05L07 |  |
| C2EF06L07 |  |
| C2EF07L07 |  |
| C2EF08L07 |  |
| C2EF09L07 |  |
| C2EF10L07 |  |
| C2EF11L07 |  |
| C2EF12L07 |  |
| C2EF13L07 |  |
| C2EF14L07 |  |
| C2EF15L07 |  |
| C2FF01L07 | 15 5-gallon buckets uncompacted AC mix |
| C2FF02L07 |  |
| C2FF03L07 |  |
| C2FF04L07 |  |
| C2FF05L07 |  |
| C2FF06L07 |  |
| C2FF07L07 |  |
| C2FF08L07 |  |
| C2FF09L07 |  |
| C2FF10L07 |  |
| C2FF11L07 |  |
| C2FF12L07 |  |
| C2FF13L07 |  |
| C2FF14L07 |  |
| C2FF15L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2GF01L07 | 15 5-gallon buckets uncompacted AC mix |
| C2GF02L07 |  |
| C2GF03L07 |  |
| C2GF04L07 |  |
| C2GF05L07 |  |
| C2GF06L07 |  |
| C2GF07L07 |  |
| C2GF08L07 |  |
| C2GF09L07 |  |
| C2GF10L07 |  |
| C2GF11L07 |  |
| C2GF12L07 |  |
| C2GF13L07 |  |
| C2GF14L07 |  |
| C2GF15L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C21H03L07 | 10 1-gallon cans virgin AC Binder (PG 64-22H) |
| C22H01L07 |  |
| C22H02L07 |  |
| C22H03L07 |  |
| C23H01L07 |  |
| C23H02L07 |  |
| C23H03L07 |  |
| C2AH01L07 |  |
| C2AH02L07 |  |
| C2BH03L07 |  |
| C2CH03L07 | 22 1-gallon cans virgin AC Binder (PG 58-28S) |
| C2CH04L07 |  |
| C2DH01L07 |  |
| C2DH02L07 |  |
| C2DH03L07 |  |
| C2DH04L07 |  |
| C2EH01L07 |  |
| C2EH02L07 |  |
| C2EH03L07 |  |
| C2EH04L07 |  |
| C2GH01L07 |  |
| C2GH02L07 |  |
| C2GH03L07 |  |
| C2GH04L07 |  |
| C2GH05L07 |  |
| C2GH06L07 |  |
| C2GH12L07 |  |
| C2GH13L07 |  |
| C2GH14L07 |  |
| C2GH15L07 |  |
| C2GH16L07 |  |
| C2GH17L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2FH03L07 | 10 1-gallon cans virgin AC Binder (PG 46-34S) |
| C2FH04L07 |  |
| C2FH05L07 |  |
| C2FH06L07 |  |
| C2FH07L07 |  |
| C2FH08L07 |  |
| C2FH09L07 |  |
| C2FH10L07 |  |
| C2FH11L07 |  |
| C2FH12L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C21H04L07 | 35 5-gallon buckets combined aggregate Gradation #1 |
| C21H05L07 |  |
| C21H09L07 |  |
| C21H10L07 |  |
| C21H11L07 |  |
| C22H04L07 |  |
| C22H05L07 |  |
| C22H08L07 |  |
| C22H09L07 |  |
| C22H10L07 |  |
| C23H04L07 |  |
| C23H05L07 |  |
| C23H11L07 |  |
| C23H12L07 |  |
| C23H13L07 |  |
| C2BH07L07 |  |
| C2BH08L07 |  |
| C2BH10L07 |  |
| C2BH11L07 |  |
| C2BH12L07 |  |
| C2DH05L07 |  |
| C2DH06L07 |  |
| C2DH10L07 |  |
| C2DH11L07 |  |
| C2DH12L07 |  |
| C2EH05L07 |  |
| C2EH06L07 |  |
| C2EH08L07 |  |
| C2EH09L07 |  |
| C2EH10L07 |  |
| C2FH13L07 |  |
| C2FH14L07 |  |
| C2FH18L07 |  |
| C2FH19L07 |  |
| C2FH20L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2AH04L07 | 10 5-gallon buckets combined aggregate Gradation #2 (w/SG) |
| C2AH05L07 |  |
| C2AH06L07 |  |
| C2AH07L07 |  |
| C2AH08L07 |  |
| C2CH05L07 |  |
| C2CH06L07 |  |
| C2CH11L07 |  |
| C2CH12L07 |  |
| C2CH13L07 |  |
| C2GH07L07 | 5 5-gallon buckets combined aggregate Gradation #3 (w/MAN SAND) |
| C2GH08L07 |  |
| C2GH18L07 |  |
| C2GH19L07 |  |
| C2GH20L07 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL) (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C21H07L07 | 10 5-gallon buckets RAP |
| C21H08L07 |  |
| C22H06L07 |  |
| C22H07L07 |  |
| C23H06L07 |  |
| C23H07L07 |  |
| C2BH09L07 |  |
| C2DH07L07 |  |
| C2EH07L07 |  |
| C2FH15L07 |  |
| C2CH08L07 | 10 5-gallon buckets RAS |
| C2CH09L07 |  |
| C2CH10L07 |  |
| C2DH08L07 |  |
| C2DH09L07 |  |
| C2FH16L07 |  |
| C2FH17L07 |  |
| C2GH09L07 |  |
| C2GH10L07 |  |
| C2GH11L07 |  |
| C23H08L07 | 3 1-gallon can chemical additive Evotherm® in manufacturer prescribed containers, with MSDS |
| C23H09L07 |  |
| C23H10L07 |  |
| C2GH21L07 | 3 1-gallon can chemical additive EvoFlex® in manufacturer prescribed containers, with MSDS |
| C2BH13L07 |  |
| C2BH14L07 |  |
| C21H12L07 | 3 1-gallon can Anti-Strip Agent Morlife T280 in manufacturer prescribed containers, with MSDS |
| C22H11L07 |  |
| C23H14L07 |  |
| C2GH22L07 | 3 1-gallon can AC Modifier IPC-70® in manufacturer prescribed containers, with MSDS |
| C2GH23L07 |  |
| C2GH24L07 |  |

TABLE 19: SAMPLES TO BE SHIPPED TO THE TURNER FAIRBANKS HIGHWAY RESEARCH CENTER (TFHRC) LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC Layer |  |
| C21H02L07 | 1 1-gallon can virgin AC Binder (PG 64-22H) |
| C2CH02L07 | 1 1-gallon can virgin AC Binder (PG 58-28S) |
| C2FH02L07 | 1 1-gallon can virgin AC Binder (PG 46-34S) |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Missouri SPS-10 project.  The previous section ended with lists of samples to be shipped to each of the two laboratories, the central lab testing contractor laboratory and the Turner-Fairbank Highway Research center.  In this section, the tests to be performed on each sample are listed.

Table 20 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Tables 21 and 22 provide new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 23 through 27 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 20: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 100 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 10 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 12 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 20 | X |  |
|  | Hamburg Wheel Track | AC09 | P75 | 10 | X |  |
|  | Fenix Fracture Energy | AC10 | P79 | 10 | X |  |
|  | Specific Gravity at 60 ° F | AE03 | P23 | 15 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 31 | X |  |
|  | Bending Beam Rheometer (BBR) Test | AE08 | P28 | 15 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 15 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 12 | X |  |
|  | PPA and Motor Oil Test | AE11 | P76 | 3 |  | X |
| B. | ORIGINAL HMAC (4 LAYERS) |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 24 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 8 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 8 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 16 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 8 | X |  |
|  | Bending Beam Rheometer (BBR) Test | AE08 | P28 | 8 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 8 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 8 | X |  |

TABLE 20: SPS-10 LABORATORY TESTING PLANS (Continued)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| C. | CRUSHED STONE/GRAVEL BASE |  |  |  |  |  |
|  | Sieve Analysis | UG02 | P41 | 2 | X |  |
|  | Atterberg Limits | UG04 | P43 | 2 | X |  |
|  | Classification and Description | UG08 | P47 | 2 | X |  |
|  | Standard Proctor | UG05 | P44 | 2 | X |  |
|  | Resilient Modulus | UG07 | P46 | 2 | X |  |
| D. | SUBGRADE |  |  |  |  |  |
|  | Sieve Analysis | SS01 | P51 | 2 | X |  |
|  | Atterberg Limits | SS03 | P43 | 2 | X |  |
|  | Classification and Description | SS04 | P52 | 2 | X |  |
|  | Standard Proctor | SS05 | P55 | 2 | X |  |
|  | Resilient Modulus | SS07 | P46 | 2 | X |  |
|  | Natural Moisture Content | SS09 | P49 | 2 | X |  |

TABLE 21: ORIGINAL AND COMBINED SPECIMEN DESCRIPTIONS

| Description Type | Status |  |  |
| --- | --- | --- | --- |
|  | Original |  | Combined1 |
| Sample No. | BA01001 | BA02001 | BAX1001 |
| Specimen ID | C21A01L07 | C21A02L07 | C21A01M07 |
| Sample No. | BG01001 | BG02001 | BGX1001 |
| Specimen ID | C21A01L02 | C21A02L02 | C21A01M02 |
| Sample No. | BS01001 | BS02001 | BSX1001 |
| Specimen ID | C21A01L01 | C21A02L01 | C21A01M01 |
| Sample No. | MS01001 | MS02001 | MSX1001 |
| Specimen ID | C21AM1L01 | C21AM2L01 | C21AM1M01 |
| Sample No. | BA01002 | BA02002 | BAX1002 |
| Specimen ID | C22A01L07 | C22A02L07 | C22A01M07 |
| Sample No. | BA01003 | BA02003 | BAX1003 |
| Specimen ID | C23A01L07 | C23A02L07 | C23A01M07 |
| Sample No. | BG01003 | BG02003 | BGX1003 |
| Specimen ID | C23A01L02 | C23A02L02 | C23A01M02 |
| Sample No. | BS01003 | BS02003 | BSX1003 |
| Specimen ID | C23A01L01 | C23A02L01 | C23A01M01 |
| Sample No. | MS01003 | MS02003 | MSX1003 |
| Specimen ID | C23AM1L01 | C23AM2L01 | C23AM1M01 |
| Sample No. | BA01061 | BA02061 | BAX1061 |
| Specimen ID | C2AA01L07 | C2AA02L07 | C2AA01M07 |
| Sample No. | BA01062 | BA02062 | BAX1062 |
| Specimen ID | C2BA01L07 | C2BA02L07 | C2BA01M07 |
| Sample No. | BA01063 | BA02063 | BAX1063 |
| Specimen ID | C2CA01L07 | C2CA02L07 | C2CA01M07 |
| Sample No. | BA01064 | BA02064 | BAX1064 |
| Specimen ID | C2DA01L07 | C2DA02L07 | C2DA01M07 |
| Sample No. | BA01065 | BA02065 | BAX1065 |
| Specimen ID | C2EA01L07 | C2EA02L07 | C2EA01M07 |
| Sample No. | BA01066 | BA02066 | BAX1066 |
| Specimen ID | C2FA01L07 | C2FA02L07 | C2FA01M07 |
| Sample No. | BA01067 | BA02067 | BAX1067 |
| Specimen ID | C2GA01L07 | C2GA02L07 | C2GA01M07 |

1. Sample No.:  After combination, the third character is changed to “X”, and the fourth character is assigned numerically. The other five characters follow the original format.  Specimen ID:  After combination “L” is changed to “M”.

TABLE 22: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BAX1001 | BAE1001 |
|  | Specimen ID | C21A01M07 | C21A01A07 |
|  | Sample No. | BA01001 | BAE1001 - ??? |
|  | Specimen ID | C21A01L06 | C21A01M06 |
|  | Sample No. | BA01001 | BAE1001 - ??? |
|  | Specimen ID | C21A01L05 | C21A01M05 |
|  | Sample No. | BA01001 | BAE1001 -??? |
|  | Specimen ID | C21A01L04 | C21A01M04 |
|  | Sample No. | BA01001 | BAE1001 - ??? |
|  | Specimen ID | C21A01L03 | C21A01M03 |
|  | Sample No. | BAX1002 | BAE1002 |
|  | Specimen ID | C22A01M07 | C22A01A07 |
|  | Sample No. | BAX1003 | BAE1003 |
|  | Specimen ID | C23A01M07 | C23A01A07 |
|  | Sample No. | BA01003 | BAE1003 - ??? |
|  | Specimen ID | C23A01L06 | C23A01M06 |
|  | Sample No. | BA01003 | BAE1003 - ??? |
|  | Specimen ID | C23A01L05 | C23A01M05 |
|  | Sample No. | BA01003 | BAE1003 - ??? |
|  | Specimen ID | C23A01L04 | C23A01M04 |
|  | Sample No. | BA01003 | BAE1003 - ??? |
|  | Specimen ID | C23A01L03 | C23A01M03 |
|  | Sample No. | BAX1061 | BAE1061 |
|  | Specimen ID | C2AA01M07 | C2AA01A07 |
|  | Sample No. | BAX1062 | BAE1062 |
|  | Specimen ID | C2BA01M07 | C2BA01A07 |
|  | Sample No. | BAX1063 | BAE1063 |
|  | Specimen ID | C2CA01M07 | C2CA01A07 |
|  | Sample No. | BAX1064 | BAE1064 |
|  | Specimen ID | C2DA01M07 | C2DA01A07 |
|  | Sample No. | BAX1065 | BAE1065 |
|  | Specimen ID | C2EA01M07 | C2EA01A07 |
|  | Sample No. | BAX1066 | BAE1066 |
|  | Specimen ID | C2FA01M07 | C2FA01A07 |
|  | Sample No. | BAX1067 | BAE1067 |
|  | Specimen ID | C2GA01M07 | C2GA01A07 |
|  | Sample No. | BR01001 | BRE1001 |
|  | Specimen ID | C21H06L07 | C21H06M07 |
|  | Sample No. | BR01063 | BRE1063 |
|  | Specimen ID | C2CH07L07 | C2CH07M07 |

TABLE 22: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS (Continued)

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| PAV | Sample No. | BAE1001 | BAP1001 |
|  | Specimen ID | C21A01A07 | C21A01B07 |
|  | Sample No. | BAE1002 | BAP1002 |
|  | Specimen ID | C22A01A07 | C22A01B07 |
|  | Sample No. | BAE1003 | BAP1003 |
|  | Specimen ID | C23A01A07 | C23A01B07 |
|  | Sample No. | BAE1061 | BAP1061 |
|  | Specimen ID | C2AA01A07 | C2AA01B07 |
|  | Sample No. | BAE1062 | BAP1062 |
|  | Specimen ID | C2BA01A07 | C2BA01B07 |
|  | Sample No. | BAE1063 | BAP1063 |
|  | Specimen ID | C2CA01A07 | C2CA01B07 |
|  | Sample No. | BAE1064 | BAP1064 |
|  | Specimen ID | C2DA01A07 | C2DA01B07 |
|  | Sample No. | BAE1065 | BAP1065 |
|  | Specimen ID | C2EA01A07 | C2EA01B07 |
|  | Sample No. | BAE1066 | BAP1066 |
|  | Specimen ID | C2FA01A07 | C2FA01B07 |
|  | Sample No. | BAE1067 | BAP1067 |
|  | Specimen ID | C2GA01A07 | C2GA01B07 |
| RTFO | Sample No. | BC01001 | BCR1001 |
|  | Specimen ID | C21H01L07 | C21H01M07 |
|  | Sample No. | BC01063 | BCR1063 |
|  | Specimen ID | C2CH01L07 | C2CH01M07 |
|  | Sample No. | BC01066 | BCR1066 |
|  | Specimen ID | C2FH01L07 | C2FH01M07 |
| RTFO + PAV | Sample No. | BC01001 | BCZ1001 |
|  | Specimen ID | C21H01L07 | C21H01A07 |
|  | Sample No. | BC01063 | BCZ1063 |
|  | Specimen ID | C2CH01L07 | C2CH01A07 |
|  | Sample No. | BC01066 | BCZ1066 |
|  | Specimen ID | C2FH01L07 | C2FH01A07 |

- Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

- Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C21A01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C22A01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C23A01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C2AA01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C2BA01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C2CA01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C2DA01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C2EA01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C2FA01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C2GA01M07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C21A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C22A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C23A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C2AA01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C2BA01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C2CA01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C2DA01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C2EA01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C2FA01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C2GA01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C21A01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C22A01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C23A01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C2AA01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C2BA01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C2CA01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C2DA01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C2EA01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C2FA01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C2GA01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C21C01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C21C02L07 | P02/AC02 |  |  |  |  | No | D |
| C21C03L07 | P02/AC02 |  |  |  |  | No | D |
| C21C04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C21C05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C21C06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C21C07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C21C08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C21C09L07 | P02/AC02 |  |  |  |  | No | D |
| C21C10L07 | P02/AC02 |  |  |  |  | Yes | S |
| C22C01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C22C02L07 | P02/AC02 |  |  |  |  | No | D |
| C22C03L07 | P02/AC02 |  |  |  |  | No | D |
| C22C04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C22C05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C22C06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C22C07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C22C08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C22C09L07 | P02/AC02 |  |  |  |  | No | D |
| C22C10L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C23C01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C23C02L07 | P02/AC02 |  |  |  |  | No | D |
| C23C03L07 | P02/AC02 |  |  |  |  | No | D |
| C23C04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C23C05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C23C06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C23C07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C23C08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C23C09L07 | P02/AC02 |  |  |  |  | No | D |
| C23C10L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2AC01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C2AC02L07 | P02/AC02 |  |  |  |  | No | D |
| C2AC03L07 | P02/AC02 |  |  |  |  | No | D |
| C2AC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2AC05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2AC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2AC07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2AC08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C2AC09L07 | P02/AC02 |  |  |  |  | No | D |
| C2AC10L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C2BC01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C2BC02L07 | P02/AC02 |  |  |  |  | No | D |
| C2BC03L07 | P02/AC02 |  |  |  |  | No | D |
| C2BC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2BC05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2BC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2BC07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2BC08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C2BC09L07 | P02/AC02 |  |  |  |  | No | D |
| C2BC10L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2CC01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C2CC02L07 | P02/AC02 |  |  |  |  | No | D |
| C2CC03L07 | P02/AC02 |  |  |  |  | No | D |
| C2CC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2CC05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2CC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2CC07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2CC08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C2CC09L07 | P02/AC02 |  |  |  |  | No | D |
| C2CC10L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C2DC01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C2DC02L07 | P02/AC02 |  |  |  |  | No | D |
| C2DC03L07 | P02/AC02 |  |  |  |  | No | D |
| C2DC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2DC05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2DC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2DC07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2DC08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C2DC09L07 | P02/AC02 |  |  |  |  | No | D |
| C2DC10L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2EC01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C2EC02L07 | P02/AC02 |  |  |  |  | No | D |
| C2EC03L07 | P02/AC02 |  |  |  |  | No | D |
| C2EC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2EC05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2EC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2EC07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2EC08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C2EC09L07 | P02/AC02 |  |  |  |  | No | D |
| C2EC10L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C2FC01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C2FC02L07 | P02/AC02 |  |  |  |  | No | D |
| C2FC03L07 | P02/AC02 |  |  |  |  | No | D |
| C2FC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2FC05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2FC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2FC07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2FC08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C2FC09L07 | P02/AC02 |  |  |  |  | No | D |
| C2FC10L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2GC01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C2GC02L07 | P02/AC02 |  |  |  |  | No | D |
| C2GC03L07 | P02/AC02 |  |  |  |  | No | D |
| C2GC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2GC05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2GC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2GC07L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2GC08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C2GC09L07 | P02/AC02 |  |  |  |  | No | D |
| C2GC10L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE OVERLAY IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C21H01L07 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| C21H01M07 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| C21H01A07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C2CH01L07 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| C2CH01M07 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| C2CH01A07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C2FH01L07 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| C2FH01M07 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| C2FH01A07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C21H06L07 | P04/AC04 |  |  |  |  | Yes | E, S |
| C21H06M07 | P23/AE03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 | No | D |
| C2CH07L07 | P04/AC04 |  |  |  |  | Yes | E, S |
| C2CH07M07 | P23/AE03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 | No | D |

1. Next Process  	D 	Remaining sample should be disposed
			S 	Remaining sample should be stored
			C	Remaining sample will be combined with another sample
			E 	Perform further testing on extracted sample
			P 	Perform further testing with PAV
			R 	Perform further testing with RFTO
			R+P  	Perform further testing with RTFO + PAV

TABLE 24: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CLTC LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C21A01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C23A01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C21A01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C23A01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C21C01L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C21C02L06 | P02/AC02 |  |  |  |  | Yes | S |
| C21C03L06 | P02/AC02 |  |  |  |  | Yes | S |
| C23C01L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C23C02L06 | P02/AC02 |  |  |  |  | Yes | S |
| C23C03L06 | P02/AC02 |  |  |  |  | Yes | S |
| C21A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C23A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C21A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C23A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C21C01L05 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C21C02L05 | P02/AC02 |  |  |  |  | Yes | S |
| C21C03L05 | P02/AC02 |  |  |  |  | Yes | S |
| C23C01L05 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C23C02L05 | P02/AC02 |  |  |  |  | Yes | S |
| C23C03L05 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 24: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CLTC LAB (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C21A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C23A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C21A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C23A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C21C01L04 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C21C02L04 | P02/AC02 |  |  |  |  | Yes | S |
| C21C03L04 | P02/AC02 |  |  |  |  | Yes | S |
| C23C01L04 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C23C02L04 | P02/AC02 |  |  |  |  | Yes | S |
| C23C03L04 | P02/AC02 |  |  |  |  | Yes | S |
| C21A01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C23A01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C21A01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C23A01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C21C01L03 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C21C02L03 | P02/AC02 |  |  |  |  | Yes | S |
| C21C03L03 | P02/AC02 |  |  |  |  | Yes | S |
| C23C01L03 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C23C02L03 | P02/AC02 |  |  |  |  | Yes | S |
| C23C03L03 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 25: TRACKING TABLE OF CRUSHED STONE/GRAVEL BASE IN THE CLTC LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C21A01M02 | P41/UG02 | P47/UG08 | P43/UG04 | P46/UG07 | P44/UG05 | Yes1 | S |
| C23A01M02 | P41/UG02 | P47/UG08 | P43/UG04 | P46/UG07 | P44/UG05 | Yes1 | S |

Table 26: TRACKING TABLE OF SUBGRADE IN THE CLTC LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C21A01M01 | P51/SS01 | P43/SS03 | P52/SS04 | P46/SS07 | P55/SS05 | Yes1 | S |
| C23A01M01 | P51/SS01 | P43/SS03 | P52/SS04 | P46/SS07 | P55/SS05 | Yes1 | S |
| C21AM1M01 | P49/SS09 |  |  |  |  | No1 | D |
| C23AM1M01 | P49/SS09 |  |  |  |  | No1 | D |

1. The moisture content sample may be disposed after testing.  However, any remaining bulk sample should be stored.

TABLE 27: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE OVERLAY IN THE TURNER FAIRBANKS HIGHWAY RESEARCH CENTER (TFHRC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C21H02L07 | P76/AE11 |  |  |  |  | Yes | S |
| C2CH02L07 | P76/AE11 |  |  |  |  | Yes | S |
| C2FH02L07 | P76/AE11 |  |  |  |  | Yes | S |