MISSOURI SPS-10 PROJECT 29AA00

# MATERIALS SAMPLING AND TESTING PLAN

For t1 (3-6 Months After Construction)

Contents

MATERIALS SAMPLING AND TESTING PLAN	0

GENERAL LAYOUT INFORMATION	1

MATERIALS SAMPLING AND FIELD TESTING	7

LABORATORY MATERIALS TESTING	27

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Missouri SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  These tables indicate transition areas between consecutive sections, as well as the buffer and monitoring areas for each section. Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION – 29AA00

| Test Section | SHRP ID | Description |
| --- | --- | --- |
| 1 | HMA Control 29AA01 | Control Section 2” SP125C w/ PG 64-22H, 24 % RAP; 0 % RAS Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| 2 | WMA Section 1 29AA02 | Foamed Asphalt Warm Mix Section with 2.0% water 2” SP125C w/ PG 64-22H, 25 % RAP; 0 % RAS Astec ® Mixing Unit, Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| 3 | WMA Section 2 29AA03 | Chemical Warm Mix Section 2” SP125C w/ PG 64-22H, 25 % RAP; 0 % RAS Evotherm® Chemical Additive 0.5%/AC Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| A | Supp. Section 1 29AA61 | Virgin Mix Section 2” SP125C w/ PG 64-22H 0 % RAP; 0 % RAS, Morlife® T280 1%/AC Combined Aggregate Gradation #2 (w/SG) |
| B | Supp. Section 2 29AA62 | RAP Mix Section 2” SP125C w/Final Extracted Binder = PG 77.1-22.3 Virgin Binder = PG 64-22H 35 % RAP, 0 % RAS, EvoFlex® Chemical Additive 3.0%/AC, Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| C | Supp. Section 3 29AA63 | RAS Mix Section 2” SP125C w/ PG 58-28S 0 % RAP; 17 % RAS, Morlife® T280 1%/AC Combined Aggregate Gradation #2 (w/SG) |
| D | Supp. Section 4 29AA64 | RAP/RAS Mix Section 2” SP125C w/ PG 58-28S 18 % RAP & 15 % RAS, Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| E | Supp. Section 5 29AA65 | RAP Mix Section 2” SP125C w/ PG 58-28S 33 % RAP, 0 % RAS, Minimum 15.0 % VMA Morlife® T280 1%/AC Combined Aggregate Gradation #1 |
| F | Supp. Section 6 29AA66 | RAP/RAS Mix Section 2” SP125C w/ Final Extracted Binder = PG 72-26.1 Virgin Binder = PG 46-34S 16 % RAP, 30 % RAS, Morlife® T280 2%/AC Combined Aggregate Gradation #1 |
| G | Supp. Section 7 29AA67 | RAS Mix Section 2” SP125C w/Final Extracted Binder = PG 77.8-25.6 Virgin Binder = PG 58-28S 0 % RAP, 33 % RAS, EvoFlex® Chemical Additive 3.5%/AC AC Modifier IPC-70 3.5%/AC, Morlife® T280 1%/AC Combined Aggregate Gradation #3 (w/MAN SAND) |

TABLE 2: TEST SECTION LAYOUT – 29AA00

| Tentative Log Mile Begin STA | Tentative Log Mile End STA | Experiment Begin STA feet | Experiment End STA feet | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
| 135.660 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA01 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 135.868 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 136.171 | 5+150 | 5+1099 | Transition |  |
| 136.171 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA02 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 136.379 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 136.696 | 5+150 | 5+1024.3 | Transition |  |
| 136.696 |  | 0-1024.3 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA03 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 136.918 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 137.207 | 5+150 | 5+876.5 | Transition |  |
| 137.207 |  | 0-876.5 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA61 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 137.401 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 137.704 | 5+150 | 5+1099 | Transition |  |
| 137.704 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA62 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 137.912 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 138.111 | 5+150 | 5+401.3 | Transition |  |

TABLE 2: TEST SECTION LAYOUT – 29AA00 (Continued)

| Tentative Log Mile Begin STA | Tentative Log Mile End STA | Experiment Begin STA feet | Experiment End STA feet | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
| 138.111 |  | 0-401.3 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA63 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 138.215 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 138.518 | 5+150 | 5+1099 | Transition |  |
| 138.726 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA64 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 138.934 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 139.237 | 5+150 | 5+1099 | Transition |  |
| 139.740 |  | 0-1099 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA65 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 139.948 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 140.185 | 5+150 | 5+599.3 | Transition |  |
| 140.185 |  | 0-599.3 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA66 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 140.326 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 140.582 | 5+150 | 5+702.2 | Transition |  |
| 140.582 |  | 0-702.2 | 0-150 | Transition |  |
|  |  | 0-150 | 0-50 | Sampling Area | 29AA67 |
|  |  | 0-50 | 0+00 | Buffer Area |  |
| 140.743 |  | 0+00 | 5+00 | Monitoring Area |  |
|  |  | 5+00 | 5+50 | Buffer Area |  |
|  |  | 5+50 | 5+150 | Sampling Area |  |
|  | 141.045 | 5+150 | 5+1096.4 | Transition |  |

Sampling Area 061

Buffer Area (50 ft)

29AA03

WMA Evotherm® Chemical Section

2” SP125C w/ PG 64-22H

25 % RAP; 0 % RAS

Buffer Area (50 ft)

Sampling Area 051

Transition (length variable)

Sampling Area 041

Buffer Area (50 ft)

29AA02

WMA Foaming Process with 2.0% water - Astec® Mixing Unit

2” SP125C w/ PG 64-22H

25 % RAP; 0 % RAS

Buffer Area (50 ft)

Sampling Area 031

Transition (length variable)

Buffer Area (50 ft)

29AA01

HMA Control Section 2” SP125C w/ PG 64-22H

24 % RAP; 0 % RAS

Buffer Area (50 ft)

Sampling Area 011

Sampling Area 021

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic (WB)

136.696

137.207

136.171

135.660

5+00

0+00

5+00

0+00

5+00

0+00

Sampling Area 101

Buffer Area (50 ft)

29AA62

RAP Mix Section

2” SP125C w/ Contractor Designed Grade

35 % RAP; 0 % RAS

Final Extracted Binder

= PG 77.1-22.3

Buffer Area (50 ft)

Sampling Area 091

Transition (length variable)

Sampling Area 081

Buffer Area (50 ft)

29AA61

Virgin Mix Section

2” SP125C w/ PG 64-22H

0 % RAP; 0 % RAS

Buffer Area (50 ft)

Sampling Area 071

Transition (length variable)

800ft

800ft

500ft

500ft

100ft

100ft

100ft

100ft

Traffic (WB)

138.111

137.704

137.207

5+00

0+00

5+00

0+00

FIGURE 1: MISSOURI SPS-10 PROJECT LAYOUT – 29AA00

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

Sampling Area 161

Buffer Area (50 ft)

29AA65

RAP Mix Section

2” SP125C w/ PG 58-28S

33 % RAP; 0 % RAS

Minimum 15.0% VMA

Buffer Area (50 ft)

Sampling Area 151

Transition (length variable)

Sampling Area 141

Buffer Area (50 ft)

29AA64

RAP/RAS Mix Section

2” SP125C w/ PG 58-28S

18 % RAP; 15 % RAS

Buffer Area (50 ft)

Sampling Area 131

Transition (length variable)

Buffer Area (50 ft)

29AA63

RAS Mix Section

2” SP125C w/ PG 58-28S

0 % RAP; 17 % RAS

Buffer Area (50 ft)

Sampling Area 111

Sampling Area 121

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic (WB)

139.740

139.237

140.185

138.726138.518

138.111

5+00

0+00

5+00

0+00

5+00

0+00

Sampling Area 201

Buffer Area (50 ft)

29AA67

RAS Mix Section

2” SP125C w/ Contractor Designed Grade

0 % RAP; 36 % RAS

Final Extracted Binder

= PG 77.8-25.6

Buffer Area (50 ft)

Sampling Area 191

Transition (length variable)

Sampling Area 181

Buffer Area (50 ft)

29AA66

RAP/RAS Mix Section

2” SP125C w/ Contractor Designed Grade

16 % RAP; 30 % RAS

Final Extracted Binder

= PG 72-26.1

Buffer Area (50 ft)

Sampling Area 171

Transition (length variable)

800ft

800ft

500ft

500ft

100ft

100ft

100ft

100ft

Traffic (WB)

141.045

140.582

140.185

5+00

0+00

5+00

0+00

FIGURE 1: MISSOURI SPS-10 PROJECT LAYOUT – 29AA00 (Continued)

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at time one (t1 is within 3 to 6 months from construction time).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 2 through 11 show the material sampling locations for each section. Tables 6 through 15 list the samples acquired from each of the ten test sections. These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Tables 16 through 17 list samples to be shipped to the Central Lab Testing Contractor (CLTC) laboratory, and the LTPP Materials Reference Library (MRL).

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Missouri SPS-10, R = “C,” representing north central region)

- C = Construction event (For Missouri SPS-10, C = 2, representing second constructed SPS-10 in the north central region)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 61

  - B – 62

  - C – 63

  - D – 64

  - E – 65

  - F – 66

  - G – 67

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

Labels and Tags

Each sample shall be labeled before packing in boxes and cartons. As a minimum, the following information shall be included on a tag or label attached to the specimen:

- SPECIMEN ID

- STATE CODE

- SHRP ID

- LOCATION DESIGNATION

- SAMPLE NUMBER

- DATE (mm-dd-yy, sampling date)

- FIELD SET (one digit number which will be 1 for the first round of sampling)

For cores, the HOLE ID shall be written directly on the core.  If the core contains more than one layer, layer boundaries shall be clearly marked, and each layer numbered.  For bulk samples, the SPECIMEN ID shall be written directly on the bag, bucket or can that contains the sample.

Packaging

Suggestions for labeling and combining the samples for shipment are as follows:

- All samples of like material (e.g., asphaltic concrete surface and binder) shall be placed in separate boxes or separate compartments of one box.

- Each sample shall have a label or tag attached that clearly identifies the material.  It is recommended that the label be color-coded by destination (e.g., contract Lab, FHWA lab, MRL, etc.).

- Each core shall be surrounded with "bubble-wrap" or other acceptable cushioning material on all sides within the shipping box.

- All bulk samples shall be marked with two labels or tags. One shall be placed inside the bag and one attached to the outside. A jar sample for moisture testing of each bulk sample shall be placed inside the bulk sample bag.

- All shipping boxes should be wood of suitable grade and construction to withstand shipping and subsequent moving without breakage of the box or damaging of samples.

- All boxes should be adequately secured by nails or screws prior to shipping.

LTPP Field Operations Information Sheets 1 and 2 shall be sent with each shipment of materials samples.

TABLE 3: PROJECT LAYER NUMBERING

| Layer No. | Project Layer Code | Thickness | Material Code | Description |
| --- | --- | --- | --- | --- |
| 1 | A |  | 294 | Subgrade – Clay with Limestone Rock, Varying Sizes |
| 2 | B | 4.5” | 302 | Base – Uncrushed Stone/Gravel |
| 3 | C | 3.0” | 01 | Existing AC Pavement |
| 4 | D | 2.8” | 01 | Existing AC Pavement |
| 5 | E | 1.0” | 01 | Existing AC Pavement |
| 6 | F | 1.6” | 01 | Existing AC Pavement |
| 7 | G | 1.75 – 2.0” | 01/91 | Experimental AC Overlay |

TABLE 4: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
|  | t1 SAMPLING (3-6 months after construction) |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 12" Core | 10 | A01101, A01102, A01103, A01161, A01162, A01163, A01164, A01165, A01166, A01167 |
|  | 6" Core | 60 | C01101-C06101, C01102-C06102, C01103-C06103, C01161-C06161, C01162-C06162, C01163-C06163, C01164-C06164, C01165-C06165, C01166-C06166, C01167-C06167 |

TABLE 5: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | t1 TESTING (3-6 months after paving) |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Core Examination and Thickness (P01/AC01) | 70 | A01101, A01102, A01103, A01161, A01162, A01163, A01164, A01165, A01166, A01167, C01101-C06101, C01102-C06102, C01103-C06103, C01161-C06161, C01162-C06162, C01163-C06163, C01164-C06164, C01165-C06165, C01166-C06166, C01167-C06167 |

5+50

5+70

Section STA:

Section: 29AA01

Description: HMAC Control Section

2” SP125C w/ PG 64-22H

24 % RAP; 0 % RAS

Morlife® T280 1%/AC

Sampling Area: 02

Sampling Interval: t1

Shoulder

C02101

C04101

C06101

2’

2’

1’

3’

2’

2’

2’

C01101

C03101

C05101

A01101

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 2: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA01 AT TIME 1 MISSOURI SPS-10

5+50

5+70

Section STA:

Section: 29AA02

Description: WMA with Foaming Process with 2.0% water - Astec ® Mixing Unit

2” SP125C w/ PG 64-22H

25 % RAP; 0 % RAS

Morlife® T280 1%/AC

Sampling Area: 04

Sampling Interval: t1

Shoulder

C02102

C04102

C06102

2’

2’

1’

3’

2’

2’

2’

C01102

C03102

C05102

A01102

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 3: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA02 AT TIME 1 MISSOURI SPS-10

5+50

5+70

Section STA:

Section: 29AA03

Description: WMA with Evotherm® Chem. Additive 0.5%/AC

2” SP125C w/ PG 64-22H

25 % RAP; 0 % RAS

Morlife® T280 1%/AC

Sampling Area: 06

Sampling Interval: t1

Shoulder

C02103

C04103

C06103

2’

2’

1’

3’

2’

2’

2’

C01103

C03103

C05103

A01103

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 4: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA03 AT TIME 1 MISSOURI SPS-10

5+50

5+70

Section STA:

Section: 29AA61

Description: Supplemental Section - Virgin Mix

2” SP125C w/ PG 64-22H

0 % RAP; 0 % RAS

Morlife® T280 1%/AC

Sampling Area: 08

Sampling Interval: t1

Shoulder

C02161

C04161

C06161

2’

2’

1’

3’

2’

2’

2’

C01161

C03161

C05161

A01161

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 5: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA61 AT TIME 1 MISSOURI SPS-10

5+50

5+70

Section STA:

Section: 29AA62

Description: Supplemental Section - RAP Mix

2” SP125C w/ Final Extracted Binder = PG 77.1-22.3

Virgin Binder = PG 64-22H

35 % RAP; 0 % RAS

EvoFlex® Chemical Additive 3.0%/AC

Morlife® T280 1%/AC

Sampling Area: 10

Sampling Interval: t1

Shoulder

C02162

C04161

C06162

2’

2’

1’

3’

2’

2’

2’

C01162

C03162

C05162

A01162

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 6: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA62 AT TIME 1 MISSOURI SPS-10

5+50

5+70

Section STA:

Section: 29AA63

Description: Supplemental Section - RAS Mix

2” SP125C w/ PG 58-28S

0 % RAP; 17 % RAS

Morlife® T280 1%/AC

Sampling Area: 12

Sampling Interval: t1

Shoulder

C02163

C04163

C06163

2’

2’

1’

3’

2’

2’

2’

C01163

C03163

C05163

A01163

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 7: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA63 AT TIME 1 MISSOURI SPS-10

5+50

5+70

Section STA:

Section: 29AA64

Description: Supplemental Section – RAP/RAS Mix

2” SP125C w/ PG 58-28S

18 % RAP; 15 % RAS

Morlife® T280 1%/AC

Sampling Area: 14

Sampling Interval: t1

Shoulder

C02164

C04164

C06164

2’

2’

1’

3’

2’

2’

2’

C01164

C03164

C05164

A01164

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 8: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA64 AT TIME 1 MISSOURI SPS-10

5+50

5+70

Section STA:

Section: 29AA65

Description: Supplemental Section - RAP Mix

2” SP125C w/ PG 58-28S

33 % RAP; 0 % RAS

Minimum 15.0% VMA

Morlife® T280 1%/AC

Sampling Area: 16

Sampling Interval: t1

Shoulder

C02165

C04165

C06165

2’

2’

1’

3’

2’

2’

2’

C01165

C03165

C05165

A01165

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 9: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA65 AT TIME 1 MISSOURI SPS-10

5+50

5+70

Section STA:

Section: 29AA66

Description: Supplemental Section – RAP/RAS Mix

2” SP125C w/ Final Extracted Binder Grade = PG 72-26.1

Virgin Binder = PG46-34S

16 % RAP; 30 % RAS

Morlife® T280 2%/AC

Sampling Area: 18

Sampling Interval: t1

Shoulder

C02166

C04166

C06166

2’

2’

1’

3’

2’

2’

2’

C01166

C03166

C05166

A01166

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 10: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA66 AT TIME 1 MISSOURI SPS-10

5+50

5+70

Section STA:

Section: 29AA67

Description: Supplemental Section - RAS Mix

2” SP125C w/ Final Extracted Binder = PG 77.8-25.6

Virgin Binder = PG58-28S

0 % RAP; 36 % RAS

EvoFlex® 3.5%AC, AC Modifier IPC-70 3.5%/AC

Morlife® T280 1%/AC

Sampling Area: 20

Sampling Interval: t1

Shoulder

C02167

C04167

C06167

2’

2’

1’

3’

2’

2’

2’

C01167

C03167

C05167

A01167

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 11: SAMPLING AND TESTING PLAN FOR TEST SECTION 29AA67 AT TIME 1 MISSOURI SPS-10

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 29AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01101 | 7 | BA01101 | C21A03L07 | 12" Core |
| C01101 | 7 | CA01101 | C21C15L07 | 6" Core |
| C02101 | 7 | CA02101 | C21C16L07 | 6" Core |
| C03101 | 7 | CA03101 | C21C17L07 | 6" Core |
| C04101 | 7 | CA04101 | C21C18L07 | 6" Core |
| C05101 | 7 | CA05101 | C21C19L07 | 6" Core |
| C06101 | 7 | CA06101 | C21C20L07 | 6" Core |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 29AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01102 | 7 | BA01102 | C22A03L07 | 12" Core |
| C01102 | 7 | CA01102 | C22C15L07 | 6" Core |
| C02102 | 7 | CA02102 | C22C16L07 | 6" Core |
| C03102 | 7 | CA03102 | C22C17L07 | 6" Core |
| C04102 | 7 | CA04102 | C22C18L07 | 6" Core |
| C05102 | 7 | CA05102 | C22C19L07 | 6" Core |
| C06102 | 7 | CA06102 | C22C20L07 | 6" Core |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 29AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01103 | 7 | BA01103 | C23A03L07 | 12" Core |
| C01103 | 7 | CA01103 | C23C15L07 | 6" Core |
| C02103 | 7 | CA02103 | C23C16L07 | 6" Core |
| C03103 | 7 | CA03103 | C23C17L07 | 6" Core |
| C04103 | 7 | CA04103 | C23C18L07 | 6" Core |
| C05103 | 7 | CA05103 | C23C19L07 | 6" Core |
| C06103 | 7 | CA06103 | C23C20L07 | 6" Core |

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 29AA61

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01161 | 7 | BA01161 | C2AA03L07 | 12" Core |
| C01161 | 7 | CA01161 | C2AC15L07 | 6" Core |
| C02161 | 7 | CA02161 | C2AC16L07 | 6" Core |
| C03161 | 7 | CA03161 | C2AC17L07 | 6" Core |
| C04161 | 7 | CA04161 | C2AC18L07 | 6" Core |
| C05161 | 7 | CA05161 | C2AC19L07 | 6" Core |
| C06161 | 7 | CA06161 | C2AC20L07 | 6" Core |

TABLE 10: SAMPLES ACQUIRED FROM TEST SECTION 29AA62

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01162 | 7 | BA01162 | C2BA03L07 | 12" Core |
| C01162 | 7 | CA01162 | C2BC15L07 | 6" Core |
| C02162 | 7 | CA02162 | C2BC16L07 | 6" Core |
| C03162 | 7 | CA03162 | C2BC17L07 | 6" Core |
| C04162 | 7 | CA04162 | C2BC18L07 | 6" Core |
| C05162 | 7 | CA05162 | C2BC19L07 | 6" Core |
| C06162 | 7 | CA06162 | C2BC20L07 | 6" Core |

TABLE 11: SAMPLES ACQUIRED FROM TEST SECTION 29AA63

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01163 | 7 | BA01163 | C2CA03L07 | 12" Core |
| C01163 | 7 | CA01163 | C2CC15L07 | 6" Core |
| C02163 | 7 | CA02163 | C2CC16L07 | 6" Core |
| C03163 | 7 | CA03163 | C2CC17L07 | 6" Core |
| C04163 | 7 | CA04163 | C2CC18L07 | 6" Core |
| C05163 | 7 | CA05163 | C2CC19L07 | 6" Core |
| C06163 | 7 | CA06163 | C2CC20L07 | 6" Core |

TABLE 12: SAMPLES ACQUIRED FROM TEST SECTION 29AA64

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01164 | 7 | BA01164 | C2DA03L07 | 12" Core |
| C01164 | 7 | CA01164 | C2DC15L07 | 6" Core |
| C02164 | 7 | CA02164 | C2DC16L07 | 6" Core |
| C03164 | 7 | CA03164 | C2DC17L07 | 6" Core |
| C04164 | 7 | CA04164 | C2DC18L07 | 6" Core |
| C05164 | 7 | CA05164 | C2DC19L07 | 6" Core |
| C06164 | 7 | CA06164 | C2DC20L07 | 6" Core |

TABLE 13: SAMPLES ACQUIRED FROM TEST SECTION 29AA65

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01165 | 7 | BA01165 | C2EA03L07 | 12" Core |
| C01165 | 7 | CA01165 | C2EC15L07 | 6" Core |
| C02165 | 7 | CA02165 | C2EC16L07 | 6" Core |
| C03165 | 7 | CA03165 | C2EC17L07 | 6" Core |
| C04165 | 7 | CA04165 | C2EC18L07 | 6" Core |
| C05165 | 7 | CA05165 | C2EC19L07 | 6" Core |
| C06165 | 7 | CA06165 | C2EC20L07 | 6" Core |

TABLE 14: SAMPLES ACQUIRED FROM TEST SECTION 29AA66

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01166 | 7 | BA01166 | C2FA03L07 | 12" Core |
| C01166 | 7 | CA01166 | C2FC15L07 | 6" Core |
| C02166 | 7 | CA02166 | C2FC16L07 | 6" Core |
| C03166 | 7 | CA03166 | C2FC17L07 | 6" Core |
| C04166 | 7 | CA04166 | C2FC18L07 | 6" Core |
| C05166 | 7 | CA05166 | C2FC19L07 | 6" Core |
| C06166 | 7 | CA06166 | C2FC20L07 | 6" Core |

TABLE 15: SAMPLES ACQUIRED FROM TEST SECTION 29AA67

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01167 | 7 | BA01167 | C2GA03L07 | 12" Core |
| C01167 | 7 | CA01167 | C2GC15L07 | 6" Core |
| C02167 | 7 | CA02167 | C2GC16L07 | 6" Core |
| C03167 | 7 | CA03167 | C2GC17L07 | 6" Core |
| C04167 | 7 | CA04167 | C2GC18L07 | 6" Core |
| C05167 | 7 | CA05167 | C2GC19L07 | 6" Core |
| C06167 | 7 | CA06167 | C2GC20L07 | 6" Core |

TABLE 16: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C21A03L07 | 12" Core |
| C22A03L07 | 12" Core |
| C23A03L07 | 12" Core |
| C2AA03L07 | 12" Core |
| C2BA03L07 | 12" Core |
| C2CA03L07 | 12" Core |
| C2DA03L07 | 12" Core |
| C2EA03L07 | 12" Core |
| C2FA03L07 | 12" Core |
| C2GA03L07 | 12" Core |
| C21C15L07 | 6" Core |
| C21C16L07 | 6" Core |
| C21C17L07 | 6" Core |
| C22C15L07 | 6" Core |
| C22C16L07 | 6" Core |
| C22C17L07 | 6" Core |
| C23C15L07 | 6" Core |
| C23C16L07 | 6" Core |
| C23C17L07 | 6" Core |
| C2AC15L07 | 6" Core |
| C2AC16L07 | 6" Core |
| C2AC17L07 | 6" Core |

TABLE 16: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (CONTINUED)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2BC15L07 | 6" Core |
| C2BC16L07 | 6" Core |
| C2BC17L07 | 6" Core |
| C2CC15L07 | 6" Core |
| C2CC16L07 | 6" Core |
| C2CC17L07 | 6" Core |
| C2DC15L07 | 6" Core |
| C2DC16L07 | 6" Core |
| C2DC17L07 | 6" Core |
| C2EC15L07 | 6" Core |
| C2EC16L07 | 6" Core |
| C2EC17L07 | 6" Core |
| C2FC15L07 | 6" Core |
| C2FC16L07 | 6" Core |
| C2FC17L07 | 6" Core |
| C2GC15L07 | 6" Core |
| C2GC16L07 | 6" Core |
| C2GC17L07 | 6" Core |

TABLE 17: SAMPLES TO BE SHIPPED TO THE LTPP MATERIALS REFERENCE LIBRARY (MRL)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C21C18L07 | 6" Core |
| C21C19L07 | 6" Core |
| C21C20L07 | 6" Core |
| C22C18L07 | 6" Core |
| C22C19L07 | 6" Core |
| C22C20L07 | 6" Core |
| C23C18L07 | 6" Core |
| C23C19L07 | 6" Core |
| C23C20L07 | 6" Core |
| C2AC18L07 | 6" Core |
| C2AC19L07 | 6" Core |
| C2AC20L07 | 6" Core |

TABLE 17: SAMPLES TO BE SHIPPED TO THE LTPP MRL (CONTINUED)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C2BC18L07 | 6" Core |
| C2BC19L07 | 6" Core |
| C2BC20L07 | 6" Core |
| C2CC18L07 | 6" Core |
| C2CC19L07 | 6" Core |
| C2CC20L07 | 6" Core |
| C2DC18L07 | 6" Core |
| C2DC19L07 | 6" Core |
| C2DC20L07 | 6" Core |
| C2EC18L07 | 6" Core |
| C2EC19L07 | 6" Core |
| C2EC20L07 | 6" Core |
| C2FC18L07 | 6" Core |
| C2FC19L07 | 6" Core |
| C2FC20L07 | 6" Core |
| C2GC18L07 | 6" Core |
| C2GC19L07 | 6" Core |
| C2GC20L07 | 6" Core |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Missouri SPS-10 project. The previous section ended with lists of samples to be shipped to each of the central lab testing contractor laboratory and the LTPP Materials Reference Library (MRL).  In this section, the tests to be performed on each sample are listed.

Table 18 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Tables 19 provides new sample numbers and specimen ID’s for samples that will be modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 20 provides tracking for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 18: SPS-10 LABORATORY TESTING PLANS FOR 3-6 MONTH CORING (t1)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: | Test Conducted By: |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | RSC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Core Exam. And Thickness | AC01 | P01 | 70 |  | X |
|  | Bulk Specific Gravity | AC02 | P02 | 30 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 10 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 20 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 10 | X |  |
|  | Bending Beam Rheometer (BBR) Test | AE08 | P28 | 10 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 10 | X |  |

TABLE 19: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BA01101 | BAE1101 |
|  | Specimen ID | C21A03L07 | C21A03M07 |
|  | Sample No. | BA01102 | BAE1102 |
|  | Specimen ID | C22A03L07 | C22A03M07 |
|  | Sample No. | BA01103 | BAE1103 |
|  | Specimen ID | C23A03L07 | C23A03M07 |
|  | Sample No. | BA01161 | BAE1161 |
|  | Specimen ID | C2AA03L07 | C2AA03M07 |
|  | Sample No. | BA01162 | BAE1162 |
|  | Specimen ID | C2BA03L07 | C2BA03M07 |
|  | Sample No. | BA01163 | BAE1163 |
|  | Specimen ID | C2CA03L07 | C2CA03M07 |
|  | Sample No. | BA01164 | BAE1164 |
|  | Specimen ID | C2DA03L07 | C2DA03M07 |
|  | Sample No. | BA01165 | BAE1165 |
|  | Specimen ID | C2EA03L07 | C2EA03M07 |
|  | Sample No. | BA01166 | BAE1166 |
|  | Specimen ID | C2FA03L07 | C2FA03M07 |
|  | Sample No. | BA01167 | BAE1167 |
|  | Specimen ID | C2GA03L07 | C2GA03M07 |

- Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

- Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 20: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |  |  |
| C21A03L07 | P04/AC04 |  |  |  |  | No | E |
| C22A03L07 | P04/AC04 |  |  |  |  | No | E |
| C23A03L07 | P04/AC04 |  |  |  |  | No | E |
| C2AA03L07 | P04/AC04 |  |  |  |  | No | E |
| C2BA03L07 | P04/AC04 |  |  |  |  | No | E |
| C2CA03L07 | P04/AC04 |  |  |  |  | No | E |
| C2DA03L07 | P04/AC04 |  |  |  |  | No | E |
| C2EA03L07 | P04/AC04 |  |  |  |  | No | E |
| C2FA03L07 | P04/AC04 |  |  |  |  | No | E |
| C2GA03L07 | P04/AC04 |  |  |  |  | No | E |
| C21A03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C22A03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C23A03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C2AA03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C2BA03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C2CA03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C2DA03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C2EA03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C2FA03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C2GA03M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |

1. Next Process

D 	Remaining sample should be disposed			S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV				R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV

TABLE 20: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (CONTINUED)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |  |  |
| C21C15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C21C16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C21C17L07 | P02/AC02 |  |  |  |  | Yes | S |
| C22C15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C22C16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C22C17L07 | P02/AC02 |  |  |  |  | Yes | S |
| C23C15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C23C16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C23C17L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2AC15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2AC16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2AC17L07 | P02/AC02 |  |  |  |  | Yes | S |

1. Next Process

D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV

TABLE 20: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (CONTINUED)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |  |  |
| C2BC15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2BC16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2BC17L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2CC15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2CC16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2CC17L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2DC15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2DC16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2DC17L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2EC15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2EC16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2EC17L07 | P02/AC02 |  |  |  |  | Yes | S |

1. Next Process

D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV

TABLE 20: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (CONTINUED)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |  |  |
| C2FC15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2FC16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2FC17L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2GC15L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C2GC16L07 | P02/AC02 |  |  |  |  | Yes | S |
| C2GC17L07 | P02/AC02 |  |  |  |  | Yes | S |

1. Next Process

D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV