Appendix C:

Material Sampling and Testing Layout

NEW MEXICO SPS-10 PROJECT (35AA00)

MATERIALS SAMPLING AND TESTING PLAN

Contents

GENERAL LAYOUT INFORMATION	2

MATERIALS SAMPLING AND FIELD TESTING	5

LABORATORY MATERIALS TESTING	29

SAMPLE LABELS - SPECIAL NOTE	41

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the New Mexico SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  Table 2 indicates transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Additionally, Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION

| Section Number | SHRP ID | Description |
| --- | --- | --- |
| 1 | 35AA01 | HMA Control Section – PG 70-28 |
| 2 | 35AA02 | WMA – Foaming Process – PG 70-28 |
| 3 | 35AA03 | WMA – Evotherm® – PG 70-28 |
| 4 | 35AA61 | WMA – Cecabase® – PG 70-28 |
| 5 | 35AA62 | WMA – Cecabase® – PG 70-28+ |

TABLE 2: TEST SECTION LAYOUT

| Begin STA | End STA | Description | Section ID |
| --- | --- | --- | --- |
| 882+24 | 881+24 | Sampling Area | 35AA01 |
| 881+24 | 880+74 | Buffer Area |  |
| 880+74 | 875+74 | Monitoring Area |  |
| 875+74 | 875+24 | Buffer Area |  |
| 875+24 | 874+24 | Sampling Area |  |
| 874+24 | 870+18 | Transition |  |
| 870+18 | 869+18 | Sampling Area | 35AA02 |
| 869+18 | 868+68 | Buffer Area |  |
| 868+68 | 863+68 | Monitoring Area |  |
| 863+68 | 863+18 | Buffer Area |  |
| 863+18 | 862+18 | Sampling Area |  |
| 862+18 | 845+97 | Transition |  |
| 845+97 | 844+97 | Sampling Area | 35AA03 |
| 844+97 | 844+47 | Buffer Area |  |
| 844+47 | 839+47 | Monitoring Area |  |
| 839+47 | 838+97 | Buffer Area |  |
| 838+97 | 837+97 | Sampling Area |  |
| 759+11 | 747+11 | Transition |  |
| 747+11 | 746+11 | Sampling Area | 35AA61 |
| 746+11 | 745+61 | Buffer Area |  |
| 745+61 | 740+61 | Monitoring Area |  |
| 740+61 | 740+11 | Buffer Area |  |
| 740+11 | 739+11 | Sampling Area |  |
| 739+11 | 732+10 | Transition |  |
| 732+10 | 731+10 | Sampling Area | 35AA62 |
| 731+10 | 730+60 | Buffer Area |  |
| 730+60 | 725+60 | Monitoring Area |  |
| 725+60 | 725+10 | Buffer Area |  |
| 725+10 | 724+10 | Sampling Area |  |
| 724+10 | 716+10 | Transition |  |

Sampling Area 061

Buffer Area (50 ft)

35AA03

WMA Chemical

Additive (Evotherm)

Buffer Area (50 ft)

Sampling Area 051

Transition (length variable)

Sampling Area 041

Buffer Area (50 ft)

35AA02

WMA Foaming Process

Buffer Area (50 ft)

Sampling Area 031

Transition (length variable)

Buffer Area (50 ft)

35AA01

HMA Control

Section

Buffer Area (50 ft)

Sampling Area 011

Sampling Area 021

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic (WB)

845+97

862+18

837+97

870+18

874+24

882+24

839+47

844+47

863+68

868+68

875+74

880+74

Sampling Area 101

Buffer Area (50 ft)

35AA62

WMA Chemical additive (Cecabase) with PG 70-28+

Buffer Area (50 ft)

Sampling Area 091

Transition (length variable)

Sampling Area 081

Buffer Area (50 ft)

35AA61

WMA Chemical additive (Cecabase) with PG 70-28

Buffer Area (50 ft)

Sampling Area 071

Transition (length variable)

800ft

800ft

500ft

500ft

100ft

100ft

100ft

100ft

Traffic (WB)

724+10

732+10

739+11

747+11

759+11

725+60

730+60

740+61

745+61

FIGURE 1: NEW MEXICO SPS-10 PROJECT LAYOUT

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at time zero (t0 is at time of construction).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 2 through 11 show the locations for the many samples and tests scheduled.  Figures 2 through 6 show density measurement layouts, and Figures 7 through 11 show the material sampling locations for each section as well as the location of DCP testing.

Tables 6 through 11 list the samples acquired from each of the five test sections as well as the asphalt plant.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 12 through 14 list samples to be shipped to the central lab testing contractor laboratory, the LTPP Materials Reference Library (MRL), and the Turner-Fairbank Highway Research Center, respectively.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For New Mexico SPS-10, R = “S,” representing southern region)

- C = Construction event (For New Mexico SPS-10, C = 2, representing second constructed SPS-10)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 61

  - B – 62

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

TABLE 3: PROJECT LAYER NUMBERING

| Layer No. | Description |
| --- | --- |
| 1 | Subgrade |
| 2 | Untreated Base |
| 3 | Historic AC |
| 4 | Original HMAC |
| 5 | Experimental AC Overlay |

TABLE 4: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
|  | DURING CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 5-gallon buckets uncompacted AC mix | 77 | F01001-F06001, F01002-F07002, F01003-F07003, F01061-F07061, F01062-F08062 |
|  | 1-gallon can virgin AC Binder (PG 70-28) | 12 | H01001 |
|  | 1-gallon can virgin AC Binder (PG 70-28+) | 13 | H01062 |
|  | 5-gallon bucket combined aggregate | 20 | H02001 |
|  | 50 lb bulk sample RAP | 1 | H03001 |
|  | 5-gallon bucket RAP | 10 | H03001 |
|  | 1-gallon chemical additive (Evotherm®) | 3 | H01003 |
|  | 1-gallon chemical additive (Cecabase®) | 3 | H01061 |
|  | 1-gallon chemical additive (Versabind®) | 1 | H04001 |
|  | POST-CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 10" Core | 10 | A01001-A02001, A01002-A02002, A01003-A02003, A01061-A02061, A01062-A02062 |
|  | 6" Core | 70 | C01001-C14001, C01002-C14002, C01003-C14003, C01061-C14061, C01062-C14062 |
| B. | ORIGINAL HMAC |  |  |
|  | 10" Core | 2 | A01002, A01061 |
|  | 6" Core | 6 | C06002, C10002, C12002, C12061-C14061 |
| C. | HISTORIC HMAC |  |  |
|  | 10" Core | 2 | A01002, A01061 |
|  | 6" Core | 6 | C06002, C10002, C12002, C12061-C14061 |
| D. | UNTREATED BASE | N/A | Sample will be collected in future monitoring interval. |
| E. | SUBGRADE | N/A | Sample will be collected in future monitoring interval. |

TABLE 5: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | PRE-CONSTRUCTION TESTING |  |  |
| A. | ORIGINAL HMAC |  |  |
|  | Elevation Survey | 5 | All Sections |
|  | POST-CONSTRUCTION TESTING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Elevation Survey | 5 | All Sections |
|  | In situ density measurement | 15 | T01001-T03001, T01002-T03002, T01003-T03003, T01061-T03061, T01062-T03062 |
|  | Core Examination and Thickness (P01/AC01) | 80 | A01001-A02001, A01002-A02002, A01003-A02003, A01061-A02061, A01062-A02062, C01001-C14001, C01002-C14002, C01003-C14003, C01061-C14061, C01062-C14062 |
| B. | ORIGINAL HMAC |  |  |
|  | Core Examination and Thickness (P01/AC01) | 8 | A01002, A01061, C06002, C10002, C12002, C12061-C14061 |
| C. | HISTORIC HMAC |  |  |
|  | Core Examination and Thickness (P01/AC01) | 8 | A01002, A01061, C06002, C10002, C12002, C12061-C14061 |
| D. | UNTREATED BASE |  |  |
|  | DCP | 8 | A01001, C12002, C14002, C14003, C13061, C14061, C13062, C14062 |
| E. | SUBGRADE |  |  |
|  | DCP | 8 | A01001, C12002, C14002, C14003, C13061, C14061, C13062, C14062 |

Section 35AA01 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03001

T02001

T01001

Traffic

FIGURE 2: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 35AA01 NEW MEXICO SPS-10

Section 35AA02 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03002

T02002

T01002

Traffic

FIGURE 3: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 35AA02 NEW MEXICO SPS-10

Section 35AA03 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03003

T02003

T01003

Traffic

FIGURE 4: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 35AA03 NEW MEXICO SPS-10

Section 35AA61 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03061

T02061

T01061

Traffic

FIGURE 5: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 35AA61 NEW MEXICO SPS-10

Section 35AA62 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03062

T02062

T01062

Traffic

FIGURE 6: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 35AA62 NEW MEXICO SPS-10

0-70

0-50

Section STA:

Section: 35AA01

Description: HMAC Control Section

Sampling Area: 01

Sampling Interval: t0

Shoulder

C02001

C04001

C06001

C08001

C10001

C12001

C14001

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01001

C03001

C05001

C07001

C09001

C11001

C13001

A01001

A02001

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

6” Core Experimental AC, Original AC, and Historic AC

6” Core Experimental AC, Original AC, and Historic AC; DCP

6” Core Experimental AC; DCP

10” Core Experimental AC

10” Core Experimental AC, Original AC, and Historic AC

10” Core Experimental AC; DCP

FIGURE 7 SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA01 AT TIME 0 NEW MEXICO SPS-10

0-70

0-50

Section STA:

Section: 35AA02

Description: Mix with WMA Chemical Additive

Sampling Area: 03

Sampling Interval: t0

Shoulder

C02002

C04002

C06002

C08002

C10002

C12002

C14002

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01002

C03002

C05002

C07002

C09002

C11002

C13002

A01002

A02002

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

6” Core Experimental AC, Original AC, and Historic AC

6” Core Experimental AC, Original AC, and Historic AC; DCP

6” Core Experimental AC; DCP

10” Core Experimental AC

10” Core Experimental AC, Original AC, and Historic AC

10” Core Experimental AC; DCP

FIGURE 8: SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA02 AT TIME 0 NEW MEXICO SPS-10

0-70

0-50

Section STA:

Section: 35AA03

Description: Mix with WMA Foaming Process

Sampling Area: 05

Sampling Interval: t0

Shoulder

C02003

C04003

C06003

C08003

C10003

C12003

C14003

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01003

C03003

C05003

C07003

C09003

C11003

C13003

A01003

A02003

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

6” Core Experimental AC, Original AC, and Historic AC

6” Core Experimental AC, Original AC, and Historic AC; DCP

6” Core Experimental AC; DCP

10” Core Experimental AC

10” Core Experimental AC, Original AC, and Historic AC

10” Core Experimental AC; DCP

FIGURE 9: SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA03 AT TIME 0 NEW MEXICO SPS-10

0-70

0-50

Section STA:

Section: 35AA61

Description: Supplemental Section 1

Sampling Area: 07

Sampling Interval: t0

Shoulder

C02061

C04061

C06061

C08061

C10061

C12061

C14061

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01061

C03061

C05061

C07061

C09061

C11061

C13061

A01061

A02061

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

6” Core Experimental AC, Original AC, and Historic AC

6” Core Experimental AC, Original AC, and Historic AC; DCP

6” Core Experimental AC; DCP

10” Core Experimental AC

10” Core Experimental AC, Original AC, and Historic AC

10” Core Experimental AC; DCP

FIGURE 10: SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA61 AT TIME 0 NEW MEXICO SPS-10

0-70

0-50

Section STA:

Section: 35AA62

Description: Supplemental Section 2

Sampling Area: 09

Sampling Interval: t0

Shoulder

C02062

C04062

C06062

C08062

C10062

C12062

C14062

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01062

C03062

C05062

C07062

C09062

C11062

C13062

A01062

A02062

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

6” Core Experimental AC, Original AC, and Historic AC

6” Core Experimental AC, Original AC, and Historic AC; DCP

6” Core Experimental AC; DCP

10” Core Experimental AC

10” Core Experimental AC, Original AC, and Historic AC

10” Core Experimental AC; DCP

FIGURE 11: SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA62 AT TIME 0 NEW MEXICO SPS-10

TABLE 6: SAMPLES ACQUIRED FROM  TEST SECTION 35AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01001 | 6 | BA01001 | S21A01L06 | 10" Core |
| A02001 | 6 | BA02001 | S21A02L06 | 10" Core |
| C01001 | 6 | CA01001 | S21C01L06 | 6" Core |
| C02001 | 6 | CA02001 | S21C02L06 | 6" Core |
| C03001 | 6 | CA03001 | S21C03L06 | 6" Core |
| C04001 | 6 | CA04001 | S21C04L06 | 6" Core |
| C05001 | 6 | CA05001 | S21C05L06 | 6" Core |
| C06001 | 6 | CA06001 | S21C06L06 | 6" Core |
| C07001 | 6 | CA07001 | S21C07L06 | 6" Core |
| C08001 | 6 | CA08001 | S21C08L06 | 6" Core |
| C09001 | 6 | CA09001 | S21C09L06 | 6" Core |
| C10001 | 6 | CA10001 | S21C10L06 | 6" Core |
| C11001 | 6 | CA11001 | S21C11L06 | 6" Core |
| C12001 | 6 | CA12001 | S21C12L06 | 6" Core |
| C13001 | 6 | CA13001 | S21C13L06 | 6" Core |
| C14001 | 6 | CA14001 | S21C14L06 | 6" Core |
| F01001 | 6 | BA04001 | S21F01L06 | 2 5-gallon buckets uncompacted AC mix |
| F02001 | 6 | BA05001 | S21F02L06 | 2 5-gallon buckets uncompacted AC mix |
| F03001 | 6 | BA06001 | S21F03L06 | 4 5-gallon buckets uncompacted AC mix |
| F04001 | 6 | BA07001 | S21F04L06 | 2 5-gallon buckets uncompacted AC mix |
| F05001 | 6 | BA08001 | S21F05L06 | 3 5-gallon buckets uncompacted AC mix |
| F06001 | 6 | BA09001 | S21F06L06 | 2 5-gallon buckets uncompacted AC mix |

Note: Sample No. BA03001 not used

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 35AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01002 | 6 | BA01002 | S22A01L06 | 10" Core |
|  | 5 | BA01002 | S22A01L05 | 10" Core |
|  | 4 | BA10002 | S22A01L04 | 10" Core |
|  | 3 | BA11002 | S22A01L03 | 10" Core |
| A02002 | 6 | BA02002 | S22A02L06 | 10" Core |
| C01002 | 6 | CA01002 | S22C01L06 | 6" Core |
| C02002 | 6 | CA02002 | S22C02L06 | 6" Core |
| C03002 | 6 | CA03002 | S22C03L06 | 6" Core |
| C04002 | 6 | CA04002 | S22C04L06 | 6" Core |
| C05002 | 6 | CA05002 | S22C05L06 | 6" Core |
| C06002 | 6 | CA06002 | S22C06L06 | 6" Core |
|  | 5 | CA06002 | S22C06L05 | 6" Core |
|  | 4 | CA15002 | S22C06L04 | 6" Core |
|  | 3 | CA18002 | S22C06L03 | 6" Core |
| C07002 | 6 | CA07002 | S22C07L06 | 6" Core |
| C08002 | 6 | CA08002 | S22C08L06 | 6" Core |
| C09002 | 6 | CA09002 | S22C09L06 | 6" Core |
| C10002 | 6 | CA10002 | S22C10L06 | 6" Core |
|  | 5 | CA10002 | S22C10L05 | 6" Core |
|  | 4 | CA16002 | S22C10L04 | 6" Core |
|  | 3 | CA19002 | S22C10L03 | 6" Core |
| C11002 | 6 | CA11002 | S22C11L06 | 6" Core |
| C12002 | 6 | CA12002 | S22C12L06 | 6" Core |
|  | 5 | CA12002 | S22C12L05 | 6" Core |
|  | 4 | CA17002 | S22C12L04 | 6" Core |
|  | 3 | CA20002 | S22C12L03 | 6" Core |
| C13002 | 6 | CA13002 | S22C13L06 | 6" Core |
| C14002 | 6 | CA14002 | S22C14L06 | 6" Core |
| F01002 | 6 | BA03002 | S22F01L06 | 2 5-gallon buckets uncompacted AC mix |
| F02002 | 6 | BA04002 | S22F02L06 | 2 5-gallon buckets uncompacted AC mix |
| F03002 | 6 | BA05002 | S22F03L06 | 2 5-gallon buckets uncompacted AC mix |
| F04002 | 6 | BA06002 | S22F04L06 | 3 5-gallon buckets uncompacted AC mix |
| F05002 | 6 | BA07002 | S22F05L06 | 2 5-gallon buckets uncompacted AC mix |
| F06002 | 6 | BA08002 | S22F06L06 | 2 5-gallon buckets uncompacted AC mix |
| F07002 | 6 | BA09002 | S22F07L06 | 2 5-gallon buckets uncompacted AC mix |

TABLE 8 SAMPLES ACQUIRED FROM TEST SECTION 35AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01003 | 6 | BA01003 | S23A01L06 | 10" Core |
| A02003 | 6 | BA02003 | S23A02L06 | 10" Core |
| C01003 | 6 | CA01003 | S23C01L06 | 6" Core |
| C02003 | 6 | CA02003 | S23C02L06 | 6" Core |
| C03003 | 6 | CA03003 | S23C03L06 | 6" Core |
| C04003 | 6 | CA04003 | S23C04L06 | 6" Core |
| C05003 | 6 | CA05003 | S23C05L06 | 6" Core |
| C06003 | 6 | CA06003 | S23C06L06 | 6" Core |
| C07003 | 6 | CA07003 | S23C07L06 | 6" Core |
| C08003 | 6 | CA08003 | S23C08L06 | 6" Core |
| C09003 | 6 | CA09003 | S23C09L06 | 6" Core |
| C10003 | 6 | CA10003 | S23C10L06 | 6" Core |
| C11003 | 6 | CA11003 | S23C11L06 | 6" Core |
| C12003 | 6 | CA12003 | S23C12L06 | 6" Core |
| C13003 | 6 | CA13003 | S23C13L06 | 6" Core |
| C14003 | 6 | CA14003 | S23C14L06 | 6" Core |
| F01003 | 6 | BA04003 | S23F01L06 | 2 5-gallon buckets uncompacted AC mix |
| F02003 | 6 | BA05003 | S23F02L06 | 2 5-gallon buckets uncompacted AC mix |
| F03003 | 6 | BA06003 | S23F03L06 | 2 5-gallon buckets uncompacted AC mix |
| F04003 | 6 | BA07003 | S23F04L06 | 3 5-gallon buckets uncompacted AC mix |
| F05003 | 6 | BA08003 | S23F05L06 | 2 5-gallon buckets uncompacted AC mix |
| F06003 | 6 | BA09003 | S23F06L06 | 2 5-gallon buckets uncompacted AC mix |
| F07003 | 6 | BA10003 | S23F07L06 | 2 5-gallon buckets uncompacted AC mix |

Note: Sample No. BA03003 not used

TABLE 9 SAMPLES ACQUIRED FROM TEST SECTION 35AA61

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01061 | 6 | BA01061 | S2AA01L06 | 10" Core |
|  | 5 | BA01061 | S2AA01L05 | 10" Core |
|  | 4 | BA10061 | S2AA01L04 | 10" Core |
|  | 3 | BA11061 | S2AA01L03 | 10" Core |
| A02061 | 6 | BA02061 | S2AA02L06 | 10" Core |
| C01061 | 6 | CA01061 | S2AC01L06 | 6" Core |
| C02061 | 6 | CA02061 | S2AC02L06 | 6" Core |
| C03061 | 6 | CA03061 | S2AC03L06 | 6" Core |
| C04061 | 6 | CA04061 | S2AC04L06 | 6" Core |
| C05061 | 6 | CA05061 | S2AC05L06 | 6" Core |
| C06061 | 6 | CA06061 | S2AC06L06 | 6" Core |
| C07061 | 6 | CA07061 | S2AC07L06 | 6" Core |
| C08061 | 6 | CA08061 | S2AC08L06 | 6" Core |
| C09061 | 6 | CA09061 | S2AC09L06 | 6" Core |
| C10061 | 6 | CA10061 | S2AC10L06 | 6" Core |
| C11061 | 6 | CA11061 | S2AC11L06 | 6" Core |
| C12061 | 6 | CA12061 | S2AC12L06 | 6" Core |
|  | 5 | CA12061 | S2AC12L05 | 6" Core |
|  | 4 | CA15061 | S2AC12L04 | 6" Core |
|  | 3 | CA18061 | S2AC12L03 | 6" Core |
| C13061 | 6 | CA13061 | S2AC13L06 | 6" Core |
|  | 5 | CA13061 | S2AC13L05 | 6" Core |
|  | 4 | CA16061 | S2AC13L04 | 6" Core |
|  | 3 | CA19061 | S2AC13L03 | 6" Core |
| C14061 | 6 | CA14061 | S2AC14L06 | 6" Core |
|  | 5 | CA14061 | S2AC14L05 | 6" Core |
|  | 4 | CA17061 | S2AC14L04 | 6" Core |
|  | 3 | CA20061 | S2AC14L03 | 6" Core |
| F01061 | 6 | BA03061 | S2AF01L06 | 2 5-gallon buckets uncompacted AC mix |
| F02061 | 6 | BA04061 | S2AF02L06 | 2 5-gallon buckets uncompacted AC mix |
| F03061 | 6 | BA05061 | S2AF03L06 | 2 5-gallon buckets uncompacted AC mix |
| F04061 | 6 | BA06061 | S2AF04L06 | 3 5-gallon buckets uncompacted AC mix |
| F05061 | 6 | BA07061 | S2AF05L06 | 2 5-gallon buckets uncompacted AC mix |
| F06061 | 6 | BA08061 | S2AF06L06 | 2 5-gallon buckets uncompacted AC mix |
| F07061 | 6 | BA09061 | S2AF07L06 | 2 5-gallon buckets uncompacted AC mix |

TABLE 10 SAMPLES ACQUIRED FROM TEST SECTION 35AA62

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01062 | 6 | BA01062 | S2BA01L06 | 10" Core |
| A02062 | 6 | BA02062 | S2BA02L06 | 10" Core |
| C01062 | 6 | CA01062 | S2BC01L06 | 6" Core |
| C02062 | 6 | CA02062 | S2BC02L06 | 6" Core |
| C03062 | 6 | CA03062 | S2BC03L06 | 6" Core |
| C04062 | 6 | CA04062 | S2BC04L06 | 6" Core |
| C05062 | 6 | CA05062 | S2BC05L06 | 6" Core |
| C06062 | 6 | CA06062 | S2BC06L06 | 6" Core |
| C07062 | 6 | CA07062 | S2BC07L06 | 6" Core |
| C08062 | 6 | CA08062 | S2BC08L06 | 6" Core |
| C09062 | 6 | CA09062 | S2BC09L06 | 6" Core |
| C10062 | 6 | CA10062 | S2BC10L06 | 6" Core |
| C11062 | 6 | CA11062 | S2BC11L06 | 6" Core |
| C12062 | 6 | CA12062 | S2BC12L06 | 6" Core |
| C13062 | 6 | CA13062 | S2BC13L06 | 6" Core |
| C14062 | 6 | CA14062 | S2BC14L06 | 6" Core |
| F01062 | 6 | BA03062 | S2BF01L06 | 2 5-gallon buckets uncompacted AC mix |
| F02062 | 6 | BA04062 | S2BF02L06 | 2 5-gallon buckets uncompacted AC mix |
| F03062 | 6 | BA05062 | S2BF03L06 | 2 5-gallon buckets uncompacted AC mix |
| F04062 | 6 | BA06062 | S2BF04L06 | 3 5-gallon buckets uncompacted AC mix |
| F05062 | 6 | BA07062 | S2BF05L06 | 2 5-gallon buckets uncompacted AC mix |
| F06062 | 6 | BA08062 | S2BF06L06 | 2 5-gallon buckets uncompacted AC mix |
| F07062 | 6 | BA09062 | S2BF07L06 | 2 5-gallon buckets uncompacted AC mix |
| F08062 | 6 | BA10062 | S2BF08L06 | 2 5-gallon buckets uncompacted AC mix |

TABLE 11: SAMPLES ACQUIRED FROM PLANT

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| H01001 | 6 | BC01001 | S21H01L6 | 1 1-gallon can virgin AC binder (PG 70-28) |
| H01001 | 6 | BC02001 | S21H02L6 | 1 1-gallon can virgin AC binder (PG 70-28) |
| H01001 | 6 | BC03001 | S21H03L6 | 10 1-gallon cans virgin AC binder (PG 70-28) |
| H01062 | 6 | BC01062 | S2BH01L6 | 1 1-gallon can virgin AC binder (PG 70-28+) |
| H01062 | 6 | BC02062 | S2BH02L6 | 1 1-gallon can virgin AC binder (PG 70-28+) |
| H01062 | 6 | BC03062 | S2BH03L6 | 11 1-gallon cans virgin AC binder (PG 70-28+) |
| H02001 | 6 | BU01001 | S21H04L6 | 20 5-gallon buckets combined aggregate |
| H03001 | 6 | BR01001 | S21H05L6 | 50 lb Bulk Sample RAP |
| H03001 | 6 | BR02001 | S21H06L6 | 10 5-gallon buckets RAP |
| H01003 | 6 | BW01003 | S23H01L6 | 3 gallon chemical additive (Evotherm®) in plastic bottles, with MSDS |
| H01061 | 6 | BW01061 | S2AH01L6 | 3 gallon chemical additive (Cecabase®) in plastic bottles, with MSDS |
| H04001 | 6 | BX01001 | S21H07L6 | 1 1-gallon can chemical additive (Versabind®), with MSDS |

TABLE 12: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S21A01L06 | 10" Core |
| S21A02L06 | 10" Core |
| S22A01L06 | 10" Core |
| S22A02L06 | 10" Core |
| S23A01L06 | 10" Core |
| S23A02L06 | 10" Core |
| S2AA01L06 | 10" Core |
| S2AA02L06 | 10" Core |
| S2BA01L06 | 10" Core |
| S2BA02L06 | 10" Core |
| S21C05L06 | 6" Core |
| S21C06L06 | 6" Core |
| S21C07L06 | 6" Core |
| S21C08L06 | 6" Core |
| S21C09L06 | 6" Core |
| S21C10L06 | 6" Core |
| S21C11L06 | 6" Core |
| S21C12L06 | 6" Core |
| S21C13L06 | 6" Core |
| S21C14L06 | 6" Core |
| S22C01L06 | 6" Core |
| S22C03L06 | 6" Core |
| S22C06L06 | 6" Core |
| S22C07L06 | 6" Core |
| S22C09L06 | 6" Core |
| S22C10L06 | 6" Core |
| S22C11L06 | 6" Core |
| S22C12L06 | 6" Core |
| S22C13L06 | 6" Core |
| S22C14L06 | 6" Core |
| S23C01L06 | 6" Core |
| S23C03L06 | 6" Core |
| S23C05L06 | 6" Core |
| S23C07L06 | 6" Core |
| S23C09L06 | 6" Core |

TABLE 12: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S23C10L06 | 6" Core |
| S23C11L06 | 6" Core |
| S23C12L06 | 6" Core |
| S23C13L06 | 6" Core |
| S23C14L06 | 6" Core |
| S2AC04L06 | 6" Core |
| S2AC06L06 | 6" Core |
| S2AC07L06 | 6" Core |
| S2AC08L06 | 6" Core |
| S2AC09L06 | 6" Core |
| S2AC10L06 | 6" Core |
| S2AC11L06 | 6" Core |
| S2AC12L06 | 6" Core |
| S2AC13L06 | 6" Core |
| S2AC14L06 | 6" Core |
| S2BC05L06 | 6" Core |
| S2BC06L06 | 6" Core |
| S2BC07L06 | 6" Core |
| S2BC08L06 | 6" Core |
| S2BC09L06 | 6" Core |
| S2BC10L06 | 6" Core |
| S2BC11L06 | 6" Core |
| S2BC12L06 | 6" Core |
| S2BC13L06 | 6" Core |
| S2BC14L06 | 6" Core |
| S21H01L06 | 1 1-gallon can of virgin AC binder (PG 70-28) |
| S2BH01L06 | 1 1-gallon can of virgin AC binder (PG 70-28+) |
| S21H05L06 | 50 lb Bulk Sample RAP |
| Original HMAC |  |
| S22A01L05 | 10" Core |
| S2AA01L05 | 10" Core |
| S22C06L05 | 6" Core |
| S22C10L05 | 6" Core |
| S22C12L05 | 6" Core |

TABLE 12: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Original HMAC |  |
| S2AC12L05 | 6" Core |
| S2AC13L05 | 6" Core |
| S2AC14L05 | 6" Core |
| Historic HMAC |  |
| S22A01L04 | 10" Core |
| S2AA01L04 | 10" Core |
| S22C06L04 | 6" Core |
| S22C10L04 | 6" Core |
| S22C12L04 | 6" Core |
| S2AC12L04 | 6" Core |
| S2AC13L04 | 6" Core |
| S2AC14L04 | 6" Core |
| S22A01L03 | 10" Core |
| S2AA01L03 | 10" Core |
| S22C06L03 | 6" Core |
| S22C10L03 | 6" Core |
| S22C12L03 | 6" Core |
| S2AC12L03 | 6" Core |
| S2AC13L03 | 6" Core |
| S2AC14L03 | 6" Core |

TABLE 13: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S21C01L06 | 6" Core |
| S21C02L06 | 6" Core |
| S21C03L06 | 6" Core |
| S21C04L06 | 6" Core |
| S22C02L06 | 6" Core |
| S22C04L06 | 6" Core |
| S22C05L06 | 6" Core |
| S22C08L06 | 6" Core |
| S23C02L06 | 6" Core |
| S23C04L06 | 6" Core |
| S23C06L06 | 6" Core |
| S23C08L06 | 6" Core |
| S2AC01L06 | 6" Core |
| S2AC02L06 | 6" Core |
| S2AC03L06 | 6" Core |
| S2AC05L06 | 6" Core |
| S2BC01L06 | 6" Core |
| S2BC02L06 | 6" Core |
| S2BC03L06 | 6" Core |
| S2BC04L06 | 6" Core |
| S21H03L6 | 10 1-gallon cans of virgin AC binder (PG 70-28) |
| S2BH03L6 | 11 1-gallon cans of virgin AC binder (PG 70-28+) |
| S21F01L06 | 2 5-gallon buckets uncompacted AC mix |
| S21F02L06 | 2 5-gallon buckets uncompacted AC mix |
| S21F03L06 | 4 5-gallon buckets uncompacted AC mix |
| S21F04L06 | 2 5-gallon buckets uncompacted AC mix |
| S21F05L06 | 3 5-gallon buckets uncompacted AC mix |
| S21F06L06 | 2 5-gallon buckets uncompacted AC mix |
| S22F01L06 | 2 5-gallon buckets uncompacted AC mix |
| S22F02L06 | 2 5-gallon buckets uncompacted AC mix |
| S22F03L06 | 2 5-gallon buckets uncompacted AC mix |
| S22F04L06 | 3 5-gallon buckets uncompacted AC mix |
| S22F05L06 | 2 5-gallon buckets uncompacted AC mix |
| S22F06L06 | 2 5-gallon buckets uncompacted AC mix |
| S22F07L06 | 2 5-gallon buckets uncompacted AC mix |

TABLE 13: SAMPLES TO BE SHIPPED TO THE LTPP MRL (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S23F01L06 | 2 5-gallon buckets uncompacted AC mix |
| S23F02L06 | 2 5-gallon buckets uncompacted AC mix |
| S23F03L06 | 2 5-gallon buckets uncompacted AC mix |
| S23F04L06 | 3 5-gallon buckets uncompacted AC mix |
| S23F05L06 | 2 5-gallon buckets uncompacted AC mix |
| S23F06L06 | 2 5-gallon buckets uncompacted AC mix |
| S23F07L06 | 2 5-gallon buckets uncompacted AC mix |
| S2AF01L06 | 2 5-gallon buckets uncompacted AC mix |
| S2AF02L06 | 2 5-gallon buckets uncompacted AC mix |
| S2AF03L06 | 2 5-gallon buckets uncompacted AC mix |
| S2AF04L06 | 3 5-gallon buckets uncompacted AC mix |
| S2AF05L06 | 2 5-gallon buckets uncompacted AC mix |
| S2AF06L06 | 2 5-gallon buckets uncompacted AC mix |
| S2AF07L06 | 2 5-gallon buckets uncompacted AC mix |
| S2BF01L06 | 2 5-gallon buckets uncompacted AC mix |
| S2BF02L06 | 2 5-gallon buckets uncompacted AC mix |
| S2BF03L06 | 2 5-gallon buckets uncompacted AC mix |
| S2BF04L06 | 3 5-gallon buckets uncompacted AC mix |
| S2BF05L06 | 2 5-gallon buckets uncompacted AC mix |
| S2BF06L06 | 2 5-gallon buckets uncompacted AC mix |
| S2BF07L06 | 2 5-gallon buckets uncompacted AC mix |
| S2BF08L06 | 2 5-gallon buckets uncompacted AC mix |
| S21H04L6 | 20 5-gallon buckets combined aggregate |
| S21H06L6 | 10 5-gallon buckets RAP |
| S23H01L6 | 3 gallon chemical additive (Evotherm®) in plastic bottles, with MSDS |
| S2AH01L6 | 3 gallon chemical additive (Cecabase®) in plastic bottles, with MSDS |
| S21H07L6 | 1 1-gallon can chemical additive (Versabind®), with MSDS |

TABLE 14: SAMPLES TO BE SHIPPED TO THE TURNER FAIRBANKS RESEARCH CENTER

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC Layer |  |
| S21H02L6 | 1 1-gallon cans virgin AC binder (PG 70-28) |
| S2BH02L6 | 1 1-gallon can virgin AC binder (PG 70-28+) |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the New Mexico SPS-10 project.  The previous section ended with lists of samples to be shipped to each of the two laboratories, the central lab testing contractor laboratory and the Turner-Fairbank Highway Research center.  In this section, the tests to be performed on each sample are listed.

Table 15 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Tables 16 and 17 provide new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 18 through 21 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 15: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 50 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 10 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 6 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 10 | X |  |
|  | Hamburg Wheel Track | AC09 | P75 | 10 | X |  |
|  | Fenix Fracture Energy | AC10 | P79 | 15 | X |  |
|  | Specific Gravity at 60 ° F | AE03 | P23 | 8 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 17 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 8 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 8 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 6 | X |  |
|  | PPA and Motor Oil Test | AE11 | P76 | 2 |  | X |
| B. | ORIGINAL HMAC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 6 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 2 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 2 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 4 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 2 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 2 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 2 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 2 | X |  |

TABLE 15: SPS-10 LABORATORY TESTING PLANS (Continued)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| C. | HISTORIC HMAC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 6 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 2 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 2 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 4 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 2 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 2 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 2 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 2 | X |  |
| D. | UTREATED BASE |  |  |  |  |  |
|  | N/A |  |  |  |  |  |
| E. | SUBGRADE |  |  |  |  |  |
|  | N/A |  |  |  |  |  |

TABLE 16: ORIGINAL AND COMBINED SPECIMEN DESCRIPTIONS

| Description Type | Status |  |  |
| --- | --- | --- | --- |
|  | Original |  | Combined1 |
| Sample No. | BA01001 | BA02001 | BAX1001 |
| Specimen ID | S21A01L06 | S21A02L06 | S21A01M06 |
| Sample No. | BA01002 | BA02002 | BAX1002 |
| Specimen ID | S22A01L06 | S22A02L06 | S22A01M06 |
| Sample No. | BA01003 | BA02003 | BAX1003 |
| Specimen ID | S23A01L06 | S23A02L06 | S23A01M06 |
| Sample No. | BA01061 | BA02061 | BAX1061 |
| Specimen ID | S2AA01L06 | S2AA02L06 | S2AA01M06 |
| Sample No. | BA01062 | BA02062 | BAX1062 |
| Specimen ID | S2BA01L06 | S2BA02L06 | S2BA01M06 |

1. Sample No.:  After combination, the third character is changed to “X,” and the fourth character is assigned numerically.  The other five characters follow the original format.

Specimen ID:  After combination, “L” is changed to “M.”

TABLE 17: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BAX1001 | BAE1001 |
|  | Specimen ID | S21A01M06 | S21A01A06 |
|  | Sample No. | BAX1002 | BAE1002 |
|  | Specimen ID | S22A01M06 | S22A01A06 |
|  | Sample No. | BAX1003 | BAE1003 |
|  | Specimen ID | S23A01M06 | S23A01A06 |
|  | Sample No. | BAX1061 | BAE1061 |
|  | Specimen ID | S2AA01M06 | S2AA01A06 |
|  | Sample No. | BAX1062 | BAE1062 |
|  | Specimen ID | S2BA01M06 | S2BA01A06 |
|  | Sample No. | BA01002 | BAE1002 |
|  | Specimen ID | S22A01L05 | S22A01M05 |
|  | Sample No. | BA01002 | BAE1002 |
|  | Specimen ID | S22A01L04 | S22A01M04 |
|  | Sample No. | BA01002 | BAE1002 |
|  | Specimen ID | S22A01L03 | S22A01M03 |
|  | Sample No. | BA01061 | BAE1061 |
|  | Specimen ID | S2AA01L05 | S2AA01M05 |
|  | Sample No. | BA01061 | BAE1061 |
|  | Specimen ID | S2AA01L04 | S2AA01M04 |
|  | Sample No. | BA01061 | BAE1061 |
|  | Specimen ID | S2AA01L03 | S2AA01M03 |
|  | Sample No. | BR01001 | BRE1001 |
|  | Specimen ID | S21H05L6 | S21H05M6 |
| PAV | Sample No. | BAE1001 | BAP1001 |
|  | Specimen ID | S21A01A06 | S21A01B06 |
|  | Sample No. | BAE1002 | BAP1002 |
|  | Specimen ID | S22A01A06 | S22A01B06 |
|  | Sample No. | BAE1003 | BAP1003 |
|  | Specimen ID | S23A01A06 | S23A01B06 |
|  | Sample No. | BAE1061 | BAP1061 |
|  | Specimen ID | S2AA01A06 | S2AA01B06 |
|  | Sample No. | BAE1062 | BAP1062 |
|  | Specimen ID | S2BA01A06 | S2BA01B06 |

TABLE 17: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS (Continued)

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| RTFO | Sample No. | BC01001 | BCR1001 |
|  | Specimen ID | S21H01L6 | S21H01M6 |
|  | Sample No. | BC01062 | BCR1062 |
|  | Specimen ID | S2BH01L6 | S2BH01M6 |
| PAV* | Sample No. | BCR1001 | BCZ1001 |
|  | Specimen ID | S21H01M6 | S21H01A6 |
|  | Sample No. | BCR1062 | BCZ1062 |
|  | Specimen ID | S2BH01M6 | S2BH01A6 |

*Here PAV aging has been assigned on RTFO aged sample (sample with R).

So, the final sample with “Z” is actually (RTFO+PAV) aged.

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S21A01L06 | P03/AC03 |  |  |  |  | Yes | C |
| S21A02L06 | P03/AC03 |  |  |  |  | Yes | C |
| S22A01L06 | P03/AC03 |  |  |  |  | Yes | C |
| S22A02L06 | P03/AC03 |  |  |  |  | Yes | C |
| S23A01L06 | P03/AC03 |  |  |  |  | Yes | C |
| S23A02L06 | P03/AC03 |  |  |  |  | Yes | C |
| S2AA01L06 | P03/AC03 |  |  |  |  | Yes | C |
| S2AA02L06 | P03/AC03 |  |  |  |  | Yes | C |
| S2BA01L06 | P03/AC03 |  |  |  |  | Yes | C |
| S2BA02L06 | P03/AC03 |  |  |  |  | Yes | C |
| S21A01M06 | P04/AC04 |  |  |  |  | No | E |
| S22A01M06 | P04/AC04 |  |  |  |  | No | E |
| S23A01M06 | P04/AC04 |  |  |  |  | No | E |
| S2AA01M06 | P04/AC04 |  |  |  |  | No | E |
| S2BA01M06 | P04/AC04 |  |  |  |  | No | E |
| S21A01A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| S22A01A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| S23A01A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| S2AA01A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| S2BA01A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| S21A01B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| S22A01B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S23A01B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| S2AA01B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| S2BA01B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| S21C05L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S21C06L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S21C07L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S21C08L06 | P02/AC02 | P79/AC10F |  |  |  | Yes | S |
| S21C09L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S21C10L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S21C11L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S21C12L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S21C13L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S21C14L06 | P02/AC02 | P75/AC09H |  |  |  | Yes | S |
| S22C01L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S22C03L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S22C06L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S22C07L06 | P02/AC02 | P79/AC10F |  |  |  | Yes | S |
| S22C09L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S22C10L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S22C11L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S22C12L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S22C13L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |

FSpare specimen for fracture test, DSpare for AMPT Dynamic Modulus, HSpare for Hamburg

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S22C14L06 | P02/AC02 | P75/AC09H |  |  |  | Yes | S |
| S23C01L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S23C03L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S23C05L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S23C07L06 | P02/AC02 | P79/AC10F |  |  |  | Yes | S |
| S23C09L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S23C10L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S23C11L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S23C12L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S23C13L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S23C14L06 | P02/AC02 | P75/AC09H |  |  |  | Yes | S |
| S2AC04L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S2AC06L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S2AC07L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S2AC08L06 | P02/AC02 | P79/AC10F |  |  |  | Yes | S |
| S2AC09L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S2AC10L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S2AC11L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S2AC12L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S2AC13L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S2AC14L06 | P02/AC02 | P75/AC09H |  |  |  | Yes | S |
| S2BC05L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S2BC06L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |

FSpare specimen for fracture test, DSpare for AMPT Dynamic Modulus, HSpare for Hamburg

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE OVERLAY IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S2BC07L06 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| S2BC08L06 | P02/AC02 | P79/AC10F |  |  |  | Yes | S |
| S2BC09L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S2BC10L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S2BC11L06 | P02/AC02 | P74/AC08D |  |  |  | Yes | S |
| S2BC12L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S2BC13L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S2BC14L06 | P02/AC02 | P75/AC09H |  |  |  | Yes | S |
| S21H01L6 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| S2BH01L6 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| S21H01M6 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| S2BH01M6 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| S21H01A6 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| S2BH01A6 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| S21H05L6 | P04/AC04 |  |  |  |  | Yes | E, S |
| S21H05M6 | P23/AE03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 | No | D |

FSpare specimen for fracture test, DSpare for AMPT Dynamic Modulus, HSpare for Hamburg

1. Next Process

D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV

TABLE 19: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S22A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S2AA01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S22A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| S2AA01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| S22C06L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S22C10L05 | P02/AC02 |  |  |  |  | Yes | S |
| S22C12L05 | P02/AC02 |  |  |  |  | Yes | S |
| S2AC12L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S2AC13L05 | P02/AC02 |  |  |  |  | Yes | S |
| S2AC14L05 | P02/AC02 |  |  |  |  | Yes | S |

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S22A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S2AA01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S22A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| S2AA01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| S22C06L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S22C10L04 | P02/AC02 |  |  |  |  | Yes | S |
| S22C12L04 | P02/AC02 |  |  |  |  | Yes | S |
| S2AC12L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S2AC13L04 | P02/AC02 |  |  |  |  | Yes | S |
| S2AC14L04 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 20: TRACKING TABLE OF HISTORIC HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S22A01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S2AA01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S22A01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| S2AA01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| S22C06L03 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S22C10L03 | P02/AC02 |  |  |  |  | Yes | S |
| S22C12L03 | P02/AC02 |  |  |  |  | Yes | S |
| S2AC12L03 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S2AC13L03 | P02/AC02 |  |  |  |  | Yes | S |
| S2AC14L03 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 21: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE OVERLAY IN THE TURNER FAIRBANKS HIGHWAY RESEARCH CENTER

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S21H02L5 | P76/AE11 |  |  |  |  | Yes | S |
| S2BH02L5 | P76/AE11 |  |  |  |  | Yes | S |

## SAMPLE LABELS - SPECIAL NOTE

During time zero material sampling, samples were labeled according to total five layers defined in Table 3. However, total six layers were identified and confirmed through coring and old construction files. TABLE 22 presents the revised and as-sampled layer numbers. Table 23 shows the list of labeled specimen ID that need to be revised accordingly.

TABLE 22: REVISED AND AS-SAMPLED LAYER NUMBERS

| Revised Layer Numbers |  | As-Sampled Layer Numbers |  |
| --- | --- | --- | --- |
| Layer Number | Description | Layer Number | Description |
| 1 | Subgrade | 1 | Subgrade |
| 2 | Untreated Base | 2 | Untreated Base |
| 3 | Historic AC - I | 3 | Historic AC |
| 4 | Historic AC - II | 4 | Original HMAC |
| 5 | Original HMAC | 5 | Experimental AC Overlay |
| 6 | Experimental AC Overlay |

TABLE 23: LABELED AND REVISED SPECIMEN ID

| Labeled Specimen ID | Revised Specimen ID |  | Labeled Specimen ID | Revised Specimen ID |
| --- | --- | --- | --- | --- |
| S21H01L5 | S21H01L6 |  | S23F01L05 | S23F01L06 |
| S21H02L5 | S21H02L6 |  | S23F02L05 | S23F02L06 |
| S21H03L5 | S21H03L6 |  | S23F03L05 | S23F03L06 |
| S2BH01L5 | S2BH01L6 |  | S23F04L05 | S23F04L06 |
| S2BH02L5 | S2BH02L6 |  | S23F05L05 | S23F05L06 |
| S2BH03L5 | S2BH03L6 |  | S23F06L05 | S23F06L06 |
| S21H04L5 | S21H04L6 |  | S23F07L05 | S23F07L06 |
| S21H05L5 | S21H05L6 |  | S2AF01L05 | S2AF01L06 |
| S21H06L5 | S21H06L6 |  | S2AF02L05 | S2AF02L06 |
| S23H01L5 | S23H01L6 |  | S2AF03L05 | S2AF03L06 |
| S2AH01L5 | S2AH01L6 |  | S2AF04L05 | S2AF04L06 |
| S21H07L5 | S21H07L6 |  | S2AF05L05 | S2AF05L06 |
| S21F01L05 | S21F01L06 |  | S2AF06L05 | S2AF06L06 |
| S21F02L05 | S21F02L06 |  | S2AF07L05 | S2AF07L06 |
| S21F03L05 | S21F03L06 |  | S2BF01L05 | S2BF01L06 |
| S21F04L05 | S21F04L06 |  | S2BF02L05 | S2BF02L06 |
| S21F05L05 | S21F05L06 |  | S2BF03L05 | S2BF03L06 |
| S21F06L05 | S21F06L06 |  | S2BF04L05 | S2BF04L06 |
| S22F01L05 | S22F01L06 |  | S2BF05L05 | S2BF05L06 |
| S22F02L05 | S22F02L06 |  | S2BF06L05 | S2BF06L06 |
| S22F03L05 | S22F03L06 |  | S2BF07L05 | S2BF07L06 |
| S22F04L05 | S22F04L06 |  | S2BF08L05 | S2BF08L06 |
| S22F05L05 | S22F05L06 |  |  |  |
| S22F06L05 | S22F06L06 |  |  |  |
| S22F07L05 | S22F07L06 |  |  |  |