NEW MEXICO SPS-10 PROJECT (35AA00)

MATERIALS SAMPLING AND TESTING PLAN – t2 CORING

AS-SAMPLED

Contents

GENERAL LAYOUT INFORMATION	1

MATERIALS SAMPLING AND FIELD TESTING	4

LABORATORY MATERIALS TESTING	15

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the New Mexico SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  Table 2 indicates transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Additionally, Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION

| Section Number | SHRP ID | Description |
| --- | --- | --- |
| 1 | 35AA01 | HMA Control Section – PG 70-28 |
| 2 | 35AA02 | WMA – Foaming Process – PG 70-28 |
| 3 | 35AA03 | WMA – Evotherm® – PG 70-28 |
| 4 | 35AA61 | WMA – Cecabase® – PG 70-28 |
| 5 | 35AA62 | WMA – Cecabase® – PG 70-28+ |

TABLE 2: TEST SECTION LAYOUT

| Begin STA | End STA | Description | Section ID |
| --- | --- | --- | --- |
| 882+24 | 881+24 | Sampling Area | 35AA01 |
| 881+24 | 880+74 | Buffer Area |  |
| 880+74 | 875+74 | Monitoring Area |  |
| 875+74 | 875+24 | Buffer Area |  |
| 875+24 | 874+24 | Sampling Area |  |
| 874+24 | 870+18 | Transition |  |
| 870+18 | 869+18 | Sampling Area | 35AA02 |
| 869+18 | 868+68 | Buffer Area |  |
| 868+68 | 863+68 | Monitoring Area |  |
| 863+68 | 863+18 | Buffer Area |  |
| 863+18 | 862+18 | Sampling Area |  |
| 862+18 | 845+97 | Transition |  |
| 845+97 | 844+97 | Sampling Area | 35AA03 |
| 844+97 | 844+47 | Buffer Area |  |
| 844+47 | 839+47 | Monitoring Area |  |
| 839+47 | 838+97 | Buffer Area |  |
| 838+97 | 837+97 | Sampling Area |  |
| 739+11 | 747+11 | Transition |  |
| 747+11 | 746+11 | Sampling Area | 35AA61 |
| 746+11 | 745+61 | Buffer Area |  |
| 745+61 | 740+61 | Monitoring Area |  |
| 740+61 | 740+11 | Buffer Area |  |
| 740+11 | 739+11 | Sampling Area |  |
| 739+11 | 732+10 | Transition |  |
| 732+10 | 731+10 | Sampling Area | 35AA62 |
| 731+10 | 730+60 | Buffer Area |  |
| 730+60 | 725+60 | Monitoring Area |  |
| 725+60 | 725+10 | Buffer Area |  |
| 725+10 | 724+10 | Sampling Area |  |
| 724+10 | 716+10 | Transition |  |

Sampling Area 061

Buffer Area (50 ft)

350A03

WMA Chemical

Additive (Evotherm)

Buffer Area (50 ft)

Sampling Area 051

Transition (length variable)

Sampling Area 041

Buffer Area (50 ft)

350A02

WMA Foaming Process

Buffer Area (50 ft)

Sampling Area 031

Transition (length variable)

Buffer Area (50 ft)

350A01

HMA Control

Section

Buffer Area (50 ft)

Sampling Area 011

Sampling Area 021

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic (WB)

845+97

862+18

837+97

870+18

874+24

882+24

839+47

844+47

863+68

868+68

875+74

880+74

Sampling Area 101

Buffer Area (50 ft)

350A62

WMA Chemical additive (Cecabase) with PG 70-28+

Buffer Area (50 ft)

Sampling Area 091

Transition (length variable)

Sampling Area 081

Buffer Area (50 ft)

350A61

WMA Chemical additive (Cecabase) with PG 70-28

Buffer Area (50 ft)

Sampling Area 071

Transition (length variable)

800ft

800ft

500ft

500ft

100ft

100ft

100ft

100ft

Traffic (WB)

724+10

732+10

739+11

747+11

739+11

725+60

730+60

740+61

745+61

FIGURE 1: NEW MEXICO SPS-10 PROJECT LAYOUT

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at time one (t2 is 12 months after construction).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 2 through 6 show the material sampling locations for each section.

Tables 6 through 11 list the samples acquired from each of the five test.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 11 and 12 list samples to be shipped to the central lab testing contractor laboratory and the LTPP Materials Reference Library (MRL).

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For New Mexico SPS-10, R = “S,” representing southern region)

- C = Construction event (For New Mexico SPS-10, C = 2, representing second constructed SPS-10)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 61

  - B – 62

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

TABLE 3: PROJECT LAYER NUMBERING

| Layer No. | Description |
| --- | --- |
| 1 | Subgrade |
| 2 | Untreated Base |
| 3 | Historic AC |
| 4 | Original HMAC |
| 5 | Experimental AC Overlay |

TABLE 4: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
|  | t-2 SAMPLING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 6" Core | 30 | C21201-C27201, C21202-C26202, C21203-C27203, C21261-C26261, C21262-C27262 |
|  | 12” Core | 4 | A03202-A04202, A03261-A03262 |
| B. | ORIGINAL HMAC | N/A | Sample not collected |
| C. | HISTORIC HMAC | N/A | Sample not collected. |
| D. | UNTREATED BASE |  |  |
|  | 6" Core | 2 | C242262,C26262 |
|  | Bulk Sample (150lb) | 2 | A03202, A03261 |
| E. | SUBGRADE |  |  |
|  | Bulk Sample (150lb), moisture content jar | 2 | A03202, A03261 |

TABLE 5: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Sample Location |
| --- | --- | --- | --- |
|  | t-2 SAMPLING |  |  |
| A. | EXPERIMENTAL HMAC |  |  |
|  | Core Examination and Thickness (P01/AC01) | 30 | C21201-C27201, C21202-C26202, C21203-C27203, C21261-C26261, C21262-C27262 |
|  | 12” Core | 4 | A03202-A04202, A03261-A03262 |

0-90

0-70

Section STA:

Section: 35AA01

Description: HMAC Control Section

Sampling Area: 01

Sampling Interval: t2

Shoulder

C22201

C24201

C26201

2’

1’

2’

2’

2’

C21201

C23201

C25201

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

C27201

2’

FIGURE 2 SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA01 AT TIME 1 NEW MEXICO SPS-10

0-90

0-70

Section STA:

Section: 35AA02

Description: Mix with WMA Foaming Process

Sampling Area: 03

Sampling Interval: t2

Shoulder

C22202

C24202

C26202

2’

3’

2’

1’

3’

2’

2’

2’

C21202

C23202

C25202

A03202

A04202

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

10” Core Experimental AC; Auger Base and Subgrade

FIGURE 3: SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA02 AT TIME 1 NEW MEXICO SPS-10

0-90

0-70

Section STA:

Section: 35AA03

Description: Mix with WMA Chemical Additive

Sampling Area: 05

Sampling Interval: t2

Shoulder

C22203

C24203

C26203

2’

1’

2’

2’

2’

C21203

C23203

C25203

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

C27203

2’

FIGURE 4: SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA03 AT TIME 1 NEW MEXICO SPS-10

0-90

0-70

Section STA:

Section: 35AA61

Description: Supplemental Section 1

Sampling Area: 07

Sampling Interval: t2

Shoulder

C22261

C24261

C26261

2’

3’

2’

1’

3’

2’

2’

2’

C21261

C232613

C25261

A03261

A04261

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

10” Core Experimental AC; Auger Base and Subgrade

FIGURE 5: SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA61 AT TIME 1 NEW MEXICO SPS-10

0-90

0-70

Section STA:

Section: 350A62

Description: Supplemental Section 2

Sampling Area: 09

Sampling Interval: t2

Shoulder

C22262

C24262

C26262

2’

1’

2’

2’

2’

C21262

C23262

C25262

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

C27262

2’

FIGURE 6: SAMPLING AND TESTING PLAN FOR TEST SECTION 35AA62 AT TIME 1 NEW MEXICO SPS-10

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 35AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C21201 | 6 | CA21201 | S21C21L06 | 6" Core |
| C22201 | 6 | CA22201 | S21C22L06 | 6" Core |
| C23201 | 6 | CA23201 | S21C23L06 | 6" Core |
| C24201 | 6 | CA24201 | S21C24L06 | 6" Core |
| C25201 | 6 | CA25201 | S21C25L06 | 6" Core |
| C26201 | 6 | CA26201 | S21C26L06 | 6" Core |
| C27201 | 6 | CA27201 | S21C27L06 | 6" Core |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 35AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C21202 | 6 | CA21202 | S22C21L06 | 6" Core |
| C22202 | 6 | CA22202 | S22C22L06 | 6" Core |
| C23202 | 6 | CA23202 | S22C23L06 | 6" Core |
| C24202 | 6 | CA24202 | S22C24L06 | 6" Core |
| C25202 | 6 | CA25202 | S22C25L06 | 6" Core |
| C26202 | 6 | CA26202 | S22C26L06 | 6" Core |
| A03202 | 6 | BA03202 | S22A03L06 | 10” Core |
| A04202 | 6 | BA04202 | S22A04L06 | 10” Core |
| A03202 | 2 | BG03202 | S22A03L02 | Untreated base, 150lb bulk sample |
| A03202 | 1 | BS03202 | S22A03L01 | Subgrade, 150lb bulk sample |

TABLE 8 SAMPLES ACQUIRED FROM TEST SECTION 35AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C21203 | 6 | CA21203 | S23C21L06 | 6" Core |
| C22203 | 6 | CA22203 | S23C22L06 | 6" Core |
| C23203 | 6 | CA23203 | S23C23L06 | 6" Core |
| C24203 | 6 | CA24203 | S23C24L06 | 6" Core |
| C25203 | 6 | CA25203 | S23C25L06 | 6" Core |
| C26203 | 6 | CA26203 | S23C26L06 | 6" Core |
| C27203 | 6 | CA27203 | S23C27L06 | 6” Core |

TABLE 9 SAMPLES ACQUIRED FROM TEST SECTION 35AA61

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C21261 | 6 | CA21261 | S2AC21L06 | 6" Core |
| C22261 | 6 | CA22261 | S2AC22L06 | 6" Core |
| C23261 | 6 | CA23261 | S2AC23L06 | 6" Core |
| C24261 | 6 | CA24261 | S2AC24L06 | 6" Core |
| C25261 | 6 | CA25261 | S2AC25L06 | 6" Core |
| C26261 | 6 | CA26261 | S2AC26L06 | 6" Core |
| A03261 | 6 | BA03261 | S2AA03L06 | 10" Core |
| A04261 | 6 | BA04261 | S2AA04L06 | 10" Core |
| A03261 | 2 | BG03261 | S2AA03L02 | Untreated base, 150lb bulk sample |
| A03261 | 1 | BS03261 | S2AA03L01 | Subgrade, 150lb bulk sample |

TABLE 10 SAMPLES ACQUIRED FROM TEST SECTION 35AA62

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C21262 | 6 | CA21262 | S2BC21L06 | 6" Core |
| C22262 | 6 | CA22262 | S2BC22L06 | 6" Core |
| C23262 | 6 | CA23262 | S2BC23L06 | 6" Core |
| C24262 | 6 | CA24262 | S2BC24L06 | 6" Core |
| C25262 | 6 | CA25262 | S2BC25L06 | 6" Core |
| C26262 | 6 | CA26262 | S2BC26L06 | 6" Core |
| C27262 | 6 | CA27262 | S2BC27L06 | 6" Core |
| C24262 | 2 | *CG01262 | S2BC24L02 | 6" Core |
| C26262 | 2 | *CG02262 | S2BC26L02 | 6" Core |

* Sample numbers CG01262 and CG02262 were shipped as CT01262 and CT02262 assuming that they were treated base layers, which was later decided as untreated base layer, hence T changed to G on sample number. These samples can be discarded or stored for combining with other bulk samples from base layer. See Material sampling plan for time period t1.

TABLE 11: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S21C21L06 | 6" Core |
| S21C22L06 | 6" Core |
| S21C23L06 | 6" Core |
| S21C24L06 | 6" Core |
| S22C21L06 | 6" Core |
| S22C22L06 | 6" Core |
| S22C23L06 | 6" Core |
| S23C21L06 | 6" Core |
| S23C22L06 | 6" Core |
| S23C23L06 | 6" Core |
| S23C24L06 | 6" Core |
| S2AC21L06 | 6" Core |
| S2AC22L06 | 6" Core |
| S2AC23L06 | 6" Core |
| S2BC21L06 | 6" Core |
| S2BC22L06 | 6" Core |
| S2BC23L06 | 6" Core |
| S2BC24L06 | 6" Core |
| S22A03L06 | 12" Core |
| S22A04L06 | 12" Core |
| S2AA03L06 | 12" Core |
| S2AA04L06 | 12" Core |
| S2BC24L02 | 6" Core |
| S2BC26L02 | 6" Core |
| S22A03L02 | Untreated base, 150lb bulk sample |
| S22A03L01 | Subgrade, 150lb bulk sample |
| S2AA03L02 | Untreated base, 150lb bulk sample |
| S2AA03L01 | Subgrade, 150lb bulk sample |

TABLE 12: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S21C25L06 | 6" Core |
| S21C26L06 | 6" Core |
| S21C27L06 | 6" Core |
| S22C24L06 | 6" Core |
| S22C25L06 | 6" Core |
| S22C26L06 | 6" Core |
| S23C25L06 | 6" Core |
| S23C26L06 | 6" Core |
| S23C27L06 | 6" Core |
| S2AC24L06 | 6" Core |
| S2AC25L06 | 6" Core |
| S2AC26L06 | 6" Core |
| S2BC25L06 | 6" Core |
| S2BC26L06 | 6" Core |
| S2BC27L06 | 6" Core |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the New Mexico SPS-10 project.  In this section, the tests to be performed on each sample are listed.

Table 15 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Tables 16 and 17 provide new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 18 through 21 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 13: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |
| --- | --- | --- | --- | --- | --- |
| A. | EXPERIMENTAL AC |  |  |  |  |
|  | Core Examination and thickness | AC01 | P01 | 37 | RSC |
|  | Bulk Specific Gravity | AC02 | P02 | 15 | CLTC |
|  | Asphalt Extraction | AC04 | P04 | 5 | CLTC |
|  | Dynamic Modulus | AC08 | P74 | 5 | CLTC |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 5 | CLTC |
|  | Bending beam rheometer | AE08 | P28 | 5 | CLTC |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 5 | CLTC |
| B. | UNTREATED BASE |  |  |  |  |
|  | Sieve Analysis | UG03 | P41 | 2 | CLTC |
|  | Classification | UG08 | P47 | 2 | CLTC |
|  | Atterberg Limits | UG04 | P43 | 2 | CLTC |
|  | Standard Proctor | UG05 | P44 | 2 | CLTC |
|  | Resilient Modulus | UG07 | P46 | 2 | CLTC |
| D. | SUBGRADE |  |  |  |  |
|  | Sieve Analysis | SS01 | P51 | 2 | CLTC |
|  | Atterberg Limits | SS03 | P43 | 2 | CLTC |
|  | Classification and Description | SS04 | P52 | 2 | CLTC |
|  | Standard Proctor | SS05 | P55 | 2 | CLTC |
|  | Resilient Modulus | SS07 | P46 | 2 | CLTC |
|  | Natural Moisture Content | SS09 | P49 | 2 | CLTC |

TABLE 14: ORIGINAL AND COMBINED SPECIMEN DESCRIPTIONS

| Description Type | Status |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Original |  |  |  | Combined1 |
| Sample No. | CA21201 | CA22201 | CA23201 | CA24201 | CAX1201 |
| Specimen ID | S21C21L06 | S21C22L06 | S21C23L06 | S21C24L06 | S21C21M06 |
| Sample No. | CA21203 | CA22203 | CA23203 | CA24203 | CAX1203 |
| Specimen ID | S23C21L06 | S23C22L06 | S23C23L06 | S23C24L06 | S23C21M06 |
| Sample No. | CA21262 | CA22262 | CA23262 | CA24262 | CAX1262 |
| Specimen ID | S2BC21L06 | S2BC22L06 | S2BC23L06 | S2BC24L06 | S2BC21M06 |

1. Sample No.:  After combination, the third character is changed to “X,” and the fourth character is assigned numerically.  The other five characters follow the original format.

Specimen ID:  After combination, “L” is changed to “M.”

TABLE 15: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | CAX1201 | CAE1201 |
|  | Specimen ID | S21C21M06 | S21C21A06 |
|  | Sample No. | BA03202 | BAE3202 |
|  | Specimen ID | S22A03L06 | S22A03M06 |
|  | Sample No. | CAX1203 | CAE1203 |
|  | Specimen ID | S23C21M06 | S23C21A06 |
|  | Sample No. | BA03261 | BAE3261 |
|  | Specimen ID | S2AA03L06 | S2AA03M06 |
|  | Sample No. | CAX1262 | CAE1262 |
|  | Specimen ID | S2BC21M06 | S2BC21A06 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 16: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |  |  |  |
| S21C21L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S21C22L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S21C23L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S22C21L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S22C22L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S22C23L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S23C21L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S23C22L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S23C23L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S2AC21L06 | P02/AC02 | P74/AC08 |  |  |  |  | Yes | C |
| S2AC22L06 | P02/AC02 | P74/AC08 |  |  |  |  | No | C |
| S2AC23L06 | P02/AC02 | P74/AC08 |  |  |  |  | No | C |
| S2BC21L06 | P02/AC02 | P74/AC08 |  |  |  |  | No | C |
| S2BC22L06 | P02/AC02 | P74/AC08 |  |  |  |  | No | C |
| S2BC23L06 | P02/AC02 | P74/AC08 |  |  |  |  | No | C |
| S21C21M06 | P04/AC04 |  |  |  |  |  | No | E |
| S22A03L06 | P04/AC04 |  |  |  |  |  | No | E |
| S23C21M06 | P04/AC04 |  |  |  |  |  | No | E |
| S2AA03L06 | P04/AC04 |  |  |  |  |  | No | E |
| S2BC21M06 | P04/AC04 |  |  |  |  |  | No | E |
| S21C21A06 | P27/AE07 | P28/AE08 | P73/AE10 |  |  |  | No | D |
| S22A03M06 | P27/AE07 | P28/AE08 | P73/AE10 |  |  |  | No | D |
| S23C21A06 | P27/AE07 | P28/AE08 | P73/AE10 |  |  |  | No | D |
| S2AA03M06 | P27/AE07 | P28/AE08 | P73/AE10 |  |  |  | No | D |
| S2BC21A06 | P27/AE07 | P28/AE08 | P73/AE10 |  |  |  | No | D |

Table 17: TRACKING TABLE OF BASE AND SUBGRADE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |  |
| S22A03L02 | P41/UG01 | P47/UG08 | P43/UG04 | P44/UG07 | P46/UG05 |  | No | D |
| S2AA03L02 | P41/UG01 | P47/UG08 | P43/UG04 | P44/UG07 | P46/UG05 |  | No | D |
| S22A03L01 | P51/SS01 | P43/SS03 | P52/SS04 | P55/SS05 | P46/SS07 |  | No | D |
| S22A03L01 | P49/SS09 |  |  |  |  |  |  |  |
| S2AA03L01 | P51/SS01 | P43/SS03 | P52/SS04 | P55/SS05 | P46/SS07 |  | No | D |
| S2AA03L01 | P49/SS09 |  |  |  |  |  |  |  |

1. Next Process

D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV