OKLAHOMA SPS-10

MATERIALS SAMPLING AND TESTING PLAN

t2 - CORING

Contents

I.	GENERAL LAYOUT INFORMATION	1

I.1.	Core test sections	2

I.2.	Supplementary test sections	4

II.	MATERIALS SAMPLING AND FIELD TESTING	6

II.1.	Identification Codes	6

II.2.	Material Sampling	9

II.2.1.	Core Test Sections	9

II.2.2.	Supplementary test sections	14

II.3.	Samples to be shipped	21

III.	LABORATORY MATERIAL TESTING	23

III.1.	Testing Plans	24

III.2.	Tracking Tables	27

# GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the SPS-10 project in terms of the location of the test sections along the roadway. Table 1 lists each section and its respective description.

Table 1. Test sections identification and description

| Section Number | Section ID | Description |
| --- | --- | --- |
| 01 | 40AA01 | HMA Control Section |
| 02 | 40AA02 | Mix with WMA Foaming Process |
| 03 | 40AA03 | Mix with WMA Chemical Additive |
| 61 | 40AA61 | WMA with PG 64-22 with 10-25% RAP/RAS |
| 62 | 40AA62 | WMA with PG 58-28 with 10-25% RAP/RAS |
| 63 | 40AA63 | SMA/WMA with PG 70-28 without RAP/RAS |

## Core test sections

Table 2 tracks the core test sections from the beginning of the initial transition area at station 00+00 to the end of the last section at station 48+50.

Table 2 indicates transition areas between each section as well as the buffer and monitoring areas for each section.  Additionally, Figure 1 provides a visual representation of the core test sections layout.

Table 2. Core test sections layout

| Description | Core Test Sections |  |  |
| --- | --- | --- | --- |
|  | Begin STA | End STA | Section ID |
| Transition | 00+00 | 04+50 |  |
| Sampling Area | 04+50 | 05+50 | 40AA01 |
| Buffer Area | 05+50 | 06+00 |  |
| Monitoring Area | 06+00 | 11+00 |  |
| Buffer Area | 11+00 | 11+50 |  |
| Sampling Area | 11+50 | 12+50 |  |
| Transition | 12+50 | 23+50 |  |
| Sampling Area | 23+50 | 24+50 | 40AA02 |
| Buffer Area | 24+50 | 25+00 |  |
| Monitoring Area | 25+00 | 30+00 |  |
| Buffer Area | 30+00 | 30+50 |  |
| Sampling Area | 30+50 | 31+50 |  |
| Transition | 31+50 | 40+50 |  |
| Sampling Area | 40+50 | 41+50 | 40AA03 |
| Buffer Area | 41+50 | 42+00 |  |
| Monitoring Area | 42+00 | 47+00 |  |
| Buffer Area | 47+00 | 47+50 |  |
| Sampling Area | 47+50 | 48+50 |  |

Sampling Area 011

Buffer Area (50 ft)

40AA01

HMA Control

Test Section

Buffer Area (50 ft)

Sampling Area 021

Transition (length variable)

Sampling Area 031

Buffer Area (50 ft)

40AA02

WMA Foaming

Process Test Section

Buffer Area (50 ft)

Sampling Area 041

Transition (length variable)

Buffer Area (50 ft)

40AA03

WMA Chemical

Additive Test Section

Buffer Area (50 ft)

Sampling Area 061

Sampling Area 051

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic

12+50

23+50

04+50

31+50

40+50

48+50

11+50

16+50

29+50

34+50

47+50

52+50

Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t2, t5, t7, t9

Figure 1. Oklahoma SPS-10 core test sections layout

## Supplementary test sections

Table 3 tracks the test sections from the beginning of the initial transition area at station 48+50 to the end of the last section at station 100+50.  Table 3 indicates transition areas between each section as well as the buffer and monitoring areas for each section.  Additionally, Figure 2 provides a visual representation of the supplementary test sections layout.

Table 3. Supplementary test sections layout

| Description | Supplementary test sections |  |  |
| --- | --- | --- | --- |
|  | Begin STA | End STA | Section ID |
| Transition | 48+50 | 54+50 |  |
| Sampling Area | 54+50 | 55+50 | 40AA61 |
| Buffer Area | 55+50 | 56+00 |  |
| Monitoring Area | 56+00 | 61+00 |  |
| Buffer Area | 61+00 | 61+50 |  |
| Sampling Area | 61+50 | 62+50 |  |
| Transition | 62+50 | 70+50 |  |
| Sampling Area | 70+50 | 71+50 | 40AA62 |
| Buffer Area | 71+50 | 72+00 |  |
| Monitoring Area | 72+00 | 77+00 |  |
| Buffer Area | 77+00 | 77+50 |  |
| Sampling Area | 77+50 | 78+50 |  |
| Transition | 78+50 | 92+50 |  |
| Sampling Area | 92+50 | 93+50 | 40AA63 |
| Buffer Area | 93+50 | 94+00 |  |
| Monitoring Area | 94+00 | 99+00 |  |
| Buffer Area | 99+00 | 99+50 |  |
| Sampling Area | 99+50 | 100+50 |  |

Sampling Area 071

Buffer Area (50 ft)

40AA61

WMA

PG 70-28 with 10-25% RAP/RAS Test Section

Buffer Area (50 ft)

Sampling Area 081

Transition (length variable)

Sampling Area 091

Buffer Area (50 ft)

40AA62

WMA

PG 64-22 with 10-25% RAP/RAS Test Section

Buffer Area (50 ft)

Sampling Area 101

Transition (length variable)

Buffer Area (50 ft)

40AA63

WMA

PG 58-28 with 10-25% RAP/RAS Test Section

Buffer Area (50 ft)

Sampling Area 121

Sampling Area 111

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic

62+50

70+50

54+50

78+50

92+50

100+50

61+50

66+50

77+50

82+50

99+50

104+50

Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t2, t5, t7, t9

Figure 2. Oklahoma SPS-10 project layout, supplementary sections

# MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the material sampling and testing activities that occur in the field as part of time 2 (t2 is at 12 months after construction). Table 4 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 5 provides the scope of material sampling for core sections and Table 9 provides the scope of material sampling for the supplemental sections.

Figure 3 through Figure 8 show the material sampling locations for each section.

Table 6 to Table 8 list the samples acquired from three core test sections and Table 10 to Table 12 list the samples acquired from three supplemental test sections. These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Table 13 and Table 14  list samples to be shipped to the central lab testing contractor laboratory and the LTPP Materials Reference Library (MRL) respectively. Finally, Table 15 through Table 17 represent the testing plans and Table 18 is for the material tracking system.

## Identification Codes

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID.   A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Oklahoma SPS-10, R = “S,” representing southern region)

- C = Construction event (For Oklahoma SPS-10, C = 4)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - 4 – 61

  - 5 – 62

  - 6 – 63

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number*

Table 4. Project layer numbering

| Layer No. | Description |
| --- | --- |
| 1 | Subgrade |
| 2 | Unbound Base |
| 3 | Original HMAC |
| 4 | Experimental AC |

Note*: The layer number is assigned with one character instead of two in the Material Tracking System as it accepts only of eight characters. The specimen ID, therefore, was reduced to eight characters during sampling.

## Material Sampling

### Core Test Sections

Table 5. Scope of material sampling for core test sections

| Material and Sample Description |  | No. of Samples per section |  |  | Sample Location |
| --- | --- | --- | --- | --- | --- |
|  |  | 01 | 02 | 03 |  |
|  | POST-CONSTRUCTION t2 SAMPLING |  |  |  |  |
| A. | EXPERIMENTAL AC |  |  |  |  |
|  | 6" Core | 7 | 7 | 7 | C29201-C35201, C23202-C29202, C29203-C35203 |

Table 6. Samples acquired from test section 40AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t2 sampling |  |  |  |  |
| C29201 | 8 | CA01201 | S41C29L8 | 6" Core |
| C30201 | 8 | CA02201 | S41C30L8 | 6" Core |
| C31201 | 8 | CA03201 | S41C31L8 | 6" Core |
| C32201 | 8 | CA04201 | S41C32L8 | 6" Core |
| C33201 | 8 | CA05201 | S41C33L8 | 6" Core |
| C34201 | 8 | CA06201 | S41C34L8 | 6" Core |
| C35201 | 8 | CA07201 | S41C35L8 | 6" Core |

Table 7. Samples acquired from test section 40AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t2 sampling |  |  |  |  |
| C23202 | 8 | CA01202 | S42C23L8 | 6" Core |
| C24202 | 8 | CA02202 | S42C24L8 | 6" Core |
| C25202 | 8 | CA03202 | S42C25L8 | 6" Core |
| C26202 | 8 | CA04202 | S42C26L8 | 6" Core |
| C27202 | 8 | CA05202 | S42C27L8 | 6" Core |
| C28202 | 8 | CA06202 | S42C28L8 | 6" Core |
| C29202 | 8 | CA07202 | S42C29L8 | 6" Core |

Table 8. Samples acquired from test section 40AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t2 sampling |  |  |  |  |
| C29203 | 8 | CA01203 | S43C29L8 | 6" Core |
| C30203 | 8 | CA02203 | S43C30L8 | 6" Core |
| C31203 | 8 | CA03203 | S43C31L8 | 6" Core |
| C32203 | 8 | CA04203 | S43C32L8 | 6" Core |
| C33203 | 8 | CA05203 | S43C33L8 | 6" Core |
| C34203 | 8 | CA06203 | S43C34L8 | 6" Core |
| C35203 | 8 | CA07203 | S43C35L8 | 6" Core |

5+70

5+90

Section STA:

Section: 40AA01

Description: HMAC Control Section

Sampling Interval: t2

Shoulder

C30201

C32201

C34201

2’

1’

3’

2’

2’

2’

2’

C29201

C31201

C33201

C29201

C35201

3’

2’

1’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

1’

Figure 3. Sampling and testing plan for test section 40AA01 at post-construction time 2 Oklahoma SPS-10

5+70

5+90

Section STA:

Section: 40AA02

Description: HMAC Control Section

Sampling Interval: t2

Shoulder

C24202

C26202

C28202

2’

1’

3’

2’

2’

2’

2’

C23202

C25202

C27202

C29202

3’

2’

1’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

1’

Figure 4. Sampling and testing plan for test section 40AA02 at post-construction time 2 Oklahoma SPS-10

5+70

5+90

Section STA:

Section: 40AA03

Description: HMAC Control Section

Sampling Interval: t2

Shoulder

C30203

C32203

C34203

2’

1’

3’

2’

2’

2’

2’

C29203

C31203

C33203

C29201

C35203

3’

2’

1’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

1’

Figure 5. Sampling and testing plan for test section 40AA03 at post-construction time 2 Oklahoma SPS-10

### Supplementary test sections

Table 9. Scope of material sampling for supplementary test sections

| POST-CONSTRUCTION t2SAMPLING |  |  |  |  |
| --- | --- | --- | --- | --- |
| EXPERIMENTAL AC |  |  |  |  |
| 6" Core | 7 | 7 | 7 | C23261-C29261, C29262-C35262, C23263-C29263 |

Table 10. Samples acquired from test section 40AA61

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t2 sampling |  |  |  |  |
| C23261 | 8 | CA01261 | S44C23L8 | 6" Core |
| C24261 | 8 | CA02261 | S44C24L8 | 6" Core |
| C25261 | 8 | CA03261 | S44C25L8 | 6" Core |
| C26261 | 8 | CA04261 | S44C26L8 | 6" Core |
| C27261 | 8 | CA05261 | S44C27L8 | 6" Core |
| C28261 | 8 | CA06261 | S44C28L8 | 6" Core |
| C29261 | 8 | CA07261 | S44C29L8 | 6" Core |

Table 11. Samples acquired from test section 40AA62

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t2 sampling |  |  |  |  |
| C29262 | 8 | CA01262 | S45C29L8 | 6" Core |
| C30262 | 8 | CA02262 | S45C30L8 | 6" Core |
| C31262 | 8 | CA03262 | S45C31L8 | 6" Core |
| C32262 | 8 | CA04262 | S45C32L8 | 6" Core |
| C33262 | 8 | CA05262 | S45C33L8 | 6" Core |
| C34262 | 8 | CA06262 | S45C34L8 | 6" Core |
| C35262 | 8 | CA07262 | S45C35L8 | 6" Core |

Table 12. Samples acquired from test section 40AA63

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| Post-construction – t2 sampling |  |  |  |  |
| C23263 | 8 | CA01263 | S46C23L8 | 6" Core |
| C24263 | 8 | CA02263 | S46C24L8 | 6" Core |
| C25263 | 8 | CA03263 | S46C25L8 | 6" Core |
| C26263 | 8 | CA04263 | S46C26L8 | 6" Core |
| C27263 | 8 | CA05263 | S46C27L8 | 6" Core |
| C28263 | 8 | CA06263 | S46C28L8 | 6" Core |
| C29263 | 8 | CA07263 | S46C29L8 | 6" Core |

5+70

5+90

Section STA:

Section: 40AA61

Description: HMAC Control Section

Sampling Interval: t2

Shoulder

C24261

C26261

C28261

2’

1’

3’

2’

2’

2’

2’

C23261

C25261

C27261

C29261

3’

2’

1’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

1’

Figure 6. Sampling and testing plan for test section 40AA61 construction time 2 Oklahoma SPS-10

5+70

5+90

Section STA:

Section: 40AA62

Description: HMAC Control Section

Sampling Interval: t2

Shoulder

C30262

C32262

C34262

2’

1’

3’

2’

2’

2’

2’

C29262

C31262

C33262

C29201

C35262

3’

2’

1’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

1’

Figure 7. Sampling and testing plan for test section 40AA62 at post-construction time 2 Oklahoma SPS-10

5+70

5+90

Section STA:

Section: 40AA63

Description: HMAC Control Section

Sampling Interval: t2

Shoulder

C24263

C26263

C28263

2’

1’

3’

2’

2’

2’

2’

C23263

C25263

C27263

C29263

3’

2’

1’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

1’

Figure 8. Sampling and testing plan for test section 40AA63 at post-construction time 2 Oklahoma SPS-10

## Samples to be shipped

Table 13. Samples to be shipped to central lab testing contractor laboratory

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S41C29L8 | 6" Core |
| S41C30L8 | 6" Core |
| S41C31L8 | 6" Core |
| S41C32L8 | 6" Core |
| S42C23L8 | 6" Core |
| S42C24L8 | 6" Core |
| S42C25L8 | 6" Core |
| S42C26L8 | 6" Core |
| S43C29L8 | 6" Core |
| S43C30L8 | 6" Core |
| S43C31L8 | 6" Core |
| S43C32L8 | 6" Core |
| S44C23L8 | 6" Core |
| S44C24L8 | 6" Core |
| S44C25L8 | 6" Core |
| S44C26L8 | 6" Core |
| S45C29L8 | 6" Core |
| S45C30L8 | 6" Core |
| S45C31L8 | 6" Core |
| S45C32L8 | 6" Core |
| S46C23L8 | 6" Core |
| S46C24L8 | 6" Core |
| S46C25L8 | 6" Core |
| S46C26L8 | 6" Core |

Table 14. Samples to be shipped to the LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S41C33L8 | 6" Core |
| S41C34L8 | 6" Core |
| S41C35L8 | 6" Core |
| S42C27L8 | 6" Core |
| S42C28L8 | 6" Core |
| S42C29L8 | 6" Core |
| S43C33L8 | 6" Core |
| S43C34L8 | 6" Core |
| S43C35L8 | 6" Core |
| S44C27L8 | 6" Core |
| S44C28L8 | 6" Core |
| S44C29L8 | 6" Core |
| S45C33L8 | 6" Core |
| S45C34L8 | 6" Core |
| S45C35L8 | 6" Core |
| S46C27L8 | 6" Core |
| S46C28L8 | 6" Core |
| S46C29L8 | 6" Core |

# LABORATORY MATERIAL TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Oklahoma SPS-10 project.  The previous section ended with lists of samples to be shipped to each of the central lab testing contractor laboratory as well as Material Reference Library.  In this section, the tests to be performed on each sample are listed.

Table 15 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Tables 20 and 21 provide new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 22 through 26 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

## Testing Plans

Table 15. SPS-10 laboratory testing plans

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |
| --- | --- | --- | --- | --- | --- |
| A. | EXPERIMENTAL AC |  |  |  |  |
|  | Core Examination and thickness | AC01 | P01 | 42 | RSC |
|  | Bulk Specific Gravity | AC02 | P02 | 18 | CLTC |
|  | Asphalt Extraction | AC04 | P04 | 24 | CLTC |
|  | Dynamic Modulus | AC08 | P74 | 6 | CLTC |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 6 | CLTC |
|  | Bending beam rheometer | AE08 | P28 | 6 | CLTC |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 6 | CLTC |

* SPS-10 Sampling and Testing guide suggests UG03 which does not exist in LTPP IMS guide.

Table 16. Original and combined specimen descriptions

1 Sample No.:  After combination, the third character is changed to “X,” and the fourth character is assigned numerically.  The other five characters follow the original format.

Specimen ID:  After combination, “L” is changed to “M.”

| Description Type | Status |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Original |  |  |  | Combined1 |
| Sample No. | CA01201 | CA02201 | CA03201 | CA04201 | CAX1201 |
| Specimen ID | S41C29L8 | S41C30L8 | S41C31L8 | S41C32L8 | S41C29M8 |
| Sample No. | CA01202 | CA02202 | CA03202 | CA04202 | CAX1202 |
| Specimen ID | S42C23L8 | S42C24L8 | S42C25L8 | S42C26L8 | S42C23M8 |
| Sample No. | CA01203 | CA02203 | CA03203 | CA04203 | CAX1203 |
| Specimen ID | S43C29L8 | S43C30L8 | S43C31L8 | S43C32L8 | S43C29M8 |
| Sample No. | CA01261 | CA02261 | CA03261 | CA04261 | CAX1261 |
| Specimen ID | S44C23L8 | S44C24L8 | S44C25L8 | S44C26L8 | S44C23M8 |
| Sample No. | CA01262 | CA02262 | CA03262 | CA04262 | CAX1262 |
| Specimen ID | S45C29L8 | S45C30L8 | S45C31L8 | S45C32L8 | S45C29M8 |
| Sample No. | CA01263 | CA02263 | CA03263 | CA04263 | CAX1263 |
| Specimen ID | S46C23L8 | S46C24L8 | S46C25L8 | S46C26L8 | S46C23M8 |

Table 17. Original and modified specimen descriptions

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | CAX1201 | CAE1201 |
|  | Specimen ID | S41C29M8 | S41C29A8 |
|  | Sample No. | CAX1202 | CAE1202 |
|  | Specimen ID | S42C23M8 | S42C23A8 |
|  | Sample No. | CAX1203 | CAE1203 |
|  | Specimen ID | S43C29M8 | S43C29A8 |
|  | Sample No. | CAX1261 | CAE1261 |
|  | Specimen ID | S44C23M8 | S44C23A8 |
|  | Sample No. | CAX1262 | CAE1262 |
|  | Specimen ID | S45C29M8 | S45C29A8 |
|  | Sample No. | CAX1263 | CAE1263 |
|  | Specimen ID | S46C23M8 | S46C30A8 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

## Tracking Tables

Table 18. Tracking table of experimental asphalt concrete in the central lab testing contractor laboratory

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |
| S41C29L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S41C30L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S41C31L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S42C23L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S42C24L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S42C25L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S43C29L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S43C30L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S43C31L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S44C23L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S44C24L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S44C25L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S45C29L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S45C30L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S45C31L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S46C23L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S46C24L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S46C25L8 | AC01/P01 | P02/AC02 | P74/AC08 | Yes | C |
| S41C32L8 | AC01/P01 |  |  | Yes | C |
| S42C26L8 | AC01/P01 |  |  | Yes | C |
| S43C32L8 | AC01/P01 |  |  | Yes | C |
| S44C26L8 | AC01/P01 |  |  | Yes | C |
| S45C32L8 | AC01/P01 |  |  | Yes | C |
| S46C26L8 | AC01/P01 |  |  | Yes | C |
| S41C32M8 | P04/AC04 |  |  | No | E |
| S42C26M8 | P04/AC04 |  |  | No | E |
| S43C32M8 | P04/AC04 |  |  | No | E |
| S44C26M8 | P04/AC04 |  |  | No | E |
| S45C32M8 | P04/AC04 |  |  | No | E |
| S46C26M8 | P04/AC04 |  |  | No | E |
| S41C29A8 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |
| S42C23A8 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |
| S43C29A8 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |
| S44C23A8 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |
| S45C29A8 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |
| S46C23A8 | P27/AE07 | P28/AE08 | P73/AE10 | No | D |

1 Next Process
	D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV