OREGON SPS-10 PROJECT

(41AA00)

# MATERIALS SAMPLING AND TESTING PLAN

Contents

GENERAL LAYOUT INFORMATION	2

MATERIALS SAMPLING AND FIELD TESTING	5

LABORATORY MATERIAL TESTING	28

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Oregon SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  Table 2 indicates transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Additionally, Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION

| Section Number | SHRP ID | Description |
| --- | --- | --- |
| AA01 | 41AA01 | HMA Control Section - 2” wearing course, 2” base course (all PG 64-28) |
| AA02 | 41AA02 | WMA – Foaming Process- 2” wearing course, 2” base course (all PG 64-28) |
| AA03 | 41AA03 | WMA – Evotherm - 2” wearing course, 2” base course (all PG 64-28) |
| AA59 | 41AA59 | WMA – Supplemental section 1 with foaming process run at hot mix temperatures- 2” wearing course, 2” base course (all PG 64-28) |
| AA60 | 41AA60 | HMA – Supplemental section 2 with 30% RAP - 2” wearing course, 2” base course (all PG 64-28) |

TABLE 2: TEST SECTION LAYOUT

| Begin STA | End STA | Description | Section ID |
| --- | --- | --- | --- |
| 1117+04 | 1125+70 | Transition | 41AA01 |
| 1125+70 | 1126+70 | Sampling Area |  |
| 1126+70 | 1127+20 | Buffer Area |  |
| 1127+20 | 1132+20 | Monitoring Area |  |
| 1132+20 | 1132+70 | Buffer Area |  |
| 1132+70 | 1133+70 | Sampling Area |  |
| 1133+70 | 1148+35 | Transition |  |
| 1148+35 | 1160+30 | Transition | 41AA02 |
| 1160+30 | 1161+30 | Sampling Area |  |
| 1161+30 | 1161+80 | Buffer Area |  |
| 1161+80 | 1166+80 | Monitoring Area |  |
| 1166+80 | 1167+30 | Buffer Area |  |
| 1167+30 | 1168+30 | Sampling Area |  |
| 1168+30 | 1182+25 | Transition |  |
| 1182+25 | 1192+30 | Transition | 41AA03 |
| 1192+30 | 1193+30 | Sampling Area |  |
| 1193+30 | 1193+80 | Buffer Area |  |
| 1193+80 | 1198+80 | Monitoring Area |  |
| 1198+80 | 1199+30 | Buffer Area |  |
| 1199+30 | 1200+30 | Sampling Area |  |
| 1200+30 | 1217+00 | Transition |  |
| 1217+00 | 1228+30 | Transition | 41AA59 |
| 1228+30 | 1229+30 | Sampling Area |  |
| 1229+30 | 1229+80 | Buffer Area |  |
| 1229+80 | 1234+80 | Monitoring Area |  |
| 1234+80 | 1235+30 | Buffer Area |  |
| 1235+30 | 1236+30 | Sampling Area |  |
| 1236+30 | 1252+60 | Transition |  |
| 1252+60 | 1262+80 | Transition | 41AA60 |
| 1262+80 | 1263+80 | Sampling Area |  |
| 1263+80 | 1264+30 | Buffer Area |  |
| 1264+30 | 1269+30 | Monitoring Area |  |
| 1269+30 | 1269+80 | Buffer Area |  |
| 1269+80 | 1270+80 | Sampling Area |  |
| 1270+80 | 1285+20 | Transition |  |

1132+20

1132+70

1133+70

1160+30

1161+80

1161+30

1148+35

1127+20

1126+70

1125+70

1114+72

1199+30

1198+80

1193+80

1193+30

1192+30

1182+25

1168+30

1167+30

1166+80

1200+30

Transition zone (1670 ft)

Sampling Area 6 (100 ft)

Buffer Area (50 ft)

41AA03

WMA Chemical Additive section

Buffer Area (50 ft)

Sampling Area 5 (100 ft)

Transition zone (1005 ft)

Transition zone (1395 ft)

Sampling Area 4 (100 ft)

Buffer Area (50 ft)

41AA02

WMA Foaming Process section

Buffer Area (50 ft)

Sampling Area 3 (100 ft)

Transition zone (1205 ft)

Transition zone (1465 ft)

Sampling Area 2 (100 ft)

Buffer Area (50 ft)

41AA01

HMA Control section

Buffer Area (50 ft)

Sampling Area 1 (100 ft)

Transition zone (1098 ft)

800 ft

800 ft

AC Mix 3

AC Mix 2

AC Mix 1

800 ft

AC Mix 5

AC Mix 4

800 ft

800 ft

1217+00

1228+30

1229+30

1234+80

1235+30

1236+30

1252+60

1262+80

1263+80

1264+30

1269+30

1270+80

1269+80

1229+80

Sampling Area 9 (100 ft)

Buffer Area (50 ft)

Buffer Area (50 ft)

Sampling Area 10 (100 ft)

Transition zone (1440 ft)

Transition zone (1020 ft)

41AA59

WMA Supplemental section 1 with foaming process run at hot mix temperatures

Buffer Area (50 ft)

Sampling Area 7 (100 ft)

Sampling Area 8 (100 ft)

Transition zone (1630 ft)

Transition zone (1130 ft)

Buffer Area (50 ft)

41AA60

HMA Supplemental section 2 with 30% RAP

Direction of Traffic (NB)

FIGURE 1: OREGON SPS-10 PROJECT LAYOUT

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at time zero (t0 is at time of construction).  Additionally, there will be three additional rounds of sampling following the time zero construction testing beginning 3-6 months following construction. These samples are not a part of the current plan but will be documented soon.  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 2 through 11 show the locations for the many samples and tests scheduled.  Figures 2 through 6 show the material sampling locations for each section as well as the location of DCP testing and Figures 7 through 11 show density measurement layouts.

Tables 6 through 11 list the samples acquired from each of the five test sections as well as the asphalt plant.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected. Text in italics denotes samples that have already been collected during the July 2015 preconstruction materials sampling.

Finally, Tables 12 through 14 list samples to be shipped to the central lab testing contractor laboratory, the LTPP Materials Reference Library (MRL), and the Turner-Fairbank Highway Research Center, respectively. The Western Regional Support Contractor will be responsible for all labeling and shipping of samples.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Oregon SPS-10, R = “W,” representing Western Region)

- C = Construction event (For Oregon SPS-10, C = 3 for 41AAXX , representing the first constructed SPS-10)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 59

  - B – 60

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C –6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

The layer numbering system was applied for each of the five sections. Based on data provided by the Oregon State DOT coupled with preconstruction coring, the sublayers were considered for each of the five sections and categorized and numbered as outlined in the tables below.

The reported layers and layer numbering for all 41AAXX sections are given in Table 3 below.

TABLE 3: LAYER NUMBERING FOR ALL 41AAXX SECTIONS

| Layer number | Project Layer code | Layer thickness (in) | Material code | Material Description |
| --- | --- | --- | --- | --- |
| 9 | I | 2.0 | 01 | Test section overlay: wearing course |
| 8* | H | 1.5 | 01 | Test section overlay: base course |
| 7 | G | 0.25 | 71 | Chip seal (only in some areas) |
| 6 | F | 2.0 | 02 | AC layer (open) |
| 5 | E | 2.0 | 01 | AC layer (dense) |
| 4 | D | 2.0 | 15 | AC layer (open and stripped) |
| 3 | C | 3.0 | 19 | AC layer (dense) |
| 2 | B | 15.0 | 200 | Volcanic rocky fill |
| 1 | A |  | 54 | Subgrade (black, clayey natural soil) |

(*) The test course will be considered together for core-based materials sampling collectively as Layer 8. However, during construction materials sampling (uncompacted mix samples) will be considered as two levels because mix from both the base course and wearing course.

0-70

3’

3’

C09001

C07001

C01001

A02001

A01001

A03001

3’

3’

Key

12” Core

6” Core

Experimental AC sample only

Location of previously sampled full depth core

0-67

0-68

2’

3’

1’

2’

Shoulder

Section STA:

0-50

0-65

0-54

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-66

Note: The test section begins at STA 0+00

A04001

A05001

C03001

DCP

C14001

C12001

C10001

C08001

C04001

C06001

C02001

C15001

C13001

C11001

C05001

FIGURE 2: OREGON SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 41AA01 AT T0

0-68

0-65

0-67

0-54

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-66

0-70

1’

1’

3’

3’

A02002

A01002

C14002

C13002

C12002

C11002

C10002

C09002

C08002

C07002

C06002

C05002

C04002

C03002

C02002

C01002

Key

12” Core

6” Core

Experimental AC sample only

Location of previously sampled full depth core

C15002

DCP

2’

3’5”

1’

Shoulder

Section STA:

0-50

Note: The test section begins at STA 0+00

C1600202

FIGURE 3: OREGON SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 41AA02 AT T0

0-68

0-67

0-66

0-65

0-70

0-53

0-54

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

Section STA:

A02003

A01003

C08003

C06003

C05003

C04003

C03003

C02003

Key

12” Core

6” Core

Experimental AC sample only

Location of previously sampled full depth core

5’5”

C15003

3’

2’

3'’

2’

Shoulder

0-50

Note: The test section begins at STA 0+00

C17003

C16003

DCP

1’’

C14003

C12003

C10003

C01003

C13003

C11003

C09003

C07003

FIGURE 4: OREGON SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 41AA03 AT T0

0-65

0-68

0-67

0-54

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-66

0-70

1’

3’

3’

A02059

A01059

C13059

C11059

C09059

C08059

C07059

C06059

C04059

C03059

C02059

C01059

C16059

Key

12” Core

6” Core

Experimental AC sample only

Location of previously sampled full depth core

6’4”

C15059

DCP

2’

2’

Shoulder

Section STA:

0-50

Note: The test section begins at STA 0+00

C05059

C14059

C12059

C10059

FIGURE 5: OREGON SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 41AA59 AT T0

0-70

1’

C14060

C13060

C11060

C09060

C07060

C05060

C04060

C03060

C02060

C01060

Key

12” Core

6” Core

Experimental AC sample only

Location of previously sampled full depth core

6’4”

3’

3’

DCP

2’

2’

Shoulder

Section STA:

0-50

0-54

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-66

0-67

0-68

Note: The test section begins at STA 0+00

3’

3’

A01060

A05060

A04060

A03060

A02060

C15060

C08060

C12060

C10060

C06060

FIGURE 6: OREGON SPS-10 MATERIALS SAMPLING LAYOUT FOR SECTION 41AA60 AT T0

Section 41AA01 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03001

T02001

T01001

Traffic

FIGURE 7: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 41AA01 OREGON SPS-10

Section 41AA02 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03002

T02002

T01002

Traffic

FIGURE 8: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 41AA02 OREGON SPS-10

Section 53AA03 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03003

T02003

T01003

Traffic

FIGURE 9: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 41AA03 OREGON SPS-10

Section 41AA59- Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T01059

T02059

T03059

Traffic

FIGURE 10: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 41AA59 OREGON SPS-10

Section 41AA60 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T01060

T02060

T03060

Traffic

FIGURE 11: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 41AA60 OREGON SPS-10

TABLE 4: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
|  | DURING CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 5-gallon buckets uncompacted AC mix | 80 | F01001, F01002, F01003, F02001, F01059, F01060 |
|  | 1-gallon can virgin AC Binder (PG 64-28) | 7 | H01001 |
|  | 5-gallon bucket combined aggregate | 5 | H02001 |
|  | 50 lb bulk sample RAP | 1 | H03001 |
|  | 5-gallon buckets RAP | 5 | H03001 |
|  | 1-gallon chemical additive (Evotherm) | 1 | H01003 |
|  | POST-CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 12" Core | 10 | A01001-A02001, A01002-A02002, A01003-A02003, A01059-A02059, A01060-A02060, |
|  | 6" Core | 70 | C01001-C14001, C01002-C14002, C01003-C14003, C01059-C14059, C01060-C14060 |
| B. | ORIGINAL HMAC |  |  |
|  | 12" Core | 2 | A02003, A01003 |
|  | 6" Core | 6 | C02001, C01002, C01003, C01059, C02059, C01060 |
| C. | ROCKY FILL |  |  |
|  | 150 lb bulk sample | 2 | A01001-A03001, A01003-A03003 |
| D. | SUBGRADE |  |  |
|  | 150 lb bulk sample | 2 | A01001-A02001, A01003-A02003 |
|  | Moisture content jar sample | 2 | A01001-A02001, A01003-A02003 |

TABLE 5: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | PRE-CONSTRUCTION TESTING |  |  |
| A. | ORIGINAL HMAC |  |  |
|  | Elevation Survey | 5 | All Sections |
|  | POST-CONSTRUCTION TESTING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Elevation Survey | 5 | All Sections |
|  | In situ density measurement | 15 | T01001-T03001, T01002-T03002, T01003-T03003, T01059 -T03059, T01060-T03060 |
|  | Core Examination and Thickness (P01/AC01) | 80 | A01001-A02001, A01002-A02002, A01003-A02003, A01059-A02059, A01060-A02060, C01001-C14001, C01002-C14002, C01003-C14003, C01059-C14059, C01060-C14060 |
| B. | ORIGINAL HMAC |  |  |
|  | Core Examination and Thickness | 8 | A02005, A01002, C02001, C01002, C01003, C01059, C02059, C01060 |
| C. | VOLCANIC ROCKY FILL |  |  |
|  | DCP | 5 | A01001, A01002, A01003, A01059, A01060 |
| D. | SUBGRADE |  |  |
|  | DCP | 5 | A01001, A01002, A01003, A01059, A01060 |

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 41AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01001 | 8 | BA01001 | W31A01L08 | 12" Core |
| A02001 | 8 | BA02001 | W31A02L08 | 12" Core |
| A03001 | 7 | BA04001 | W31A03L07 | 12" Core |
|  | 6 | BA05001 | W31A03L06 | 12" Core |
|  | 5 | BA06001 | W31A03L05 | 12" Core |
|  | 4 | BA07001 | W31A03L04 | 12" Core |
| A03001, A04001, A05001 | 1 | BS01001 | W31A03L01 | 150 lb Bulk Sample |
|  | 1 | MS01001 | W31A03W01 | Moisture content jar sample |
|  | 2 | BS01001 | W31A03L02 | 150 lb Bulk Sample |
| C01001 | 8 | CA01001 | W31C01L08 | 6" Core |
| C02001 | 8 | CA02001 | W31C02L08 | 6" Core |
| C03001 | 8 | CA03001 | W31C03L08 | 6" Core |
| C04001 | 8 | CA04001 | W31C04L08 | 6" Core |
| C05001 | 8 | CA05001 | W31C05L08 | 6" Core |
| C06001 | 8 | CA06001 | W31C06L08 | 6" Core |
| C07001 | 8 | CA07001 | W31C07L08 | 6" Core |
| C08001 | 8 | CA08001 | W31C08L08 | 6" Core |
| C09001 | 8 | CA09001 | W31C09L08 | 6" Core |
| C10001 | 8 | CA10001 | W31C10L08 | 6" Core |
| C11001 | 8 | CA11001 | W31C11L08 | 6" Core |
| C12001 | 8 | CA12001 | W31C12L08 | 6" Core |
| C13001 | 8 | CA13001 | W31C13L08 | 6" Core |
| C14001 | 8 | CA14001 | W31C14L08 | 6" Core |
| C15001 | 7 | CA16001 | W31C15L07 | 6" Core |
|  | 6 | CA17001 | W31C15L06 | 6" Core |
|  | 5 | CA18001 | W31C15L05 | 6" Core |
|  | 4 | CA19001 | W31C15L04 | 6" Core |
| F01001 | 8 | BA08001 | W31F01L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 22, 2015) |
| F01001 | 8 | BA08001 | W31F02L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 22, 2015) |
| F01001 | 8 | BA08001 | W31F03L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 22, 2015) |
| F01001 | 8 | BA08001 | W31F04L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 22, 2015) |
| F01001 | 8 | BA08001 | W31F05L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 22, 2015) |
| F01001 | 8 | BA08001 | W31F06L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 22, 2015) |
| F01001 | 8 | BA08001 | W31F07L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 22, 2015) |
| F01001 | 8 | BA08001 | W31F08L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 22, 2015) |
| F01001 | 8 | BA09001 | W31F01L07 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01001 | 8 | BA09001 | W31F02L07 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01001 | 8 | BA09001 | W31F03L07 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01001 | 8 | BA09001 | W31F04L07 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01001 | 8 | BA09001 | W31F05L07 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01001 | 8 | BA09001 | W31F06L07 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01001 | 8 | BA09001 | W31F07L07 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01001 | 8 | BA09001 | W31F08L07 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |

Note: Specimens in italics have previously been collected

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 41AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01001 | 8 | BA01002 | W32A01L07 | 12" Core |
| A02001 | 7 | BA02002 | W32A02L07 | 12" Core |
| C01002 | 7 | CA01002 | W32C01L07 | 6" Core |
| C02002 | 7 | CA02002 | W32C02L07 | 6" Core |
| C03002 | 7 | CA03002 | W32C03L07 | 6" Core |
| C04002 | 7 | CA04002 | W32C04L07 | 6" Core |
| C05002 | 7 | CA05002 | W32C05L07 | 6" Core |
| C06002 | 7 | CA06002 | W32C06L07 | 6" Core |
| C07002 | 7 | CA07002 | W32C07L07 | 6" Core |
| C08002 | 7 | CA08002 | W32C08L07 | 6" Core |
| C09002 | 7 | CA09002 | W32C09L07 | 6" Core |
| C10002 | 7 | CA10002 | W32C10L07 | 6" Core |
| C11002 | 7 | CA11002 | W32C11L07 | 6" Core |
| C12002 | 7 | CA12002 | W32C12L07 | 6" Core |
| C13002 | 7 | CA13002 | W32C13L07 | 6" Core |
| C14002 | 7 | CA14002 | W32C14L07 | 6" Core |
| C15002 | 6 | CA17002 | W32C15L06 | 6" Core |
|  | 5 | CA19002 | W32C15L05 | 6" Core |
|  | 4 | CA21002 | W32C15L04 | 6" Core |
|  | 3 | CA23002 | W32C15L03 | 6" Core |
| C16002 | 6 | CA18002 | W32C16L06 | 6" Core |
|  | 5 | CA20002 | W32C16L05 | 6" Core |
|  | 4 | CA22002 | W32C16L04 | 6" Core |
|  | 3 | CA24002 | W32C16L03 | 6" Core |
| F01002 | 8 | BA05002 | W32F01L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01002 | 8 | BA05002 | W32F02L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01002 | 8 | BA05002 | W32F03L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01002 | 8 | BA05002 | W32F04L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01002 | 8 | BA05002 | W32F05L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01002 | 8 | BA05002 | W32F06L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01002 | 8 | BA05002 | W32F07L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01002 | 8 | BA05002 | W32F08L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01002 | 8 | BA06002 | W32F01L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01002 | 8 | BA06002 | W32F02L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01002 | 8 | BA06002 | W32F03L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01002 | 8 | BA06002 | W32F04L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01002 | 8 | BA06002 | W32F05L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01002 | 8 | BA06002 | W32F06L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01002 | 8 | BA06002 | W32F07L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01002 | 8 | BA06002 | W32F01L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |

Note: Specimens in italics have previously been collected

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 41AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01003 | 8 | BA01003 | W33A01L08 | 12" Core |
| A02003 | 8 | BA02003 | W33A02L08 | 12" Core |
| C01003 | 8 | CA01003 | W33C01L08 | 6" Core |
| C02003 | 8 | CA02003 | W33C02L07 | 6" Core |
| C03003 | 8 | CA03003 | W33C03L07 | 6" Core |
| C04003 | 8 | CA04003 | W33C04L07 | 6" Core |
| C05003 | 8 | CA05003 | W33C05L07 | 6" Core |
| C06003 | 8 | CA06003 | W33C06L07 | 6" Core |
| C07003 | 8 | CA07003 | W33C07L07 | 6" Core |
| C08003 | 8 | CA08003 | W33C08L07 | 6" Core |
| C09003 | 8 | CA09003 | W33C09L07 | 6" Core |
| C10003 | 8 | CA10003 | W33C10L07 | 6" Core |
| C11003 | 8 | CA11003 | W33C11L07 | 6" Core |
| C12003 | 8 | CA12003 | W33C12L07 | 6" Core |
| C13003 | 8 | CA13003 | W33C13L07 | 6" Core |
| C14003 | 8 | CA14003 | W33C14L07 | 6" Core |
| C15003 | 6 | CA18003 | W33C15L06 | 6" Core |
|  | 5 | CA21003 | W33C15L05 | 6" Core |
|  | 4 | CA24003 | W33C15L04 | 6" Core |
|  | 3 | CA27003 | W33C15L03 | 6" Core |
| C16003 | 6 | CA19003 | W33C16L06 | 6" Core |
|  | 5 | CA22003 | W33C16L05 | 6" Core |
|  | 4 | CA25003 | W33C16L04 | 6" Core |
|  | 3 | CA28003 | W33C16L03 | 6" Core |
| C17003 | 6 | CA20003 | W33C17L06 | 6" Core |
|  | 5 | CA23003 | W33C17L05 | 6" Core |
|  | 4 | CA26003 | W33C17L04 | 6" Core |
|  | 3 | CA29003 | W33C17L03 | 6" Core |
| F01003 | 8 | BA03003 | W33F01L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01003 | 8 | BA03003 | W33F02L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01003 | 8 | BA03003 | W33F03L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01003 | 8 | BA03003 | W33F04L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01003 | 8 | BA03003 | W33F05L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01003 | 8 | BA03003 | W33F06L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01003 | 8 | BA03003 | W33F07L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01003 | 8 | BA03003 | W33F08L08 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01003 | 8 | BA04003 | W33F01L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01003 | 8 | BA04003 | W33F02L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01003 | 8 | BA04003 | W33F03L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01003 | 8 | BA04003 | W33F04L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01003 | 8 | BA04003 | W33F05L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01003 | 8 | BA04003 | W33F06L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01003 | 8 | BA04003 | W33F07L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |
| F01003 | 8 | BA04003 | W33F08L09 | 1 5-gallon bucket uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |

Note: Specimens in italics have previously been collected

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 41AA59

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01059 | 8 | BA01059 | W3AA01L08 | 12" Core |
| A02059 | 8 | BA02059 | W3AA02L08 | 12" Core |
| C01059 | 8 | CA01059 | W3AC01L08 | 6" Core |
| C02059 | 8 | CA02059 | W3AC02L08 | 6" Core |
| C03059 | 8 | CA03059 | W3AC03L08 | 6" Core |
| C04059 | 8 | CA04059 | W3AC04L08 | 6" Core |
| C05059 | 8 | CA05059 | W3AC05L08 | 6" Core |
| C06059 | 8 | CA06059 | W3AC06L08 | 6" Core |
| C07059 | 8 | CA07059 | W3AC07L08 | 6" Core |
| C08059 | 8 | CA08059 | W3AC08L08 | 6" Core |
| C09059 | 8 | CA09059 | W3AC09L08 | 6" Core |
| C10059 | 8 | CA10059 | W3AC10L08 | 6" Core |
| C11059 | 8 | CA11059 | W3AC11L08 | 6" Core |
| C12059 | 8 | CA12059 | W3AC12L08 | 6" Core |
| C13059 | 8 | CA13059 | W3AC13L08 | 6" Core |
| C14059 | 8 | CA14059 | W3AC14L08 | 6" Core |
| C15059 | 7 | CA15059 | W3AC15L07 | 6" Core |
|  | 6 | CA17059 | W3AC15L06 | 6" Core |
|  | 5 | CA19059 | W3AC15L05 | 6" Core |
|  | 4 | CA21059 | W3AC15L04 | 6" Core |
|  | 3 | CA23059 | W3AC15L03 | 6" Core |
| C16059 | 7 | CA16059 | W3AC16L07 | 6" Core |
|  | 6 | CA18059 | W3AC16L06 | 6" Core |
|  | 5 | CA20059 | W3AC16L05 | 6" Core |
|  | 4 | CA22059 | W3AC16L04 | 6" Core |
|  | 3 | CA24059 | W3AC16L03 | 6" Core |
| F01059 | 8 | BA03059 | W3AF01-F08L08 | 8 5-gallon buckets uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01059 | 8 | BA04059 | W3AF01-F08L09 | 8 5-gallon buckets uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |

Note: Specimens in italics have previously been collected

TABLE 10: SAMPLES ACQUIRED FROM TEST SECTION 41AA60

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01060 | 8 | BA01060 | W3BA01L08 | 12" Core |
| A02060 | 8 | BA02060 | W3BA02L08 | 12" Core |
| A03060 | 7 | BA03060 | W3BA03L07 | 12" Core |
|  | 6 | BA04060 | W3BA03L06 | 12" Core |
|  | 5 | BA05060 | W3BA03L05 | 12" Core |
|  | 4 | BA06060 | W3BA03L04 | 12" Core |
|  | 3 | BA07060 | W3BA03L03 | 12" Core |
| A03060, A04060, A05060 | 1 | BS01060 | W3BA03L01 | 150 lb Bulk Sample |
|  | 1 | MS01060 | W3BA03W01 | Moisture content jar sample |
|  | 2 | BS01060 | W3BA03L02 | 150 lb Bulk Sample |
| C01060 | 8 | CA01060 | W3BC01L08 | 6" Core |
| C02060 | 8 | CA02060 | W3BC02L08 | 6" Core |
| C03060 | 8 | CA03060 | W3BC03L08 | 6" Core |
| C04060 | 8 | CA04060 | W3BC04L08 | 6" Core |
| C05060 | 8 | CA05060 | W3BC05L08 | 6" Core |
| C06060 | 8 | CA06060 | W3BC06L08 | 6" Core |
| C07060 | 8 | CA07060 | W3BC07L08 | 6" Core |
| C08060 | 8 | CA08060 | W3BC08L08 | 6" Core |
| C09060 | 8 | CA09060 | W3BC09L08 | 6" Core |
| C10060 | 8 | CA10060 | W3BC10L08 | 6" Core |
| C11060 | 8 | CA11060 | W3BC11L08 | 6" Core |
| C12060 | 8 | CA12060 | W3BC12L08 | 6" Core |
| C13060 | 8 | CA13060 | W3BC13L08 | 6" Core |
| C14060 | 8 | CA14060 | W3BC14L08 | 6" Core |
| C15060 | 7 | CA15060 | W3BC15L07 | 6" Core |
|  | 6 | CA15060 | W3BC15L06 | 6" Core |
|  | 5 | CA15060 | W3BC15L05 | 6" Core |
|  | 4 | CA15060 | W3BC15L04 | 6" Core |
|  | 3 | CA15060 | W3BC15L03 | 6" Core |
| F01060 | 8 | BA08060 | W3BF01-F08L08 | 8 5-gallon buckets uncompacted AC mix (1 of 2 lifts collected Sep 23, 2015) |
| F01060 | 8 | BA09060 | W3BF01-F08L09 | 8 5-gallon buckets uncompacted AC mix (1 of 2 lifts collected Sep 24, 2015) |

Note: Specimens in italics have previously been collected

TABLE 11: SAMPLES ACQUIRED FROM PLANT

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| H01001 | 8 | BC01001 | W31H01L08 | 1 1-gallon can virgin AC binder (PG 64-28) |
| H01001 | 8 | BC02001 | W31H02L08 | 1 1-gallon can virgin AC binder (PG 64-28) |
| H01001 | 8 | BC03001 | W31H03L08 | 5 1-gallon cans virgin AC binder (PG 64-28) |
| H02001 | 8 | BU01001 | W31H04L08 | 5 5-gallon buckets combined aggregate |
| H03001 | 8 | BR01001 | W31H05L08 | 50 lb Bulk Sample RAP |
| H03001 | 8 | BR02001 | W31H06L08 | 5 5-gallon buckets RAP |
| H01003 | 8 | BW01003 | W33H01L08 | 1 gallon chemical additive (Evotherm) in manufacturer prescribed containers, with MSDS |

TABLE 12: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| W31A01L08 | 12” core |
| W31A02L08 | 12” core |
| W31C01L08 | 6” core |
| W31C02L08 | 6” core |
| W31C03L08 | 6” core |
| W31C04L08 | 6” core |
| W31C05L08 | 6” core |
| W31C06L08 | 6” core |
| W31C07L08 | 6” core |
| W31C08L08 | 6” core |
| W31C09L08 | 6” core |
| W31C10L08 | 6” core |
| W32A01L08 | 12” core |
| W32A02L08 | 12” core |
| W32C01L08 | 6” core |
| W32C02L08 | 6” core |
| W32C03L08 | 6” core |
| W32C04L08 | 6” core |
| W32C05L08 | 6” core |
| W32C06L08 | 6” core |
| W32C07L08 | 6” core |
| W32C08L08 | 6” core |
| W32C09L08 | 6” core |
| W32C10L08 | 6” core |
| W33A01L08 | 12” core |
| W33A02L08 | 12” core |
| W33C01L08 | 6” core |
| W33C02L08 | 6” core |
| W33C03L08 | 6” core |
| W33C04L08 | 6” core |
| W33C05L08 | 6” core |
| W33C06L08 | 6” core |
| W33C07L08 | 6” core |
| W33C08L08 | 6” core |

TABLE 12: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| W33C09L08 | 6” core |
| W33C10L08 | 6” core |
| W3AA01L08 | 12” core |
| W3AA02L08 | 12” core |
| W3AC01L08 | 6” core |
| W3AC02L08 | 6” core |
| W3AC03L08 | 6” core |
| W3AC04L08 | 6” core |
| W3AC05L08 | 6” core |
| W3AC06L08 | 6” core |
| W3AC07L08 | 6” core |
| W3AC08L08 | 6” core |
| W3AC09L08 | 6” core |
| W3AC10L08 | 6” core |
| W3BA01L08 | 12” core |
| W3BA02L08 | 12” core |
| W3BC01L08 | 6” core |
| W3BC02L08 | 6” core |
| W3BC03L08 | 6” core |
| W3BC04L08 | 6” core |
| W3BC05L08 | 6” core |
| W3BC06L08 | 6” core |
| W3BC07L08 | 6” core |
| W3BC08L08 | 6” core |
| W3BC09L08 | 6” core |
| W3BC10L08 | 6” core |
| W31H01L08 | 1 1-gallon can of virgin AC binder (PG 64-28) |
| W31H05L08 | 50 lb Bulk Sample RAP |
| ORIGINAL HMAC |  |
| W31A03L07 | 12” core |
| W31A03L06 |  |
| W31A03L05 |  |
| W31A03L04 |  |
| W31A03L03 |  |

TABLE 12: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| W31C15L07 | 6" Core |
| W31C15L06 |  |
| W31C15L05 |  |
| W31C15L04 |  |
| W31C15L03 |  |
| W32C16L07 | 6" Core |
| W32C16L06 |  |
| W32C16L05 |  |
| W32C16L04 |  |
| W32C16L03 |  |
| W33C16L07 | 6" Core |
| W33C16L06 |  |
| W33C16L05 |  |
| W33C16L04 |  |
| W33C16L03 |  |
| W33C17L07 | 6" Core |
| W33C17L06 |  |
| W33C17L05 |  |
| W33C17L04 |  |
| W33C17L03 |  |
| W3AC16L07 | 6" Core |
| W3AC16L06 |  |
| W3AC16L05 |  |
| W3AC16L04 |  |
| W3AC16L03 |  |
| W3BA03L07 | 12" Core |
| W3BA03L06 |  |
| W3BA03L05 |  |
| W3BA03L04 |  |
| W3BA03L03 |  |
| W3BC15L07 | 6" Core |
| W3BC15L06 |  |
| W3BC15L05 |  |
| W3BC15L04 |  |
| W3BC15L03 |  |

TABLE 12: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Rocky, Volcanic Base Fill |  |
| W31A01L02 | 150 lb Bulk Sample |
| W3BA01L02 | 150 lb Bulk Sample |
| Subgrade |  |
| W31A03L01 | 150 lb Bulk Sample |
| W31A03W01 | Moisture content jar sample |
| W3BA03L01 | 150 lb Bulk Sample |
| W3BA03W01 | Moisture content jar sample |

TABLE 13: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| W31C11L08 | 6” core |
| W31C12L08 | 6” core |
| W31C13L08 | 6” core |
| W31C14L08 | 6” core |
| W32C11L08 | 6” core |
| W32C12L08 | 6” core |
| W32C13L08 | 6” core |
| W32C14L08 | 6” core |
| W33C11L08 | 6” core |
| W33C12L08 | 6” core |
| W33C13L08 | 6” core |
| W33C14L08 | 6” core |
| W32C11L08 | 6” core |
| W32C12L08 | 6” core |
| W32C13L08 | 6” core |
| W32C14L08 | 6” core |
| W33C11L08 | 6” core |
| W33C12L08 | 6” core |
| W33C13L08 | 6” core |
| W33C14L08 | 6” core |
| W3AC11L08 | 6” core |
| W3AC12L08 | 6” core |
| W3AC13L08 | 6” core |

TABLE 13: SAMPLES TO BE SHIPPED TO THE LTPP MRL (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| W3AC14L08 | 6" Core |
| W3BC11L08 | 6" Core |
| W3BC12L08 | 6" Core |
| W3BC13L08 | 6" Core |
| W3BC14L08 | 6" Core |
| W31H03L08 | 5 1-gallon cans virgin AC binder (PG 64-28) |
| W31H04L08 | 5 5-gallon buckets combined aggregate |
| W31H06L08 | 5 5-gallon buckets RAP |
| W33H01L08 | 1 gallon chemical additive (Evotherm) in manufacturer prescribed containers, with MSDS |
| W31F01L09 | 8 5-gallon buckets uncompacted AC mix |
| W31F01L08 | 8 5-gallon buckets uncompacted AC mix |
| W32F01L09 | 8 5-gallon buckets uncompacted AC mix |
| W32F01L08 | 8 5-gallon buckets uncompacted AC mix |
| W33F01L09 | 8 5-gallon buckets uncompacted AC mix |
| W33F01L08 | 8 5-gallon buckets uncompacted AC mix |
| W3AF01L09 | 8 5-gallon buckets uncompacted AC mix |
| W3AF01L08 | 8 5-gallon buckets uncompacted AC mix |
| W3BF01L09 | 8 5-gallon buckets uncompacted AC mix |
| W3BF01L08 | 8 5-gallon buckets uncompacted AC mix |

TABLE 14: SAMPLES TO BE SHIPPED TO THE TURNER FAIRBANKS RESEARCH CENTER

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC Layer |  |
| W31H02L08 | 1 1-gallon can virgin AC binder (PG 64-28) |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Oregon SPS-10 project.  The previous section ended with lists of samples to be shipped to each of the two laboratories, the central lab testing contractor laboratory and the Turner-Fairbank Highway Research center.  In this section, the tests to be performed on each sample are listed.

Table 21 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Table 22 provides new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 23 through 29 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 15: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 60 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 12 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 6 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 6 | X |  |
|  | Hamburg Wheel Track | AC09 | P75 | 12 | X |  |
|  | Fenix Fracture Energy | AC10 | P79 | 18 | X |  |
|  | Specific Gravity at 60 ° F | AE03 | P23 | 8 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 18 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 8 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 8 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 6 | X |  |
|  | PPA and Motor Oil Test | AE11 | P76 | 1 |  | X |
| B. | ORIGINAL HMAC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 10 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 2 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 2 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 2 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 2 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 2 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 2 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 2 | X |  |

TABLE 15: SPS-10 LABORATORY TESTING PLANS (Continued)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| C. | ROCKY VOLCANIC FILL |  |  |  |  |  |
|  | Washed Sieve Analysis | UG02 | P41 | 2 | X |  |
|  | Standard Proctor | UG05 | P44 | 2 | X |  |
|  | Atterberg Limits | UG04 | P43 | 2 | X |  |
|  | Resilient Modulus | UG07 | P46 | 2 | X |  |
|  | Classification and Description | UG08 | P47 | 2 | X |  |
| D. | SUBGRADE |  |  |  |  |  |
|  | Sieve Analysis | SS01 | P51 | 2 | X |  |
|  | Atterberg Limits | SS03 | P43 | 2 | X |  |
|  | Classification and Description | SS04 | P52 | 2 | X |  |
|  | Standard Proctor | SS05 | P55 | 2 | X |  |
|  | Resilient Modulus | SS07 | P46 | 2 | X |  |
|  | Natural Moisture Content | SS09 | P49 | 2 | X |  |

TABLE 16: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BA01001 | BAE1001 |
|  | Specimen ID | W31A01L09 | W31A01A09 |
|  | Sample No. | BA03001 | BAE3001 |
|  | Specimen ID | W31A01L08 | W31A01A08 |
|  | Sample No. | BA05001 | BAE5001 |
|  | Specimen ID | W31A01L07 | W31A01A07 |
|  | Sample No. | BA06001 | BAE6001 |
|  | Specimen ID | W31A01L06 | W31A01A06 |
|  | Sample No. | BA07001 | BAE7001 |
|  | Specimen ID | W31A01L05 | W31A01A05 |
|  | Sample No. | BA08001 | BAE8001 |
|  | Specimen ID | W31A01L04 | W31A01A04 |
|  | Sample No. | BA09001 | BAE9001 |
|  | Specimen ID | W31A01L03 | W31A01A03 |
|  | Sample No. | BA01060 | BAE1060 |
|  | Specimen ID | W3BA01L09 | W3BA01A09 |
|  | Sample No. | BA03060 | BAE3060 |
|  | Specimen ID | W3BA01L08 | W3BA01A08 |
|  | Sample No. | BA05060 | BAE5060 |
|  | Specimen ID | W3BA01L07 | W3BA01A07 |
|  | Sample No. | BA06060 | BAE6060 |
|  | Specimen ID | W3BA01L06 | W3BA01A06 |
|  | Sample No. | BA07060 | BAE7060 |
|  | Specimen ID | W3BA01L05 | W3BA01A05 |
|  | Sample No. | BA08060 | BAE8060 |
|  | Specimen ID | W3BA01L04 | W3BA01A04 |
|  | Sample No. | BA09060 | BAE9060 |
|  | Specimen ID | W3BA01L03 | W3BA01A03 |
|  | Sample No. | BA02001 | BAE2001 |
|  | Specimen ID | W31A02L09 | W31A02A09 |
|  | Sample No. | BA04001 | BAE4001 |
|  | Specimen ID | W31A02L08 | W31A02A08 |
|  | Sample No. | BA01002 | BAE1002 |
|  | Specimen ID | W32A01L09 | W32A01A09 |
|  | Sample No. | BA03002 | BAE3002 |
|  | Specimen ID | W32A01L08 | W32A01A08 |
|  | Sample No. | BA02002 | BAE2002 |

TABLE 16: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS (Continued)

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Process |
| Extraction (continued) | Specimen ID | W32A02L09 | W32A02A09 |
|  | Sample No. | BA04002 | BAE4002 |
|  | Specimen ID | W32A02L08 | W32A02A08 |
|  | Sample No. | BA01003 | BAE1003 |
|  | Specimen ID | W33A01L09 | W33A01A09 |
|  | Sample No. | BA03003 | BAE3003 |
|  | Specimen ID | W33A01L08 | W33A01A08 |
|  | Sample No. | BA02003 | BAE2003 |
|  | Specimen ID | W33A02L09 | W33A02A09 |
|  | Sample No. | BA04003 | BAE4003 |
|  | Specimen ID | W33A02L08 | W33A02A08 |
|  | Sample No. | BA01059 | BAE1059 |
|  | Specimen ID | W3AA01L09 | W3AA01A09 |
|  | Sample No. | BA03059 | BAE3059 |
|  | Specimen ID | W3AA01L08 | W3AA01A08 |
|  | Sample No. | BA02059 | BAE2059 |
|  | Specimen ID | W3AA02L09 | W3AA02A09 |
|  | Sample No. | BA04059 | BAE4059 |
|  | Specimen ID | W3AA02L08 | W3AA02A08 |
|  | Sample No. | BA02060 | BAE2060 |
|  | Specimen ID | W3BA02L09 | W3BA02A09 |
|  | Sample No. | BA04060 | BAE4060 |
|  | Specimen ID | W3BA02L08 | W3BA02A08 |
|  | Sample No. | BR01001 | BRE1001 |
|  | Specimen ID | W31H05L09 | W31H05A09 |
| PAV | Sample No. | BAE2001 | BAP2001 |
|  | Specimen ID | W31A02A09 | W31A02B09 |
|  | Sample No. | BAE4001 | BAP4001 |
|  | Specimen ID | W31A02A08 | W31A02B08 |
|  | Sample No. | BAE1002 | BAP1002 |
|  | Specimen ID | W32A01A09 | W32A01B09 |
|  | Sample No. | BAE3002 | BAP3002 |
|  | Specimen ID | W32A01A08 | W32A01B08 |
|  | Sample No. | BAE2002 | BAP2002 |
|  | Specimen ID | W32A02A09 | W32A02B09 |
|  | Sample No. | BAE4002 | BAP4002 |
|  | Specimen ID | W32A02A08 | W32A02B08 |

TABLE 16: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS (Continued)

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Process |
| PAV (Continued) | Sample No. | BAE1003 | BAP1003 |
|  | Specimen ID | W33A01A09 | W33A01B09 |
|  | Sample No. | BAE3003 | BAP3003 |
|  | Specimen ID | W33A01A08 | W33A01B08 |
|  | Sample No. | BAE2003 | BAP2003 |
|  | Specimen ID | W33A02A09 | W33A02B09 |
|  | Sample No. | BAE4003 | BAP4003 |
|  | Specimen ID | W33A02A08 | W33A02B08 |
|  | Sample No. | BAE1059 | BAP1059 |
|  | Specimen ID | W3AA01A09 | W3AA01B09 |
|  | Sample No. | BAE3059 | BAP3059 |
|  | Specimen ID | W3AA01A08 | W3AA01B08 |
|  | Sample No. | BAE2059 | BAP2059 |
|  | Specimen ID | W3AA02A09 | W3AA02B09 |
|  | Sample No. | BAE4059 | BAP4059 |
|  | Specimen ID | W3AA02A08 | W3AA02B08 |
|  | Sample No. | BAE2060 | BAP2060 |
|  | Specimen ID | W3BA02A09 | W3BA02B09 |
|  | Sample No. | BAE4060 | BAP4060 |
|  | Specimen ID | W3BA02A08 | W3BA02B08 |
| RTFO | Sample No. | BC01001 | BCR1001 |
|  | Specimen ID | W31H01L09 | W31H01M09 |
| RTFO + PAV | Sample No. | BC01001 | BCZ1001 |
|  | Specimen ID | W31H01L09 | W31H01M09 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

Tables 17-23 below utilize the following codes to dictate the ‘next process’ undergone by each specimen.

D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W31A01L09 | P03/AC03 |  |  |  |  | Yes | C |
| W31A02L09 | P03/AC03 |  |  |  |  | Yes | C |
| W31A01L08 | P03/AC03 |  |  |  |  | Yes | C |
| W31A02L08 | P03/AC03 |  |  |  |  | Yes | C |
| W32A01L09 | P03/AC03 |  |  |  |  | Yes | C |
| W32A02L09 | P03/AC03 |  |  |  |  | Yes | C |
| W32A01L08 | P03/AC03 |  |  |  |  | Yes | C |
| W32A02L08 | P03/AC03 |  |  |  |  | Yes | C |
| W33A01L09 | P03/AC03 |  |  |  |  | Yes | C |
| W33A02L09 | P03/AC03 |  |  |  |  | Yes | C |
| W33A01L08 | P03/AC03 |  |  |  |  | Yes | C |
| W33A02L08 | P03/AC03 |  |  |  |  | Yes | C |
| W3AA01L09 | P03/AC03 |  |  |  |  | Yes | C |
| W3AA02L09 | P03/AC03 |  |  |  |  | Yes | C |
| W3AA01L08 | P03/AC03 |  |  |  |  | Yes | C |
| W3AA02L08 | P03/AC03 |  |  |  |  | Yes | C |
| W3BA01L09 | P03/AC03 |  |  |  |  | Yes | C |
| W3BA02L09 | P03/AC03 |  |  |  |  | Yes | C |
| W3BA01L08 | P03/AC03 |  |  |  |  | Yes | C |
| W3BA02L08 | P03/AC03 |  |  |  |  | Yes | C |
| W31A01L09 | P04/AC04 |  |  |  |  | No | E |
| W31A01L08 | P04/AC04 |  |  |  |  | No | E |

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W32A01L09 | P04/AC04 |  |  |  |  | No | E |
| W32A01L08 | P04/AC04 |  |  |  |  | No | E |
| W33A01L09 | P04/AC04 |  |  |  |  | No | E |
| W33A01L08 | P04/AC04 |  |  |  |  |  |  |
| W3AA01L09 | P04/AC04 |  |  |  |  |  |  |
| W3AA01L08 | P04/AC04 |  |  |  |  |  |  |
| W3BA01L09 | P04/AC04 |  |  |  |  |  |  |
| W3BA01L08 | P04/AC04 |  |  |  |  |  |  |
| W31A01A09 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W31A01A08 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W32A01A09 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W32A01A08 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W33A01A09 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W33A01A08 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W3AA01A09 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W3AA01A08 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W3BA01A09 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W3BA01A08 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W31A01B09 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W31A01B08 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W32A01B09 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W32A01B08 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W33A01B09 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W33A01B08 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W31A01B09 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W31A01B08 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W3AA01B09 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W3AA01B08 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W3BA01B09 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W3BA01B08 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W31C01L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W31C01L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W31C02L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W31C02L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W31C03L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W31C03L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W31C04L09 | P02/AC02 |  |  |  |  | Yes | S |
| W31C04L08 | P02/AC02 |  |  |  |  | Yes | S |
| W31C05L09 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W31C05L08 | P02/AC02 | P74/AC08 |  |  |  | No | D |

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W31C06L09 | P02/AC02 |  |  |  |  | Yes | S |
| W31C06L08 | P02/AC02 |  |  |  |  | Yes | S |
| W31C07L09 | P02/AC02 |  |  |  |  | Yes | S |
| W31C07L08 | P02/AC02 |  |  |  |  | Yes | S |
| W31C08L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W31C08L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W31C09L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W31C09L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W31C10L09 | P02/AC02 |  |  |  |  | Yes | S |
| W31C10L08 | P02/AC02 |  |  |  |  | Yes | S |
| W32C01L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W32C01L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W32C02L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W32C02L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W32C03L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W32C03L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W32C04L09 | P02/AC02 |  |  |  |  | Yes | S |
| W32C04L08 | P02/AC02 |  |  |  |  | Yes | S |
| W32C05L09 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W32C05L08 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W32C06L09 | P02/AC02 |  |  |  |  | Yes | S |
| W32C06L08 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W32C07L09 | P02/AC02 |  |  |  |  | Yes | S |
| W32C07L08 | P02/AC02 |  |  |  |  | Yes | S |
| W32C08L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W32C08L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W32C09L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W32C09L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W32C10L09 | P02/AC02 |  |  |  |  | Yes | S |
| W32C10L08 | P02/AC02 |  |  |  |  | Yes | S |
| W33C01L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W33C01L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W33C02L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W33C02L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W33C03L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W33C03L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W33C04L09 | P02/AC02 |  |  |  |  | Yes | S |
| W33C04L08 | P02/AC02 |  |  |  |  | Yes | S |
| W33C05L09 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W33C05L08 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W33C06L09 | P02/AC02 |  |  |  |  | Yes | S |
| W33C06L08 | P02/AC02 |  |  |  |  | Yes | S |
| W33C07L09 | P02/AC02 |  |  |  |  | Yes | S |
| W33C07L08 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W33C08L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W33C08L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W33C09L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W33C09L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W33C10L09 | P02/AC02 |  |  |  |  | Yes | S |
| W33C10L08 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC01L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3AC01L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3AC02L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3AC02L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3AC03L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3AC03L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3AC04L09 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC04L08 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC05L09 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3AC05L08 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3AC06L09 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC06L08 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC07L09 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC07L08 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC08L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W3AC08L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W3AC09L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W3AC09L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W3AC10L09 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC10L08 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC01L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3BC01L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3BC02L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3BC02L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3BC03L09 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3BC03L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W3BC04L09 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC04L08 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC05L09 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3BC05L08 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3BC06L09 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC06L08 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC07L09 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC07L08 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC08L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W3BC08L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W3BC09L09 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W3BC09L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W3BC10L09 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC10L08 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL ASPHALT TANK BINDER IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W31H01L09 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| W31H01L08 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| W31H01M09 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| W31H01M08 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| W31H01A09 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| W31H01A08 | P27/AE07 | P28/AE08 |  |  |  | No | D |

TABLE 19:  TRACKING TABLE OF STOCKPILE RAP IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W31H05L09 | P04/AC04 |  |  |  |  | Yes | E, S |
| W31H05M09 | P23/AE03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 | No | D |

TABLE 20: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W31A01L07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W31A01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W31A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W31A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W31A01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W3BA01L07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W3BA01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W3BA01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W3BA01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W3BA01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W31A01M07 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W31A01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W31A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W31A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W31A01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |

TABLE 20: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W3BA01M07 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W3BA01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W3BA01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W3BA01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W3BA01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W31C01L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W31C02L07 | P02/AC02 |  |  |  |  | Yes | S |
| W31C03L07 | P02/AC02 |  |  |  |  | Yes | S |
| W31C01L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W31C02L06 | P02/AC02 |  |  |  |  | Yes | S |
| W31C03L06 | P02/AC02 |  |  |  |  | Yes | S |
| W31C01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W31C02L05 | P02/AC02 |  |  |  |  | Yes | S |
| W31C03L05 | P02/AC02 |  |  |  |  | Yes | S |
| W31C01L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W31C02L04 | P02/AC02 |  |  |  |  | Yes | S |
| W31C03L04 | P02/AC02 |  |  |  |  | Yes | S |
| W31C01L03 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W31C02L03 | P02/AC02 |  |  |  |  | Yes | S |
| W31C03L03 | P02/AC02 |  |  |  |  | Yes | S |
| W32C01L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W32C02L07 | P02/AC02 |  |  |  |  | Yes | S |
| W32C03L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 20: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W32C01L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W32C02L06 | P02/AC02 |  |  |  |  | Yes | S |
| W32C03L06 | P02/AC02 |  |  |  |  | Yes | S |
| W32C01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W32C02L05 | P02/AC02 |  |  |  |  | Yes | S |
| W32C03L05 | P02/AC02 |  |  |  |  | Yes | S |
| W32C01L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W32C02L04 | P02/AC02 |  |  |  |  | Yes | S |
| W32C03L04 | P02/AC02 |  |  |  |  | Yes | S |
| W32C01L03 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W32C02L03 | P02/AC02 |  |  |  |  | Yes | S |
| W32C03L03 | P02/AC02 |  |  |  |  | Yes | S |
| W33C01L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W33C02L07 | P02/AC02 |  |  |  |  | Yes | S |
| W33C03L07 | P02/AC02 |  |  |  |  | Yes | S |
| W33C01L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W33C02L06 | P02/AC02 |  |  |  |  | Yes | S |
| W33C03L06 | P02/AC02 |  |  |  |  | Yes | S |
| W33C01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W33C02L05 | P02/AC02 |  |  |  |  | Yes | S |
| W33C03L05 | P02/AC02 |  |  |  |  | Yes | S |
| W33C01L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W33C02L04 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 20: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W33C03L04 | P02/AC02 |  |  |  |  | Yes | S |
| W33C01L03 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W33C02L03 | P02/AC02 |  |  |  |  | Yes | S |
| W33C03L03 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC01L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3AC02L07 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC03L07 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC01L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3AC02L06 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC03L06 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3AC02L05 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC03L05 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC01L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3AC02L04 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC03L04 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC01L03 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3AC02L03 | P02/AC02 |  |  |  |  | Yes | S |
| W3AC03L03 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC01L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3BC02L07 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC03L07 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC01L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |

TABLE 20: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W3BC02L06 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC03L06 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3BC02L05 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC03L05 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC01L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3BC02L04 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC03L04 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC01L03 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W3BC02L03 | P02/AC02 |  |  |  |  | Yes | S |
| W3BC03L03 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 21: TRACKING TABLE OF ROCKY VOLCANIC FILL IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W31A03L02 | P41/UG02 | P47/UG08 | P43/UG04 | P44/UG05 | P47/UG07 | Yes | S |
| W3BA03L02 | P41/UG02 | P47/UG08 | P43/UG04 | P44/UG05 | P47/UG07 | Yes | S |

TABLE 22: TRACKING TABLE OF SUBGRADE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W31A03L01 | P51/SS01 | P43/SS03 | P52/SS04 | P55/SS05 | P46/SS07 | Yes1 | S |
| W3BA03L01 | P51/SS01 | P43/SS03 | P52/SS04 | P55/SS05 | P46/SS07 | Yes1 | S |
| W31A03W01 | P49/SS09 |  |  |  |  | No1 | D |
| W3BA03W01 | P49/SS09 |  |  |  |  | No1 | D |

1. The moisture content sample may be disposed after testing.  However, any remaining bulk sample should be stored.

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE OVERLAY IN THE TURNER FAIRBANKS HIGHWAY RESEARCH CENTER

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W31H02L09 | P76/AE11 |  |  |  |  | Yes | S |