TEXAS SPS-10

MATERIALS SAMPLING PLAN

6 MONTHS (t1)

Contents

GENERAL LAYOUT INFORMATION	1

MATERIALS SAMPLING AND FIELD TESTING	4

LABORATORY MATERIAL TESTING	15

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections from the beginning of the initial transition area at station 455+00 to the end of the last section at station 506+50.  Table 2 indicates transition areas between each section as well as the buffer and monitoring areas for each section.  Additionally, Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION

| Section Number | Section ID | Description |
| --- | --- | --- |
| 03 | 48AA03 | Mix with WMA Chemical Additive |
| 01 | 48AA01 | HMA Control Section |
| 02 | 48AA02 | Mix with WMA Foaming Process |

TABLE 2: TEST SECTION LAYOUT

| Begin STA | End STA | Description | Section ID |
| --- | --- | --- | --- |
| 463+50 | 464+50 | Sampling Area | 48AA03 |
| 464+50 | 465+00 | Buffer Area |  |
| 465+00 | 470+00 | Monitoring Area |  |
| 470+00 | 470+50 | Buffer Area |  |
| 470+50 | 471+50 | Sampling Area |  |
| 471+50 | 481+50 | Transition |  |
| 481+50 | 482+50 | Sampling Area | 48AA01 |
| 482+50 | 483+00 | Buffer Area |  |
| 483+00 | 488+00 | Monitoring Area |  |
| 488+00 | 488+50 | Buffer Area |  |
| 488+50 | 489+50 | Sampling Area |  |
| 489+50 | 498+50 | Transition |  |
| 498+50 | 499+50 | Sampling Area | 48AA02 |
| 499+50 | 500+00 | Buffer Area |  |
| 500+00 | 505+00 | Monitoring Area |  |
| 505+00 | 505+50 | Buffer Area |  |
| 505+50 | 506+50 | Sampling Area |  |

Sampling Area 011

Buffer Area (50 ft)

48AA03

WMA Chemical Additive Test Section

Buffer Area (50 ft)

Sampling Area 021

Transition (length variable)

Sampling Area 031

Buffer Area (50 ft)

48AA01

HMA Control Text Section

Buffer Area (50 ft)

Sampling Area 041

Transition (length variable)

Buffer Area (50 ft)

48AA02

WMA Foaming Process Test Section

Buffer Area (50 ft)

Sampling Area 061

Sampling Area 051

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

Traffic

471+50

481+50

463+50

489+50

498+50

506+50

465+00

470+00

483+00

488+00

500+00

505+00

FIGURE 1: TEXAS SPS-10 PROJECT LAYOUT

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the material sampling and testing activities that occur in the field as part of time 0 (t0 is at time of construction).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 2 through 7 show the locations for the many samples and tests scheduled.  Figures 2 through 4 show density measurement layouts, and Figures 5 through 7 show the material sampling locations for each section as well as the location of DCP testing.

Tables 6 through 9 list the samples acquired from each of the three test sections as well as the asphalt plant.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 10 through 12 list samples to be shipped to the central lab testing contractor laboratory, the LTPP Materials Reference Library (MRL), and the Turner Fairbanks Research Center, respectively.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID.   A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Texas SPS-10, R = “S,” representing southern region)

- C = Construction event (For Texas SPS-10, C = 1, representing first constructed SPS-10)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

TABLE 3: PROJECT LAYER NUMBERING

| Layer No. | Description |
| --- | --- |
| 1 | Subgrade |
| 2 | Cement Stabilized Subbase |
| 3 | Unbound Flexible Base |
| 4 | Underseal |
| 5 | Original HMAC |
| 6 | Experimental AC |

TABLE 4: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
| A. | EXPERIMENTAL AC |  |  |
|  | Bulk Sample from Test Pit | 4 | A01102-A02101, A01103-A02103 |
|  | 6" Core | 19 | C15101-C21101, C15102-C20102, C15103-C20103 |
| B. | ORIGINAL HMAC |  |  |
|  | Bulk Sample from Test Pit | 2 | A01102, A01103 |
| C. | FLEXIBLE BASE |  |  |
|  | 150 lb bulk sample | 2 | A01102, A01103 |
| D. | CEMENT STABILIZED SUBBASE |  |  |
|  | 6" CORE | 2 | C15102, C15103 |
| E. | SUBGRADE |  |  |
|  | 150 lb Bulk Sample and Moisture Content Jar | 2 | A01102, A01103 |

TABLE 5: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
| A. | EXPERIMENTAL AC |  |  |
|  | Core Examination and Thickness (P01/AC01) | 23 | A01102-A02101, A01103-A02103, C15101-C21101, C15102-C20102, C15103-C20103 |
| B. | ORIGINAL HMAC |  |  |
|  | Core Examination and Thickness (P01/AC01) | 2 | A01102, A01103 |
| C. | FLEXIBLE BASE |  |  |
|  | DCP | 3 | C15101, C15102, C15103 |
| D. | CEMENT STABILIZED SUBBASE |  |  |
|  | Core Examination and Thickness (P01/AC01) | 2 | C15102, C15103 |
| E. | SUBGRADE |  |  |
|  | DCP | 3 | C15101, C15102, C15103 |

1’

A01103/A02103

1’

1’

1’

5+50

5+70

Section STA:

Section: 48AA03

Description: Mix with WMA Chemical Additive

Sampling Area: 02

Sampling Interval: t1

Shoulder

C16103/C18103/C20103

\

C15103/C17103/C19103

6” Core Experimental AC

6” Core Experimental AC and Stabilized Subbase; DCP

12” x 12” Bulk Experimental AC and Bulk Original AC

Bulk Base and Subgrade

1’

2’

1’

4’

6’

1’

1’

1’

1’

1’

1’

FIGURE 2: SAMPLING AND TESTING PLAN FOR TEST SECTION 48AA03 AT TIME 1
TEXAS SPS-10

5+50

5+70

Section STA:

Section: 48AA01

Description: HMAC Control Section

Sampling Area: 04

Sampling Interval: t1

Shoulder

C16101

C18101

C20101

2’

1’

2’

2’

2’

C15101

C17101

C19101

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

C21101

2’

6” Core Experimental AC

6” Core Experimental AC; DCP

FIGURE 3: SAMPLING AND TESTING PLAN FOR TEST SECTION 48AA01 AT TIME 1
TEXAS SPS-10

1’

A01102/A02102

1’

1’

1’

5+50

5+70

Section STA:

Section: 48AA02

Description: Mix With WMA Foaming Process

Sampling Area: 06

Sampling Interval: t1

Shoulder

C16102/C18102/C20102

\

C15102/C17102/C19102

6” Core Experimental AC

6” Core Experimental AC and Stabilized Subbase; DCP

12” x 12” Bulk Experimental AC and Bulk Original AC

Bulk Base and Subgrade

1’

2’

1’

4’

6’

1’

1’

1’

1’

1’

1’

FIGURE 4: SAMPLING AND TESTING PLAN FOR TEST SECTION 48AA02 AT TIME 1
TEXAS SPS-10

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 48AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01103 | 6 | BA01103 | S13A01L06 | Bulk sample from test pit |
|  | 5 |  | S13A01L05 | Bulk sample from test pit |
|  | 3 | BG01103 | S13A01L03 | 150 lb Bulk Sample |
|  | 1 | BS01103 | S13A01L01 | 150 lb Bulk Sample and Moisture Content Jar |
| A02103 | 6 | BA02103 | S13A02L06 | Bulk sample from test pit |
| C15103 | 6 | CA15103 | S13C15L06 | 6" Core |
|  | 2 | CT01103 | S13C15L02 | 6" Core |
| C16103 | 6 | CA16103 | S13C16L06 | 6" Core |
| C17103 | 6 | CA17103 | S13C17L06 | 6" Core |
| C18103 | 6 | CA18103 | S13C18L06 | 6" Core |
| C19103 | 6 | CA19103 | S13C19L06 | 6" Core |
| C20103 | 6 | CA20103 | S13C20L06 | 6" Core |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 48AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C15101 | 6 | CA15101 | S11C15L06 | 6" Core |
| C16101 | 6 | CA16101 | S11C16L06 | 6" Core |
| C17101 | 6 | CA17101 | S11C17L06 | 6" Core |
| C18101 | 6 | CA18101 | S11C18L06 | 6" Core |
| C19101 | 6 | CA19101 | S11C19L06 | 6" Core |
| C20101 | 6 | CA20101 | S11C20L06 | 6" Core |
| C21101 | 6 | CA21101 | S11C21L06 | 6" Core |

TABLE 8 SAMPLES ACQUIRED FROM TEST SECTION 48AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01102 | 6 | BA01102 | S12A01L06 | Bulk sample from test pit |
|  | 5 |  | S12A01L05 | Bulk sample from test pit |
|  | 3 | BG01102 | S12A01L03 | 150 lb Bulk Sample |
|  | 1 | BS01102 | S12A01L01 | 150 lb Bulk Sample and Moisture Content Jar |
| A02102 | 6 | BA02102 | S12A02L06 | Bulk sample from test pit |
| C15102 | 6 | CA15102 | S12C15L06 | 6" Core |
|  | 2 | CT01102 | S12C15L02 | 6" Core |
| C16102 | 6 | CA16102 | S12C16L06 | 6" Core |
| C17102 | 6 | CA17102 | S12C17L06 | 6" Core |
| C18102 | 6 | CA18102 | S12C18L06 | 6" Core |
| C19102 | 6 | CA19102 | S12C19L06 | 6" Core |
| C20102 | 6 | CA20102 | S12C20L06 | 6" Core |

TABLE 9: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S13A01L06 | Bulk sample from test pit |
| S13A02L06 | Bulk sample from test pit |
| S13C15L06 | 6" Core |
| S13C16L06 | 6" Core |
| S13C17L06 | 6" Core |
| S11C15L06 | 6" Core |
| S11C16L06 | 6" Core |
| S11C17L06 | 6" Core |
| S11C18L06 | 6" Core |
| S12A01L06 | Bulk sample from test pit |
| S12A02L06 | Bulk sample from test pit |
| S12C15L06 | 6" Core |
| S12C16L06 | 6" Core |
| S12C17L06 | 6" Core |
| Original HMAC |  |
| S13A01L05 | Bulk sample from test pit |
| S12A01L05 | Bulk sample from test pit |
| Flexible Base |  |
| S13A01L03 | 150 lb Bulk Sample |
| S12A01L03 | 150 lb Bulk Sample |
| Cement Stabilized Subbase |  |
| S13C15L02 | 6" Core |
| S12C15L02 | 6" Core |
| Subgrade |  |
| S13A01L01 | 150 lb Bulk Sample and Moisture Content Jar |
| S12A01L01 | 150 lb Bulk Sample and Moisture Content Jar |

TABLE 10: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| S13C18L06 | 6" Core |
| S13C19L06 | 6" Core |
| S13C20L06 | 6" Core |
| S11C19L06 | 6" Core |
| S11C20L06 | 6" Core |
| S11C21L06 | 6" Core |
| S12C18L06 | 6" Core |
| S12C19L06 | 6" Core |
| S12C20L06 | 6" Core |

## LABORATORY MATERIAL TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Texas SPS-10 project.  The previous section ended with lists of samples to be shipped to each of the two laboratories, the central lab testing contractor laboratory and the Turner Fairbanks Research center.  In this section, the tests to be performed on each sample are listed.

Table 13 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Tables 14 and 15 provide new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 16 through 21 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 11: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 30 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 6 3 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 4 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 6 | X |  |
|  | Hamburg Wheel Track | AC09 | P75 | 6 | X |  |
|  | Fenix Fracture Energy | AC10 | P79 | 9 | X |  |
|  | Specific Gravity at 60 ° F | AE03 | P23 | 5 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 10 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 5 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 5 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 4 | X |  |
|  | PPA and Motor Oil Test | AE11 | P76 | 1 |  | X |
| B. | ORIGINAL HMAC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 6 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 2 0 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 2 0 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 4 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 2 0 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 2 0 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 2 0 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 2 0 | X |  |

TABLE 11: SPS-10 LABORATORY TESTING PLANS (Continued)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| C. | FLEXIBLE BASE |  |  |  |  |  |
|  | Washed Sieve Analysis | UG02 | P41 | 2 0 | X |  |
|  | Standard Proctor | UG05 | P44 | 2 0 | X |  |
|  | Atterberg Limits | UG04 | P43 | 2 0 | X |  |
|  | Resilient Modulus | UG07 | P46 | 2 0 | X |  |
|  | Classification and Description | UG08 | P47 | 2 0 | X |  |
| D. | CEMENT STABILIZED SUBBASE |  |  |  |  |  |
|  | Identification and Description of Treated Material and Type of Treatment | TB01 | P31 | 2 0 | X |  |
| E. | SUBGRADE |  |  |  |  |  |
|  | Sieve Analysis | SS01 | P51 | 2 0 | X |  |
|  | Atterberg Limits | SS03 | P43 | 2 0 | X |  |
|  | Classification and Description | SS04 | P52 | 2 0 | X |  |
|  | Standard Proctor | SS05 | P55 | 2 0 | X |  |
|  | Resilient Modulus | SS07 | P46 | 2 0 | X |  |
|  | Natural Moisture Content | SS09 | P49 | 2 0 | X |  |

TABLE 12: ORIGINAL AND COMBINED SPECIMEN DESCRIPTIONS

| Description Type | Status |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Original |  |  |  |  |  |  |  | Combined1 |
| Sample No. | BA01001 | BA02001 |  |  |  |  |  |  | BAX1001 |
| Specimen ID | S11A01L06 | S11A02L06 |  |  |  |  |  |  | S11A01M06 |
| Sample No. | BA01002 | BA02002 |  |  |  |  |  |  | BAX1002 |
| Specimen ID | S12A01L06 | S12A02L06 |  |  |  |  |  |  | S12A01M06 |
| Sample No. | BA01003 | BA02003 |  |  |  |  |  |  | BAX1003 |
| Specimen ID | S13A01L06 | S13A02L06 |  |  |  |  |  |  | S13A01M06 |
| Sample No. | CA05001 | CA06001 | CA07001 | CA08001 | CA09001 | CA10001 | CA11001 | CA14001 | CAX1001 |
| Specimen ID | S11C05L06 | S11C06L06 | S11C07L06 | S11C08L06 | S11C09L06 | S11C10L06 | S11C11L06 | S11C14L06 | S11C05M06 |
| Sample No. | CA05002 | CA06002 | CA07002 | CA08002 | CA09002 | CA10002 | CA11002 | CA14002 | CAX1002 |
| Specimen ID | S12C05L06 | S12C06L06 | S12C07L06 | S12C08L06 | S12C09L06 | S12C10L06 | S12C11L06 | S12C14L06 | S12C05M06 |
| Sample No. | CA05003 | CA06003 | CA07003 | CA08003 | CA09003 | CA10003 | CA11003 | CA14003 | CAX1003 |
| Specimen ID | S13C05L06 | S13C06L06 | S13C07L06 | S13C08L06 | S13C09L06 | S13C10L06 | S13C11L06 | S13C14L06 | S13C05M06 |

1. Sample No.:  After combination, the third character is changed to “X,” and the fourth character is assigned numerically.  The other five characters follow the original format.

Specimen ID:  After combination, “L” is changed to “M.”

TABLE 13: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | CAX1001 | CAE1001 |
|  | Specimen ID | S11C05M06 | S11C05A06 |
|  | Sample No. | CAX1002 | CAE1002 |
|  | Specimen ID | S12C05M06 | S12C05A06 |
|  | Sample No. | CAX1003 | CAE1003 |
|  | Specimen ID | S13C05M06 | S13C05A06 |
|  | Sample No. | BA03002 | BAE2002 |
|  | Specimen ID | S12A01L05 | S12A01M05 |
|  | Sample No. | BA03003 | BAE2003 |
|  | Specimen ID | S13A01L05 | S13A01M05 |
|  | Sample No. | BR01001 | BRE1001 |
|  | Specimen ID | S11H05L6 | S11H05M6 |
| PAV | Sample No. | CAE1001 | CAP1001 |
|  | Specimen ID | S11C05A06 | S11C05B06 |
|  | Sample No. | CAE1002 | CAP1002 |
|  | Specimen ID | S12C05A06 | S12C05B06 |
|  | Sample No. | CAE1003 | CAP1003 |
|  | Specimen ID | S13C05A06 | S13C05B06 |
| RTFO | Sample No. | BC01001 | BCR1001 |
|  | Specimen ID | S11H01L6 | S11H01M6 |
| RTFO + PAV | Sample No. | BC01001 | BCZ1001 |
|  | Specimen ID | S11H01L6 | S11H01A6 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 14: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S11C05L06 | P02/AC02 | P79/AC10 |  |  |  | No | C |
| S11C06L06 | P02/AC02 | P79/AC10 |  |  |  | No | C |
| S11C07L06 | P02/AC02 | P79/AC10 |  |  |  | No | C |
| S11C08L06 | P02/AC02 |  |  |  |  | Yes | C |
| S11C09L06 | P02/AC02 | P74/AC08 |  |  |  | No | C |
| S11C10L06 | P02/AC02 |  |  |  |  | Yes | C |
| S11C11L06 | P02/AC02 |  |  |  |  | Yes | C |
| S11C12L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S11C13L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S11C14L06 | P02/AC02 |  |  |  |  | Yes | C |
| S12C05L06 | P02/AC02 | P79/AC10 |  |  |  | No | C |
| S12C06L06 | P02/AC02 | P79/AC10 |  |  |  | No | C |
| S12C07L06 | P02/AC02 | P79/AC10 |  |  |  | No | C |
| S12C08L06 | P02/AC02 |  |  |  |  | Yes | C |
| S12C09L06 | P02/AC02 | P74/AC08 |  |  |  | No | C |
| S12C10L06 | P02/AC02 |  |  |  |  | Yes | C |
| S12C11L06 | P02/AC02 |  |  |  |  | Yes | C |
| S12C12L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S12C13L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S12C14L06 | P02/AC02 |  |  |  |  | Yes | C |

TABLE 14: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S13C05L06 | P02/AC02 | P79/AC10 |  |  |  | No | C |
| S13C06L06 | P02/AC02 | P79/AC10 |  |  |  | No | C |
| S13C07L06 | P02/AC02 | P79/AC10 |  |  |  | No | C |
| S13C08L06 | P02/AC02 |  |  |  |  | Yes | C |
| S13C09L06 | P02/AC02 | P74/AC08 |  |  |  | No | C |
| S13C10L06 | P02/AC02 |  |  |  |  | Yes | C |
| S13C11L06 | P02/AC02 |  |  |  |  | Yes | C |
| S13C12L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S13C13L06 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| S13C14L06 | P02/AC02 |  |  |  |  | Yes | C |
| S11H01L6 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| S11H01M6 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| S11H01A6 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| S11H05L6 | P04/AC04 |  |  |  |  | Yes | E, S |
| S11H05M6 | P23/AE03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 | No | D |

TABLE 14: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S11A01L06 | P03/AC03 |  |  |  |  | Yes | C |
| S11A02L06 | P03/AC03 |  |  |  |  | Yes | C |
| S12A01L06 | P03/AC03 |  |  |  |  | Yes | C |
| S12A02L06 | P03/AC03 |  |  |  |  | Yes | C |
| S13A01L06 | P03/AC03 |  |  |  |  | Yes | C |
| S13A02L06 | P03/AC03 |  |  |  |  | Yes | C |
| S11C05M06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S12C05M06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S13C05M06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S11C05A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| S12C05A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| S13C05A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| S11C05B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| S12C05B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| S13C05B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |

1. Next Process
	D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV

TABLE 15: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S12A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S13A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| S12A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| S13A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| S12C05L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S12C06L05 | P02/AC02 |  |  |  |  | Yes | S |
| S12C07L05 | P02/AC02 |  |  |  |  | Yes | S |
| S13C05L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| S13C06L05 | P02/AC02 |  |  |  |  | Yes | S |
| S13C07L05 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 16: TRACKING TABLE OF FLEXIBLE BASE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S12A01L03 | P41/UG02 | P47/UG08 | P43/UG04 | P46/UG07 | P44/UG05 | Yes | S |
| S13A01L03 | P41/UG02 | P47/UG08 | P43/UG04 | P46/UG07 | P44/UG05 | Yes | S |

TABLE 17: TRACKING TABLE OF CEMENT STABALIZED SUBBASE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S12C05L02 | P31/TB01 |  |  |  |  | Yes | S |
| S13C05L02 | P31/TB01 |  |  |  |  | Yes | S |

Table 18: TRACKING TABLE OF SUBGRADE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S12A01L01 | P51/SS01 | P43/SS03 | P52/SS04 | P46/SS07 | P55/SS05 | Yes1 | S |
| S13A01L01 | P51/SS01 | P43/SS03 | P52/SS04 | P46/SS07 | P55/SS05 | Yes1 | S |
| S12A01L01 | P49/SS09 |  |  |  |  | No1 | D |
| S13A01L01 | P49/SS09 |  |  |  |  | No1 | D |

1. The moisture content sample may be disposed after testing.  However, any remaining bulk sample should be stored.

TABLE 19: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE LAYER IN THE TURNER FAIRBANKS HIGHWAY RESEARCH CENTER

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| S11H02L6 | P76/AE11 |  |  |  |  | Yes | S |