WASHINGTON SPS-10 PROJECT

(53AAXX and 53BAXX)

# AS SAMPLED MATERIALS SAMPLING AND TESTING PLAN

Contents

AS SAMPLED MATERIALS SAMPLING AND TESTING PLAN	1

GENERAL LAYOUT INFORMATION	2

MATERIALS SAMPLING AND FIELD TESTING	5

LABORATORY MATERIALS TESTING	39

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Washington SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  Table 2 indicates transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Additionally, Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION

| Section Number | SHRP ID | Description |
| --- | --- | --- |
| AA01 | 53AA01 | HMA Control Section – PG 70-28 |
| AA02 | 53AA02 | WMA – Foaming Process with 100 gyrations and PG 70-28 |
| AA03 | 53AA03 | WMA – Evotherm with 100 gyrations and PG 70-28 |
| BA01 | 53BA01 | HMA Control Section with 100 gyrations and PG 70-28 |
| BA59 | 53BA59 | WMA – Supplemental section 1 with 60 gyrations and PG 70-28 |
| BA60 | 53BA60 | WMA – Supplemental section 2 with 60 gyrations and PG 76-28 |

TABLE 2: TEST SECTION LAYOUT

| Begin STA | End STA | Description | Section ID |
| --- | --- | --- | --- |
| L463+00 WB | L455+00 WB | Transition | 53AA01 (WB) |
| L455+00 WB | L454+00 WB | Sampling Area |  |
| L454+00 WB | L453+50 WB | Buffer Area |  |
| L453+50 WB | L448+50 WB | Monitoring Area |  |
| L448+50 WB | L448+00 WB | Buffer Area |  |
| L448+00 WB | L447+00 WB | Sampling Area |  |
| L426+00 WB | L418+00 WB | Transition | 53AA03 (WB) |
| L418+00 WB | L417+00 WB | Sampling Area |  |
| L417+00 WB | L416+50 WB | Buffer Area |  |
| L416+50 WB | L411+50 WB | Monitoring Area |  |
| L411+50 WB | L411+00 WB | Buffer Area |  |
| L411+00 WB | L410+00 WB | Sampling Area |  |
| L410+00 WB | L402+00 WB | Transition | 53AA02 (WB) |
| L402+00 WB | L401+00 WB | Sampling Area |  |
| L401+00 WB | L400+50 WB | Buffer Area |  |
| L400+50 WB | L395+50 WB | Monitoring Area |  |
| L395+50 WB | L395+00 WB | Buffer Area |  |
| L395+00 WB | L394+00 WB | Sampling Area |  |
| L394+00 EB | L402+00 EB | Transition | 53BA59 (EB) |
| L402+00 EB | L403+00 EB | Sampling Area |  |
| L403+00 EB | L403+50 EB | Buffer Area |  |
| L403+50 EB | L408+50 EB | Monitoring Area |  |
| L408+50 EB | L409+00 EB | Buffer Area |  |
| L409+00 EB | L410+00 EB | Sampling Area |  |
| L410+00 EB | L418+00 EB | Transition | 53BA60 (EB) |
| L418+00 EB | L419+00 EB | Sampling Area |  |
| L419+00 EB | L419+50 EB | Buffer Area |  |
| L419+50 EB | L424+50 EB | Monitoring Area |  |
| L424+50 EB | L425+00 EB | Buffer Area |  |
| L425+00 EB | L426+00 EB | Sampling Area |  |
| L447+00 EB | L455+00 EB | Transition | 53BA01 (EB) |
| L455+00 EB | L456+00 EB | Sampling Area |  |
| L456+00 EB | L456+50 EB | Buffer Area |  |
| L456+50 EB | L461+50 EB | Monitoring Area |  |
| L461+50 EB | L462+00 EB | Buffer Area |  |
| L462+00 EB | L463+00 EB | Sampling Area |  |

Direction of Traffic (WB)

L455+00

L463+00

L447+00

L426+00

L418+00

800 ft

L410+00

L402+00

L394+00

800 ft

800 ft

L453+50

L448+50

Transition zone (800 ft)

Sampling Area 11 (100 ft)

Gap (2100 ft)

L416+50

L411+50

Transition zone (800 ft)

Buffer Area (50 ft)

Sampling Area 7 (100 ft)

Sampling Area 8 (100 ft)

53AA01

HMA Control section 1 with PG 70-28 and 100 gyrations

Buffer Area (50 ft)

Transition zone (800 ft)

Buffer Area (50 ft)

Sampling Area 9 (100 ft)

Sampling Area 10 (100 ft)

53AA03

WMA Chemical additive (Evotherm) with PG 70-28 and 100 gyrations

Buffer Area (50 ft)

L400+50

L395+50

Buffer Area (50 ft)

53AA02

WMA Foaming process with PG 70-28 and 100 gyrations

Buffer Area (50 ft)

Sampling Area 12 (100 ft)

L424+50

L408+50

L461+50

L461+50

Gap (2100 ft)

L403+50

Buffer Area (50 ft)

53BA60

WMA Supplemental section 1with PG 70-28 and 60 gyrations

Sampling Area 6 (100 ft)

Sampling Area 5 (100 ft)

Buffer Area (50 ft)

Transition zone (800 ft)

Buffer Area (50 ft)

53BA59

WMA Supplemental section 2with PG 76-28 and 60 gyrations

Sampling Area 4 (100 ft)

Sampling Area 3 (100 ft)

Buffer Area (50 ft)

53BA01

HMA Control section 2 with PG 70-28 and 100 gyrations

Sampling Area 2 (100 ft)

Sampling Area 1 (100 ft)

Buffer Area (50 ft)

Transition zone (800 ft)

L421+50

Transition zone (800 ft)

Buffer Area (50 ft)

L419+50

L411+50

L456+50

L447+00

L455+00

L426+00

L418+00

L410+00

800 ft

800 ft

L463+00

800 ft

L394+00

L402+00

Direction of Traffic (EB)

FIGURE 1: WASHINGTON SPS-10 PROJECT LAY

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at time zero (t0 is at time of construction).  Tables 3 through 8 provide the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 9 provides the scope of material sampling, and Table 10 provides the scope of field testing.

Figures 2 through 13 show the locations for the many samples and tests scheduled.  Figures 2 through 7 show density measurement layouts, and Figures 8 through 13 show the material sampling locations for each section as well as the location of DCP testing.

Tables 11 through 17 list the samples acquired from each of the six test sections as well as the asphalt plant.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 18 through 20 list samples to be shipped to the central lab testing contractor laboratory, the LTPP Materials Reference Library (MRL), and the Turner-Fairbank Highway Research Center, respectively.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Washington SPS-10, R = “W,” representing western region)

- C = Construction event (For Washington SPS-10, C = 1 for 53AAXX , representing the first constructed SPS-10 and C = 2 for 53BAXX, representing the second constructed SPS-10)

- T = Test Section Number

  - 1 – 01 Both control sections are numbered section 1 and are differentiated by the construction event such that both 53AA01 and 53BA01 are control sections

  - 2 – 02

  - 3 – 03

  - A – 59

  - B – 60

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C –6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

The layer numbering system was applied for each of the six sections. Based on data provided by the Washington State DOT, the sublayers were considered for each of the six sections and categorized and numbered as outlined in the tables below.

The reported layers and layer numbering for section 53AA01 are given in Table 3 below.

TABLE 3: LAYER NUMBERING FOR SECTION 53AA01

| Layer number | Project Layer code | Layer thickness (in) | Material code | Year constructed | Material Description |
| --- | --- | --- | --- | --- | --- |
| 7 | J | 2 | 01 |  | HMA Overlay |
| 6 | I | 2.25 | 01 | 2002 | ACP Class ½ inch PG 70-28 |
| 5 | H | 2.75 | 01 | 1982 | ACP Class B AR400W |
| 4 | F | 4.0 | 01 | 1968 | ACP Class B AR400W |
| 3 | C | 4.2 | 303 | 1968 | Crushed Stone |
| 2 | B | 9.6 |  | 1968 | Untreated Base |
| 1 | A |  |  |  | Subgrade |

The reported layers and layer numbering for section 53BA01 are given in Table 4 below.

TABLE 4: LAYER NUMBERING FOR SECTION 53BA01

| Layer number | Project Layer code | Layer thickness (in) | Material code | Year constructed | Material Description |
| --- | --- | --- | --- | --- | --- |
| 7 | J | 1.875 | 01 |  | HMA Overlay |
| 6 | I | 2.625 | 01 | 2002 | ACP Class ½ inch PG 70-28 |
| 5 | G | 2.5 | 01 | 1977 | ACP Class B AR400W |
| 4 | F | 2.5 | 01 | 1964 | ACP Class B AR400W* |
| 3 | C | 3 | 303 | 1964 | Crushed Stone* |
| 2 | B | 12 |  | 1964 | Untreated Base |
| 1 | A |  |  |  | Subgrade |

The reported layers and layer numbering for section 53AA02 are given in Table 5 below.

TABLE 5: LAYER NUMBERING FOR SECTIONS 53AA02

| Layer number | Project Layer code | Layer thickness (in) | Material code | Year constructed | Material Description |
| --- | --- | --- | --- | --- | --- |
| 7 | K | 2.25 | 01 |  | Experimental WMA Overlay |
| 6 | I | 3.0 | 01 | 2002 | ACP Class ½ inch PG 70-28 |
| 5 | H | 2.25 | 01 | 1982 | ACP Class B AR400W |
| 4 | F | 2.5 | 01 | 1968 | ACP Class B AR400W |
| 3 | C | 4.2 | 303 | 1968 | Crushed Stone |
| 2 | B | 9.6 |  | 1968 | Untreated Base |
| 1 | A |  |  |  | Subgrade |

The reported layers and layer numbering for section 53AA03 are given in Table 6 below.

TABLE 6: LAYER NUMBERING FOR SECTIONS 53AA03

| Layer number | Project Layer code | Layer thickness (in) | Material code | Year constructed | Material Description |
| --- | --- | --- | --- | --- | --- |
| 7 | L | 2.25 | 01 |  | Experimental WMA Overlay |
| 6 | I | 3.0 | 01 | 2002 | ACP Class ½ inch PG 70-28 |
| 5 | H | 2.25 | 01 | 1982 | ACP Class B AR400W |
| 4 | F | 2.5 | 01 | 1968 | ACP Class B AR400W |
| 3 | C | 4.2 | 303 | 1968 | Crushed Stone |
| 2 | B | 9.6 |  | 1968 | Untreated Base |
| 1 | A |  |  |  | Subgrade |

The reported layers and layer numbering for section 53BA59 are given in Table 7 below.

TABLE 7: LAYER NUMBERING FOR SECTIONS 53BA59

| Layer number | Project Layer code | Layer thickness (in) | Material code | Year constructed | Material Description |
| --- | --- | --- | --- | --- | --- |
| 8 | M | 2.25 | 01 | 2002 | Experimental WMA Overlay |
| 7 | I | 2.0 | 01 | 2002 | ACP Class ½ inch PG 70-28 |
| 6 | H | 2 | 01 | 1982 | ACP Class B AR400W |
| 5 | F | 2.5 | 01 | 1968 | ACP Class B AR400W |
| 4 | E | 0.25 | 01 | 1943 | ACP Class B AR400W |
| 3 | D | 7.0 |  | 1937 | PCCP |
| 2 | C | 6.0 | 303 | 1937 | Crushed Stone |
| 1 | A |  |  |  | Subgrade |

The reported layers and layer numbering for section 53BA60 are given in Table 8 below.

TABLE 8: LAYER NUMBERING FOR SECTIONS 53BA60

| Layer number | Project Layer code | Layer thickness (in) | Material code | Year constructed | Material Description |
| --- | --- | --- | --- | --- | --- |
| 8 | N | 2.25 | 01 | 2002 | Experimental WMA Overlay |
| 7 | I | 2.0 | 01 | 2002 | ACP Class ½ inch PG 70-28 |
| 6 | H | 2.25 | 01 | 1982 | ACP Class B AR400W |
| 5 | F | 2.5 | 01 | 1968 | ACP Class B AR400W |
| 4 | E | 0.375 | 01 | 1943 | ACP Class B AR400W |
| 3 | D | 7.0 |  | 1937 | PCCP |
| 2 | C | 6.0 | 303 | 1937 | Crushed Stone |
| 1 | A |  |  |  | Subgrade |

Section STA:

0-68

0-67

0-66

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-70

0-50

Shoulder

C02001

2’

1’

3’

C01001

C03001

2’

C04001

C05001

C07001

C09001

C11001

C13001

C06001

C08001

C10001

C12001

C14001

3’

A01001

A02001

DCP

Key

12” Core

6” Core

Experimental AC sample only

Base and subgrade sample only

Experimental and existing AC sample

Experimental AC, existing AC, base, and subgrade sample

Experimental AC, existing AC, and subgrade sample

FIGURE 2: WASHINGTON SPS-10 PROJECT LAYOUT FOR SECTION 53AA01

0-68

0-66

0-70

0-67

0-65

0-64

0-63

0-62

0-61

0-60

0-59

0-58

0-57

0-56

0-55

0-50

Section STA:

Shoulder

C02002

2’

1’

3’

C01002

C03002

2’

C04002

C05002

C07002

C09002

C11002

C13002

C08002

C10002

C12002

C14002

3’

A01002

2’

A03002

A04002

A05002

A06002

A02002

DCP

C06002

Key

12” Core

6” Core

Experimental AC sample only

Base, subbase, and subgrade sample only

Experimental and existing AC sample

Experimental AC, existing AC, base, and subgrade sample

Experimental AC, existing AC, and subgrade sample

FIGURE 3: WASHINGTON SPS-10 PROJECT LAYOUT FOR SECTION 53AA02

0-50

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-67

0-70

0-66

0-68

Section STA:

Shoulder

C02003

2’

1’

3’

C01003

C03003

2’

C04003

C05003

C07003

C09003

C11003

C13003

C08003

C10003

C12003

C14003

3’

A01003

A02003

2’

A03003

A04003

A05003

A06003

DCP

C06003

Key

12” Core

6” Core

Experimental AC sample only

Base, subbase and subgrade sample only

Experimental and existing AC sample

Experimental AC, existing AC, base, and subgrade sample

Experimental AC, existing AC, and subgrade sample

FIGURE 4: WASHINGTON SPS-10 PROJECT LAYOUT FOR SECTION 53AA03

0-50

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-67

0-70

0-66

0-68

Section STA:

Shoulder

C16001

2’

1’

3’

C15001

C17001

2’

C18001

C19001

C21001

C23001

C25001

C27001

C20001

C22001

C24001

C26001

C28001

3’

A03001

A04001

DCP

Key

12” Core

6” Core

Experimental AC sample only

Base and subgrade sample only

Experimental and existing AC sample

Experimental AC, existing AC, base, and subgrade sample

Experimental AC, existing AC, and subgrade sample

FIGURE 5: WASHINGTON SPS-10 PROJECT LAYOUT FOR SECTION 53BA01

0-50

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-67

0-70

0-66

0-68

Section STA:

Shoulder

C02059

2’

1’

3’

C01059

C03059

2’

C04059

C05059

C07059

C11059

C13059

C06059

C08059

C10059

C12059

C14059

3’

A01059

A02059

DCP

C09059

Key

12” Core

6” Core

Experimental AC sample only

Base and subgrade sample only

Experimental and existing AC sample

Experimental AC, existing AC, base, and subgrade sample

Experimental AC, existing AC, and subgrade sample

FIGURE 6: WASHINGTON SPS-10 PROJECT LAYOUT FOR SECTION 53BA59

0-50

0-55

0-56

0-57

0-58

0-59

0-60

0-61

0-62

0-63

0-64

0-65

0-67

0-70

0-66

0-68

Section STA:

Shoulder

C02060

2’

1’

3’

C01060

C03060

2’

C04060

C05060

C07060

C09060

C11060

C13060

C06060

C08060

C10060

C12060

C14060

3’

A01060

A02060

DCP

Key

12” Core

6” Core

Experimental AC sample only

Base and subgrade sample only

Experimental and existing AC sample

Experimental AC, existing AC, base, and subgrade sample

Experimental AC, existing AC, and subgrade sample

FIGURE 7: WASHINGTON SPS-10 PROJECT LAYOUT FOR SECTION 53BA60

Section 53AA01 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03001

T02001

T01001

Traffic

FIGURE 8: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 53AA01 WASHINGTON SPS-10

Section 53AA02 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03002

T02002

T01002

Traffic

FIGURE 9: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 53AA02 WASHINGTON SPS-10

Section 53AA03 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03003

T02003

T01003

Traffic

FIGURE 10: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 53AA03 WASHINGTON SPS-10

Section 53BA01 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T06001

T05001

T04001

Traffic

FIGURE 11: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 53BA01 WASHINGTON SPS-10

Section 53BA59 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03059

T02059

T01059

Traffic

FIGURE 12: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 53BA59 WASHINGTON SPS-10

Section 53BA60 - Monitoring Area

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03060

T02060

T01060

Traffic

FIGURE 13: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 53BA60 WASHINGTON SPS-10

TABLE 9: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
|  | DURING CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 5-gallon buckets uncompacted AC mix | 48 | F01001, F01002, F01003, F02001, F01059, F01060 |
|  | 1-gallon can virgin AC Binder (PG 70-28) | 7 | H01001 |
|  | 1-gallon can virgin AC Binder (PG 76-28) | 7 | H01060 |
|  | 5-gallon bucket combined aggregate | 30 | H02001 |
|  | 50 lb bulk sample RAP | 1 | H03001 |
|  | 5-gallon bucket RAP | 5 | H03001 |
|  | 1-gallon chemical additive (Evotherm) | 1 | H01003 |
|  | POST-CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 12" Core | 12 | A01001-A02001, A03001-A04001, A01002-A02002, A01003-A02003, A01059-A02059, A01060-A02060 |
|  | 6" Core | 84 | C01001-C14001, C15001-C28001, C01002-C14002, C01003-C14003, C01059-C14059, C01060-C14060 |
| B. | ORIGINAL HMAC |  |  |
|  | 12" Core | 8 | A03001- A04001, A01002-A02002, A01003-A01004, A01059, A01060 |
|  | 6" Core | 18 | C15001-C20001, C01002-C03002, C01003-C03003, C01059-C03059, C01060-C03060 |
| C. | CRUSHED STONE |  |  |
|  | 150 lb bulk sample | 2 | A01002 -A06002, A01003-A06003 |
| D. | UNTREATED BASE |  |  |
|  | 150 lb bulk sample | 2 | A01002 -A06002, A01003-A06003 |
| E. | SUBGRADE |  |  |
|  | 150 lb bulk sample | 4 | A01001-A04001; A03002-A06002, A03003-A06003 |
|  | Moisture content jar sample | 4 | A01001-A04001; A03002-A06002, A03003-A06003 |

TABLE 10: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | PRE-CONSTRUCTION TESTING |  |  |
| A. | ORIGINAL HMAC |  |  |
|  | Elevation Survey | 6 | All Sections |
|  | POST-CONSTRUCTION TESTING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Elevation Survey | 6 | All Sections |
|  | In situ density measurement | 18 | T01001-T03001, T04001-T06001, T01002-T03002, T01003-T03003, T01059 -T03059, T01060-T03060 |
|  | Core Examination and Thickness (P01/AC01) | 96 | A01001-A02001, A03001-A04001, A01002-A02002, A01003-A02003, A01059-A02059, A01060-A02060, C01001-C14001, C15001-C28001, C01002-C14002, C01003-C14003, C01059-C14059, C01060-C14060 |
| B. | ORIGINAL HMAC |  |  |
|  | Core Examination and Thickness | 26 | A03001- A04001, A01002-A02002, A01003-A01004, A01059, A01060, C15001-C20001, C01002-C03002, C01003-C03003, C01059-C03059, C01060-C03060 |
| C. | CRUSHED STONE |  |  |
|  | DCP | 6 | A01001, A02002, C02003, A03001, C02059, C02060 |
| D. | UNTREATED BASE |  |  |
|  | DCP | 6 | A01001, A02002, C02003, A03001, C02059, C02060 |
| E. | SUBGRADE |  |  |
|  | DCP | 6 | A01001, A02002, C02003, A03001, C02059, C02060 |

TABLE 11: SAMPLES ACQUIRED FROM TEST SECTION 53AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01001 | 7 | BA01001 | W11A01L07 | 12" Core |
|  | 6 | BA03001 | W11A01L06 | 12" Core |
|  | 5 | BA05001 | W11A01L05 | 12" Core |
|  | 4 | BA07001 | W11A01L04 | 12" Core |
| A02001 | 7 | BA02001 | W11A02L07 | 12" Core |
|  | 6 | BA04001 | W11A02L06 | 12" Core |
|  | 5 | BA06001 | W11A02L05 | 12" Core |
|  | 4 | BA08001 | W11A02L04 | 12" Core |
| A01001, A02001 | 1 | BS01001 | W11A01L01 | 150 lb Bulk Sample |
|  | 1 | MS01001 | W11A01W01 | Moisture content jar sample |
| C01001 | 7 | CA01001 | W11C01L07 | 6" Core |
| C02001 | 7 | CA02001 | W11C02L07 | 6" Core |
| C03001 | 7 | CA03001 | W11C03L07 | 6" Core |
| C04001 | 7 | CA04001 | W11C04L07 | 6" Core |
| C05001 | 7 | CA05001 | W11C05L07 | 6" Core |
| C06001 | 7 | CA06001 | W11C06L07 | 6" Core |
| C07001 | 7 | CA07001 | W11C07L07 | 6" Core |
| C08001 | 7 | CA08001 | W11C08L07 | 6" Core |
| C09001 | 7 | CA09001 | W11C09L07 | 6" Core |
| C10001 | 7 | CA10001 | W11C10L07 | 6" Core |
| C11001 | 7 | CA11001 | W11C11L07 | 6" Core |
| C12001 | 7 | CA12001 | W11C12L07 | 6" Core |
| C13001 | 7 | CA13001 | W11C13L07 | 6" Core |
| C14001 | 7 | CA14001 | W11C14L07 | 6" Core |
| F01001 | 7 | BA09001 | W11F01-F08L07 | 8 5-gallon buckets uncompacted AC mix |

TABLE 12: SAMPLES ACQUIRED FROM TEST SECTION 53AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01002 | 7 | BA01002 | W12A01L07 | 12" Core |
|  | 6 | BA03002 | W12A01L06 | 12" Core |
|  | 5 | BA05002 | W12A01L05 | 12" Core |
|  | 4 | BA07002 | W12A01L04 | 12" Core |
| A02002 | 7 | BA02002 | W12A02L07 | 12" Core |
|  | 6 | BA04002 | W12A02L06 | 12" Core |
|  | 5 | BA06002 | W12A02L05 | 12" Core |
|  | 4 | BA08002 | W12A02L04 | 12" Core |
| A01002, A02002, A03002, A04002, A05002, A06002 | 3 | BG01002 | W12A01L03 | 150 lb Bulk Sample |
|  | 2 | BG02002 | W12A01L02 | 150 lb Bulk Sample |
|  | 1 | BS01002 | W12A01L01 | 150 lb Bulk Sample |
|  | 1 | MS01002 | W12A01W01 | Moisture content jar sample |
| C01002 | 7 | CA01002 | W12C01L07 | 6" Core |
|  | 6 | CA15002 | W12C01L06 | 6" Core |
|  | 5 | CA18002 | W12C01L05 | 6" Core |
|  | 4 | CA21002 | W12C01L04 | 6" Core |
| C02002 | 7 | CA02002 | W12C02L07 | 6" Core |
| C03002 | 7 | CA03002 | W12C03L07 | 6" Core |
|  | 6 | CA16002 | W12C03L06 | 6" Core |
|  | 5 | CA19002 | W12C03L05 | 6" Core |
|  | 4 | CA22002 | W12C03L04 | 6" Core |
| C04002 | 7 | CA04002 | W12C04L07 | 6" Core |
| C05002 | 7 | CA05002 | W12C05L07 | 6" Core |
|  | 6 | CA17002 | W12C05L06 | 6" Core |
|  | 5 | CA20002 | W12C05L05 | 6" Core |
|  | 4 | CA23002 | W12C05L04 | 6" Core |
| C06002 | 7 | CA06002 | W12C06L07 | 6" Core |
| C07002 | 7 | CA07002 | W12C07L07 | 6" Core |
| C08002 | 7 | CA08002 | W12C08L07 | 6" Core |
| C09002 | 7 | CA09002 | W12C09L07 | 6" Core |
| C10002 | 7 | CA10002 | W12C10L07 | 6" Core |
| C11002 | 7 | CA11002 | W12C11L07 | 6" Core |
| C12002 | 7 | CA12002 | W12C12L07 | 6" Core |
| C13002 | 7 | CA13002 | W12C13L07 | 6" Core |

TABLE 12: SAMPLES ACQUIRED FROM TEST SECTION 53AA02 (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C14002 | 7 | CA14002 | W12C14L07 | 6" Core |
| F01002 | 7 | BA09002 | W12F01-F08L07 | 8 5-gallon buckets uncompacted AC mix |

TABLE 13: SAMPLES ACQUIRED FROM TEST SECTION 53AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01003 | 7 | BA01003 | W13A01L07 | 12" Core |
|  | 6 | BA03003 | W13A01L06 | 12" Core |
|  | 5 | BA05003 | W13A01L05 | 12" Core |
|  | 4 | BA07003 | W13A01L04 | 12" Core |
| A02003 | 7 | BA02003 | W13A02L07 | 12" Core |
|  | 6 | BA04003 | W13A02L06 | 12" Core |
|  | 5 | BA06003 | W13A02L05 | 12" Core |
|  | 4 | BA08003 | W13A02L04 | 12" Core |
| A01003, A02003, A03003, A04003, A05003, A06003 | 3 | BG01003 | W13A01L03 | 150 lb Bulk Sample |
|  | 2 | BG01003 | W13A01L02 | 150 lb Bulk Sample |
|  | 1 | BS01003 | W13A01L01 | 150 lb Bulk Sample |
|  | 1 | MS01003 | W13A01W01 | Moisture content jar sample |
| C01003 | 7 | CA01003 | W13C01L07 | 6" Core |
| C02003 | 7 | CA02003 | W13C02L07 | 6" Core |
|  | 6 | CA16003 | W13C02L06 | 6" Core |
|  | 5 | CA19003 | W13C02L05 | 6" Core |
|  | 4 | CA22003 | W13C02L04 | 6" Core |
| C03003 | 7 | CA03003 | W13C03L07 | 6" Core |
| C04003 | 7 | CA04003 | W13C04L07 | 6" Core |
|  | 6 | CA17003 | W13C04L06 | 6" Core |
|  | 5 | CA20003 | W13C04L05 | 6" Core |
|  | 4 | CA23003 | W13C04L04 | 6" Core |
| C05003 | 7 | CA05003 | W13C05L07 | 6" Core |
| C06003 | 7 | CA06003 | W13C06L07 | 6" Core |
|  | 6 | CA18003 | W13C06L06 | 6" Core |
|  | 5 | CA21003 | W13C06L05 | 6" Core |
|  | 4 | CA24003 | W13C06L04 | 6" Core |
| C07003 | 7 | CA07003 | W13C07L07 | 6" Core |
| C08003 | 7 | CA08003 | W13C08L07 | 6" Core |
| C09003 | 7 | CA09003 | W13C09L07 | 6" Core |
| C10003 | 7 | CA10003 | W13C10L07 | 6" Core |
| C11003 | 7 | CA11003 | W13C11L07 | 6" Core |
| C12003 | 7 | CA12003 | W13C12L07 | 6" Core |
| C13003 | 7 | CA13003 | W13C13L07 | 6" Core |

TABLE 13: SAMPLES ACQUIRED FROM TEST SECTION 53AA03 (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C14003 | 7 | CA14003 | W13C14L07 | 6" Core |
| F01003 | 7 | BA09003 | W13F01-F08L07 | 8 5-gallon buckets uncompacted AC mix |

TABLE 14: SAMPLES ACQUIRED FROM TEST SECTION 53BA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A03001 | 7 | BA07001 | W21A01L07 | 12" Core |
|  | 6 | BA10001 | W21A01L06 | 12" Core |
|  | 5 | BA12001 | W21A01L05 | 12" Core |
|  | 4 | BA14001 | W21A01L04 | 12" Core |
| A04001 | 7 | BA08001 | W21A02L07 | 12" Core |
|  | 6 | BA11001 | W21A02L06 | 12" Core |
|  | 5 | BA13001 | W21A02L05 | 12" Core |
|  | 4 | BA15001 | W21A02L04 | 12" Core |
| A03001, A04001 | 1 | BS02001 | W21A01L01 | 150 lb Bulk Sample |
|  | 1 | MS02001 | W21A01W01 | Moisture content jar sample |
| C15001 | 7 | CA15001 | W21C15L07 | 6" Core |
| C16001 | 7 | CA16001 | W21C16L07 | 6" Core |
|  | 6 | CA27001 | W21C16L06 | 6" Core |
|  | 5 | CA33001 | W21C16L05 | 6" Core |
|  | 4 | CA39001 | W21C16L04 | 6" Core |
| C17001 | 7 | CA17001 | W21C17L07 | 6" Core |
| C18001 | 7 | CA18001 | W21C18L07 | 6" Core |
|  | 6 | CA28001 | W21C18L06 | 6" Core |
|  | 5 | CA34001 | W21C18L05 | 6" Core |
|  | 4 | CA40001 | W21C18L04 | 6" Core |
| C19001 | 7 | CA19001 | W21C19L07 | 6" Core |
| C20001 | 7 | CA20001 | W21C20L07 | 6" Core |
|  | 6 | CA29001 | W21C20L06 | 6" Core |
|  | 5 | CA35001 | W21C20L05 | 6" Core |
|  | 4 | CA41001 | W21C20L04 | 6" Core |
| C21001 | 7 | CA21001 | W21C21L07 | 6" Core |
| C22001 | 7 | CA22001 | W21C22L07 | 6" Core |
|  | 6 | CA30001 | W21C22L06 | 6" Core |
|  | 5 | CA36001 | W21C22L05 | 6" Core |
|  | 4 | CA42001 | W21C22L04 | 6" Core |
| C23001 | 7 | CA23001 | W21C23L07 | 6" Core |
| C24001 | 7 | CA24001 | W21C24L07 | 6" Core |
|  | 6 | CA31001 | W21C24L06 | 6" Core |
|  | 5 | CA37001 | W21C24L05 | 6" Core |
|  | 4 | CA43001 | W21C24L04 | 6" Core |

TABLE 14: SAMPLES ACQUIRED FROM TEST SECTION 53BA01 (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C25001 | 7 | CA25001 | W21C25L07 | 6" Core |
| C26001 | 7 | CA26001 | W21C26L07 | 6" Core |
|  | 6 | CA32001 | W21C26L06 | 6" Core |
|  | 5 | CA38001 | W21C26L05 | 6" Core |
|  | 4 | CA44001 | W21C26L04 | 6" Core |
| C27001 | 7 | CA27001 | W21C27L07 | 6" Core |
| C28001 | 7 | CA28001 | W21C28L07 | 6" Core |
| F01001 | 7 | BA09001 | W21F01L07 | 8 5-gallon buckets uncompacted AC mix |

TABLE 15: SAMPLES ACQUIRED FROM TEST SECTION 53BA59

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01059 | 8 | BA01059 | W2AA01L08 | 12" Core |
|  | 7 | BA03059 | W2AA01L07 | 12" Core |
|  | 6 | BA04059 | W2AA01L06 | 12" Core |
|  | 5 | BA05059 | W2AA01L05 | 12" Core |
|  | 4 | BA06059 | W2AA01L04 | 12" Core |
| A02059 | 8 | BA02059 | W2AA02L08 | 12" Core |
| C01059 | 8 | CA01059 | W2AC01L08 | 6" Core |
|  | 7 | CA15059 | W2AC01L07 | 6" Core |
|  | 6 | CA20059 | W2AC01L06 | 6" Core |
|  | 5 | CA25059 | W2AC01L05 | 6" Core |
|  | 4 | CA30059 | W2AC01L04 | 6" Core |
| C02059 | 8 | CA02059 | W2AC02L08 | 6" Core |
|  | 7 | CA16059 | W2AC02L07 | 6" Core |
|  | 6 | CA21059 | W2AC02L06 | 6" Core |
|  | 5 | CA26059 | W2AC02L05 | 6" Core |
|  | 4 | CA31059 | W2AC02L04 | 6" Core |
| C03059 | 8 | CA03059 | W2AC03L08 | 6" Core |
|  | 7 | CA17059 | W2AC03L07 | 6" Core |
|  | 6 | CA22059 | W2AC03L06 | 6" Core |
|  | 5 | CA27059 | W2AC03L05 | 6" Core |
|  | 4 | CA32059 | W2AC03L04 | 6" Core |
| C04059 | 8 | CA04059 | W2AC04L08 | 6" Core |
| C05059 | 8 | CA05059 | W2AC05L08 | 6" Core |
| C06059 | 8 | CA06059 | W2AC06L08 | 6" Core |
| C07059 | 8 | CA07059 | W2AC07L08 | 6" Core |
| C08059 | 8 | CA08059 | W2AC08L08 | 6" Core |
|  | 7 | CA18059 | W2AC08L07 | 6" Core |
|  | 6 | CA23059 | W2AC08L06 | 6" Core |
|  | 5 | CA28059 | W2AC08L05 | 6" Core |
|  | 4 | CA33059 | W2AC08L04 | 6" Core |
| C09059 | 8 | CA09059 | W2AC09L08 | 6" Core |
| C10059 | 8 | CA10059 | W2AC10L08 | 6" Core |
|  | 7 | CA19059 | W2AC10L07 | 6" Core |
|  | 6 | CA24059 | W2AC10L06 | 6" Core |
|  | 5 | CA29059 | W2AC10L05 | 6" Core |
|  | 4 | CA34059 | W2AC10L04 | 6" Core |

TABLE 15: SAMPLES ACQUIRED FROM TEST SECTION 53BA59 (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| C11059 | 8 | CA11059 | W2AC11L08 | 6" Core |
| C12059 | 8 | CA12059 | W2AC12L08 | 6" Core |
| C13059 | 8 | CA13059 | W2AC13L08 | 6" Core |
| C14059 | 8 | CA14059 | W2AC14L08 | 6" Core |
| F01059 | 8 | BA07059 | W2AF01-F08L08 | 8 5-gallon buckets uncompacted AC mix |

TABLE 16: SAMPLES ACQUIRED FROM TEST SECTION 53BA60

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01060 | 8 | BA01060 | W2BA01L08 | 12" Core |
|  | 7 | BA03060 | W2BA01L07 | 12" Core |
|  | 6 | BA04060 | W2BA01L06 | 12" Core |
|  | 5 | BA05060 | W2BA01L05 | 12" Core |
|  | 4 | BA06060 | W2BA01L04 | 12" Core |
| A02060 | 8 | BA02060 | W2BA02L08 | 12" Core |
| C01060 | 8 | CA01060 | W2BC01L08 | 6" Core |
| C02060 | 8 | CA02060 | W2BC02L08 | 6" Core |
|  | 7 | CA15060 | W2BC02L07 | 6" Core |
|  | 6 | CA18060 | W2BC02L06 | 6" Core |
|  | 5 | CA21060 | W2BC02L05 | 6" Core |
|  | 4 | CA24060 | W2BC02L04 | 6" Core |
| C03060 | 8 | CA03060 | W2BC03L08 | 6" Core |
| C04060 | 8 | CA04060 | W2BC04L08 | 6" Core |
|  | 7 | CA16060 | W2BC04L07 | 6" Core |
|  | 6 | CA19060 | W2BC04L06 | 6" Core |
|  | 5 | CA22060 | W2BC04L05 | 6" Core |
|  | 4 | CA25060 | W2BC04L04 | 6" Core |
| C05060 | 8 | CA05060 | W2BC05L08 | 6" Core |
| C06060 | 8 | CA06060 | W2BC06L08 | 6" Core |
|  | 7 | CA17060 | W2BC06L07 | 6" Core |
|  | 6 | CA20060 | W2BC06L06 | 6" Core |
|  | 5 | CA23060 | W2BC06L05 | 6" Core |
|  | 4 | CA26060 | W2BC06L04 | 6" Core |
| C07060 | 8 | CA07060 | W2BC07L08 | 6" Core |
| C08060 | 8 | CA08060 | W2BC08L08 | 6" Core |
| C09060 | 8 | CA09060 | W2BC09L08 | 6" Core |
| C10060 | 8 | CA10060 | W2BC10L08 | 6" Core |
| C11060 | 8 | CA11060 | W2BC11L08 | 6" Core |
| C12060 | 8 | CA12060 | W2BC12L08 | 6" Core |
| C13060 | 8 | CA13060 | W2BC13L08 | 6" Core |
| C14060 | 8 | CA14060 | W2BC14L08 | 6" Core |
| F01060 | 8 | BA07060 | W2BF01-F08L08 | 8 5-gallon buckets uncompacted AC mix |

TABLE 17: SAMPLES ACQUIRED FROM PLANT

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| H01001 | 7 | BC01001 | W11H01L06 | 1 1-gallon can virgin AC binder (PG 70-28) |
| H01001 | 7 | BC02001 | W11H02L06 | 1 1-gallon can virgin AC binder (PG 70-28) |
| H01001 | 7 | BC03001 | W11H03L06 | 5 1-gallon cans virgin AC binder (PG 70-28) |
| H01060 | 8 | BC01060 | W2BH01L08 | 1 1-gallon can virgin AC binder (PG 76-28) |
| H01060 | 8 | BC02060 | W2BH02L08 | 1 1-gallon can virgin AC binder (PG 76-28) |
| H01060 | 8 | BC04060 | W2BH04L08 | 5 1-gallon cans virgin AC binder (PG 76-28) |
| H02001 | 7 | BU01001 | W11H04L06 | 5 5-gallon buckets combined aggregate |
| H03001 | 7 | BR01001 | W11H05L06 | 50 lb Bulk Sample RAP |
| H03001 | 7 | BR02001 | W11H06L06 | 5 5-gallon buckets RAP |
| H01003 | 7 | BW01003 | W13H01L07 | 1 gallon chemical additive (Evotherm) in manufacturer prescribed containers, with MSDS |

TABLE 18: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| W11A01L07 | 12” core |
| W11A02L07 | 12” core |
| W11C01L07 | 6” core |
| W11C02L07 | 6” core |
| W11C03L07 | 6” core |
| W11C04L07 | 6” core |
| W11C05L07 | 6” core |
| W11C06L07 | 6” core |
| W11C07L07 | 6” core |
| W11C08L07 | 6” core |
| W11C09L07 | 6” core |
| W11C10L07 | 6” core |
| W12A01L07 | 12” core |
| W12A02L07 | 12” core |
| W12C01L07 | 6” core |
| W12C02L07 | 6” core |
| W12C03L07 | 6” core |
| W12C04L07 | 6” core |
| W12C05L07 | 6” core |
| W12C06L07 | 6” core |
| W12C07L07 | 6” core |
| W12C08L07 | 6” core |
| W12C09L07 | 6” core |
| W12C10L07 | 6” core |
| W13A01L07 | 12” core |
| W13A02L07 | 12” core |
| W13C01L07 | 6” core |
| W13C02L07 | 6” core |
| W13C03L07 | 6” core |
| W13C04L07 | 6” core |
| W13C05L07 | 6” core |
| W13C06L07 | 6” core |
| W13C07L07 | 6” core |
| W13C08L07 | 6” core |

TABLE 18: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| W13C09L07 | 6” core |
| W13C10L07 | 6” core |
| W21A01L07 | 12” core |
| W21A02L07 | 12” core |
| W21C15L07 | 6” core |
| W21C16L07 | 6” core |
| W21C17L07 | 6” core |
| W21C18L07 | 6” core |
| W21C19L07 | 6” core |
| W21C20L07 | 6” core |
| W21C21L07 | 6” core |
| W21C22L07 | 6” core |
| W21C23L07 | 6” core |
| W21C24L07 | 6” core |
| W2AA01L08 | 12” core |
| W2AA02L08 | 12” core |
| W2AC01L07 | 6” core |
| W2AC02L08 | 6” core |
| W2AC03L08 | 6” core |
| W2AC04L08 | 6” core |
| W2AC05L08 | 6” core |
| W2AC06L08 | 6” core |
| W2AC07L08 | 6” core |
| W2AC08L08 | 6” core |
| W2AC09L08 | 6” core |
| W2AC10L08 | 6” core |
| W2BA01L08 | 12” core |
| W2BA02L08 | 12” core |
| W2BC01L08 | 6” core |
| W2BC02L08 | 6” core |
| W2BC03L08 | 6” core |
| W2BC04L08 | 6” core |
| W2BC05L08 | 6” core |

TABLE 18: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| W2BC06L08 | 6” core |
| W2BC07L08 | 6” core |
| W2BC08L08 | 6” core |
| W2BC09L08 | 6” core |
| W2BC10L08 | 6” core |
| W11H01L07 | 1 1-gallon can of virgin AC binder (PG 70-28) |
| W2BH01L07 | 1 1-gallon can of virgin AC binder (PG 76-28) |
| W11H05L07 | 50 lb Bulk Sample RAP |
| Original HMAC |  |
| W11A01L06 | 12" Core |
| W11A01L05 |  |
| W11A01L04 |  |
| W11A02L06 | 12" Core |
| W11A02L05 |  |
| W11A02L04 |  |
| W12A01L06 | 12" Core |
| W12A01L05 |  |
| W12A01L04 |  |
| W12A02L06 | 12" Core |
| W12A02L05 |  |
| W12A02L04 |  |
| W12C01L06 | 6" Core |
| W12C01L05 |  |
| W12C01L04 |  |
| W12C03L06 | 6" Core |
| W12C03L05 |  |
| W12C03L04 |  |
| W12C05L06 | 6" Core |
| W12C05L05 |  |
| W12C05L04 |  |
| W13A01L06 | 12" Core |
| W13A01L05 |  |
| W13A01L04 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| W13A02L06 | 12" Core |
| W13A02L05 |  |
| W13A02L04 |  |
| W13C02L06 | 6" Core |
| W13C02L05 |  |
| W13C02L04 |  |
| W13C04L06 | 6" Core |
| W13C04L05 |  |
| W13C04L04 |  |
| W13C06L06 | 6" Core |
| W13C06L05 |  |
| W13C06L04 |  |
| W21A01L06 | 12" Core |
| W21A01L05 |  |
| W21A01L04 |  |
| W21A02L06 | 12" Core |
| W21A02L05 |  |
| W21A02L04 |  |
| W21C16L06 | 6" Core |
| W21C16L05 |  |
| W21C16L04 |  |
| W21C18L06 | 6" Core |
| W21C18L05 |  |
| W21C18L04 |  |
| W21C20L06 | 6" Core |
| W21C20L05 |  |
| W21C20L04 |  |
| W21C22L06 | 6" Core |
| W21C22L05 |  |
| W21C22L04 |  |
| W21C24L06 | 6" Core |
| W21C24L05 |  |
| W21C24L04 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| W21C26L06 | 6" Core |
| W21C26L05 |  |
| W21C26L04 |  |
| W2AA01L07 | 12" Core |
| W2AA01L06 |  |
| W2AA01L05 |  |
| W2AA01L04 |  |
| W2AC01L07 | 6" Core |
| W2AC01L06 |  |
| W2AC01L05 |  |
| W2AC01L04 |  |
| W2AC02L07 | 6" Core |
| W2AC02L06 |  |
| W2AC02L05 |  |
| W2AC02L04 |  |
| W2AC03L07 | 6" Core |
| W2AC03L06 |  |
| W2AC03L05 |  |
| W2AC03L04 |  |
| W2BA01L07 | 12" Core |
| W2BA01L06 |  |
| W2BA01L05 |  |
| W2BA01L04 |  |
| W2BC02L07 | 6" Core |
| W2BC02L06 |  |
| W2BC02L05 |  |
| W2BC02L04 |  |
| W2BC04L07 | 6" Core |
| W2BC04L06 |  |
| W2BC04L05 |  |
| W2BC04L04 |  |
| W2BC06L07 | 6" Core |
| W2BC06L06 |  |
| W2BC06L05 |  |
| W2BC06L04 |  |

TABLE 18: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Crushed Stone Base |  |
| W12A01L03 | 150 lb Bulk Sample |
| W13A01L03 | 150 lb Bulk Sample |
| Untreated Base |  |
| W12A01L02 | 150 lb Bulk Sample |
| W13A01L02 | 150 lb Bulk Sample |
| Subgrade |  |
| W11A01L01 | 150 lb bulk sample |
| W13A01L01 | 150 lb Bulk Sample |
| W11A01W01 | Moisture content jar sample |
| W13A01W01 | Moisture content jar sample |

TABLE 19: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| W11C11L07 | 6" Core |
| W11C12L07 | 6" Core |
| W11C13L07 | 6" Core |
| W11C14L07 | 6" Core |
| W12C11L07 | 6" Core |
| W12C12L07 | 6" Core |
| W12C13L07 | 6" Core |
| W12C14L07 | 6" Core |
| W13C11L07 | 6" Core |
| W13C12L07 | 6" Core |
| W13C13L07 | 6" Core |
| W13C14L07 | 6" Core |
| W21C23L07 | 6" Core |
| W21C25L07 | 6" Core |
| W21C27L07 | 6" Core |
| W21C28L07 | 6" Core |
| W2AC11L08 | 6" Core |
| W2AC12L08 | 6" Core |
| W2AC13L08 | 6" Core |
| W2AC14L08 | 6" Core |
| W2BC11L08 | 6" Core |
| W2BC12L08 | 6" Core |
| W2BC13L08 | 6" Core |
| W2BC14L08 | 6" Core |
| W11H03L07 | 5 1-gallon cans of virgin AC binder (PG 70-28) |
| W2BH03L08 | 5 1-gallon cans of virgin AC binder (PG 76-28) |
| W11F01L07 | 8 5-gallon buckets uncompacted AC mix |
| W12F01L07 | 8 5-gallon buckets uncompacted AC mix |
| W13F01L07 | 8 5-gallon buckets uncompacted AC mix |
| W21F01L07 | 8 5-gallon buckets uncompacted AC mix |
| W2AF01L08 | 8 5-gallon buckets uncompacted AC mix |
| W2BF01L08 | 8 5-gallon buckets uncompacted AC mix |
| W11H04L07 | 5 5-gallon buckets combined aggregate |
| W11H06L08 | 5 5-gallon buckets RAP |
| W13H01L07 | 1 gallon chemical additive (Evotherm) in manufacturer prescribed containers, with MSDS |

TABLE 20: SAMPLES TO BE SHIPPED TO THE TURNER FAIRBANKS RESEARCH CENTER

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC Layer |  |
| W11H01L07 | 1 1-gallon can of virgin AC binder (PG 70-28) |
| W2BH01L08 | 1 1-gallon can of virgin AC binder (PG 76-28) |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Washington SPS-10 project.  The previous section ended with lists of samples to be shipped to each of the two laboratories, the central lab testing contractor laboratory and the Turner-Fairbank Highway Research center.  In this section, the tests to be performed on each sample are listed.

Table 21 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Table 22 provides new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 23 through 29 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 21: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 60 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 12 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 6 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 6 | X |  |
|  | Hamburg Wheel Track | AC09 | P75 | 12 | X |  |
|  | Fenix Fracture Energy | AC10 | P79 | 18 | X |  |
|  | Specific Gravity at 60 ° F | AE03 | P23 | 8 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 18 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 8 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 8 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 6 | X |  |
|  | PPA and Motor Oil Test | AE11 | P76 | 1 |  | X |
| B. | ORIGINAL HMAC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 10 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 2 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 2 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 2 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 2 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 2 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 2 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 2 | X |  |

TABLE 21: SPS-10 LABORATORY TESTING PLANS (Continued)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| C. | CRUSHED STONE |  |  |  |  |  |
|  | Washed Sieve Analysis | UG02 | P41 | 2 | X |  |
|  | Standard Proctor | UG05 | P44 | 2 | X |  |
|  | Atterberg Limits | UG04 | P43 | 2 | X |  |
|  | Resilient Modulus | UG07 | P46 | 2 | X |  |
|  | Classification and Description | UG08 | P47 | 2 | X |  |
| D. | UNTREATED BASE |  |  |  |  |  |
|  | Washed Sieve Analysis | UG02 | P41 | 2 | X |  |
|  | Standard Proctor | UG05 | P44 | 2 | X |  |
|  | Atterberg Limits | UG04 | P43 | 2 | X |  |
|  | Resilient Modulus | UG07 | P46 | 2 | X |  |
|  | Classification and Description | UG08 | P47 | 2 | X |  |
| E. | SUBGRADE (2 test for each type) |  |  |  |  |  |
|  | Sieve Analysis | SS01 | P51 | 4 | X |  |
|  | Atterberg Limits | SS03 | P43 | 4 | X |  |
|  | Classification and Description | SS04 | P52 | 4 | X |  |
|  | Standard Proctor | SS05 | P55 | 4 | X |  |
|  | Resilient Modulus | SS07 | P46 | 4 | X |  |
|  | Natural Moisture Content | SS09 | P49 | 4 | X |  |

TABLE 22: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BA01001 | BAE1001 |
|  | Specimen ID | W11A01L07 | W11A01A07 |
|  | Sample No. | BA01002 | BAE1002 |
|  | Specimen ID | W12A01L07 | W12A01A07 |
|  | Sample No. | BA01003 | BAE1003 |
|  | Specimen ID | W13A01L07 | W13A01A07 |
|  | Sample No. | BA07001 | BAE2001 |
|  | Specimen ID | W21A01L07 | W21A01A07 |
|  | Sample No. | BA01059 | BAE1059 |
|  | Specimen ID | W2AA01L08 | W2AA01A08 |
|  | Sample No. | BA01060 | BAE1060 |
|  | Specimen ID | W2BA01L08 | W2BA01A08 |
|  | Sample No. | BA04001 | BAE4001 |
|  | Specimen ID | W11A01L06 | W11A01A06 |
|  | Sample No. | BA06001 | BAE6001 |
|  | Specimen ID | W11A01L05 | W11A01A05 |
|  | Sample No. | BA08001 | BAE8001 |
|  | Specimen ID | W11A01L04 | W11A01A04 |
|  | Sample No. | BA04002 | BAE4002 |
|  | Specimen ID | W12A01L06 | W12A01A06 |
|  | Sample No. | BA06002 | BAE6002 |
|  | Specimen ID | W12A01L05 | W12A01A05 |
|  | Sample No. | BA08002 | BAE8002 |
|  | Specimen ID | W12A01L04 | W12A01A04 |
|  | Sample No. | BA04003 | BAE4003 |
|  | Specimen ID | W13A01L06 | W13A01A06 |
|  | Sample No. | BA06003 | BAE6003 |
|  | Specimen ID | W13A01L05 | W13A01A05 |
|  | Sample No. | BA08003 | BAE8003 |
|  | Specimen ID | W13A01L04 | W13A01A04 |
|  | Sample No. | BA10001 | BAE10001 |
|  | Specimen ID | W21A01L06 | W21A01A06 |
|  | Sample No. | BA12001 | BAE12001 |
|  | Specimen ID | W21A01L05 | W21A01A05 |
|  | Sample No. | BA14001 | BAE14001 |
|  | Specimen ID | W21A01L04 | W21A01A04 |
|  | Sample No. | BA04059 | BAE4059 |

TABLE 22: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS (Continued)

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction (continued) | Specimen ID | W2AA01L07 | W2AA01A07 |
|  | Sample No. | BA05059 | BAE5059 |
|  | Specimen ID | W2AA01L06 | W2AA01A06 |
|  | Sample No. | BA06059 | BAE6059 |
|  | Specimen ID | W2AA01L05 | W2AA01A05 |
|  | Sample No. | BA07059 | BAE7059 |
|  | Specimen ID | W2AA01L04 | W2AA01A04 |
|  | Sample No. | BA04060 | BAE4060 |
|  | Specimen ID | W2BA01L07 | W2BA01A07 |
|  | Sample No. | BA05060 | BAE5060 |
|  | Specimen ID | W2BA01L06 | W2BA01A06 |
|  | Sample No. | BA06060 | BAE6060 |
|  | Specimen ID | W2BA01L05 | W2BA01A05 |
|  | Sample No. | BA07060 | BAE7060 |
|  | Specimen ID | W2BA01L04 | W2BA01A04 |
|  | Sample No. | BR01001 | BRE1001 |
|  | Specimen ID | W11H05L07 | W11H05M07 |
| PAV | Sample No. | BAE1001 | BAP1001 |
|  | Specimen ID | W11A01A07 | W11A01B07 |
|  | Sample No. | BAE1002 | BAP1002 |
|  | Specimen ID | W12A01A07 | W12A01B07 |
|  | Sample No. | BAE1003 | BAP1003 |
|  | Specimen ID | W13A01A07 | W13A01B07 |
|  | Sample No. | BAE2001 | BAP2001 |
|  | Specimen ID | W21A01A07 | W21A01B07 |
|  | Sample No. | BAE1059 | BAP1059 |
|  | Specimen ID | W2AA01A08 | W2AA01B08 |
|  | Sample No. | BAE1060 | BAP1060 |
|  | Specimen ID | W2BA01A08 | W2BA01B08 |
|  | Sample No. | BAE4001 | BAP4001 |
|  | Specimen ID | W11A01A06 | W11A01B06 |
|  | Sample No. | BAE6001 | BAP6001 |
|  | Specimen ID | W11A01A05 | W11A01B05 |
|  | Sample No. | BAE8001 | BAP8001 |
|  | Specimen ID | W11A01A04 | W11A01B04 |
|  | Sample No. | BAE4002 | BAP4002 |
|  | Specimen ID | W12A01A06 | W12A01B06 |

TABLE 22: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS (Continued)

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| PAV (continued) | Sample No. | BAE6002 | BAP6002 |
|  | Specimen ID | W12A01A05 | W12A01B05 |
|  | Sample No. | BAE8002 | BAP8002 |
|  | Specimen ID | W12A01A04 | W12A01B04 |
|  | Sample No. | BAE4003 | BAP4003 |
|  | Specimen ID | W13A01A06 | W13A01B06 |
|  | Sample No. | BAE6003 | BAP6003 |
|  | Specimen ID | W13A01A05 | W13A01B05 |
|  | Sample No. | BAE8003 | BAP8003 |
|  | Specimen ID | W13A01A04 | W13A01B04 |
|  | Sample No. | BAE10001 | BAP10001 |
|  | Specimen ID | W21A01A06 | W21A01B06 |
|  | Sample No. | BAE12001 | BAP12001 |
|  | Specimen ID | W21A01A05 | W21A01B05 |
|  | Sample No. | BAE14001 | BAP14001 |
|  | Specimen ID | W21A01A04 | W21A01B04 |
|  | Sample No. | BAE4059 | BAP4059 |
|  | Specimen ID | W2AA01A07 | W2AA01B07 |
|  | Sample No. | BAE5059 | BAP5059 |
|  | Specimen ID | W2AA01A06 | W2AA01B06 |
|  | Sample No. | BAE6059 | BAP6059 |
|  | Specimen ID | W2AA01A05 | W2AA01B05 |
|  | Sample No. | BAE7059 | BAP7059 |
|  | Specimen ID | W2AA01A04 | W2AA01B04 |
|  | Sample No. | BAE4060 | BAP4060 |
|  | Specimen ID | W2BA01A07 | W2BA01B07 |
|  | Sample No. | BAE5060 | BAP5060 |
|  | Specimen ID | W2BA01A06 | W2BA01B06 |
|  | Sample No. | BAE6060 | BAP6060 |
|  | Specimen ID | W2BA01A05 | W2BA01B05 |
|  | Sample No. | BAE7060 | BAP7060 |
|  | Specimen ID | W2BA01A04 | W2BA01B04 |
| RTFO | Sample No. | BC01001 | BCR1001 |
|  | Specimen ID | W11H01L07 | W11H01M07 |
|  | Sample No. | BC01060 | BCR1060 |
|  | Specimen ID | W2BH01L08 | W2BH01M08 |

TABLE 22: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS (Continued)

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| RTFO + PAV | Sample No. | BC01001 | BCZ1001 |
|  | Specimen ID | W11H01L07 | W11H01M07 |
|  | Sample No. | BC01060 | BCZ1005 |
|  | Specimen ID | W2BH01L08 | W2BH01M08 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W11A01L07 | P03/AC03 |  |  |  |  | Yes | C |
| W11A02L07 | P03/AC03 |  |  |  |  | Yes | C |
| W12A01L07 | P03/AC03 |  |  |  |  | Yes | C |
| W12A02L07 | P03/AC03 |  |  |  |  | Yes | C |
| W13A01L07 | P03/AC03 |  |  |  |  | Yes | C |
| W13A02L07 | P03/AC03 |  |  |  |  | Yes | C |
| W21A01L07 | P03/AC03 |  |  |  |  | Yes | C |
| W21A02L07 | P03/AC03 |  |  |  |  | Yes | C |
| W2AA01L08 | P03/AC03 |  |  |  |  | Yes | C |
| W2AA02L08 | P03/AC03 |  |  |  |  | Yes | C |
| W2BA01L08 | P03/AC03 |  |  |  |  | Yes | C |
| W2BA02L08 | P03/AC03 |  |  |  |  | Yes | C |
| W11A01L07 | P04/AC04 |  |  |  |  | No | E |
| W12A01L07 | P04/AC04 |  |  |  |  | No | E |
| W13A01L07 | P04/AC04 |  |  |  |  | No | E |
| W21A01L07 | P04/AC04 |  |  |  |  | No | E |
| W2AA01L08 | P04/AC04 |  |  |  |  | No | E |
| W2BA01L08 | P04/AC04 |  |  |  |  | No | E |
| W11A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W12A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W13A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W21A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W2BA01A08 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| W11A01B07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W12A01B07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W13A01B07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W21A01B07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W2AA01B08 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W2BA01B08 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| W11C01L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W11C02L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W11C03L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W11C04L07 | P02/AC02 |  |  |  |  | Yes | S |
| W11C05L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W11C06L07 | P02/AC02 |  |  |  |  | Yes | S |
| W11C07L07 | P02/AC02 |  |  |  |  | Yes | S |
| W11C08L07 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W11C09L07 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W11C10L07 | P02/AC02 |  |  |  |  | Yes | S |
| W12C01L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W12C02L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W12C03L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W12C04L07 | P02/AC02 |  |  |  |  | Yes | S |
| W12C05L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W12C06L07 | P02/AC02 |  |  |  |  | Yes | S |
| W12C07L07 | P02/AC02 |  |  |  |  | Yes | S |
| W12C08L07 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W12C09L07 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W12C10L07 | P02/AC02 |  |  |  |  | Yes | S |
| W13C01L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W13C02L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W13C03L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W13C04L07 | P02/AC02 |  |  |  |  | Yes | S |
| W13C05L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W13C06L07 | P02/AC02 |  |  |  |  | Yes | S |
| W13C07L07 | P02/AC02 |  |  |  |  | Yes | S |
| W13C08L07 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W13C09L07 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W13C10L07 | P02/AC02 |  |  |  |  | Yes | S |
| W21C15L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W21C16L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W21C17L07 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W21C18L07 | P02/AC02 |  |  |  |  | Yes | S |
| W21C19L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W21C20L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W21C21L07 | P02/AC02 |  |  |  |  | Yes | S |
| W21C22L07 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W21C23L07 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W21C24L07 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC01L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W2AC02L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W2AC03L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W2AC04L08 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC05L08 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W2AC06L08 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC07L08 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC08L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W2AC09L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W2AC10L08 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC01L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W2BC02L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W2BC03L08 | P02/AC02 | P79/AC10 |  |  |  | No | D |
| W2BC04L08 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC05L08 | P02/AC02 |  |  |  |  | No | D |
| W2BC06L08 | P02/AC02 | P74/AC08 |  |  |  | Yes | S |
| W2BC07L08 | P02/AC02 | P74/AC08 |  |  |  | Yes | S |
| W2BC08L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |

TABLE 23: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W2BC09L08 | P02/AC02 | P75/AC09 |  |  |  | No | D |
| W2BC10L08 | P02/AC02 |  |  |  |  | Yes | S |

1. Next Process

D 	Remaining sample should be disposed
			S 	Remaining sample should be stored
			C	Remaining sample will be combined with another sample
			E 	Perform further testing on extracted sample
			P 	Perform further testing with PAV
			R 	Perform further testing with RFTO

TABLE 24: TRACKING TABLE OF EXPERIMENTAL ASPHALT TANK BINDER IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W11H01L08 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| W2BH01L08 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| W11H01M07 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| W2BH01M08 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| W11H01A07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| W2BH01A08 | P27/AE07 | P28/AE08 |  |  |  | No | D |

TABLE 25: TRACKING TABLE OF STOCKPILE RAP IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W11H05L07 | P04/AC04 |  |  |  |  | Yes | E, S |
| W11H05M07 | P23/AE03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 | No | D |

TABLE 26: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W11A01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W11A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W11A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W11A02L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W11A02L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W11A02L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W12A01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W12A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W12A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W12A02L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W12A02L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W12A02L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W13A01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W13A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W13A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W13A02L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W13A02L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W13A02L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W21A01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W21A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W21A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W21A02L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |

TABLE 26: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W21A02L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W21A02L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W2AA01L07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W2AA01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W2AA01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W2AA01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W2BA01L07 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W2BA01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W2BA01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W2BA01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| W11A01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W11A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W11A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W11A02M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W11A02M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W11A02M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W12A01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W12A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W12A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W12A02M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W12A02M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W12A02M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |

TABLE 26: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W13A01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W13A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W13A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W13A02M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W13A02M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W13A02M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W21A01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W21A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W21A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W21A02M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W21A02M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W21A02M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W2AA01M07 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W2AA01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W2AA01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W2AA01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W2BA01M07 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W2BA01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W2BA01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W2BA01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| W12C01L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W12C03L06 | P02/AC02 |  |  |  |  | Yes | S |
| W12C05L06 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 26: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W12C01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W12C03L05 | P02/AC02 |  |  |  |  | Yes | S |
| W12C05L05 | P02/AC02 |  |  |  |  | Yes | S |
| W12C01L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W12C03L04 | P02/AC02 |  |  |  |  | Yes | S |
| W12C05L04 | P02/AC02 |  |  |  |  | Yes | S |
| W13C02L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W13C04L06 | P02/AC02 |  |  |  |  | Yes | S |
| W13C06L06 | P02/AC02 |  |  |  |  | Yes | S |
| W13C02L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W13C04L05 | P02/AC02 |  |  |  |  | Yes | S |
| W13C06L05 | P02/AC02 |  |  |  |  | Yes | S |
| W13C02L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W13C04L04 | P02/AC02 |  |  |  |  | Yes | S |
| W13C06L04 | P02/AC02 |  |  |  |  | Yes | S |
| W21C16L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W21C18L06 | P02/AC02 |  |  |  |  | Yes | S |
| W21C20L06 | P02/AC02 |  |  |  |  | Yes | S |
| W21C22L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W21C24L06 | P02/AC02 |  |  |  |  | Yes | S |
| W21C26L06 | P02/AC02 |  |  |  |  | Yes | S |
| W21C16L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W21C18L05 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 26: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W21C20L05 | P02/AC02 |  |  |  |  | Yes | S |
| W21C22L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W21C24L05 | P02/AC02 |  |  |  |  | Yes | S |
| W21C26L05 | P02/AC02 |  |  |  |  | Yes | S |
| W21C16L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W21C18L04 | P02/AC02 |  |  |  |  | Yes | S |
| W21C20L04 | P02/AC02 |  |  |  |  | Yes | S |
| W21C22L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W21C24L04 | P02/AC02 |  |  |  |  | Yes | S |
| W21C26L04 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC01L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W2AC02L07 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC03L07 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC08L07 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC10L07 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC01L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W2AC02L06 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC03L06 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC08L06 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC10L06 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC01L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W2AC02L05 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 26: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W2AC03L05 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC08L05 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC10L05 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC01L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W2AC02L04 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC03L04 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC08L04 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC10L04 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC02L07 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W2BC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC02L06 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W2BC04L06 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC06L06 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC02L05 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W2BC04L05 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC06L05 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC02L04 | P02/AC02 | P74/AC08 |  |  |  | No | D |
| W2BC04L04 | P02/AC02 |  |  |  |  | Yes | S |
| W2BC06L04 | P02/AC02 |  |  |  |  | Yes | S |
| W2AC03L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 27: TRACKING TABLE OF CRUSHED STONE AND UNTREATED BASE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W12A01L03 | P41/UG02 | P47/UG08 | P43/UG04 | P44/UG05 | P46/UG07 | Yes | S |
| W13A01L03 | P41/UG02 | P47/UG08 | P43/UG04 | P44/UG05 | P46/UG07 | Yes | S |
| W12A01L02 | P41/UG02 | P47/UG08 | P43/UG04 | P44/UG05 | P46/UG07 | Yes | S |
| W13A01L02 | P41/UG02 | P47/UG08 | P43/UG04 | P44/UG05 | P46/UG07 | Yes | S |

TABLE 28: TRACKING TABLE OF SUBGRADE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W12A01L01 | P51/SS01 | P43/SS03 | P52/SS04 | P55/SS05 | P46/SS07 | Yes1 | S |
| W13A01L01 | P51/SS01 | P43/SS03 | P52/SS04 | P55/SS05 | P46/SS07 | Yes1 | S |
| W12A01W01 | P49/SS09 |  |  |  |  | No1 | D |
| W13A01W01 | P49/SS09 |  |  |  |  | No1 | D |

1. The moisture content sample may be disposed after testing.  However, any remaining bulk sample should be stored.

TABLE 29: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE OVERLAY IN THE TURNER FAIRBANKS HIGHWAY RESEARCH CENTER

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| W11H02L07 | P76/AE11 |  |  |  |  | Yes | S |