MANITOBA SPS-10 PROJECT 83AA00

# MATERIALS SAMPLING AND TESTING PLAN

For t0 (At and Immediately After Construction)

Contents

MATERIALS SAMPLING AND TESTING PLAN	0

GENERAL LAYOUT INFORMATION	1

MATERIALS SAMPLING AND FIELD TESTING	4

LABORATORY MATERIALS TESTING	30

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Manitoba SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  These tables indicate transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Additionally, Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION – 83AA00

| Test Section | SHRP ID | Description |
| --- | --- | --- |
| A | 83AA01 | HMA Control Section |
| B | 83AA02 | Warm Mix Section – Foaming Process with 1.0% water |
| C | 83AA61 | Warm Mix Section – Foaming Process and Chemical Additive (0.3% Evotherm plus 1.0% water) |
| D | 83AA03 | Warm Mix Section – Chemical Additive – 0.3% Evotherm |

TABLE 2: TEST SECTION LAYOUT – 83AA00

| Project Begin STA | Project End STA | Experiment Begin STA feet (meter) | Experiment End STA feet (meter) | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | Transition | RD 70 W East Bound |
| 475+00 | 475+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA01 |
| 475+29 | 475+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 475+45 | 476+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 476+97 | 477+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 477+13 | 477+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 477+50 | 480+00 |  |  | Transition |  |
| 480+00 | 480+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA02 |
| 480+29 | 480+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 480+45 | 481+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 481+97 | 482+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 482+13 | 482+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 482+50 | 485+00 |  |  | Transition |  |
| 485+00 | 485+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA61 |
| 485+29 | 485+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 485+45 | 486+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 486+97 | 487+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 487+13 | 487+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 487+50 | 490+00 |  |  | Transition |  |
| 490+00 | 490+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA03 |
| 490+29 | 490+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 490+45 | 491+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 491+97 | 492+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 492+13 | 492+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 492+50 | 495+00 |  |  | Transition |  |

Sampling Area 011

Buffer Area (50 ft)

83AA01

HMA Control Section

Buffer Area (50 ft)

Sampling Area 021

Transition (length variable)

Sampling Area 031

Buffer Area (50 ft)

83AA02

WMA Foaming Process with 1.0% water

Buffer Area (50 ft)

Sampling Area 041

Transition (length variable)

Buffer Area (50 ft)

83AA61

WMA Foaming Process and Chemical Additive (0.3% Evotherm plus 1.0% water)

Buffer Area (50 ft)

Sampling Area 061

Sampling Area 051

800ft

800ft

800ft

500ft

500ft

500ft

100ft

100ft

100ft

100ft

100ft

100ft

EB Traffic

477+50

480+00

475+00

482+50

485+00

487+50

475+45

476+97

480+45

481+97

485+45

486+97

Sampling Area 071

Buffer Area (50 ft)

83AA03

WMA Chemical Additive with 0.3% Evotherm

Buffer Area (50 ft)

Sampling Area 081

Transition (length variable)

800ft

500ft

100ft

100ft

EB Traffic

490+00

492+50

495+00

490+45

491+97

FIGURE 1: MANITOBA SPS-10 PROJECT LAYOUT – 83AA00

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides for the materials sampling and testing activities that will occur in the field at time zero (t0 is at time of construction).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 2 through 9 show the locations for the many samples and tests scheduled.  Figures 2 through 5 show density measurement layouts and Figures 6 through 9 show the material sampling locations for each section as well as the location of DCP testing.

Tables 6 through 10 list the samples acquired from each of the four test sections as well as the asphalt plant.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 11 through 13 list samples to be shipped to the central lab testing contractor laboratory, the LTPP Materials Reference Library (MRL), and the Turner-Fairbank Highway Research Center, respectively.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Manitoba SPS-10, R = “C,” representing north central region)

- C = Construction event (For Manitoba SPS-10, C = 1, representing first constructed SPS-10)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 61

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

Labels and Tags

Each sample shall be labeled before packing in boxes and cartons. As a minimum, the following information shall be included on a tag or label attached to the specimen:

- SPECIMEN ID

- STATE CODE

- SHRP ID

- LOCATION DESIGNATION

- SAMPLE NUMBER

- DATE (mm-dd-yy, sampling date)

- FIELD SET (one digit number which will be 1 for the first round of sampling)

For cores, the HOLE ID shall be written directly on the core.  If the core contains more than one layer, layer boundaries shall be clearly marked, and each layer numbered.  For bulk samples, the SPECIMEN ID shall be written directly on the bag, bucket or can that contains the sample.

Packaging

Suggestions for labeling and combining the samples for shipment are as follows:

- All samples of like material (e.g., asphaltic concrete surface and binder) shall be placed in separate boxes or separate compartments of one box.

- Each sample shall have a label or tag attached that clearly identifies the material.  It is recommended that the label be color-coded by destination (e.g., contract Lab, FHWA lab, MRL, etc.)

- Each core shall be surrounded with "bubble-wrap" or other acceptable cushioning material on all sides within the shipping box.

- All bulk samples shall be marked with two labels or tags. One shall be placed inside the bag and one attached to the outside. A jar sample for moisture testing of each bulk sample shall be placed inside the bulk sample bag.

- All shipping boxes should be wood of suitable grade and construction to withstand shipping and subsequent moving without breakage of the box or damaging of samples.

- All boxes should be adequately secured by nails or screws prior to shipping.

LTPP Field Operations Information Sheets 1 and 2 shall be sent with each shipment of materials samples

TABLE 3: PROJECT LAYER NUMBERING

| Layer No. | Project Layer Code | Thickness | Material Code | Description |
| --- | --- | --- | --- | --- |
| 1 | A |  | 57 | Subgrade - Sand |
| 2 | B | 1.8 - 3.5” (45 – 90 mm) | 46 | Sand Asphalt Base |
| 3 | C | 7.5 - 9.0” (190 – 230 mm) | 01 | Existing AC Pavement - 1” (25mm) to be milled |
| 4 | D |  | 01 |  |
| 5 | E |  | 01 |  |
| 6 | F | 2” (50 mm) | 01 | Experimental AC overlay |

TABLE 4: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
|  | DURING CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC (PLANT) |  |  |
|  | 1-gallon can virgin AC Binder (150/200 Type A) | 1 | H01001 |
|  |  | 1 | H02001 |
|  |  | 10 | H03001, H01002-H03002, H01061-H03061, H01003-H03003 |
|  | 5-gallon bucket combined aggregate | 20 | H04001-H08001, H04002-H08002, H04061-H08061, H04003-H08003 |
|  | 5-gallon bucket RAP | 10 | H09001-H10001, H09002-H11002, H09061-H10061, H09003-H11003 |
|  | 50 lb bulk sample RAP | 1 | H11001 |
|  | 1-gallon chemical additive (0.3% +/- 0.1% Evotherm) | 3 | H11061-H12061, H12003 |
| A. | EXPERIMENTAL AC (FIELD) |  |  |
|  | 5-gallon buckets uncompacted AC mix | 60 | F01001-F15001, F01002-F15002, F01061-F15061, F01003-F15003 |
|  | 12" Core | 8 | A01001-A02001, A01002-A02002, A01061-A02061, A01003-A02003 |
|  | 6" Core | 56 | C01001-C14001, C01002-C14002, C01061-C14061, C01003-C14003 |
| B. | ORIGINAL HMAC LAYERS (3 LAYERS) |  |  |
|  | 12" Core | 2 | A01001, A01003 |
|  | 6" Core | 6 | C01001-C03001, C01003-C03003 |
| C. | SAND ASPHALT BASE |  |  |
|  | 12" Core | 2 | A01001, A01003 |
|  | 6" Core | 6 | C01001-C03001, C01003-C03003 |
| D. | SUBGRADE |  |  |
|  | 150 lb bulk sample | 2 | A01001-A02001, A01003-A02003 |
|  | Moisture content jar sample | 2 | A01001-A02001, A01003-A02003 |

TABLE 5: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | PRE-CONSTRUCTION TESTING |  |  |
| A. | ORIGINAL HMAC |  |  |
|  | Elevation Survey | 4 | All Sections |
|  | POST-CONSTRUCTION TESTING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Elevation Survey | 4 | All Sections |
|  | In situ density measurement | 12 | T01001-T03001, T01002-T03002, T01061-T03061, T01003-T03003 |
|  | Core Examination and Thickness (P01/AC01) | 64 | A01001-A02001, A01002-A02002, A01061-A02061, A01003-A02003, C01001-C14001, C01002-C14002, C01061-C14061, C01003-C14003 |
| B. | ORIGINAL HMAC LAYERS (3 LAYERS) |  |  |
|  | Core Examination and Thickness (P01/AC01) | 8 | A01001, A01003, C01001-C03001, C01003-C03003 |
| C. | SAND ASPHALT BASE |  |  |
|  | Core Examination and Thickness (P01/AC01) | 8 | A01001, A01003, C01001-C03001, C01003-C03003 |
| D. | SUBGRADE |  |  |
|  | DCP | 4 | C14001, C14002, C14061, C14003 |

Section 83AA01 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03001

T02001

T01001

Traffic

FIGURE 2: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 83AA01 MANITOBA SPS-10

Section 83AA02 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03002

T02002

T01002

Traffic

FIGURE 3: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 83AA02 MANITOBA SPS-10

Section 83AA61 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03003

T02003

T01003

Traffic

FIGURE 4: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 83AA61 MANITOBA SPS-10

Section 83AA03 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03061

T02061

T01061

Traffic

FIGURE 5: DENSITY MEASUREMENT LAYOUT FOR TEST SECTION 83AA03 MANITOBA SPS-10

0-70

0-50

Section STA:

Section: 83AA01

Description: HMAC Control Section

Sampling Area: 01

Sampling Interval: t0

Shoulder

C02001

C04001

C06001

C08001

C10001

C12001

C14001

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01001

C03001

C05001

C07001

C09001

C11001

C13001

A01001

A02001

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

6” Core Experimental AC and Original HMAC

6” Core Experimental AC; DCP

12” Core Experimental AC

12” Core Experimental AC; Auger Subgrade

12” Core Experimental AC and Original HMAC; Auger Subgrade

FIGURE 7: SAMPLING AND TESTING PLAN FOR TEST SECTION 83AA01 AT TIME 0 MANITOBA SPS-10

0-70

0-50

Section STA:

Section: 83AA02

Description: WMA Foaming Process with 1.0% water

Sampling Area: 03

Sampling Interval: t0

Shoulder

C02002

C04002

C06002

C08002

C10002

C12002

C14002

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01002

C03002

C05002

C07002

C09002

C11002

C13002

A01002

A02002

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

6” Core Experimental AC and Original HMAC

6” Core Experimental AC; DCP

12” Core Experimental AC

12” Core Experimental AC; Auger Subgrade

12” Core Experimental AC and Original HMAC; Auger Subgrade

FIGURE 8: SAMPLING AND TESTING PLAN FOR TEST SECTION 83AA02 AT TIME 0 MANITOBA SPS-10

0-70

0-50

Section STA:

Section: 83AA61

Description: WMA Foaming Process and Chemical Additive (0.3% Evotherm plus 1.0% water)

Sampling Area: 05

Sampling Interval: t0

Shoulder

C02061

C04061

C06061

C08061

C10061

C12061

C14061

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01061

C03061

C05061

C07061

C09061

C11061

C13061

A01061

A02061

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

6” Core Experimental AC and Original HMAC

6” Core Experimental AC; DCP

12” Core Experimental AC

12” Core Experimental AC; Auger Subgrade

12” Core Experimental AC and Original HMAC; Auger Subgrade

FIGURE 9: SAMPLING AND TESTING PLAN FOR TEST SECTION 83AA61 AT TIME 0 MANITOBA SPS-10

0-70

0-50

Section STA:

Section: 83AA03

Description: WMA Chemical Additive with 0.3% Evotherm

Sampling Area: 07

Sampling Interval: t0

Shoulder

C02003

C04003

C06003

C08003

C10003

C12003

C14003

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01003

C03003

C05003

C07003

C09003

C11003

C13003

A01003

A02003

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

6” Core Experimental AC and Original HMAC

6” Core Experimental AC; DCP

12” Core Experimental AC

12” Core Experimental AC; Auger Subgrade

12” Core Experimental AC and Original HMAC; Auger Subgrade

FIGURE 10: SAMPLING AND TESTING PLAN FOR TEST SECTION 83AA03 AT TIME 0 MANITOBA SPS-10

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 83AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01001 | 6 | BA01001 | C11A01L06 | 12" Core |
|  | 5 |  | C11A01L05 |  |
|  | 4 |  | C11A01L04 |  |
|  | 3 |  | C11A01L03 |  |
|  | 2 | BT01001 | C11A01L02 |  |
|  | 1 | BS01001 | C11A01L01 | 75 lb. Bulk Sample |
|  |  | MS01001 | C11AM1L01 | Moisture Content Jar Sample |
| A02001 | 6 | BA02001 | C11A02L06 | 12" Core |
|  | 1 | BS02001 | C11A02L01 | 75 lb. Bulk Sample |
|  |  | MS02001 | C11AM2L01 | Moisture Content Jar Sample |
| C01001 | 6 | CA01001 | C11C01L06 | 6" Core |
|  | 5 |  | C11C01L05 |  |
|  | 4 |  | C11C01L04 |  |
|  | 3 |  | C11C01L03 |  |
|  | 2 | CT01001 | C11C01L02 |  |
| C02001 | 6 | CA02001 | C11C02L06 | 6" Core |
|  | 5 |  | C11C02L05 |  |
|  | 4 |  | C11C02L04 |  |
|  | 3 |  | C11C02L03 |  |
|  | 2 | CT02001 | C11C02L02 |  |
| C03001 | 6 | CA03001 | C11C03L06 | 6" Core |
|  | 5 |  | C11C03L05 |  |
|  | 4 |  | C11C03L04 |  |
|  | 3 |  | C11C03L03 |  |
|  | 2 | CT01001 | C11C03L02 | Core damaged – do not log and send to lab |
| C04001 | 6 | CA04001 | C11C04L06 | 6" Core |
| C05001 | 6 | CA05001 | C11C05L06 | 6" Core |
| C06001 | 6 | CA06001 | C11C06L06 | 6" Core |
| C07001 | 6 | CA07001 | C11C07L06 | 6" Core |
| C08001 | 6 | CA08001 | C11C08L06 | 6" Core |
| C09001 | 6 | CA09001 | C11C09L06 | 6" Core |
| C10001 | 6 | CA10001 | C11C10L06 | 6" Core |
| C11001 | 6 | CA11001 | C11C11L06 | 6" Core |
| C12001 | 6 | CA12001 | C11C12L06 | 6" Core |
| C13001 | 6 | CA13001 | C11C13L06 | 6" Core |
| C14001 | 6 | CA14001 | C11C14L06 | 6" Core |

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 83AA01 (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| F01001 F02001 F03001 F04001 F05001 F06001 F07001 F08001 F09001 F10001 F11001 F12001 F13001 F14001 F15001 | 6 | BA03001 BA04001 BA05001 BA06001 BA07001 BA08001 BA09001 BA10001 BA11001 BA12001 BA13001 BA14001 BA15001 BA16001 BA17001 | C11F01L06 C11F02L06 C11F03L06 C11F04L06 C11F05L06 C11F06L06 C11F07L06 C11F08L06 C11F09L06 C11F10L06 C11F11L06 C11F12L06 C11F13L06 C11F14L06 C11F15L06 | 15 5-gallon buckets uncompacted AC mix |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 83AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01002 | 6 | BA01002 | C12A01L06 | 12" Core |
| A02002 | 6 | BA02002 | C12A02L06 | 12" Core |
| C01002 | 6 | CA01002 | C12C01L06 | 6" Core |
| C02002 | 6 | CA02002 | C12C02L06 | 6" Core |
| C03002 | 6 | CA03002 | C12C03L06 | 6" Core |
| C04002 | 6 | CA04002 | C12C04L06 | 6" Core |
| C05002 | 6 | CA05002 | C12C05L06 | 6" Core |
| C06002 | 6 | CA06002 | C12C06L06 | 6" Core |
| C07002 | 6 | CA07002 | C12C07L06 | 6" Core |
| C08002 | 6 | CA08002 | C12C08L06 | 6" Core |
| C09002 | 6 | CA09002 | C12C09L06 | 6" Core |
| C10002 | 6 | CA10002 | C12C10L06 | 6" Core |
| C11002 | 6 | CA11002 | C12C11L06 | 6" Core |
| C12002 | 6 | CA12002 | C12C12L06 | 6" Core |
| C13002 | 6 | CA13002 | C12C13L06 | 6" Core |
| C14002 | 6 | CA14002 | C12C14L06 | 6" Core |
| F01002 F02002 F03002 F04002 F05002 F06002 F07002 F08002 F09002 F10002 F11002 F12002 F13002 F14002 F15002 | 6 | BA03002 BA04002 BA05002 BA06002 BA07002 BA08002 BA09002 BA10002 BA11002 BA12002 BA13002 BA14002 BA15002 BA16002 BA17002 | C12F01L06 C12F02L06 C12F03L06 C12F04L06 C12F05L06 C12F06L06 C12F07L06 C12F08L06 C12F09L06 C12F10L06 C12F11L06 C12F12L06 C12F13L06 C12F14L06 C12F15L06 | 15 5-gallon buckets uncompacted AC mix |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 83AA61

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01061 | 6 | BA01061 | C1AA01L06 | 12" Core |
| A02061 | 6 | BA02061 | C1AA02L06 | 12" Core |
| C01061 | 6 | CA01061 | C1AC01L06 | 6" Core |
| C02061 | 6 | CA02061 | C1AC02L06 | 6" Core |
| C03061 | 6 | CA03061 | C1AC03L06 | 6" Core |
| C04061 | 6 | CA04061 | C1AC04L06 | 6" Core |
| C05061 | 6 | CA05061 | C1AC05L06 | 6" Core |
| C06061 | 6 | CA06061 | C1AC06L06 | 6" Core |
| C07061 | 6 | CA07061 | C1AC07L06 | 6" Core |
| C08061 | 6 | CA08061 | C1AC08L06 | 6" Core |
| C09061 | 6 | CA09061 | C1AC09L06 | 6" Core |
| C10061 | 6 | CA10061 | C1AC10L06 | 6" Core |
| C11061 | 6 | CA11061 | C1AC11L06 | 6" Core |
| C12061 | 6 | CA12061 | C1AC12L06 | 6" Core |
| C13061 | 6 | CA13061 | C1AC13L06 | 6" Core |
| C14061 | 6 | CA14061 | C1AC14L06 | 6" Core |
| F01061 F02061 F03061 F04061 F05061 F06061 F07061 F08061 F09061 F10061 F11061 F12061 F13061 F14061 F15061 | 6 | BA03061 BA04061 BA05061 BA06061 BA07061 BA08061 BA09061 BA10061 BA11061 BA12061 BA13061 BA14061 BA15061 BA16061 BA17061 | C1AF01L06 C1AF02L06 C1AF03L06 C1AF04L06 C1AF05L06 C1AF06L06 C1AF07L06 C1AF08L06 C1AF09L06 C1AF10L06 C1AF11L06 C1AF12L06 C1AF13L06 C1AF14L06 C1AF15L06 | 15 5-gallon buckets uncompacted AC mix |

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 83AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01003 | 6 | BA01003 | C13A01L06 | 12" Core |
|  | 5 |  | C13A01L05 |  |
|  | 4 |  | C13A01L04 |  |
|  | 3 |  | C13A01L03 |  |
|  | 2 | BT01003 | C13A01L02 |  |
|  | 1 | BS01003 | C13A01L01 | 75 lb. Bulk Sample |
|  |  | MS01003 | C13AM1L01 | Moisture Content Jar Sample |
| A02003 | 6 | BA02003 | C13A02L06 | 12" Core |
|  | 1 | BS02003 | C13A02L01 | 75 lb. Bulk Sample |
|  |  | MS02003 | C13AM2L01 | Moisture Content Jar Sample |
| C01003 | 6 | CA01003 | C13C01L06 | 6" Core |
|  | 5 |  | C13C01L05 |  |
|  | 4 |  | C13C01L04 |  |
|  | 3 |  | C13C01L03 |  |
|  | 2 | CT01003 | C13C01L02 |  |
| C02003 | 6 | CA02003 | C13C02L06 | 6" Core |
|  | 5 |  | C13C02L05 |  |
|  | 4 |  | C13C02L04 |  |
|  | 3 |  | C13C02L03 |  |
|  | 2 | CT02003 | C13C02L02 | Core partially recovered |
| C03003 | 6 | CA03003 | C13C03L06 | 6" Core |
|  | 5 |  | C13C03L05 |  |
|  | 4 |  | C13C03L04 |  |
|  | 3 |  | C13C03L03 |  |
|  | 2 | CT01003 | C13C03L02 |  |
| C04003 | 6 | CA04003 | C13C04L06 | 6" Core |
| C05003 | 6 | CA05003 | C13C05L06 | 6" Core |
| C06003 | 6 | CA06003 | C13C06L06 | 6" Core |
| C07003 | 6 | CA07003 | C13C07L06 | 6" Core |
| C08003 | 6 | CA08003 | C13C08L06 | 6" Core |
| C09003 | 6 | CA09003 | C13C09L06 | 6" Core |
| C10003 | 6 | CA10003 | C13C10L06 | 6" Core |
| C11003 | 6 | CA11003 | C13C11L06 | 6" Core |
| C12003 | 6 | CA12003 | C13C12L06 | 6" Core |
| C13003 | 6 | CA13003 | C13C13L06 | 6" Core |
| C14003 | 6 | CA14003 | C13C14L06 | 6" Core |

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 83AA03 (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| F01003 F02003 F03003 F04003 F05003 F06003 F07003 F08003 F09003 F10003 F11003 F12003 F13003 F14003 F15003 | 6 | BA03003 BA04003 BA05003 BA06003 BA07003 BA08003 BA09003 BA10003 BA11003 BA12003 BA13003 BA14003 BA15003 BA16003 BA17003 | C13F01L06 C13F02L06 C13F03L06 C13F04L06 C13F05L06 C13F06L06 C13F07L06 C13F08L06 C13F09L06 C13F10L06 C13F11L06 C13F12L06 C13F13L06 C13F14L06 C13F15L06 | 15 5-gallon buckets uncompacted AC mix |

TABLE 10: SAMPLES ACQUIRED FROM PLANT

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| H01001 | 6 | BC01001 | C11H01L06 | 1 1-gallon can virgin AC Binder (150/200 Type A) |
| H02001 | 6 | BC02001 | C11H02L06 | 1 1-gallon can virgin AC Binder (150/200 Type A) |
| H03001 H01002 H02002 H03002 H01061 H02061 H03061 H01003 H02003 H03003 | 6 | BC03001 BC01002 BC02002 BC03002 BC01061 BC02061 BC03061 BC01003 BC02003 BC03003 | C11H03L06 C12H01L06 C12H02L06 C12H03L06 C1AH01L06 C1AH02L06 C1AH03L06 C13H01L06 C13H02L06 C13H03L06 | 10 1-gallon cans virgin AC Binder (150/200 Type A) |
| H04001 H05001 H06001 H07001 H08001 H04002 H05002 H06002 H07002 H08002 H04061 H05061 H06061 H07061 H08061 H04003 H05003 H06003 H07003 H08003 | 6 | BU01001 BU02001 BU03001 BU04001 BU05001 BU01002 BU02002 BU03002 BU04002 BU05002 BU01061 BU02061 BU03061 BU04061 BU05061 BU01003 BU02003 BU03003 BU04003 BU05003 | C11H04L06 C11H05L06 C11H06L06 C11H07L06 C11H08L06 C12H04L06 C12H05L06 C12H06L06 C12H07L06 C12H08L06 C1AH04L06 C1AH05L06 C1AH06L06 C1AH07L06 C1AH08L06 C13H04L06 C13H05L06 C13H06L06 C13H07L06 C13H08L06 | 20 5-gallon buckets combined aggregate |

TABLE 10: SAMPLES ACQUIRED FROM PLANT (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| H09001 H10001 H09002 H10002 H11002 H09061 H10061 H09003 H10003 H11003 | 6 | BR01001 BR02001 BR01002 BR02002 BR03002 BR01061 BR02061 BR01003 BR02003 BR03003 | C11H09L06 C11H10L06 C12H09L06 C12H10L06 C12H11L06 C1AH09L06 C1AH10L06 C13H09L06 C13H10L06 C13H11L06 | 10 5-gallon buckets RAP |
| H11061 H12061 H12003 | 6 | BW01061 BW02061 BW01003 | C1AH11L06 C1AH12L06 C13H12L06 | 3 gallon chemical additive (0.3% +/- 0.1% Evotherm) in manufacturer prescribed containers, with MSDS |
| H11001 | 6 | BR03001 | C11H11L06 | 50 lb. Bulk Sample RAP |

TABLE 11: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C11A01L06 | 12" Core |
| C11A02L06 | 12" Core |
| C12A01L06 | 12" Core |
| C12A02L06 | 12" Core |
| C1AA01L06 | 12" Core |
| C1AA02L06 | 12" Core |
| C13A01L06 | 12" Core |
| C13A02L06 | 12" Core |
| C11C01L06 | 6" Core |
| C11C02L06 | 6" Core |
| C11C03L06 | 6" Core |
| C11C04L06 | 6" Core |
| C11C05L06 | 6" Core |
| C11C06L06 | 6" Core |
| C11C07L06 | 6" Core |
| C11C08L06 | 6" Core |
| C11C09L06 | 6" Core |
| C11C10L06 | 6" Core |
| C12C01L06 | 6" Core |
| C12C02L06 | 6" Core |
| C12C03L06 | 6" Core |
| C12C04L06 | 6" Core |
| C12C05L06 | 6" Core |
| C12C06L06 | 6" Core |
| C12C07L06 | 6" Core |
| C12C08L06 | 6" Core |
| C12C09L06 | 6" Core |
| C12C10L06 | 6" Core |
| C13C01L06 | 6" Core |
| C13C02L06 | 6" Core |
| C13C03L06 | 6" Core |
| C13C04L06 | 6" Core |
| C13C05L06 | 6" Core |

TABLE 11: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID |  | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| C13C06L06 |  | 6" Core |
| C13C07L06 |  | 6" Core |
| C13C08L06 |  | 6" Core |
| C13C09L06 |  | 6" Core |
| C13C10L06 |  | 6" Core |
| C1AC01L06 |  | 6" Core |
| C1AC02L06 |  | 6" Core |
| C1AC03L06 |  | 6" Core |
| C1AC04L06 |  | 6" Core |
| C1AC05L06 |  | 6" Core |
| C1AC06L06 |  | 6" Core |
| C1AC07L06 |  | 6" Core |
| C1AC08L06 |  | 6" Core |
| C1AC09L06 |  | 6" Core |
| C1AC10L06 |  | 6" Core |
| C11H01L06 |  | 1 1-gallon can of virgin AC Binder (150/200 Type A) |
| C11H11L06 |  | 50 lb. Bulk Sample RAP |
| Original HMAC |  |  |  |
| C11A01L05 | 12" Core |  |  |
| C13A01L05 | 12" Core |  |  |
| C11C01L05 | 6" Core |  |  |
| C11C02L05 | 6" Core |  |  |
| C11C03L05 | 6" Core |  |  |
| C13C01L05 | 6" Core |  |  |
| C13C02L05 | 6" Core |  |  |
| C13C03L05 | 6" Core |  |  |

TABLE 11: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID |  | Type of Sample |
| --- | --- | --- |
| Original HMAC |  |  |  |
| C11A01L04 | 12" Core |  |  |
| C13A01L04 | 12" Core |  |  |
| C11C01L04 | 6" Core |  |  |
| C11C02L04 | 6" Core |  |  |
| C11C03L04 | 6" Core |  |  |
| C13C01L04 | 6" Core |  |  |
| C13C02L04 | 6" Core |  |  |
| C13C03L04 | 6" Core |  |  |
| Original HMAC |  |  |  |
| C11A01L03 | 12" Core |  |  |
| C13A01L03 | 12" Core |  |  |
| C11C01L03 | 6" Core |  |  |
| C11C02L03 | 6" Core |  |  |
| C11C03L03 | 6" Core |  |  |
| C13C01L03 | 6" Core |  |  |
| C13C02L03 | 6" Core |  |  |
| C13C03L03 | 6" Core |  |  |
| Original Sand Asphalt Base |  |  |  |
| C11A01L02 | 12" Core |  |  |
| C13A01L02 | 12" Core |  |  |
| C11C01L02 | 6" Core |  |  |
| C11C02L02 | 6" Core |  |  |
| C11C03L02 | 6" Core (Core damaged – do not log and send to lab) |  |  |
| C13C01L02 | 6" Core |  |  |
| C13C02L02 | 6" Core (Core partially recovered) |  |  |
| C13C03L02 | 6" Core |  |  |
| Subgrade |  |  |  |
| C11A01L01 | 75 lb. Bulk Sample |  |  |
| C11A02L01 | 75 lb. Bulk Sample |  |  |
| C13A01L01 | 75 lb. Bulk Sample |  |  |
| C13A02L01 | 75 lb. Bulk Sample |  |  |
| C11AM1L01 | Moisture Content Jar Sample |  |  |
| C11AM2L01 | Moisture Content Jar Sample |  |  |
| C13AM1L01 | Moisture Content Jar Sample |  |  |
| C13AM2L01 | Moisture Content Jar Sample |  |  |

TABLE 12: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C11C11L06 | 6" Core |
| C11C12L06 | 6" Core |
| C11C13L06 | 6" Core |
| C11C14L06 | 6" Core |
| C12C11L06 | 6" Core |
| C12C12L06 | 6" Core |
| C12C13L06 | 6" Core |
| C12C14L06 | 6" Core |
| C1AC11L06 | 6" Core |
| C1AC12L06 | 6" Core |
| C1AC13L06 | 6" Core |
| C1AC14L06 | 6" Core |
| C13C11L06 | 6" Core |
| C13C12L06 | 6" Core |
| C13C13L06 | 6" Core |
| C13C14L06 | 6" Core |
| C11H04L06 | 20 5-gallon buckets combined aggregate |
| C11H05L06 |  |
| C11H06L06 |  |
| C11H07L06 |  |
| C11H08L06 |  |
| C12H04L06 |  |
| C12H05L06 |  |
| C12H06L06 |  |
| C12H07L06 |  |
| C12H08L06 |  |
| C1AH04L06 |  |
| C1AH05L06 |  |
| C1AH06L06 |  |
| C1AH07L06 |  |
| C1AH08L06 |  |
| C13H04L06 |  |
| C13H05L06 |  |
| C13H06L06 |  |
| C13H07L06 |  |
| C13H08L06 |  |

TABLE 12: SAMPLES TO BE SHIPPED TO THE LTPP MRL (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C11H03L06 | 10 1-gallon can of virgin AC Binder (150/200 Type A) |
| C12H01L06 |  |
| C12H02L06 |  |
| C12H03L06 |  |
| C1AH01L06 |  |
| C1AH02L06 |  |
| C1AH03L06 |  |
| C13H01L06 |  |
| C13H02L06 |  |
| C13H03L06 |  |
| C11H09L06 | 10 5-gallon buckets RAP |
| C11H10L06 |  |
| C12H09L06 |  |
| C12H10L06 |  |
| C12H11L06 |  |
| C1AH09L06 |  |
| C1AH10L06 |  |
| C13H09L06 |  |
| C13H10L06 |  |
| C13H11L06 |  |
| C11F01L06 | 15 5-gallon buckets uncompacted AC mix |
| C11F02L06 |  |
| C11F03L06 |  |
| C11F04L06 |  |
| C11F05L06 |  |
| C11F06L06 |  |
| C11F07L06 |  |
| C11F08L06 |  |
| C11F09L06 |  |
| C11F10L06 |  |
| C11F11L06 |  |
| C11F12L06 |  |
| C11F13L06 |  |
| C11F14L06 |  |
| C11F15L06 |  |

TABLE 12: SAMPLES TO BE SHIPPED TO THE LTPP MRL (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C12F01L06 | 15 5-gallon buckets uncompacted AC mix |
| C12F02L06 |  |
| C12F03L06 |  |
| C12F04L06 |  |
| C12F05L06 |  |
| C12F06L06 |  |
| C12F07L06 |  |
| C12F08L06 |  |
| C12F09L06 |  |
| C12F10L06 |  |
| C12F11L06 |  |
| C12F12L06 |  |
| C12F13L06 |  |
| C12F14L06 |  |
| C12F15L06 |  |
| C13F01L06 | 15 5-gallon buckets uncompacted AC mix |
| C13F02L06 |  |
| C13F03L06 |  |
| C13F04L06 |  |
| C13F05L06 |  |
| C13F06L06 |  |
| C13F07L06 |  |
| C13F08L06 |  |
| C13F09L06 |  |
| C13F10L06 |  |
| C13F11L06 |  |
| C13F12L06 |  |
| C13F13L06 |  |
| C13F14L06 |  |
| C13F15L06 |  |

TABLE 12: SAMPLES TO BE SHIPPED TO THE LTPP MRL (Continued)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C1AF01L06 | 15 5-gallon buckets uncompacted AC mix |
| C1AF02L06 |  |
| C1AF03L06 |  |
| C1AF04L06 |  |
| C1AF05L06 |  |
| C1AF06L06 |  |
| C1AF07L06 |  |
| C1AF08L06 |  |
| C1AF09L06 |  |
| C1AF10L06 |  |
| C1AF11L06 |  |
| C1AF12L06 |  |
| C1AF13L06 |  |
| C1AF14L06 |  |
| C1AF15L06 |  |
| C1AH11L06 | 3 1-gallon chemical additive (0.3% +/- 0.1% Evotherm) in manufacturer prescribed containers, with MSDS |
| C1AH12L06 |  |
| C13H12L06 |  |

TABLE 13: SAMPLES TO BE SHIPPED TO THE TURNER FAIRBANKS RESEARCH CENTER (TFHRC)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC Layer |  |
| C11H02L06 | 1 1-gallon can of virgin AC Binder (150/200 Type A) |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Manitoba SPS-10 projects.  The previous section ended with lists of samples to be shipped to each of the two laboratories, the central lab testing contractor laboratory and the Turner-Fairbank Highway Research center.  In this section, the tests to be performed on each sample are listed.

Table 14 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Tables 15 and 16 provide new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Tables 17 through 21 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a particular test is complete.

TABLE 14: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 40 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 4 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 5 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 8 | X |  |
|  | Hamburg Wheel Track | AC09 | P75 | 4 | X |  |
|  | Fenix Fracture Energy | AC10 | P79 | 4 | X |  |
|  | Specific Gravity at 60 ° F | AE03 | P23 | 6 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 12 | X |  |
|  | Bending Beam Rheometer (BBR) Test | AE08 | P28 | 6 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 6 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 5 | X |  |
|  | PPA and Motor Oil Test | AE11 | P76 | 1 |  | X |
| B. | ORIGINAL HMAC (3 LAYERS) |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 18 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 6 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 6 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 12 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 6 | X |  |
|  | Bending Beam Rheometer (BBR) Test | AE08 | P28 | 6 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 6 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 6 | X |  |

TABLE 14: SPS-10 LABORATORY TESTING PLANS (Continued)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| C. | SAND ASPHALT BASE |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 6 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 2 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 2 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 4 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 2 | X |  |
|  | Bending Beam Rheometer (BBR) Test | AE08 | P28 | 2 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 2 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 2 | X |  |
| D. | SUBGRADE |  |  |  |  |  |
|  | Sieve Analysis | SS01 | P51 | 2 | X |  |
|  | Atterberg Limits | SS03 | P43 | 2 | X |  |
|  | Classification and Description | SS04 | P52 | 2 | X |  |
|  | Standard Proctor | SS05 | P55 | 2 | X |  |
|  | Resilient Modulus | SS07 | P46 | 2 | X |  |
|  | Natural Moisture Content | SS09 | P49 | 2 | X |  |

TABLE 15: ORIGINAL AND COMBINED SPECIMEN DESCRIPTIONS

| Description Type | Status |  |  |
| --- | --- | --- | --- |
|  | Original |  | Combined1 |
| Sample No. | BA01001 | BA02001 | BAX1001 |
| Specimen ID | C11A01L06 | C11A02L06 | C11A01M06 |
| Sample No. | BS01001 | BS02001 | BSX1001 |
| Specimen ID | C11A01L01 | C11A02L01 | C11A01M01 |
| Sample No. | MS01001 | MS02001 | MSX1001 |
| Specimen ID | C11AM1L01 | C11AM2L01 | C11AM1M01 |
| Sample No. | BA01002 | BA02002 | BAX1002 |
| Specimen ID | C12A01L06 | C12A02L06 | C12A01M06 |
| Sample No. | BA01003 | BA02003 | BAX1003 |
| Specimen ID | C13A01L06 | C13A02L06 | C13A01M06 |
| Sample No. | BS01003 | BS02003 | BSX1003 |
| Specimen ID | C13A01L01 | C13A02L01 | C13A01M01 |
| Sample No. | MS01003 | MS02003 | MSX1003 |
| Specimen ID | C13AM1L01 | C13AM2L01 | C13AM1M01 |
| Sample No. | BA01061 | BA02061 | BAX1061 |
| Specimen ID | C1AA01L06 | C1AA02L06 | C1AA01M06 |

1. Sample No.:  After combination, the third character is changed to “X”, and the fourth character is assigned numerically. The other five characters follow the original format.  Specimen ID:  After combination “L” is changed to “M”.

TABLE 16: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BAX1001 | BAE1001 |
|  | Specimen ID | C11A01M06 | C11A01A06 |
|  | Specimen ID | C11A01L05 | C11A01M05 |
|  | Specimen ID | C11A01L04 | C11A01M04 |
|  | Specimen ID | C11A01L03 | C11A01M03 |
|  | Sample No. | BT01001 | BTE1001 |
|  | Specimen ID | C11A01L02 | C11A01M02 |
|  | Sample No. | BAX1002 | BAE1002 |
|  | Specimen ID | C12A01M06 | C12A01A06 |
|  | Sample No. | BAX1003 | BAE1003 |
|  | Specimen ID | C13A01M06 | C13A01A06 |
|  | Specimen ID | C13A01L05 | C13A01M05 |
|  | Specimen ID | C13A01L04 | C13A01M04 |
|  | Specimen ID | C13A01L03 | C13A01M03 |
|  | Sample No. | BT01003 | BTE1003 |
|  | Specimen ID | C13A01L02 | C13A01M02 |
|  | Sample No. | BAX1061 | BAE1061 |
|  | Specimen ID | C1AA01M06 | C1AA01A06 |
|  | Sample No. | BR03001 | BRE1001 |
|  | Specimen ID | C11H11L06 | C11H11M06 |
| PAV | Sample No. | BAE1001 | BAP1001 |
|  | Specimen ID | C11A01A06 | C11A01B06 |
|  | Sample No. | BAE1002 | BAP1002 |
|  | Specimen ID | C12A01A06 | C12A01B06 |
|  | Sample No. | BAE1003 | BAP1003 |
|  | Specimen ID | C13A01A06 | C13A01B06 |
|  | Sample No. | BAE1061 | BAP1061 |
|  | Specimen ID | C1AA01A06 | C1AA01B06 |
| RTFO | Sample No. | BC01001 | BCR1001 |
|  | Specimen ID | C11H01L06 | C11H01M06 |
| RTFO + PAV | Sample No. | BC01001 | BCZ1001 |
|  | Specimen ID | C11H01L06 | C11H01A06 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C11A01M06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C12A01M06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C13A01M06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C1AA01M06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C11A01A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C12A01A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C13A01A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C1AA01A06 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| C11A01B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C12A01B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C13A01B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C1AA01B06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C11C01L06 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C11C02L06 | P02/AC02 |  |  |  |  | No | D |
| C11C03L06 | P02/AC02 |  |  |  |  | No | D |
| C11C04L06 | P02/AC02 |  |  |  |  | Yes | S |
| C11C05L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C11C06L06 | P02/AC02 |  |  |  |  | Yes | S |
| C11C07L06 | P02/AC02 |  |  |  |  | Yes | S |
| C11C08L06 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C11C09L06 | P02/AC02 |  |  |  |  | No | D |
| C11C10L06 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C12C01L06 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C12C02L06 | P02/AC02 |  |  |  |  | No | D |
| C12C03L06 | P02/AC02 |  |  |  |  | No | D |
| C12C04L06 | P02/AC02 |  |  |  |  | Yes | S |
| C12C05L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C12C06L06 | P02/AC02 |  |  |  |  | Yes | S |
| C12C07L06 | P02/AC02 |  |  |  |  | Yes | S |
| C12C08L06 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C12C09L06 | P02/AC02 |  |  |  |  | No | D |
| C12C10L06 | P02/AC02 |  |  |  |  | Yes | S |
| C13C01L06 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C13C02L06 | P02/AC02 |  |  |  |  | No | D |
| C13C03L06 | P02/AC02 |  |  |  |  | No | D |
| C13C04L06 | P02/AC02 |  |  |  |  | Yes | S |
| C13C05L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C13C06L06 | P02/AC02 |  |  |  |  | Yes | S |
| C13C07L06 | P02/AC02 |  |  |  |  | Yes | S |
| C13C08L06 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C13C09L06 | P02/AC02 |  |  |  |  | No | D |
| C13C10L06 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 17: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C1AC01L06 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| C1AC02L06 | P02/AC02 |  |  |  |  | No | D |
| C1AC03L06 | P02/AC02 |  |  |  |  | No | D |
| C1AC04L06 | P02/AC02 |  |  |  |  | Yes | S |
| C1AC05L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C1AC06L06 | P02/AC02 |  |  |  |  | Yes | S |
| C1AC07L06 | P02/AC02 |  |  |  |  | Yes | S |
| C1AC08L06 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| C1AC09L06 | P02/AC02 |  |  |  |  | No | D |
| C1AC10L06 | P02/AC02 |  |  |  |  | Yes | S |
| C11H01L06 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| C11H01M06 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| C11H01A06 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| C11H11L06 | P04/AC04 |  |  |  |  | Yes | E, S |
| C11H11M06 | P23/AE03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 | No | D |

1. Next Process  	D 	Remaining sample should be disposed
		S 	Remaining sample should be stored
		C	Remaining sample will be combined with another sample
		E 	Perform further testing on extracted sample
		P 	Perform further testing with PAV
		R 	Perform further testing with RFTO
		R+P  	Perform further testing with RTFO + PAV

TABLE 18: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CLTC LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C11A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C13A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C11A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C13A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C11C01L05 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C11C02L05 | P02/AC02 |  |  |  |  | Yes | S |
| C11C03L05 | P02/AC02 |  |  |  |  | Yes | S |
| C13C01L05 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C13C02L05 | P02/AC02 |  |  |  |  | Yes | S |
| C13C03L05 | P02/AC02 |  |  |  |  | Yes | S |
| C11A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C13A01L04 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C11A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C13A01M04 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C11C01L04 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C11C02L04 | P02/AC02 |  |  |  |  | Yes | S |
| C11C03L04 | P02/AC02 |  |  |  |  | Yes | S |
| C13C01L04 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C13C02L04 | P02/AC02 |  |  |  |  | Yes | S |
| C13C03L04 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 18: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CLTC LAB (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C11A01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C13A01L03 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C11A01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C13A01M03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C11C01L03 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C11C02L03 | P02/AC02 |  |  |  |  | Yes | S |
| C11C03L03 | P02/AC02 |  |  |  |  | Yes | S |
| C13C01L03 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C13C02L03 | P02/AC02 |  |  |  |  | Yes | S |
| C13C03L03 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 19: TRACKING TABLE OF SAND ASPHALT BASE IN THE CLTC LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C11A01L02 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C13A01L02 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| C11A01M02 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C13A01M02 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| C11C01L02 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C11C02L02 | P02/AC02 |  |  |  |  | Yes | S |
| C11C03L02 | P02/AC02 |  |  |  |  | Yes | Damaged |
| C13C01L02 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C13C02L02 | P02/AC02 |  |  |  |  | Yes | S (Partial) |
| C13C03L02 | P02/AC02 |  |  |  |  | Yes | S |

Table 20: TRACKING TABLE OF SUBGRADE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C11A01M01 | P51/SS01 | P43/SS03 | P52/SS04 | P46/SS07 | P55/SS05 | Yes1 | S |
| C13A01M01 | P51/SS01 | P43/SS03 | P52/SS04 | P46/SS07 | P55/SS05 | Yes1 | S |
| C11AM1M01 | P49/SS09 |  |  |  |  | No1 | D |
| C13AM1M01 | P49/SS09 |  |  |  |  | No1 | D |

1. The moisture content sample may be disposed after testing.  However, any remaining bulk sample should be stored.

TABLE 21: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE OVERLAY IN THE TFHRC LAB

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| C11H02L06 | P76/AE11 |  |  |  |  | Yes | S |

1. Next Process  	D 	Remaining sample should be disposed
		S 	Remaining sample should be stored
		C	Remaining sample will be combined with another sample
		E 	Perform further testing on extracted sample
		P 	Perform further testing with PAV
		R 	Perform further testing with RFTO
		R+P  	Perform further testing with RTFO + PAV