MANITOBA SPS-10 PROJECT 83AA00

# MATERIALS SAMPLING AND TESTING PLAN

# For t2 (12 Months After Construction)

Contents

MATERIALS SAMPLING AND TESTING PLAN	0

GENERAL LAYOUT INFORMATION	1

MATERIALS SAMPLING AND FIELD TESTING	4

LABORATORY MATERIALS TESTING	15

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Manitoba SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  These tables indicate transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Figure 1 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION – 83AA00

| SHRP ID | Description |
| --- | --- |
| 83AA01 | HMA Control Section |
| 83AA02 | Warm Mix Section – Foaming Process with 1.0% water |
| 83AA61 | Warm Mix Section – Foaming Process and Chemical Additive (0.3% Evotherm® plus 1.0% water) |
| 83AA03 | Warm Mix Section – Chemical Additive – 0.3% Evotherm® |

TABLE 2: TEST SECTION LAYOUT – 83AA00

| Project Begin STA | Project End STA | Experiment Begin STA feet (meter) | Experiment End STA feet (meter) | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | Transition | RD 70 W East Bound |
| 475+00 | 475+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA01 |
| 475+29 | 475+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 475+45 | 476+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 476+97 | 477+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 477+13 | 477+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 477+50 | 480+00 |  |  | Transition |  |
| 480+00 | 480+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA02 |
| 480+29 | 480+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 480+45 | 481+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 481+97 | 482+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 482+13 | 482+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 482+50 | 485+00 |  |  | Transition |  |
| 485+00 | 485+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA61 |
| 485+29 | 485+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 485+45 | 486+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 486+97 | 487+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 487+13 | 487+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 487+50 | 490+00 |  |  | Transition |  |
| 490+00 | 490+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA03 |
| 490+29 | 490+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 490+45 | 491+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 491+97 | 492+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 492+13 | 492+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 492+50 | 495+00 |  |  | Transition |  |

472+44

Sampling Area 011 – 100ft (30.5m)

Buffer Area – 50ft (15.25m)

83AA01

HMA Control Section

500ft (152.5m)

Buffer Area – 50ft (15.25m)

Sampling Area 021 – 100ft (30.5m)

Transition (length variable)

Sampling Area 031 – 100ft (30.5m)

Buffer Area – 50ft (15.25m)

83AA02

WMA Foaming Process with 1.0% water

500ft (152.5m)

Buffer Area – 50ft (15.25m)

Sampling Area 041 – 100ft (30.5m)

Transition (length variable)

Buffer Area – 50ft (15.25m)

83AA61

WMA Foaming Process and Chemical Additive (0.3% Evotherm®  plus 1.0% water)

500ft (152.5m)

Buffer Area – 50ft (15.25m)

Sampling Area 061 – 100ft (30.5m)

Sampling Area 051 – 100ft (30.5m)

800ft (244m)

EB Traffic

477+44

480+00

475+00

482+44

485+00

487+44

475+45

476+97

480+45

481+97

485+45

486+97

800ft (244m)

800ft (244m)

Transition Area – 840ft (256m)

Transition - 840ft (256m)

Sampling Area 071 – 100ft (30.5m)

Buffer Area – 50ft (15.25m)

83AA03

WMA Chemical Additive with 0.3% Evotherm®

500ft (152.5m)

Buffer Area (50 ft)

Sampling Area 081 – 100ft (30.5m)

Transition Area – 840ft (256m)

EB Traffic

490+00

492+44

495+00

490+45

491+97

487+44

800ft (244m)

FIGURE 1: MANITOBA SPS-10 PROJECT LAYOUT – 83AA00

1. Odd numbered sampling areas used for t0, t2, t4, t6, t8, t10; even numbered sampling areas used for t1, t3, t5, t7, t9

## MATERIALS SAMPLING AND FIELD TESTING

This section provides the materials sampling and testing activities that will occur in the field at time two (t2 is 12 months from construction time).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling. Table 5 includes the scope of field testing to be performed in t2.

Figures 2 through 5 show the material sampling locations for each section. Tables 6 through 9 list the samples acquired from each of the four test sections.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Tables 10 and 11 list samples to be shipped to the central lab testing contractor laboratory, and the LTPP Materials Reference Library (MRL), respectively.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t  = Sampling time interval

- XX  = Section number

Sample Number: S-M-##-t-XX

- S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Manitoba SPS-10, R = “C,” representing north central region)

- C = Construction event (For Manitoba SPS-10, C = 1, representing first constructed SPS-10)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 61

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

Labels and Tags

Each sample shall be labeled before packing in boxes and cartons. As a minimum, the following information shall be included on a tag or label attached to the specimen:

- SPECIMEN ID

- STATE CODE

- SHRP ID

- LOCATION DESIGNATION

- SAMPLE NUMBER

- DATE (mm-dd-yy, sampling date)

- FIELD SET (one digit number which will be 1 for the first round of sampling)

For cores, the HOLE ID shall be written directly on the core.  If the core contains more than one layer, layer boundaries shall be clearly marked, and each layer numbered.  For bulk samples, the SPECIMEN ID shall be written directly on the bag, bucket or can that contains the sample.

Packaging

Suggestions for labeling and combining the samples for shipment are as follows:

- All samples of like material (e.g., asphaltic concrete surface and binder) shall be placed in separate boxes or separate compartments of one box.

- Each sample shall have a label or tag attached that clearly identifies the material.  It is recommended that the label be color-coded by destination (e.g., contract Lab, FHWA lab, MRL, etc.)

- Each core shall be surrounded with "bubble-wrap" or other acceptable cushioning material on all sides within the shipping box.

- All bulk samples shall be marked with two labels or tags. One shall be placed inside the bag and one attached to the outside. A jar sample for moisture testing of each bulk sample shall be placed inside the bulk sample bag.

- All shipping boxes should be wood of suitable grade and construction to withstand shipping and subsequent moving without breakage of the box or damaging of samples.

- All boxes should be adequately secured by nails or screws prior to shipping.

LTPP Field Operations Information Sheets 1 and 2 shall be sent with each shipment of materials samples

TABLE 3: PROJECT LAYER NUMBERING

| Layer No. | Project Layer Code | Thickness | Material Code | Description |
| --- | --- | --- | --- | --- |
| 1 | A | N/A | 57 | Subgrade - Sand |
| 2 | B | 1.8 - 3.5” (45 – 90 mm) | 46 | Sand Asphalt Base |
| 3 | C | 7.5 - 9.0” (190 – 230 mm) | 01 | Existing AC Pavement - 1” (25mm) to be milled |
| 4 | D |  | 01 |  |
| 5 | E |  | 01 |  |
| 6 | F | 2” (50 mm) | 01 | Experimental AC overlay |

TABLE 4: SCOPE OF MATERIAL SAMPLING

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
|  | t2 SAMPLING (12 months after construction) |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | 12" Core | 4 | A01201, A01202, A01261, A01203 |
|  | 6" Core | 24 | C01201-C06201, C01202-C06202, C01261-C06261, C01203-C06203 |

TABLE 5: SCOPE OF FIELD TESTING

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | t2 TESTING (12 months after paving) |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Core Examination and Thickness (P01/AC01) | 28 | A01201, A01202, A01261, A01203, C01201-C06201, C01202-C06202, C01261-C06261, C01203-C06203 |

0-90

0-70

Section STA:

Section: 83AA01

Description: HMAC Control Section

Sampling Area: 01

Sampling Interval: t2

Shoulder

C02201

C04201

C06201

2’

2’

1’

3’

2’

2’

2’

C01201

C03201

C05201

A01201

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 2: SAMPLING AND TESTING PLAN FOR TEST SECTION 83AA01 AT TIME 2 MANITOBA SPS-10

0-90

0-70

Section STA:

Section: 83AA02

Description: WMA with Foaming Process

Sampling Area: 03

Sampling Interval: t2

Shoulder

C02202

C04202

C06202

2’

2’

1’

3’

2’

2’

2’

C01202

C03202

C05202

A01202

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 3: SAMPLING AND TESTING PLAN FOR TEST SECTION 83AA02 AT TIME 2 MANITOBA SPS-10

0-90

0-70

Section STA:

Section: 83AA61

Description: Supplemental Section - WMA with Chemical Additive plus water

Sampling Area: 05

Sampling Interval: t2

Sampling Interval: t0

Shoulder

C02261

C04261

C06261

2’

2’

1’

3’

2’

2’

2’

C01261

C03261

C05261

A01261

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 4: SAMPLING AND TESTING PLAN FOR TEST SECTION 83AA61 AT TIME 2 MANITOBA SPS-10

0-90

0-70

Section STA:

Section: 83AA03

Description: WMA with Chemical Additive

Sampling Area: 07

Sampling Interval: t2

Shoulder

C02203

C04203

C06203

2’

2’

1’

3’

2’

2’

2’

C01203

C03203

C05203

A01203

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

FIGURE 5: SAMPLING AND TESTING PLAN FOR TEST SECTION 83AA03 AT TIME 2 MANITOBA SPS-10

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 83AA01

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01201 | 6 | BA01201 | C11A04L06 | 12" Core |
| C01201 | 6 | CA01201 | C11C21L06 | 6" Core |
| C02201 | 6 | CA02201 | C11C22L06 | 6" Core |
| C03201 | 6 | CA03201 | C11C23L06 | 6" Core |
| C04201 | 6 | CA04201 | C11C24L06 | 6" Core |
| C05201 | 6 | CA05201 | C11C25L06 | 6" Core |
| C06201 | 6 | CA06201 | C11C26L06 | 6" Core |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 83AA02

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01202 | 6 | BA01202 | C12A04L06 | 12" Core |
| C01202 | 6 | CA01202 | C12C21L06 | 6" Core |
| C02202 | 6 | CA02202 | C12C22L06 | 6" Core |
| C03202 | 6 | CA03202 | C12C23L06 | 6" Core |
| C04202 | 6 | CA04202 | C12C24L06 | 6" Core |
| C05202 | 6 | CA05202 | C12C25L06 | 6" Core |
| C06202 | 6 | CA06202 | C12C26L06 | 6" Core |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 83AA61

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01261 | 6 | BA01261 | C1AA04L06 | 12" Core |
| C01261 | 6 | CA01261 | C1AC21L06 | 6" Core |
| C02261 | 6 | CA02261 | C1AC22L06 | 6" Core |
| C03261 | 6 | CA03261 | C1AC23L06 | 6" Core |
| C04261 | 6 | CA04261 | C1AC24L06 | 6" Core |
| C05261 | 6 | CA05261 | C1AC25L06 | 6" Core |
| C06261 | 6 | CA06261 | C1AC26L06 | 6" Core |

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 83AA03

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01203 | 6 | BA01203 | C13A04L06 | 12" Core |
| C01203 | 6 | CA01203 | C13C21L06 | 6" Core |
| C02203 | 6 | CA02203 | C13C22L06 | 6" Core |
| C03203 | 6 | CA03203 | C13C23L06 | 6" Core |
| C04203 | 6 | CA04203 | C13C24L06 | 6" Core |
| C05203 | 6 | CA05203 | C13C25L06 | 6" Core |
| C06203 | 6 | CA06203 | C13C26L06 | 6" Core |

TABLE 10: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C11A04L06 | 12" Core |
| C12A04L06 | 12" Core |
| C1AA04L06 | 12" Core |
| C13A04L06 | 12" Core |
| C11C21L06 | 6" Core |
| C11C22L06 | 6" Core |
| C11C23L06 | 6" Core |
| C12C21L06 | 6" Core |
| C12C22L06 | 6" Core |
| C12C23L06 | 6" Core |
| C1AC21L06 | 6" Core |
| C1AC22L06 | 6" Core |
| C1AC23L06 | 6" Core |
| C13C21L06 | 6" Core |
| C13C22L06 | 6" Core |
| C13C23L06 | 6" Core |

TABLE 11: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| C11C24L06 | 6" Core |
| C11C25L06 | 6" Core |
| C11C26L06 | 6" Core |
| C12C24L06 | 6" Core |
| C12C25L06 | 6" Core |
| C12C26L06 | 6" Core |
| C1AC24L06 | 6" Core |
| C1AC25L06 | 6" Core |
| C1AC26L06 | 6" Core |
| C13C24L06 | 6" Core |
| C13C25L06 | 6" Core |
| C13C26L06 | 6" Core |

## LABORATORY MATERIALS TESTING

The purpose of this section is to provide an outline for the laboratory testing that is planned for the Manitoba SPS-10 projects.  The previous section ended with lists of samples to be shipped to each of the central lab testing contractor laboratory and the LTPP Materials Reference Library (MRL).  In this section, the tests to be performed on each sample are listed.

Table 12 provides listings of laboratory tests to be performed for the experimental layer. The table includes the associated laboratory testing protocol for each laboratory test. It is imperative that the protocols listed be strictly followed during testing.

Table 13 provides new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory. The provided sample numbers and specimen ID’s should be used in order to ensure proper tracking using the Materials Tracking System (MTS).

Table 14 is the tracking table for tests to be conducted on each material specimen.  This table provides indication of how to process a sample after a particular test is complete.

TABLE 12: SPS-10 LABORATORY TESTING PLANS for 12-month coring (t2)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC |
| A. | EXPERIMENTAL AC |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 9 | X |
|  | Asphalt Content (Extracted) | AC04 | P04 | 4 | X |
|  | Dynamic Modulus | AC08 | P74 | 4 | X |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 4 | X |
|  | Bending Beam Rheometer (BBR) Test | AE08 | P28 | 4 | X |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 4 | X |

TABLE 13: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BA01201 | BAE1201 |
|  | Specimen ID | C11A04L06 | C11A04M06 |
|  | Sample No. | BA01202 | BAE1202 |
|  | Specimen ID | C12A04L06 | C12A04M06 |
|  | Sample No. | BA01261 | BAE1261 |
|  | Specimen ID | C1AA04L06 | C1AA04M06 |
|  | Sample No. | BA01203 | BAE1203 |
|  | Specimen ID | C13A04L06 | C13A04M06 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 14: TRACKING TABLE OF EXPERIMENTAL ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |  |  |
| C11A04L06 | P04/AC04 |  |  |  |  | No | E |
| C12A04L06 | P04/AC04 |  |  |  |  | No | E |
| C1AA04L06 | P04/AC04 |  |  |  |  | No | E |
| C13A04L06 | P04/AC04 |  |  |  |  | No | E |
| C11A04M06 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C12A04M06 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C1AA04M06 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C13A04M06 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| C11C21L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C11C22L06 | P02/AC02 |  |  |  |  | Yes | S |
| C11C23L06 | P02/AC02 |  |  |  |  | Yes | S |
| C12C21L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C12C22L06 | P02/AC02 |  |  |  |  | Yes | S |
| C12C23L06 | P02/AC02 |  |  |  |  | Yes | S |
| C1AC21L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C1AC22L06 | P02/AC02 |  |  |  |  | Yes | S |
| C1AC23L06 | P02/AC02 |  |  |  |  | Yes | S |
| C13C21L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| C13C22L06 | P02/AC02 |  |  |  |  | Yes | S |
| C13C23L06 | P02/AC02 |  |  |  |  | Yes | S |

1. Next Process

D 	Remaining sample should be disposed
	S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample
	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV
	R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV