LONG-TERM PAVEMENT PERFORMANCE

SPECIFIC PAVEMENT STUDIES

One Year Report on LTPP 83AA00, SPS-10 Project

WestLake–Gladstone, Manitoba

Report No. FHWA-

Prepared by

Stantec Consulting Inc.

1000 Young Street, Suite 470

Tonawanda, NY  14150

United States of America

Prepared for

U.S. Department of Transportation

Federal Highway Administration

Office of Acquisition Management

1200 New Jersey Ave., SE

Washington, D.C. 20950

January 1, 2017

FOREWORD

Warm Mix Asphalt (WMA) technology is part of the Federal Highway Administration’s (FHWA) Every Day Counts program, and has been implemented by Highway Agencies throughout the United States and Canada. A variety of WMA technologies have been designed to allow for production and compaction of asphalt concrete at temperatures lower than conventional Hot Mix Asphalt (HMA).

Recognizing that a knowledge gap exists in the comparison of WMA and HMA over the performance life of each type of pavement, the FHWA Long-Term Pavement Performance (LTPP) program initiated the Specific Pavement Study 10 (SPS-10) experiment, “Warm Mix Asphalt Overlay of Asphalt Pavement Study”. The Manitoba SPS-10 site in the Municipality of WestLake–Gladstone (83AA00) is the first site constructed in the North Central region of the LTPP program as part of this national experiment to study the short- and long-term performance of WMA in comparison with HMA. The data presented summarizes the performance of the road section before the resurfacing, and up to approximately 1 year after.

NOTICE

This document is disseminated under the sponsorship of the Department of Transportation in the interest of information exchange. The United States Government assumes no liability for its contents or use thereof.

The United States Government does not endorse products or manufacturers. Trade or manufacturer’s names appear herein only because they are considered essential to the object of this document.

QUALITY ASSURANCE STATEMENT

The Federal Highway Administration (FHWA) provides high-quality information to serve Government, industry, and the public in a manner that promotes public understanding. Standards and policies are used to ensure and maximize the quality, objectivity, utility, and integrity of its information. FHWA periodically reviews quality issues and adjusts its programs and processes to ensure continuous quality improvement.

| 1. Report No. FHWA-RD- |  | 2. Government Accession No. |  | 3. Recipient’s Catalog No. |  |
| --- | --- | --- | --- | --- | --- |
| 4. Title and Subtitle LTPP Specific Pavement Studies 10 (SPS-10) Project 83AA00: Warm Mix Asphalt Overlay Study on Provincial Trunk Highway 16 (PTH 16) 1 Year Report, also known as Yellowhead Highway, in the Municipality of WestLake–Gladstone, Province of Manitoba, Canada |  |  |  | 5. Report Date January 1, 2017 |  |
|  |  |  |  | 6. Performing Operations Code |  |
| 7. Author(s) Giannin Viecili, Carlos Leal, Basel Abukhater, Gabe Cimini |  |  |  | 8. Performing Operations Report No. |  |
| 9. Performing Organization Name and Address Stantec Consulting Inc. 1000 Young Street, Suite 470 Tonawanda NY 14150 United States of America |  |  |  | 10. Work Unit No. (TRAIS) |  |
|  |  |  |  | 11. Contract or Grant No. |  |
| 12. Sponsoring Agency Name and Address Federal Highway Administration LTPP-Division, HRDI-13 Turner-Fairbanks Highway Research Center 6300 Georgetown Pike McLean, Virginia 22101 |  |  |  | 13. Type of Report and Period Covered |  |
|  |  |  |  | 14. Sponsoring Agency Code |  |
| 15. Supplementary Notes Contracting Officer’s Representative (COR): Jack Springer – Turner-Fairbank Highway Research Center |  |  |  |  |  |
| 16. Abstract This report documents the construction activities related to the Manitoba SPS-10 (83AA00) project as part of the Long-Term Pavement Performance (LTPP) program’s Warm Mix Asphalt (WMA) study. Project 83AA00 was constructed on the eastbound right lane of Provincial Trunk Highway 16 (PTH 16), also known as Yellowhead Highway, in The Municipality of WestLake–Gladstone, Province of Manitoba, Canada. The project site included four test sections: a hot-mix asphalt (HMA) control section, a WMA foaming process with 1.0% water, a WMA foaming process and chemical additive (0.3% Evotherm® and 1.0% water) and a WMA chemical additive (0.3% Evotherm®). The data presented in this report highlights the performance of the road section before the resurfacing, and up to approximately 1 year after. |  |  |  |  |  |
| 17. Key Words Warm Mix Asphalt, WMA, Long-Term Pavement Performance, LTPP, Pavement, Specific Pavement Studies, Construction, SPS-10, Hot Mix Asphalt, Sampling, Monitoring, Survey, Materials, 83AA00, Manitoba, Evotherm®, Foaming Process, Chemical Additive |  |  | 18. Distribution Statement |  |  |
| 19. Security Classification (of this report) Unclassified | 20. Security Classification (of this page) Unclassified |  | 21. No. of Pages |  | 22. Price |

Form DOT F 1700.7 (8-72) Reproduction of completed page authorized.

TABLE OF CONTENTS

chapter 1: INTRODUCTION	1

GENERAL OVERVIEW OF SPS-10 STUDY	1

PROJECT OVERVIEW	2

chapter 2: PROJECT DESCRIPTION	4

PHYSICAL ATTRIBUTES	4

PAVEMENT STRUCTURE	7

Materials…........	7

CLIMATE	9

TRAFFIC	10

chapter 3: PERFORMANCE DATA	13

surface DISTRESS DATA	13

83AA01………………………	13

83AA02…………	14

83AA03…………	14

83AA61…………	15

Rutting…………..	18

LONGITUDINAL PROFILE	18

Texture…………….	20

DEFLECTION	21

Maximum Normalized Deflection (D1)	21

Subgrade Resilient Modulus (MR)	23

Effective Pavement Modulus (EP)	24

Effective Asphalt Concrete Modulus (EAC)	25

Effective Aggregate Modulus (EAgg)	26

Effective Structural Number (SNEFF)	27

FRICTION	28

TESTING	28

Dynamic Cone Penetration	28

chapter 4: SUMMARY	31

Appendix A: Photographs	34

Acknowledgements	44

LIST OF FIGURES

Figure 1: Manitoba SPS-10 Location Overview	4

Figure 2: Detailed Layout of SPS-10 Test Sections in Manitoba	5

Figure 3: Site Overview of 83AA01 – From West, Facing East	6

Figure 4: Pavement Cross Section (a) pre-overlay (b) post-overlay	7

Figure 5: Vehicle Class Distribution for Eastbound, Lane 1 of PTH 16 for 2015	11

Figure 6: Location of the AVC and WIM Devices in relation to SPS 10 site	12

Figure 7: Penetration vs Number of Blows	28

Figure 8: CBR vs. DCP	28

Figure 9: Modulus vs. CBR	29

Figure 10: 83AA01 After Construction	33

Figure 11: 83AA01 After Construction	33

Figure 12: 83AA01 After Construction	34

Figure 13: 83AA02 After Construction	34

Figure 14: 83AA02 After Construction	35

Figure 15: 83AA02 After Construction	35

Figure 16: 83AA03 After Construction	36

Figure 17: 83AA03 After Construction	36

Figure 18: 83AA03 After Construction	37

Figure 19: 83AA61 After Construction	37

Figure 20: 83AA61 After Construction	38

Figure 21: 83AA61 After Construction	38

Figure 22: 83AA01 – June 9, 2015 Pre-Overlay Transverse Cracking	39

Figure 23: 83AA01 – August 16, 2016 Post-Overlay Reflective Transverse Cracking	39

Figure 24: 83AA02 – May 4, 2015 Pre-Overlay Transverse Cracking	40

Figure 25: 83AA02 – August 16, 2016 Post-Overlay Reflective Transverse Cracking	40

Figure 26: 83AA03 – May 5, 2015 Pre-Overlay Transverse Cracking	41

Figure 27: 83AA03 – August 17, 2016 Post-Overlay Reflective Transverse Cracking	41

Figure 28: 83AA61 – May 4, 2015 Pre-Overlay Transverse Cracking	42

Figure 29: 83AA61 – August 17, 2016 Post-Overlay Reflective Transverse Cracking	42

LIST OF TABLES

Table 1: Test Section Identification and Description – 83AA00	3

Table 2: Overlay Thickness in Test Sections	7

Table 3: Manitoba SPS-10 Asphalt Concrete Aggregate Combination	8

Table 4: Average Weather Data at Gladstone Weather Station (5041049)	9

Table 5: Average Weather Data at Gladstone South Weather Station (50410N0)	9

Table 6: FHWA-LTPP Vehicle Classes with Definitions	10

Table 7: Traffic Data 2015-2016 83AA00	12

Table 8: Distress Severities for Each Test Section Prior to and Following Construction………………………………………………………………	        15

Table 9: Rutting Depth at 83AA00	17

Table 10: Average IRI for each Test Section	18

Table 11: Average Existing Texture Mean Profile Depth (MPD) for each Test Section	19

Table 12: Summary of Maximum Normalized Deflection (D1)	21

Table 13: Summary of Subgrade Resilient Modulus (MR)	22

Table 14: Summary of Effective Pavement Modulus (EP)	23

Table 15: Summary of Effective Asphalt Concrete Modulus (EAC)	24

Table 16: Summary of Effective Aggregate Modulus (EAgg)	25

Table 17: Summary of Effective Structural Number (SNEFF)	26

Table 18: Dynamic Cone Penetration Testing (8 kg Hammer) Results for 83AA00	27

LIST OF ACRONYMS

| AADT; Average Annual Daily Traffic. AASHTO; American Association of Highways and Transportation. AC; Asphalt Concrete. AVC; Automated Vehicle Classifier. AVR; Automatic Vehicle Recognition. CA; Coarse Aggregate. CBR; California Bearing Ratio. CF; Coarse Fraction. DCP; Dynamic Cone Penetration. DHV; Design Hourly Volume. FHWA; Federal Highway Administration. FWD; Falling Weight Deflectometer. GPS; Global Positioning System. HMA; Hot Mix Asphalt. HPMS; Highway Performance Monitoring System. IA; Intermediate Aggregate. IDT; Indirect Tensile. IRI; International Roughness Index. LTPP; Long-Term Pavement Performance. MDS; Manual Distress Survey. MIT; Manitoba Infrastructure and Transportation. MPD; Mean Profile Depth. NCHRP; National Cooperative Highway Research Program. RAP; Recycled Asphalt Pavement. RAS; Recycled Asphalt Shingles. RSC; Regional Support Contractor. SD; Standard Deviation. SHRP; Strategic Highway Research Program. SPS; Specific Pavement Study. VFA; Voids Filled with Asphalt. VMA; Voids in Mineral Aggregate. WIM; Weight-In-Motion. WMA; Warm Mix Asphalt. |  |
| --- | --- |

# chapter 1: INTRODUCTION

The Long-Term Pavement Performance (LTPP) program started in 1987 as part of the Strategic Highway Research Program (SHRP). Since 1992, the LTPP program has been managed by the Federal Highway Administration (FHWA). The LTPP program monitors the performance of in-service pavements. The primary mission of this program is to understand how and why pavements perform as they do. To accomplish this goal, researchers collect pavement performance data using standard data collection procedures and protocols on a variety of pavement types. This information is stored in a database that can be used by pavement engineers and researchers worldwide to advance the science of pavement engineering.

The LTPP program identified the need for investigating specific construction, maintenance, and rehabilitation practices. The LTPP program designed experiments referred to as Specific Pavement Studies (SPS) to investigate the long-term effects of these practices on pavement performance.

This report discusses the performance of a SPS-10 experiment involving the rehabilitation of a road section in Manitoba using Warm Mix Asphalt (WMA) and Hot Mix Asphalt (HMA). The data presented summarizes the performance of the road section before the resurfacing, and up to approximately 1 year after.

## GENERAL OVERVIEW OF SPS-10 STUDY

The LTPP Specific Pavement Studies 10 (SPS-10) experiment is designed to capture information on the performance of Warm Mix Asphalt (WMA) in comparison to Hot Mix Asphalt (HMA), both in the short and long term. For the purposes of the experiment, WMA is defined by the LTPP program, as asphalt mixtures produced at least 30F (16.7C) below normal hot mix asphalt production temperatures, or asphalt produced at or below 275F (135C). The experiment provides the ability to directly compare performance of WMA to HMA, thereby evaluating the difference in relative performance between WMA and HMA. Field performance will be captured over the long-term, and data from laboratory testing of WMA materials will be provided to researchers looking to evaluate various characteristics of WMA. Collectively, this information will be used for a better understanding of the potential benefits and disadvantages of WMA and for performance predictions.

The objectives of the SPS-10 experiment are to:

- Evaluate and improve the practical aspects of implementing the Warm Mix Asphalt (WMA) system through a hands-on field trial by interested highway agencies.

- Compare the performance of the WMA technologies against mixes designed with current highway agencies’ Hot Mix Asphalt specifications, asphalt-aggregate specifications, and mix design procedures.

- Provide long-term performance data for evaluation and refinement of the WMA technologies, design procedures, and models.

- Test the sensitivity of the WMA technology relative to low temperature cracking, fatigue, or permanent deformation distress factors.

- Provide highway agencies the opportunity to evaluate the performance of other experimental features by the construction of supplemental sections.

The SPS-10 experiment is intended for test sections not previously in the LTPP program. Because these sections have been nominated into the program prior to rehabilitation, all construction activities, materials properties, and sampling over the entire history of the roadway on which the test sections are located shall be documented in this report.

## PROJECT OVERVIEW

The LTPP SPS-10 project known as 83AA00 is located in the Municipality of WestLake Gladstone, a rural municipality in the Canadian province of Manitoba, along the eastbound driving lane of Provincial Trunk Highway 16 (PTH 16), also known as Yellowhead Highway, which also forms part of the Trans-Canada Highway. These test sections represent the first SPS 10 experiment constructed in Canada and in the North Central region of the LTPP program. The average existing pavement structure included 8.1 inches (205 mm) of asphalt concrete and 5.3 inches (135 mm) of sand asphalt base above the natural subgrade soil.

The Manitoba SPS-10 experiment includes a total of four different test sections: one using the agency’s standard HMA, as a control section, one using a WMA foaming process, one using a WMA chemical additive, and one using a WMA foaming process and chemical additive combination. The Asphalt Concrete (AC) mixes for the SPS-10 sections on this project were designed using the Marshall mix design method in accordance with all applicable Manitoba Infrastructure and Transportation (MIT) specifications. The WMA foaming process test section used the AESCO/Madsen Static Inline Vortex Mixer (known as the Eco-Foam II) foaming technology and the WMA chemical additive test section used the Evotherm® chemical technology. The mix designs incorporated fifteen percent (15%) of Recycled Asphalt Pavement (RAP) material. All mix designs were prepared by the Materials Engineering Branch, a central engineering and specialized support group within the Engineering & Operations Division of Manitoba Infrastructure and Transportation (MIT). The mix designs were prepared in MIT’s Winnipeg, Manitoba central laboratory. Table 1 lists each section and its respective description. The SPS-10 test sections in Manitoba were constructed on August 21, 2015.

Table 1: Test Section Identification and Description – 83AA00

| Test Section | Description |
| --- | --- |
| 83AA01 | Control Section – Hot Mix Asphalt |
| 83AA02 | WMA Core Section – Foaming Process (1.0% water) |
| 83AA61 | WMA Supplemental Section – Foaming Process and Chemical Additive (1.0% water, 0.3% Evotherm®) |
| 83AA03 | WMA Core Section – Chemical Additive (0.3% Evotherm®) |

# chapter 2: PROJECT DESCRIPTION

This section presents the project location, description and other physical attributes associated with the Manitoba SPS-10 project.

## PHYSICAL ATTRIBUTES

The Manitoba SPS-10 project is located on Provincial Trunk Highway (PTH) 16 in the Municipality of WestLake–Gladstone, Manitoba as shown in Figure 1 below. The test sections are located approximately 98 miles (157 km) west of Winnipeg, Manitoba. PTH 16 is a two-lane undivided highway.

Original Photo: © 2016 Google® (see acknowledgments section)

Figure 1: Manitoba SPS-10 Location Overview

The four test sections are located on the eastbound lane between Manitoba Provincial Road 260 and 69 Road West. The test sections begin approximately 1,242 ft (378 m) east of Manitoba Provincial Road 260 on PTH 16 and end approximately 1,407 ft (429 m) west of 69 Road West. Figure 3 shows the locations of individual test sections. The red dots indicate the beginning of the test sections. The test sections are constructed on a section of PTH 16 with no noticeable vertical curves, horizontal curves, or lane widening.

Original Photo: © 2016 Google® (see acknowledgments section)

Figure 2: Detailed Layout of SPS-10 Test Sections in Manitoba

Figure 3 shows test section 83AA01 at the time of pre-construction, looking east from the first station, it also shows a broad overview of all four test sections in the distance. Appendix A shows images of the road sections prior to, during and after construction.

Figure 3: Site Overview of 83AA01 – From West, Facing East

## PAVEMENT STRUCTURE

The traffic lanes are 12 ft (3.7 m) wide with a 10 ft (3.0 m) wide paved shoulder. The shoulder was paved using WMA with a foaming process of 1.0% water (similar to the mix used in test section 83AA02). The construction of the SPS-10 experiment included the milling of 1 inch (25 mm) and an overlay of 2 inch (50 mm) of either HMA (83AA01) or WMA (83AA02, 83AA03 and 83AA61) mixes. The existing pavement structure and post-construction structures are shown in Figure 4. The overlay thickness for each test section is listed in Table 2.

Pre-Overlay				 	     Post-Overlay

(b)

(a)

Figure 4: Pavement Cross Section (a) pre-overlay (b) post-overlay

Table 2: Overlay Thickness in Test Sections

| Section | Average Overlay Thickness – inch (mm) |
| --- | --- |
| 83AA01 | 2.5 (63.5) |
| 83AA02 | 2.3 (58.4) |
| 83AA61 | 2.3 (58.4) |
| 83AA03 | 2.3 (58.4) |

## Materials

The asphalt concrete used in this project was produced, constructed, and compacted by Nelson River Construction Inc. The asphalt mix design was created by Manitoba Infrastructure and Transportation (MIT). The mix design was produced using the Marshall mix design in accordance with all applicable specification requirements of MIT. Appendix B contains the original mix design as well as the quality control checks performed by MIT from samples collected during construction.

Components of the mix design were kept similar for all test sections with the exception of mixing technologies and mixing temperatures. Four mixing technologies were utilized:

- Conventional Hot Mix Asphalt (HMA) – Section 83AA01

- Warm Mix Asphalt (WMA) using a Foaming Process with 1.0% water – Section 83AA02

- Warm Mix Asphalt (WMA) using a Foaming Process and a Chemical Additive (1.0% water, 0.3% Evotherm®) – Section 83AA61

- Warm Mix Asphalt (WMA) using a Chemical Additive (0.3% Evotherm®) – Section 83AA03

The Design Asphalt Concrete mixing temperature for hot mix was 302°F (150°C) and 272°F (133°C) for warm mix. The WMA foaming process test sections were constructed using the AESCO/Madsen Static Inline Vortex Mixer (known as the Eco-Foam II) foaming technology. Evotherm®, the chemical additive used in WMA test sections, was supplied by Husky Energy Inc.

The combined aggregate used in the SPS-10 overlay included crushed stone, manufactured sand, washed sand, and Recycled Asphalt Pavement (RAP) aggregates. The raw aggregates and RAP were mixed from four stockpiles in the asphalt concrete mix plant. Table 3 shows the aggregate combination from the mix design used in this project.

Table 3: Manitoba SPS-10 Asphalt Concrete Aggregate Combination

| Stockpile | Percentage Used |
| --- | --- |
| Crushed Course Aggregate (Granite) | 22% |
| Washed (Natural) Sand/Fine Aggregate | 28% |
| Manufactured (Processed) Sand/Fine Aggregate | 35% |
| Recycled Asphalt Pavement (RAP) | 15% |

## Climate

Climate data for Gladstone, Manitoba is collected from two weather stations, Gladstone (5041049) and Gladstone South (50410N0), located at 50°13’00.0” N, 98°57’00.0” W and 50°11’00.0” N, 99°01’00.0” W, respectively. The Gladstone station is approximately 5 miles (8 km) away from project 83AA00, where as the Gladstone South station is approximately 3.4 miles (5.5 km) away. The weather data is accessible through Environment Canada. Table 4 and Table 5 show the average daily high and low air temperature, as well as the average snowfall and rainfall at both weather stations. The Average Annual Freeze Index for project 83AA00 is 1,703°C•days. As per LTPP definitions, the project is in a Dry, Freeze climatic zone.

Table 4: Average Weather Data at Gladstone Weather Station (5041049)

| Data Type | Jan | Feb | Mar | Apr | May | Jun | Jul | Aug | Sep | Oct | Nov | Dec |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Average daily high air temperature, °F (°C) | 9 (-13) | 20 (-6) | 31 (0) | 48 (9) | 65 (18) | 74 (24) | 76 (25) | 77 (25) | 66 (19) | 50 (10) | 29 (-2) | 17 (-9) |
| Average daily low air temperature °F (°C) | -8 (-22) | 4 (-16) | 14 (-10) | 27 (-3) | 41 (5) | 52 (11) | 55 (13) | 53 (12) | 44 (7) | 31 (0) | 14 (-10) | 1 (-17) |
| Average snow fall, inch (cm) | 9.6 (24) | 6.4 (16) | 5.9 (15) | 3.1 (8) | 1.3 (3) | 0.0 (0) | 0.0 (0) | 0.0 (0) | 0.2 (0.5) | 2.4 (6) | 7.1 (18) | 9.0 (23) |
| Average rain fall, inch (mm) | 0.0 (0) | 0.0 (0) | 0.2 (6) | 0.9 (22) | 2.0 (50) | 2.9 (72) | 3.6 (92) | 2.4 (62) | 1.9 (48) | 1.2 (31) | 0.1 (4) | 0.0 (0) |

Table 5: Average Weather Data at Gladstone South Weather Station (50410N0)

| Data Type | Jan | Feb | Mar | Apr | May | Jun | Jul | Aug | Sep | Oct | Nov | Dec |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Average daily high air temperature °F (°C) | 12 (-11) | 18 (-8) | 30 (-1) | 52 (11) | 67 (19) | 74 (23) | 80 (27) | 77 (25) | 66 (19) | 53 (12) | 32 (0) | 16 (-9) |
| Average daily low air temperature °F (°C) | -8 (-22) | -3 (-19) | 11 (-12) | 28 (-2) | 40 (4) | 50 (10) | 54 (12) | 51 (11) | 42 (6) | 31 (-1) | 15 (-9) | -3 (-19) |
| Average snow fall, inch (cm) | 6.6 (17) | 6.2 (16) | 7.2 (18) | 4.0 (10) | 0.2 (1) | 0.0 (0) | 0.0 (0) | 0.0 (0) | 0.0 (0) | 1.3 (3) | 6.2 (16) | 6.7 (17) |
| Average rain fall, inch (mm) | 0.7 (18) | 0.6 (15) | 0.9 (23) | 1.2 (30) | 2.2 (56) | 2.8 (71) | 2.6 (66) | 2.8 (71) | 2.2 (56) | 1.2 (30) | 0.8 (20) | 0.7 (18) |

## TRAFFIC

Traffic is classified as light on the PTH 16, which is a Rural Principal Arterial functional class roadway. Typically, Class 9 and greater dominate the total vehicles on this roadway. Class 9 represents five-axle truck and trailer combinations, as listed in Table 6. The vehicle Class distribution for the project in 2015 can be seen in Figure 5.

Table 6: FHWA-LTPP Vehicle Classes with Definitions

| Class | Description |
| --- | --- |
| 1 | Motorcycles |
| 2 | Passenger Cars |
| 3 | Pickups/Vans |
| 4 | Buses |
| 5 | 6 tire two-axle single unit trucks |
| 6 | Three axle single unit trucks |
| 7 | Four or more axle single unit trucks |
| 8 | Four or fewer axle truck and trailer combinations |
| 9 | Five axle truck and trailer combinations |
| 10 | Six or more axle truck and trailer combinations |
| 11 | Five or fewer axle multis |
| 12 | Six axle multis |
| 13 | Seven or more axle multis |
| 14 | Errors/Unknown |

Figure 5: Vehicle Class Distribution for Eastbound, Lane 1 of PTH 16 for 2015

The approximate location of the Automated Vehicle Classifier (AVC) and Weigh in Motion (WIM) devices is the intersection of Provincial Trunk Highway 83 and PTH 16. Figure 6 shows the approximate location, denoted by the red circled area. Data collected for the full year of 2015 and from January to April of 2016 is presented in Table 7 below.

AVC data was received from Manitoba Traffic Station 44. WIM and AVC data was also received from Manitoba Traffic Station 80, which is approximately 130 miles (208 km) west of the SPS-10 site. After reviewing data from both stations, it was found that the data was similar, thus WIM and AVC data from Station 80 was used.

Table 7: Traffic Data 2015-2016 83AA00

| Year | Class Days | Weight Days | Estimated Annual Trucks | Percent Trucks | ESALs/Class 9 |
| --- | --- | --- | --- | --- | --- |
| 2015 | 292 | 339 | 75,101 | 23.8 | 1.2 |
| 2016 | 84 | 105 | 90,742 | - | 2.2 |

SPS 10 Site 208 km East

N

Original Photo: © 2016 Google® (see acknowledgments section)

Figure 6: Location of the AVC and WIM Devices in relation to SPS 10 site

# chapter 3: PERFORMANCE DATA

## surface DISTRESS DATA

Manual Distress Surveys (MDS) were conducted by LTPP certified distress raters based on the LTPP Distress Identification Manual (DIM), FHWA-HRT-13-092 revised May 2014, on the project prior to construction and directly following construction on October 6, 2015 and again on May 3-4, and August 16-17, 2016. In the preliminary MDS's no distress was found, however in May and August 2016 all test sections in this project displayed both longitudinal non-wheelpath and transverse cracking. Details are as follows and can be seen in Table 8, supporting photos are provided in Appendix A.

### 83AA01

Prior to the project construction on June 9, 2015 the test section 83AA01 exhibited low severity fatigue cracking at 31.5 ft2  (2.9 m2), low severity non-wheelpath unsealed and sealed longitudinal cracking at 415.0 ft and 37.7 ft (126.5 m and 11.5 m), low severity unsealed and sealed transverse cracking at 155.8 ft and 12.1 ft (47.5 m and 3.7 m) and moderate severity unsealed transverse cracking at 109.3 ft (33.3 m). Test section 83AA01 did not exhibit any distresses in the preliminary survey conducted following the construction on October 6, 2015.

In an additional MDS performed on May 3, 2016 both longitudinal and transverse cracking was found. It was observed that there was 451.8 ft (173.7 m) of low severity, non-wheelpath, unsealed, longitudinal cracking. Note that a longitudinal crack occurred approximately 13 ft (4 m) from the shoulder at the construction joint between east and westbound paving that spanned the length of the section. It was also found that there was 224.4 ft (68.4 m) of low severity, transverse cracking that occurred at dispersed points of the test section.

The most recent survey, on August 16, 2016, indicated the longitudinal cracking increased to 574.1 ft (175 m) and the transverse cracking remained the same at 224.4 ft (68.4 m).

The transverse cracking found post-construction is reflective cracking.

### 83AA02

Prior to the project construction on May 4, 2015 the test section 83AA02 exhibited low severity fatigue cracking at 81.9 ft2 (7.6 m2), low severity non-wheelpath unsealed and sealed longitudinal cracking at 38.1 ft and 24.9 ft (11.6 m and 7.6 m), moderate severity non-wheelpath unsealed and sealed longitudinal cracking at 300.2 ft and 200.1 ft (91.5 m and 61.0 m), low severity unsealed transverse cracking at 97.1 ft (29.6 m), moderate severity unsealed and sealed transverse cracking at 141.1 ft and 12.8 ft (43.0 m and 3.9 m), and high severity unsealed transverse cracking at 64.0 ft (19.5 m). Test section 83AA02 did not exhibit any distresses in the survey conducted following construction on October 6, 2015.

In an additional MDS performed on May 3, 2016 both longitudinal and transverse cracking was found. It was observed that there was 510.8 ft (155.7 m) of low severity, non-wheelpath, unsealed, longitudinal cracking. Most of this consists of a crack that occurred approximately 13 ft (4 m) from the shoulder at the construction joint between east and westbound paving that spanned the length of the section. It was also found that there was 190.3 ft (58.0 m) of low severity, transverse cracking that occurred at dispersed points of the test section.

The most recent survey, on August 16, 2016, indicated the longitudinal cracking increased to 518.0 ft (157.9 m) and the transverse cracking slightly increased to 190.9 ft (58.2 m).

The transverse cracking found post-construction is reflective cracking.

### 83AA03

Prior to the project construction on May 5, 2015 the test section 83AA03 exhibited low severity fatigue cracking at 571.5 ft2 (53.1 m2), moderate severity non-wheelpath unsealed longitudinal cracking at 500.3 ft (152.5 m), low severity unsealed transverse cracking at 145.7 ft (44.4 m), moderate severity unsealed and sealed transverse cracking at 266.1 ft and 21.7 ft (81.1 m and 6.6 m) and high severity unsealed transverse cracking at 22.3 ft (6.8 m). Test section 83AA03 did not exhibit any distresses in the preliminary survey conducted following the construction on October 6, 2015.

In an additional MDS performed on May 4, 2016 both longitudinal and transverse cracking was identified. It was observed that there was 606.6 ft (184.9 m) of low severity, non-wheelpath, unsealed, longitudinal cracking. Most of this consists of a crack that occurred approximately 13 ft (4 m) from the shoulder at the construction joint between east and westbound paving that spanned the length of the section. A few longitudinal cracks were located at the lane to shoulder joint. It was also found that there was 253.6 ft (77.3 m) of low severity, transverse cracking that occurred at dispersed points of the test section.

The most recent survey, on August 17, 2016, indicated the longitudinal cracking increased to 617.8 ft (188.3 m) and the transverse cracking found was only 252.6 ft (77.0 m). The decrease in cracking could be due to temperature variations at time of survey.

The transverse cracking found post-construction is reflective cracking.

### 83AA61

Prior to the project construction on May 4, 2015 the test section 83AA61 exhibited low severity fatigue cracking at 3.6 ft2 (0.3 m2), moderate severity non-wheelpath unsealed longitudinal cracking at 500.3 ft (152.5 m), low severity unsealed and sealed transverse cracking at 51.2 ft and 27.9 ft (15.6 m and 8.5 m), moderate severity unsealed transverse cracking at 25.6 ft (7.8 m) and high severity unsealed transverse cracking at 102.7 ft (31.3 m). Test section 83AA61 did not exhibit any distresses in the preliminary survey conducted following the construction on October 6, 2015.

In an additional MDS performed on May 4, 2016 both longitudinal and transverse cracking was perceived. It was observed that there was 461.3 ft (140.6 m) of low severity and 42.3 ft (12.9 m) of moderate severity, non-wheelpath, unsealed, longitudinal cracking. Most of this consists of a crack that occurred approximately 13 ft (4 m) from the shoulder at the construction joint between east and westbound paving that spanned the length of the section. It was also found that there was 174.5 ft (53.2 m) of low severity, transverse cracking that occurred at dispersed points of the test section.

The most recent survey, on August 17, 2016, indicated there was 461.3 ft (140.6 m) of low severity and 45.9 ft (14.0 m) of moderate severity, non-wheelpath, unsealed, longitudinal cracking. In regards to transverse cracking, 162.1 ft (49.4 m) was low severity and 12.5 ft (3.8 m) was found to be of a moderate severity level.

The transverse cracking found post-construction is reflective cracking.

Table 8: Distress Severities for Each Test Section Prior to and Following Construction

| Test Section | Survey Date | Distress Type |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Fatigue ft2 (m2) | Longitudinal Cracking ft (m) |  |  |  |  |  | Transverse Cracking ft (m) |  |  |  |  |  |  |
|  |  | Low | Low |  | Moderate |  | High |  | Low |  | Moderate |  | High |  |  |
|  |  |  | Total | Sealed | Total | Sealed | Total | Sealed | Total | Sealed | Total | Sealed | Total | Sealed |
| 83AA01 | *6/9/2015 | 31.2 (2.9) | 452.8 (138.0) | 37.7 (11.5) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 168.0 (51.2) | 12.1 (3.7) | 109.3 (33.3) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
|  | 10/6/2015 | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
|  | 5/3/2016 | 0.0 (0.0) | 569.9 (173.7) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 224.4 (68.4) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
|  | 8/16/2016 | 0.0 (0.0) | 574.1 (175.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 224.4 (68.4) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
| 83AA02 | *5/4/2015 | 81.8 (7.6) | 63.0 (19.2) | 24.9 (7.6) | 500.3 (152.5) | 200.1 (61.0) | 0.0 (0.0) | 0.0 (0.0) | 97.1 (29.6) | 0.0 (0.0) | 144.0 (43.9) | 12.8 (3.9) | 64.0 (19.5) | 0.0 (0.0) |
|  | 10/6/2015 | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
|  | 5/3/2016 | 0.0 (0.0) | 510.8 (155.7) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 190.3 (58.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
|  | 8/16/2016 | 0.0 (0.0) | 518.0 (157.9) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 190.9 (58.2) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
| 83AA03 | *5/5/2015 | 571.6 (53.1) | 0.0 (0.0) | 0.0 (0.0) | 500.3 (152.5) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 79.1 (24.1) | 27.9 (8.5) | 25.6 (7.8) | 0.0 (0.0) | 102.7 (31.3) | 0.0 (0.0) |
|  | 10/6/2015 | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
|  | 5/4/2016 | 0.0 (0.0) | 606.6 (184.9) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 253.6 (77.3) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
|  | 8/17/2016 | 0.0 (0.0) | 617.8 (188.3) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 252.6 (77.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |

| Test Section | Survey Date | Distress Type |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Fatigue ft2 (m2) | Longitudinal Cracking ft (m) |  |  |  |  |  | Transverse Cracking ft (m) |  |  |  |  |  |
|  |  | Low | Low |  | Moderate |  | High |  | Low |  | Moderate |  | High |  |
|  |  |  | Total | Sealed | Total | Sealed | Total | Sealed | Total | Sealed | Total | Sealed | Total | Sealed |
| 83AA61 | *5/4/2015 | 3.2 (0.3) | 0.0 (0.0) | 0.0 (0.0) | 500.3 (152.5) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 145.7 (44.4) | 0.0 (0.0) | 287.7 (87.7) | 21.7 (6.6) | 22.3 (6.8) | 0.0 (0.0) |
|  | 10/6/2015 | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
|  | 5/4/2016 | 0.0 (0.0) | 461.3 (140.6) | 0.0 (0.0) | 42.3 (12.9) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 174.5 (53.2) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
|  | 8/17/2016 | 0.0 (0.0) | 461.3 (140.6) | 0.0 (0.0) | 45.9 (14.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 162.1 (49.4) | 0.0 (0.0) | 12.5 (3.8) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |
| *Note: This data is pre-overlay. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

### Rutting

Rutting is defined as a longitudinal surface depression in the wheelpath. Table 9 indicates the rutting at each visit for each test section. The pre-overlay and August 2016 rutting data was collected using a FACE Dipstick® Model 2200 Profiler, and the October 2015 and May 2016 rutting data was collected using a FACE Dipstick® Model 2000 Profiler.

Table 9: Rutting Depth at 83AA00

| Section | Date | Rutting Depth (mm) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Left |  |  |  | Right |  |  |  | Mean Left/Right |
|  |  | Min | Max | Mean | SD | Min | Max | Mean | SD |  |
| 83AA01 | *6/9/2015 | 0.55 | 3.58 | 1.31 | 0.99 | 1.70 | 3.70 | 2.45 | 0.66 | 1.88 |
|  | 10/6/2015 | 0.07 | 0.38 | 0.27 | 0.10 | 0.27 | 0.67 | 0.46 | 0.12 | 0.37 |
|  | 5/3/2016 | 0.15 | 0.48 | 0.33 | 0.09 | 0.23 | 0.55 | 0.41 | 0.11 | 0.37 |
|  | 8/16/2016 | 0.20 | 0.90 | 0.53 | 0.18 | 0.07 | 0.47 | 0.29 | 0.12 | 0.41 |
| 83AA02 | *5/4/2015 | 0.00 | 1.80 | 0.85 | 0.47 | 0.90 | 2.15 | 1.46 | 0.40 | 1.16 |
|  | 10/6/2015 | 0.20 | 0.85 | 0.47 | 0.15 | 0.05 | 0.48 | 0.31 | 0.13 | 0.39 |
|  | 5/3/2016 | 0.25 | 1.05 | 0.43 | 0.23 | 0.05 | 0.60 | 0.24 | 0.16 | 0.34 |
|  | 8/16/2016 | 0.55 | 1.60 | 0.83 | 0.29 | 0.07 | 0.80 | 0.47 | 0.23 | 0.65 |
| 83AA03 | *5/5/2015 | 1.77 | 4.87 | 3.02 | 1.06 | 1.00 | 4.02 | 2.71 | 0.98 | 2.87 |
|  | 10/6/2015 | 0.12 | 0.78 | 0.45 | 0.21 | 0.00 | 0.55 | 0.35 | 0.17 | 0.40 |
|  | 5/4/2016 | 0.04 | 0.70 | 0.51 | 0.20 | 0.10 | 0.63 | 0.35 | 0.16 | 0.43 |
|  | 8/17/2016 | 0.30 | 1.35 | 0.97 | 0.30 | 0.10 | 1.10 | 0.57 | 0.31 | 0.77 |
| 83AA61 | *5/4/2015 | 0.20 | 2.25 | 1.24 | 0.57 | 1.98 | 3.55 | 2.61 | 0.52 | 1.93 |
|  | 10/6/2015 | 0.13 | 0.84 | 0.36 | 0.19 | 0.17 | 0.65 | 0.46 | 0.15 | 0.41 |
|  | 5/4/2016 | 0.05 | 1.08 | 0.35 | 0.27 | 0.30 | 0.55 | 0.46 | 0.09 | 0.41 |
|  | 8/17/2016 | 0.07 | 1.70 | 0.78 | 0.44 | 0.25 | 0.75 | 0.43 | 0.15 | 0.61 |

*Note: This data is pre-overlay.

## LONGITUDINAL PROFILE

The International Roughness Index (IRI) is a statistic calculated from a longitudinal profile measured with an Ames Engineering 8300 Survey Pro High Speed Profiler (LTPP unit 830112) in the inside and outside wheelpaths of pavement. The average of these two statistics is reported as the roughness of the pavement section. It is recorded in meters per kilometer (m/km). The average IRI determined for each section before and after the overlay is presented in Table 10.

Table 10: Average IRI for each Test Section

| Section | Test Date | Avg. Air Temp. ° F (°C) | Avg. IRI in/mi (m/km) | Avg. Left Wheelpath IRI in/mi (m/km) | Avg. Right Wheelpath IRI in/mi (m/km) |
| --- | --- | --- | --- | --- | --- |
| 83AA01 | *6/4/2015 | 73.4 (23) | 100.1 (1.58) | 99.5 (1.57) | 101.4 (1.60) |
|  | 10/7/2015 | 50.0 (10) | 40.5 (0.64) | 36.1 (0.57) | 44.4 (0.70) |
|  | 5/2/2016 | 73.4 (23) | 41.2 (0.65) | 36.1 (0.57) | 45.6 (0.72) |
|  | 8/20/2016 | 73.4 (23) | 40.5 (0.64) | 36.1 (0.57) | 45.6 (0.72) |
| 83AA02 | *5/5/2015 | 78.8 (26) | 94.4 (1.49) | 98.8 (1.56) | 90.0 (1.42) |
|  | 10/7/2015 | 50.0 (10) | 34.8 (0.55) | 33.6 (0.53) | 36.1 (0.57) |
|  | 5/2/2016 | 71.6 (22) | 35.4 (0.56) | 34.8 (0.55) | 36.7 (0.58) |
|  | 8/20/2016 | 71.6 (22) | 35.4 (0.56) | 34.8 (0.55) | 36.7 (0.58) |
| 83AA03 | *5/5/2015 | 78.8 (26) | 109.6 (1.73) | 122.3 (1.93) | 96.3 (1.52) |
|  | 10/7/2015 | 50.0 (10) | 35.4 (0.56) | 31.7 (0.50) | 39.3 (0.62) |
|  | 5/2/2016 | 71.6 (22) | 35.4 (0.56) | 32.3 (0.51) | 38.6 (0.61) |
|  | 8/20/2016 | 71.6 (22) | 35.4 (0.56) | 32.3 (0.51) | 38.6 (0.61) |
| 83AA61 | *5/5/2015 | 78.8 (26) | 116.6 (1.84) | 120.4 (1.90) | 112.1 (1.77) |
|  | 10/7/2015 | 50.0 (10) | 40.5 (0.64) | 36.1 (0.57) | 45.0 (0.71) |
|  | 5/2/2016 | 73.4 (23) | 40.5 (0.64) | 37.4 (0.59) | 43.7 (0.69) |
|  | 8/20/2016 | 73.4 (23) | 40.5 (0.64) | 37.4 (0.59) | 43.7 (0.69) |

*Note: This data is pre-overlay.

The average temperature in the Fall testing, following construction, was 50°F (10°C), and the Spring testing was 72.5°F (22.5°C) . Temperature differences may influence the IRI results. Overall, the IRI was observed to decrease significantly after the overlay. The variation in the IRI of Fall 2015 and Spring 2016 was found to be insignificant.

### TEXTURE

Pavement surface texture data was collected simultaneously with longitudinal profile data. The Ames Engineering 8300 Survey Pro High Speed Profiler is capable of determining macrotexture depth at highway speeds. Macrotexture is the primary component of high-speed, wet skid resistance. The mean profile depth (MPD) represents the surface texture of pavements. The calculation of MPD from a profile of pavement macrotexture is derived from ASTM E1845-Standard Practice for Calculating Pavement Macrotexture Mean Profile Depth. The texture data is presented in Table 11. Pavement surface texture can affect road safety (friction and rolling resistance), vehicle fuel economy, vibration, and tire wear, as well as noise to vehicle occupants and the surrounding communities.

Table 11: Average Texture Mean Profile Depth (MPD) for each Test Section

| Section | Test Date | Mean Profile Depth (mm) |  |  |
| --- | --- | --- | --- | --- |
|  |  | Left | Right | Average |
| 83AA01 | *6/4/2015 | 1.45 | 1.51 | 1.48 |
|  | 10/7/2015 | 0.55 | 0.46 | 0.50 |
|  | 5/2/2016 | 0.63 | 0.63 | 0.63 |
|  | 8/20/2016 | 0.59 | 0.58 | 0.59 |
| 83AA02 | *5/5/2015 | 1.44 | 1.46 | 1.45 |
|  | 10/7/2015 | 0.64 | 0.57 | 0.60 |
|  | 5/2/2016 | 0.70 | 0.70 | 0.70 |
|  | 8/20/2016 | 0.67 | 0.68 | 0.67 |
| 83AA03 | *5/5/2015 | 1.53 | 1.49 | 1.51 |
|  | 10/7/2015 | 0.60 | 0.53 | 0.57 |
|  | 5/2/2016 | 0.67 | 0.64 | 0.65 |
|  | 8/20/2016 | 0.64 | 0.63 | 0.63 |
| 83AA61 | *5/5/2015 | 1.43 | 1.47 | 1.45 |
|  | 10/7/2015 | 0.60 | 0.54 | 0.57 |
|  | 5/2/2016 | 0.66 | 0.64 | 0.65 |
|  | 8/20/2016 | 0.63 | 0.62 | 0.63 |

*Note: This data is pre-overlay.

## DEFLECTION

A Dynatest Falling Weight Deflectometer (FWD), model 8002 with CP-15 LTPP specifications, was used to perform deflection testing before the rehabilitation. The AASHTO 1993 analysis procedure along with the ELMOD 6.0® software were used for the FWD back-calculation analysis. ELMOD created by Dynatest, analyzes the pavement response from the FWD by determining the modulus, stress and strain of each significant layer. The software considers the use of calculated and allowable forces at critical points within the pavement structure, loading, stress and strain relationships, and pavement distress.

The deflections are recorded from nine sensors, each located at varying distances from the load cell. However, for back-calculated parameters only data from eight sensors are used, the data from the sensor in front of the load plate (D9) has been excluded for processing purposes.

### Maximum Normalized Deflection (D1)

The maximum normalized deflection D1, measured at the center of the load plate, is an indicator of the overall pavement stiffness (strength). The deflection at this location is a function of the pavement layer stiffness, including the subgrade soil support beneath the pavement. High deflection values indicate a weak or thin pavement structure. Low deflection values generally indicate a strong or thick pavement structure. Summary statistics of the maximum normalized deflection are presented below in Table 12.

Table 12: Summary of Maximum Normalized Deflection (D1)

| Section | Date | D1 Minimum (µm) | D1 Maximum (µm) | D1 Average (µm) | D1 Standard Deviation |
| --- | --- | --- | --- | --- | --- |
| 83AA01 | *6/9/2015 | 105 | 200 | 133 | 28 |
|  | 10/6/2015 | 115 | 158 | 133 | 10 |
|  | 5/3/2016 | 117 | 158 | 134 | 11 |
|  | 8/16/2016 | 110 | 158 | 127 | 11 |
| 83AA02 | *5/4/2015 | 104 | 137 | 114 | 9 |
|  | 10/6/2015 | 104 | 161 | 119 | 14 |
|  | 5/3/2016 | 115 | 190 | 133 | 18 |
|  | 8/16/2016 | 96 | 150 | 114 | 13 |
| 83AA03 | *5/5/2015 | 123 | 256 | 161 | 34 |
|  | 10/6/2015 | 117 | 187 | 144 | 19 |
|  | 5/4/2016 | 117 | 203 | 147 | 23 |
|  | 8/17/2016 | 111 | 175 | 129 | 16 |
| 83AA61 | *5/4/2015 | 89 | 119 | 104 | 8 |
|  | 10/6/2015 | 86 | 124 | 102 | 10 |
|  | 5/5/2016 | 88 | 152 | 108 | 15 |
|  | 8/17/2016 | 87 | 123 | 101 | 8 |

*Note: This data is pre-overlay.

### Subgrade Resilient Modulus (MR)

The unadjusted Subgrade Soil Resilient Modulus (MR) is shown in Table 13. The strength of the material underneath the placed layers is determined using the load, deflections and distance from the center of load plate. Data from sensors further away from the load are used to represent deeper subsurface material in the deflection basin method. Based on the AASHTO 1993 Pavement Design Guide, the subgrade support can be characterized by the MR values.

Table 13: Summary of Subgrade Resilient Modulus (MR)

| Section | Date | MR Minimum (MPa) | MR Maximum (MPa) | MR Average (MPa) | MR Standard Deviation |
| --- | --- | --- | --- | --- | --- |
| 83AA01 | *6/9/2015 | 125 | 159 | 142 | 10.3 |
|  | 10/6/2015 | 145 | 189 | 164 | 11.8 |
|  | 5/3/2016 | 137 | 164 | 151 | 8.4 |
|  | 8/16/2016 | 142 | 185 | 159 | 12.1 |
| 83AA02 | *5/4/2015 | 153 | 187 | 171 | 9.6 |
|  | 10/6/2015 | 164 | 195 | 180 | 9.0 |
|  | 5/3/2016 | 155 | 182 | 169 | 8.6 |
|  | 8/16/2016 | 163 | 195 | 179 | 9.3 |
| 83AA03 | *5/5/2015 | 122 | 187 | 161 | 17.0 |
|  | 10/6/2015 | 152 | 207 | 178 | 14.2 |
|  | 5/4/2016 | 138 | 183 | 165 | 12.8 |
|  | 8/17/2016 | 151 | 206 | 181 | 14.4 |
| 83AA61 | *5/4/2015 | 176 | 201 | 189 | 7.4 |
|  | 10/6/2015 | 188 | 216 | 203 | 8.2 |
|  | 5/5/2016 | 185 | 211 | 199 | 8.1 |
|  | 8/17/2016 | 197 | 226 | 214 | 8.4 |

*Note: This data is pre-overlay.

### Effective Pavement Modulus (EP)

The Effective Pavement Modulus of Elasticity (EP) is a representation of overall pavement stiffness (the combined stiffness of all pavement layers above the subgrade), and is used to calculate the effective structural number. The backcalculation results are provided in Table 14.

EP is dependent on the overall pavement thickness and the integrity of the pavement layers. EP values of new flexible pavements usually range between 1,000 MPa to 1,700 MPa depending on the overall pavement thickness. High EP values indicate a stronger pavement structure.

Table 14: Summary of Effective Pavement Modulus (EP)

| Section | Date | EP Minimum (MPa) | EP Maximum (MPa) | EP Average (MPa) | EP Standard Deviation |
| --- | --- | --- | --- | --- | --- |
| 83AA01 | *6/9/2015 | 2,146 | 9,576 | 6,144 | 2368 |
|  | 10/6/2015 | 2,240 | 5,573 | 3,922 | 764 |
|  | 5/3/2016 | 2,489 | 5,762 | 4,161 | 857 |
|  | 8/16/2016 | 2,236 | 6,406 | 4,591 | 991 |
| 83AA02 | *5/4/2015 | 2,620 | 5,462 | 4,305 | 717 |
|  | 10/6/2015 | 1,853 | 4,362 | 3,539 | 703 |
|  | 5/3/2016 | 1,410 | 4,018 | 2,958 | 627 |
|  | 8/16/2016 | 2,092 | 5,781 | 3,904 | 894 |
| 83AA03 | *5/5/2015 | 972 | 5,138 | 3,486 | 1179 |
|  | 10/6/2015 | 1,613 | 4,824 | 3,469 | 988 |
|  | 5/4/2016 | 1,423 | 5,230 | 3,590 | 1092 |
|  | 8/17/2016 | 1,826 | 6,154 | 4,396 | 1120 |
| 83AA61 | *5/4/2015 | 5,222 | 10,799 | 8,002 | 1506 |
|  | 10/6/2015 | 3,692 | 9,055 | 6,578 | 1301 |
|  | 5/5/2016 | 2,367 | 9,013 | 6,041 | 1644 |
|  | 8/17/2016 | 3,806 | 8,730 | 6,352 | 1125 |

*Note: This data is pre-overlay.

### Effective Asphalt Concrete Modulus (EAC)

The Effective Modulus of Elasticity of Asphalt Concrete (EAC) is a representation of the stiffness of the asphalt concrete. The backcalculation was completed using ELMOD® software. The results are provided in Table 15.

EAC values are dependent on the asphalt thickness and the integrity of the asphalt layers. High values of EAC indicate a stronger asphalt layer.

Table 15: Summary of Effective Asphalt Concrete Modulus (EAC)

| Section | Date | EAC Minimum (MPa) | EAC Maximum (MPa) | EAC Average (MPa) | 84th Percentile (MPa) | Log EAC Standard Deviation |
| --- | --- | --- | --- | --- | --- | --- |
| 83AA01 | * 6/9/2015 | 1,208 | 10,059 | 3,654 | 2,279 | 1.6 |
|  | 10/6/2015 | 1,095 | 10,256 | 4,395 | 2,984 | 1.5 |
|  | 5/3/2016 | 1,661 | 7,711 | 3,968 | 3,035 | 1.3 |
|  | 8/16/2016 | 2,116 | 7,579 | 4,223 | 3,308 | 1.3 |
| 83AA02 | *5/4/2015 | 2,392 | 8,640 | 4,742 | 3,673 | 1.3 |
|  | 10/6/2015 | 1,136 | 10,839 | 3,906 | 2,751 | 1.4 |
|  | 5/3/2016 | 1,675 | 4,355 | 3,264 | 2,622 | 1.2 |
|  | 8/16/2016 | 2,310 | 5,052 | 3,485 | 2,970 | 1.2 |
| 83AA03 | *5/5/2015 | 757 | 10,675 | 4,132 | 2,241 | 1.8 |
|  | 10/6/2015 | 1,539 | 13,709 | 3,559 | 2,879 | 1.2 |
|  | 5/4/2016 | 1,760 | 3,757 | 2,758 | 2,392 | 1.2 |
|  | 8/17/2016 | 1,881 | 4,465 | 3,087 | 2,578 | 1.2 |
| 83AA61 | *5/4/2015 | 2,408 | 8,688 | 4,566 | 3,628 | 1.3 |
|  | 10/6/2015 | 2,365 | 8,567 | 4,586 | 3,603 | 1.3 |
|  | 5/5/2016 | 1,855 | 14,852 | 3,780 | 2,852 | 1.3 |
|  | 8/17/2016 | 2,426 | 5,822 | 3,678 | 3,087 | 1.2 |

*Note: This data is pre-overlay.

### Effective Aggregate Modulus (EAgg)

The Effective Aggregate Modulus of Elasticity (EAgg) is a representation of the stiffness of the aggregate/granular layer. EAgg values are dependent on the granular thickness and the integrity of the granular layers. High values of EAgg indicate a stronger granular layer.

The backcalculation was completed using ELMOD® software, results are provided in Table 16.

Table 16: Summary of Effective Aggregate Modulus (EAgg)

| Section | Date | EAgg Minimum (MPa) | EAgg Maximum (MPa) | EAgg Average (MPa) | 84th Percentile (MPa) | Log EAgg Standard Deviation |
| --- | --- | --- | --- | --- | --- | --- |
| 83AA01 | *6/9/2015 | 927 | 17,370 | 4,234 | 2,242 | 1.9 |
|  | 10/6/2015 | 159 | 32,711 | 2,956 | 1,095 | 2.7 |
|  | 5/3/2016 | 169 | 28,104 | 2,516 | 969 | 2.6 |
|  | 8/16/2016 | 184 | 19,852 | 2,745 | 1,178 | 2.3 |
| 83AA02 | *5/4/2015 | 474 | 11,893 | 1,913 | 1,078 | 1.8 |
|  | 10/6/2015 | 211 | 20,968 | 3,248 | 1,267 | 2.6 |
|  | 5/3/2016 | 250 | 12,240 | 1,416 | 704 | 2.0 |
|  | 8/16/2016 | 515 | 6,383 | 1,940 | 1,175 | 1.7 |
| 83AA03 | *5/5/2015 | 128 | 32,399 | 3,185 | 1,151 | 2.8 |
|  | 10/6/2015 | 142 | 38,770 | 3,632 | 1,123 | 3.2 |
|  | 5/4/2016 | 70 | 18,193 | 2,807 | 770 | 3.6 |
|  | 8/17/2016 | 95 | 38,310 | 3,437 | 982 | 3.5 |
| 83AA61 | *5/4/2015 | 1,064 | 36,649 | 11,675 | 6,152 | 1.9 |
|  | 10/6/2015 | 277 | 59,887 | 8,146 | 2,752 | 3.0 |
|  | 5/5/2016 | 1,507 | 48,371 | 7,926 | 3,691 | 2.1 |
|  | 8/17/2016 | 582 | 52,337 | 10,489 | 4,250 | 2.5 |

*Note: This data is pre-overlay.

### Effective Structural Number (SNEFF)

The effective strength or structural capacity of the existing pavement is traditionally represented by the effective structural number. Low SNEFF values indicate low structural capacity and high SNEFF values indicate high structural capacity.

The backcalculation results for the Structural Number are provided in Table 17.

Table 17: Summary of Effective Structural Number (SNEFF)

| Section | Date | SNEFF Minimum | SNEFF Maximum | SNEFF Average | SNEFF Standard Deviation |
| --- | --- | --- | --- | --- | --- |
| 83AA01 | *6/9/2015 | 105 | 172 | 146 | 21 |
|  | 10/6/2015 | 114 | 154 | 137 | 9 |
|  | 5/3/2016 | 118 | 156 | 139 | 10 |
|  | 8/16/2016 | 114 | 162 | 144 | 11 |
| 83AA02 | *5/4/2015 | 133 | 170 | 157 | 9 |
|  | 10/6/2015 | 125 | 166 | 154 | 11 |
|  | 5/3/2016 | 114 | 161 | 145 | 11 |
|  | 8/16/2016 | 130 | 182 | 159 | 13 |
| 83AA03 | *5/5/2015 | 73 | 126 | 109 | 15 |
|  | 10/6/2015 | 92 | 133 | 118 | 12 |
|  | 5/4/2016 | 88 | 137 | 119 | 14 |
|  | 8/17/2016 | 96 | 144 | 128 | 12 |
| 83AA61 | *5/4/2015 | 127 | 162 | 146 | 9 |
|  | 10/6/2015 | 122 | 164 | 147 | 10 |
|  | 5/5/2016 | 105 | 164 | 142 | 14 |
|  | 8/17/2016 | 123 | 162 | 145 | 9 |

*Note: This data is pre-overlay.

## FRICTION

The province of Manitoba does not preform surface friction testing.

## TESTING

### Dynamic Cone Penetration

The Dynamic Cone Penetration (DCP) test is used to assess the condition of the subgrade beneath pavement. From this test, the DCP Index, California Bearing Ratio (CBR) and subgrade modulus are obtained. Table 18 presents the DCP results from this project. Figure 6 shows the relationship between the penetration and number of blows. A difference can be noticed between test sections 83AA02 and 83AA61 from that of 83AA01 and 83AA03. This difference can be attributed to seasonal variations due to the time of year the testing was performed. Sections AA01 and AA03 were tested in late August of 2015, whilst sections AA02 and AA61 were tested in early May of 2016. Figure 7 and 8 display the CBR vs DCP Index and Subgrade Modulus.

Table 18: Dynamic Cone Penetration Testing (8 kg Hammer) Results for 83AA00

| Section | Test Date | Top of Stratum (mm) | Bottom of Stratum (mm) | Total Blow Count | DCP (mm/blow) | *Layer Log CBR | **Layer CBR (USACE) | †Subgrade Modulus (MPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 83AA01 | 08/23/15 | 356 | 1339 | 498 | 2.0 | 2.1 | 136 | 409 |
| 83AA02 | 05/03/16 | 405 | 977 | 257 | 2.2 | 2.1 | 119 | 375 |
| 83AA03 | 08/23/15 | 407 | 1351 | 438 | 2.2 | 2.1 | 124 | 384 |
| 83AA61 | 05/04/16 | 432 | 980 | 319 | 1.7 | 2.2 | 159 | 452 |

*Layer Log CBR =2.465-1.12*LOG(DCP)

**Layer CBR (USACE) =292/(DCP^1.12)

†Subgrade Modulas = 17.6*(CBR)^0.64

Figure 7: Penetration vs Number of Blows

Figure 8: CBR vs. DCP

Figure 9: Modulus vs. CBR

# chapter 4: SUMMARY

This report discussed the one year performance of a SPS-10 experiment involving the mill and overlay of a road section in the municiplatity of WestLake–Gladstone, Manitoba in August 2015. The experiment provides the ability to directly compare performance of WMA to HMA, thereby evaluating the difference in relative performance between WMA and HMA. Project background, structure, climate, traffic, and performance data has been provided to summarize the one year performance of the 83AA00 sections.

For Gladstone, Manitoba the Average Annual Freeze Index is 1703°C•days. As per LTPP definitions, the project is in a Dry, Freeze climatic zone. The average daily high temperature ranges from 9 to 81°F (-13 to 27 °C). The average daily low temperature ranges from -7.6 to 55°F (-22 to 13 °C). The average snow fall ranges from 0 to 9.6 inches (0 to 24 cm) and the average rain fall ranges from 0 to 3.6 inches (0 to 92 mm).

A summary of each of the sections their performance is provided below.

83AA01

- Conventional Hot Mix Asphalt section.

- Average overlay thickness is 2.28 inches (58 mm).

- Longitudinal and transverse cracking has been found since construction.

- Mean rutting depth has increased from 0.015 inches (0.37 mm) to 0.016 inches (0.41 mm) from October 6th 2015 to August 16th, 2016.

- Average IRI remained at 40.6 in/mi (0.64 m/km) from October 7th 2015 to May 2nd, 2016.

- The mean average profile depth has increased from 0.020 inches (0.50mm) to 0.023 inches (0.59 mm) from October 7th, 2015 to August 20th, 2016.

- The subgrade resilient modulas values indicate the presence of a fair to strong subgrade from October 2015 to August 2016.

- Average effective pavement modulas values ranged from 3,922 to 4,591 MPa from October 6th, 2015 to August 16th, 2016.

- Average effective asphalt concrete modulas values ranged from 3,968 to 4,395 MPa from October 6th, 2015 to August 16th, 2016.

- Average effective aggregate modulas values ranged from 2,516 to 2,956 MPa from October 6th, 2015 to August 16th, 2016.

- The average SNEFF increased from 137 to 144 from October 6th, 2015 to August 16th, 2016.

- The dynamic cone penetration testing indicates the subgrade resilient modulas was 1,410 MPa on August 23rd, 2015.

83AA02

- Warm Mix Asphalt section using a Foaming Process with 1.0% water.

- Average overlay thickness is 2.28 inches (58 mm).

- Longitudinal and transverse cracking has been found since construction.

- Rutting depth has increased from 0.015 inches (0.39) to 0.026 inches (0.65 mm) from October 6th 2015 to August 16th, 2016.

- Average IRI increased from 34.8 in/mi (0.55 m/km) to 35.5 in/mi (0.56 m/km) from October 7th 2015 to May 2nd, 2016.

- The mean average profile depth has increased from 0.024 inches (0.60 mm) to 0.026 inches (0.67 mm) from October 7th, 2015 to August 20th, 2016.

- The subgrade resilient modulas values indicate the presence of a strong subgrade from October 2015 to August 2016.

- Average effective pavement modulas values ranged from 3,539 to 4,958 MPa from October 6th, 2015 to August 16th, 2016.

- Average effective asphalt concrete modulas values ranged from 3,264 to 3,906 MPa from October 6th, 2015 to August 16th, 2016.

- Average effective aggregate modulas values ranged from 1,416 to 3,248 MPa from October 6th, 2015 to August 16th, 2016.

- The average SNEFF increased from 154 to 159 from October 6th, 2015 to August 16th, 2016.

- The dynamic cone penetration testing indicates the subgrade resilient modulas was 921 MPa on May 3rd, 2016.

83AA03

- Warm Mix Asphalt section using a Foaming Process and a Chemical Additive (0.3% Evotherm® plus 1.0% water).

- Average overlay thickness is 2.47 inches (63 mm).

- Longitudinal and transverse cracking has been found since construction.

- Rutting depth has increased from 0.016 inches (0.40mm) to 0.030 inches (0.77 mm) from October 6th 2015 to August 17th, 2016.

- Average IRI remained at 35.5 in/mi (0.56 m/km) from October 7th 2015 to May 2nd, 2016.

- The mean average profile depth has increased from 0.022 inches (0.57 mm) to 0.025 inches (0.63 mm) from October 7th, 2015 to August 20th, 2016.

- The subgrade resilient modulas values indicate the presence of a fair to strong subgrade from October 2015 to August 2016.

- Average effective pavement modulas values ranged from 3,469 to 4,396 MPa from October 6th, 2015 to August 16th, 2016.

- Average effective asphalt concrete modulas values ranged from 2,758 to 3,559 MPa from October 6th, 2015 to August 17th, 2016.

- Average effective aggregate modulas values ranged from 2,807 to 3,632 MPa from October 6th, 2015 to August 17th, 2016.

- The average SNEFF increased from 118 to 128 from October 6th, 2015 to August 17th, 2016.

- The dynamic cone penetration testing indicates the subgrade resilient modulas was 1,278 MPa on August 23rd, 2015.

83AA61

- Warm Mix Asphalt section using a Chemical Additive (0.3% Evotherm®)

- Average overlay thickness is 2.34 inches (59 mm).

- Longitudinal and transverse cracking has been found since construction.

- Rutting depth has increased from 0.016 inches (0.41  mm) to 0.024 inches (0.61 mm) from October 6th 2015 to August 17th, 2016.

- Average IRI remained at 40.6 in/mi (0.64 m/km) from October 7th 2015 to May 2nd, 2016.

- The mean average profile depth has increased from 0.022 inches (0.57 mm) to 0.025 inches (0.63 mm) from October 7th, 2015 to August 20th, 2016.

- The subgrade resilient modulas values indicate the presence of a strong subgrade from October 2015 to August 2016.

- Average effective pavement modulas values ranged from 6,041 to 6,578 MPa from October 6th, 2015 to August 16th, 2016.

- Average effective asphalt concrete modulas values ranged from 3,678 to 4,586 MPa from October 6th, 2015 to August 17th, 2016.

- Average effective aggregate modulas values ranged from 7,926 to 10,489 MPa from October 6th, 2015 to August 17th, 2016.

- The average SNEFF decreased from 147 to 145 from October 6th, 2015 to August 17th, 2016.

- The dynamic cone penetration testing indicates the subgrade resilient modulas was 1,225 MPa on May 4th, 2016.

This report was prepared with the information available at the time of preparation.

# Appendix A: Photographs

Figure 10: 83AA01 After Construction

Figure 11: 83AA01 After Construction

08/16/2016

Figure 12: 83AA01 After Construction

Figure 13: 83AA02 After Construction

Figure 14: 83AA02 After Construction

08/16/2016

Figure 15: 83AA02 After Construction

Figure 16: 83AA03 After Construction

Figure 17: 83AA03 After Construction

08/17/2016

Figure 18: 83AA03 After Construction

Figure 19: 83AA61 After Construction

Figure 20: 83AA61 After Construction

08/17/2016

Figure 21: 83AA61 After Construction

Figure 22: 83AA01 – June 9, 2015 Pre-Overlay Transverse Cracking

Figure 23: 83AA01 – August 16, 2016 Post-Overlay Reflective Transverse Cracking

Figure 24: 83AA02 – May 4, 2015 Pre-Overlay Transverse Cracking

Figure 25: 83AA02 – August 16, 2016 Post-Overlay Reflective Transverse Cracking

Figure 26: 83AA03 – May 5, 2015 Pre-Overlay Transverse Cracking

Figure 27: 83AA03 – August 17, 2016 Post-Overlay Reflective Transverse Cracking

Figure 28: 83AA61 – May 4, 2015 Pre-Overlay Transverse Cracking

Figure 29: 83AA61 – August 17, 2016 Post-Overlay Reflective Transverse Cracking

# Acknowledgements

The original map is the copyright property of Google® Earth TM and can be accessed from https://google.com/earth. The map overlays showing site and test sections location were developed as a result of this research project. The overlays include text label showing the project location and red dots showing the layout of test sections along PTH 16.

http://climate.weather.gc.ca/advanceSearch/searchHistoricData_e.html