LONG-TERM PAVEMENT PERFORMANCE

SPECIFIC PAVEMENT STUDIES

Construction Report on LTPP 83AA00, SPS-10 Project

WestLake–Gladstone, Manitoba

Report No. FHWA-

Prepared by

Stantec Consulting Inc.

1000 Young Street, Suite 470

Tonawanda, NY  14150

United States of America

Prepared for

U.S. Department of Transportation

Federal Highway Administration

Office of Acquisition Management

1200 New Jersey Ave., SE

Washington, D.C. 20950

January 1, 2016

FOREWORD

Warm Mix Asphalt (WMA) technology is part of the Federal Highway Administration’s (FHWA) Every Day Counts program, and has been implemented by Highway Agencies throughout the United States and Canada. A variety of WMA technologies have been designed to allow for production and compaction of asphalt concrete at temperatures lower than conventional Hot Mix Asphalt (HMA).

Recognizing that a knowledge gap exists in the comparison of WMA and HMA over the performance life of each type of pavement, the FHWA Long-Term Pavement Performance (LTPP) program initiated the Specific Pavement Study 10 (SPS-10) experiment, “Warm Mix Asphalt Overlay of Asphalt Pavement Study”. The Manitoba SPS-10 site in the Municipality of WestLake–Gladstone (83AA00) is the first site constructed in the North Central region of the LTPP program as part of this national experiment to study the short- and long-term performance of WMA in comparison with HMA. This report highlights the corresponding construction information.

NOTICE

This document is disseminated under the sponsorship of the Department of Transportation in the interest of information exchange. The United States Government assumes no liability for its contents or use thereof.

The United States Government does not endorse products or manufacturers. Trade or manufacturer’s names appear herein only because they are considered essential to the object of this document.

QUALITY ASSURANCE STATEMENT

The Federal Highway Administration (FHWA) provides high-quality information to serve Government, industry, and the public in a manner that promotes public understanding. Standards and policies are used to ensure and maximize the quality, objectivity, utility, and integrity of its information. FHWA periodically reviews quality issues and adjusts its programs and processes to ensure continuous quality improvement.

| 1. Report No. FHWA-RD- |  | 2. Government Accession No. |  | 3. Recipient’s Catalog No. |  |
| --- | --- | --- | --- | --- | --- |
| 4. Title and Subtitle LTPP Specific Pavement Studies 10 (SPS-10) Project 83AA00: Warm Mix Asphalt Overlay Study on Provincial Trunk Highway 16 (PTH 16), also known as Yellowhead Highway, in the Municipality of WestLake–Gladstone, Province of Manitoba, Canada |  |  |  | 5. Report Date January 1, 2016 |  |
|  |  |  |  | 6. Performing Operations Code |  |
| 7. Author(s) Carlos Leal, Basel Abukhater, Gabe Cimini |  |  |  | 8. Performing Operations Report No. |  |
| 9. Performing Organization Name and Address Stantec Consulting Inc. 1000 Young St. Suite 470 Tonawanda NY 14150 United States of America |  |  |  | 10. Work Unit No. (TRAIS) |  |
|  |  |  |  | 11. Contract or Grant No. |  |
| 12. Sponsoring Agency Name and Address Federal Highway Administration LTPP-Division, HRDI-13 Turner-Fairbanks Highway Research Center 6300 Georgetown Pike McLean, Virginia 22101 |  |  |  | 13. Type of Report and Period Covered |  |
|  |  |  |  | 14. Sponsoring Agency Code |  |
| 15. Supplementary Notes Contracting Officer’s Representative (COR): Jack Springer – Turner-Fairbank Highway Research Center |  |  |  |  |  |
| 16. Abstract This report documents the construction activities related to the Manitoba SPS-10 (83AA00) project as part of the Long-Term Pavement Performance (LTPP) program’s Warm Mix Asphalt (WMA) study. Project 83AA00 was constructed on the eastbound lane of Provincial Trunk Highway 16 (PTH 16), also known as Yellowhead Highway, in The Municipality of WestLake–Gladstone, Province of Manitoba, Canada. The project site included four test sections: a hot mix asphalt (HMA) control section, a WMA foaming process with 1.0% water, a WMA foaming process and chemical additive (0.3% Evotherm® and 1.0% water) and a WMA chemical additive (0.3% Evotherm®). This report includes the details of the project and the associated construction events. |  |  |  |  |  |
| 17. Key Words Warm Mix Asphalt, WMA, Long-Term Pavement Performance, LTPP, Pavement, Specific Pavement Studies, Construction, SPS-10, Hot Mix Asphalt, HMA, Sampling, Monitoring, Survey, Materials, 83AA00, Manitoba, Evotherm®, Foaming Process, Chemical Additive |  |  | 18. Distribution Statement |  |  |
| 19. Security Classification (of this report) Unclassified | 20. Security Classification (of this page) Unclassified |  | 21. No. of Pages |  | 22. Price |

Form DOT F 1700.7 (8-72) Reproduction of completed page authorized.

TABLE OF CONTENTS

chapter 1: INTRODUCTION	1

General Overview of SPS-10 Study	1

Project Overview	2

Report Organization	3

chapter 2: PROJECT DESCRIPTION	4

TEST SECTION LAYOUT	4

PHYSICAL ATTRIBUTES	7

PAVEMENT STRUCTURE	10

Project Geometry	11

Climate	11

Traffic	13

Supplemental Test Sections	14

Project Personnel	14

chapter 3: CONSTRUCTION DETAILS	15

Project Timeline	15

Materials	17

Equipment	18

Construction Events	23

Post-Construction Events	29

chapter 4: SUMMARY	35

chapter 5: KEY OBSERVATIONS	36

performance DATA	36

Surface Distress	36

83AA01	36

83AA02	36

83AA03	36

83AA61	37

Rutting	39

LONGITUDINAL PROFILE	40

Texture	40

DEFLECTION	41

CONSTRUCTION	44

Appendix A: Construction Photographs	45

Appendix B: Mix Designs	59

Appendix C: Materials Sampling and Testing Layouts	63

Appendix D: Other Construction Documents	69

Appendix E: Complete Set of SPS-10 Data Sheets	71

Appendix F: SPS-10 Deviation Report	72

Acknowledgements	74

LIST OF FIGURES

Figure 1: Manitoba SPS-10 Project Layout – 83AA00	6

Figure 2: Manitoba SPS-10 Location Overview	7

Figure 3: Detailed Layout of SPS-10 Test Sections in Manitoba	8

Figure 4: Site Overview of 83AA01 – From West, Facing East	9

Figure 5: Manitoba SPS-10 Location Topography	10

Figure 6: Pavement Cross Section (a) pre-overlay (b) post-overlay	11

Figure 7: Planned Location for the AVC Installation	13

Figure 8: Location of Asphalt Concrete Mix Plant	18

Figure 9: Asphalt Concrete Drum Mixer used in 83AA00	19

Figure 10: Typical End-Dump Truck used in Construction of 83AA00	19

Figure 11: Blaw-Knox Mobile Conveyor 330 (MC-330)	20

Figure 12: Blaw-Knox Mobile Conveyor 330 (MC-330)	21

Figure 13: Vögele Vision 5200-2 Tracked Paver	21

Figure 14: Volvo DD138HF Compactor (Breakdown Compaction)	22

Figure 15: Ingersoll Rand DD-138HF Compactor (Intermediate Compaction)	22

Figure 16: Volvo PT240R Pneumatic Tire Compactor (Final Compaction)	23

Figure 17: Broce Broom 350	24

Figure 18: Tack Coat Application Truck	24

Figure 19: Temporary Overlay Thickness Benchmark	30

Figure 20: Temporary Benchmark Used in Survey to Determine Overlay Thickness	31

Figure 21: Distance between Milling Edge and As-Built Overlay Edge	32

Figure 22: Distance between Milling Edge and As-Built Lane Edge	33

Figure 23: Normalized Deflection for test sections 83AA01 and 83AA02	43

Figure 24: Normalized Deflection for test sections 83AA03 and 83AA61	44

Figure 25: 83AA01 Before Construction	45

Figure 26: 83AA01 During Construction	45

Figure 27: 83AA01 After Construction	46

Figure 28: 83AA02 Before Construction	46

Figure 29: 83AA02 During Construction	47

Figure 30: 83AA02 After Construction	47

Figure 31: 83AA03 Before Construction	48

Figure 32: 83AA03 During Construction	48

Figure 33: 83AA03 After Construction	49

Figure 34: 83AA61 Before Construction	49

Figure 35: 83AA61 During Construction	50

Figure 36: 83AA61 After Construction	50

Figure 37: Asphalt Plant Overview	51

Figure 38: Asphalt Plant Overview	51

Figure 39: Asphalt Plant Operations	52

Figure 40: Asphalt Plant – Cold Feed Bins	52

Figure 41: Asphalt Plant – Asphalt Binder	53

Figure 42: Asphalt Plant – Cold Feed Conveyer	53

Figure 43: Asphalt Plant – Storage Tank and AC Discharge Area	54

Figure 44: Asphalt Plant – Evotherm®	54

Figure 45: Asphalt Plant – Asphalt Concrete Drum Mixer	55

Figure 46: Paving Operations - Paver	55

Figure 47: Paving Operations - Hopper	56

Figure 48: Paving Operations – End-Dump Truck	56

Figure 49: Paving Operations – End-Dump Truck to Hopper	57

Figure 50: Paving Operations – Hopper to Paver	57

Figure 51: Paving Operations on 83AA00	58

Figure 52: Density Measurement Layout for Test Section 83AA01 Manitoba SPS-10	63

Figure 53: Density Measurement Layout for Test Section 83AA02 Manitoba SPS-10	63

Figure 54: Density Measurement Layout for Test Section 83AA61 Manitoba SPS-10	64

Figure 55: Density Measurement Layout for Test Section 83AA03 Manitoba SPS-10	64

Figure 56: Sampling and Testing Layout for Test Section 83AA01 at Time 0 Manitoba SPS-10	65

Figure 57: Sampling and Testing Layout for Test Section 83AA02 at Time 0 Manitoba SPS-10	66

Figure 58: Sampling and Testing Layout for Test Section 83AA61 at Time 0 Manitoba SPS-10	67

Figure 59: Sampling and Testing Layout for Test Section 83AA03 at Time 0 Manitoba SPS-10	68

LIST OF TABLES

Table 1: Test Section Identification and Description – 83AA00	4

Table 2: Test Section Layout – 83AA00	5

Table 3: Average Weather Data at Gladstone Weather Station (5041049)	12

Table 4: Average Weather Data at Gladstone South Weather Station (50410N0)	12

Table 5: Project Timeline	16

Table 6: Manitoba SPS-10 Asphalt Concrete Aggregate Combination	17

Table 7: Paving Timeline and Width for Test Sections	25

Table 8: Number of Trucks used to Pave Test Sections and Transition Segments	26

Table 9: Mixing and Laydown Temperatures for the Four Test Sections in °F (°C)	27

Table 10: Compaction Data for Test Sections	28

Table 11: Measured Shoulder Widths	28

Table 12: Nuclear Density Gauge Data	29

Table 13: Average Distance between Milling Edge and As-Built Lane Edge	34

Table 14: Overlay Thickness in Test Sections	34

Table 15: Pavement Structure of Test Sections	34

Table 16: Distress Severities for Each Test Section Prior to and Following Construction	38

Table 17: Rutting Depth at 83AA00	39

Table 18: Average IRI for each Test Section	40

Table 19: Average Texture Mean Profile Depth (MPD) for each Test Section	41

LIST OF ACRONYMS

| AASHTO | American Association of Highways and Transportation |
| --- | --- |
| AADT | Average Annual Daily Traffic |
| AC | Asphalt Concrete |
| AVR | Automatic Vehicle Recognition |
| CA | Coarse Aggregate |
| CF | Coarse Fraction |
| DHV | Design Hourly Volume |
| FHWA | Federal Highway Administration |
| FWD | Falling Weight Deflectometer |
| HMA | Hot Mix Asphalt |
| HPMS | Highway Performance Monitoring System |
| IA | Intermediate Aggregate |
| IDT | Indirect Tensile |
| IRI | International Roughness Index |
| LTPP | Long-Term Pavement Performance |
| MIT | Manitoba Infrastructure and Transportation |
| MPD | Mean Profile Depth |
| NCHRP | National Cooperative Highway Research Program |
| RAP | Recycled Asphalt Pavement |
| RAS | Recycled Asphalt Shingles |
| RSC | Regional Support Contractor |
| SHRP | Strategic Highway Research Program |
| SPS | Specific Pavement Study |
| SD | Standard Deviation |
| VFA | Voids Filled with Asphalt |
| VMA | Voids in Mineral Aggregate |
| WMA | Warm Mix Asphalt |
| WIM | Weight-In-Motion |

# chapter 1: INTRODUCTION

The Long-Term Pavement Performance (LTPP) program started in 1987 as part of the Strategic Highway Research Program (SHRP). Since 1992, the LTPP program has been managed by the Federal Highway Administration (FHWA). The LTPP program monitors the performance of in-service pavements. The primary mission of this program is to understand how and why pavements perform as they do. To accomplish this goal, researchers collect pavement performance data using standard data collection procedures and protocols on a variety of pavement types. This information is stored in a database that can be used by pavement engineers and researchers worldwide to advance the science of pavement engineering.

The LTPP program identified the need for investigating specific construction, maintenance, and rehabilitation practices. The LTPP program designed experiments referred to as Specific Pavement Studies (SPS) to investigate the long-term effects of these practices on pavement performance.

## General Overview of SPS-10 Study

The LTPP Specific Pavement Studies 10 (SPS-10) experiment is designed to capture information on the performance of Warm Mix Asphalt (WMA) in comparison to Hot Mix Asphalt (HMA), both in the short and long term. For the purposes of the experiment, WMA is defined by the LTPP program, as asphalt mixtures produced at least 30F (16.7C) below normal hot mix asphalt production temperatures, or asphalt produced at or below 275F (135C). The experiment provides the ability to directly compare performance of WMA to HMA, thereby evaluating the difference in relative performance between WMA and HMA. Field performance will be captured over the long-term, and data from laboratory testing of WMA materials will be provided to researchers looking to evaluate various characteristics of WMA. Collectively, this information will be used for a better understanding of the potential benefits and disadvantages of WMA and for performance predictions.

The objectives of the SPS-10 experiment are to:

- Evaluate and improve the practical aspects of implementing the Warm Mix Asphalt (WMA) system through a hands-on field trial by interested highway agencies.

- Compare the performance of the WMA technologies against mixes designed with current highway agencies’ Hot Mix Asphalt specifications, asphalt-aggregate specifications, and mix design procedures.

- Provide long-term performance data for evaluation and refinement of the WMA technologies, design procedures, and models.

- Test the sensitivity of the WMA technology relative to low temperature cracking, fatigue, or permanent deformation distress factors.

- Provide highway agencies the opportunity to evaluate the performance of other experimental features by the construction of supplemental sections.

The SPS-10 experiment is intended for test sections not previously in the LTPP program. Because these sections have been nominated into the program prior to rehabilitation, all construction activities, materials properties, and sampling over the entire history of the roadway on which the test sections are located shall be documented in this report.

## Project Overview

The LTPP SPS-10 project known as 83AA00 is located in the Municipality of WestLake-Gladstone, a rural municipality in the Canadian province of Manitoba, along the eastbound driving lane of Provincial Trunk Highway 16 (PTH 16), also known as Yellowhead Highway, which also forms part of the Trans-Canada Highway. These test sections represent the first SPS-10 experiment constructed in Canada and in the North Central region of the LTPP program. The average existing pavement structure included 8.1 inches (205 mm) of asphalt concrete and 5.3 inches (135 mm) of sand asphalt base above the natural subgrade soil.

The Manitoba SPS-10 experiment includes a total of four different test sections: one using the agency’s standard HMA, as a control section, one using a WMA foaming process, one using a WMA chemical additive, and one using a WMA foaming process and chemical additive combination. The Asphalt Concrete (AC) mixes for the SPS-10 sections on this project were designed using the Marshall mix design method in accordance with all applicable Manitoba Infrastructure and Transportation (MIT) specifications. The WMA foaming process test section used the AESCO/Madsen Static Inline Vortex Mixer (known as the Eco-Foam II) foaming technology and the WMA chemical additive test section used the Evotherm® chemical technology. The mix designs incorporated fifteen percent (15%) of Recycled Asphalt Pavement (RAP) material. All mix designs were prepared by the Materials Engineering Branch, a central engineering and specialized support group within the Engineering & Operations Division of Manitoba Infrastructure and Transportation (MIT). The mix designs were prepared in MIT’s Winnipeg, Manitoba central laboratory.

The expected milling thickness of the current HMA surface layer is 1 inch (25 mm), where a 2 inch (50 mm) HMA or WMA overlay will be applied. The construction details of this report provide information on the structural design used for this project.

## Report Organization

The report sections and their respective contents are organized as follows:

Chapter 2 presents the project location, description, and other attributes of the project.

Chapter 3 describes the materials and construction procedures and detailed construction sequence and operations.

Chapter 4 provides a summary of the test section construction.

Chapter 5 contains documentation of the key construction observations.

Appendix A contains a collection of construction photographs from the project.

Appendix B contains the mix designs for the test sections.

Appendix C contains the materials sampling and testing layouts.

Appendix D contains construction documents including construction plans, specifications, and special provisions of the project; strip charts during production; daily logs and field notes of activities, equipment, and weather.

Appendix E contains the LTPP SPS-10 Construction Forms.

Appendix F contains the Deviation Report.

# chapter 2: PROJECT DESCRIPTION

This section presents the project location, description and other physical attributes associated with the Manitoba SPS-10 project.

## TEST SECTION LAYOUT

This section of the report provides a description of the Manitoba SPS-10 project in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  This table indicates transition areas between consecutive sections, as well as the buffer, sampling and monitoring areas for each section.  Additionally, Figure 1 provides a visual representation of the overall project layout. Sufficient transition area is provided between consecutive sections to ensure steady-state operation of each asphalt mix.

Table 1: Test Section Identification and Description – 83AA00

| Test Section | Description |
| --- | --- |
| 83AA01 | Control Section – Hot Mix Asphalt |
| 83AA02 | WMA Core Section – Foaming Process (1.0% water) |
| 83AA61 | WMA Supplemental Section – Foaming Process and Chemical Additive (1.0% water, 0.3% Evotherm®) |
| 83AA03 | WMA Core Section – Chemical Additive (0.3% Evotherm®) |

Table 2: Test Section Layout – 83AA00

| Project Begin STA meter | Project End STA meter | Experiment Begin STA feet (meter) | Experiment End STA feet (meter) | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | START | RD 70 W East Bound |
| 475+00 | 475+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA01 |
| 475+29 | 475+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 475+45 | 476+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 476+97 | 477+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 477+13 | 477+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 477+50 | 480+00 |  |  | Transition |  |
| 480+00 | 480+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA02 |
| 480+29 | 480+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 480+45 | 481+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 481+97 | 482+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 482+13 | 482+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 482+50 | 485+00 |  |  | Transition |  |
| 485+00 | 485+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA61 |
| 485+29 | 485+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 485+45 | 486+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 486+97 | 487+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 487+13 | 487+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 487+50 | 490+00 |  |  | Transition |  |
| 490+00 | 490+29 | 0-150 (0-49) | 0-50 (0-16) | Sampling Area | 83AA03 |
| 490+29 | 490+45 | 0-50 (0-16) | 0+00 (0+00) | Buffer Area |  |
| 490+45 | 491+97 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 491+97 | 492+13 | 5+00 (1+52) | 5+50 (1+68) | Buffer Area |  |
| 492+13 | 492+50 | 5+50 (1+68) | 6+50 (2+01) | Sampling Area |  |
| 492+50 | 495+00 |  |  | END |  |

Sampling Area 011 – 100 ft (30.5 m)

Buffer Area – 50 ft (15.25 m)

83AA01

HMA Control Section

500 ft (152.5 m)

Sampling Area 09

Buffer Area – 50 ft (15.25 m)

Sampling Area 021 – 100 ft (30.5 m)

Transition – 840 ft (256 m)

Sampling Area 031 – 100 ft (30.5 m)

Buffer Area – 50 ft (15.25 m)

83AA02

WMA Foaming Process (1.0% water)

500 ft (152.5 m)

Sampling Area 10

Buffer Area – 50 ft (15.25 m)

Sampling Area 041 – 100 ft (30.5 m)

Transition - 840 ft (256 m)

Buffer Area – 50 ft (15.25 m)

83AA61

WMA Foaming Process and Chemical Additive (1.0% water, 0.3% Evotherm®)

500 ft (152.5 m)

Sampling Area 11

Buffer Area – 50 ft (15.25 m)

Sampling Area 061 – 100 ft (30.5 m)

Sampling Area 051 – 100 ft (30.5 m)

800 ft (244 m)

800 ft (244 m)

800 ft (244 m)

EB Traffic

477+44

480+00

475+00

482+44

485+00

487+44

475+45

476+97

480+45

481+97

485+45

486+97

Sampling Area 071 – 100 ft (30.5 m)

Buffer Area – 50 ft (15.25 m)

83AA03

WMA Chemical Additive

(0.3% Evotherm®)

500 ft (152.5 m)

Sampling Area 12

Buffer Area – 50 ft (15.25 m)

Sampling Area 081 – 100 ft (30.5 m)

Transition - 840 ft (256 m)

800 ft (244 m)

EB Traffic

490+00

492+44

495+00

490+45

491+97

Transition - 840 ft (256 m)

Figure 1: Manitoba SPS-10 Project Layout – 83AA00

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

## PHYSICAL ATTRIBUTES

The Manitoba SPS-10 project is located on Provincial Trunk Highway (PTH) 16 in the Municipality of WestLake–Gladstone, Manitoba as shown in Figure 2 below. The test sections are located approximately 98 miles (157 km) west of Winnipeg, Manitoba. PTH 16 is a two-lane undivided highway.

Original Photo: © 2016 Google® (see acknowledgments section)

Figure 2: Manitoba SPS-10 Location Overview

The four test sections are located on the eastbound lane between Manitoba Provincial Road 260 and 69 Road West. The test sections begin approximately 1,242 ft (378 m) east of Manitoba Provincial Road 260 on PTH 16 and end approximately 1,407 ft (429 m) west of 69 Road West. Figure 3 shows the locations of individual test sections. The red dots indicate the beginning of the test sections. The test sections are constructed on a section of PTH 16 with no noticeable vertical curves, horizontal curves, or lane widening.

Original Photo: © 2016 Google® (see acknowledgments section)

Figure 3: Detailed Layout of SPS-10 Test Sections in Manitoba

Figure 4 shows test section 83AA01 at the time of pre-construction, looking east from the first station, it also shows a broad overview of all four test sections in the distance.

Figure 4: Site Overview of 83AA01 – From West, Facing East

As defined by T. Corkery, the SPS-10 site is located within the physiographic region defined as the Manitoba Lowlands in the Red River Plain, close to the borders of the Interlake-Westlake Plain and Lower Assiniboine Delta. The Red River Plain is one of the flattest regions in North America. The topography of the site is shown in Figure 5.

83AA03

83AA02

83AA61

83AA01

69 Rd W

N

Source: © Online Topo Maps (see acknowledgements section)

Figure 5: Manitoba SPS-10 Location Topography

## PAVEMENT STRUCTURE

The SPS-10 test sections in Manitoba were constructed on August 21, 2015. The traffic lanes are 12 ft (3.7 m) wide with a 10 ft (3.0 m) wide paved shoulder. The shoulder was paved using WMA with a foaming process of 1.0% water (similar to the mix used in test section 83AA02). The construction of the SPS-10 experiment included the milling of 1 inch (25 mm) and an overlay of 2 inch (50 mm) of either HMA (83AA01) or WMA (83AA02, 83AA03 and 83AA61) mixes. The existing pavement structure and post-construction structures are shown in Figure 6.

(a) Pre-Overlay					(b) Post-Overlay

Figure 6: Pavement Cross Section (a) pre-overlay (b) post-overlay

## Project Geometry

All the test sections are located in relatively flat geographical areas with grades of 1% or less with no embankments, no rolling hills, or cut-fill transitions. The four sections are all contained within a 1.24 miles (2 km) segment of the roadway which contains no major intersections.

## Climate

Climate data for Gladstone, Manitoba is collected from two weather stations, Gladstone (5041049) and Gladstone South (50410N0), located at 50°13’00.0” N, 98°57’00.0” W and 50°11’00.0” N, 99°01’00.0” W, respectively. The Gladstone station is approximately 5 miles (8 km) away from project 83AA00, where as the Gladstone South station is approximately 3.4 miles (5.5 km) away. The weather data is accessible through Environment Canada. Table 3 and Table 4 show the average daily high and low air temperature, as well as the average snowfall and rainfall at both weather stations. The Average Annual Freeze Index for project 83AA00 is 1,703°C•days. As per LTPP definitions, the project is in a Dry, Freeze climatic zone.

Table 3: Average Weather Data at Gladstone Weather Station (5041049)

| Data Type | Jan | Feb | Mar | Apr | May | Jun | Jul | Aug | Sep | Oct | Nov | Dec |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Average daily high air temperature, °F (°C) | 9 (-13) | 20 (-6) | 31 (0) | 48 (9) | 65 (18) | 74 (24) | 76 (25) | 77 (25) | 66 (19) | 50 (10) | 29 (-2) | 17 (-9) |
| Average daily low air temperature °F (°C) | -8 (-22) | 4 (-16) | 14 (-10) | 27 (-3) | 41 (5) | 52 (11) | 55 (13) | 53 (12) | 44 (7) | 31 (0) | 14 (-10) | 1 (-17) |
| Average snow fall, inch (cm) | 9.6 (24) | 6.4 (16) | 5.9 (15) | 3.1 (8) | 1.3 (3) | 0.0 (0) | 0.0 (0) | 0.0 (0) | 0.2 (0.5) | 2.4 (6) | 7.1 (18) | 9.0 (23) |
| Average rain fall, inch (mm) | 0.0 (0) | 0.0 (0) | 0.2 (6) | 0.9 (22) | 2.0 (50) | 2.9 (72) | 3.6 (92) | 2.4 (62) | 1.9 (48) | 1.2 (31) | 0.1 (4) | 0.0 (0) |

Table 4: Average Weather Data at Gladstone South Weather Station (50410N0)

| Data Type | Jan | Feb | Mar | Apr | May | Jun | Jul | Aug | Sep | Oct | Nov | Dec |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Average daily high air temperature °F (°C) | 12 (-11) | 18 (-8) | 30 (-1) | 52 (11) | 67 (19) | 74 (23) | 80 (27) | 77 (25) | 66 (19) | 53 (12) | 32 (0) | 16 (-9) |
| Average daily low air temperature °F (°C) | -8 (-22) | -3 (-19) | 11 (-12) | 28 (-2) | 40 (4) | 50 (10) | 54 (12) | 51 (11) | 42 (6) | 31 (-1) | 15 (-9) | -3 (-19) |
| Average snow fall, inch (cm) | 6.6 (17) | 6.2 (16) | 7.2 (18) | 4.0 (10) | 0.2 (1) | 0.0 (0) | 0.0 (0) | 0.0 (0) | 0.0 (0) | 1.3 (3) | 6.2 (16) | 6.7 (17) |
| Average rain fall, inch (mm) | 0.7 (18) | 0.6 (15) | 0.9 (23) | 1.2 (30) | 2.2 (56) | 2.8 (71) | 2.6 (66) | 2.8 (71) | 2.2 (56) | 1.2 (30) | 0.8 (20) | 0.7 (18) |

## Traffic

Traffic data has yet to be collected for this SPS-10 project, but traffic estimates provided by MIT as part of the site nomination process indicate an Average Annual Daily Traffic (AADT) of 2,990 in the project lane. Of this value, 24% of the traffic is projected to be Heavy Trucks and Combinations. Annual Equivalent Single Axle Loads (ESALs) during the first year of the twenty-year design period are estimated at 439,000 ESALs.

MIT is currently working on the installation of an Automatic Vehicle Classification (AVC) device to monitor traffic types on the test sections. The planned approximate location of the AVC device is between the intersection of Manitoba Provincial Road 260 with PTH 16 and the sampling area of test section 83AA01. Figure 7 shows the approximate location of the planned AVC installation, as denoted by the red circled area.

Original Photo: © 2016 Google® (see acknowledgments section)

Figure 7: Planned Location for the AVC Installation

## Supplemental Test Sections

In addition to the three SPS-10 experiment core sections, highway agencies may construct supplemental test sections on an SPS-10 site to investigate other factors of interest. Manitoba Infrastructure and Transportation executed the construction of one supplemental section in the SPS-10 experiment located at site 83AA00. The supplemental section was overlaid with Warm Mix Asphalt using a Foaming Process and a Chemical Additive (1.0% water, 0.3% Evotherm®). The test section was entitled 83AA61 and was constructed between test sections 83AA02 and 83AA03, as illustrated in Figure 1 and Figure 3. Physical attributes of this section are similar to the other sections and are included in the Physical Attributes section of this report.

## Project Personnel

The key project personnel are listed below:

Manitoba Infrastructure and Transportation (MIT):

Project Manager: Ben Wallace

Materials Assessment Technologist (On-site representative): Andre Dupuis

Surfacing Materials Engineer: Tara Liske

Pavement Research Engineer: Elena Oberez

Engineering Aid (Inspector monitoring the pavement compaction/temperature): Giselle Marcq

Nelson River Construction Inc. (Construction Contractor):

Plant Manager: Rockie Laba

Paving Foreman: Peter Laba

Construction Superintendent: James Peetsma

Stantec Consulting Inc. (LTPP Regional Support Contractor (RSC)):

Project Manager: Gabe Cimini

Pre-Overlay Monitoring: Doug Marshall

Construction Documentation: Brandt Henderson, Mohab El-Hakim, Kurtis Pettitt

Material Sampling: Brandt Henderson, Mohab El-Hakim, Kurtis Pettitt

Coring Coordination: Brandt Henderson, Mohab El-Hakim, Kurtis Pettitt

Post-Overlay Monitoring: Alfred Lip

Supporting Team: Basel Abukhater, Carlos Leal, Jesse Dickes, Tony Wagner

# chapter 3: CONSTRUCTION DETAILS

This section describes the materials and detailed construction procedures associated with the LTPP SPS-10 project 83AA00 in Manitoba.

## Project Timeline

Initial site visit activities comprised of laying out the test sections, and collecting pre-overlay performance measurements, which were performed between June 5, 2015 and June 9, 2015. The performance measurements collected include: Manual Distress Survey’s (MDS), Falling Weight Deflectometer (FWD) measurements, longitudinal profile measurements, transverse profile measurements, surface texture measurements, and elevation surveys for each test section.

A pre-overlay meeting took place on-site on August 7, 2015. The sampling and construction phase of the project took place between August 18, 2015 and August 26, 2015. The project timeline is shown in Table 5.

Table 5: Project Timeline

| Date | Task Performed | Personnel |
| --- | --- | --- |
| June 5-9, 2015 | Pre-Overlay Monitoring: MDS, FWD and elevation survey | Doug Marshall |
| July 18, 2015 | Milling Operations | Nelson River Construction Inc. |
| August 7, 2015 | On-site pre-construction meeting with the contractor and the agency (MIT). LTPP RSC staff visited the asphalt plant to coordinate the sampling of raw materials. | Mohab El-Hakim / Kurtis Pettitt |
| August 17-18, 2015 | Post-Milling Elevation Survey | Mohab El-Hakim/ Brandt Henderson / Kurtis Pettitt |
| August 19, 2015 | Sampled blended aggregate, bulk RAP and processed RAP samples from the asphalt plant | Mohab El-Hakim/ Brandt Henderson / Kurtis Pettitt |
| August 20, 2015 | Visited asphalt plant to collect information and required data for the LTPP Construction Forms | Mohab El-Hakim/ Brandt Henderson / Kurtis Pettitt |
| August 21, 2015 | Paving completed on all four test sections. Temperatures were monitored while producing asphalt mixes in the asphalt plant and on site. Sampling of uncompacted asphalt concrete and virgin asphalt binder was performed. | Mohab El-Hakim (On-site)/ Brandt Henderson (On-site) / Kurtis Pettitt (In Asphalt plant) |
| August 23, 2015 | Coring and post-overlay monitoring performed on test section 83AA01. Post-overlay survey performed on test section 83AA61 and 7 of the 6” cores were extracted. All 12” and 6” cores from test section 83AA03 were extracted. | Mohab El-Hakim/ Brandt Henderson / Kurtis Pettitt |
| August 24, 2015 | Coring and post-overlay monitoring performed on test section 83AA02. Remaining cores from test section 83AA61 were extracted. Post-overlay monitoring for test section 83AA03 was performed. | Mohab El-Hakim/ Brandt Henderson / Kurtis Pettitt |
| August 26, 2015 | Collected Nuclear Density Gauge measurements on all four test sections. Monitored paving of shoulder for the test sections. | Mohab El-Hakim |

## Materials

The asphalt concrete used in this project was produced, constructed, and compacted by Nelson River Construction Inc. The asphalt mix design was created by Manitoba Infrastructure and Transportation (MIT). The mix design was produced using the Marshall mix design in accordance with all applicable specification requirements of MIT. Appendix B contains the original mix design as well as the quality control checks performed by MIT from samples collected during construction.

Components of the mix design were kept similar for all test sections with the exception of mixing technologies and mixing temperatures. Four mixing technologies were utilized:

- Conventional Hot Mix Asphalt (HMA) – Section 83AA01

- Warm Mix Asphalt (WMA) using a Foaming Process with 1.0% water – Section 83AA02

- Warm Mix Asphalt (WMA) using a Foaming Process and a Chemical Additive (1.0% water, 0.3% Evotherm®) – Section 83AA61

- Warm Mix Asphalt (WMA) using a Chemical Additive (0.3% Evotherm®) – Section 83AA03

The Design Asphalt Concrete mixing temperature for hot mix was 302°F (150°C) and 272°F (133°C) for warm mix. The WMA foaming process test sections were constructed using the AESCO/Madsen Static Inline Vortex Mixer (known as the Eco-Foam II) foaming technology. Evotherm®, the chemical additive used in WMA test sections, was supplied by Husky Energy Inc.

The combined aggregate used in the SPS-10 overlay included crushed stone, manufactured sand, washed sand, and Recycled Asphalt Pavement (RAP) aggregates. The raw aggregates and RAP were mixed from four stockpiles in the asphalt concrete mix plant. Table 6 shows the aggregate combination from the mix design used in this project.

Table 6: Manitoba SPS-10 Asphalt Concrete Aggregate Combination

| Stockpile | Percentage Used |
| --- | --- |
| Crushed Course Aggregate (Granite) | 22% |
| Washed (Natural) Sand/Fine Aggregate | 28% |
| Manufactured (Processed) Sand/Fine Aggregate | 35% |
| Recycled Asphalt Pavement (RAP) | 15% |

## Equipment

The asphalt concrete mix plant for this project was a mobile drum mix plant operated by the primary contractor, Nelson River Construction Inc. The drum model is a Barber Greene DM70, with a 3-tonne batch size capacity.

The plant was located on Manitoba Provincial Road 352, approximately 2.5 miles (4 km) north of Arden, Manitoba. The coordinates of the asphalt concrete mix plant are 50°18’28.3”N, 99°17’9.6’’W. Figure 8 shows the approximate location of the plant and SPS-10 83AA00 site.

Original Photo: © 2016 Google® (see acknowledgments section)

Figure 8: Location of Asphalt Concrete Mix Plant

The plant was located approximately 13.7 miles (21.7 km) northwest of the project test sections. Figure 9 shows an image of the asphalt concrete drum mixer at the plant. The distance corresponded to a haul time of approximately 20-30 minutes in regular traffic conditions. Typical end-dump trucks, shown in Figure 10, were used to haul the asphalt concrete to site. Each truck hauled an average net weight of approximately 31.3 US short tons (28.4 metric tons) of asphalt concrete per trip.

Figure 9: Asphalt Concrete Drum Mixer used in 83AA00

Figure 10: Typical End-Dump Truck used in Construction of 83AA00

The paving equipment used to construct project 83AA00 included:

Blaw-Knox Mobile Conveyor 330 (MC-330) –Figure 11 and Figure 12

Vögele Vision 5200-2 Tracked Paver – Figure 13

Volvo DD138HF Double Drum Vibratory Compactor – 14.9-ton (13.5 tonne) breakdown compactor – Figure 14

Ingersoll Rand DD-138HF Double Drum Vibratory Compactor – 13.7 ton (13.5 tonne) intermediate compactor – Figure 15

Volvo ABG PT240R Pneumatic Tire Compactor – unballasted 18.1 ton (16.4 tonne) final compactor – Figure 16

Figure 11: Blaw-Knox Mobile Conveyor 330 (MC-330)

Figure 12: Blaw-Knox Mobile Conveyor 330 (MC-330)

Figure 13: Vögele Vision 5200-2 Tracked Paver

Figure 14: Volvo DD138HF Compactor (Breakdown Compaction)

Figure 15: Ingersoll Rand DD-138HF Compactor (Intermediate Compaction)

Figure 16: Volvo PT240R Pneumatic Tire Compactor (Final Compaction)

## Construction Events

All four test sections of the project were constructed on August 21, 2015. The average ambient air temperature during paving was 59⁰F (15⁰C). Tack coat application for test sections 83AA01 and 83AA02 occurred at approximately 6:30a.m. Tack coat application for test sections 83AA61 and 83AA03 occurred at approximately 11:00a.m. A Broce broom was used to clean the road surface of debris prior to the tack coat application. A Broce broom is a machine with a mounted wafer rotating brush that removes debris as it passes over the road. The Broce broom and the truck used to apply the tack coat are shown in Figures 17 and 18, respectively.

Figure 17: Broce Broom 350

Figure 18: Tack Coat Application Truck

Table 7 shows the as-built construction timeline of each test section, the average actual haul time from the asphalt plant to the site during construction, the average time between asphalt truck arrivals and asphalt laydown and the total number of passes by all weighted rollers for each test section.

Table 7: Paving Timeline and Width for Test Sections

| Section | Time Paving Began | Time Paving Finished | Average Haul Time (min) | Average Time Between Arrival and Laydown (min) | Single Pass Paving Width ft (m) | Number of Passes by Rollers |
| --- | --- | --- | --- | --- | --- | --- |
| 83AA01 | 11:05 | 11:26 | 27 | 21 | 12.14 (3.7) | 17 |
| 83AA02 | 11:55 | 12:22 | 26 | 19 | 12.14 (3.7) | 17 |
| 83AA61 | 12:54 | 13:22 | 29 | 18 | 12.14 (3.7) | 17 |
| 83AA03 | 13:44 | 14:17 | 31 | 13 | 12.14 (3.7) | 17 |

The paving crew successfully switched asphalt mixes within the 820 ft (250 m) transition segment between test sections. The paving team ensured that at least a full truck containing the subsequent test sections asphalt mix design, would be used within the transition segment. This practice ensured purging of any residues of the previous mix in the paver prior to the start of paving on the following test section. Table 8 lists the approximate number of trucks used to pave each test section as well as the transition segment between test sections.

Table 8: Number of Trucks used to Pave Test Sections and Transition Segments

| Section | Number of Trucks used to Pave the Section | Notes |
| --- | --- | --- |
| 83AA01 | 5 trucks of HMA |  |
| Transition Segment between 83AA01 and 83AA02 | 3 trucks of HMA |  |
|  | 1 truck of WMA (Foaming process with 1.0% water) |  |
| 83AA02 | 5 trucks of WMA (Foaming process with 1.0% water) | The 5th truck was used for the last 30 ft (9 m) in the test section. Most of the 5th truck was used to pave the transition segment |
| Transition Segment between 83AA02 and 83AA61 | 2 trucks of WMA (Foaming process with 1.0% water) |  |
|  | 2 trucks of WMA (Foaming process and Chemical Additive – 0.3% Evotherm® plus 1.0% water) |  |
| 83AA61 | 4 trucks of WMA (Foaming process and Chemical Additive – 0.3% Evotherm® plus 1.0% water) |  |
| Transition Segment between 83AA61 and 83AA03 | 2 trucks of WMA (Foaming process and Chemical Additive – 0.3% Evotherm® plus 1.0% water) |  |
|  | 1 truck of WMA (Chemical Additive – 0.3% Evotherm®) |  |
| 83AA03 | 6 truck of WMA (Chemical Additive – 0.3% Evotherm®) | Portion of the 1st truck was used in the transition segment but most of the truck was used on the test section |

Detailed construction information was recorded for each of the four sections. Documented information includes lift thickness, soil survey data, paving widths, air temperature, asphalt temperature, compaction effort, and density. For a more detailed breakdown of variables, including disaggregated values, please see Appendix D and Appendix E.

SAF-T-LOG® handheld thermometers were used to measure temperatures at several different locations during construction as well as in the asphalt plant. Table 9 shows the average, minimum, maximum, and recorded number of records for plant mixing and laydown temperature for each of the four sections. The laydown temperature was measured just behind the screed of the paver. The AC mix for test section AA01 was produced at the design mix temperature of 302°F (150°C). The WMA test sections were produced within 2°F (1.1⁰C) of the design mix temperature 272°F (133°C). Table 9 shows that test section AA02 was produced 1°F (0.6⁰C) above, test section AA61 was produced 2°F (1.1⁰C) below and test section AA03 was produced 2°F (1.1⁰C) above design mix temperatures. The temperature differences between HMA and WMA mixes are in accordance with the LTPP SPS-10 experiment design. The mixing and paving temperatures for the WMA technologies were within 4°F (2.2⁰C) between test sections and approximately 30°F (16.7°C) below the HMA temperature.

Table 9: Mixing and Laydown Temperatures for the Four Test Sections in °F (°C)

| Section | Mixing Temperature |  |  |  | Laydown Temperature |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | No. of Records | Min | Max | Avg | No. of Records | Min | Max | Avg |
| AA01 | 20 | 294 (146) | 305 (152) | 302 (150) | 14 | 262 (128) | 271 (133) | 267 (131) |
| AA02 | 20 | 268 (131) | 278 (137) | 273 (134) | 17 | 239 (115) | 250 (121) | 243 (117) |
| AA61 | 17 | 264 (129) | 275 (135) | 270 (132) | 15 | 232 (111) | 244 (118) | 239 (115) |
| AA03 | 14 | 273 (134) | 275 (135) | 274 (134) | 18 | 237 (114) | 244 (118) | 240 (116) |

Compaction events were recorded in order to describe the compaction effort for each test section. Compactor data including weight, compactor type, vibration frequency, vibration amplitude and number of coverages completed on each section are included in Table 10. Coverage values describe the number of passes a vehicle has completed on the section.

Table 10: Compaction Data for Test Sections

| Compaction Stage |  | Breakdown | Intermediate | Final |
| --- | --- | --- | --- | --- |
| Compactor Type |  | Double Drum Vibrator | Pneumatic Tire Roller Compactor | Steel-Wheel Tandem |
| Compactor Model |  | Volvo DD138HF | Ingersoll Rand DD-138HF | Westcon PT240R |
| Compactor Weight - US short-ton (Metric Tonne) |  | 14.9 (13.5) | 13.7 (12.4) | 14.0 (12.7) |
| Tire Pressure – Kpa (psi) |  | NA | 689 (100) | NA |
| Vibration | Frequency (VPM) | 3200 | NA | NA |
|  | Amplitude – inch (mm) | 0.019 (0.4826) | NA | NA |
| Speed – mph (km/h) |  | 3 (5) | 4 (6) | 3 (5) |
| Coverage (no. of passes) |  | 7 | 7 | 3 |

Shoulder Information

The shoulders were constructed with the following bound and unbound material:

4 inches (100 mm) Bituminous Pavement, Class “B”

6 inches Granular Base Course, Class “A”

Approximately 4 inches (100 mm) of pulverized Bituminous Pavement and Granular Base Course (Varies)

The average shoulder widths for each section are detailed in Table 11. The specifications for shoulder construction are given in Appendix D.

Table 11: Measured Shoulder Widths

| Section | Station | Paved Shoulder Width, ft (m) | Gravel Shoulder Width, ft (m) |
| --- | --- | --- | --- |
| AA01 | 0-90 | 10.0 (3.05) | 8.0 (2.4) |
|  | 1+00 | 10.1 (3.1) | 6.1 (1.9) |
| AA02 | 0+00 | 9.4 (2.9) | 7.1 (2.2) |
|  | 5+00 | 9.4 (2.9) | 8.2 (2.5) |
| AA03 | 0+00 | 9.2 (2.8) | 7.9 (2.4) |
| AA61 | 0-90 | 9.3 (2.8) | 8.0 (2.4) |

## Post-Construction Events

MIT provided a nuclear density gauge (Troxler 3440) to perform density measurements on the test sections. This equipment was calibrated on February 2, 2015. Density measurements were recorded at three locations distributed evenly along the 500 ft (152 m) monitoring area for each of the four sections on August 8, 2015. Table 12 shows the minimum, maximum, average, standard deviation and recorded number of bulk density measurements measured in pounds per cubic feet and average percent compaction by test section. MIT requires that the pavement be compacted to a minimum 97% of 148.9 lb/ft3 (2,385 kg/m3). The standard specifications for shoulder preparation (No. 700: 7.3.1.3) is given in Appendix D. All four-test section met this requirement exceeding a minimum 144.5 lb/ft3 (2,314 kg/m3). Test section AA01 was compacted to a density greater than the required 148.9 lb/ft3 (2,385 kg/m3).

Table 12: Nuclear Density Gauge Data

| Section | Bulk Density – lb/ft3 (kg/m3) |  |  |  |  | Average Percentage Compaction | Percentage Marshall Density 148.9 lb/ft3 (2,385 kg/m3) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Minimum | Maximum | Average | Standard Deviation | No. of Records |  |  |
| AA01 | 148.6 (2,380) | 151.3 (2,423) | 149.8 (2,400) | 0.803 (13) | 12 | 100% | 100.6% |
| AA02 | 145.6 (2,332) | 147.6 (2,365) | 146.7 (2,350) | 0.59 (9) | 12 | 98.3% | 98.5% |
| AA61 | 146.8 (2,352) | 148.9 (2,385) | 148.0 (2,371) | 0.69 (11) | 12 | 98.8% | 99.4% |
| AA03 | 147.1 (2,357) | 149.9 (2,401) | 148.5 (2,380) | 0.93 (15) | 12 | 99.2% | 99.8% |

A field survey was conducted to accurately measure the thickness of the compacted overlay. Benchmarks were installed prior to the overlay and were created using steel rods hammered deep into the ground at the edge of the paved shoulder. Figure 19 illustrates one of the temporary benchmarks installed for the post-milling and post-overlay monitoring.

The post-milling survey was performed three days prior to the overlay on August 18, 2015. The post-overlay survey was performed within the two days after the overlay installation on August 23 and 24, 2015. The dates of post-paving elevation survey on individual test sections are presented in Table 5.

Benchmark

Figure 19: Temporary Overlay Thickness Benchmark

Field survey measurements were taken every 50 ft (15.24 m) on the longitudinal direction and at offsets of 0, 3, 6, 9 and 12 ft (0, 0.9, 1.8, 2.7 and 3.7 m) from the lane edge. The lane edge was identified in the pre-overlay survey as the longitudinal line representing the edge of the milling surface as presented in Figure 20. The milling edge was the start point to measure the offset to perform the survey work.

Assumed Lane Edge for Pre-Paving Survey

Figure 20: Temporary Benchmark Used in Survey to Determine Overlay Thickness

The post-overlay field elevation survey was performed on the same offset points used in the post-milling field survey; however, the overlay edge was slightly shifted from the milling edge as illustrated in Figures 21 and 22. The shift between milling edge and as-built overlay lane edge was measured every 500 ft (152 m) at each test section. The average distance between the edge of the milling surface and the overlay edge is shown in Table 13. The minimum, maximum, average, and standard deviation of overlay thicknesses for each test section are shown in Table 14. The pavement structure of the test sections based on cored samples is shown in Table 15.

Figure 21: Distance between Milling Edge and As-Built Overlay Edge

Figure 22: Distance between Milling Edge and As-Built Lane Edge

Table 13: Average Distance between Milling Edge and As-Built Lane Edge

| Section | AA01 | AA02 | AA61 | AA03 |
| --- | --- | --- | --- | --- |
| Average Distance between Milling Edge and Overlay Edge – inch (mm) | 12.6 (320) | 9.0 (229) | 14.0 (356) | 14.9 (378) |

Table 14: Overlay Thickness in Test Sections

| Section | Overlay Thickness – inch (mm) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Minimum | Maximum | Average | Standard Deviation |
| AA01 | 1.77 (45) | 2.99 (76) | 2.28 (58) | 0.23 (5.9) |
| AA02 | 1.85 (47) | 2.72 (69) | 2.28 (58) | 0.21 (5.2) |
| AA61 | 1.93 (49) | 2.87 (73) | 2.47 (63) | 0.24 (6.0) |
| AA03 | 1.77 (45) | 2.76 (70) | 2.34 (59) | 0.18 (4.7) |

Table 15: Pavement Structure of Test Sections

| Section | Bound Treated Base inch (mm) | AC Layer – inch (mm) |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Interlayer | Binder Course | Surface Layer | Overlay |
| AA01 | 5.8 (147.3) | 3.2 (81.3) | 1.7 (43.2) | 1.7 (43.2) | 2.5 (63.5) |
| AA02 | 5.7 (144.8) | 3.1 (78.7) | 2.2 (55.9) | 1.8 (45.7) | 2.3 (58.4) |
| AA61 | 4.5 (114.3) | 3.2 (81.3) | 2.3 (58.4) | 1.8 (45.7) | 2.3 (58.4) |
| AA03 | 3.9 (99.1) | 3.1 (78.7) | 1.7 (43.2) | 1.2 (30.5) | 2.3 (58.4) |

# chapter 4: SUMMARY

The 83AA00 project is the first SPS-10 experiment in Canada and in the North Central region of the LTPP program. The project included four test sections (83AA01, 83AA02, 83AA03 and 83AA61) designed to capture the performance differences between Warm Mix Asphalt and conventional Hot Mix Asphalt. The Manitoba SPS-10 project is located on Provincial Trunk Highway (PTH) 16 in the Municipality of WestLake–Gladstone, Manitoba. The test sections are located approximately 98 miles (157 km) west of Winnipeg, Manitoba. Within the project limits, PTH 16 is a two-lane undivided highway.

The construction consisted of a 2 inch (50.8 mm) overlay. Section 83AA01 was built using conventional hot mix asphalt. The other three test sections were constructed using warm mix technology. Construction of all three test sections began with milling on July 18 and were completed on August 26, 2015.

The project construction was performed according the project scope and detailed construction plan.

# chapter 5: KEY OBSERVATIONS

It should be noted that there was minor material variability identified by MIT compared to the mix design during the construction of the first test section (83AA01). Further investigation was performed by MIT in the asphalt plant. The investigation concluded that the loader operator in the asphalt plant was confused between crushed fines and natural fines. This error resulted in the production of HMA and WMA with low air voids in all test sections (2.6% to 3.3%). The error was corrected in subsequent loads of fine aggregates to the mixing drum. However, the air void percentage gradually increased as the pavement operation progressed on the LTPP test sections. MIT performed quality control checks on samples collected from all four sections. The air voids determined from the quality control samples were 2.6%, 2.8%, 3.0% and 3.3% for the 83AA01, 83AA02, 83AA61 and 83AA03, respectively.

## performance DATA

Manual Distress Surveys (MDS) were conducted by certified raters based on the LTPP Distress Identification Manual (DIM), FHWA-HRT-13-092 revised May 2014, on the project prior to construction and directly following construction on October 6, 2015. Details are as follows and can be seen in Table 16, supporting photos are provided in Appendix A.

## Surface Distress

### 83AA01

Prior to the project construction on June 9, 2015 the test section 83AA01 exhibited low severity fatigue cracking at 31.5 ft2 (2.9 m2), low severity non-wheelpath unsealed and sealed longitudinal cracking at 415.0 ft and 37.7 ft (126.5 m and 11.5 m), low severity unsealed and sealed transverse cracking at 155.8 ft and 12.1 ft (47.5 m and 3.7 m) and moderate severity unsealed transverse cracking at 109.3 ft (33.3 m). Test section 83AA01 did not exhibit any distresses in the initial survey conducted following construction on October 6, 2015.

### 83AA02

Prior to the project construction on May 4, 2015 the test section 83AA02 exhibited low severity fatigue cracking 81.9 ft2 (7.6 m2), low severity non-wheelpath unsealed and sealed longitudinal cracking at 38.1 ft and 24.9 ft (11.6 m and 7.6 m), moderate severity non-wheelpath unsealed and sealed longitudinal cracking at 300.2 ft and 200.1 ft (91.5 m and 61.0 m), low severity unsealed transverse cracking at 97.1 ft (29.6 m), moderate severity unsealed and sealed transverse cracking at 141.1 ft and 12.8 ft (43.0 m and 3.9 m), and high severity unsealed transverse cracking at 64.0 ft (19.5 m). Test section 83AA02 did not exhibit any distresses in the initial survey conducted following construction on October 6, 2015.

### 83AA03

Prior to the project construction on May 5, 2015 the test section 83AA03 exhibited low severity fatigue cracking at 571.5 ft2 (53.1 m2), moderate severity non-wheelpath unsealed longitudinal cracking at 500.3 ft (152.5 m), low severity unsealed transverse cracking at 145.7 ft (44.4 m), moderate severity unsealed and sealed transverse cracking at 266.1 ft and 21.7 ft (81.1 m and 6.6 m) and high severity unsealed transverse cracking at 22.3 ft (6.8 m). Test section 83AA03 did not exhibit any distresses in the initial survey conducted following construction on October 6, 2015.

### 83AA61

Prior to the project construction on May 4, 2015 the test section 83AA61 exhibited low severity fatigue cracking at 3.6 ft2 (0.3 m2), moderate severity non-wheelpath unsealed longitudinal cracking at 500.3 ft (152.5 m), low severity unsealed and sealed transverse cracking at 51.2 ft and 27.9 ft (15.6 m and 8.5 m), moderate severity unsealed transverse cracking at 25.6 ft (7.8 m) and high severity unsealed transverse cracking at 102.7 ft (31.3 m). Test section 83AA61 did not exhibit any distresses in the initial survey conducted following construction on October 6, 2015.

Table 16: Distress Severities for Each Test Section Prior to and Following Construction

| Test Section | Survey Date |  |  | Distress Type |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Fatigue ft2 (m2) | Longitudinal cracking ft (m) |  |  |  |  |  |  | Transverse cracking ft (m) |  |  |  |  |  |  |  |  |  |  |
|  |  | Low | Low |  |  | Moderate |  | High |  | Low |  |  | Moderate |  |  |  |  | High |  |  |
|  |  |  | Total |  | Sealed | Total | Sealed | Total | Sealed | Total |  | Sealed | Total |  | Sealed |  |  | Total | Sealed |  |
| 83AA01 | *6/9/2015 | 31.2 (2.9) | 452.8 (138.0) |  | 37.7 (11.5) | 0.00 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 168.0 (51.2) |  | 12.1 (3.7) | 109.3 (33.3) |  | 0.0 (0.0) |  |  | 0.0 (0.0) | 0.0 (0.0) |  |
|  | 10/6/2015 | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) |  |  | 0.0 (0.0) | 0.0 (0.0) |  |
| 83AA02 | *5/4/2015 | 81.8 (7.6) | 63.0 (19.2) |  | 24.9 (7.6) | 500.3 (152.5) | 200.1 (61.0) | 0.0 (0.0) | 0.0 (0.0) | 97.1 (29.6) |  | 0.0 (0.0) | 144.0 (43.9) |  | 12.8 (3.9) |  |  | 64.0 (19.5) | 0.0 (0.0) |  |
|  | 10/6/2015 | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) |  |  | 0.0 (0.0) | 0.0 (0.0) |  |
| 83AA03 | *5/5/2015 | 571.6 (53.1) | 0.0 (0.0) |  | 0.0 (0.0) | 500.3 (152.5) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 79.1 (24.1) |  | 27.9 (8.5) | 25.6 (7.8) |  | 0.0 (0.0) |  |  | 102.7 (31.3) | 0.0 (0.0) |  |
|  | 10/6/2015 | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) |  |  | 0.0 (0.0) | 0.0 (0.0) |  |
| 83AA61 | *5/4/2015 | 3.2 (0.3) | 0.0 (0.0) |  | 0.0 (0.0) | 500.3 (152.5) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 145.7 (44.4) |  | 0.0 (0.0) | 287.7 (87.7) |  | 21.7 (6.6) |  |  | 22.3 (6.8) | 0.0 (0.0) |  |
|  | 10/6/2015 | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) | 0.0 (0.0) |  | 0.0 (0.0) |  |  | 0.0 (0.0) | 0.0 (0.0) |  |
| *Note: This data is pre-overlay. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

### Rutting

Rutting is defined as a longitudinal surface depression in the wheel path. Table 17 indicates the rutting at each point in time at project 83AA00. The pre-overlay rutting data was collected using a Face Dipstick® Model 2200 Profiler. The October 2015 rutting data was collected using a Face Dipstick® Model 2000 Profiler.

Table 17: Rutting Depth at 83AA00

| Section | Date | Rutting Depth inches (mm) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Left |  |  |  | Right |  |  |  | Mean Left/Right |
|  |  | Min | Max | Mean | SD | Min | Max | Mean | SD |  |
| 83AA01 | *6/9/2015 | 0.02 (0.55) | 0.14 (3.58) | 0.05 (1.31) | 0.04 (0.99) | 0.07 (1.70) | 0.15 (3.70) | 0.10 (2.45) | 0.03 (0.66) | 0.07 (1.88) |
|  | 10/6/2015 | 0.00 (0.07) | 0.01 (0.38) | 0.01 (0.27) | 0.00 (0.10) | 0.01 (0.27) | 0.03 (0.67) | 0.02 (0.46) | 0.00 (0.12) | 0.01 (0.37) |
| 83AA02 | *5/4/2015 | 0.00 (0.00) | 0.07 (1.80) | 0.03 (0.85) | 0.02 (0.47) | 0.04 (0.90) | 0.08 (2.15) | 0.06 (1.46) | 0.02 (0.40) | 0.05 (1.16) |
|  | 10/6/2015 | 0.01 (0.20) | 0.03 (0.85) | 0.02 (0.47) | 0.01 (0.15) | 0.00 (0.05) | 0.02 (0.48) | 0.01 (0.31) | 0.01 (0.13) | 0.02 (0.39) |
| 83AA03 | *5/5/2015 | 0.07 (1.77) | 0.19 (4.87) | 0.12 (3.02) | 0.04 (1.06) | 0.04 (1.00) | 0.16 (4.02) | 0.11 (2.71) | 0.04 (0.98) | 0.11 (2.87) |
|  | 10/6/2015 | 0.00 (0.12) | 0.03 (0.78) | 0.02 (0.45) | 0.01 (0.21) | 0.00 (0.00) | 0.02 (0.55) | 0.01 (0.35) | 0.01 (0.17) | 0.02 (0.40) |
| 83AA61 | *5/4/2015 | 0.01 (0.20) | 0.09 (2.25) | 0.05 (1.24) | 0.02 (0.57) | 0.08 (1.98) | 0.14 (3.55) | 0.10 (2.61) | 0.02 (0.52) | 0.08 (1.93) |
|  | 10/6/2015 | 0.01 (0.13) | 0.03 (0.84) | 0.01 (0.36) | 0.01 (0.19) | 0.01 (0.17) | 0.03 (0.65) | 0.02 (0.46) | 0.01 (0.15) | 0.02 (0.41) |

*Note: This data is pre-overlay.

## LONGITUDINAL PROFILE

The International Roughness Index (IRI) is a statistic calculated from a longitudinal profile measured with an Ames Engineering 8300 Survey Pro High Speed Profiler (LTPP unit 830112) in the inside and outside wheelpaths of pavement. The average of these two statistics is reported as the roughness of the pavement section. It is recorded in meters per kilometer (m/km). The average IRI determined for each section is presented in Table 18 below.

Table 18: Average IRI for each Test Section

| Section | Test Date | Avg. Air Temp. °F (°C) | Average IRI in/mi (m/km) |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Average | Left Wheelpath | Right Wheelpath |
| 83AA01 | *6/4/2015 | 73.4 (23) | 100.11 (1.58) | 99.48 (1.57) | 101.38 (1.60) |
|  | 10/7/2015 | 50.0 (10) | 40.55 (0.64) | 36.12 (0.57) | 44.35 (0.70) |
| 83AA02 | *5/5/2015 | 78.8 (26) | 94.41 (1.49) | 98.84 (1.56) | 89.97 (1.42) |
|  | 10/7/2015 | 50.0 (10) | 34.85 (0.55) | 33.58 (0.53) | 36.12 (0.57) |
| 83AA03 | *5/5/2015 | 78.8 (26) | 109.61 (1.73) | 122.28 (1.93) | 96.31 (1.52) |
|  | 10/7/2015 | 50.0 (10) | 35.48 (0.56) | 31.68 (0.50) | 39.28 (0.62) |
| 83AA61 | *5/5/2015 | 78.8 (26) | 116.58 (1.84) | 120.38 (1.90) | 112.15 (1.77) |
|  | 10/7/2015 | 50.0 (10) | 40.55 (0.64) | 36.12 (0.57) | 44.99 (0.71) |

*Note: This data is pre-overlay.

### Texture

Pavement surface texture data was collected simultaneously with longitudinal profile data. The Ames Engineering 8300 Survey Pro High Speed Profiler is capable of determining macrotexture depth at highway speeds. Macrotexture is the primary component of high-speed, wet skid resistance. The mean profile depth (MPD) represents the surface texture of pavements. The calculation of MPD from a profile of pavement macrotexture is derived from ASTM E1845-Standard Practice for Calculating Pavement Macrotexture Mean Profile Depth. The texture data is presented in Table 19. Pavement surface texture can affect road safety (friction and rolling resistance), vehicle fuel economy, vibration, and tire wear, as well as noise to vehicle occupants and the surrounding communities.

Table 19: Average Texture Mean Profile Depth (MPD) for each Test Section

| Section | Test Date | Mean Profile Depth in (mm) |  |  |
| --- | --- | --- | --- | --- |
|  |  | Left | Right | Average |
| 83AA01 | *6/4/2015 | 0.057 (1.45) | 0.059 (1.51) | 0.058 (1.48) |
|  | 10/7/2015 | 0.022 (0.55) | 0.18 (0.46) | 0.020 (0.50) |
| 83AA02 | *5/5/2015 | 0.057 (1.44) | 0.057 (1.46) | 0.057 (1.45) |
|  | 10/7/2015 | 0.025 (0.64) | 0.022 (0.57) | 0.024 (0.60) |
| 83AA03 | *5/5/2015 | 0.060 (1.53) | 0.059 (1.49) | 0.059 (1.51) |
|  | 10/7/2015 | 0.024 (0.60) | 0.021 (0.53) | 0.022 (0.57) |
| 83AA61 | *5/5/2015 | 0.056 (1.43) | 0.058 (1.47) | 0.057 (1.45) |
|  | 10/7/2015 | 0.024 (0.60) | 0.021 (0.54) | 0.022 (0.57) |

*Note: This data is pre-overlay.

## DEFLECTION

A Dynatest Falling Weight Deflectometer (FWD), model 8002 with CP-15 LTPP specifications, was used to perform deflection testing before the rehabilitation. The AASHTO 1993 analysis procedure along with the ELMOD 6.0® software were used for the FWD back-calculation analysis. ELMOD created by Dynatest, analyzes the pavement response from the FWD by determining the modulus, stress and strain of each significant layer. The software considers the use of calculated and allowable forces at critical points within the pavement structure, loading, stress and strain relationships, and pavement distress.

The deflections are recorded from nine sensors, each located at varying distances from the load cell. However, for back-calculated parameters only data from eight sensors are used, the data from the sensor in front of the load plate (D9) has been excluded for processing purposes. To yield comparable results, the deflection data from these surveys were normalized to 8.99 kip (40 kN) load under a load plate of 5.9 inch (150 mm) radius, producing a pressure of 81.9 lb/in2 (565 kPa). The measured deflections and the pavement layer information were used to determine the resilient moduli of the subgrade and pavement structure. The analysis was completed for each test point. The back-calculated results are shown in Table 20. Figure 23 and Figure 24 show results from all sensors for each test section.

Table 20: Back-Calculation Results for 83AA00

| Section | Date | D1 Average (µm) | MR Average (MPa) | EP Average (MPa) | EAC Average (MPa) | EAgg Average (MPa) | SNEFF Average |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 83AA01 | *6/9/2015 | 133 | 45.9 | 6,144 | 11,822 | 1,429 | 5.7 |
|  | 10/6/2015 | 133 | 52.5 | 3,922 | 7,030 | 997 | 5.4 |
| 83AA02 | *5/4/2015 | 114 | 55.4 | 4,305 | 11,854 | 645 | 6.2 |
|  | 10/6/2015 | 119 | 57.7 | 3,539 | 7,827 | 815 | 6.1 |
| 83AA03 | *5/5/2015 | 161 | 55.7 | 3,486 | 8,655 | 261 | 4.3 |
|  | 10/6/2015 | 144 | 59.6 | 3,469 | 7,070 | 431 | 4.6 |
| 83AA61 | *5/4/2015 | 104 | 61 | 8,002 | 13,790 | 1,988 | 5.7 |
|  | 10/6/2015 | 102 | 65.5 | 6,578 | 12,065 | 1,253 | 5.8 |

*Note: This data is pre-overlay.

Figure 23: Normalized Deflection for test sections 83AA01 and 83AA02

Figure 24: Normalized Deflection for test sections 83AA03 and 83AA61

## CONSTRUCTION

The project team did not witness equipment breakdowns that would directly impact the construction of project 83AA00. The equipment in the asphalt plant and on-site were functioning at typical rates of productivity.

The construction of the four test sections was performed on a sunny day with no rain events. The day following the test section construction witnessed a thunderstorm accompanied by heavy rain.

# Appendix A: Construction Photographs

Figure 25: 83AA01 Before Construction

Figure 26: 83AA01 During Construction

Figure 27: 83AA01 After Construction

Figure 28: 83AA02 Before Construction

Figure 29: 83AA02 During Construction

Figure 30: 83AA02 After Construction

Figure 31: 83AA03 Before Construction

Figure 32: 83AA03 During Construction

Figure 33: 83AA03 After Construction

Figure 34: 83AA61 Before Construction

Figure 35: 83AA61 During Construction

Figure 36: 83AA61 After Construction

Figure 37: Asphalt Plant Overview

Figure 38: Asphalt Plant Overview

Figure 39: Asphalt Plant Operations

Figure 40: Asphalt Plant – Cold Feed Bins

Figure 41: Asphalt Plant – Asphalt Binder

Figure 42: Asphalt Plant – Cold Feed Conveyer

Figure 43: Asphalt Plant – Storage Tank and AC Discharge Area

Figure 44: Asphalt Plant – Evotherm®

Figure 45: Asphalt Plant – Asphalt Concrete Drum Mixer

Figure 46: Paving Operations - Paver

Figure 47: Paving Operations - Hopper

Figure 48: Paving Operations – End-Dump Truck

Figure 49: Paving Operations – End-Dump Truck to Hopper

Figure 50: Paving Operations – Hopper to Paver

Figure 51: Paving Operations on 83AA00

Appendix B: Mix Designs

| STATE | Manitoba |  |  |  |
| --- | --- | --- | --- | --- |
| SECTION | 83AA01 | 83AA02 | 83AA03 | 83AA61 |
| C/S | Core |  |  | Supplemental |
| HWY | Provincial Trunk Highway 16 Eastbound |  |  |  |
| CLASS | Rural Principal Arterial - Other |  |  |  |
| GPS | 50.22567, -99.07133 |  |  |  |
| STATUS | Constructed August 2015 |  |  |  |
| TRAFFIC | AADT: 2,990 ESALs: 439,000 |  |  |  |
| CLIMATE | Dry, Freeze |  |  |  |
| PAVEMENT | 8.0" Hot-mix Asphalt Concrete below test layer (post-mill) |  |  |  |
| BASE | 5.0" Sand Asphalt |  |  |  |
| SUBBASE | No Subbase |  |  |  |
| SUBGRADE | Sand |  |  |  |
| MILL | Mill 1" |  |  |  |
| O/L | 2" |  |  |  |
| WMA |  |  |  |  |
| HMA |  |  |  |  |
| AC TYPE | Marshall Mix - Bituminous Mix B | Marshall Mix - Bituminous Mix B | Marshall Mix - Bituminous Mix B | Marshall Mix - Bituminous Mix B |
| VIRGIN BINDER | 150/200 pen | 150/200 pen | 150/200 pen | 150/200 pen |
| AC % | 4.6% | 4.6% | 4.6% | 4.6% |
| RAP | 15% | 15% | 15% | 15% |
| RAS | 0% | 0% | 0% | 0% |
| FINAL AC % | 5.5% | 5.5% | 5.5% | 5.5% |
| ADDITIVE #1 | - | Aesco/Madsen Foaming Technology (water) | Evotherm® | Aesco/Madsen Foaming Technology (water) |
| % | - | 1.0% | 0.3% | 1.0% |
| ADDITIVE #2 | - | - | - | Evotherm® |
| % | - | - | - | 0.3% |
| AGGREGATE | Nominal Max size 1/2" | Nominal Max size 1/2" | Nominal Max size 1/2" | Nominal Max size 1/2" |

# Appendix C: Materials Sampling and Testing Layouts

Figure 52: Density Measurement Layout for Test Section 83AA01 Manitoba SPS-10

Figure 53: Density Measurement Layout for Test Section 83AA02 Manitoba SPS-10

Figure 54: Density Measurement Layout for Test Section 83AA61 Manitoba SPS-10

Figure 55: Density Measurement Layout for Test Section 83AA03 Manitoba SPS-10

Figure 56: Sampling and Testing Layout for Test Section 83AA01 at Time 0 Manitoba SPS-10

Figure 57: Sampling and Testing Layout for Test Section 83AA02 at Time 0 Manitoba SPS-10

Figure 58: Sampling and Testing Layout for Test Section 83AA61 at Time 0 Manitoba SPS-10

Figure 59: Sampling and Testing Layout for Test Section 83AA03 at Time 0 Manitoba SPS-10

# Appendix D: Other Construction Documents

Standard Specification for Bituminous Pavement –   PTH 16

Recycled Bituminous Pavement, Class “B”

In general, Recycled Bituminous Pavement on PTH 16 shall be constructed as follows:

For the SPS-10 Project 83AA00, with Project Beginning at Station 475+00 and Project Ending at Station 495+00, the depth specifications for the bituminous pavement are 50mm (main lanes) and 100mm (shoulder).

Shoulder Preparation, Type II (Modified)

Notwithstanding Specification 700.7.3.1.3 the following shall apply:

The Contractor shall prepare the shoulder surface by pulverizing the existing asphalt pavement and shoulder gravel such that no particle has a dimension greater than 50mm in any plane. The Contractor shall pulverize the existing 0.8m paved shoulder and 1.2m gravel shoulder to an average depth of 100mm and cut the existing shoulder to an average depth of 250mm below the top of the existing bituminous pavement at the test locations.

Specification No. 700

7.3.1.3		Type II Shoulder Preparation

Type II Shoulder Preparation will involve cutting the existing shoulder adjacent to the pavement and blading the resulting material outward to achieve a crossfall and width as shown in the Tender. If the existing shoulders are not uniform, varying depths of cut may be required to achieve the necessary width. New granular base course shall be added and compacted to the level of the existing pavement prior to

constructing the first lift of pavement adjacent thereto.

The prepared shoulders shall be sufficiently compacted to allow for the placement of

new granular material.

New granular material shall be compacted as follows:

a) to 98% AASHTO Standard Dry Density when the shoulders are to be paved; or

b) to 95% AASHTO Standard Dry Density when the shoulders are to be granular.

The Contractor shall schedule this work to ensure that drop-offs are backfilled and compacted, or a fillet constructed, before terminating work each day.

# Appendix E: Complete Set of SPS-10 Data Sheets

# Appendix F: SPS-10 Deviation Report

| LTPP SPS-10 Project Deviation Report Project Summary Sheet | State Code 83 Project Code AA00 |
| --- | --- |
| Project Classification Information |  |
| SPS Experiment Number: 10 | State or Province: Manitoba |
| LTPP Region: □ North Atlantic ■ North Central □ Southern □ Western |  |
| Climate Zone: ■ Dry-Freeze □ Dry-No Freeze □ Wet-Freeze □ Wet-No Freeze |  |
| Traffic: □ High ■ Low |  |
| Construction Start Date: July 18, 2015 | Construction End Date: August 26, 2015 |
| Deviation Summary |  |
| Site Location Deviations: ■ No Deviations □ Minor Deviations □ Significant Deviations |  |
| Construction Deviations: □ No Deviations ■ Minor Deviations □ Significant Deviations |  |
| Data Collection and Processing Status Summary |  |
| Inventory Data: ■ Complete Submission □ Incomplete □ Data Not Available □ N/A |  |
| Materials Data: ■ All Scheduled Samples Obtained and Tested □ Incomplete/No Test Data |  |
| Construction Data: ■ All Required Data Obtained □ Incomplete/Missing Data Elements |  |
| Historical Traffic Data: ■ All Required Historical Estimates Submitted □ Required Estimates Not Submitted □ N/A |  |
| Traffic Monitoring Equipment: □ WIM Installed On-Site □ AVC Installed On-Site □ ATR Installed On-Site ■ No Equipment Installed |  |
| Traffic Monitoring: ■ Preferred □ Continuous □ Minimum □ Below Minimum □ Site Related |  |
| Traffic Monitoring Data: ■ Monitoring Data Submitted □ No Monitoring Data Submitted |  |
| FWD Measurements: ■ Preconstruction Tests Performed □ Construction Tests Performed ■ Post-Construction Tests Performed |  |
| Profile/Texture Measurements: ■ Preconstruction Tests Performed ■ Post-Construction Tests Performed |  |
| Distress Measurements: ■ Preconstruction Tests Performed ■ Post-Construction Tests Performed |  |
| Rehabilitation Data: ■ Complete Submission □ Incomplete □ Data Not Available □ N/A |  |
| Report Status |  |
| Materials Sampling and Test Plan: ■ Document Prepared □ Final Submitted to FHWA |  |
| Construction Report: ■ Document Prepared □ Final Submitted to FHWA |  |

| LTPP SPS-10 Project Deviation Report Construction Guidelines Deviations | State Code 83 Project Code AA00 |
| --- | --- |
| ■ Comments Pertain to All Test Sections on Project □ Comments Pertain Only to Section(s): (Specify) ______________________________________________ |  |
| Construction Guidelines Deviation Comments: MIT identified minor material variability compared to the mix design during the construction of the first test section (83AA01). Further investigation was performed by MIT in the asphalt plant. The investigation concluded that the loader operator in the asphalt plant was confused between crushed fines and natural fines. This error resulted in the production of HMA and WMA with low air voids in all test sections (2.6% to 3.3%). The error was corrected in subsequent loads of fine aggregates to the mixing drum. However, the air void percentage gradually increased as the pavement operation was progressing on the LTPP test sections. MIT performed quality control checks on samples collected from the four sections. The air voids determined from the quality control samples were 2.6%, 2.8%, 3.0% and 3.3% for the 83AA01, 83AA02, 83AA61 and 83AA03 respectively. |  |

Prepared by: Giannin Viecili	         Date: September 2016

# Acknowledgements

The original map is the copyright property of Google® Earth TM and can be accessed from https://google.com/earth. The map overlays showing site, test sections, AC mix plant, and planned AVC installation locations were developed as a result of this research project. The overlays include text labels showing the project, AC mix plant, and AVC installation locations; and red dots showing the layout of test sections along PTH 16.

The original map is the copyright property of Online Topo Maps® and can be accessed from http://onlinetopomaps.net. The map overlays showing the topography of the site were developed as a result of this research project. The overlays include red dots and text labels along PTH 16 showing the layout of the test sections.

Geography of Manitoba: Its Land and People, 1996

http://climate.weather.gc.ca/advanceSearch/searchHistoricData_e.html