ONTARIO SPS-10 PROJECT 87AA00

# MATERIALS SAMPLING AND TESTING PLAN

For t3 (18 Months After Construction)

Contents

MATERIALS SAMPLING AND TESTING PLAN	0

GENERAL LAYOUT INFORMATION	1

MATERIALS SAMPLING AND FIELD TESTING	5

LABORATORY MATERIALS TESTING	22

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Ontario SPS-10 project 87AA00 in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  Table 2 indicates transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Figure 1 presents an overview of the highway and the sequence of test sections on the northbound lane. Additionally, Figure 2 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION – 87AA00

| Section Number | SHRP ID | Description |
| --- | --- | --- |
| 01 | 87AA01 | Control Section 2” Superpave 12.5 FC2 (PG 58-28) Hot Mix Asphalt 15% RAP |
| 02 | 87AA02 | WMA Core Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Foaming Process Water Dosage: 2.0% of Virgin Asphalt Cement 15% RAP |
| 03 | 87AA03 | WMA Core Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Chemical 1 – Evotherm® M1 Additive Dosage: 0.3% of Virgin Asphalt Cement 15% RAP |
| 04 | 87AA61 | WMA Supplemental Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Chemical 2 – WarmGrip® E5 Additive Dosage: 0.5% of Virgin Asphalt Cement 15% RAP |
| 05 | 87AA62 | WMA Supplemental Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Organic – Rediset® WMX 8017 Additive Dosage: 1.5% of Virgin Asphalt Cement 15% RAP |

87AA01

HMA Control Section
Superpave 12.5 FC2

(PG 58-28)

Transition

87AA02

WMA Foaming Process

Superpave 12.5 FC2

(PG 58-28)

Transition

87AA03

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
Evotherm® M1

827ft

252m

19+254

21+030

19+002

820ft

250m

Transition

87AA61

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
WarmGrip® E5

Transition

87AA62

WMA Organic Additive
Superpave 12.5 FC2
(PG 58-28)
Rediset® WMX 8017

820ft

250m

886ft

270m

886ft

270m

21+280

23+000

23+250

11+280

11+550

12+750

13+020

NOTE: St. 24+616 = St. 10+000

FIGURE 1: ONTARIO SPS-10 87AA00 PROJECT LAYOUT

Northbound Traffic

TABLE 2: TEST SECTION LAYOUT – 87AA00

| Project Begin STA | Project End STA | Experiment Begin STA feet (meter) | Experiment End STA feet (meter) | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
| 18+250 | 19+002 |  |  | START | East Gwillimbury |
| 19+002 | 19+037.05 | 0-165 (0-50.3) | 0-50 (0-15.25) | Sampling Area | 87AA01 |
| 19+037.05 | 19+052.30 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 19+052.30 | 19+204.62 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 19+204.62 | 19+219.87 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 19+219.87 | 19+254 | 5+50 (1+67.25) | 5+162(2+01.38) | Sampling Area |  |
| 19+254 | 21+030 |  |  | Transition |  |
| 21+030 | 21+066.33 | 0-159(0-48.58) | 0-50 (0-15.25) | Sampling Area | 87AA02 |
| 21+066.33 | 21+078.58 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 21+078.58 | 21+231.06 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 21+231.06 | 21+246.31 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 21+246.31 | 21+280 | 5+50 (1+67.25) | 5+161(2+00.94) | Sampling Area |  |
| 21+280 | 23+000 |  |  | Transition |  |
| 23+000 | 23+031.53 | 0-154(0-46.78) | 0-50 (0-15.25) | Sampling Area | 87AA03 |
| 23+031.53 | 23+046.78 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 23+046.78 | 23+199.55 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 23+199.55 | 23+214.8 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 23+214.8 | 23+250 | 5+50 (1+67.25) | 5+166(2+02.45) | Sampling Area |  |
| 23+250 | 11+280 |  |  | Transition (24+616=10+000) | Georgina |
| 11+280 | 11+334.38 | 0-228(0-69.63) | 0-50 (0-15.25) | Sampling Area | 87AA61 |
| 11+334.38 | 11+349.63 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 11+349.63 | 11+501.82 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 11+501.82 | 11+517.07 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 11+517.07 | 11+550 | 5+50 (1+67.25) | 5+158(2+00.18) | Sampling Area |  |
| 11+550 | 12+750 |  |  | Transition |  |
| 12+750 | 12+806.29 | 0-235(0-71.54) | 0-50 (0-15.25) | Sampling Area | 87AA62 |
| 12+806.29 | 12+821.54 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 12+821.54 | 12+973.84 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 12+973.84 | 12+989.09 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 12+989.09 | 13+020 | 5+50 (1+67.25) | 5+151(1+98.16) | Sampling Area |  |
| 13+020 | 13+830 |  |  | END |  |

Sampling Area 011 – 110ft (34.0m)

Buffer Area – 50ft (15.25m)

87AA01

HMA Control Section
Superpave 12.5 FC2

(PG 58-28)

500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 021 – 110ft (34.0m)

Transition (1.776km)

Sampling Area 031 – 111ft (34.5m)

Buffer Area – 50ft (15.25m)

87AA02

WMA Foaming Process

Superpave 12.5 FC2

(PG 58-28)
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 041 – 109ft (33.5m)

Transition (1.720km)

Buffer Area – 50ft (15.25m)

87AA03

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
Evotherm® M1
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 061 – 110ft (34.0m)

Sampling Area 051 – 110ft (34.0m)

827ft (252m)

820ft (250m)

820ft (250m)

NB Traffic

19+254

21+030

19+002

21+280

23+000

23+250

19+052.306

19+204.620

21+078.580

21+231.060

23+046.780

23+199.550

Sampling Area 071 – 131ft (40.6m)

Buffer Area – 50ft (15.25m)

87AA61

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
WarmGrip® E5
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 081 – 122ft (37.4m)

Transition (1.200km)

Sampling Area 091 – 117ft (36.0m)

Buffer Area – 50ft (15.25m)

87AA62

WMA Organic Additive
Superpave 12.5 FC2
(PG 58-28)
Rediset® WMX 8017
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 101 – 136ft (42.0m)

886ft (270m)

886ft (270m)

NB Traffic

11+280

11+550

12+750

13+020

11+349.630

11+501.820

12+821.540

12+973.840

24+616=10+000

Transition (2.646km)

FIGURE 2: ONTARIO SPS-10 PROJECT LAYOUT – 87AA00

NOTE: St. 24+616 = St. 10+000

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides the materials sampling and testing activities that will occur in the field at time three (t3 is 18 months after construction).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 3 through 12 show the locations for the many samples and tests scheduled.  Figures 3 through 7 show density measurement layouts and Figures 8 through 12 show the material sampling locations for each section as well as the location of DCP testing.

Tables 6 through 10 list the samples acquired from each of the five test sections. Table 11 lists the samples to be collected from the asphalt plant.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 12 through 14 list samples to be shipped to the Central Lab Testing Contractor (CLTC) laboratory, the LTPP Materials Reference Library (MRL), and the Turner-Fairbank Highway Research Center (TFHRC), respectively.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t = Sampling time interval

- XX = Section number

Sample Number: S-M-##-t-XX
S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Ontario SPS-10, R = “A,” representing north Atlantic region)

- C = Construction event (For Ontario SPS-10, C = 1, representing first constructed SPS-10 in the North Bound and C = 2 represents the SPS-10 in the South Bound)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 61

  - B – 62

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

Labels and Tags

Each sample shall be labeled before packing in boxes and cartons. As a minimum, the following information shall be included on a tag or label attached to the specimen:

- SPECIMEN ID

- STATE CODE

- SHRP ID

- LOCATION DESIGNATION

- SAMPLE NUMBER

- DATE (mm-dd-yy, sampling date)

- FIELD SET (one digit number which will be 1 for the first round of sampling)

For cores, the HOLE ID shall be written directly on the core.  If the core contains more than one layer, layer boundaries shall be clearly marked, and each layer numbered.  For bulk samples, the SPECIMEN ID shall be written directly on the bag, bucket or can that contains the sample.

Packaging

Suggestions for labeling and combining the samples for shipment are as follows:

- All samples of like material (e.g., asphaltic concrete surface and binder) shall be placed in separate boxes or separate compartments of one box.

- Each sample shall have a label or tag attached that clearly identifies the material.  It is recommended that the label be color-coded by destination (e.g., contract Lab, FHWA lab, MRL, etc.).

- Each core shall be surrounded with "bubble-wrap" or other acceptable cushioning material on all sides within the shipping box.

- All bulk samples shall be marked with two labels or tags. One shall be placed inside the bag and one attached to the outside. A jar sample for moisture testing of each bulk sample shall be placed inside the bulk sample bag.

- All shipping boxes should be wood of suitable grade and construction to withstand shipping and subsequent moving without breakage of the box or damaging of samples.

- All boxes should be adequately secured by nails or screws prior to shipping.

LTPP Field Operations Information Sheets 1 and 2 shall be sent with each shipment of materials samples.

TABLE 3: PROJECT LAYER NUMBERING

| Project Layer Code | Layer No. | Description | Material Code | Thickness |
| --- | --- | --- | --- | --- |
| A | 1 | Subgrade | 55 |  |
| B | 2 | Granular Subbase | 23 | 7” – 10” (175-250 mm) |
| C | 3 | Granular Base | 23 | 6’’ (150 mm) |
| D | 4 | Old Pulverized AC Pavement | 14 | 6’’–10” (150-250 mm) |
| E | 5 | Existing AC Pavement (1.5” to be Milled) | 01 | 6” (150 mm) |
| F | 6 | Experimental AC Overlay Binder Layer – Superpave 19.0 | 01 | 2” (50 mm) |
| G | 7 | Experimental AC Overlay Surface Layer – Superpave 12.5 FC2 | 01 | 2” (50 mm) |

TABLE 4: SCOPE OF MATERIAL SAMPLING FROM NB 87AA00

| Material and Sample Description |  | No. of Samples | Sample Location |
| --- | --- | --- | --- |
| A. | t3 SAMPLING (18 months after construction) |  |  |
|  | 6" Core | 30 | C01301-C06301, C01302-C06302, C01303-C06303, C01361-C06361, C01362-C06362 |
|  | 12" Core (6’’ Core replacement) | 20 | A01301-A04301, A01302-A04302, A01303-A04303, A01361-A04361, A01362-A04362 |

TABLE 5: SCOPE OF FIELD TESTING FOR NB 87AA00

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | t3 TESTING (18 months after paving) |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Core Examination and Thickness (P01/AC01) | 50 | C01301-C06301, C01302-C06302, C01303-C06303, C01361-C06361, C01362-C06362 A01301-A04301, A01302-A04302, A01303-A04303, A01361-A04361, A01362-A04362 |

Section 87AA01 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03001

T02001

T01001

Traffic

FIGURE 3: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA01 ONTARIO SPS-10

Section 87AA02 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03002

T02002

T01002

Traffic

FIGURE 4: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA02 ONTARIO SPS-10

Section 87AA03 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03003

T02003

T01003

Traffic

FIGURE 5: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA03 ONTARIO SPS-10

Section 87AA61 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03061

T02061

T01061

Traffic

FIGURE 6: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA61 ONTARIO SPS-10

Section 87AA62 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03062

T02062

T01062

Traffic

FIGURE 7: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA62 ONTARIO SPS-10

C063011

C053011

C04301

5+50

5+70

Section STA:

Section: 87AA01

Description: HMAC Control Section

Sampling Area: 02

Sampling Interval: t3

Shoulder

C02301

2’

2’

1’

2’

2’

2’

C01301

C03301

A01301

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

Four 6” cores replacing one 12” Core Experimental AC

A02301

A03301

A04301

2’

1’

FIGURE 8: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA01 AT TIME 3 ONTARIO SPS-10

1’

C063021

C053021

C04302

5+50

5+70

Section STA:

Section: 87AA02

Description: Mix with WMA Foaming Process

Sampling Area: 04

Sampling Interval: t3

Shoulder

C02302

2’

2’

2’

2’

C01302

C03302

A01302

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

Four 6” cores replacing one 12” Core Experimental AC

A02302

A03302

A04302

2’

1’

2’

1’

FIGURE 9: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA02 AT TIME 3 ONTARIO SPS-10

1’

C063031

C053031

C04303

5+50

5+70

Section STA:

Section: 87AA03

Description: Mix with WMA Chemical Additive

Sampling Area: 06

Sampling Interval: t3

Shoulder

C02303

2’

2’

2’

2’

C01303

C03303

A01303

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

Four 6” cores replacing one 12” Core Experimental AC

A02303

A03303

A04303

2’

1’

2’

1’

FIGURE 10: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA03 AT TIME 3 ONTARIO SPS-10

1’

C063611

C053611

C04361

5+50

5+70

Section STA:

Section: 87AA61

Description: Supplemental Section 1

Sampling Area: 08

Sampling Interval: t3

Shoulder

C02361

2’

2’

2’

2’

C01361

C03361

A01361

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

Four 6” cores replacing one 12” Core Experimental AC

A02361

A03361

A04361

2’

1’

2’

1’

FIGURE 11: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA61 AT TIME 3 ONTARIO SPS-10

1’

C063621

C053621

C04362

5+50

5+70

Section STA:

Section: 87AA62

Description: Supplemental Section 2

Sampling Area: 10

Sampling Interval: t3

Shoulder

C02362

2’

2’

2’

2’

C01362

C03362

A01362

3’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

Four 6” cores replacing one 12” Core Experimental AC

A02362

A03362

A04362

2’

1’

2’

1’

FIGURE 12: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA62 AT TIME 3 ONTARIO SPS-10

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 87AA01 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01301 | 7 | BA01301 | A11A08L07 | 6” Core |
| A01301 | 6 | BA01301 | A11A08L06 | 6” Core |
| A02301 | 7 | BA02301 | A11A09L07 | 6” Core |
| A02301 | 6 | BA02301 | A11A09L06 | 6” Core |
| A03301 | 7 | BA03301 | A11A10L07 | 6” Core |
| A03301 | 6 | BA03301 | A11A10L06 | 6” Core |
| A04301 | 7 | BA04301 | A11A11L07 | 6” Core |
| A04301 | 6 | BA04301 | A11A11L06 | 6” Core |
| C01301 | 7 | CA01301 | A11C27L07 | 6" Core |
| C02301 | 7 | CA02301 | A11C28L07 | 6" Core |
| C03301 | 7 | CA03301 | A11C29L07 | 6" Core |
| C04301 | 7 | CA04301 | A11C30L07 | 6" Core |
| C05301 | 7 | CA05301 | A11C31L07 | 6" Core |
| C06301 | 7 | CA06301 | A11C32L07 | 6" Core |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 87AA02 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01302 | 7 | BA01302 | A12A08L07 | 6” Core |
| A02302 | 7 | BA02302 | A12A09L07 | 6” Core |
| A03302 | 7 | BA03302 | A12A10L07 | 6” Core |
| A04302 | 7 | BA04302 | A12A11L07 | 6” Core |
| C01302 | 7 | CA01302 | A12C27L07 | 6" Core |
| C02302 | 7 | CA02302 | A12C28L07 | 6" Core |
| C03302 | 7 | CA03302 | A12C29L07 | 6" Core |
| C04302 | 7 | CA04302 | A12C30L07 | 6" Core |
| C05302 | 7 | CA05302 | A12C31L07 | 6" Core |
| C06302 | 7 | CA06302 | A12C32L07 | 6" Core |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 87AA03 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01303 | 7 | BA01303 | A13A08L07 | 6" Core |
| A02303 | 7 | BA02303 | A13A09L07 | 6" Core |
| A03303 | 7 | BA03303 | A13A10L07 | 6" Core |
| A04303 | 7 | BA04303 | A13A11L07 | 6" Core |
| C01303 | 7 | CA01303 | A13C27L07 | 6" Core |
| C02303 | 7 | CA02303 | A13C28L07 | 6" Core |
| C03303 | 7 | CA03303 | A13C29L07 | 6" Core |
| C04303 | 7 | CA04303 | A13C30L07 | 6" Core |
| C05303 | 7 | CA05303 | A13C31L07 | 6" Core |
| C06303 | 7 | CA06303 | A13C32L07 | 6" Core |

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 87AA61 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01361 | 7 | BA01361 | A1AA08L07 | 6" Core |
| A02361 | 7 | BA02361 | A1AA09L07 | 6" Core |
| A03361 | 7 | BA03361 | A1AA10L07 | 6" Core |
| A04361 | 7 | BA04361 | A1AA11L07 | 6" Core |
| C01361 | 7 | CA01361 | A1AC27L07 | 6" Core |
| C02361 | 7 | CA02361 | A1AC28L07 | 6" Core |
| C03361 | 7 | CA03361 | A1AC29L07 | 6" Core |
| C04361 | 7 | CA04361 | A1AC30L07 | 6" Core |
| C05361 | 7 | CA05361 | A1AC31L07 | 6" Core |
| C06361 | 7 | CA06361 | A1AC32L07 | 6" Core |

TABLE 10: SAMPLES ACQUIRED FROM TEST SECTION 87AA62 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample |
| --- | --- | --- | --- | --- |
| A01362 | 7 | BA01362 | A1BA08L07 | 6" Core |
| A02362 | 7 | BA02362 | A1BA09L07 | 6" Core |
| A03362 | 7 | BA03362 | A1BA10L07 | 6" Core |
| A04362 | 7 | BA04362 | A1BA11L07 | 6" Core |
| C01362 | 7 | CA01362 | A1BC27L07 | 6" Core |
| C02362 | 7 | CA02362 | A1BC28L07 | 6" Core |
| C03362 | 7 | CA03362 | A1BC29L07 | 6" Core |
| C04362 | 7 | CA04362 | A1BC30L07 | 6" Core |
| C05362 | 7 | CA05362 | A1BC31L07 | 6" Core |
| C06362 | 7 | CA06362 | A1BC32L07 | 6" Core |

TABLE 11: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| AA01 | A11A08L07 | 6" Core |
|  | A11A09L07 | 6" Core |
|  | A11A10L07 | 6" Core |
|  | A11A11L07 | 6" Core |
| AA02 | A12A08L07 | 6" Core |
|  | A12A09L07 | 6" Core |
|  | A12A10L07 | 6" Core |
|  | A12A11L07 | 6" Core |
| AA03 | A13A08L07 | 6" Core |
|  | A13A09L07 | 6" Core |
|  | A13A10L07 | 6" Core |
|  | A13A11L07 | 6" Core |
| AA61 | A1AA08L07 | 6" Core |
|  | A1AA09L07 | 6" Core |
|  | A1AA10L07 | 6" Core |
|  | A1AA11L07 | 6" Core |
| AA62 | A1BA08L07 | 6" Core |
|  | A1BA09L07 | 6" Core |
|  | A1BA10L07 | 6" Core |
|  | A1BA11L07 | 6" Core |
| AA01 | A11C27L07 | 6" Core |
| AA01 | A11C28L07 | 6" Core |
| AA01 | A11C29L07 | 6" Core |
| AA02 | A12C27L07 | 6" Core |
| AA02 | A12C28L07 | 6" Core |
| AA02 | A12C29L07 | 6" Core |
| AA03 | A13C27L07 | 6" Core |
| AA03 | A13C28L07 | 6" Core |
| AA03 | A13C29L07 | 6" Core |
| AA61 | A1AC27L07 | 6" Core |
| AA61 | A1AC28L07 | 6" Core |
| AA61 | A1AC29L07 | 6" Core |
| AA62 | A1BC27L07 | 6" Core |
| AA62 | A1BC28L07 | 6" Core |
| AA62 | A1BC29L07 | 6" Core |

TABLE 12: SAMPLES TO BE SHIPPED TO MTO

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| AA01 | A11C30L07 | 6" Core |
| AA01 | A11C31L07 | 6" Core |
| AA01 | A11C32L07 | 6" Core |
| AA02 | A12C30L07 | 6" Core |
| AA02 | A12C31L07 | 6" Core |
| AA02 | A12C32L07 | 6" Core |
| AA03 | A13C30L07 | 6" Core |
| AA03 | A13C31L07 | 6" Core |
| AA03 | A13C32L07 | 6" Core |
| AA61 | A1AC30L07 | 6" Core |
| AA61 | A1AC31L07 | 6" Core |
| AA61 | A1AC32L07 | 6" Core |
| AA62 | A1BC30L07 | 6" Core |
| AA62 | A1BC31L07 | 6" Core |
| AA62 | A1BC32L07 | 6" Core |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Ontario SPS-10 projects.  The previous section ended with lists of samples to be shipped to each of the two laboratories, the central lab testing contractor (CLTC) laboratory and the Turner-Fairbank Highway Research Center (TFHRC).  In this section, the tests to be performed on each sample are listed.

Table 15 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Tables 16 and 17 provide new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used to ensure proper tracking using the Materials Tracking System (MTS).

Tables 18 through 25 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a specific test is complete.

TABLE 13: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: | Test Conducted By: |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | RSC |
| A. | EXPERIMENTAL AC |  |  |  |  |  |
|  | Core Exam. And Thickness | AC01 | P01 | 50 |  | X |
|  | Bulk Specific Gravity | AC02 | P02 | 15 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 10 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 10 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 10 | X |  |
|  | Bending Beam Rheometer (BBR) Test | AE08 | P28 | 10 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 10 | X |  |

TABLE 14: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Process | Description Type | Status |  |
| --- | --- | --- | --- |
|  |  | Original | Modified1 |
| Extraction | Sample No. | BA01301 | BAE1301 |
|  | Specimen ID | A11A08L07 | A11A08M07 |
|  | Sample No. | BA01302 | BAE1302 |
|  | Specimen ID | A12A08L07 | A12A08M07 |
|  | Sample No. | BA01303 | BAE1303 |
|  | Specimen ID | A13A08L07 | A13A08M07 |
|  | Sample No. | BA01361 | BAE1361 |
|  | Specimen ID | A1AA08L07 | A1AA08M07 |
|  | Sample No. | BA01362 | BAE1362 |
|  | Specimen ID | A1BA08L07 | A1BA08M07 |

- Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.

- Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 15: TRACKING TABLE OF EXPERIMENTAL AC SURFACE LAYER IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |  |  |
| A11A08L07 | P04/AC04 |  |  |  |  | No | E |
| A12A08L07 | P04/AC04 |  |  |  |  | No | E |
| A13A08L07 | P04/AC04 |  |  |  |  | No | E |
| A1AA08L07 | P04/AC04 |  |  |  |  | No | E |
| A1BA08L07 | P04/AC04 |  |  |  |  | No | E |
| A11A08M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| A12A08M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| A13A08M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| A1AA08M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |
| A1BA08M07 | P27/AE07 | P28/AE08 | P73/AE10 |  |  | No | D |

1. Next Process

D 	Remaining sample should be disposed			S 	Remaining sample should be stored
	C	Remaining sample will be combined with another sample	E 	Perform further testing on extracted sample
	P 	Perform further testing with PAV				R 	Perform further testing with RFTO
	R+P  	Perform further testing with RTFO + PAV

TABLE 15: TRACKING TABLE OF EXPERIMENTAL AC SURFACE LAYER IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY (CONTINUED)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third |  |  |  |  |
| A11C27L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A11C28L07 | P02/AC02 |  |  |  |  | Yes | S |
| A11C29L07 | P02/AC02 |  |  |  |  | Yes | S |
| A12C27L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A12C28L07 | P02/AC02 |  |  |  |  | Yes | S |
| A12C29L07 | P02/AC02 |  |  |  |  | Yes | S |
| A13C27L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A13C28L07 | P02/AC02 |  |  |  |  | Yes | S |
| A13C29L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1AC27L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A1AC28L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1AC29L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1BC27L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A1BC28L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1BC29L07 | P02/AC02 |  |  |  |  | Yes | S |

1. Next Process

D 	Remaining sample should be disposed				P 	Perform further testing with PAV
		S 	Remaining sample should be stored					R 	Perform further testing with RFTO
		C	Remaining sample will be combined with another sample		R+P  	Perform further testing with RTFO + PAV

E 	Perform further testing on extracted sample