ONTARIO SPS-10 PROJECT 87AA00

# MATERIALS SAMPLING AND TESTING PLAN

For t0 (At and Immediately After Construction)

Contents

MATERIALS SAMPLING AND TESTING PLAN	0

GENERAL LAYOUT INFORMATION	1

MATERIALS SAMPLING AND FIELD TESTING	5

LABORATORY MATERIALS TESTING	38

## GENERAL LAYOUT INFORMATION

This section of the plan provides a description of the Ontario SPS-10 project 87AA00 in terms of the location of the test sections along the roadway.  Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  Table 2 indicates transition areas between consecutive sections, as well as the buffer and monitoring areas for each section.  Figure 1 presents an overview of the highway and the sequence of test sections on the northbound lane. Additionally, Figure 2 provides a visual representation of the overall project layout.

TABLE 1: TEST SECTION IDENTIFICATION AND DESCRIPTION – 87AA00

| Section Number | SHRP ID | Description |
| --- | --- | --- |
| 01 | 87AA01 | Control Section 2” Superpave 12.5 FC2 (PG 58-28) Hot Mix Asphalt 15% RAP |
| 02 | 87AA02 | WMA Core Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Foaming Process Water Dosage: 2.0% of Virgin Asphalt Cement 15% RAP |
| 03 | 87AA03 | WMA Core Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Chemical 1 – Evotherm® M1 Additive Dosage: 0.3% of Virgin Asphalt Cement 15% RAP |
| 04 | 87AA61 | WMA Supplemental Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Chemical 2 – WarmGrip® E5 Additive Dosage: 0.5% of Virgin Asphalt Cement 15% RAP |
| 05 | 87AA62 | WMA Supplemental Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Organic – Rediset® WMX 8017 Additive Dosage: 1.5% of Virgin Asphalt Cement 15% RAP |

87AA01

HMA Control Section
Superpave 12.5 FC2

(PG 58-28)

Transition

87AA02

WMA Foaming Process

Superpave 12.5 FC2

(PG 58-28)

Transition

87AA03

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
Evotherm® M1

827ft

252m

19+254

21+030

19+002

820ft

250m

Transition

87AA61

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
WarmGrip® E5

Transition

87AA62

WMA Organic Additive
Superpave 12.5 FC2
(PG 58-28)
Rediset® WMX 8017

820ft

250m

886ft

270m

886ft

270m

21+280

23+000

23+250

11+280

11+550

12+750

13+020

NOTE: St. 24+616 = St. 10+000

FIGURE 1: ONTARIO SPS-10 87AA00 PROJECT LAYOUT

Northbound Traffic

TABLE 2: TEST SECTION LAYOUT – 87AA00

| Project Begin STA | Project End STA | Experiment Begin STA feet (meter) | Experiment End STA feet (meter) | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
| 18+250 | 19+002 |  |  | START | East Gwillimbury |
| 19+002 | 19+037.05 | 0-165 (0-50.3) | 0-50 (0-15.25) | Sampling Area | 87AA01 |
| 19+037.05 | 19+052.30 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 19+052.30 | 19+204.62 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 19+204.62 | 19+219.87 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 19+219.87 | 19+254 | 5+50 (1+67.25) | 5+162(2+01.38) | Sampling Area |  |
| 19+254 | 21+030 |  |  | Transition |  |
| 21+030 | 21+066.33 | 0-159(0-48.58) | 0-50 (0-15.25) | Sampling Area | 87AA02 |
| 21+066.33 | 21+078.58 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 21+078.58 | 21+231.06 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 21+231.06 | 21+246.31 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 21+246.31 | 21+280 | 5+50 (1+67.25) | 5+161(2+00.94) | Sampling Area |  |
| 21+280 | 23+000 |  |  | Transition |  |
| 23+000 | 23+031.53 | 0-154(0-46.78) | 0-50 (0-15.25) | Sampling Area | 87AA03 |
| 23+031.53 | 23+046.78 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 23+046.78 | 23+199.55 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 23+199.55 | 23+214.8 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 23+214.8 | 23+250 | 5+50 (1+67.25) | 5+166(2+02.45) | Sampling Area |  |
| 23+250 | 11+280 |  |  | Transition (24+616=10+000) | Georgina |
| 11+280 | 11+334.38 | 0-228(0-69.63) | 0-50 (0-15.25) | Sampling Area | 87AA61 |
| 11+334.38 | 11+349.63 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 11+349.63 | 11+501.82 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 11+501.82 | 11+517.07 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 11+517.07 | 11+550 | 5+50 (1+67.25) | 5+158(2+00.18) | Sampling Area |  |
| 11+550 | 12+750 |  |  | Transition |  |
| 12+750 | 12+806.29 | 0-235(0-71.54) | 0-50 (0-15.25) | Sampling Area | 87AA62 |
| 12+806.29 | 12+821.54 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 12+821.54 | 12+973.84 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 12+973.84 | 12+989.09 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 12+989.09 | 13+020 | 5+50 (1+67.25) | 5+151(1+98.16) | Sampling Area |  |
| 13+020 | 13+830 |  |  | END |  |

Sampling Area 011 – 110ft (34.0m)

Buffer Area – 50ft (15.25m)

87AA01

HMA Control Section
Superpave 12.5 FC2

(PG 58-28)

500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 021 – 110ft (34.0m)

Transition (1.776km)

Sampling Area 031 – 111ft (34.5m)

Buffer Area – 50ft (15.25m)

87AA02

WMA Foaming Process

Superpave 12.5 FC2

(PG 58-28)
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 041 – 109ft (33.5m)

Transition (1.720km)

Buffer Area – 50ft (15.25m)

87AA03

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
Evotherm® M1
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 061 – 110ft (34.0m)

Sampling Area 051 – 110ft (34.0m)

827ft (252m)

820ft (250m)

820ft (250m)

NB Traffic

19+254

21+030

19+002

21+280

23+000

23+250

19+052.306

19+204.620

21+078.580

21+231.060

23+046.780

23+199.550

Sampling Area 071 – 131ft (40.6m)

Buffer Area – 50ft (15.25m)

87AA61

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
WarmGrip® E5
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 081 – 122ft (37.4m)

Transition (1.200km)

Sampling Area 091 – 117ft (36.0m)

Buffer Area – 50ft (15.25m)

87AA62

WMA Organic Additive
Superpave 12.5 FC2
(PG 58-28)
Rediset® WMX 8017
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 101 – 136ft (42.0m)

886ft (270m)

886ft (270m)

NB Traffic

11+280

11+550

12+750

13+020

11+349.630

11+501.820

12+821.540

12+973.840

24+616=10+000

Transition (2.646km)

FIGURE 2: ONTARIO SPS-10 PROJECT LAYOUT – 87AA00

NOTE: St. 24+616 = St. 10+000

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

## MATERIALS SAMPLING AND FIELD TESTING

This section of the plan provides the materials sampling and testing activities that will occur in the field at time zero (t0 is at time of construction).  Table 3 provides the project layer numbering schema.  It is very important that the project layer numbering be consistent to ensure that the resulting data is not misunderstood.  Table 4 provides the scope of material sampling, and Table 5 provides the scope of field testing.

Figures 3 through 12 show the locations for the many samples and tests scheduled.  Figures 3 through 7 show density measurement layouts and Figures 8 through 12 show the material sampling locations for each section as well as the location of DCP testing.

Tables 6 through 10 list the samples acquired from each of the five test sections. Table 11 lists the samples to be collected from the asphalt plant.  These tables define the sample number and specimen ID for every sample collected during the experiment. These tables will assist in the proper labeling of each sample as they are collected.

Finally, Tables 12 through 14 list samples to be shipped to the Central Lab Testing Contractor (CLTC) laboratory, the LTPP Materials Reference Library (MRL), and the Turner-Fairbank Highway Research Center (TFHRC), respectively.

There are three primary sample identification codes used in the materials sampling and testing plan: sample location, sample number, and specimen ID. A description of each code format follows.

Sample Location: S-LL-t -XX

- S = Sample location type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gauge

  - H – samples obtained from the HMA plant

- LL = Sample location number

- t = Sampling time interval

- XX = Section number

Sample Number: S-M-##-t-XX
S = Sample type

  - C – core sample

  - B – bulk sample

  - M – moisture sample

- M = Material type

  - A – asphalt concrete

  - C – asphalt cement

  - R – RAP

  - W – warm mix asphalt additive

  - T – treated, bound, or stabilized base/subbase

  - G – untreated, unbound granular base/subbase

  - S – subgrade soil or fill material

  - U – combined aggregate used in asphalt concrete mixes

- ## = Sample number

- t = Sampling time interval

- XX = Section number

Specimen ID: R-C-T-S-NN-L-##

- R = RSC Code (For Ontario SPS-10, R = “A,” representing north Atlantic region)

- C = Construction event (For Ontario SPS-10, C = 1, representing first constructed SPS-10 in the North Bound and C = 2 represents the SPS-10 in the South Bound)

- T = Test Section Number

  - 1 – 01

  - 2 – 02

  - 3 – 03

  - A – 61

  - B – 62

- S = Sample Location Type

  - A – bound, compacted bulk sample (12 inch diameter core)

  - F – bound bulk sample (uncompacted bulk mix obtained on site)

  - U – combined aggregate used in asphalt concrete mixes

  - C – 4 or 6 inch diameter core

  - T – nuclear density/moisture gage

  - H – samples obtained from the HMA plant

- NN = Sample Location Number

- L = “L,” representing layer

- ## = Layer Number

Labels and Tags

Each sample shall be labeled before packing in boxes and cartons. As a minimum, the following information shall be included on a tag or label attached to the specimen:

- SPECIMEN ID

- STATE CODE

- SHRP ID

- LOCATION DESIGNATION

- SAMPLE NUMBER

- DATE (mm-dd-yy, sampling date)

- FIELD SET (one digit number which will be 1 for the first round of sampling)

For cores, the HOLE ID shall be written directly on the core.  If the core contains more than one layer, layer boundaries shall be clearly marked, and each layer numbered.  For bulk samples, the SPECIMEN ID shall be written directly on the bag, bucket or can that contains the sample.

Packaging

Suggestions for labeling and combining the samples for shipment are as follows:

- All samples of like material (e.g., asphaltic concrete surface and binder) shall be placed in separate boxes or separate compartments of one box.

- Each sample shall have a label or tag attached that clearly identifies the material.  It is recommended that the label be color-coded by destination (e.g., contract Lab, FHWA lab, MRL, etc.).

- Each core shall be surrounded with "bubble-wrap" or other acceptable cushioning material on all sides within the shipping box.

- All bulk samples shall be marked with two labels or tags. One shall be placed inside the bag and one attached to the outside. A jar sample for moisture testing of each bulk sample shall be placed inside the bulk sample bag.

- All shipping boxes should be wood of suitable grade and construction to withstand shipping and subsequent moving without breakage of the box or damaging of samples.

- All boxes should be adequately secured by nails or screws prior to shipping.

LTPP Field Operations Information Sheets 1 and 2 shall be sent with each shipment of materials samples.

TABLE 3: PROJECT LAYER NUMBERING

| Project Layer Code | Layer No. | Description | Material Code | Thickness |
| --- | --- | --- | --- | --- |
| A | 1 | Subgrade | 55 |  |
| B | 2 | Granular Subbase | 23 | 7” – 10” (175-250 mm) |
| C | 3 | Old Pulverized AC Pavement | 14 | 7” – 14” (175-350 mm) |
| D | 4 | Granular Base | 23 | 8” (200 mm) |
| E | 5 | Existing AC Pavement (1.5” to be Milled) | 01 | 6” (150 mm) |
| F | 6 | Experimental AC Overlay Binder Layer – Superpave 19.0 | 01 | 2” (50 mm) |
| G | 7 | Experimental AC Overlay Surface Layer – Superpave 12.5 FC2 | 01 | 2” (50 mm) |

TABLE 4: SCOPE OF MATERIAL SAMPLING FROM NB 87AA00

| Material and Sample Description |  | No. of Samples (Ship to) | Sample Location |
| --- | --- | --- | --- |
|  | DURING CONSTRUCTION SAMPLING |  |  |
| A. | EXPERIMENTAL AC SURFACE LAYER (PLANT) |  |  |
|  | 1-gallon can virgin AC Binder (PG 58-28) | 1 (CLTC) 1 (TFHRC) 10 (MRL) | H01001 H02001 H03001, H11001-14001, H05002-H09002 |
|  | 1-gallon can AC Binder (PG 58-28) mixed with Evotherm® M1 | 1 (CLTC) 1 (TFHRC) 10 (MRL) | H01003 H02003 H03003-H12003 |
|  | 1-gallon can AC Binder (PG 58-28) mixed with WarmGrip® E5 | 1 (CLTC) 1 (TFHRC) 10 (MRL) | H01061 H02061 H03061-H12061 |
|  | 1-gallon can AC Binder (PG 58-28) mixed with Rediset® WMX 8017 | 1 (CLTC) 1 (TFHRC) 10 (MRL) | H01062 H02062 H03062-H12062 |
|  | 5-gallon bucket combined aggregate | 20 (MRL) | H04001-H07001, H10002-H13002, H13003-H16003, H13061-H16061, H13062-H16062 |
|  | 50 lb bulk sample RAP | 1 (CLTC) | H08001 |
|  | 5-gallon bucket RAP | 10 (MRL) | H09001-H10001, H14002-H15002, H17003-H18003, H17061-H18061, H17062-H18062 |
|  | 1-gallon chemical additive (Evotherm® M1) | 1 (MRL) | H19003 |
|  | 1-gallon chemical additive (WarmGrip® E5) | 1 (MRL) | H19061 |
|  | 1-gallon chemical additive (Rediset® WMX 8017 | 1 (MRL) | H19062 |

TABLE 4: SCOPE OF MATERIAL SAMPLING FROM NB 87AA00 (Continued)

| Material and Sample Description |  | No. of Samples (Ship to) | Sample Location |
| --- | --- | --- | --- |
| A. | EXPERIMENTAL AC (FIELD) |  |  |
|  | 5-gallon buckets uncompacted AC mix (Surface Layer) | 75 (MRL) | F01001-F15001, F01002-F15002, F01003-F15003, F01061-F15061, F01062-F15062 |
|  | 12" Core (Binder & Surface Layer) | 10 (CLTC) | A01001-A02001, A01002-A02002, A01003-A02003, A01061-A02061, A01062-A02062 |
|  | 6" Core (Binder & Surface Layer) | 70 (50 to CLTC) (20 to MRL) | C01001-C14001, C01002-C14002, C01003-C14003, C01061-C14061, C01062-C14062 |
| B. | ORIGINAL HMAC LAYER (1 LAYER) |  |  |
|  | 12" Core | 2 (CLTC) | A01001, A01003 |
|  | 6" Core | 6 (CLTC) | C01001-C03001, C01003-C03003 |
| C. | GRANULAR BASE |  |  |
|  | 150 lb bulk sample (collected in 4x75 lb sample bags) | 2 (CLTC) 2 (MRL) | A01001-A02001 A01003-A02003 |
| D. | PULVERIZED PAVEMENT (if present) |  |  |
|  | 150 lb bulk sample (collected in 4x75 lb sample bags) | 2 (CLTC) 2 (MRL) | A01001-A02001 A01003-A02003 |
| E. | GRANULAR SUBBASE |  |  |
|  | 150 lb bulk sample (collected in 4x75 lb sample bags) | 2 (CLTC) 2 (MRL) | A01001-A02001 A01003-A02003 |
| F. | SUBGRADE |  |  |
|  | 150 lb bulk sample (collected in 4x75 lb sample bags) | 2 (CLTC) 2 (MRL) | A01001-A02001 A01003-A02003 |
|  | Moisture content jar sample | 2 (CLTC) 2 (MRL) | A01001-A02001 A01003-A02003 |

TABLE 5: SCOPE OF FIELD TESTING FOR NB 87AA00

| Material and Test Description |  | No. of Tests | Location Designation |
| --- | --- | --- | --- |
|  | PRE-CONSTRUCTION TESTING |  |  |
| A. | ORIGINAL HMAC |  |  |
|  | Elevation Survey | 5 | All Sections |
|  | POST-CONSTRUCTION TESTING |  |  |
| A. | EXPERIMENTAL AC |  |  |
|  | Elevation Survey | 5 | All Sections |
|  | In situ density measurement (surface layer) | 15* | T01001-T03001, T01002-T03002, T01003-T03003, T01061-T03061, T01062-T03062 |
|  | Core Examination and Thickness (P01/AC01) | 80 | A01001-A02001, A01002-A02002, A01003-A02003, A01061-A02061, A01062-A02062, C01001-C14001, C01002-C14002, C01003-C14003, C01061-C14061, C01062-C14062 |
| B. | ORIGINAL HMAC LAYER (1 LAYER) |  |  |
|  | Core Examination and Thickness (P01/AC01) | 8 | A01001, A01003, C01001-C03001, C01003-C03003 |
| C. | GRANULAR BASE |  |  |
|  | DCP | 5 | A01001, A01002, A01003, A01061, A01062 |
| D. | PULVERIZED PAVEMENT (if present) |  |  |
|  | Examination and Classification (TB01/P31) DCP | 2 | A01001-A02001, A01003-A02003 |
| E. | GRANULAR SUBBASE |  |  |
|  | DCP | 5 | A01001, A01002, A01003, A01061, A01062 |
| F. | SUBGRADE |  |  |
|  | DCP | 5 | A01001, A01002, A01003, A01061, A01062 |

* Each location has 4 readings, rotating 90deg in between each reading (4 readings within a test, 60 readings total)

Section 87AA01 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03001

T02001

T01001

Traffic

FIGURE 3: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA01 ONTARIO SPS-10

Section 87AA02 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03002

T02002

T01002

Traffic

FIGURE 4: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA02 ONTARIO SPS-10

Section 87AA03 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03003

T02003

T01003

Traffic

FIGURE 5: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA03 ONTARIO SPS-10

Section 87AA61 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03061

T02061

T01061

Traffic

FIGURE 6: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA61 ONTARIO SPS-10

Section 87AA62 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03062

T02062

T01062

Traffic

FIGURE 7: DENSITY MEASUREMENT LAYOUT FOR SURFACE LAYERS OF TEST SECTION 87AA62 ONTARIO SPS-10

0-70

0-50

Section STA:

Section: 87AA01

Description: HMAC Control Section

Sampling Area: 01

Sampling Interval: t0

Write Hole ID as well as AA for Project ID on Cores

Shoulder

C02001

C04001

C06001

C08001

C10001

C12001

C14001

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01001

C03001

C05001

C07001

C09001

C11001

C13001

A01001

A02001

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

12” Core Experimental AC; Auger Base, Subbase and Subgrade

12” Core Experimental AC and Original HMAC; Auger Base, Subbase and Subgrade; DCP

FIGURE 8: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA01 AT TIME 0 ONTARIO SPS-10

0-70

0-50

Section STA:

Section: 87AA02

Description: Mix with WMA Foaming Process

Sampling Area: 03

Sampling Interval: t0

Write Hole ID as well as AA for Project ID on Cores

Shoulder

C02002

C04002

C06002

C08002

C10002

C12002

C14002

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01002

C03002

C05002

C07002

C09002

C11002

C13002

A01002

A02002

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 9: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA02 AT TIME 0 ONTARIO SPS-10

0-70

0-50

Section STA:

Section: 87AA03

Description: Mix with WMA Chemical Additive

Sampling Area: 05

Sampling Interval: t0

Write Hole ID as well as AA for Project ID on Cores

Shoulder

C02003

C04003

C06003

C08003

C10003

C12003

C14003

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01003

C03003

C05003

C07003

C09003

C11003

C13003

A01003

A02003

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

12” Core Experimental AC; Auger Base, Subbase and Subgrade

12” Core Experimental AC and Original HMAC; Auger Base, Subbase and Subgrade; DCP

FIGURE 10: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA03 AT TIME 0 ONTARIO SPS-10

0-70

0-50

Section STA:

Section: 87AA61

Description: Supplemental Section 1

Sampling Area: 07

Sampling Interval: t0

Write Hole ID as well as AA for Project ID on Cores

Shoulder

C02061

C04061

C06061

C08061

C10061

C12061

C14061

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01061

C03061

C05061

C07061

C09061

C11061

C13061

A01061

A02061

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 11: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA61 AT TIME 0 ONTARIO SPS-10

0-70

0-50

Section STA:

Section: 87AA62

Description: Supplemental Section 2

Sampling Area: 09

Sampling Interval: t0

Write Hole ID as well as AA for Project ID on Cores

Shoulder

C02062

C04062

C06062

C08062

C10062

C12062

C14062

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01062

C03062

C05062

C07062

C09062

C11062

C13062

A01062

A02062

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

FIGURE 12: SAMPLING AND TESTING PLAN FOR TEST SECTION 87AA62 AT TIME 0 ONTARIO SPS-10

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 87AA01 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01001 | 7 6 | BA01001 | A11A01L07 A11A01L06 | 12" Core | CLTC |
|  | 5 |  | A11A01L05 |  |  |
|  | 4 | BG01001 | A11A01L04 | 75 lb. Bulk Sample (Base) |  |
|  | 3 | BT01001 | A11A01L03 | 75 lb. Bulk Sample (Pulverized AC) |  |
|  | 2 | BG02001 | A11A01L02 | 75 lb. Bulk Sample (Subbase) |  |
|  | 1 | BS01001 | A11A01L01 | 75 lb. Bulk Sample (Subgrade) |  |
|  |  | MS01001 | A11AM1L01 | Moisture Content Jar Sample |  |
| A02001 | 7 | BA02001 | A11A02L07 | 12" Core |  |
|  | 6 |  | A11A02L06 |  |  |
|  | 4 | BG03001 | A11A02L04 | 75 lb. Bulk Sample (Base) |  |
|  | 3 | BT02001 | A11A02L03 | 75 lb. Bulk Sample (Pulverized AC) |  |
|  | 2 | BG04001 | A11A02L02 | 75 lb. Bulk Sample (Subbase) |  |
|  | 1 | BS02001 | A11A02L01 | 75 lb. Bulk Sample (Subgrade) |  |
|  |  | MS02001 | A11AM2L01 | Moisture Content Jar Sample |  |
| C01001 | 7 6 | CA01001 | A11C01L07 A11C01L06 | 6" Core | CLTC |
|  | 5 |  | A11C01L05 |  |  |
| C02001 | 7 6 | CA02001 | A11C02L07 A11C02L06 | 6" Core |  |
|  | 5 |  | A11C02L05 |  |  |
| C03001 | 7 6 | CA03001 | A11C03L07 A11C03L06 | 6" Core |  |
|  | 5 |  | A11C03L05 |  |  |
| C04001 | 7 | CA04001 | A11C04L07 | 6" Core | CLTC |
|  | 6 |  | A11C04L06 |  |  |
| C05001 | 7 | CA05001 | A11C05L07 | 6" Core |  |
|  | 6 |  | A11C05L06 |  |  |
| C06001 | 7 | CA06001 | A11C06L07 | 6" Core |  |
|  | 6 |  | A11C06L06 |  |  |
| C07001 | 7 | CA07001 | A11C07L07 | 6" Core |  |
|  | 6 |  | A11C07L06 |  |  |
| C08001 | 7 | CA08001 | A11C08L07 | 6" Core |  |
|  | 6 |  | A11C08L06 |  |  |
| C09001 | 7 | CA09001 | A11C09L07 | 6" Core |  |
|  | 6 |  | A11C09L06 |  |  |
| C10001 | 7 | CA10001 | A11C10L07 | 6" Core |  |
|  | 6 |  | A11C10L06 |  |  |
| C11001 | 7 | CA11001 | A11C11L07 | 6" Core | MRL |
|  | 6 |  | A11C11L06 |  |  |
| C12001 | 7 | CA12001 | A11C12L07 | 6" Core |  |
|  | 6 |  | A11C12L06 |  |  |
| C13001 | 7 | CA13001 | A11C13L07 | 6" Core |  |
|  | 6 |  | A11C13L06 |  |  |
| C14001 | 7 | CA14001 | A11C14L07 | 6" Core |  |
|  | 6 |  | A11C14L06 |  |  |

TABLE 6: SAMPLES ACQUIRED FROM TEST SECTION 87AA01 NB (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| F01001 | 7 | BA03001 | A11F01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02001 |  | BA04001 | A11F02L07 |  |  |
| F03001 |  | BA05001 | A11F03L07 |  |  |
| F04001 |  | BA06001 | A11F04L07 |  |  |
| F05001 |  | BA07001 | A11F05L07 |  |  |
| F06001 |  | BA08001 | A11F06L07 |  |  |
| F07001 |  | BA09001 | A11F07L07 |  |  |
| F08001 |  | BA10001 | A11F08L07 |  |  |
| F09001 |  | BA11001 | A11F09L07 |  |  |
| F10001 |  | BA12001 | A11F10L07 |  |  |
| F11001 |  | BA13001 | A11F11L07 |  |  |
| F12001 |  | BA14001 | A11F12L07 |  |  |
| F13001 |  | BA15001 | A11F13L07 |  |  |
| F14001 |  | BA16001 | A11F14L07 |  |  |
| F15001 |  | BA17001 | A11F15L07 |  |  |

TABLE 7: SAMPLES ACQUIRED FROM TEST SECTION 87AA02 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01002 | 7 | BA01002 | A12A01L07 | 12" Core | CLTC |
|  | 6 |  | A12A01L06 |  |  |
| A02002 | 7 | BA02002 | A12A02L07 | 12" Core |  |
|  | 6 |  | A12A02L06 |  |  |
| C01002 | 7 | CA01002 | A12C01L07 | 6" Core | CLTC |
|  | 6 |  | A12C01L06 |  |  |
| C02002 | 7 | CA02002 | A12C02L07 | 6" Core |  |
|  | 6 |  | A12C02L07 |  |  |
| C03002 | 7 | CA03002 | A12C03L07 | 6" Core |  |
|  | 6 |  | A12C03L06 |  |  |
| C04002 | 7 | CA04002 | A12C04L07 | 6" Core |  |
|  | 6 |  | A12C04L06 |  |  |
| C05002 | 7 | CA05002 | A12C05L07 | 6" Core |  |
|  | 6 |  | A12C05L06 |  |  |
| C06002 | 7 | CA06002 | A12C06L07 | 6" Core |  |
|  | 6 |  | A12C06L06 |  |  |
| C07002 | 7 | CA07002 | A12C07L07 | 6" Core |  |
|  | 6 |  | A12C07L06 |  |  |
| C08002 | 7 | CA08002 | A12C08L07 | 6" Core |  |
|  | 6 |  | A12C08L06 |  |  |
| C09002 | 7 | CA09002 | A12C09L07 | 6" Core |  |
|  | 6 |  | A12C09L06 |  |  |
| C10002 | 7 | CA10002 | A12C10L07 | 6" Core |  |
|  | 6 |  | A12C10L06 |  |  |
| C11002 | 7 | CA11002 | A12C11L07 | 6" Core | MRL |
|  | 6 |  | A12C11L06 |  |  |
| C12002 | 7 | CA12002 | A12C12L07 | 6" Core |  |
|  | 6 |  | A12C12L06 |  |  |
| C13002 | 7 | CA13002 | A12C13L07 | 6" Core |  |
|  | 6 |  | A12C13L06 |  |  |
| C14002 | 7 | CA14002 | A12C14L07 | 6" Core |  |
|  | 6 |  | A12C14L06 |  |  |
| F01002 | 7 | BA03002 | A12F01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02002 |  | BA04002 | A12F02L07 |  |  |
| F03002 |  | BA05002 | A12F03L07 |  |  |
| F04002 |  | BA06002 | A12F04L07 |  |  |
| F05002 |  | BA07002 | A12F05L07 |  |  |
| F06002 |  | BA08002 | A12F06L07 |  |  |
| F07002 |  | BA09002 | A12F07L07 |  |  |
| F08002 |  | BA10002 | A12F08L07 |  |  |
| F09002 |  | BA11002 | A12F09L07 |  |  |
| F10002 |  | BA12002 | A12F10L07 |  |  |
| F11002 |  | BA13002 | A12F11L07 |  |  |
| F12002 |  | BA14002 | A12F12L07 |  |  |
| F13002 |  | BA15002 | A12F13L07 |  |  |
| F14002 |  | BA16002 | A12F14L07 |  |  |
| F15002 |  | BA17002 | A12F15L07 |  |  |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 87AA03 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01003 | 7 | BA01003 | A13A01L07 | 12" Core | CLTC |
|  | 6 |  | A13A01L06 |  |  |
|  | 5 |  | A13A01L05 |  |  |
|  | 4 | BG01003 | A13A01L04 | 75 lb. Bulk Sample (Base) | MRL |
|  | 3 | BT01003 | A13A01L03 | 75 lb. Bulk Sample (Pulverized AC) |  |
|  | 2 | BG02003 | A13A01L02 | 75 lb. Bulk Sample (Subbase) |  |
|  | 1 | BS01003 | A13A01L01 | 75 lb. Bulk Sample (Subgrade) |  |
|  |  | MS01003 | A13AM1L01 | Moisture Content Jar Sample |  |
| A02003 | 7 | BA02003 | A13A02L07 | 12" Core | CLTC |
|  | 6 |  | A13A02L06 |  |  |
|  | 4 | BG03003 | A13A02L04 | 75 lb. Bulk Sample (Base) | MRL |
|  | 3 | BT02003 | A13A02L03 | 75 lb. Bulk Sample (Pulverized AC) |  |
|  | 2 | BG04003 | A13A02L02 | 75 lb. Bulk Sample (Subbase) |  |
|  | 1 | BS02003 | A13A02L01 | 75 lb. Bulk Sample (Subgrade) |  |
|  |  | MS02003 | A13AM2L01 | Moisture Content Jar Sample |  |
| C01003 | 7 6 | CA01003 | A13C01L07 A13C01L06 | 6" Core | CLTC |
|  | 5 |  | A13C01L05 |  |  |
| C02003 | 7 6 | CA02003 | A13C02L07 A13C02L06 | 6" Core |  |
|  | 5 |  | A13C02L05 |  |  |
| C03003 | 7 6 | CA03003 | A13C03L07 A13C03L06 | 6" Core |  |
|  | 5 |  | A13C03L05 |  |  |
| C04003 | 7 | CA04003 | A13C04L07 | 6" Core | CLTC |
|  | 6 |  | A13C04L06 |  |  |
| C05003 | 7 | CA05003 | A13C05L07 | 6" Core |  |
|  | 6 |  | A13C05L06 |  |  |
| C06003 | 7 | CA06003 | A13C06L07 | 6" Core |  |
|  | 6 |  | A13C06L06 |  |  |
| C07003 | 7 | CA07003 | A13C07L07 | 6" Core |  |
|  | 6 |  | A13C07L06 |  |  |
| C08003 | 7 | CA08003 | A13C08L07 | 6" Core |  |
|  | 6 |  | A13C08L06 |  |  |
| C09003 | 7 | CA09003 | A13C09L07 | 6" Core |  |
|  | 6 |  | A13C09L06 |  |  |
| C10003 | 7 | CA10003 | A13C10L07 | 6" Core |  |
|  | 6 |  | A13C10L06 |  |  |
| C11003 | 7 | CA11003 | A13C11L07 | 6" Core | MRL |
|  | 6 |  | A13C11L06 |  |  |
| C12003 | 7 | CA12003 | A13C12L07 | 6" Core |  |
|  | 6 |  | A13C12L06 |  |  |
| C13003 | 7 | CA13003 | A13C13L07 | 6" Core |  |
|  | 6 |  | A13C13L06 |  |  |
| C14003 | 7 | CA14003 | A13C14L07 | 6" Core |  |
|  | 6 |  | A13C14L06 |  |  |

TABLE 8: SAMPLES ACQUIRED FROM TEST SECTION 87AA03 NB (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| F01003 | 7 | BA03003 | A13F01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02003 |  | BA04003 | A13F02L07 |  |  |
| F03003 |  | BA05003 | A13F03L07 |  |  |
| F04003 |  | BA06003 | A13F04L07 |  |  |
| F05003 |  | BA07003 | A13F05L07 |  |  |
| F06003 |  | BA08003 | A13F06L07 |  |  |
| F07003 |  | BA09003 | A13F07L07 |  |  |
| F08003 |  | BA10003 | A13F08L07 |  |  |
| F09003 |  | BA11003 | A13F09L07 |  |  |
| F10003 |  | BA12003 | A13F10L07 |  |  |
| F11003 |  | BA13003 | A13F11L07 |  |  |
| F12003 |  | BA14003 | A13F12L07 |  |  |
| F13003 |  | BA15003 | A13F13L07 |  |  |
| F14003 |  | BA16003 | A13F14L07 |  |  |
| F15003 |  | BA17003 | A13F15L07 |  |  |

TABLE 9: SAMPLES ACQUIRED FROM TEST SECTION 87AA61 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01061 | 7 | BA01061 | A1AA01L07 | 12" Core | CLTC |
|  | 6 |  | A1AA01L06 |  |  |
| A02061 | 7 | BA02061 | A1AA02L07 | 12" Core |  |
|  | 6 |  | A1AA02L06 |  |  |
| C01061 | 7 | CA01061 | A1AC01L07 | 6" Core | CLTC |
|  | 6 |  | A1AC01L06 |  |  |
| C02061 | 7 | CA02061 | A1AC02L07 | 6" Core |  |
|  | 6 |  | A1AC02L06 |  |  |
| C03061 | 7 | CA03061 | A1AC03L07 | 6" Core |  |
|  | 6 |  | A1AC03L06 |  |  |
| C04061 | 7 | CA04061 | A1AC04L07 | 6" Core |  |
|  | 6 |  | A1AC04L06 |  |  |
| C05061 | 7 | CA05061 | A1AC05L07 | 6" Core |  |
|  | 6 |  | A1AC05L06 |  |  |
| C06061 | 7 | CA06061 | A1AC06L07 | 6" Core |  |
|  | 6 |  | A1AC06L06 |  |  |
| C07061 | 7 | CA07061 | A1AC07L07 | 6" Core |  |
|  | 6 |  | A1AC07L06 |  |  |
| C08061 | 7 | CA08061 | A1AC08L07 | 6" Core |  |
|  | 6 |  | A1AC08L06 |  |  |
| C09061 | 7 | CA09061 | A1AC09L07 | 6" Core |  |
|  | 6 |  | A1AC09L06 |  |  |
| C10061 | 7 | CA10061 | A1AC10L07 | 6" Core |  |
|  | 6 |  | A1AC10L06 |  |  |
| C11061 | 7 | CA11061 | A1AC11L07 | 6" Core | MRL |
|  | 6 |  | A1AC11L06 |  |  |
| C12061 | 7 | CA12061 | A1AC12L07 | 6" Core |  |
|  | 6 |  | A1AC12L06 |  |  |
| C13061 | 7 | CA13061 | A1AC13L07 | 6" Core |  |
|  | 6 |  | A1AC13L06 |  |  |
| C14061 | 7 | CA14061 | A1AC14L07 | 6" Core |  |
|  | 6 |  | A1AC14L06 |  |  |
| F01061 | 7 | BA03061 | A1AF01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02061 |  | BA04061 | A1AF02L07 |  |  |
| F03061 |  | BA05061 | A1AF03L07 |  |  |
| F04061 |  | BA06061 | A1AF04L07 |  |  |
| F05061 |  | BA07061 | A1AF05L07 |  |  |
| F06061 |  | BA08061 | A1AF06L07 |  |  |
| F07061 |  | BA09061 | A1AF07L07 |  |  |
| F08061 |  | BA10061 | A1AF08L07 |  |  |
| F09061 |  | BA11061 | A1AF09L07 |  |  |
| F10061 |  | BA12061 | A1AF10L07 |  |  |
| F11061 |  | BA13061 | A1AF11L07 |  |  |
| F12061 |  | BA14061 | A1AF12L07 |  |  |
| F13061 |  | BA15061 | A1AF13L07 |  |  |
| F14061 |  | BA16061 | A1AF14L07 |  |  |
| F15061 |  | BA17061 | A1AF15L07 |  |  |

TABLE 10: SAMPLES ACQUIRED FROM TEST SECTION 87AA62 (North Bound)

| Sample Location | Layer Number | Sample No. | Specimen ID | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- |
| A01062 | 7 | BA01062 | A1BA01L07 | 12" Core | CLTC |
|  | 6 |  | A1BA01L06 |  |  |
| A02062 | 7 | BA02062 | A1BA02L07 | 12" Core |  |
|  | 6 |  | A1BA02L06 |  |  |
| C01062 | 7 | CA01062 | A1BC01L07 | 6" Core | CLTC |
|  | 6 |  | A1BC01L06 |  |  |
| C02062 | 7 | CA02062 | A1BC02L07 | 6" Core |  |
|  | 6 |  | A1BC02L06 |  |  |
| C03062 | 7 | CA03062 | A1BC03L07 | 6" Core |  |
|  | 6 |  | A1BC03L06 |  |  |
| C04062 | 7 | CA04062 | A1BC04L07 | 6" Core |  |
|  | 6 |  | A1BC04L06 |  |  |
| C05062 | 7 | CA05062 | A1BC05L07 | 6" Core |  |
|  | 6 |  | A1BC05L06 |  |  |
| C06062 | 7 | CA06062 | A1BC06L07 | 6" Core |  |
|  | 6 |  | A1BC06L06 |  |  |
| C07062 | 7 | CA07062 | A1BC07L07 | 6" Core |  |
|  | 6 |  | A1BC07L06 |  |  |
| C08062 | 7 | CA08062 | A1BC08L07 | 6" Core |  |
|  | 6 |  | A1BC08L06 |  |  |
| C09062 | 7 | CA09062 | A1BC09L07 | 6" Core |  |
|  | 6 |  | A1BC09L06 |  |  |
| C10062 | 7 | CA10062 | A1BC10L07 | 6" Core |  |
|  | 6 |  | A1BC10L06 |  |  |
| C11062 | 7 | CA11062 | A1BC11L07 | 6" Core | MRL |
|  | 6 |  | A1BC11L06 |  |  |
| C12062 | 7 | CA12062 | A1BC12L07 | 6" Core |  |
|  | 6 |  | A1BC12L06 |  |  |
| C13062 | 7 | CA13062 | A1BC13L07 | 6" Core |  |
|  | 6 |  | A1BC13L06 |  |  |
| C14062 | 7 | CA14062 | A1BC14L07 | 6" Core |  |
|  | 6 |  | A1BC14L06 |  |  |
| F01062 | 7 | BA03062 | A1BF01L07 | 15 5-gallon buckets uncompacted AC mix | MRL |
| F02062 |  | BA04062 | A1BF02L07 |  |  |
| F03062 |  | BA05062 | A1BF03L07 |  |  |
| F04062 |  | BA06062 | A1BF04L07 |  |  |
| F05062 |  | BA07062 | A1BF05L07 |  |  |
| F06062 |  | BA08062 | A1BF06L07 |  |  |
| F07062 |  | BA09062 | A1BF07L07 |  |  |
| F08062 |  | BA10062 | A1BF08L07 |  |  |
| F09062 |  | BA11062 | A1BF09L07 |  |  |
| F10062 |  | BA12062 | A1BF10L07 |  |  |
| F11062 |  | BA13062 | A1BF11L07 |  |  |
| F12062 |  | BA14062 | A1BF12L07 |  |  |
| F13062 |  | BA15062 | A1BF13L07 |  |  |
| F14062 |  | BA16062 | A1BF14L07 |  |  |
| F15062 |  | BA17062 | A1BF15L07 |  |  |

TABLE 11: SAMPLES ACQUIRED FROM PLANT

| Sample Location | Layer Number | Sample No. | Specimen ID | Test Section | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- | --- |
| H01001 | 7 | BC01001 | A11H01L07 | AA01 | 1 1-gallon can virgin AC Binder (PG 58-28) | CLTC |
| H02001 | 7 | BC02001 | A11H02L07 | AA01 | 1 1-gallon can virgin AC Binder (PG 58-28) | TFHRC |
| H03001 | 7 | BC03001 | A11H03L07 | AA01 | 10 1-gallon cans virgin AC Binder (PG 58-28) | MRL |
| H11001 |  | BC11001 | A11H11L07 | AA01 |  |  |
| H12001 |  | BC12001 | A11H12L07 | AA01 |  |  |
| H13001 |  | BC13001 | A11H13L07 | AA01 |  |  |
| H14001 |  | BC14001 | A11H14L07 | AA01 |  |  |
| H05002 |  | BC05002 | A12H05L07 | AA02 |  |  |
| H06002 |  | BC06002 | A12H06L07 | AA02 |  |  |
| H07002 |  | BC07002 | A12H07L07 | AA02 |  |  |
| H08002 |  | BC08002 | A12H08L07 | AA02 |  |  |
| H09002 |  | BC09002 | A12H09L07 | AA02 |  |  |
| H01003 | 7 | BC01003 | A13H01L07 | AA03 | 1 1-gallon can AC Binder (PG 58-28) mixed with Evotherm® M1 | CLTC |
| H02003 | 7 | BC02003 | A13H02L07 | AA03 | 1 1-gallon can AC Binder (PG 58-28) mixed with Evotherm® M1 | TFHRC |
| H03003 | 7 | BC03003 | A13H03L07 | AA03 | 10 1-gallon can AC Binder (PG 58-28) mixed with Evotherm® M1 | MRL |
| H04003 |  | BC04003 | A13H04L07 | AA03 |  |  |
| H05003 |  | BC05003 | A13H05L07 | AA03 |  |  |
| H06003 |  | BC06003 | A13H06L07 | AA03 |  |  |
| H07003 |  | BC07003 | A13H07L07 | AA03 |  |  |
| H08003 |  | BC08003 | A13H08L07 | AA03 |  |  |
| H09003 |  | BC09003 | A13H09L07 | AA03 |  |  |
| H10003 |  | BC10003 | A13H10L07 | AA03 |  |  |
| H11003 |  | BC11003 | A13H11L07 | AA03 |  |  |
| H12003 |  | BC12003 | A13H12L07 | AA03 |  |  |
| H01061 | 7 | BC01061 | A1AH01L07 | AA61 | 1 1-gallon can AC Binder (PG 58-28) mixed with WarmGrip® E5 | CLTC |
| H02061 | 7 | BC02061 | A1AH02L07 | AA61 | 1 1-gallon can AC Binder (PG 58-28) mixed with WarmGrip® E5 | TFHRC |
| H03061 | 7 | BC03061 | A1AH03L07 | AA61 | 10 1-gallon can AC Binder (PG 58-28) mixed with WarmGrip® E5 | MRL |
| H04061 |  | BC04061 | A1AH04L07 | AA61 |  |  |
| H05061 |  | BC05061 | A1AH05L07 | AA61 |  |  |
| H06061 |  | BC06061 | A1AH06L07 | AA61 |  |  |
| H07061 |  | BC07061 | A1AH07L07 | AA61 |  |  |
| H08061 |  | BC08061 | A1AH08L07 | AA61 |  |  |
| H09061 |  | BC09061 | A1AH09L07 | AA61 |  |  |
| H10061 |  | BC10061 | A1AH10L07 | AA61 |  |  |
| H11061 |  | BC11061 | A1AH11L07 | AA61 |  |  |
| H12061 |  | BC12061 | A1AH12L07 | AA61 |  |  |
| H01062 | 7 | BC01062 | A1BH01L07 | AA62 | 1 1-gallon can AC Binder (PG 58-28) mixed with Rediset® WMX 8017 | CLTC |
| H02062 | 7 | BC02062 | A1BH02L07 | AA62 | 1 1-gallon can AC Binder (PG 58-28) mixed with Rediset® WMX 8017 | TFHRC |

TABLE 11: SAMPLES ACQUIRED FROM PLANT (Continued)

| Sample Location | Layer Number | Sample No. | Specimen ID | Test Section | Type of Sample | Ship to |
| --- | --- | --- | --- | --- | --- | --- |
| H03062 | 7 | BC03062 | A1BH03L07 | AA62 | 10 1-gallon can AC Binder (PG 58-28) mixed with Rediset® WMX 8017 | MRL |
| H04062 |  | BC04062 | A1BH04L07 | AA62 |  |  |
| H05062 |  | BC05062 | A1BH05L07 | AA62 |  |  |
| H06062 |  | BC06062 | A1BH06L07 | AA62 |  |  |
| H07062 |  | BC07062 | A1BH07L07 | AA62 |  |  |
| H08062 |  | BC08062 | A1BH08L07 | AA62 |  |  |
| H09062 |  | BC09062 | A1BH09L07 | AA62 |  |  |
| H10062 |  | BC10062 | A1BH10L07 | AA62 |  |  |
| H11062 |  | BC11062 | A1BH11L07 | AA62 |  |  |
| H12062 |  | BC12062 | A1BH12L07 | AA62 |  |  |
| H04001 | 7 | BU01001 | A11H04L07 | AA01 | 20 5-gallon buckets combined aggregate | MRL |
| H05001 |  | BU02001 | A11H05L07 | AA01 |  |  |
| H06001 |  | BU03001 | A11H06L07 | AA01 |  |  |
| H07001 |  | BU04001 | A11H07L07 | AA01 |  |  |
| H10002 |  | BU01002 | A12H10L07 | AA02 |  |  |
| H11002 |  | BU02002 | A12H11L07 | AA02 |  |  |
| H12002 |  | BU03002 | A12H12L07 | AA02 |  |  |
| H13002 |  | BU04002 | A12H13L07 | AA02 |  |  |
| H13003 |  | BU01003 | A13H13L07 | AA03 |  |  |
| H14003 |  | BU02003 | A13H14L07 | AA03 |  |  |
| H15003 |  | BU03003 | A13H15L07 | AA03 |  |  |
| H16003 |  | BU04003 | A13H16L07 | AA03 |  |  |
| H13061 |  | BU01061 | A1AH13L07 | AA61 |  |  |
| H14061 |  | BU02061 | A1AH14L07 | AA61 |  |  |
| H15061 |  | BU03061 | A1AH15L07 | AA61 |  |  |
| H16061 |  | BU04061 | A1AH16L07 | AA61 |  |  |
| H13062 |  | BU01062 | A1BH13L07 | AA62 |  |  |
| H14062 |  | BU02062 | A1BH14L07 | AA62 |  |  |
| H15062 |  | BU03062 | A1BH15L07 | AA62 |  |  |
| H16062 |  | BU04062 | A1BH16L07 | AA62 |  |  |
| H08001 | 7 | BR01001 | A11H08L07 | AA01 | 50 lb. Bulk Sample RAP | CLTC |
| H09001 | 7 | BR02001 | A11H09L07 | AA01 | 10 5-gallon buckets RAP | MRL |
| H10001 |  | BR03001 | A11H10L07 | AA01 |  |  |
| H14002 |  | BR01002 | A12H14L07 | AA02 |  |  |
| H15002 |  | BR02002 | A12H15L07 | AA02 |  |  |
| H17003 |  | BR01003 | A13H17L07 | AA03 |  |  |
| H18003 |  | BR02003 | A13H18L07 | AA03 |  |  |
| H17061 |  | BR01061 | A1AH17L07 | AA61 |  |  |
| H18061 |  | BR02061 | A1AH18L07 | AA61 |  |  |
| H17062 |  | BR01062 | A1BH17L07 | AA62 |  |  |
| H18062 |  | BR02062 | A1BH18L07 | AA62 |  |  |
| H19003 | 7 | BW01003 | A13H19L07 | AA03 | 1 1-gallon can chemical additive Evotherm® M1 | MRL |
| H19061 | 7 | BW01061 | A1AH19L07 | AA61 | 1 1-gallon can chemical additive WarmGrip® E5 | MRL |
| H19062 | 7 | BW01062 | A1BH19L07 | AA62 | 1 1-gallon can chemical additive Rediset® WMX 8017 | MRL |

TABLE 12: SAMPLES TO BE SHIPPED TO CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| AA01 | A11A01L07 | 12" Core |
| AA01 | A11A02L07 | 12" Core |
| AA02 | A12A01L07 | 12" Core |
| AA02 | A12A02L07 | 12" Core |
| AA03 | A13A01L07 | 12" Core |
| AA03 | A13A02L07 | 12" Core |
| AA61 | A1AA01L07 | 12" Core |
| AA61 | A1AA02L07 | 12" Core |
| AA62 | A1BA01L07 | 12" Core |
| AA62 | A1BA02L07 | 12" Core |
| AA01 | A11C01L07 | 6" Core |
| AA01 | A11C02L07 | 6" Core |
| AA01 | A11C03L07 | 6" Core |
| AA01 | A11C04L07 | 6" Core |
| AA01 | A11C05L07 | 6" Core |
| AA01 | A11C06L07 | 6" Core |
| AA01 | A11C07L07 | 6" Core |
| AA01 | A11C08L07 | 6" Core |
| AA01 | A11C09L07 | 6" Core |
| AA01 | A11C10L07 | 6" Core |
| AA02 | A12C01L07 | 6" Core |
| AA02 | A12C02L07 | 6" Core |
| AA02 | A12C03L07 | 6" Core |
| AA02 | A12C04L07 | 6" Core |
| AA02 | A12C05L07 | 6" Core |
| AA02 | A12C06L07 | 6" Core |
| AA02 | A12C07L07 | 6" Core |
| AA02 | A12C08L07 | 6" Core |
| AA02 | A12C09L07 | 6" Core |
| AA02 | A12C10L07 | 6" Core |
| AA03 | A13C01L07 | 6" Core |
| AA03 | A13C02L07 | 6" Core |
| AA03 | A13C03L07 | 6" Core |
| AA03 | A13C04L07 | 6" Core |
| AA03 | A13C05L07 | 6" Core |

TABLE 12: SAMPLES TO BE SHIPPED TO CLTC LAB (Continued)

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| AA03 | A13C06L07 | 6" Core |
| AA03 | A13C07L07 | 6" Core |
| AA03 | A13C08L07 | 6" Core |
| AA03 | A13C09L07 | 6" Core |
| AA03 | A13C10L07 | 6" Core |
| AA61 | A1AC01L07 | 6" Core |
| AA61 | A1AC02L07 | 6" Core |
| AA61 | A1AC03L07 | 6" Core |
| AA61 | A1AC04L07 | 6" Core |
| AA61 | A1AC05L07 | 6" Core |
| AA61 | A1AC06L07 | 6" Core |
| AA61 | A1AC07L07 | 6" Core |
| AA61 | A1AC08L07 | 6" Core |
| AA61 | A1AC09L07 | 6" Core |
| AA61 | A1AC10L07 | 6" Core |
| AA62 | A1BC01L07 | 6" Core |
| AA62 | A1BC02L07 | 6" Core |
| AA62 | A1BC03L07 | 6" Core |
| AA62 | A1BC04L07 | 6" Core |
| AA62 | A1BC05L07 | 6" Core |
| AA62 | A1BC06L07 | 6" Core |
| AA62 | A1BC07L07 | 6" Core |
| AA62 | A1BC08L07 | 6" Core |
| AA62 | A1BC09L07 | 6" Core |
| AA62 | A1BC10L07 | 6" Core |
| AA01 | A11H01L07 | 1 1-gallon can of virgin AC Binder (PG 58-28) |
| AA03 | A13H01L07 | 1 1-gallon can of AC Binder (PG 58-28) mixed with Evotherm® M1 |
| AA61 | A1AH01L07 | 1 1-gallon can of AC Binder (PG 58-28) mixed with WarmGrip® E5 |
| AA62 | A1BH01L07 | 1 1-gallon can of AC Binder (PG 58-28) mixed with Rediset® WMX 8017 |
| AA01 | A11H06L07 | 50 lb Bulk Sample RAP |

TABLE 12: SAMPLES TO BE SHIPPED TO CLTC LAB (Continued)

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC Binder Layer |  |  |
| AA01 | A11A01L06 | 12" Core |
| AA03 | A13A01L06 | 12" Core |
| AA01 | A11C01L06 | 6" Core |
| AA01 | A11C02L06 | 6" Core |
| AA01 | A11C03L06 | 6" Core |
| AA01 | A11C04L06 | 6" Core |
| AA01 | A11C05L06 | 6" Core |
| AA01 | A11C06L06 | 6" Core |
| AA01 | A11C07L06 | 6" Core |
| AA01 | A11C08L06 | 6" Core |
| AA01 | A11C09L06 | 6" Core |
| AA01 | A11C10L06 | 6" Core |
| AA03 | A13C01L06 | 6" Core |
| AA03 | A13C02L06 | 6" Core |
| AA03 | A13C03L06 | 6" Core |
| Original HMAC |  |  |
| AA01 | A11A01L05 | 12" Core |
| AA03 | A13A01L05 | 12" Core |
| AA01 | A11C01L05 | 6" Core |
| AA01 | A11C02L05 | 6" Core |
| AA01 | A11C03L05 | 6" Core |
| AA03 | A13C01L05 | 6" Core |
| AA03 | A13C02L05 | 6" Core |
| AA03 | A13C03L05 | 6" Core |
| Granular Base |  |  |
| AA01 | A11A01L04 | 75 lb. Bulk Sample (Base) |
| AA01 | A11A02L04 | 75 lb. Bulk Sample (Base) |
| AA03 | A13A01L04 | 75 lb. Bulk Sample (Base) |
| AA03 | A13A02L04 | 75 lb. Bulk Sample (Base) |
| Pulverized Pavement (if present) |  |  |
| AA01 | A11A01L03 | 75 lb. Bulk Sample (Pulverized AC) |
| AA01 | A11A02L03 | 75 lb. Bulk Sample (Pulverized AC) |
| AA03 | A13A01L03 | 75 lb. Bulk Sample (Pulverized AC) |
| AA03 | A13A02L03 | 75 lb. Bulk Sample (Pulverized AC) |

TABLE 12: SAMPLES TO BE SHIPPED TO CLTC LAB (Continued)

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Granular Subbase |  |  |
| AA01 | A11A01L02 | 75 lb. Bulk Sample (Subbase) |
| AA01 | A11A02L02 | 75 lb. Bulk Sample (Subbase) |
| AA03 | A13A01L02 | 75 lb. Bulk Sample (Subbase) |
| AA03 | A13A02L02 | 75 lb. Bulk Sample (Subbase) |
| Subgrade |  |  |
| AA01 | A11A01L01 | 75 lb. Bulk Sample (Subgrade) |
| AA01 | A11AM1L01 | Moisture Content Jar Sample |
| AA01 | A11A02L01 | 75 lb. Bulk Sample (Subgrade) |
| AA01 | A11AM2L01 | Moisture Content Jar Sample |
| AA03 | A13A01L01 | 75 lb. Bulk Sample (Subgrade) |
| AA03 | A13AM1L01 | Moisture Content Jar Sample |
| AA03 | A13A02L01 | 75 lb. Bulk Sample (Subgrade) |
| AA03 | A13AM2L01 | Moisture Content Jar Sample |

TABLE 13: SAMPLES TO BE SHIPPED TO THE LTPP MRL

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| AA01 | A11C11L07 | 6" Core |
| AA01 | A11C12L07 | 6" Core |
| AA01 | A11C13L07 | 6" Core |
| AA01 | A11C14L07 | 6" Core |
| AA02 | A12C11L07 | 6" Core |
| AA02 | A12C12L07 | 6" Core |
| AA02 | A12C13L07 | 6" Core |
| AA02 | A12C14L07 | 6" Core |
| AA03 | A13C11L07 | 6" Core |
| AA03 | A13C12L07 | 6" Core |
| AA03 | A13C13L07 | 6" Core |
| AA03 | A13C14L07 | 6" Core |
| AA61 | A1AC11L07 | 6" Core |
| AA61 | A1AC12L07 | 6" Core |
| AA61 | A1AC13L07 | 6" Core |
| AA61 | A1AC14L07 | 6" Core |
| AA62 | A1BC11L07 | 6" Core |
| AA62 | A1BC12L07 | 6" Core |
| AA62 | A1BC13L07 | 6" Core |
| AA62 | A1BC14L07 | 6" Core |

TABLE 13: SAMPLES TO BE SHIPPED TO THE LTPP MRL (Continued)

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| AA01 | A11H03L07 | 4 1-gallon can of virgin AC Binder (PG 58-28) |
| AA02 | A12H01L07 |  |
| AA02 | A12H02L07 |  |
| AA02 | A12H03L07 |  |
| AA03 | A13H03L07 | 4 1-gallon can of virgin AC Binder (PG 58-28) mixed with Evotherm® M1 |
| AA03 | A13H04L07 |  |
| AA03 | A13H05L07 |  |
| AA03 | A13H06L07 |  |
| AA61 | A1AH03L07 | 4 1-gallon can of virgin AC Binder (PG 58-28) mixed with WarmGrip® E5 |
| AA61 | A1AH04L07 |  |
| AA61 | A1AH05L07 |  |
| AA61 | A1AH06L07 |  |
| AA62 | A1BH03L07 | 4 1-gallon can of virgin AC Binder (PG 58-28) mixed with Rediset® WMX 8017 |
| AA62 | A1BH04L07 |  |
| AA62 | A1BH05L07 |  |
| AA62 | A1BH06L07 |  |
| AA01 | A11F01L07 | 15 5-gallon buckets uncompacted AC mix |
| AA01 | A11F02L07 |  |
| AA01 | A11F03L07 |  |
| AA01 | A11F04L07 |  |
| AA01 | A11F05L07 |  |
| AA01 | A11F06L07 |  |
| AA01 | A11F07L07 |  |
| AA01 | A11F08L07 |  |
| AA01 | A11F09L07 |  |
| AA01 | A11F10L07 |  |
| AA01 | A11F11L07 |  |
| AA01 | A11F12L07 |  |
| AA01 | A11F13L07 |  |
| AA01 | A11F14L07 |  |
| AA01 | A11F15L07 |  |

TABLE 13: SAMPLES TO BE SHIPPED TO THE LTPP MRL (Continued)

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| AA02 | A12F01L07 | 15 5-gallon buckets uncompacted AC mix |
| AA02 | A12F02L07 |  |
| AA02 | A12F03L07 |  |
| AA02 | A12F04L07 |  |
| AA02 | A12F05L07 |  |
| AA02 | A12F06L07 |  |
| AA02 | A12F07L07 |  |
| AA02 | A12F08L07 |  |
| AA02 | A12F09L07 |  |
| AA02 | A12F10L07 |  |
| AA02 | A12F11L07 |  |
| AA02 | A12F12L07 |  |
| AA02 | A12F13L07 |  |
| AA02 | A12F14L07 |  |
| AA02 | A12F15L07 |  |
| AA03 | A13F01L07 | 15 5-gallon buckets uncompacted AC mix |
| AA03 | A13F02L07 |  |
| AA03 | A13F03L07 |  |
| AA03 | A13F04L07 |  |
| AA03 | A13F05L07 |  |
| AA03 | A13F06L07 |  |
| AA03 | A13F07L07 |  |
| AA03 | A13F08L07 |  |
| AA03 | A13F09L07 |  |
| AA03 | A13F10L07 |  |
| AA03 | A13F11L07 |  |
| AA03 | A13F12L07 |  |
| AA03 | A13F13L07 |  |
| AA03 | A13F14L07 |  |
| AA03 | A13F15L07 |  |

TABLE 13: SAMPLES TO BE SHIPPED TO THE LTPP MRL (Continued)

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| AA61 | A1AF01L07 | 15 5-gallon buckets uncompacted AC mix |
| AA61 | A1AF02L07 |  |
| AA61 | A1AF03L07 |  |
| AA61 | A1AF04L07 |  |
| AA61 | A1AF05L07 |  |
| AA61 | A1AF06L07 |  |
| AA61 | A1AF07L07 |  |
| AA61 | A1AF08L07 |  |
| AA61 | A1AF09L07 |  |
| AA61 | A1AF10L07 |  |
| AA61 | A1AF11L07 |  |
| AA61 | A1AF12L07 |  |
| AA61 | A1AF13L07 |  |
| AA61 | A1AF14L07 |  |
| AA61 | A1AF15L07 |  |
| AA62 | A1BF01L07 | 15 5-gallon buckets uncompacted AC mix |
| AA62 | A1BF02L07 |  |
| AA62 | A1BF03L07 |  |
| AA62 | A1BF04L07 |  |
| AA62 | A1BF05L07 |  |
| AA62 | A1BF06L07 |  |
| AA62 | A1BF07L07 |  |
| AA62 | A1BF08L07 |  |
| AA62 | A1BF09L07 |  |
| AA62 | A1BF10L07 |  |
| AA62 | A1BF11L07 |  |
| AA62 | A1BF12L07 |  |
| AA62 | A1BF13L07 |  |
| AA62 | A1BF14L07 |  |
| AA62 | A1BF15L07 |  |

TABLE 13: SAMPLES TO BE SHIPPED TO THE LTPP MRL (Continued)

| Section | Specimen ID | Type of Sample |
| --- | --- | --- |
| Experimental AC |  |  |
| AA01 | A11H04L07 | 10 5-gallon buckets combined aggregate |
| AA01 | A11H05L07 |  |
| AA02 | A12H04L07 |  |
| AA02 | A12H05L07 |  |
| AA03 | A13H07L07 |  |
| AA03 | A13H08L07 |  |
| AA61 | A1AH07L07 |  |
| AA61 | A1AH08L07 |  |
| AA62 | A1BH07L07 |  |
| AA62 | A1BH08L07 |  |
| AA01 | A11H07L07 | 5 5-gallon buckets RAP |
| AA02 | A12H06L07 |  |
| AA03 | A13H09L07 |  |
| AA61 | A1AH09L07 |  |
| AA62 | A1BH09L07 |  |

TABLE 14: SAMPLES TO BE SHIPPED TO THE TURNER FAIRBANKS HIGHWAY RESEARCH CENTER (TFHRC)

| Specimen ID | Type of Sample |
| --- | --- |
| Experimental AC |  |
| A11H02L07 | 1 1-gallon can of virgin AC Binder (PG 58-28) |
| A13H02L07 | 1 1-gallon can of AC Binder (PG 58-28) mixed with Evotherm® M1 |
| A1AH02L07 | 1 1-gallon can of AC Binder (PG 58-28) mixed with Rediset® WMX 8017 |
| A1BH02L07 | 1 1-gallon can of AC Binder (PG 58-28) mixed with WarmGrip® E5 |

## LABORATORY MATERIALS TESTING

It is the intent of this section of the sampling and testing plan to provide an outline for the laboratory testing that is planned for the Ontario SPS-10 projects.  The previous section ended with lists of samples to be shipped to each of the two laboratories, the central lab testing contractor (CLTC) laboratory and the Turner-Fairbank Highway Research Center (TFHRC).  In this section, the tests to be performed on each sample are listed.

Table 15 provides listings of laboratory tests to be performed for each material type and pavement layer as well as the associated laboratory testing protocol. It is imperative that the protocols listed be strictly followed during testing.

Tables 16 and 17 provide new sample numbers and specimen ID’s for samples that will either be combined or modified in the laboratory.  The provided sample numbers and specimen ID’s should be used to ensure proper tracking using the Materials Tracking System (MTS).

Tables 18 through 25 provide tracking tables for the testing to be conducted for each material type.  These tables itemize the testing to occur on each sample and provide indication of how to process a sample after a specific test is complete.

TABLE 15: SPS-10 LABORATORY TESTING PLANS

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| A. | EXPERIMENTAL AC SURFACE LAYER |  |  |  |  |  |
|  | Bulk Specific Gravity | AC02 | P02 | 50 | X |  |
|  | Maximum Specific Gravity | AC03 | P03 | 5 | X |  |
|  | Asphalt Content (Extracted) | AC04 | P04 | 5 | X |  |
|  | Dynamic Modulus | AC08 | P74 | 10 | X |  |
|  | Hamburg Wheel Track | AC09 | P75 | 10 | X |  |
|  | Fenix Fracture Energy | AC10 | P79 | 20 | X |  |
|  | Specific Gravity at 60 ° F | AE03 | P23 | 5 | X |  |
|  | Dynamic Shear Rheometer (DSR) Test | AE07 | P27 | 10 | X |  |
|  | Superpave Direct Tension (DT) Test | AE08 | P28 | 5 | X |  |
|  | Multiple Stress Creep Recovery (MSCR) | AE10 | P73 | 5 | X |  |
|  | Gradation of Aggregate | AG04 | P14 | 5 | X |  |
|  | PPA and Motor Oil Test | AE11 | P76 | 4 |  | X |

TABLE 15: SPS-10 LABORATORY TESTING PLANS (Continued)

| Material Type and Properties |  | LTPP Designation |  | LTPP Protocol |  | No. of Tests per Layer |  | Test Conducted By: |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  | CLTC | TFHRC |  |
| B. |  | Experimental AC Binder Layer |  |  |  |  |  |  |  |  |  |  |
|  |  | Bulk Specific Gravity |  | AC02 |  | P02 |  | 12 |  | X |  |  |
|  |  | Maximum Specific Gravity |  | AC03 |  | P03 |  | 4 |  | X |  |  |
|  |  | Asphalt Content (Extracted) |  | AC04 |  | P04 |  | 4 |  | X |  |  |
|  |  | Dynamic Modulus |  | AC08 |  | P74 |  | 8 |  | X |  |  |
|  |  | Dynamic Shear Rheometer (DSR) Test |  | AE07 |  | P27 |  | 4 |  | X |  |  |
|  |  | Superpave Direct Tension (DT) Test |  | AE08 |  | P28 |  | 4 |  | X |  |  |
|  |  | Multiple Stress Creep Recovery (MSCR) |  | AE10 |  | P73 |  | 4 |  | X |  |  |
|  |  | Gradation of Aggregate |  | AG04 |  | P14 |  | 4 |  | X |  |  |
| C. |  | ORIGINAL HMAC (1 LAYER) |  |  |  |  |  |  |  |  |  |  |
|  |  | Bulk Specific Gravity |  | AC02 |  | P02 |  | 12 |  | X |  |  |
|  |  | Maximum Specific Gravity |  | AC03 |  | P03 |  | 4 |  | X |  |  |
|  |  | Asphalt Content (Extracted) |  | AC04 |  | P04 |  | 4 |  | X |  |  |
|  |  | Dynamic Modulus |  | AC08 |  | P74 |  | 8 |  | X |  |  |
|  |  | Dynamic Shear Rheometer (DSR) Test |  | AE07 |  | P27 |  | 4 |  | X |  |  |
|  |  | Superpave Direct Tension (DT) Test |  | AE08 |  | P28 |  | 4 |  | X |  |  |
|  |  | Multiple Stress Creep Recovery (MSCR) |  | AE10 |  | P73 |  | 4 |  | X |  |  |
|  |  | Gradation of Aggregate |  | AG04 |  | P14 |  | 4 |  | X |  |  |

TABLE 15: SPS-10 LABORATORY TESTING PLANS (Continued)

| Material Type and Properties |  | LTPP Designation | LTPP Protocol | No. of Tests per Layer | Test Conducted By: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | CLTC | TFHRC |
| D. | GRANULAR BASE |  |  |  |  |  |
|  | Washed Sieve Analysis | UG02 | P41 | 4 | X |  |
|  | Standard Proctor | UG05 | P44 | 4 | X |  |
|  | Atterberg Limits | UG04 | P43 | 4 | X |  |
|  | Resilient Modulus | UG07 | P46 | 4 | X |  |
|  | Classification and Description | UG08 | P47 | 4 | X |  |
| E. | PULVERIZED PAVEMENT (if present) |  |  |  |  |  |
|  | Identification and Description of Pulverized Pavement Material | TB01 | P31 | 4 | X |  |
| F. | GRANULAR SUBBASE |  |  |  |  |  |
|  | Washed Sieve Analysis | UG02 | P41 | 4 | X |  |
|  | Standard Proctor | UG05 | P44 | 4 | X |  |
|  | Atterberg Limits | UG04 | P43 | 4 | X |  |
|  | Resilient Modulus | UG07 | P46 | 4 | X |  |
|  | Classification and Description | UG08 | P47 | 4 | X |  |
| G. | SUBGRADE |  |  |  |  |  |
|  | Sieve Analysis | SS01 | P51 | 4 | X |  |
|  | Atterberg Limits | SS03 | P43 | 4 | X |  |
|  | Classification and Description | SS04 | P52 | 4 | X |  |
|  | Standard Proctor | SS05 | P55 | 4 | X |  |
|  | Resilient Modulus | SS07 | P46 | 4 | X |  |
|  | Natural Moisture Content | SS09 | P49 | 4 | X |  |

TABLE 16: ORIGINAL AND COMBINED SPECIMEN DESCRIPTIONS

| Section | Description Type | Status |  |  |
| --- | --- | --- | --- | --- |
|  |  | Original |  | Combined1 |
| AA01 | Sample No. | BA01001 | BA02001 | BAX1001 |
|  | Specimen ID | A11A01L07 | A11A02L07 | A11A01M07 |
| AA02 | Sample No. | BA01002 | BA02002 | BAX1002 |
|  | Specimen ID | A12A01L07 | A12A02L07 | A12A01M07 |
| AA03 | Sample No. | BA01003 | BA02003 | BAX1003 |
|  | Specimen ID | A13A01L07 | A13A02L07 | A13A01M07 |
| AA61 | Sample No. | BA01061 | BA02061 | BAX1061 |
|  | Specimen ID | A1AA01L07 | A1AA02L07 | A1AA01M07 |
| AA62 | Sample No. | BA01062 | BA02062 | BAX1062 |
|  | Specimen ID | A1BA01L07 | A1BA02L07 | A1BA01M07 |
| AA01 | Sample No. | BG01001 | BG03001 | BGX1001 |
|  | Specimen ID | A11A01L04 | A11A03L04 | A11A01M04 |
| AA03 | Sample No. | BG01003 | BG03003 | BGX1003 |
|  | Specimen ID | A13A01L04 | A13A03L04 | A13A01M04 |
| AA01 | Sample No. | BT01001 | BT02001 | BTX1001 |
|  | Specimen ID | A11A01L03 | A11A02L03 | A11A01M03 |
| AA03 | Sample No. | BT01003 | BT02003 | BTX1003 |
|  | Specimen ID | A13A01L03 | A13A02L03 | A13A01M03 |
| AA01 | Sample No. | BG02001 | BG04001 | BGX2001 |
|  | Specimen ID | A11A01L02 | A11A03L02 | A11A01M02 |
| AA03 | Sample No. | BG02003 | BG04003 | BGX2003 |
|  | Specimen ID | A13A01L02 | A13A03L02 | A13A01M02 |
| AA01 | Sample No. | BS01001 | BS03001 | BSX1001 |
|  | Specimen ID | A11A01L01 | A11A03L01 | A11A01M01 |
| AA03 | Sample No. | BS01003 | BS03003 | BSX1003 |
|  | Specimen ID | A13A01L01 | A13A03L01 | A13A01M01 |
| AA01 | Sample No. | MS01001 | MS02001 | MSX1001 |
|  | Specimen ID | A11AM1L01 | A11AM2L01 | A11AM1M01 |
| AA03 | Sample No. | MS01003 | MS02003 | MSX1003 |
|  | Specimen ID | A13AM1L01 | A13AM2L01 | A13AM1M01 |

1. Sample No.:  After combination, the third character is changed to “X,” and the fourth character is assigned numerically.  The other five characters follow the original format.

Specimen ID:  After combination, “L” is changed to “M.”

TABLE 17: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS

| Section | Process | Description Type | Status |  |
| --- | --- | --- | --- | --- |
|  |  |  | Original | Modified1 |
| AA01 | Extraction | Sample No. | BAX1001 | BAE1001 |
|  |  | Specimen ID | A11A01M07 | A11A01A07 |
| AA02 |  | Sample No. | BAX1002 | BAE1002 |
|  |  | Specimen ID | A12A01M07 | A12A01A07 |
| AA03 |  | Sample No. | BAX1003 | BAE1003 |
|  |  | Specimen ID | A13A01M07 | A13A01A07 |
| AA61 |  | Sample No. | BAX1061 | BAE1061 |
|  |  | Specimen ID | A1AA01M07 | A1AA01A07 |
| AA62 |  | Sample No. | BAX1062 | BAE1062 |
|  |  | Specimen ID | A1BA01M07 | A1BA01A07 |
| AA01 |  | Sample No. | BA03001 | BAE2001 |
|  |  | Specimen ID | A11A01L06 | A11A01M06 |
| AA03 |  | Sample No. | BA03003 | BAE2003 |
|  |  | Specimen ID | A13A01L06 | A13A01M06 |
| AA01 |  | Sample No. | BA03001 | BAE2001 |
|  |  | Specimen ID | A11A01L05 | A11A01M05 |
| AA03 |  | Sample No. | BA03003 | BAE2003 |
|  |  | Specimen ID | A13A01L05 | A13A01M05 |
| AA01 |  | Sample No. | BR01001 | BRE1001 |
|  |  | Specimen ID | A11H06L07 | A11H06M07 |
| AA01 | PAV | Sample No. | BAE1001 | BAP1001 |
|  |  | Specimen ID | A11A01A07 | A11A01B07 |
| AA02 |  | Sample No. | BAE1002 | BAP1002 |
|  |  | Specimen ID | A12A01A07 | A12A01B07 |
| AA03 |  | Sample No. | BAE1003 | BAP1003 |
|  |  | Specimen ID | A13A01A07 | A13A01B07 |
| AA61 |  | Sample No. | BAE1061 | BAP1061 |
|  |  | Specimen ID | A1AA01A07 | A1AA01B07 |
| AA62 |  | Sample No. | BAE1062 | BAP1062 |
|  |  | Specimen ID | A1BA01A07 | A1BA01B07 |

TABLE 17: ORIGINAL AND MODIFIED SPECIMEN DESCRIPTIONS (Continued)

| Section | Process | Description Type | Status |  |
| --- | --- | --- | --- | --- |
|  |  |  | Original | Modified1 |
| AA01 | RTFO | Sample No. | BC01001 | BCR1001 |
|  |  | Specimen ID | A11H01L07 | A11H01M07 |
| AA03 |  | Sample No. | BC01003 | BCR1003 |
|  |  | Specimen ID | A13H01L07 | A13H01M07 |
| AA61 |  | Sample No. | BC01061 | BCR1061 |
|  |  | Specimen ID | A1AH01L07 | A1AH01M07 |
| AA62 |  | Sample No. | BC01062 | BCR1062 |
|  |  | Specimen ID | A1BH01L07 | A1BH01M07 |
| AA01 | RTFO + PAV | Sample No. | BC01001 | BCZ1001 |
|  |  | Specimen ID | A11H01L07 | A11H01A07 |
| AA03 |  | Sample No. | BC01003 | BCZ1003 |
|  |  | Specimen ID | A13H01L07 | A13H01A07 |
| AA61 |  | Sample No. | BC01061 | BCZ1061 |
|  |  | Specimen ID | A1AH01L07 | A1AH01A07 |
| AA62 |  | Sample No. | BC01062 | BCZ1062 |
|  |  | Specimen ID | A1BH01L07 | A1BH01A07 |

1. Sample No.:  After modification, the third character is changed to “E” for extracted, “P” for PAV, “R” for RTFO or “Z” for RTFO+PAV.  The fourth character is assigned numerically.  Specimen ID:  After modification, “L” is changed to “M.”  If the sample has already been combined or modified, the letter is advanced alphabetically beginning with “A.”

TABLE 18: TRACKING TABLE OF EXPERIMENTAL AC SURFACE LAYER IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11A01M07 | P03/AC03 | P04/AC04 |  |  |  | Yes | E |
| A12A01M07 | P03/AC03 | P04/AC04 |  |  |  | Yes | E |
| A13A01M07 | P03/AC03 | P04/AC04 |  |  |  | Yes | E |
| A1AA01M07 | P03/AC03 | P04/AC04 |  |  |  | Yes | E |
| A1BA01M07 | P03/AC03 | P04/AC04 |  |  |  | Yes | E |
| A11A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| A12A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| A13A01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| A1AA01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| A1BA01A07 | P23/AE03 | P27/AE07 | P73/AE10 | P14/AG04 |  | Yes | P |
| A11A01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| A12A01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| A13A01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| A1AA01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| A1BA01B07 | P27/AE07 | P28/AE08 |  |  |  | No | D |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL AC SURFACE LAYER IN THE CLTC LAB (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11C01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| A11C02L07 | P02/AC02 |  |  |  |  | No | D |
| A11C03L07 | P02/AC02 |  |  |  |  | No | D |
| A11C04L07 | P02/AC02 |  |  |  |  | Yes | S |
| A11C05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A11C06L07 | P02/AC02 |  |  |  |  | Yes | S |
| A11C07L07 | P02/AC02 |  |  |  |  | Yes | S |
| A11C08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| A11C09L07 | P02/AC02 |  |  |  |  | No | D |
| A11C10L07 | P02/AC02 |  |  |  |  | Yes | S |
| A12C01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| A12C02L07 | P02/AC02 |  |  |  |  | No | D |
| A12C03L07 | P02/AC02 |  |  |  |  | No | D |
| A12C04L07 | P02/AC02 |  |  |  |  | Yes | S |
| A12C05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A12C06L07 | P02/AC02 |  |  |  |  | Yes | S |
| A12C07L07 | P02/AC02 |  |  |  |  | Yes | S |
| A12C08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| A12C09L07 | P02/AC02 |  |  |  |  | No | D |
| A12C10L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL AC SURFACE LAYER IN THE CLTC LAB (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A13C01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| A13C02L07 | P02/AC02 |  |  |  |  | No | D |
| A13C03L07 | P02/AC02 |  |  |  |  | No | D |
| A13C04L07 | P02/AC02 |  |  |  |  | Yes | S |
| A13C05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A13C06L07 | P02/AC02 |  |  |  |  | Yes | S |
| A13C07L07 | P02/AC02 |  |  |  |  | Yes | S |
| A13C08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| A13C09L07 | P02/AC02 |  |  |  |  | No | D |
| A13C10L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1AC01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| A1AC02L07 | P02/AC02 |  |  |  |  | No | D |
| A1AC03L07 | P02/AC02 |  |  |  |  | No | D |
| A1AC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1AC05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A1AC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1AC07L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1AC08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| A1AC09L07 | P02/AC02 |  |  |  |  | No | D |
| A1AC10L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL AC SURFACE LAYER IN THE CLTC LAB (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A1BC01L07 | P02/AC02 | P79/AC10 (performed on 3 cores + 1 spare) |  |  |  | No | D |
| A1BC02L07 | P02/AC02 |  |  |  |  | No | D |
| A1BC03L07 | P02/AC02 |  |  |  |  | No | D |
| A1BC04L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1BC05L07 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A1BC06L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1BC07L07 | P02/AC02 |  |  |  |  | Yes | S |
| A1BC08L07 | P02/AC02 | P75/AC09(performed on 2 cores + 1 spare) |  |  |  | No | D |
| A1BC09L07 | P02/AC02 |  |  |  |  | No | D |
| A1BC10L07 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 18: TRACKING TABLE OF EXPERIMENTAL AC SURFACE LAYER IN THE CLTC LAB (Continued)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process1 |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11H01L07 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| A11H01M07 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| A11H01A07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| A13H01L07 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| A13H01M07 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| A13H01A07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| A1AH01L07 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| A1AH01M07 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| A1AH01A07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| A1BH01L07 | P23/AE03 | P27/AE07 |  |  |  | Yes | R, R+P, S |
| A1BH01M07 | P27/AE07 | P73/AE10 |  |  |  | No | D |
| A1BH01A07 | P27/AE07 | P28/AE08 |  |  |  | No | D |
| A11H06L07 | P04/AC04 |  |  |  |  | Yes | E, S |
| A11H06M07 | P23/AE03 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 | No | D |

1. Next Process 	D 	Remaining sample should be disposed
		S 	Remaining sample should be stored
		C	Remaining sample will be combined with another sample
		E 	Perform further testing on extracted sample
		P 	Perform further testing with PAV
		R 	Perform further testing with RFTO
		R+P 	Perform further testing with RTFO + PAV

TABLE 19: TRACKING TABLE OF EXPERIMENTAL AC BINDER LAYER IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11A01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| A13A01L06 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| A11A01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| A13A01M06 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| A11C01L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A11C02L06 | P02/AC02 |  |  |  |  | Yes | S |
| A11C03L06 | P02/AC02 |  |  |  |  | Yes | S |
| A13C01L06 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A13C02L06 | P02/AC02 |  |  |  |  | Yes | S |
| A13C03L06 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 20: TRACKING TABLE OF ORIGINAL HOT MIX ASPHALT CONCRETE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| A13A01L05 | P03/AC03 | P04/AC04 |  |  |  | No | E |
| A11A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| A13A01M05 | P27/AE07 | P28/AE08 | P73/AE10 | P14/AG04 |  | No | D |
| A11C01L05 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A11C02L05 | P02/AC02 |  |  |  |  | Yes | S |
| A11C03L05 | P02/AC02 |  |  |  |  | Yes | S |
| A13C01L05 | P02/AC02 | P74/AC08 (2 dyn. mod. tests performed on different specim. from the 3 cores) |  |  |  | No | D |
| A13C02L05 | P02/AC02 |  |  |  |  | Yes | S |
| A13C03L05 | P02/AC02 |  |  |  |  | Yes | S |

TABLE 21: TRACKING TABLE OF BASE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11A01M04 | P41/UG02 | P47/UG08 | P43/UG04 | P46/UG07 | P44/UG05 | Yes | S |
| A13A01M04 | P41/UG02 | P47/UG08 | P43/UG04 | P46/UG07 | P44/UG05 | Yes | S |

TABLE 22: TRACKING TABLE OF PULVERIZED ASPHALT BASE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11A01M03 | P31/TB01 |  |  |  |  | Yes | S |
| A13A01M03 | P31/TB01 |  |  |  |  | Yes | S |

TABLE 23: TRACKING TABLE OF SUBBASE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11A01M02 | P41/UG02 | P47/UG08 | P43/UG04 | P46/UG07 | P44/UG05 | Yes | S |
| A13A01M02 | P41/UG02 | P47/UG08 | P43/UG04 | P46/UG07 | P44/UG05 | Yes | S |

TABLE 24: TRACKING TABLE OF SUBGRADE IN THE CENTRAL LAB TESTING CONTRACTOR (CLTC) LABORATORY

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11A01M01 | P51/SS01 | P43/SS03 | P52/SS04 | P46/SS07 | P55/SS05 | Yes1 | S |
| A13A01M01 | P51/SS01 | P43/SS03 | P52/SS04 | P46/SS07 | P55/SS05 | Yes1 | S |
| A11AM1M01 | P49/SS09 |  |  |  |  | No1 | D |
| A13AM1M01 | P49/SS09 |  |  |  |  | No1 | D |

1. The moisture content sample may be disposed after testing.  However, any remaining bulk sample should be stored.

TABLE 25: TRACKING TABLE OF EXPERIMENTAL AC SURFACE LAYER OVERLAY IN THE TURNER FAIRBANKS HIGHWAY RESEARCH CENTER (TFHRC)

| Specimen ID | Steps Involved in Laboratory Handling and Testing Sequence |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Required Laboratory Tests Per Layer |  |  |  |  | Extra Sample | Next Process |
|  | First | Second | Third | Fourth | Fifth |  |  |
| A11H02L07 | P76/AE11 |  |  |  |  | Yes | S |
| A13H02L07 | P76/AE11 |  |  |  |  | Yes | S |
| A1AH02L07 | P76/AE11 |  |  |  |  | Yes | S |
| A1BH02L07 | P76/AE11 |  |  |  |  | Yes | S |