LONG-TERM PAVEMENT PERFORMANCE

SPECIFIC PAVEMENT STUDIES

Construction Report on LTPP 87AA00, SPS-10 Project

York Region - Greater Toronto Area, Ontario, Canada

Report No. FHWA-…

Prepared by

Stantec Consulting Inc.

1000 Young St., Suite # 470,

Tonawanda, NY 14150

United States of America

Prepared for

U.S. Department of Transportation

Federal Highway Administration

Office of Acquisition Management

1200 New Jersey Ave., SE

Washington, D.C. 20950

June 2017

# Foreword

Warm Mix Asphalt (WMA) technology is part of the Federal Highway Administration’s (FHWA) Every Day Counts program, and has been implemented by Highway Agencies throughout the United States and Canada. A variety of WMA technologies have been designed to allow for production and compaction of asphalt concrete at temperatures lower than conventional Hot Mix Asphalt (HMA).

Recognizing that a knowledge gap exists in the comparison of WMA and HMA over the performance life of each type of pavement, the FHWA Long-Term Pavement Performance

(LTPP) program initiated the Specific Pavement Study 10 (SPS-10) experiment, “Warm Mix Asphalt Overlay of Asphalt Pavement Study”. The Ontario SPS-10 site in York Region, Ontario (87AA00) is the second site constructed in the North Atlantic region of the LTPP program as part of this national experiment to study the short and long-term performance of WMA in comparison with HMA. This report highlights the corresponding construction information.

# Notice

This document is disseminated under the sponsorship of the Department of Transportation in the interest of information exchange. The United States Government assumes no liability for its contents or use thereof.

The United States Government does not endorse products or manufacturers. Trade or manufacturer’s names appear herein only because they are considered essential to the object of this document.

# Quality Assurance Statement

The Federal Highway Administration (FHWA) provides high-quality information to serve Government, industry, and the public in a manner that promotes public understanding. Standards and policies are used to ensure and maximize the quality, objectivity, utility, and integrity of its information. FHWA periodically reviews quality issues and adjusts its programs and processes to ensure continuous quality improvement.

| 1. Report No. FHWA-RD-… |  | 2. Government Accession No. … |  | 3. Recipient’s Catalog No. … |  |
| --- | --- | --- | --- | --- | --- |
| 4. Title and Subtitle LTPP Specific Pavement Studies 10 (SPS-10) Project 87AA00: Warm Mix Asphalt Overlay Study on Provincial Highway 48, in York Region - Greater Toronto Area, Province of Ontario, Canada |  |  |  | 5. Report Date June 2017 |  |
|  |  |  |  | 6. Performing Operations Code … |  |
| 7. Author(s) Mizan Moges, Carlos Leal, Basel Abukhater, Gabe Cimini |  |  |  | 8. Performing Operations Report No. … |  |
| 9. Performing Organization Name and Address Stantec Consulting Inc. 1000 Young St. Suite 470 Tonawanda NY 14150 United States of America |  |  |  | 10. Work Unit No. (TRAIS) … |  |
|  |  |  |  | 11. Contract or Grant No. … |  |
| 12. Sponsoring Agency Name and Address Federal Highway Administration LTPP-Division, HRDI-13 Turner-Fairbanks Highway Research Center 6300 Georgetown Pike McLean, Virginia 22101 |  |  |  | 13. Type of Report and Period Covered … |  |
|  |  |  |  | 14. Sponsoring Agency Code … |  |
| 15. Supplementary Notes Contracting Officer’s Representative (COR): Jack Springer – Turner-Fairbank Highway Research Center |  |  |  |  |  |
| 16. Abstract This report documents the construction activities related to the Ontario SPS-10 (87AA00) project as part of the Long-Term Pavement Performance (LTPP) program’s Warm Mix Asphalt (WMA) study. Project 87AA00 was constructed on the northbound lane of Provincial Highway 48 (King’s Highway), in York Region - Greater Toronto Area, Province of Ontario, Canada. The project site included five test sections: a hot-mix asphalt (HMA) control section, a WMA foaming process, a WMA chemical additive (Evotherm® M1), a WMA chemical additive (Warm Grip® E5), and a WMA organic additive (Rediset® WMX 8017). This report includes the details of the project and the associated construction events. |  |  |  |  |  |
| 17. Key Words Warm Mix Asphalt, WMA, Long-Term Pavement Performance, LTPP, Pavement, Specific Pavement Studies, SPS-10, Construction, Sampling, Materials, 87AA00, Ontario, Evotherm® M1, Rediset® WMX 8017, Warm Grip® E5, Foaming Process, Chemical Additive, Organic Additive |  |  | 18. Distribution Statement … |  |  |
| 19. Security Classification (of this report) Unclassified | 20. Security Classification (of this page) Unclassified |  | 21. No. of Pages … |  | 22. Price … |

Form DOT F 1700.7 (8-72) Reproduction of completed page authorized.

TABLE OF CONTENTS

Foreword	2

Notice	2

Quality Assurance Statement	2

Chapter 1: INTRODUCTION	1

General Overview of SPS-10 Study	1

Project Overview	2

Report Organization	3

Chapter 2: PROJECT DESCRIPTION	4

Test Section Layout	4

Physical Attributes	7

Project Geometry	18

Climate	20

Traffic	22

Supplemental Test Sections	22

Project Personnel	22

Project timeline	23

Chapter 3: CONSTRUCTION DETAILS	26

Materials	26

Equipment	28

Construction Events	42

Post-Construction Events (DCP and core thickness measurements?)	A.49

Chapter 4: SUMMARY	A.55

Chapter 5: KEY OBSERVATIONS	A.56

Acknowledgments	F.91

LIST OF FIGURES

Figure 1: Ontario SPS-10 87AA00 – Project Layout	6

Figure 2: Ontario SPS-10 87AA00 – Location Overview	7

Figure 3: Detailed Layout of SPS-10 87AA00 Test Sections in Ontario	8

Figure 4: Pavement Cross Section a) pre-overlay b) post-overlay	9

Figure 5: Site Overview of 87AA01	11

Figure 6: Site Overview of 87AA02	12

Figure 7:  Site Overview of 87AA03	12

Figure 8:  Site Overview of 87AA61	13

Figure 9: Site Overview of 87AA62	13

Figure 10: Pre-Overlay Normalized Deflection for Sections 83AA01, 83AA02, 83AA03, 83AA61, and 83AA62	16

Figure 11:  Post-Overlay Normalized Deflection Sections 83AA01, 83AA02, 83AA03, 83AA61, and 83AA62	17

Figure 12: Sat-T-Log® Thermometer	28

Figure 13: Fluke® 62 Max + IR Thermometer	29

Figure 14: Raytek MiniTemp MT6 IR Thermometer	29

Figure 15: Location of Asphalt Concrete Mix Plant	30

Figure 16: Aggregate Stock Piles	32

Figure 17: RAP Stock Piles	32

Figure 18: Asphalt Mix Plant - Cold Feed Bins	33

Figure 19: Asphalt Mix Plant Control Center	33

Figure 20: Asphalt Mix Plant - Conveyor Belt	34

Figure 21: Asphalt Mix Plant – Mixing Drum	34

Figure 22: Asphalt Mix Plant - Baghouse	35

Figure 23: Asphalt Mix Plant – Asphalt Cement Storage Tanks	35

Figure 24: Asphalt Mix Plant - Pugmill	36

Figure 25: Asphalt Mix Plant – Storage Silos	36

Figure 26: Asphalt Mix Plant - Truck Loading Area	37

Figure 30: Bruell 741 – Sweep Pavement Surface of Debris Pre-Overlay	38

Figure 31: Etnyre Black-Topper - Used to Apply Tack Coat to Surface	38

Figure 32: Typical End-Dump Truck – Used to transport AC from Plant to Hopper on Site	39

Figure 33: WEILER Hopper with Conveyor Model SB-1542 – Used to Buffer Between AC Truck and Paver to Ensure Paving Flow	39

Figure 34: CAT Paver, Model AP1055F	40

Figure 35: Break Down Roller - HAMM Articulated Tandem Roller, Model HD + 140, Operating Weight with Cab: 31989.1 lbs.	40

Figure 36: Intermediate Roller - Caterpillar Pneumatic Roller, Model PS-300C, Operating Weight: 14000.0 lbs.	41

Figure 37: Final Roller - CAT Split Drum Tandem Vibratory Roller, Model CD54B, Operating Weight: 22311.0 lbs.	41

Figure 39: Thermal Image at Station ~400m, South of Ravenshoe Road	A.47

Figure 40: Thermal Image at Station ~417m, Section 87AA02	A.47

Figure 40: Customized Equipment to Extract 12 inch Cores	A.50

Figure 41: Coring	A.50

Figure 42: Core Hole Filling	A.51

Figure 43: Dynamic Cone Penetrometer	A.52

Figure 44: Nuclear Density Gage	A.53

Figure 46: Assumed Lane Edge -Benchmark Used to Determine Overlay Thickness	A.54

Figure 46: Centerline Joint – Interlocked Pavement (west looking east)	A.56

Figure 47: 87AA62 Tack Coat Removal by AC Trucks (west looking east)	A.56

Figure 48: Tack Coat Removal by Hopper and Paver	A.57

Figure 49: AC Mix Dropped on Road Prior to Paver	A.58

Figure 50: Boulder Caught in Paver Requiring AC Addition to Test Section 87AA63	A.59

Figure 51: 87AA03 Longitudinal Line Left by Roller Compactors	A.60

Figure 52: 87AA62 AC Bulge Left by Roller Compactors	A.60

Figure 53: 87AA64 AC Bulge Left by Intermediate Roller Compactor	A.61

Figure 54: 87AA66 Longitudinal Crack Left by Rollers	A.61

Figure 55: AC Sticking to Roller Compactor CB36B	A.62

Figure 56	A.1

Figure 57	A.1

Figure 58	A.2

Figure 59	A.2

Figure 60	A.3

Figure 61	A.3

Figure 62	A.4

Figure 63	A.4

Figure 64	A.5

Figure 65	A.5

Figure 66	A.6

Figure 67	A.6

Figure 68	A.7

Figure 69	A.7

Figure 70	A.8

Figure 69: Density Measurement Layout for Surface Layers of Test Section 87AA01 Ontario SPS-10	C.1

Figure 70: Density Measurement Layout for Surface Layers of Test Section 87AA02 Ontario SPS-10	C.1

Figure 71: Density Measurement Layout for Surface Layers of Test Section 87AA03 Ontario SPS-10	C.2

Figure 72: Density Measurement Layout for Surface Layers of Test Section 87AA61 Ontario SPS-10	C.2

Figure 73: Density Measurement Layout for Surface Layers of Test Section 87AA62 Ontario SPS-10	C.3

Figure 74: Sampling and Testing Plan for Test Section 87AA01 at Time 0 Ontario SPS-10	C.5

Figure 75: Sampling and Testing Plan for Test Section 87AA02 at Time 0 Ontario SPS-10	C.6

Figure 78: Sampling and Testing Plan for Test Section 87AA03 at Time 0 Ontario SPS-10	C.7

Figure 79: Sampling and Testing Plan for Test Section 87AA61 at Time 0 Ontario SPS-10	C.8

Figure 80: Sampling and Testing Plan for Test Section 87AA62 at Time 0 Ontario SPS-10	C.9

Figure 81: Core Hole Locations Post-Back Fill, Prior to Secondary Milling/Filling	F.87

Figure 82: 87AA01 Core Hole Locations Post-Secondary Milling/Filling	F.87

Figure 83: 87AA02 and 20AA03 Core Hole Locations Post-Secondary Milling/Filling	F.88

Figure 84: 87AA61 and 20AA62 Core Hole Locations Post-Secondary Milling/Filling	F.88

Figure 85: 87AA63 and 20AA64 Core Hole Locations Post-Secondary Milling/Filling	F.89

Figure 86: 87AA65 and 20AA66 Core Hole Locations Post-Secondary Milling/Filling	F.89

Figure 87: 87AA67 Core Hole Locations Post-Secondary Milling/Filling	F.90

LIST OF TABLES

Table 1: Test Section Identification and Description –87AA00	4

Table 2: Test Section Layout –87AA00	5

Table 3: Layer Properties	10

Table 4: Average IRI for each Test Section Pre-Overlay	14

Table 5: Average IRI for each Test Section Post-Overlay	14

Table 6: Average Texture Mean Profile Depth (MPD) for each Test Section Pre-overlay	15

Table 7: Average Texture Mean Profile Depth (MPD) for each Test Section Post-overlay	15

Table 8: Average Weather Data at Udora Weather Station, ON from 1989-2006	20

Table 9: Hourly Air Temperature Data at Uxbridge West Weather Station, ON from June 13th to June 24th, 2017	20

Table 10: Daily Rainfall Data at Uxbridge West Weather Station, ON from June 13th to June 24th, 2017	21

Table 11: Monthly Freeze Index (Degree F • Days) - Weather Data at Udora Weather Station, ON from 1989-2017	21

Table 12: Project Timeline	24

Table 13: Ontario SPS-10 Asphalt Concrete Binder and Additives	27

Table 14: Ontario SPS-10 Asphalt Concrete Matrix and Aggregate Composition	27

Table 15: Ontario SPS-10 Asphalt Concrete	27

Table 16: Construction Timeline for Test Sections	43

Table 17: Number of Trucks used to Pave Test Sections	44

Table 18: Mixing and Exhaust Temperatures for the Five Mix Designs in °F	45

Table 19: Truck Plant Temperatures for the Five Mix Designs in °F	45

Table 20: Delivery, Laydown and Air Temperatures for the Five Test Sections in °F	46

Table 21: Average Temperatures in °F	46

Table 22: Compaction Data for Test Sections	A.48

Table 23: Nuclear Density Gauge Data	A.52

Table 24: Overlay Thickness in Test Sections – (from Elevation survey or Cores?)	A.54

Table 25: Site Temperature for Section 87AA01	D.36

Table 26: Site Temperature for Section 87AA02	D.37

Table 27: Site Temperature for Section 87AA03	D.38

Table 28: Site Temperature for Section 87AA61	D.40

Table 29: Site Temperature for Section 87AA62	D.41

Table 30: Plant Temperature for Section 87AA01	D.42

Table 31: Plant Temperature for Section 87AA02	D.43

Table 32: Plant Temperature for Section 87AA03	D.44

Table 33: Plant Temperature for Section 87AA61	D.45

Table 34: Plant Temperature for Section 87AA62	D.46

Table 35: Recorded average monthly climate data values collected in Eldon, MO, US (Station GHCND:USC0023503) between 1960 and 2016.	D.47

Table 36: Recorded daily air temperature and rain fall collected at the Lee C Fine Memorial Airport, MO, US for dates October 3-6, and 10-12, 2016.	D.48

LIST OF ACRONYMS

| AASHTO | American Association of Highways and Transportation |
| --- | --- |
| AADT | Average Annual Daily Traffic |
| AC | Asphalt Concrete |
| AVR | Automatic Vehicle Recognition |
| CA | Coarse Aggregate |
| CF | Coarse Fraction |
| DHV | Design Hourly Volume |
| FHWA | Federal Highway Administration |
| FWD | Falling Weight Deflectometer |
| HMA | Hot Mix Asphalt |
| HPMS | Highway Performance Monitoring System |
| IA | Intermediate Aggregate |
| IDT | Indirect Tensile |
| LTPP | Long-Term Pavement Performance |
| MTO | Ministry of Transportation Ontario |
| NCHRP | National Cooperative Highway Research Program |
| RAP | Recycled Asphalt Pavement |
| RAS | Recycled Asphalt Shingles |
| RSC | Regional Support Contractor |
| SHRP | Strategic Highway Research Program |
| SPS | Specific Pavement Study |
| VFA | Voids Filled with Asphalt |
| VMA | Voids in Mineral Aggregate |
| WMA | Warm Mix Asphalt |
| WIM | Weight-In-Motion |

# Chapter 1: INTRODUCTION

The Long-Term Pavement Performance (LTPP) program started in 1987 as part of the Strategic Highway Research Program (SHRP). Since 1992, the LTPP program has been managed by the Federal Highway Administration (FHWA). The LTPP program monitors the performance of in-service pavements. The primary mission of this program is to understand how and why pavements perform as they do. To accomplish this goal, researchers collect pavement performance data using standard data collection procedures and protocols on a variety of pavement types. This information is stored in a database that can be used by pavement engineers and researchers worldwide to advance the science of pavement engineering.

The LTPP program identified the need for investigating specific construction, maintenance and rehabilitation practices. The LTPP program designed experiments referred to as Specific Pavement Studies (SPS) to investigate the short and long-term effects of these practices on pavement performance.

## General Overview of SPS-10 Study

The LTPP Specific Pavement Studies 10 (SPS-10) experiment is designed to capture information on the performance of Warm Mix Asphalt (WMA) in comparison to Hot Mix Asphalt (HMA), both in the short and long term. For the purposes of the experiment, WMA is defined by LTPP as asphalt mixtures produced at least 30F (-34.4C) below normal hot-mix asphalt production temperatures, or asphalt produced at or below 275F (135C). The experiment provides the ability to directly compare performance of WMA to HMA, thereby evaluating the difference in relative performance between WMA and HMA. Field performance will be captured over the long term and data from laboratory testing of WMA materials will be provided to researchers looking to evaluate various characteristics of WMA. Collectively, this information will be used for a better understanding of the potential benefits and disadvantages of WMA and for performance predictions.

The objectives of the SPS-10 experiment are to:

Evaluate and improve the practical aspects of implementing the Warm Mix Asphalt (WMA) system through a hands-on field trial by interested highway agencies.

Compare the performance of the WMA technologies against mixes designed with current highway agencies’ Hot Mix Asphalt specifications, asphalt-aggregate specifications, and mix design procedures.

Provide long-term performance data for evaluation and refinement of the WMA technologies, design procedures, and models.

Test the sensitivity of the WMA technology relative to low temperature cracking, fatigue, or permanent deformation distress factors.

Provide highway agencies the opportunity to evaluate the performance of other experimental features by the construction of supplemental sections.

The SPS-10 experiment is intended for test sections not previously in the LTPP program. Because these sections have been nominated into the program prior to rehabilitation, all construction activities, materials properties, and sampling over the entire history of the roadway on which the test sections are located shall be documented in this report.

## Project Overview

The Ontario SPS-10 project known as 87AA00 is located in York Region – Greater Toronto Area, in the Province of Ontario, along the northbound driving lane of Provincial Highway 48 (King’s Highway). These test sections represent the second SPS-10 experiment constructed in the North Atlantic region of the LTPP program. The existing pavement structure included an average thickness of 6.3-inch (159 mm) of asphalt concrete and 11.2-inch (285 mm) of unbounded granular base above the natural subgrade consisting of sandy silt soil with gravel.

This Ontario SPS-10 experiment includes a total of five different test sections: three core sections and two supplemental section. The core sections include: a section using the agency’s standard HMA as a control section, a section using WMA foaming process, and a section using WMA with chemical additive Evotherm® M1. The supplemental sections include: a section using WMA with chemical additive Warm Grip® E5, and a section using WMA with organic additive Rediset® WMX 8017. The Asphalt Concrete (AC) mixes for the SPS-10 sections on this project were designed using a Superpave mix design method in accordance with all applicable Ontario Provincial Standard Specifications or Publications. All mix designs were proposed by the contractor; Coco Paving Inc. and then reviewed and approved by the Ministry of Transportation Ontario, Materials Engineering and Research Office (MERO). A 2.0-inch (50 mm) WMA or HMA overlay was applied to an existing average 6.3-inch (159 mm) of asphalt concrete. Chapter 3: Construction Details, of this report provides information on the structural design used for this project.

## Report Organization

The report chapters, appendices and their respective contents are organized as follows:

Chapter 2 presents the project location, description, and other attributes of the project.

Chapter 3 describes the materials and construction procedures and detailed construction sequence and operations.

Chapter 4 provides a summary of the test section construction.

Chapter 5 contains documentation of the key construction observations.

Appendix A contains a collection of construction photographs from the project.

Appendix B contains the mix designs for each test section.

Appendix C contains the materials sampling and testing layouts.

Appendix D contains construction documents including construction plans, specifications, and special provisions of the project; strip charts during production; daily logs and field notes of activities, equipment, and weather.

Appendix E contains the LTPP SPS-10 Construction Forms.

Appendix F contains the Deviation Report.

# Chapter 2: PROJECT DESCRIPTION

This chapter presents the project location, description and other physical attributes associated with the Ontario SPS-10 project.

## Test Section Layout

This section of the report provides a description of the Ontario SPS-10 project in terms of the location of the test sections along Provincial Highway 48. Table 1 lists each section and its respective description. Table 2 tracks the test sections according to their corresponding station numbers.  This table indicates transition areas between consecutive sections, as well as the buffer, sampling and monitoring areas for each section. Additionally, Figure 1 provides a visual representation of the overall project layout. Sufficient transition area is provided between consecutive sections to ensure steady-state operation of each asphalt mix.

Table 1: Test Section Identification and Description –87AA00

| SHRP ID | Description |
| --- | --- |
| 87AA01 | Control Section 2” Superpave 12.5 FC2 (PG 58-28) Hot Mix Asphalt 15% RAP |
| 87AA02 | WMA Core Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Foaming Process Water Dosage: 2.0% of Virgin Asphalt Cement 15% RAP |
| 87AA03 | WMA Core Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Chemical 1 – Evotherm® M1 Additive Dosage: 0.3% of Virgin Asphalt Cement 15% RAP |
| 87AA61 | WMA Supplemental Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Chemical 2 – WarmGrip® E5 Additive Dosage: 0.5% of Virgin Asphalt Cement 15% RAP |
| 87AA62 | WMA Supplemental Section 2” Superpave 12.5 FC2 (PG 58-28) Warm Mix Asphalt: Organic – Rediset® WMX 8017 Additive Dosage: 1.5% of Virgin Asphalt Cement 15% RAP |

Table 2: Test Section Layout –87AA00

| Project Begin STA | Project End STA | Experiment Begin STA feet (meter) | Experiment End STA feet (meter) | Description | Section ID |
| --- | --- | --- | --- | --- | --- |
| 18+250 | 19+002 |  |  | START | East Gwillimbury |
| 19+002 | 19+037.05 | 0-165 (0-50.3) | 0-50 (0-15.25) | Sampling Area | 87AA01 |
| 19+037.05 | 19+052.30 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 19+052.30 | 19+204.62 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 19+204.62 | 19+219.87 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 19+219.87 | 19+254 | 5+50 (1+67.25) | 5+162(2+01.38) | Sampling Area |  |
| 19+254 | 21+030 |  |  | Transition |  |
| 21+030 | 21+066.33 | 0-159(0-48.58) | 0-50 (0-15.25) | Sampling Area | 87AA02 |
| 21+066.33 | 21+078.58 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 21+078.58 | 21+231.06 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 21+231.06 | 21+246.31 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 21+246.31 | 21+280 | 5+50 (1+67.25) | 5+161(2+00.94) | Sampling Area |  |
| 21+280 | 23+000 |  |  | Transition |  |
| 23+000 | 23+031.53 | 0-154(0-46.78) | 0-50 (0-15.25) | Sampling Area | 87AA03 |
| 23+031.53 | 23+046.78 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 23+046.78 | 23+199.55 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 23+199.55 | 23+214.8 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 23+214.8 | 23+250 | 5+50 (1+67.25) | 5+166(2+02.45) | Sampling Area |  |
| 23+250 | 11+280 |  |  | Transition (24+616=10+000) | Georgina |
| 11+280 | 11+334.38 | 0-228(0-69.63) | 0-50 (0-15.25) | Sampling Area | 87AA61 |
| 11+334.38 | 11+349.63 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 11+349.63 | 11+501.82 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 11+501.82 | 11+517.07 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 11+517.07 | 11+550 | 5+50 (1+67.25) | 5+158(2+00.18) | Sampling Area |  |
| 11+550 | 12+750 |  |  | Transition |  |
| 12+750 | 12+806.29 | 0-235(0-71.54) | 0-50 (0-15.25) | Sampling Area | 87AA62 |
| 12+806.29 | 12+821.54 | 0-50 (0-15.25) | 0+00 (0+00) | Buffer Area |  |
| 12+821.54 | 12+973.84 | 0+00 (0+00) | 5+00 (1+52) | Monitoring Area |  |
| 12+973.84 | 12+989.09 | 5+00 (1+52) | 5+50 (1+67.25) | Buffer Area |  |
| 12+989.09 | 13+020 | 5+50 (1+67.25) | 5+151(1+98.16) | Sampling Area |  |
| 13+020 | 13+830 |  |  | END |  |

Sampling Area 011 – 110ft (34.0m)

Buffer Area – 50ft (15.25m)

87AA01

HMA Control Section
Superpave 12.5 FC2

(PG 58-28)

500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 021 – 110ft (34.0m)

Transition (1.776km)

Sampling Area 031 – 111ft (34.5m)

Buffer Area – 50ft (15.25m)

87AA02

WMA Foaming Process

Superpave 12.5 FC2

(PG 58-28)
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 041 – 109ft (33.5m)

Transition (1.720km)

Buffer Area – 50ft (15.25m)

87AA03

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
Evotherm® M1
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 061 – 110ft (34.0m)

Sampling Area 051 – 110ft (34.0m)

827ft (252m)

820ft (250m)

820ft (250m)

NB Traffic

19+254

21+030

19+002

21+280

23+000

23+250

19+052.306

19+204.620

21+078.580

21+231.060

23+046.780

23+199.550

Sampling Area 071 – 131ft (40.6m)

Buffer Area – 50ft (15.25m)

87AA61

WMA Chemical Additive
Superpave 12.5 FC2
(PG 58-28)
WarmGrip® E5
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 081 – 122ft (37.4m)

Transition (1.200km)

Sampling Area 091 – 117ft (36.0m)

Buffer Area – 50ft (15.25m)

87AA62

WMA Organic Additive
Superpave 12.5 FC2
(PG 58-28)
Rediset® WMX 8017
500ft (152.4m)

Buffer Area – 50ft (15.25m)

Sampling Area 101 – 136ft (42.0m)

886ft (270m)

886ft (270m)

NB Traffic

11+280

11+550

12+750

13+020

11+349.630

11+501.820

12+821.540

12+973.840

24+616=10+000

Transition (2.646km)

Figure 1: Ontario SPS-10 87AA00 – Project Layout

1. Odd sampling areas used for t0, t2, t4, t6, t8, t10; even sampling areas used for t1, t3, t5, t7, t9

Note: St. 24+616 = St. 10+000

## Physical Attributes

As previously mentioned, the Ontario SPS-10 project 87AA00 is located on Provincial Highway 48 in York Region – Greater Toronto Area, Ontario as shown in Figure 2 below. The test sections are located approximately 17.4 miles (28 km) northeast of Newmarket, Ontario. Highway 48, also known as King’s Highway 48, is a two-lane undivided highway.

N

Original Photo: © 2017 Google® (see acknowledgments section)

Figure 2: Ontario SPS-10 87AA00 – Location Overview

The five test sections are located on the northbound lane of Highway 48, between Ontario Highway 79 and Ontario Highway 13. Figure 3 shows the layout of the test sections on Highway 48. Highway 48 is classified as rural principal arterial two-lane undivided highway, with a speed limit of 50mph (80 km/h) within the project limits.

N

Original Photo: © 2017 Google® (see acknowledgments section)

Figure 3: Detailed Layout of SPS-10 87AA00 Test Sections in Ontario

History

Highway 48 was first constructed in the late 1930’s, and links the town of Markham to Highway 12 near Beaverton. Over the years, Highway 48 extended in length from its original length of 6 miles (10 Km) in 1937, to a total length of 80 miles (129 km) in the late 1990’s. In 1998, the northern section of Highway 48 was one of the causalities of mass highway downloading in Ontario, resulting in a section of the highway being transferred to the Regional Municipality of Durham and the City of Kawartha Lakes. Currently, the length of Highway 48 is approximately 41.2 miles (66 km).

Highway 48 was originally surfaced with gravel, and later paved in its entirety in the mid 1950’s. The existing surface of Highway 48 was opened to traffic in 2016, following a rehabilitation project, with estimated cost of $16.99 Million. The project was completed between July to September 2016, and included the resurfacing of approximately 70% of the highway (i.e. 46.5 km), stretching from North of Regional Road 9 to South Junction of Highway12/48 (Beaverton By-pass). The project also included: joint replacement, concrete patching, culvert replacement as well as repair of all safety improvements.

Experiment

The SPS-10 test sections in Ontario were constructed on June 13th through June 24th, 2017 using a Superpave mix design specified in Chapter 3: CONSTRUCTION DETAILS under Materials sub-section. Field testing identified the pre-overlay pavement structure included an average of 6.3 inch of hot-mix asphalt concrete, 11.2 inch of unbounded granular base, 7.9 inch of Type B AC base, and 8.7 inch of granular subbase above the natural subgrade consisting of sandy silt soil with gravel.

The traffic lanes are 12 ft (3.7 m) wide, with a 10.0 ft (3.05 m) wide granular surface outer shoulder. The paved width of the outside shoulder is 1ft-wide. For this experiment, the shoulders were filled using Granular Type “A”. Prior to the overlay, the existing HMA layer was milled to a thickness of 1.5 inch.

The existing and post-construction pavement structures are shown in Figure 4. Table 3 details the layer properties before and after overlay.

Pre-Overlay				 	     Post-Overlay

(a)

(b)

Figure 4: Pavement Cross Section a) pre-overlay b) post-overlay

Table 3: Layer Properties

| Pre-overlay |  |  | Post-overlay (06/2017) |  | Layer |
| --- | --- | --- | --- | --- | --- |
|  |  |  | 2" | SP 12.5 FC2 Surface Course (PG 58-28) | 1 |
|  |  |  | 2" | SP 12.5 FC2 Binder Course (PG 58-28) | 4 |
| 6.3" | HMA |  | 1.5" | Mill Depth | 3 |
|  |  |  | 4.8" | HMA |  |
| 11.2" | Granular Base |  | 11.2" | Granular Base | 5 |
| 7.9" | Type B AC Base |  | 7.9" |  | 5 |
|  |  |  |  | Type B AC Base |  |
| 8.7" | Granular Subbase |  | 8.7" | Granular Subbase | 6 |
|  | Subgrade |  |  | Subgrade | 7 |

Pavement Condition

Prior to the project construction in June 2017 test section 87AA01 exhibited the following distresses: low severity fatigue cracking (37.5 m2), moderate severity fatigue cracking (14.4 m2), low severity unsealed transverse cracking (124.6 m), moderate severity unsealed transverse cracking (14.5 m) and high severity unsealed transverse cracking (3.7 m). Section 87AA01 also exhibited low severity non-wheel path unsealed longitudinal cracking (8.6 m), moderate severity non-wheel path unsealed longitudinal cracking (111.2 m), and raveling (4.2 m2).

Prior to the project construction in June 2017 test section 87AA02 exhibited the following distresses: low severity fatigue cracking (39.9 m2), moderate severity fatigue cracking (59.1 m2), low severity edge cracking (45.8 m), moderate severity edge cracking (106.8 m), low severity unsealed transverse cracking (114.4 m), and moderate severity unsealed transverse cracking (22.1 m).  Section 87AA02 also exhibited low severity non-wheel path unsealed longitudinal cracking (24 m), and moderate severity non-wheel path unsealed longitudinal cracking (87.8 m).

Prior to the project construction in June 2017, test section 87AA03 exhibited the following distresses: low severity fatigue cracking (191.7 m2), moderate severity fatigue cracking (38.4 m2), low severity edge cracking (10 m), and low severity unsealed transverse cracking (11.6 m). Section 87AA03 also exhibited non-wheel path unsealed longitudinal cracking of low severity (15 m), moderate severity (14.3 m), and high severity (174 m), as well as low severity patch deterioration (6.1 m2), and raveling (289.8 m2).

Prior to the project construction in June 2017 test section 87AA61 exhibited the following distresses: low severity fatigue cracking (37.7 m2), moderate severity fatigue cracking (81.9 m2), high severity fatigue cracking (2.8 m2), low severity edge cracking (24.3 m), moderate severity edge cracking (30.5 m), low severity unsealed transverse cracking (116.4 m), moderate severity unsealed transverse cracking (28.4 m), and high severity unsealed transverse cracking (1.6 m). Section 87AA61 also exhibited non-wheel path unsealed longitudinal cracking of low severity (42.5 m), moderate severity (8 m), and high severity (74.7 m), as well as raveling (502 m2).

Prior to the project construction in June 2017 test section 87AA62 exhibited the following distresses: low severity fatigue cracking (123.2 m2), low severity edge cracking (25.8 m), low severity unsealed transverse cracking (71.4 m), and moderate severity unsealed transverse cracking (54.8 m).

Following the overlay construction, all test sections exhibited zero distress. Figure 5 to Figure 9 illustrate the pre-and post-overlay condition of the test sections.

(a) Pre-Overlay					(b) Post-Overlay

Figure 5: Site Overview of 87AA01

(a) Pre-Overlay					(b) Post-Overlay

Figure 6: Site Overview of 87AA02

(a) Pre-Overlay					(b) Post-Overlay

Figure 7:  Site Overview of 87AA03

(a) Pre-Overlay					(b) Post-Overlay

Figure 8:  Site Overview of 87AA61

(a) Pre-Overlay					(b) Post-Overlay

Figure 9: Site Overview of 87AA62

Longitudinal Profile

Roughness data was collected using an Ames Engineering 8300 Survey Pro High Speed Profiler (LTPP unit 830112). This specialized vehicle is equipped with accelerometers that measure the vertical acceleration of the vehicle as it bounces in response to the pavement surface profile and laser height sensors that measure the distance between the vehicle and the pavement surface each mounted to the front bumper. The vehicle measures the longitudinal profile of the pavement surface at 30-meter intervals, in the inside and outside wheel path, in terms of the International Roughness Index (IRI). The pre-overlay and post-overlay average International Roughness Index (IRI) for each test section is listed in Table 4 and Table 5.

Table 4: Average IRI for each Test Section Pre-Overlay

| State Code | SHRP ID | Test Date (MM/DD/YYYY) | Avg. Air Temp. | Avg. IRI (m/km) | Avg. Left Wheelpath IRI (m/km) | Avg. Right Wheelpath IRI (m/km) |
| --- | --- | --- | --- | --- | --- | --- |
| 87 | AA01 | 05/10/2017 | 12 | 1.02 | 1.024 | 1.016 |
| 87 | AA02 | 05/10/2017 | 12 | 1.00 | 1.295 | 0.714 |
| 87 | AA03 | 05/10/2017 | 11 | 1.02 | 1.149 | 0.890 |
| 87 | AA61 | 05/10/2017 | 13 | 0.85 | 1.118 | 0.587 |
| 87 | AA62 | 05/10/2017 | 12 | 0.72 | 0.765 | 0.679 |

Table 5: Average IRI for each Test Section Post-Overlay

| State Code | SHRP ID | Test Date (MM/DD/YYYY) | Avg. Air Temp. | Avg. IRI (m/km) | Avg. Left Wheelpath IRI (m/km) | Avg. Right Wheelpath IRI (m/km) |
| --- | --- | --- | --- | --- | --- | --- |
| 87 | AA01 |  |  |  |  |  |
| 87 | AA02 |  |  |  |  |  |
| 87 | AA03 |  |  |  |  |  |
| 87 | AA61 |  |  |  |  |  |
| 87 | AA62 |  |  |  |  |  |

Texture

Pavement surface texture data was collected simultaneously with longitudinal profile data. The Ames Engineering 8300 Survey Pro High Speed Profiler is capable of determining macrotexture depth at highway speeds. Macrotexture is the primary component of high-speed, wet skid resistance. The mean profile depth (MPD) represents the surface texture of pavements. The calculation of MPD from a profile of pavement macrotexture is derived from ASTM E1845-Standard Practice for Calculating Pavement Macrotexture Mean Profile Depth. The pre-overlay and post-overlay Average Texture Mean Profile Depth for each test section is shown in Table 6 and Table 7 below.

Table 6: Average Texture Mean Profile Depth (MPD) for each Test Section Pre-overlay

| Section | Texture MPD Section Average (mm) | Survey Date |
| --- | --- | --- |
| 87AA01 | 0.96 | 05/10/2017 |
| 87AA02 | 1.13 | 05/10/2017 |
| 87AA03 | 1.66 | 05/10/2017 |
| 87AA61 | 1.15 | 05/10/2017 |
| 87AA62 | 0.95 | 05/10/2017 |

Table 7: Average Texture Mean Profile Depth (MPD) for each Test Section Post-overlay

| Section | Texture MPD Section Average (mm) | Date |
| --- | --- | --- |
| 87AA01 |  |  |
| 87AA02 |  |  |
| 87AA03 |  |  |
| 87AA61 |  |  |
| 87AA62 |  |  |

Deflection

A Dynatest Falling Weight Deflectometer (FWD), model 8002 LTPP unit 129 and LTPP unit 058, was used to perform deflection testing before and after the overlay installment, respectively. The AASHTO 1993 analysis procedure and ELMOD 6.0® were used for the FWD back-calculation analysis. ELMOD created by Dynatest, analyzes the pavement response from the FWD by determining the modulus, stress and strain of each significant layer. The software considers the use of calculated and allowable forces at critical points within the pavement structure, loading, stress and strain relationships, and pavement distress. The deflections are recorded from nine sensors, each located at varying distances from the load cell. However, for back-calculated parameters, only data from eight sensors are used. The data from the sensor in front of the load plate (D9) was excluded for processing purposes.

The deflections recorded from each sensor, located at varying distances from the load cell as noted in the legend, are shown. In order to yield comparable results, the deflection data from these surveys was normalized to 8.99-kip (40 kN) load under a load plate of 5.9-inch (150 mm) radius, producing a pressure of 81.9 lb/in2 (565 kPa). Figure 10 and Figure 11 show the results from all sensors for each test section.

Figure 10: Pre-Overlay Normalized Deflection for Sections 83AA01, 83AA02, 83AA03, 83AA61, and 83AA62

Figure 11:  Post-Overlay Normalized Deflection Sections 83AA01, 83AA02, 83AA03, 83AA61, and 83AA62

## Project Geometry

Test sections 87AA01 through 87AA62 are located on the northbound lane of Provincial Highway 48. The five test sections are all contained within a 5.1-mile (8.2 km) segment of the roadway.

Shoulder Information

The outer shoulder is 10.0 ft (3.05 m) wide, and is composed of a granular surface type. The paved width of the outside shoulder is 1ft-wide. The surface and base thickness of the shoulder are 3.5 and 6.0 inches, respectively.

Median Information

There is no median separating the north and southbound traffic.

## Climate

Climate data for the project is collected from two weather stations: Udora weather station and Uxbridge West weather station. These stations are located at Global Positioning System (GPS) coordinates 44°15’00” N, 79°10’58” W and 44°05’54” N, 79°09’49” W, respectively. Udora station is located approximately 11.7 miles (18.9 km) east of project site 87AA00. Uxbridge West station is located approximately 13.8 miles (22.2 km) south-east of project site 87AA00.

Table 8 shows the average daily high air temperature, average daily low air temperature, mean daily air temperature, average rainfall and average snowfall year-round from 1989-2006 from Udora weather station. Table 9 and Table 10 show the hourly air temperature and the daily rainfall measured at Uxbridge West station for the duration of construction, initial sampling and secondary testing from June 13th to 24th, 2017. The monthly freeze index measured at Udora station between 1989 and 2017 is shown in Table 11. The Average Annual Freeze Index for is estimated to be 163.6°F•days. As per LTPP definitions, the project is in a Wet, Freeze climatic zone.

Table 8: Average Weather Data at Udora Weather Station, ON from 1989-2006

| Data Type | Jan | Feb | Mar | Apr | May | Jun | Jul | Aug | Sep | Oct | Nov | Dec |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Average daily high air temperature, °F (°C) | 26.5 (-3.1) | 28.9 (-1.7) | 38.2 (3.4) | 52.2 (11.2) | 64.7 (18.2) | 75.0 (23.9) | 78.1 (25.6) | 77.1 (25.1) | 69.2 (20.7) | 56.1 (13.4) | 43.2 (6.2) | 31.6 (-0.2) |
| Average daily low air temperature °F (°C) | 10.9 (-11.7) | 11.7 (-11.3) | 20.6 (-6.3) | 32.4 (0.2) | 43.1 (6.2) | 53.6 (12.0) | 57.1 (13.9) | 55.6 (13.1) | 48.7 (9.3) | 38.9 (3.8) | 29.5 (-1.4) | 18.0 (-7.8) |
| Mean daily air temperature °F (°C) | 18.7 (-7.4) | 20.3 (-6.5) | 29.4 (-1.4) | 42.3 (5.7) | 53.9 (12.2) | 64.3 (17.9) | 67.6 (19.8) | 66.4 (19.1) | 58.9 (15.0) | 47.5 (8.6) | 36.3 (2.4) | 24.8 (-4.0) |
| Average rain fall, inch (mm) | 1.0 (25.7) | 0.7 (18.3) | 1.1 (27.2) | 2.3 (58.9) | 3.2 (82.1) | 4.2 (106.6) | 3.4 (86.4) | 2.9 (73.9) | 3.4 (87.3) | 2.9 (72.9) | 2.6 (64.8) | 1.0 (24.6) |
| Average snow fall, inch (mm) | 15.5 (39.3) | 10.9 (27.7) | 10.2 (25.8) | 3.6 (9.1) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.0 (0.0) | 0.8 (2.0) | 7.2 (18.4) | 13.9 (35.4) |

Table 9: Hourly Air Temperature Data at Uxbridge West Weather Station, ON from June 13th to June 24th, 2017

| Data Type | 5:00 PM | 6:00 PM | 7:00 PM | 8:00 PM | 9:00 PM | 10:00 PM | 11:00 PM | 12:00 AM | 1:00 AM | 2:00 AM | 3:00 AM | 4:00 AM | 5:00 AM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Hourly air temperature 06/13/2017, °F (°C) | 70.9 (21.6) | 71.8 (22.1) | 71.4 (21.9) | 67.3 (19.6) | 63.0 (17.2) | 60.3 (15.7) | 59.7 (15.4) | 57.4 (14.1) | 56.1 (13.4) | 55.4 (13.0) | 57.4 (14.1) | 55.0 (12.8) | 56.5 (13.6) |
| Hourly air temperature 06/14/2017, °F (°C) | 72.9 (22.7) | 70.5 (21.4) | 67.1 (19.5) | 62.4 (16.9) | 59.2 (15.1) | 57.7 (14.3) | 59.2 (15.1) | 59.5 (15.3) | 58.5 (14.7) | 56.8 (13.8) | 57.7 (14.3) | 58.1 (14.5) | 58.1 (14.5) |
| Hourly air temperature 06/21/2017, °F (°C) | 69.1 (20.6) | 69.1 (20.6) | 66.2 (19.0) | 66.6 (17.0) | 57.6 (14.2) | 55.2 (12.9) | 53.1 (11.7) | 52.3 (11.3) | 51.3 (10.7) | 49.8(9.9) | 48.7 (9.3) | 47.8 (8.8) | 48.2 (9.0) |
| Hourly air temperature 06/23/2017, °F (°C) | 73.6 (23.1) | 69.3 (20.7) | 67.6 (19.8) | 66.7 (19.3) | 65.5 (18.6) | 64.8 (18.2) | 62.8 (17.1) | 59.5 (15.3) | 59.7 (15.4) | 58.8(14.9) | 58.6 (14.8) | 58.3 (14.6) | 57.4 (14.1) |
| Hourly air temperature 06/24/2017, °F (°C) | 69.4 (20.8) | 68.5 (20.3) | 66.6 (19.2) | 61.7 (16.5) | 57.2 (14.0) | 55.8 (13.2) | 54.3 (12.4) | 54.1 (12.3) | 52.3 (11.3) | 54.7 (12.6) | 54.7 (12.6) | 53.8 (12.1) | 55.4 (13.0) |

Table 10: Daily Rainfall Data at Uxbridge West Weather Station, ON from June 13th to June 24th, 2017

| Date | Daily Rainfall inch (mm) |
| --- | --- |
| 06/13/2017 | 0.00 (0.0) |
| 06/14/2017 | 0.00 (0.0) |
| 06/212017 | 0.00 (0.0) |
| 06/23/2017 | 0.00 (0.0) |
| 06/24/2017 | 0.00 (0.0) |

Table 11: Monthly Freeze Index (Degree F • Days) - Weather Data at Udora Weather Station, ON from 1989-2017

| Date |  | Average Monthly Freeze Index (degree days) |
| --- | --- | --- |
| Years | Month | °F |
| 1989-2017 | Jan. | 414.6 |
|  | Feb | 410.5 |
|  | Mar. | 370.4 |
|  | Apr. | 73.3 |
|  | May | Non-Freezing (Thaw) Period |
|  | Jun. |  |
|  | Jul. |  |
|  | Aug. |  |
|  | Sept. |  |
|  | Oct. | 11.9 |
|  | Nov. | 230.2 |
|  | Dec. | 452.8 |

## Traffic

Traffic estimates provided by MTO as part of the site nomination process indicate an Average Annual Daily Traffic (AADT) of 5000 in the project lane. Twelve percent (12%) of this traffic is projected to be heavy trucks and combinations. Annual Equivalent Single Axle Loads (ESALs) during the first year of the fifteen-year design period are estimated at 220,000 ESALs. The existing HMA pavement surface was opened to traffic in 2016. Provincial Highway 48 is classified as a rural principal arterial two-lane undivided highway with a speed limit of 50mph (80 km/h) within the project limits.

## Supplemental Test Sections

In addition to the three SPS-10 experiment core sections, highway agencies may construct supplemental test sections on an SPS-10 site to investigate other factors of interest to the agency. Ministry of Transportation of Ontario (MTO) executed the construction of two supplemental test sections in the SPS-10 experiment located along the northbound lane of Highway 48. All 2 supplemental test sections utilized PG 58-28 with the same amounts of RAP and variable additives, one with chemical and another section with organic additive. Mix designs for all five test sections are detailed in Chapter 3, Materials sub-section.

## Project Personnel

The key project personnel are listed below:

Ministry of Transportation Ontario (MTO) – Construction and Materials:

- Construction and materials Liaison Engineer:

- Field Materials Engineer:

- Field Materials Engineer:

- Senior Research and Development Assistant:

Coco Paving Inc. (Construction Contractor):

- General Manager:

- Plant Manager:

- Paving Foreman:

- Construction Superintendent:

Materials Reference Library (MRL):

- Project Manager:

Central Laboratory Testing Center (CLTC):

- Project Manager:

Turner Fairbanks Highway Research Center (TFHRC):

- Project Manager:

Stantec Consulting Inc. (LTPP Regional Support Contractor):

- Project Manager: Gabe Cimini

- Project Coordinator: Carlos Leal

- Pre-Overlay Monitoring: Alfred Lip,

- Construction Documentation: Carlos Leal

- Material Sampling: Tony Wagner,

- Coring Coordination: Alfred Lip

- Post-Overlay Monitoring: Alfred Lip,

- Supporting Team:

## Project timeline

A pre-overlay meeting took place on-site on June 13th, 2017. The initial site visit activities completed on May 8-11, 2017 comprised of, laying out the test sections, and collecting pre-overlay performance measurements. The performance measurements collected included, Manual Distress Survey’s (MDS), Falling Weight Deflectometer (FWD) measurements, transverse and profile measurements, and surface texture measurements for each individual test section. Pre-overlay longitudinal profile measurements were completed on May 10th, 2017. The elevation surveys were also conducted for each section prior to overlay. Three rounds of elevation surveys were performed: initial (pre-construction), post-milling, and post-HMA binder course application. The construction phase and the raw materials sampling of the project took place June 13th through June 24th, 2017. The post overlay testing and sampling took place on June 13th through 14th, 2017 and June 21st through 24th, 2017. Post construction testing comprised of identification of layout and paint application as well as collecting post-overlay performance measurement.

The performance measurements collected include, MDS, FWD, transverse profile measurements, surface texture measurements and elevation surveys. Nuclear Density Gage testing took place on June 13-14th, 2017 for test sections 87AA01, and 87AA03, June 21-24, 2017 for test sections 87AA02, 87AA61, and 87AA62. Filling of shoulders with Gran A took place on October 7th, 2016 through October 10th, 2016. Sample labeling and packaging for shipment took place on June 27 - 30, 2017. Paint Striping of all test section was completed for all sections immediately after construction. Sampling of virgin chemical additives (Evotherm®, Warm Grip® E5) was not possible on site, as binders were terminally blended with the additives. Samples of these two chemicals blended with binders were shipped to location on date. Post-overlay longitudinal profile measurements were completed on June 25th, 2017. The project timeline is shown in Table 12.

Table 12: Project Timeline

| Date | Task Performed | Personnel |
| --- | --- | --- |
| May 8-11, 2017 | Pre-Overlay Monitoring: FWD, MDS, Transverse Profile, Longitudinal Profile, and Surface Texture | Tony Wager/ Doug Marshall/ Chris Olmedo |
| May 17 -June 6, 2017 | Elevation surveys: (pre-construction, post-milling and post-binder course) | Doug Marshall/ Tony Wagner/???? |
| June 13, 2017 | Pre-Overlay Meeting | Gabe Cimini / Carlos Leal / MTO staff / Coco Paving Inc. staff |
| June 13-14, 2017 | Paving completed on test sections AA01 and AA03. Temperatures were monitored and recorded during production in the asphalt plant, delivery temperatures on site and asphalt laydown temperatures. Sampling of uncompacted asphalt concrete was performed on site. Nuclear Gauge Density measurements were collected before and after the overlay. Paint striping complete by Coco Paving immediately following construction. | Coco Paving, Inc. staff On site staff: Alfred Lip / Carlos Leal / Cassandra Lewis / Gabe Cimini / Brant Henderson/Ahmed Haggag /Marty Dos Santos/ Brayden LeBrun/ Sali Abdulnour / Giannin Viecili Staff at Asphalt Plant: Tony Wagner / Christopher Lewis |
| June 13, 2017 | Sampled RAP, AC Binder and chemical additive Evotherm®. | Coco Paving, Inc. staff Staff at Asphalt Plant: Tony Wagner / Christopher Lewis |
| June 13-14, 2017 | Sampled combined aggregate AA01 and AA03. | Tony Wagner / Christopher Lewis |
| June 14, 2017 | Sampled asphalt cement (binder) and chemical additive Warm Grip® E5. | Tony Wagner / Christopher Lewis |
| June 14, 2017 | Sampled asphalt cement (binder) and organic additive Rediset® WMX 8017 | Tony Wagner / Christopher Lewis |
| June 21-24, 2017 | Paving completed on test sections AA02, AA61, and AA62. Temperatures were monitored and recorded during production in the asphalt plant, delivery temperatures on site and asphalt laydown temperatures. Sampling of uncompacted asphalt concrete was performed on site. Nuclear Gauge Density measurements were collected before and after the overlay. | Coco Paving, Inc. staff On site staff: Alfred Lip / Carlos Leal / Cassandra Lewis / Gabe Cimini / Brant Henderson/Ahmed Haggag /Marty Dos Santos/ Brayden LeBrun/Sali Abdulnour / Giannin Viecili Staff at Asphalt Plant: Tony Wagner / Christopher Lewis |
|  | Coring and post-overlay monitoring including MDS, FWD and elevation survey performed. | Coco Paving staff / Alfred Lip / Tony Wagner / ???? |
|  | Shoulder filling with Granular “A” material | Contractor: Coco Paving Inc. |
| June 27 -30, 2017 | Sample labeling and packing for shipment - shipment | Brandt Henderson / Ahmed Haggag / Brayden LeBrun |
| June 25, 2017 | Post-Overlay longitudinal profiling measurement collection | Alfred Lip / Doug Marshall |

# Chapter 3: CONSTRUCTION DETAILS

This chapter describes the materials and detailed construction procedures associated with the LTPP SPS-10 project 87AA00 in Ontario.

## Materials

Prior to overlay the road surface was prepped using tack coat, type SS-1, with a residual AC of 30% and applied to the surface at a rate of 0.35kg/m2. The construction contractor Coco Paving Inc. produced, constructed, and compacted the asphalt concrete used in the project. The mixes were designed and developed by the contractor and approved by the Ministry of Transportation Ontario, Materials Engineering and Research Office (MERO).

A Superpave Mix Design (SP 12.5FC 2) was used in accordance with all applicable specification requirements of MTO for all test sections. SP 12.5FC 2 is a Superpave 12.5 mm (1/2 inch) nominal max aggregate size surface course mix with skid resistance (FC stands for Friction Course). Appendix B contains the original mix designs. The design mixing temperature for hot mix and warm mix were 293°F (145°C) and 266°F (130°C), respectively. The shoulders were filled using Granular Base Course, Type “A” material.

The four WMA sections were constructed using foaming technology, two types of chemical additives, and an organic additive. Chemical Additives are defined as water-free (non-aqueous) chemistry packages that modify the binder properties to enhance coating, adhesion, and workability at reduced temperatures.  These include surfactants, fatty-acid chemical additives, cationic surface-active agents, and rheology modifiers. Organic Additives on the other hand, are plant-based, wax-based, or sulfur-extended materials designed to provide viscosity reduction, aid in asphaltenes dispersion, and act as a lubricant at mixing temperatures below that of conventional HMA.

The chemical additives used were Evotherm® M1and Warm Grip® E5. The organic additive used was Rediset® WMX 8017. Although Rediset WMX is a combination of organic and chemical additives, it is intended to modify the rheological properties of the binder, thus is classified as a chemical additive. The Rediset® WMX 8017 additive is in pellet form (add a photo). It is added into hot liquid asphalt cement at a temperature that is above the melting point of the additive. The tank is equipped with a mixer and the melted Rediset is mixed into the asphalt cement.  It is added in a solid state and it melts in the asphalt cement. The blend is mixed via a mixer on the tank. The additive is miscible and remains mixed into the asphalt cement.

The chemical additive Evotherm® M1 was obtained from MeadWestvaco Corporation Asphalt Innovations, North Charleston, SC. WarmGrip® E5 was obtained from Arrmaz Chemicals in Tulsa, OK. The organic additive Rediset® WMX 8017 was obtained from Akzo Nobel Surface Chemistry LLC, Chicago, IL.

The WMA foaming process test section (87AA02) was constructed using Gencor Ultrafoam GX2™ foaming technology. Water is introduced to the AC in-line at the drum to achieve the desired foaming effect as per manufactures’ specification.

The aggregates were obtained from the Fowler Rosewarne Quarry (B17-013). Hydrated lime is added to course and fine aggregate, at a 1% dosage. The lime supplied by Beachville, was added in slurry form. RAP material with 15% AC was obtained from the milling completed on Highway 48. The asphalt cement binder PG 58-28 was supplied from Coco’s Millhaven Terminal Plant in Bath, ON. The AC binder and additives composition is shown in Table 13. The AC matrix and aggregate composition is shown in Table 14. Table 15 shows the composition of the AC mix by weight.

Table 13: Ontario SPS-10 Asphalt Concrete Binder and Additives

| Test Section | Mix Type | Binder | % of Binder Replacement by RAP | % of Binder Replacement by RAS | Additives |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Evotherm® M1 | WarmGrip® E5 | Rediset® WMX 8017 | Water |
| 87AA01 | HMA | PG 58-28 | 15 | 0 | 0 | 0 | 0 | 0 |
| 87AA02 | WMA | PG 58-28 | 15 | 0 | 0 | 0 | 0 | 2%/AC |
| 87AA03 | WMA | PG 58-28 | 15 | 0 | 0.3%/AC | 0 | 0 | 0 |
| 87AA61 | WMA | PG 58-28 | 15 | 0 | 0 | 0.5%/AC | 0 | 0 |
| 87AA62 | WMA | PG 58-28 | 15 | 0 | 0 | 0 | 1.5%/AC | 0 |

Table 14: Ontario SPS-10 Asphalt Concrete Matrix and Aggregate Composition

| Test Section | Matrix |  |  | Grain |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | % Voids in Mineral Aggregate (VMA) | % Voids Filled with Asphalt Binder (VFA) | % Voids | % CA#1 Course Aggregates | % FA#1 Fine Aggregates | % RAP | % RAS |
| 87AA01 | 14.7 | 72.8 | 4.0 | 37.0 | 48.0 | 15.0 | 0 |
| 87AA02 | 14.7 | 72.9 | 4.0 | 37.0 | 48.0 | 15.0 | 0 |
| 87AA03 | 14.7 | 72.6 | 4.0 | 37.0 | 48.0 | 15.0 | 0 |
| 87AA61 | 14.8 | 72.8 | 4.0 | 37.0 | 48.0 | 15.0 | 0 |
| 87AA62 | 14.7 | 72.8 | 4.0 | 37.0 | 48.0 | 15.0 | 0 |

Table 15: Ontario SPS-10 Asphalt Concrete Mixture

| Test Section | % AC | % Solid Dry Aggregate |
| --- | --- | --- |
| 87AA01 | 5.0 | 95.0 |
| 87AA02 | 5.0 | 95.0 |
| 87AA03 | 5.0 | 95.0 |
| 87AA61 | 5.0 | 95.0 |
| 87AA62 | 5.0 | 95.0 |

## Equipment

At the Asphalt Plant a Sat-T-Log® handheld probe thermometer was used to measure the mixing and internal AC via truck temperatures in °F. The same device was used to record delivery temperatures on site, see Figure 21. The range of this thermometer is -148 to 2500°F (-100 to 1372°C) with a resolution of 0.1° when reading temperatures below 600°F (300°C) and an accuracy of ±0.7°F (0.4°C). A K Type Thermocouple probe was used with this device which is 24 inches (61.0 cm) long. Plant exhaust temperatures were measured by the contractor Coco Paving Inc. using computer equipment in the control office as the collection location was not accessible with manual devices. To measure AC surface temperature as the mix leaves the plant a Fluke® 62 Max + handheld infrared thermometer was used, see Figure 21. On-site laydown temperatures were also measured using this thermometer. This device can measure temperature in the range -22°F to 650°F (-30°C to 650°C) with a resolution of 0.1° and an accuracy of ±1°C or ±1.0% of reading, whichever is greater. To measure air temperature on site a Raytek® MiniTemp® MT6 infrared gun was used, see Figure 23. This device can measure in the range of -20°F to 932°F (-30°C to 500°C) with a resolution of 0.1° and an accuracy of ±2.7°F (±1.5°C). To measure the GPS coordinates of sampling locations an Etrex Garmin device (FHWA LTPP-NARO 000100) was used.

Figure 12: Sat-T-Log® Thermometer

Figure 13: Fluke® 62 Max + IR Thermometer

Figure 14: Raytek MiniTemp MT6 IR Thermometer

The asphalt concrete mix plant for this project was a drum mix plant operated by the contractor, Coco Paving Inc. The plant was located at 10475 Keele Street, Maple, ON L6A 1R7, on average 33.6 miles (54km) southwest of the test sections. The Global Positioning System (GPS) coordinates of the asphalt concrete mix plant are 43°51’51.18” N, -79°30’44.03’’W. Figure 24 shows the approximate location of the plant relative to the project 87AA00 site.

Coco Asphalt Mixing Plant

N

Original Photo: © 2017 Google® (see acknowledgments section)

Figure 15: Location of Asphalt Concrete Mix Plant

The plant is located approximately 31.2 miles (50.2km) from test section 87AA01 and 36.1 miles (58.1km) from test section 87AA62. The distances corresponded to an average haul time of 45 minutes, in regular traffic conditions.

The asphalt concrete mix plant used to construct project 87AA00 was a Drum Mix Plant with 9 1\2 Gencor style drum 400 tph with 135 mbto burner from Cedarapids Inc. It included:

Figure 16: Asphalt Mix Plant - Aggregate Stock Piles

Figure 17: Asphalt Mix Plant - RAP Stock Piles

Figure 18: Asphalt Mix Plant - Cold Feed Bins

Figure 19: Asphalt Mix Plant - Control Center

Figure 20: Asphalt Mix Plant - Conveyor Belt

Figure 21: Asphalt Mix Plant – Mixing Drum

Figure 22: Asphalt Mix Plant - Baghouse

Figure 23: Asphalt Mix Plant – Asphalt Cement Storage Tanks

Figure 24: Asphalt Mix Plant - Pugmill

Figure 25: Asphalt Mix Plant – Storage Silos

Figure 26: Asphalt Mix Plant - Truck Loading Area

The paving equipment used to construct project 87AA00 included:

- Bruell Sweeper - Model 741

- Etnyre Black-Topper Centennial – Tack Coat Application

- WEILER Hopper with Conveyor, Model SB-1542

- CAT Paver, Model AP1055F

- Break Down Roller - HAMM Articulated Tandem Roller, Model HD + 140, Operating Weight with Cab: 31989.1 lbs.

- Intermediate Roller - Caterpillar Pneumatic Roller, Model PS-300C, Operating Weight: 14000.0 lbs.

- Final Roller -. CAT Split Drum Tandem Vibratory Roller, Model CD54B, Operating Weight: 22311.0 lbs.

Figure 27: Bruell 741 Sweeper– Sweep Pavement Surface of Debris Pre-Overlay

Figure 28: Etnyre Black-Topper - Used to Apply Tack Coat to Surface

Figure 29: Typical End-Dump Truck – Used to transport AC from Plant to Hopper on Site

Figure 30: WEILER Hopper with Conveyor Model SB-1542 – Used to Buffer Between AC Truck and Paver to Ensure Paving Flow

Figure 31: CAT Paver, Model AP1055F

Figure 32: Break Down Roller - HAMM Articulated Tandem Roller, Model HD + 140, Operating Weight with Cab: 31989.1 lbs.

Figure 36: Intermediate Roller - Caterpillar Pneumatic Roller, Model PS-300C, Operating Weight: 14000.0 lbs.

Figure 37: Final Roller - CAT Split Drum Tandem Vibratory Roller, Model CD54B, Operating Weight: 22311.0 lbs.

## Construction Events

Test section 87AA01was constructed on June 13th, 2017. A Broce broom was used to sweep the road surface of debris prior to tac coat application. Tac coat application on test section 87AA01 was completed at approximately 7:30pm.

Test sections 87AA03 was constructed on June 14th, 2017. The Broce Broom swept the road surface prior to tack coat application. Tack coat application on test section 87AA03 was completed at approximately 7:15pm. The tack coat equipment malfunctioned at around 70ft, which led to the multiple application of tack Coat on the east side of the lane.

Test sections 87AA61 was constructed on June 21st, 2017. The Broce Broom swept the road surface prior to tack coat application. Tack coat application on test section 87AA61 was completed at approximately 7:44pm. The tack coat equipment sprayed only ¼ width of lane (edge closest to shoulder) starting at approximately 83ft up to 240 ft and sprayed the remaining ¾ width of lane over the same length.

Test sections 87AA62 was constructed on June 23rd, 2017. The Broce Broom swept the road surface prior to tack coat application. Tack coat application on test section 87AA62 was completed at approximately 9:52pm. The tack coat equipment sprayed only the right side of the section first due to a malfunction and sprayed the left side starting from around 250 ft to 400 ft.

Test sections 87AA02 was constructed on June 24th, 2017. The Broce Broom swept the road surface prior to tack coat application. Tack coat application on test section 87AA02 was completed at approximately 9:28pm. The tack coat was observed to drip on the pavement due to tack coat waiting.

Table 17 below, shows the as-built construction timeline of each test section, the average haul distance and time from the asphalt plant to the test site during construction and the location the trucks turned around to meet the hopper. Paving operations occurred at 14ft paving width ,giving a 12ft paved lane and 2ft of mainline mix on the shoulders. Shoulder filling with Granular Type “A” material occurred on June 07 through June 10, 2017 for all test sections. The lane striping was completed on Date and Date 1, 2017.

Table 16: Construction Timeline for Test Sections

| Section | Paving Start | Paving End | Paving Duration (minutes) | Average Haul Distance (miles) | Average Haul Time (minutes) | Turn Around Location |
| --- | --- | --- | --- | --- | --- | --- |
| 87AA01 | 20:19 | 20:34 | 15 | 7.7 | 14 | Route 52 |
| 87AA02 | 13:17 | 13:39 | 22 | 6.5 | 14 | Cave Drive |
| 87AA03 | 21:54 | 22:06 | 12 | 5.5 | 13 | Private Driveway |
| 87AA61 | 20:39 | 20:53 | 14 | 5.9 | 13 | Private Driveway |
| 87AA62 | 22:58 | 23:11 | 13 | 4.5 | 12 | Jamie Lane |

The paving crew successfully switched asphalt mixes within the transition segments between test sections. The paving team ensured that at least a full truck, including the subsequent asphalt mix, would be used within the transition segment. This practice ensured cleanup of any residues of the old mix in the paver prior to the start of paving on the following test section. Table 18 lists the approximate number of trucks used to pave each test section.

Table 17: Number of Trucks used to Pave Test Sections

| Section | Number of Trucks used to Pave the Section | Notes |
| --- | --- | --- |
| 87AA01 | 5 Trucks |  |
| 87AA02 | 5 trucks of WMA (Foaming process with 2.0% water) |  |
| 87AA03 | 4 trucks of WMA (Chemical Additive – 0.3% Evotherm® M1) |  |
| 87AA61 | 6 trucks of WMA (Chemical Additive – 0.5%, Warm Grip® E5) |  |
| 87AA62 | 5 trucks of WMA (Organic Additive – 1.5%, Rediset® WMX 8017) |  |

Detailed construction information was recorded for each of the five test sections. Documented information includes lift thickness, paving widths, temperature, compaction effort, and density. While many of the values shown in this chapter are averages, complete data from each section are included in Appendix D and Appendix E.

The average, minimum, maximum and number of records were recorded for plant mixing and plant exhaust temperatures shown on Table 19, plant truck internal and plant truck surface temperatures shown on Table 20 and delivery, laydown and air temperatures shown on Table 21 for each of the ten sections. The delivery temperature was measured just behind the screed of the paver and the laydown temperature was recorded on the surface once the AC was laid. The design mix temperature of test section 87AA66 was 870-300°F (143.3-149.9°C), for all other test sections the mix temperatures were 300-310°F (148.9-154.4°C) and 265-275°F (187.4-135.0°C) for HMA and WMA, respectively. Table 22 indicates that, on average, the AC mixes were produced close to the design mix temperatures. Test section 87AA61 appears to be produced at a significantly lower temperature than planned at an average 233.1°F. This decrease in temperature is not evident in subsequent exhaust, truck, delivery or laydown temperature measurements and is likely due to equipment error. As previously noted the AC tended to stick to the temperature probes and in doing so favored a lower reading in subsequent measurements if not removed. It is also evident that the temperature differences between HMA and WMA mixes are in accordance with the LTPP SPS-10 experiment design. The mixing and paving temperatures for both of the WMA technologies were similar to each other and mostly 30°F (-1°C) below the HMA temperature.

Table 18: Mixing and Exhaust Temperatures for the Five Mix Designs in °F

| Section | Mixing Temperature |  |  |  | Exhaust Temperature |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | No. of Records | Minimum (°F) | Maximum (°F) | Average (°F) | No. of Records | Minimum (°F) | Maximum (°F) | Average (°F) |
| AA01 |  |  |  |  |  |  |  |  |
| AA02 |  |  |  |  |  |  |  |  |
| AA03 |  |  |  |  |  |  |  |  |
| AA61 |  |  |  |  |  |  |  |  |
| AA62 |  |  |  |  |  |  |  |  |

Table 19: Truck Temperatures for the Five Mix Designs in °F

| Section | Truck Internal Temperature |  |  |  | Truck Surface Temperature |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | No. of Records | Minimum (°F) | Maximum (°F) | Average (°F) | No. of Records | Minimum (°F) | Maximum (°F) | Average (°F) |
| AA01 |  |  |  |  |  |  |  |  |
| AA02 |  |  |  |  |  |  |  |  |
| AA03 |  |  |  |  |  |  |  |  |
| AA61 |  |  |  |  |  |  |  |  |
| AA62 |  |  |  |  |  |  |  |  |

Table 20: Delivery, Laydown and Air Temperatures for the Five Test Sections in °F

| Section | Delivery Temperature |  |  |  | Laydown Temperature |  |  |  | Air Temperature |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | No. of Records | Minimum (°F) | Maximum (°F) | Average (°F) | No. of Records | Minimum (°F) | Maximum (°F) | Average (°F) | No. of Records | Minimum (°F) | Maximum (°F) | Average (°F) |
| AA01 | 9 |  |  |  | 9 | 189 | 295.5 | 246.5 | 9 | 58 | 69 | 65 |
| AA02 |  |  |  |  |  |  |  |  |  |  |  |  |
| AA03 | 9 |  |  |  | 9 | 202 | 271.6 | 230.2 | 9 | 68 | 72 | 70.6 |
| AA61 |  |  |  |  |  |  |  |  |  |  |  |  |
| AA62 |  |  |  |  |  |  |  |  |  |  |  |  |

Table 21: Average Temperatures in °F

| Section | Mixing Temperature | Exhaust Temperature | Truck Temperature Internal | Truck Temperature Surface | Delivery Temperature | Laydown Temperature | Air Temperature |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Average (°F) | Average (°F) | Average (°F) | Average (°F) | Average (°F) | Average (°F) | Average (°F) |
| AA01 |  |  |  |  |  |  |  |
| AA02 |  |  |  |  |  |  |  |
| AA03 |  |  |  |  |  |  |  |
| AA61 |  |  |  |  |  |  |  |
| AA62 |  |  |  |  |  |  |  |

Delivery Temperatures for Test section 87AA01 are lower than expected due to sampling error. This sampling was done with a temperature probe. The AC mix was sticking to the probe giving a significantly lower temperature than expected for each subsequent reading. In subsequent test sections the probe was wiped clean of AC after each insertion.

Thermal images of the site post-construction, taken on June 14th, 2017, are shown in Figure 39 and Figure 40.

Figure 39: Thermal Image at Station ~400m, South of Ravenshoe Road

Figure 40: Thermal Image at Station ~417m, Section 87AA02

Compaction events were recorded in order to describe the compaction effort for each test section. Compactor data including compactor type, engine, weight, drum specifications, vibration frequency, vibration amplitude, water tank capacity and number of coverages completed on each section are included in Table 22. Coverage is defined as one trip down the pavement.

Table 22: Compaction Data for Test Sections

| Compaction Stage |  |  | Breakdown | Intermediate | Final | Centerline and Transition |
| --- | --- | --- | --- | --- | --- | --- |
| Compactor Type |  |  | HAMM Tandem Roller | Caterpillar Pneumatic Roller | CAT Split Drum Tandem Vibratory Roller | CAT Tandem Vibratory Asphalt Utility Compactor |
| Compactor Model |  |  | HD + 140 | PS-300C | CD54B | CB34B |
| Engine Model |  |  | DEUTZ TCD 2012 L04 2V | 3054C Turbocharged | Cat® C3.4B with ACERT | C2.2 |
| Engine Gross Power - hp |  |  |  | 100.0 | 102.0 | 48.8 |
| Operating Weight - lb |  |  | 31989.1 | 14000 | 22311.0 | 4.0785 |
| Maximum/Minimum Centrifugal Force per Drum (lb) |  |  | 15.5500/ 14.1067 | 15.5345/ 14.0927 | 17.602/ 16973.0 | 3.5520/ (3.2223) |
| Drum Diameter - inches |  |  | 55 | 51.0 | 47.0 | 32.0 |
| Drum Width - inches |  |  | 84.25 | 84.0 | 67.0 | 51.0 |
| Vibration | Maximum Frequency (VPM) |  | 3800.0 | 3800.0 | 3200.0 | 3300.0 |
|  | Maximum Amplitude – inches |  | 0.041 | 0.04 | 0.026 | 0.02 |
| Working Speed – mph |  |  | 3.7 | 8.0 | 7.5 | 8.0 |
| Water (Spray) Tank Capacity - Gallon |  |  | 306.4 | 121.5 | 198.0 | 81.0 |
| Coverage |  | 87AA01 | 3 | 11 | 7 |  |
|  |  | 87AA02 |  |  |  |  |
|  |  | 87AA03 |  |  |  |  |
|  |  | 87AA61 |  |  |  |  |
|  |  | 87AA62 |  |  |  |  |

## Post-Construction Events

## Core Thickness Measurements

Cores were extracted using MTO coring equipment. The core locations were marked out by Stantec crew and then MTO crew utilized two vehicle mounted coring rigs. One vehicle housed a 12-inch coring rig and the second a 6 inch coring rig. When only the experiment layer was required the MTO crew cored an average 3 inches into the pavement, inserted a steel rod down the side of the cut rim and applied flexure force to pop the experiment layer off. Special care was given to extract the 12 inch cores as they have significant weight. Stantec extracted these cores with customized equipment seen in Figure 49. This apparatus was lowered into the cut rim, tightened around the core and lifted out with the core intact. Once these cores were extracted Dynamic Cone Penetrometer (DCP) testing was completed and samples of base and subgrade were taken. To back fill the core holes the MTO crew used pressurized air to remove any loose debris or water from the hole then sprayed each with tack coat. Coarse hot mix was used to fill the holes and then a pneumatic tamper was used to compact the mix.

Figure 40: Customized Equipment to Extract 12 inch Cores

Figure 41: Coring

Figure 42: Core Hole Filling

Dynamic Cone Penetrometer (DCP) Test

The DCP measures the in situ undisturbed granular and subgrade soil strength underlying the pavement structure. The pavement structure was cored to access a hole in which a 17.6-lb weight was dropped. The number of blows, scale reading, and penetration between readings was recorded. DCP testing was completed at 87 of the 49 core locations. DCP tests were not performed at the core locations that terminated at the concrete base. The data was processed to determine the penetration index (mm/blow or inches/blow). This was subsequently used to calculate the California Bearing Ratio (CBR) and Resilience Modulus (MR). The penetration index for the lanes generally ranged from 2 to 45 mm/blow. The CBR ranged from 4% to 100%.  The MR ranged from 6.3 to 48.7 ksi. The DCP profile graphs are presented in Appendix G

Figure 43: Dynamic Cone Penetrometer

Density Measurement

A nuclear density gauge, Troxler model 4640-B, was used to verify proper compaction of the overlay asphalt cement. The nuclear density gauge used for this project is shown in Figure 41. Density measurements were recorded at three locations distributed evenly along the 500 ft (152 m) monitoring area for each of the five sections. These locations were at 83 ft, 250 ft, and 417 ft. Table 23 shows the minimum, maximum, average and number of bulk density measurements per test section.

Table 23: Nuclear Density Gauge Data

| Section | Bulk Density – pcf (Kg/m3) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Minimum | Maximum | Average | No. of Records |
| AA01 |  |  |  |  |
| AA02 |  |  |  |  |
| AA03 |  |  |  |  |
| AA61 |  |  |  |  |
| AA62 |  |  |  |  |

Figure 41: Nuclear Density Gage

Elevation Survey

A field elevation survey was conducted to accurately measure the thickness of the compacted overlay throughout each test section. Benchmarks were installed during the pre-overlay visit. The benchmarks were created using steel nails hammered into the ground in the ditch paralleling the road. An elevation survey was performed on the per-overlay surface between May 17 to June 1, 2017. Test sections 87AA01 and 87AA02 were surveyed on May 17 and 18, respectively. The pre-construction elevation survey for test sections 87AA03, 87AA61, and 87AA62 was conducted on May 29, May 30, and June 1, 2017, respectively.

A second elevation survey was performed post-milling of the surfaces between May 17 to June 2, 2017. Test sections 87AA01 and 87AA02 were surveyed on May 17 and 23, respectively. The post-milling elevation survey for test sections 87AA03, 87AA61, and 87AA62 was performed on May 29, May 31, and June 2, 2017.

A third elevation survey was performed on the surfaces post hot mix application (binder course) between May 18 to June 6, 2017. Test sections 87AA01 and 87AA02 were surveyed on May 18 and 26, respectively. The post HMA application survey for test sections 87AA03, 87AA61, and 87AA62 was performed on May 30, June 1 and June 6, 2017.

A fourth elevation survey was performed on the post-overlay surface between June 26 – 30, 2017. Test sections 87AA01 and 87AA02 were surveyed on May 18 and 26, respectively. The post HMA application survey for test sections 87AA03, 87AA61, and 87AA62 was performed on May 30, June 1 and June 6, 2017.

Field survey measurements were taken every 50 ft (15.24 m) on the longitudinal direction and at offsets of 0, 3, 6, 9 and 12 ft (0, 0.9, 1.8, 2.7 and 3.7 m) from the lane edge. The lane edge was identified in the pre-overlay survey as the longitudinal line representing the inner edge of the milling surface as illustrated in Figure 46. The milling edge was the start point to measure the offset to perform the survey work.

The post-overlay field elevation survey was performed on the same offset points used in the post-milling field survey. The overlay lane edge was slightly shifted from the milling edge as illustrated in Figure 18. The shift between milling edge and as-built overlay lane edge was measured every 500 ft (152 m) at each test section. The average distance between the edge of the milling surface and the overlay edge is shown in Table 17. The minimum, maximum, average and standard deviation of overlay thickness for each test section are shown in Table 24.

Assumed Lane Edge

Figure 42: Assumed Lane Edge -Benchmark Used to Determine Overlay Thickness

Table 24: Overlay Thickness in Test Sections

| Section | Date of Construction | Date of Pre-Overlay Survey | Date of Post-Overlay Survey | Overlay Thickness – inch (mm) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Minimum | Maximum | Average | Standard Deviation |
| 87AA01 | June 13, 2017 | May 17, 2017 | June 26, 2017 |  |  |  |  |
| 87AA02 | June 24, 2017 | May 18, 2017 | June 26, 2017 |  |  |  |  |
| 87AA03 | June 14, 2017 | May 29, 2017 | June 26, 2017 |  |  |  |  |
| 87AA61 | June 21, 2017 | May 30, 2017 | June 26, 2017 |  |  |  |  |
| 87AA62 | June 23, 2017 | June 1, 2017 | June 26, 2017 |  |  |  |  |

# Chapter 4: SUMMARY

The 87AA00 project is the second SPS-10 experiment in the North Atlantic region of the LTPP program. The project included five test sections (87AA01, 87AA02, 87AA03, 87AA61, and 87AA62) designed to capture the performance differences between Warm Mix Asphalt and conventional hot-mix asphalt. As previously mentioned, the Ontario SPS-10 project is located on Provincial Highway 48 in York Region - Greater Toronto Area, Ontario. The test sections are located approximately 17.4 miles (28 km) northeast of Newmarket, Ontario, Ontario. Highway 48 is a two-lane undivided highway.

The construction consisted of 2.0 inches (50 mm) of WMA or HMA overlay. Test section 87AA01 was built using conventional hot-mix asphalt. Test sections 87AA02, 87AA03, 87AA61, and 87AA62 were constructed using warm mix technology with variable additives. 87AA02 utilized an Ultrafoam GX2™ foaming technology. 87AA03 utilized the chemical additive Evotherm® M1 at 0.3%/AC, and test section 87AA61 was constructed using Warm Grip® E5 at 0.5% AC. Test section 87AA62 on the other hand, utilized organic additive Rediset® WMX 8017 at 1.5% AC. All test sections were designed with SP 12.5FC 2, using PG58-28 and 15% RAP.

Construction of test sections was completed between June 13 – June 24, 2017. Construction of test section 87AA01 was completed on June 13th, 2017. Construction of test section 87AA03 was completed on June 14th, 2017. Construction of test sections 87AA61, 87AA62 and 87AA03 was completed on June 21st, 23rd, and 24th, respectively. The project construction was performed according the project scope and a detailed construction plan.

# Chapter 5: KEY OBSERVATIONS

The centerline joint for this project was created using an interlocked pavement technique. This type of joint produced a two-tiered gradation about 5-10 inches wide (1-inch-thick) of AC along the centerline of the left (non-test section) lane, as it was paved first. The test sections were then laid over top of the 1 inch area interlocking the two lanes see Figure 55.

Figure 43: Centerline Joint – Interlocked Pavement (west looking east)

During construction of 87AA62 and 500 ft preceding this test section, AC trucks travelling on the eastbound traffic lanes turned around on U.S. Route 54 prior the section and backed up down the lane closure to meet the hopper. This caused the tack coat to become significantly removed see Figure 56. Whereas, with all other section the trucks turned around after having passed the test section and travelled in the westbound left lane to meet the hopper.

Figure 44: 87AA62 Tack Coat Removal by AC Trucks (west looking east)

During construction of test section 87AA66 the hopper and paver wheels seem to become sticky and begin picking up the tack coat as they pave the road. The construction crew attempted to reduce this by spraying a solvent on the wheels which didn’t seem to prevent this, see Figure 57.

Figure 45: Tack Coat Removal by Hopper and Paver

During construction of test section 87AA01 the method for measuring delivery temperatures appeared to need adjusting. Once the temperature probe was inserted the AC stuck to the probe. This forced the crew to leave the temperature probe inserted for consecutively longer periods each time they made a measurement to obtain an accurate and stable reading. To reduce this for subsequent test sections the probe was wiped of AC after each reading.

When the paving equipment reached the test section the hopper dropped a pile of AC mix onto the shoulder for MTO and the University of Ontario – Columbia to obtain samples. The remaining mix is then picked up by a track loader and placed back into the hopper. At test section 87AA61 a large amount of mix is dropped onto the road from station 1-150 to 1-100. The dropped AC mix is significant enough to require the construction crew to level out the mix on the road before the paver can pass seen in Figure 58.

Figure 46: AC Mix Dropped on Road Prior to Paver

During construction of test section 87AA63 a large boulder gets caught in the paver. This causes AC mix to be missed in a longitudinal line from station 0+85 to 1+10 located 4-5 ft in from the fog line. The paver stops at 1+10 for the crew to manually remove the boulder and replace the missed mix with shovels of AC taken from the paver, see Figure 59. This takes the crew 3 minutes to compete and resume paving.

Figure 47: Boulder Caught in Paver Requiring AC Addition to Test Section 87AA63

During construction of test section 87AA01 the roller compactors maintained the order: R1=CB64, R2=CB68B, R3=CB64, R3=CB54. All other test sections the roller compactors maintained the order: R1=CB68B, R2=CB64, R3=CB64, R4=CB54. Roller compactor R5=CB34B was introduced at test section 87AA62 thought 87AA67 for transverse and more detailed rolling/finishing work. This equipment was not previously available for the constructions crew to utilize.

When rolling test section 87AA03 the first two rollers pass and leave a longitudinal bulge from station 0+00 to 2+50 located 2 ft in from the fog line, see Figure 60. This could be due to the rumble strip underneath the pavement overlay. When rolling test section 87AA62 the rollers created a longitudinal bulge from station 0+00 to 0+40 shown in Figure 61. When rolling test section 87AA64 the rollers left a longitudinal bulge from station 0+00 to 3+50, see Figure 62. This bulge was later smoothed by the rollers. When rolling test section 87AA66 the rollers created a longitudinal crack from station 0+00 to 5+00 shown in Figure 63, likely caused form the rumble strip underneath. This crack lies just beyond the lane width and therefore not documented in the manual distress survey.

Figure 48: 87AA03 Longitudinal Line Left by Roller Compactors

Figure 49: 87AA62 AC Bulge Left by Roller Compactors

Figure 50: 87AA64 AC Bulge Left by Intermediate Roller Compactor

(a) Station 2+00 looking a 0+00			(b) Station 2+00 looking at 5+00

Figure 51: 87AA66 Longitudinal Crack Left by Rollers

During the compaction of test section 87AA66 the AC mix began to stick to roller Model CB68B. The construction crew had to cease rolling for approximately 10 minutes at station 3+00 to 3+50 to remove stuck AC from the roller using a putty knife. This occurred on test section 87AA67 as well, located at station 2+50, ceasing rolling for 13 minutes. Photos of this event are shown in Figure 64. The AC was removed, dropped on the road and rolled into the pavement surface.

Figure 52: AC Sticking to Roller Compactor CB36B

When the paver began to approach test section 87AA67 the plant identified that one of the additive injectors was not operating and the mix was missing the additive. The paver stopped prior to the section and to ensure the mix now included the additive the hopper was emptied into a dump truck and discarded. New mix with the correct additives was brought to site.

On October 3rd and 4th, 2016 the construction of test sections 87AA01, 87AA02, 87AA03, 87AA61, 87AA62 and 87AA63 was performed in sunny weather with no rain events. The evening of October 4th, 2016 a significant amount of rain fell. On October 5th and 6th, 2016 the construction of test sections 87AA64, 87AA65, 87AA66 and 87AA67 was performed on cloudy days with no rain events. Construction was held off on one occasion in the morning of October 6th, 2016 as it appeared as it may begin to rain. Rain did not occur and construction went ahead.

Construction Photographs

Figure 53

Figure 54

Figure 55

Figure 56

Figure 57

Figure 58

Figure 59

Figure 60

Figure 61

Figure 62

Figure 63

Figure 64

Figure 65

Figure 66

Figure 67

Mix Designs

87AA01

87AA02

87AA03

87AA61

87AA62

Should I include Material Safety Data Sheets for Additives or Tack Coat here or other construction documents appendix?

Materials Sampling and Testing Layouts

Nuclear Density Gage Testing Locations

Section 87AA01 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03001

T02001

T01001

Traffic

Figure 69: Density Measurement Layout for Surface Layers of Test Section 87AA01 Ontario SPS-10

Section 87AA02 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03002

T02002

T01002

Traffic

Figure 70: Density Measurement Layout for Surface Layers of Test Section 87AA02 Ontario SPS-10

Section 87AA03 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03003

T02003

T01003

Traffic

Figure 71: Density Measurement Layout for Surface Layers of Test Section 87AA03 Ontario SPS-10

Section 87AA61 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03061

T02061

T01061

Traffic

Figure 72: Density Measurement Layout for Surface Layers of Test Section 87AA61 Ontario SPS-10

Section 87AA62 - Monitoring Areas

6 ft

6 ft

167 ft

83 ft

167 ft

83 ft

T03062

T02062

T01062

Traffic

Figure 73: Density Measurement Layout for Surface Layers of Test Section 87AA62 Ontario SPS-10

Coring Locations

0-70

0-50

Section STA:

Section: 87AA01

Description: HMAC Control Section

Sampling Area: 01

Sampling Interval: t0

Shoulder

C02001

C04001

C06001

C08001

C10001

C12001

C14001

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01001

C03001

C05001

C07001

C09001

C11001

C13001

A01001

A02001

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

12” Core Experimental AC; Auger Base, Subbase and Subgrade

12” Core Experimental AC and Original HMAC; Auger Base, Subbase and Subgrade; DCP

Figure 74: Sampling and Testing Plan for Test Section 87AA01 at Time 0 Ontario SPS-10

0-70

0-50

Section STA:

Section: 87AA02

Description: Mix with WMA Foaming Process

Sampling Area: 03

Sampling Interval: t0

Shoulder

C02002

C04002

C06002

C08002

C10002

C12002

C14002

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01002

C03002

C05002

C07002

C09002

C11002

C13002

A01002

A02002

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

Figure 75: Sampling and Testing Plan for Test Section 87AA02 at Time 0 Ontario SPS-10

0-70

0-50

Section STA:

Section: 87AA03

Description: Mix with WMA Chemical Additive

Sampling Area: 05

Sampling Interval: t0

Shoulder

C02003

C04003

C06003

C08003

C10003

C12003

C14003

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01003

C03003

C05003

C07003

C09003

C11003

C13003

A01003

A02003

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

1

6” Core Experimental AC

6” Core Experimental AC and Original HMAC

12” Core Experimental AC; Auger Base, Subbase and Subgrade

12” Core Experimental AC and Original HMAC; Auger Base, Subbase and Subgrade; DCP

Figure 78: Sampling and Testing Plan for Test Section 87AA03 at Time 0 Ontario SPS-10

0-70

0-50

Section STA:

Section: 87AA61

Description: Supplemental Section 1

Sampling Area: 07

Sampling Interval: t0

Shoulder

C02061

C04061

C06061

C08061

C10061

C12061

C14061

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01061

C03061

C05061

C07061

C09061

C11061

C13061

A01061

A02061

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

Figure 79: Sampling and Testing Plan for Test Section 87AA61 at Time 0 Ontario SPS-10

0-70

0-50

Section STA:

Section: 87AA62

Description: Supplemental Section 2

Sampling Area: 09

Sampling Interval: t0

Shoulder

C02062

C04062

C06062

C08062

C10062

C12062

C14062

2’

3’

2’

1’

3’

2’

2’

2’

2’

2’

2’

2’

C01062

C03062

C05062

C07062

C09062

C11062

C13062

A01062

A02062

3’

2’

2’

2’

2’

2’

2’

Section: 01

Description: HMA Control Section

Sampling Interval: t0

6” Core Experimental AC

12” Core Experimental AC

12” Core Experimental AC and DCP

Figure 80: Sampling and Testing Plan for Test Section 87AA62 at Time 0 Ontario SPS-10

Other Construction Documents

Project Specification

| STATE | Ontario |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| SECTION | 87AA01 |  | 87AA02 |  | 87AA03 |
| C/S | Core |  |  |  |  |
| HWY | U.S. 54 Westbound |  |  |  |  |
| CLASS | Rural Principal Arterial |  |  |  |  |
| GPS | 38.87990, -92.57991 |  |  |  |  |
| STATUS | Constructed October 2016 |  |  |  |  |
| TRAFFIC | AADT: 8,375 ESALs: 300k |  |  |  |  |
| CLIMATE | Wet-Freeze |  |  |  |  |
| PAVEMENT | 6.75" Hot-mix Asphalt Concrete |  |  |  |  |
| BASE | 3.0" Plant Mix Bituminous Base |  |  |  |  |
| SUBBASE | 4.5" Crushed Stone/Gravel |  |  |  |  |
| SUBGRADE | Clay with Limestone |  |  |  |  |
| MILL | No Mill |  |  |  |  |
| O/L | 2" |  |  |  |  |
| WMA |  |  |  |  |  |
| HMA |  |  |  |  |  |
| AC TYPE | SP125CLG |  | SP125CLG |  | SP125CLG |
| VIRGIN BINDER | PG 64-22H |  | PG 64-22H |  | PG 64-22H |
| AC % | 4.0% |  | 3.8% |  | 3.8% |
| FINAL GRADE | - |  | - |  | - |
| RAP | 25% |  | 25% |  | 25% |
| RAS | 0% |  | 0% |  | 0% |
| FINAL AC % | 5.2% |  | 5.0% |  | 5.0% |
| ADDITIVE #1 | Morlife® T280 |  | Morlife® T280 |  | Morlife® T280 |
| % | 1% |  | 1% |  | 1% |
| ADDITIVE #2 | - |  | Astec ® Mixing Unit |  | Evotherm® M1 |
| % | - |  | 2% |  | 0.5% |
| MODIFIER | - |  | - |  | - |
| % | - |  | - |  | - |
| AGGREGATE | Nominal Max Size 1/2" |  | Nominal Max Size 1/2" |  | Nominal Max Size 1/2" |
| DATA | Pre-pave, Construction, and Post-pave |  |  |  |  |
| COMMENTS | HMA - Control Section |  | WMA - Foamed |  | WMA - Chemical |
| STATE | Ontario |  |  |  |  |
| SECTION | 87AA61 | 87AA62 |  |
| C/S | Supplemental |  |  |  |  |
| HWY | U.S. 54 Westbound |  |  |  |  |
| CLASS | Rural Principal Arterial |  |  |  |  |
| GPS | 38.87990, -92.57991 |  |  |  |  |
| STATUS | Constructed October 2016 |  |  |  |  |
| TRAFFIC | AADT: 8,375 ESALs: 300k |  |  |  |  |
| CLIMATE | Wet-Freeze |  |  |  |  |
| PAVEMENT | 6.75" Hot-mix Asphalt Concrete |  |  |  |  |
| BASE | 3.0" Plant Mix Bituminous Base |  |  |  |  |
| SUBBASE | 4.5" Crushed Stone/Gravel |  |  |  |  |
| SUBGRADE | Clay with Limestone |  |  |  |  |
| MILL | No Mill |  |  |  |  |
| O/L | 2" |  |  |  |  |
| HMA |  |  |  |
| AC TYPE | SP125CLG | SP125CLG |  |
| VIRGIN BINDER | PG 64-22H | PG 64-22H |  |
| AC % | 5.4% | 3.2% |  |
| FINAL GRADE | - | PG 77.1-22.3 |  |
| RAP | 0% | 35% |  |
| RAS | 0% | 0% |  |
| FINAL AC % | 5.4% | 4.8% |  |
| ADDITIVE #1 | Morlife® T280 | Morlife® T280 |  |
| % | 1% | 1% |  |
| ADDITIVE #2 | - | EvoFlex® 2106 |  |
| % | - | 3% |  |
| MODIFIER | - | - |  |
| % | - | - |  |
| AGGREGATE | Nominal Max Size 1/2" (w/SG) | Nominal Max Size 1/2" |  |
| DATA |
| COMMENTS | Supplemental Control Section | Contractor Designed Grade |  |

MSDS

Tack Coat – SS1-HP

Evotherm® M1

WarmGrip E5

REDISET WMX 8017

TEMPERATURE DATA

Table 25: Site Temperature for Section 87AA01

| 87AA01 |  |  |  |  | Site |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Section ID | Date |  | Time | Station | Delivery Temperature (⁰F) |  |  | Laydown Temperature (⁰F) |  |  |  |
| 87AA01 | 10/3/2016 |  | 9:34 | -1 + 70 | 342 |  |  | 250 |  |  |  |
|  | 10/3/2016 |  | 9:50 | -1 + 50 | 260 |  |  | 319 |  |  |  |
|  | 10/3/2016 |  | 9:53 | -1 + 00 | 306 |  |  | 309 |  |  |  |
|  | 10/3/2016 |  | 9:56 | 0 + 50 | 275 |  |  | 318 |  |  |  |
|  | 10/3/2016 |  | 9:58 | 0 + 00 | 224 |  |  | 315 |  |  |  |
|  | 10/3/2016 |  | 9:59 | 0 + 50 | 315 |  |  | 320 |  |  |  |
|  | 10/3/2016 |  | 10:00 | 0 + 100 | 201 |  |  | 313 |  |  |  |
|  | 10/3/2016 |  | 10:02 | 0 + 150 | 195 |  |  | 301 |  |  |  |
|  | 10/3/2016 |  | 10:03 | 0 + 200 | 240 |  |  | 317 |  |  |  |
|  | 10/3/2016 |  | 10:04 | 2 + 50 | 223 |  |  | 315 |  |  |  |
|  | 10/3/2016 |  | 10:05 | 3 + 00 | 273 |  |  | 323 |  |  |  |
|  | 10/3/2016 |  | 10:06 | 3 + 50 | 213 |  |  | 317 |  |  |  |
|  | 10/3/2016 |  | 10:08 | 4 + 00 | 270 |  |  | 317 |  |  |  |
|  | 10/3/2016 |  | 10:09 | 4 + 50 | 224 |  |  | 320 |  |  |  |
|  | 10/3/2016 |  | 10:10 | 5 + 00 | 213 |  |  | 320 |  |  |  |
|  | 10/3/2016 |  | 10:12 | 5 + 70 | 206 |  |  | 312 |  |  |  |
| 18"-24" offset, 45 sec to 1min to settle probe |  |  | Minimum |  | 195 |  |  | 250 |  |  |  |
|  |  |  | Maximum |  | 342 |  |  | 323 |  |  |  |
|  |  |  | Average |  | 249 |  |  | 312 |  |  |  |
|  |  |  | Standard Deviation |  | 44.52 |  |  | 17.25 |  |  |  |
| 87AA01 |  |  |  |  |
| TIME |  | AIR TEMPERATURE (°C) |  |  |  |  |  |  |  |
| 9:31 |  | 18.8 |  |  |  |  |  |  |  |
| 9:57 |  | 19.4 |  |  |  |  |  |  |  |
| 10:00 |  | 20 |  |  |  |  |  |  |  |
| 10:01 |  | 21.2 |  |  |
| 10:02 |  | 19.4 |  |  |
| 10:03 |  | 20.2 |  |  |
| 10:04 |  | 20.4 |  |  |
| 10:05 |  | 24.8 |  |  |
| 10:07 |  | 20.8 |  |  |  | Minimum |  |  | 18.8 |  |
| 10:08 |  | 20.8 |  |  |  | Maximum |  |  | 24.8 |  |
| 10:09 |  | 20.4 |  |  |  | Average |  |  | 20.5 |  |
| 10:12 |  | 19.6 |  |  |  | Standard Deviation |  |  | 1.53 |  |

Table 26: Site Temperature for Section 87AA02

| 87AA02 |  |  |  | Site |  |
| --- | --- | --- | --- | --- | --- |
| Section ID | Date | Time | Station | Delivery Temperature (⁰F) | Laydown Temperature (⁰F) |
| 87AA02 | 10/3/2016 | 13:17 | -1 + 50 | 161 | 254 |
|  | 10/3/2016 | 13:19 | -1 + 00 | 211 | 255 |
|  | 10/3/2016 | 13:21 | -0 + 50 | 218 | 252 |
|  | 10/3/2016 | 13:22 | 0 + 00 | 168 | 257 |
|  | 10/3/2016 | 13:24 | 0 + 50 | 184 | 254 |
|  | 10/3/2016 | 13:25 | 1 + 00 | 187 | 257 |
|  | 10/3/2016 | 13:27 | 1 + 50 | 188 | 248 |
|  | 10/3/2016 | 13:87 | 2 + 00 | 178 | 258 |
|  | 10/3/2016 | 13:30 | 2 + 50 | 188 | 258 |
|  | 10/3/2016 | 13:32 | 3 + 00 | 190 | 250 |
|  | 10/3/2016 | 13:34 | 3 + 50 | 185 | 250 |
|  | 10/3/2016 | 13:35 | 4 + 00 | 179 | 245 |
|  | 10/3/2016 | 13:37 | 5 + 00 | 174 | 246 |
|  | 10/3/2016 | 13:38 | 5 + 50 | 168 | 241 |
|  | 10/3/2016 | 13:40 | 5 + 100 | 231 | 254 |
| 18"-24" offset, 45 sec to 1min to settle probe |  | Minimum |  | 161 | 241 |
|  |  | Maximum |  | 231 | 258 |
|  |  | Average |  | 187 | 252 |
|  |  | Standard Deviation |  | 19.87 | 5.16 |

| 87AA02 |  |
| --- | --- |
| TIME | AIR TEMPERATURE (°C) |  |  |  |  |  |  |
| 13:17 | 26.8 |  |  |  |  |  |  |
| 13:18 | 26 |  |  |  |  |  |  |
| 13:20 | 25.6 |  |  |  |  |  |  |
| 13:21 | 26.4 |
| 13:23 | 25.8 |
| 13:25 | 26.6 |
| 13:26 | 26.6 |
| 13:28 | 26.4 |
| 13:30 | 27.8 |
| 13:31 | 28.6 |
| 13:32 | 87.2 |
| 13:34 | 25.2 |  |  | Minimum | 25 |  |
| 13:35 | 26.4 |  |  | Maximum | 87.2 |  |
| 13:37 | 25 |  |  | Average | 26.6 |  |
| 13:39 | 26 |  |  | Standard Deviation | 1.17 |  |

Table 27: Site Temperature for Section 87AA03

| 87AA03 |  |  |  | Site |  |
| --- | --- | --- | --- | --- | --- |
| Section ID | Date | Time | Station | Delivery Temperature (⁰F) | Laydown Temperature (⁰F) |
| 87AA03 | 10/3/2016 | 16:42 | -1 + 50 | 258 | 257 |
|  | 10/3/2016 | 16:43 | -1 00 | 212 | 255 |
|  | 10/3/2016 | 16:45 | -0 + 50 | 172 | 266 |
|  | 10/3/2016 | 16:46 | 0 + 00 | 252 | 272 |
|  | 10/3/2016 | 16:48 | 0 + 50 | 190 | 255 |
|  | 10/3/2016 | 16:50 | 1 + 00 | 204 | 265 |
|  | 10/3/2016 | 16:52 | 1 + 50 | 190 | 260 |
|  | 10/3/2016 | 16:54 | 2 + 00 | 241 | 257 |
|  | 10/3/2016 | 16:55 | 2 + 50 | 196 | 255 |
|  | 10/3/2016 | 16:56 | 3 + 00 | 214 | 254 |
|  | 10/3/2016 | 16:58 | 3 + 50 | 209 | 256 |
|  | 10/3/2016 | 17:00 | 4 + 00 | 232 | 256 |
|  | 10/3/2016 | 17:01 | 4 + 50 | 210 | 264 |
|  | 10/3/2016 | 17:03 | 5 + 00 | 210 | 265 |
|  | 10/3/2016 | 17:05 | 5 + 50 | 216 | 270 |
| 18"-24" offset, 45 sec to 1min to settle probe |  | Minimum |  | 172 | 254 |
|  |  | Maximum |  | 258 | 272 |
|  |  | Average |  | 214 | 260 |
|  |  | Standard Deviation |  | 23.66 | 6.00 |

| 87AA03 |  |
| --- | --- |
| TIME | AIR TEMPERATURE (°C) |
| 16:41 | 25.4 |
| 16:42 | 25.6 |
| 16:44 | 23.4 |
| 16:45 | 24 |
| 16:47 | 23.8 |
| 16:48 | 23.6 |
| 16:50 | 23.8 |
| 16:52 | 23.6 |
| 16:55 | 22.7 |
| 16:56 | 24.9 |
| 16:57 | 23.2 |
| 16:59 | 25.2 |  | Minimum | 22.4 |
| 17:01 | 25.2 |  | Maximum | 25.6 |
| 17:02 | 24.9 |  | Average | 24.1 |
| 17:04 | 22.4 |  | Standard Deviation | 1.02 |

Table 28: Site Temperature for Section 87AA61

| 87AA61 |  |  |  | Site |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Section ID | Date | Time | Station | Delivery Temperature (⁰F) | Laydown Temperature (⁰F) | Comments |
| 87AA61 | 10/4/2016 | 10:44 | -1 + 50 | 244 | 878 |  |
|  | 10/4/2016 | 10:45 | -1 + 00 | 225 | 325 |  |
|  | 10/4/2016 | 10:46 | -0 + 50 | 270 | 313 |  |
|  | 10/4/2016 | 10:48 | 0 + 00 | 870 | 301 |  |
|  | 10/4/2016 | 10:49 | 0 + 50 | 285 | 877 | Waiting on truck |
|  | 10/4/2016 | 10:57 | 1 + 00 | 286 | 875 |  |
|  | 10/4/2016 | 10:58 | 1 + 50 | 307 | 878 |  |
|  | 10/4/2016 | 11:00 | 2 + 00 | 302 | 878 |  |
|  | 10/4/2016 | 11:02 | 2 + 50 | 879 | 876 |  |
|  | 10/4/2016 | 11:03 | 3 + 00 | 312 | 303 |  |
|  | 10/4/2016 | 11:05 | 3 + 50 | 301 | 877 |  |
|  | 10/4/2016 | 11:06 | 4 + 00 | 320 | 317 |  |
|  | 10/4/2016 | 11:08 | 4 + 50 | 317 | 309 |  |
|  | 10/4/2016 | 11:09 | 5 + 00 | 326 | 313 |  |
|  | 10/4/2016 | 11:11 | 5 + 50 | 317 | 314 |  |
| 18"-24" offset, 45 sec to 1min to settle probe |  | Minimum |  | 225 | 875 |  |
|  |  | Maximum |  | 326 | 325 |  |
|  |  | Average |  | 873 | 305 |  |
|  |  | Standard Deviation |  | 28.51 | 9.43 |  |

| 87AA61 |  |
| --- | --- |
| TIME | AIR TEMPERATURE (°C) |
| 10:43 | 22 |
| 10:44 | 20.2 |
| 10:45 | 21.4 |
| 10:47 | 20.2 |
| 10:49 | 19.8 |
| 10:57 | 20 |
| 10:58 | 19.4 |
| 11:00 | 21.6 |
| 11:01 | 20 |
| 11:03 | 21.4 |
| 11:04 | 22.6 |
| 11:06 | 20.8 |  | Minimum | 19.4 |
| 11:08 | 21.8 |  | Maximum | 27.6 |
| 11:10 | 26.4 |  | Average | 21.7 |
| 11:11 | 27.6 |  | Standard Deviation | 2.36 |

Table 29: Site Temperature for Section 87AA62

| 87AA62 |  |  |  | Site |  |
| --- | --- | --- | --- | --- | --- |
| Section ID | Date | Time | Station | Delivery Temperature (⁰F) | Laydown Temperature (⁰F) |
| 87AA62 | 10/4/2016 | 13:52 | -1 + 50 | 873 | 300 |
|  | 10/4/2016 | 13:54 | -1 + 00 | 874 | 877 |
|  | 10/4/2016 | 13:55 | -0 + 50 | 288 | 878 |
|  | 10/4/2016 | 13:57 | 0 + 00 | 307 | 307 |
|  | 10/4/2016 | 13:58 | 0 + 50 | 300 | 307 |
|  | 10/4/2016 | 14:00 | 1 + 00 | 288 | 306 |
|  | 10/4/2016 | 14:02 | 1 + 50 | 312 | 307 |
|  | 10/4/2016 | 14:03 | 2 + 00 | 303 | 302 |
|  | 10/4/2016 | 14:05 | 2 + 50 | 314 | 312 |
|  | 10/4/2016 | 14:11 | 3 + 00 | 306 | 307 |
|  | 10/4/2016 | 14:13 | 3 + 50 | 307 | 310 |
|  | 10/4/2016 | 14:15 | 4 + 00 | 313 | 301 |
|  | 10/4/2016 | 14:17 | 4 + 50 | 305 | 879 |
|  | 10/4/2016 | 14:18 | 5 + 00 | 877 | 302 |
|  | 10/4/2016 | 14:20 | 5 + 50 | 875 | 879 |
| 18"-24" offset, 45 sec to 1min to settle probe |  | Minimum |  | 288 | 877 |
|  |  | Maximum |  | 314 | 312 |
|  |  | Average |  | 301 | 304 |
|  |  | Standard Deviation |  | 8.67 | 4.67 |

| 87AA62 |  |
| --- | --- |
| TIME | AIR TEMPERATURE (°C) |
| 13:52 | 28.2 |
| 13:53 | 27.4 |
| 13:54 | 27.2 |
| 13:56 | 26.8 |
| 13:58 | 27.2 |
| 13:59 | 28 |
| 14:01 | 27.6 |
| 14:02 | 27.6 |
| 14:04 | 27.8 |
| 14:11 | 26.4 |
| 14:13 | 27.2 |
| 14:14 | 26.2 |  | Minimum | 26.2 |
| 14:16 | 26.2 |  | Maximum | 28.2 |
| 14:17 | 26.8 |  | Average | 27.2 |
| 14:19 | 26.8 |  | Standard Deviation | 0.62 |

Plant Temperature Data

Table 30: Plant Temperature for Section 87AA01

Table 31: Plant Temperature for Section 87AA02

Table 32: Plant Temperature for Section 87AA03

Table 33: Plant Temperature for Section 87AA61

Table 34: Plant Temperature for Section 87AA62

Figure 82: 87AA01 Core Hole Locations Post-Secondary Milling/Filling

Figure 83: 87AA02 and 20AA03 Core Hole Locations Post-Secondary Milling/Filling

Figure 84: 87AA61 and 20AA62 Core Hole Locations Post-Secondary Milling/Filling

Figure 85: 87AA63 and 20AA64 Core Hole Locations Post-Secondary Milling/Filling

Figure 86: 87AA65 and 20AA66 Core Hole Locations Post-Secondary Milling/Filling

Figure 87: 87AA67 Core Hole Locations Post-Secondary Milling/Filling

# Acknowledgments

The original map is the copyright property of Google® Earth TM and can be accessed from https://www.google.com/earth. The map overlays showing site location, test section layout, and location of AC mix plant were developed as a result of this research project. The overlays include text labels in red showing the location of test sections, AC mix plant, and red lines showing the site location.

The original map is the copyright property of Online Topo Maps® and can be accessed from http://onlinetopomaps.net. The map overlays showing test sections layout were developed as a result of this research project. The overlays include red lines along Route 54 showing the layout of the test sections.